## Mechanical tensile test results

The Figures below display the results of the mechanical tensile tests conducted on various elastomer materials according to the ASTM D412-16 standard at three different strain rates. The elastomer materials included in this test group, in order, are Natural Rubber 60±5 shore A (NR60), Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60), Neoprene Rubber 60±5 shore A (NEO60), Cold Castable Polyether 60±5 shore A (CCP60), and Cold Castable Polyether 80±5 shore A (CCP80).

Figure 1: Engineering stress-strain curve of the Natural Rubber 60±5 shore A (NR60) at standard strain rate. Note: The standard strain rate indicates that the NR60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 2: Engineering stress-strain curve of the Natural Rubber 60±5 shore A (NR60) at standard strain rate. Note: The standard strain rate indicates that the NR60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 3: Engineering stress-strain curve of the Natural Rubber 60±5 shore A (NR60) at standard strain rate. Note: The standard strain rate indicates that the NR60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 4: Engineering stress-strain curve of the Natural Rubber 60±5 shore A (NR60) at moderate strain rate. Note: The moderate strain rate indicates that the NR60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 5: Engineering stress-strain curve of the Natural Rubber 60±5 shore A (NR60) at moderate strain rate. Note: The moderate strain rate indicates that the NR60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 6: Engineering stress-strain curve of the Natural Rubber 60±5 shore A (NR60) at moderate strain rate. Note: The moderate strain rate indicates that the NR60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 7: Engineering stress-strain curves of the Natural Rubber 60±5 shore A (NR60) at standard and moderate strain rates. Note: The standard and moderate strain rates indicate that the NR60 samples are tensioned at a velocity of 8mm/s and 16mm/s, respectively. These two strain rates (0.32 s-1 and 0.64 s-1) were achieved by setting the crosshead velocity of the tensile testing machine to the 8mm/s and 16mm/s, respectively.

Figure 8: Engineering stress-strain curve of the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) at standard strain rate. Note: The standard strain rate indicates that the EPDM60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 9: Engineering stress-strain curve of the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) at standard strain rate. Note: The standard strain rate indicates that the EPDM60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 10: Engineering stress-strain curve of the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) at standard strain rate. Note: The standard strain rate indicates that the EPDM60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 11: Engineering stress-strain curve of the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) at moderate strain rate. Note: The moderate strain rate indicates that the EPDM60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 12: Engineering stress-strain curve of the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) at moderate strain rate. Note: The moderate strain rate indicates that the EPDM60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 13: Engineering stress-strain curve of the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) at moderate strain rate. Note: The moderate strain rate indicates that the EPDM60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 14: Engineering stress-strain curves of the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) at standard and moderate strain rates. Note: The standard and moderate strain rates indicate that the EPDM60 samples are tensioned at a velocity of 8mm/s and 16mm/s, respectively. These two strain rates (0.32 s-1 and 0.64 s-1) were achieved by setting the crosshead velocity of the tensile testing machine to the 8mm/s and 16mm/s, respectively.

Figure 15: Engineering stress-strain curve of the Neoprene Rubber 60±5 shore A (NEO60) at standard strain rate. Note: The standard strain rate indicates that the NEO60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 16: Engineering stress-strain curve of the Neoprene Rubber 60±5 shore A (NEO60) at standard strain rate. Note: The standard strain rate indicates that the NEO60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 17: Engineering stress-strain curve of the Neoprene Rubber 60±5 shore A (NEO60) at standard strain rate. Note: The standard strain rate indicates that the NEO60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 18: Engineering stress-strain curve of the Neoprene Rubber 60±5 shore A (NEO60) at moderate strain rate. Note: The moderate strain rate indicates that the NEO60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 19: Engineering stress-strain curve of the Neoprene Rubber 60±5 shore A (NEO60) at moderate strain rate. Note: The moderate strain rate indicates that the NEO60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 20: Engineering stress-strain curve of the Neoprene Rubber 60±5 shore A (NEO60) at moderate strain rate. Note: The moderate strain rate indicates that the NEO60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 21: Engineering stress-strain curves of the Neoprene Rubber 60±5 shore A (NEO60) at standard and moderate strain rates. Note: The standard and moderate strain rates indicate that the NEO60 samples are tensioned at a velocity of 8mm/s and 16mm/s, respectively. These two strain rates (0.32 s-1 and 0.64 s-1) were achieved by setting the crosshead velocity of the tensile testing machine to the 8mm/s and 16mm/s, respectively.

Figure 22: Engineering stress-strain curve of the Cold Castable Polyether 60±5 shore A (CCP60) at standard strain rate. Note: The standard strain rate indicates that the CCP60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 23: Engineering stress-strain curve of the Cold Castable Polyether 60±5 shore A (CCP60) at standard strain rate. Note: The standard strain rate indicates that the CCP60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 24: Engineering stress-strain curve of the Cold Castable Polyether 60±5 shore A (CCP60) at standard strain rate. Note: The standard strain rate indicates that the CCP60 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 25: Engineering stress-strain curve of the Cold Castable Polyether 60±5 shore A (CCP60) at moderate strain rate. Note: The moderate strain rate indicates that the CCP60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 26: Engineering stress-strain curve of the Cold Castable Polyether 60±5 shore A (CCP60) at moderate strain rate. Note: The moderate strain rate indicates that the CCP60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 27: Engineering stress-strain curve of the Cold Castable Polyether 60±5 shore A (CCP60) at moderate strain rate. Note: The moderate strain rate indicates that the CCP60 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 28: Engineering stress-strain curves of the Cold Castable Polyether 60±5 shore A (CCP60) at standard and moderate strain rates. Note: The standard and moderate strain rates indicate that the CCP60 samples are tensioned at a velocity of 8mm/s and 16mm/s, respectively. These two strain rates (0.32 s-1 and 0.64 s-1) were achieved by setting the crosshead velocity of the tensile testing machine to the 8mm/s and 16mm/s, respectively.

Figure 29: Engineering stress-strain curves of the Cold Castable Polyether 80±5 shore A (CCP80) at standard strain rate. Note: The standard strain rate indicates that the CCP80 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 30: Engineering stress-strain curves of the Cold Castable Polyether 80±5 shore A (CCP80) at standard strain rate. Note: The standard strain rate indicates that the CCP80 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 31: Engineering stress-strain curves of the Cold Castable Polyether 80±5 shore A (CCP80) at standard strain rate. Note: The standard strain rate indicates that the CCP80 sample is tensioned at a velocity of 8mm/s. This strain rate (0.32 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 8mm/s.

Figure 32: Engineering stress-strain curves of the Cold Castable Polyether 80±5 shore A (CCP80) at moderate strain rate. Note: The moderate strain rate indicates that the CCP80 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 33: Engineering stress-strain curves of the Cold Castable Polyether 80±5 shore A (CCP80) at moderate strain rate. Note: The moderate strain rate indicates that the CCP80 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 34: Engineering stress-strain curves of the Cold Castable Polyether 80±5 shore A (CCP80) at moderate strain rate. Note: The moderate strain rate indicates that the CCP80 sample is tensioned at a velocity of 16mm/s. This strain rate (0.64 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 16mm/s.

Figure 35: Engineering stress-strain curves of the Cold Castable Polyether 80±5 shore A (CCP80) at standard and moderate strain rates. Note: The standard and moderate strain rates indicate that the CCP80 samples are tensioned at a velocity of 8mm/s and 16mm/s, respectively. These two strain rates (0.32 s-1 and 0.64 s-1) were achieved by setting the crosshead velocity of the tensile testing machine to the 8mm/s and 16mm/s, respectively.

Figure 36: Average of the engineering stress-strain curve at standard and moderate strain rates and raw engineering stress-strain curve at high strain rate related to the Natural Rubber 60±5 shore A (NR60) within the 0-100% range of strain. Note: The high strain rate indicates that the NR60 sample is tensioned at a velocity of 100mm/s. This strain rate (4 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 100mm/s. Unwanted harmonic material response (or fluctuated response) of the stress-strain curve at high strain rate resulted from the slack of tensile clamp fixture.

Figure 37: Average of the engineering stress-strain curve at standard and moderate strain rates and raw engineering stress-strain curve at high strain rate related to the Ethylene Propylene Diene Monomer rubber 60±5 shore A (EPDM60) within the 0-100% range of strain. Note: The high strain rate indicates that the EPDM60 sample is tensioned at a velocity of 100mm/s. This strain rate (4 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 100mm/s. Unwanted harmonic material response (or fluctuated response) of the stress-strain curve at high strain rate resulted from the slack of tensile clamp fixture.

Figure 38: Average of the engineering stress-strain curve at standard and moderate strain rates and raw engineering stress-strain curve at high strain rate related to the Neoprene Rubber 60±5 shore A (NEO60) within the 0-100% range of strain. Note: The high strain rate indicates that the NEO60 sample is tensioned at a velocity of 100mm/s. This strain rate (4 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 100mm/s. Unwanted harmonic material response (or fluctuated response) of the stress-strain curve at high strain rate resulted from the slack of tensile clamp fixture.

Figure 39: Average of the engineering stress-strain curve at standard and moderate strain rates and raw engineering stress-strain curve at high strain rate related to the Cold Castable Polyether 60±5 shore A (CCP60) within the 0-100% range of strain. Note: The high strain rate indicates that the CCP60 sample is tensioned at a velocity of 100mm/s. This strain rate (4 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 100mm/s. Unwanted harmonic material response (or fluctuated response) of the stress-strain curve at high strain rate resulted from the slack of tensile clamp fixture.

Figure 40: Average of the engineering stress-strain curve at standard and moderate strain rates and raw engineering stress-strain curve at high strain rate related to the Cold Castable Polyether 80±5 shore A (CCP80) within the 0-100% range of strain. Note: The high strain rate indicates that the CCP80 sample is tensioned at a velocity of 100mm/s. This strain rate (4 s-1) was achieved by setting the crosshead velocity of the tensile testing machine to 100mm/s. Unwanted harmonic material response (or fluctuated response) of the stress-strain curve at high strain rate resulted from the slack of tensile clamp fixture.