Wood fireproofing coatings based on biobased phenolic resins

Pedro L. de Hoyos-Martíneza,b, Hamed Issaouib, Rene Herreraa, Jalel Labidia, Fatima Charrier-El Bouhtouryb*

a Chemical and environmental engineering department, University of the Basque Country, Plaza Europa, 1, 20018, Donostia-San sebastián, Spain.

b  University of Pau and Pays de l’Adour, E2S UPPA, CNRS, IPREM, IUT des Pays de l’Adour, 371 Rue de Ruisseau, 40004 Mont de Marsan, France.

*Corresponding author: Fatima Charrier-El Bouhtoury, fatima.charrier@univ-pau.fr

ABSTRACT:

Different formulations of phenolic resins based on two natural products namely lignin and tannins, were implemented as biobased fireproofing coatings for wood. Moreover, inorganic nanoparticles were included as additives for improving the thermal resistance of the coatings. The biobased coatings formulations were first characterized for their structure and thermal properties via FTIR and thermogravimetric analyses (TGA). Then, their fireproofing performance was assessed over a softwood and a hardwood species. Various parameters were studied as the heat released during combustion, the integrity of the samples and the flames propagation. Furthermore, their performance respecting the mentioned parameters was evaluated with respect to two different commercial formulations (top ranked fireproofing coatings). It was confirmed that the risks derived from the exposure of wood to fire were significantly reduced after the application of the biobased coatings: the heat release during combustion was reduced, a protective effect was achieved concerning wood integrity and the propagation of the flames was significantly delayed. Besides, these parameters displayed a better performance on beech wood compared to maritime pine wood. Finally it was observed that the results obtained by the biobased coating formulation RA and RB were comparable to those achieved by the commercial fireproofing assessed.

KEYWORDS: coatings, fireproofing, lignin, tannins, phenolic resin, nanoclay, nanosilicate,

INTRODUCTION

Nowadays, wood represents one of the main materials employed, especially in the field of construction, due to its mechanical and structural properties e.g. excellent ratio strength to weight1. Besides, it is also regaining importance owing to its versatility and environmentally friendly features2. Nevertheless, there are some risks inherent to wood such as fire, which can considerably compromise the structure and performance of this material. Moreover, since wood is widely integrated within our daily life, wood-derived fires can lead to hazardous situations to humans. Consequently, the protection of wood against fire is of significant importance owing to structural, environmental and safety reasons. The elements used in the protection of wood against fire are generally refer to as fireproofing compounds. They are capable of improving the susceptibility of wood against fire by decreasing the heat released during the early stages of combustion, reducing the smoke and volatiles exhausted and delaying the spread of the flames along the material3. Respecting these compounds, there has been an evolution among the last decades. Traditionally, the most common flame-retardants were based halogenated compounds. However, the major problem with this type of compounds was the broad range of adverse consequences to humans such as inmunotoxicity, reproductive toxicity and carcinogenic effects4. Accordingly, they have been gradually substituted by other performing and non-toxic compounds e.g. boron, phosphorous or nitrogen-based. Another class of flame-retardants employed in the recent years, is the silicon-based compounds5. They have been reported to improve considerably the flame retardancy as either fillers, polymers or copolymers6. Thus, they help to the formation of a protective barrier during combustion, which hinders the heat transfer into the material7. Furthermore, they lead to the reduction of the heat release upon combustion8. Within this group, there are certain types attracting a great deal of attention lately. On the one hand the silsesquioxanes, which are based on a silicate-caged structure with an inner core of silicon and oxygen and an exterior part constituted of organic components ([RSiO1.5]8)9. These compounds can add different interesting functionalities within their structure (R groups)10, which is an advantage since it allows their utilization in several applications. On the other hand, layered materials such as clays, which are composed of silicate layers with different dispersion morphologies. Montmorillonite is one of the most significant examples of this type11. It is a natural 2-1 sheet phyllosilicate belonging to the family of smectites12. Its importance relies on the fact that it can be organically modified introducing different functional groups within its structure13. Another interesting approach to the topic of fire proofing compounds, is the implementation is the implementation of nanocomposites14. Their main strength is the low amount needed to ameliorate the fireproofing character, owing to their large surface area15. In this sense, the use of nanoclays and nanosilicates, especially dispersed in polymer matrices have been already reported, showing a good performance against fire16,17.

In the protection of wood against fire, besides the selection of the proper fireproofing compounds, it is of significant importance the process to introduce those compounds into the wood structure (chemical modification of wood). One possibility is the inclusion of flame-retardant into the bulk structure of wood via impregnation. This treatment is associated with the introduction of the flame-retardant additives directly into the cell wall of wood18. Another option is the modification of wood surface by the means of flame-retardants via coating19. In particular, the use of fireproofing coatings is reported as one of the most effective ways to protect substrates against fire20. Its major advantage is the concentration of the fireproofing properties of the flame-retardant at the surface, which can allow the protection of the bulk of the material21. However, owing to the inherent porosity of the wood as a substrate, it is necessary to consider some morphological, physical and chemical aspects to achieve an effective application of protective products22. On the one hand, the wood porosity and bulk density, which are inversely proportional, can significantly influence the adsorption and surface impregnability of coating products23. Dimensional variations of the wood (swelling and shrinkage) can also affect the coating performance in terms of decreasing adhesion or cracking. The pH value displays certain influence during the curing process and can result in discoloration of the coating or lower adhesions as well. Furthermore, the wood substrate must have a moisture content about 8-12 % to avoid problems in the uniformity of the film formation and roughness of the coating24.

In the protection of wood by means of fireproofing coatings, there has been also an evolution as for the previously mentioned flame-retardants. Thereby it is known that traditionally, water-soluble silicates have been used as wood coating and impregnants, owing to their ability to melt and their intumescent effect25. However, nowadays wood coatings are designed to retard ignition and rate of burn rather than to provide the fire-resistive barrier which is more typical for other materials26,27. These coatings are generally based on different synthetic polymers. For instance, epoxy and melamine formaldehyde resins, which are derived from partial esters of polyols28, can be combined with different flame-retardant compounds. In fact, the combination of these type of polymers with phosphate and borate derivatives has already been described in the literature27,29. Concerning the application of silicon-based compounds in wood coatings, there are several works within the literature and the industry: the use of a butyl acrylate-based formulation incorporating some organically modified montmorillonite clay30 or the elaboration of silicone coatings with dispersed carbon nanotubes based on an acrylonitrile synthetic rubber31. Other state-of-the-art works have been also presented in the recent years such as the use of transparent UV-curable coatings from phosphazene-based compounds32 or the addition of nanoparticles as clay nanopowder from montmorillonite and cellulose nanofibers33 for the elaboration of organic-inorganic hybrid coatings based on polyurethanes34. From the previously mentioned synthetic polymers, phenol-formaldehyde resins (PF) are of considerable relevance, since they are reported to display fire resistant features and to meet properly the requirements for reaction to fire3. Nevertheless, they present drawbacks related to their dependence on fossil sources and to their toxicity35. Consequently, there is an ongoing tendency towards the substitution of the toxic and non-renewable raw materials e.g. phenol or formaldehyde present in these resins, by others of similar chemical nature, but obtained from natural and renewable sources36,37. The phenolic resins in which the components are obtained from renewable, natural or non-oil-derived raw materials are referred to as biobased phenolic resins38. In this type of resins, phenol is generally substituted by different natural phenolic compounds, among which lignin and tannins are extensively used39. On the one hand, lignin is a natural polyphenolic polymer, which is known for being an abundant by-product from the pulp and paper industry. Despite of the mentioned availability, lignin is currently underutilized for higher-value applications40. For this reason, its use in the synthesis of lignin-derived polymers constitutes an appropriate option to switch this situation. On the other hand, tannins are the second most abundant natural source of polyphenolic compound after lignin41. They are widely abundant in nature, especially in some parts of the plants such as bark, leaves, seeds, roots and rhizomes42. Their utilization in phenolic resins is well set in the market e.g. adhesives applications43, since they can provide similar reactivity and interactions to aldehydes, thanks to their structure44. Nevertheless, the main disadvantage of the tannin utilization for the synthesis of phenolic resins is their direct competition with other higher-value applications in areas such as medicine and pharmacology. Accordingly, in the recent years, the combination of tannins and lignin as a substitute for phenol in biobased phenolic resins has been reported45–47.

The interest of this work relies on the employment of fireproofing coatings for wood based on biobased phenolic resins. Thereby it was possible to replace the toxic and non-renewable compounds typical from the phenol formaldehyde resins (PF), by other natural and renewable compounds (≈90% content) and still maintain the protective effect of the coatings. In this case, phenol was substituted by lignin and tannins (natural polyphenolic compounds) and glyoxal was employed as an alternative to formaldehyde (lower toxicity and volatility). These coatings were applied onto two wood species namely maritime pine (Pinus pinaster) and beech (Fagus sylvatica). Following to this, their protective effect against fire was assessed by means of several analyses. Furthermore, the other important point of this work was the comparison of the protective effect achieved by the biobased coatings with that accomplished by two commercial products available in the market. Thus, it was possible to assess properly the performance of the fireproofing coatings based on the biobased phenolic resins.

MATERIALS AND METHODS

Materials

The lignin employed within this work was extracted by means of an organosolv process from wood residues of maritime pine (Pinus pinaster). The mentioned residues were based on the remaining parts coming from wood industry activities e.g. small pieces of panels, wood chips, etc. The organosolv process was implemented by using an ethanol solution (70%) and a rate liquid to solid 6:1. The extraction was performed during 90 minutes at 200ºC in a 1.5 L stainless steel Parr reactor. After this reaction, the liquor was filtered to separate it from the solid residue. Then lignin contained was precipitated by adding acidified water (pH 2) to the liquor with a ratio 2:1 v/v. This mixture was left overnight to promote the lignin precipitation. Finally, the lignin was filtered from the suspension and it was dried at 50ºC during 2-3 days. The tannins used consisted in a commercial extract from mimosa (Acacia meransii), which was commercialized under the name Tanfood and supplied by TANAC S.A (Brazil). Two different types of inorganic nanoparticles were utilized namely Delite 43B (nanoclay) and SO1458-Trisilanol Phenyl POSS (nanosilicate). The nanoclay was kindly provided by Laviosa Advance Mineral Solutions (Italy) and the nanosilicate by Hybrid Plastics Inc. (USA). Hexamethylenetetramine (99%) and sodium hydroxide pellets were purchased from Fisher Scientific.

Two different commercial fireproofing coatings were selected to assess the efficiency of the coatings based on the biobased phenolic resins. Both commercial formulations were ranked with the highest possible classification for wood protection against fire, according to standard UNE EN 13501-1:2007+A1:2009 (Bs2d0). On the one hand, a water-borne fireproofing coating (CEDRIA B-77) was purchased from BASMODEC (Gipuzkoa). On the other hand, a two-phase formulation polyurethane based (Quidedur AIG-7110) was kindly provided by NAILAN Parquets-Barnices (Bizkaia)

Synthesis of the resins

The process employed for the synthesis of the resins was based on the previous preparation of the phenolic raw materials i.e. lignin and tannins. Thereby, the lignin was first subjected to a process of functionalization in two stages namely glyoxalation and modification with inorganic nanoparticles (hybridization). Shortly, an aqueous suspension of lignin was prepared with a concentration 27.86±1.04% (w/w). Then a solution sodium hydroxide solution (30%) was added to set the pH at 12-12.5 and to achieve the complete dissolution of lignin. When the desired pH was reached and the lignin was totally dissolved, glyoxal solution was added (40% in water) with molar ratio lignin to glyoxal solution 1:1.44. Following to that the glyoxalation reaction was performed at 58ºC, during 8h and by using mechanical agitation (450 rpm). To the glyoxalated lignins, the inorganic nanoparticles were added (5% w/w with respect to the solid lignin in solution) at 40ºC with magnetic agitation (550 rpm). The reaction was left overnight until the complete dissolution of the nanoparticles. The mentioned process of functionalization has been already comprehensively described in a previous work48. On the other hand, a tannins solution was prepared based on the commercial mimosa extracts, which displayed a Stiasny number of 89.46±2.4649. The solution was done by dissolving the commercial mimosa extract in acetone (30%) at a concentration 45% (w/w). Once, the tannins were homogeneously dissolved, a solution of NaOH 30% (w/v) in water was added to fix the pH within the range 10-10.5. Then, a hexamine solution 30% (w/w) was poured into the tannins phase with a ratio hexamine solids: tannin solids 1:20. Just after the addition of the hexamine, the functionalized lignin phase was added to the tannins phase with a ratio functionalized-lignin: tannin-solution 1:1. The formulations of the resins synthesized are presented in table 1 as well as the amounts of the different components. The total amount of biobased materials on dry basis reached ≈90% and avoided the employment toxic of compounds such as formaldehyde and phenol.

Table 1. Different formulations of the resins synthesized and their compositions

| Formulation | Components % (w/w) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Lignin phase |  | Inorganic nanoparticles |  | Tannins | Hexamine |
|  | Lignin | Glyoxal | Dellite 43B | Trisilanol POSS |  |  |
| Reference | 45.62 | 6.48 | --- | --- | 45.62 | 2.28 |
| RA | 44.61 | 6.33 | 2.23 | --- | 44.60 | 2.23 |
| RB |  |  | --- | 2.23 |  |  |

Chemical characterization of the resins

The different formulations of the resins were analyzed chemically based on several physical-chemical parameters and other important properties. All the presented properties were measured in triplicate for each sample.

The pH of the liquid fraction was determined by using a pH meter “CRISON basic 20”.

The density was calculated gravimetrically by measuring the weight of known volume (5mL) of a volumetric flask filled with the liquid fraction.

For the determination of the apparent viscosity, a viscometer (Fungilab) was used with a low viscosity adapter (LCP) APM/B. The measurement was carried out with a resin volume of 6 mL, a cylindrical spindle TL5 and a rotational speed of 5-10 rpm. The values of the apparent viscosity were taken after a period of 1h, when no significant differences were observed.

The content of nonvolatile compounds was obtained following the procedure ASTM D4426-01: Standard Test Method for Determination of Percent Nonvolatile Content of Liquid Phenolic Resins Used for Wood Laminating.

Process of coating application

Two wood species were selected for the deposition of the resins previously synthesized: a softwood specie (maritime pine) and a hardwood specie (beech). Information related to the anatomy and intrinsic properties of both wood species is included in Appendix A1 of Supporting information with comparison purpose in further analyses. Thereby, the influence of the wood specie over the performance of the coatings could be analyzed. Then two samples of each species were cut with dimensions 300x80x20 mm, using a table saw with a circular saw. The smaller samples of wood used in the different analyses for the assessment of the fireproofing properties, were cut from these bigger panels of wood.

For the application of the biobased phenolic resins as a coating, the wood samples were previously prepared. The wooden surfaces were sanded using fine abrasive paper as a pretreatment to obtain uniform surfaces as smooth and even as possible prior to coating application. First, each surface was sanded with the paper of grain size 80, then grain paper 100 was applied and finally sanded with grain paper 120. After each sanding process the surfaces were dedusted (brushing out of pores). Then, they were conditioned for 7 days at specific conditions of temperature and relative humidity (25 ºC and 65%).

Concerning the deposition of the resins over the wood surface, two important features were considered namely mass of resin applied and method of application. The process followed for selecting those parameters is described in Appendix A2 of Supporting Information. Thus, the amount of coating added to the wood surface was 62.5 g∙m-2 and the deposition of resins was carried out with a brush. The coating curing and drying was performed during 12-15h in an oven at 60ºC. Further discussion concerning these set parameters is included in Appendix A2 of Supporting Information.

Characterization of the coatings

The characterization of the coatings was carried out concerning its chemical structure (FTIR analysis) and thermal resistance (TGA analysis). Prior to those analyses, a liquid sample of the different formulations of the resins (Reference, RA and RB) was cured at the defined conditions (60 ºC and 15 h) over an aluminum plate. Then the cured resin samples were crushed in a mortar and the powder was ready to use for the characterization analysis.

Fourier transformed infrared spectroscopy analysis (FTIR)

This test was performed on a Spectrum Two FTIR Spectrometer PerkinElmer (USA) with a L1050231 Universal Attenuated Total Reflectance accessory (ATR). First, a background spectrum was collected to subtract it from the spectrum of the sample. Then, a few mg of the sample were analyzed, with a number of 64 scans accumulated in transmission mode and a resolution of 4 cm−1. The spectrum was obtained in the range of 4000−400 cm−1.

Thermogravimetric analysis (TGA)

This analysis was executed in a TA instrument thermogravimetric analysis (TGA) Q5000 IR equipment, under dynamic nitrogen flow with a flow rate of 40 mL min−1. Samples in the range of 5−10 mg were placed in a platinum crucible and heated in a temperature range of 30−800 °C at a constant heating rate of 10 °C min−1 under a N2 (airflow 60mL∙min-1). For the quantitative calculations, the response factors between the weight gain (thermogravimetric) and the mass loss rate (differential thermogravimetric) were determined.

Evaluation of the fireproofing properties of the coating

Different experiments, which were carried out directly on the coated-wood samples, were implemented to assess the performance of the coatings against fire exposure and derived thermal properties. Hence, the wood protection achieved could be elucidated. Each of the samples (control and coated wood) was performed the following experiments in triplicate.

Analysis of the heat release during combustion

This test was carried out by means of a Parr 6200 Calorimeter equipped with a Parr 1108 oxygen bomb. The samples employed were prepared with a size of 20x20x3 mm. The procedure followed is described in Appendix B1 of Supporting Information.

Flammability analysis of the coatings

This test was performed according to the procedure UNE-EN 60695-11-10 (2014) Fire hazard testing - Part 11-10: Test flames - 50 W horizontal and vertical flame test methods

Analysis of the heat transfer properties of the coatings

This test was performed with conductimeter instrument “Hot Disk TPS 1500” and a probe Kapton Ref. 5456 of 3.189 mm radius. The samples employed were prepared with a size of 30x20x10 mm. The procedure followed is described in Appendix B2 of Supporting Information.

Data Analysis

The collected data were statistically analyzed according to the normality and homogeneity values of variances by a multiple comparison procedure analysis of variance (ANOVA). The Bonferroni Significant Difference (BSD) and the Tukey test were applied after rejecting the null hypothesis. The software used for this statistical analysis was Origin 2017.

RESULTS AND DISCUSSION

Chemical characterization of the resins

The resins were first characterized for the typical physical-chemical parameters and the results are shown in table 2.

Table 2. Physical-chemical parameters of the different biobased phenolic resins and the commercial formulations.

| Parameters | Biobased resin formulations |  |  | Commercial formulations |  |
| --- | --- | --- | --- | --- | --- |
|  | RREFERENCE | RA | RB | B77a | Quidedurb |
| Density (g∙cm-3) | 1.13±0.02* | 1.14±0.00* | 1.14±0.02* | 1.07 | 1.01-1.03 |
| pH | 8.58±0.02♠(1) | 8.88±0.02♠ | 8.82±0.01♠ | 7.71±0.03♠(1) | 9.11±0.11♠(1) |
| Viscosity (mPa∙s) | 73.00±3.68* | 73.75±3.18* | 73.80±4.24* | 200-300 | 74.3±4.03* |
| NVC % (w/w) | 36.81±0.36♠(1) | 37.42±0.07♠ | 37.41±0.03♠ | 35.11±0.13♠(1) | 36.21±0.19♠(1) |
| ANOVAOneWay: *The population means are not significantly different at the 0.05 level. ♠The population means are significantly different at the 0.05 level. Bonferroni and Tukey test among the same parameter: 1 The difference of the mean is significantly different at the 0.05 level. No number in superscript indicates that the difference of the mean is not significant at the 0.05 level. |  |  |  | aB77: water borne fireproofing coating based on acrylic resin bQuidedur: two-phase polyurethane based fireproofing coating. |  |

With respect to the previous results, it was seen that the determined parameters presented values with no significant differences for the biobased resin formulations, as shown by the ANOVA analysis. Nevertheless, the differences detected (pH and NVC), which at first sight may appear slight, followed analogous tendencies. The pH of the resins formulations showed rather alkaline values. This was expected since the pH of the tannins phase was set at 10.4. Besides the lignin, which was the other main raw material, was dissolved at an alkaline pH prior to the glyoxalation reaction. The fact that the pH was slightly reduced from that of the tannins phase was related to  a slight amount of unreacted glyoxal (acidic pH 2-3.5), which could have remained in the glyoxalated lignin phase. Concerning the densities of the different formulations, they were lower than the ones reported in the literature for other phenolic resins based on the phenol formaldehyde type50,51. This was due to the considerable amount of solvent employed in the synthesis of the different formulations (ratio Liquid/Solid>1), which was water (waterborne type resin). This had also a direct influence over the percentage of non-volatile compounds, which was lower than 50%. The values determined for this parameter were around 40% and presented a slight increase in the formulations where inorganic nanoparticles were added, owing to the little increment of the solid content. The values of the NVC were lower compared to other works from the literature52,53 and especially compared to the typical phenol formaldehyde resins54. The apparent viscosity was another parameter displaying a similar tendency to the density and the non-volatile content. Consequently, the values of the viscosity exhibited low values as well as compared with other similar phenolic resins reported in the literature55,56. Concerning the commercial products, significant differences were observed between some of the studied parameters. The coating based on a two-phase polyurethane (Quidedur) displayed more similarities to the biobased resin formulations, than the waterborne based on acrylic resin (B77). This was especially evidenced in the case of the viscosity. The coating Quidedur presented a viscosity within the range of the biobased resin formulation, whereas the coating B77 showed a range of viscosities considerably higher as provided by the supplier in the corresponding technical data sheet. This parameter is of relevant importance since it can influence the capacity of spreading the coating onto the wood surface and the penetration of the coating into the pores of wood57. In respect to the pH and the percentage of non-volatile compounds (NVC), again the values of the coating Quidedur were closer to those of the biobased formulations than the values of the coating B77. Nevertheless, in this case the differences were significantly lower than for the case of the viscosity. The biobased resins only presented a slightly higher amount of solids compared to the coating B77. Concerning the pH, all the coating formulations displayed alkaline values, being the biobased ones within the range of both commercial coatings B77 (≈8) and Quidedur (≈9). Considering that the biobased resins (mainly RA and RB) and the commercial formulation Quidedur presented physical chemical parameters within a narrow range, they could be expected to display a similar behavior and compatibility towards wood. This would be of significant relevance to achieve a comparable performance respecting the fire protection of wood.

Characterization of the coatings

Fourier transformed infrared spectroscopy analysis (FTIR)

The chemical structure of the coatings was analyzed and the main linkages between the different components and the major functional groups were elucidated. In figure 2, the spectra of the individual components namely functionalized lignin and tannin, and that of the resins formulations are shown.

Figure 2. Infrared spectra of the components (FL: functionalized lignin-(A) with Dellite 43B and (B) with Trisilanol POSS, TM: mimosa tannin) and different resins formulations: a) formulation Reference, b) formulation RA and c) formulation RB.

It was clear from the previous figure that the spectra of the cured resins (coatings) were greatly influenced by their components. Thus, the signals from the main groups of both the functionalized lignin and mimosa tannin were found in the cured resin spectra. The main signal was the one detected in the range 3500-3300 cm-1 (broad and strong) associated with the hydroxyl groups. This was expected since the polyphenolic resins synthesized displayed an abundance of hydroxyl groups. Between 3000-2900 cm-1, a medium-sharp band was seen related to the methyl and methylene groups. The mentioned signal is more prominent in the spectra the functionalized lignin than in the mimosa tannin since these units are more abundant within its structure. Consequently, it might be attributed to the lignin-derived fractions present within the resin structure. Nevertheless, it could be also due to the reaction between lignin and tannin by means of methylene groups (-CH2 and –CH-) as proposed by Pizzi, 201658. He reported a mechanism for the reaction between tannins and glyoxalated lignin cured by hexamine (figure 3). The mentioned mechanism consisted of the faster reaction between tannins and hexamine, which were connected via C-N bonds. Then, glyoxalated lignin units were connected with the reacted tannins-hexamine moieties by means of intermediate methylene groups. Thus, in this case the presence of a significant signal in the resins, would confirm the reaction between both components (lignin and tannins).

Figure 3. Proposed mechanism of reaction between tannins and lignin in the resins formulations, as described in Pizzi, 201658.

In the next range (1600-1400 cm-1), several peaks were detected characteristic from conjugated linkages from the aromatic rings. These peaks observed in the resins were associated with the multiple aromatic rings present within the structure of both the lignin and tannin. At 1370 cm-1 a medium-weak and broad signal can be seen in the resins spectra, related to the deformation of the O-H linkage. This was derived from the tannin fractions, which contain various phenolic groups attached to the flavan-3-ol moieties. In fact, a similar medium and broad signal was observed in the spectra of the mimosa tannin. An important signal was detected at 1235 cm-1 attributed to the bond C-N from amine (blue circle), as described in the already-mentioned reaction mechanism. Besides, this assignment was in agreement with the work of Sumathirathne and Karunanayake, 2017 on the synthesis of tannin-phenol resins cured with hexamine59. They related the presence of a peak at 1239 cm-1 to the stretching of the C-N bond coupled with the stretching of other adjacent bonds in other molecules. This signal confirmed the curing reaction between the tannin fractions and hexamine 46. Another significant band was observed in the range 1150-900 cm-1 for the resins spectra. In this interval, different signals related to the C-O linkage were determined. The most significant contribution was that of C-O bonds derived from the primary and secondary alcohols present within the functionalized lignin structures. On the other hand, another contribution to the C-O band was that of the furan heterocycles of the flavan-3-ol units from the tannin fraction. Besides these contributions, in the mentioned interval there was also the signal of Si-O-Si stretching derived from the inorganic parts of the structure of the functionalized lignins. Between 900-400 cm-1, the signals detected corresponded only to the linkages and functional groups of the inorganic nanoparticles added during the synthesis of the resins (Delite 43B and Trisilanol POSS). The assignments for the above-mentioned signals detected in the different formulations of the resins are summarized and listed in table C1 in Appendix C.

Thermogravimetric analysis (TGA)

This method was used as an approximate indicator of the actual thermal resistance of the cured resins. This could provide an idea of the fireproofing performance of the coatings and of the effect achieved by the inorganic nanoparticles in the coating formulations. In figure 4, the thermogravimetric and derivative thermogravimetric curves for the different cured resins formulations are displayed. Additionally the curves of the raw materials were added to Appendix C2 of Supporting Information, with comparison purposes. Here it was seen that the stages of degradation detected in the raw materials namely functionalized lignins and tannins, were found in the curves of the resin (especially detected in the case of DTG curves). The degradation of the cured resins occurred through several steps. The first one (80-110 ºC) was majorly attributed to the vaporization of the moisture from the coatings in powder-state.. Then main stage of degradation was located in the range of 295-300 ºC and represented 20% of the mass loss of the cured resins. This stage was located between the main stages of degradation of the major constituents, namely mimosa tannins (≈250ºC) and organosolv lignin (≈400ºC) as showed in Appendix C2 of supporting information. Accordingly, it would be related to the rupture of interunit linkages of the lignin fractions. Between lignin units C-C and - bonds are reported to cleave between 275-350ºC60. Furthermore, this stage would be also associated with the break of tannins units. Following this stage, two other degradation steps (≈10% weight loss) were detected between 350-370 ºC and 475-485 ºC respectively.

Figure 4. Curves of the thermal analysis of the different resin formulations cured (coatings).

The previous degradation stages occurred at temperatures similar to those reported in a previous work for the functionalized lignins alone48. Nevertheless, in this case of the cured resins the percentage of weight loss associated with each stage, was considerably reduced compared with that of the modified lignins alone (Appendix C2 of supporting information). This corroborates the presence of a polymeric structure of greater thermal resistance than that of it constituents alone, which would have been builtduring the curing of the resins. Thereby, it would be confirmed the reaction of the lignin with the tannin and the curing agent. In table 3, the main parameters determined from the analysis are presented. It was seen that the stages of degradation occurred within a narrow range of temperature in the different formulations of the coatings. However, the mass loss had a different development among the different cured resins. It was seen in table 3 and figure 4 that the loss of mass started to diverge between the resins formulations as the temperature increased, especially for RA and RB compared to Reference. Consequently, slight differences were regarded concerning T10%, whereas considerable differences were encountered in the temperature at which the resins had lost half of their mass (T50%). Besides, the residue remaining after thermal degradation was slightly higher in RA and RB formulations as well. All these results were attributed to the fact that formulations RA and RB had within their structure Dellite 43B and Trisilanol POSS respectively. These inorganic compounds are widely reported to provide a synergic effect regarding the flame-retardancy and thermal resistance61,62.

Table 3. Thermogravimetric parameters determined for the different formulations of the cured resins.

| Formulations | T10% (ºC) | T50% (ºC) | Residue (wt. %) | Degradation stages (ºC) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Reference | 202.75 | 657.51 | 45.96 | 99.56 | 296.23 | 358.92 | 475.11 |
| RA | 215.19 | 745.07 | 48.13 | 77.07 | 299.62 | 361.02 | 480.75 |
| RB | 214.46 | 759.13 | 48.55 | 81.10 | 301.71 | 367.30 | 482.85 |

Assessment of the performance of the coatings

Retention of the coatings

Before testing the performance of the coatings against different thermal parameters related to fire exposure, the retention of the resins onto the wood samples was assessed. With this intention, the resins were deposited onto the wood surface and cured + dried according to the parameters defined in the corresponding section of materials and methods. After this process, the weight percentage gain (WPG) was determined to elucidate the degree of retention of the resins in each wood species (table 4). The measurements for this parameter as well as the relative humidity were carried out in triplicate for each sample.

Table 4. Relative humidity and weight percentage gain of the wood samples before and after the application of the coating.

| Parameters | Samples | Wood species |  |
| --- | --- | --- | --- |
|  |  | Maritime Pine | Beech |
| Relative Humidity (%) | Non coated | 11.85±0.54(1-a,b) | 13.99±0.39(1-a,b) |
|  | Coating Reference | 10.40±0.35(a) | 12.34±0.21(a) |
|  | Coating RA | 10.90±0.70 | 13.13±0.90 |
|  | Coating RB | 11.03±0.28 | 13.09±0.19 |
|  | Coating B77 | 10.31±0.76(b) | 11.98±0.19(b) |
|  | Coating Quidedur | 11.52±0.38 | 13.54±0.29(1-b) |
| Weight Percentage Gain (%) | Coating Reference | 31.37±1.36(a) | 45.79±3.16(a) |
|  | Coating RA | 36.63±3.04 | 46.74±0.40(b) |
|  | Coating RB | 32.37±0.10(b) | 47.74±1.59 |
|  | Coating B77 | 36.48±2.50 | 47.14±1.89(c) |
|  | Coating Quidedur | 42.82±1.11(1-a,b) | 55.34±2.46(1-a,b,c) |
| ANOVAOneWay: The population means are significantly different at the 0.05 level. Bonferroni and Tukey test among the same wood specie: 1 The difference of the mean is significantly different to the specific samples (a,b,c) at the 0.05 level. No superscript indicates that the difference of the mean is not significant at the 0.05 level. |  |  |  |

As shown in the previous table, the coated wood samples of beech displayed a higher weight percentage gain (WPG) than the maritime pine ones. This means that a greater degree of retention of the coating was achieved on the former wood species. The surface preparation can have some influence on the coating penetration because sanding reduces the number of open-cell capillaries in which the product can flow24. Nevertheless, the substrate preparation was similar in both tested species. Therefore, the differences in WPG between wood species would be mainly influenced by the anatomical structure of each wood substrate (properties presented in Annex A1 of Supporting information). On the one hand, in the softwood species (maritime pine) the coating penetration is dominated by three mechanisms. Firstly, the outer longitudinal tracheid’s is filled, then the coating passes through the rays and finally from the ray cells to adjacent longitudinal tracheids in the latewood63,64. The transport from rays to tracheids is almost completely limited to pine sapwood. Thus, the origin of the sample might influence the WPG, owing to the differences in early- and latewood portions. On the other hand, the penetration mechanisms in the hardwood species (beech) are simplified to filling the vessels and the first cells of rays, and then occasionally the axial parenchym and sklerenchym. Consequently, the vessels fill more deeply and penetration into axial parenchym and sklerenchym might be more pronounced. Hence, a greater WPG was achieved in the samples of beech wood compared to that of the softwood. Concerning the relative humidity of the samples, the major divergences were observed especially between species, since it represents an intrinsic parameter of each wood type. Moreover, it was seen in both species that the addition of the coatings reduced the relative humidity of the wood samples. This tendency could be related to the presence of the coating layer onto the wood surface, which hindered the wood absorption of water from the ambience. This phenomenon was detected in both wood species.

Analysis of the combustibility of the wood samples

This technique was carried out to evaluate the influence of the coating formulations over the heat release during the combustion of the wood samples. The samples were put into a calorimetry pump with and without coating to evaluate the influence of the application of the coating on wood on this parameter. The results concerning the heat produced during the combustion of the wood samples are presented in figure 4.

Figure 5. Heat of combustion of the wood samples before and after the application of the coatings.

The heat of combustion determined, showed higher values in the samples of maritime pine wood compared to those of beech wood. This is normally associated with the higher lignin content of conifers compared to hardwood species65. Moreover, it is also due to the presence of a greater amount of resin, oil and wax in softwood species. These compounds, which take part typically of the extractives, are reported to increase the heat of combustion of wood species66. The calorific values of the control samples determined, expressed as HHV, were within the typical ranges of maritime pine wood (19.55-20.99 MJ∙Kg-1) and beech wood (19.33-19.21 MJ∙Kg-1) as reported in the literature67,68. However, after the application of the coating the caloric values of the samples were reduced. This means that the heat released from wood during combustion was lower and therefore the combustibility of the samples was decreased. This tendency was more marked in the coated samples of beech wood than in the maritime pine ones. This could be attributed to the significant presence of resins in the wood of maritime pine69. The mentioned resins would hinder the interaction between the functional groups of the wood surface and those of the coatings and the retention of the resin on the surface. Moreover, during combustion the resins would be exudated and released through the wood pores. This may induce small cracking in the protective surface layer of the coating. Concerning the performance of the different formulations it was observed that the highest reduction was achieved by the commercial formulations B77 and Quidedur, especially in the case of martime pine. Nevertheless, the results obtained for the RA and RB were in a closer range as well confirming a similar efficiency to that of the commercial products as it was observed in the case of beech. Here they achieved a heat released upon combustion even slightly lower than those of commercial coatings did.

Based on the results described previously and the data of the masses of the wood samples and the coatings applied, it was calculated the reduction of the combustibility achieved related to the mass of coating used (table D1 in Appendix D). Thereby it was seen that even with a small amount of coating the reduction of the heat-release during combustion was significant, especially in the case of beech wood ≈8 KJ∙g-1 or 8 MJ∙Kg-1  and 9 KJ∙g-1 or 8 MJ∙Kg-1 for the biobased and commercial coatings respectively). Within the biobased coatings, the reduction was higher in the case of the RA and RB formulations compared to the Reference. The mentioned parameter achieved by the coatings was related to the presence of the inorganic heat resistant components (Dellite 43B, Trisilanol POSS). These components could balance the action of lignin, which is known by its considerable calorific value70. Consequently, these components were also proved to improve the thermal performance on these coating formulations regarding the heat release during combustion.

Coatings flammability and fire resistance assessment

This analysis was based on the standard UNE-EN 60695-11-10:2014 and it was carried out for the horizontal combustion with a contact angle between the wood samples and the flame of 45 º and samples with dimensions 125x13x3 mm. During the exposure of the samples to flames, significant divergences were seen between the control samples (without coating) and the coated ones. On the one hand, in the control samples a fast ignition, combustion and spread of the flames were observed. In some of these samples (mainly maritime pine ones), black fumes were also exhausted and an intense glowing was observed during combustion. Besides, exudation and dripping were seen during the fire exposure as well. These events were attributed to the higher extractive content of maritime pine wood compared to beech wood71. On the other hand, in the coated wood samples the phenomena described previously developed differently, both in the case of the biobased coatings and the commercial ones. Thereby, the combustion of the samples displayed a lower impact on the integrity of the wood samples. It seemed that the combustion was occurring directly onto the coating layer and around the wood bulk. Other important facts were that no black fumes were not exhausted and that no glowing was observed. Moreover, the propagation of the flames along the wood was slowed down. These phenomena described previously were measure by means of two main parameters, namely integrity of the wood samples and flame propagation along the wood.

Figure 6. Performance of the biobased and commercial coating formulations: a) assessment of the fire resistance achieved by the coatings, b) assessment of the flame retardancy achieved by the coatings

On the one hand, the integrity of the samples was determined by the  mass degradation of the wood samples after combustion, described as the percentage of wood remaining after fire exposure (Figure 6A). Thus, it was evaluated the performance of the coating respecting the fire resistance of the wood samples.

Concerning the previous results, it was clear that the coatings achieved an enhanced thermal resistance of wood. Moreover, the coating application aided to maintain wood integrity during combustion. This was evidenced by the increment of the residue of wood remaining after combustion, which was between 10-15% and up to 55% for the maritime pine wood and beech wood samples respectively. In both control and coated samples, the wood species displayed a significant influence. Hence, it was observed that maritime pine wood samples were burnt easier than those of beech wood. Within the biobased coatings, it was observed that the formulations with inorganic nanoparticles (RA and RB) resulted in a fire resistance of the wood samples improved with respect to the Reference formulation. This was in agreement with the results obtained in the thermogravimetric analysis (TGA). This effect was more evidenced in the beech wood samples than the maritime pine ones. Compared to commercial formulations (B77 and Quidedur), biobased coatings presented a similar performance in the maritime pine samples. However, in the beech ones the fire resistance achieved by the commercial formulation Quidedur was 10% higher, compared to the biobased formulations RA, RB. In both maritime pine and beech wood, the performance of the commercial coating B77 was lower than those of RA and RB (especially in later species). This was associated with the viscosity of the coatings in the resins state. As showed previously in table 2, the viscosity of the biobased resins formulations was considerably lower than that of B77. Thus, a higher viscosity of this later formulation would influence negatively its deposition along the wood surface and its penetration into the wood pores, resulting in a worse outcome.

On the other hand, the flame retardancy of the wood samples before and after the application of the coatings was determined. Thereby, it was analyzed  the influence of the coating on the flame propagation along the wood. The results (Figure 6B) showed a significant influence of the coatings on flame propagation. Thereby in control samples, the flames spread rapidly, whereas in the coated wood samples the advancement was slowed down. This was readily observed from the linear combustion speed (LCS), which was calculated as depicted in equation 1

LCS=[L/t]∙[60s/min]				           (1)

where	L: length of the wood sample damaged

t: time elapsed during sample damage

In the case of the biobased coatings, it was seen that the application of the coatings reduced the linear combustion speed by 50% in maritime pine wood samples and by 70-80% in beech wood samples approximately. Moreover, it was observed a higher delay of the flame propagation in the RA and RB compared to the Reference. This confirmed the positive effect of the inorganic nanoparticles towards the fire protection of wood, which was already reported in the previous section. Compared to the commercial formulation, it was seen that the biobased coatings displayed a similar efficiency respecting the flame retardancy. Thus, only significant divergences were detected between the biobased coatings and the formulation Quidedur in the case of maritime pine.This means that in those samples the coating provided a self-extinguishing effect for the flames. Considering the previous results and based on the standard method used (UNE-EN 60695-11-10:2014) the coatings were categorized regarding horizontal burning between HB (self-extinguishing), meaning that the linear combustion speed was below 40 mm∙min-1 and HB75, meaning that their linear combustion speed was above 40 mm∙min-1 but below 75 mm∙min-1  as showed in figure 6B. In this respect, the best performance was achieved by the commercial formulation Quidedur (HB in the case of maritime pine and beech wood), followed by the biobased formulations RA and RB and the commercial one B77 (HB75 in maritime pine and HB in beech wood). The Reference formulation was not able to reach HB classification neither in maritime pine nor in beech wood.  as. Based on the previous classification, the coatings HB would be appropriate  for the surface protection of wood structural elements and interior fittings, whereas those with HB75 would preferably be used in wood exterior element.

From this assay, it was seen that the coatings achieved a better performance regarding the thermal resistance of the samples and the flame propagation on beech wood than in maritime pine wood. This was attributed to a lower content of extracts of the former species that it is reported to have minor influence over the coating properties such as penetration and retention on the wood63. Then, since a higher amount of coating was retained in the beech wood samples, they showed and improved effect over the studied parameters compared to the maritime pine wood samples.

Assessment of the heat transfer properties of the coatings

This analysis was performed to determine the influence of the coatings over the transfer of heat through the wood surface. The results are shown in table 5, displaying the values of the thermal conductivity and thermal diffusivity of the samples.

Table 5. Properties related to the heat transfer through the wood surface of the coated and uncoated samples.

| Parameters | Samples | Wood species |  |
| --- | --- | --- | --- |
|  |  | Maritime Pine | Beech |
| Conductivity (W∙m-1∙K-1) | Non coated | 0.17±0.01* | 0.21±0.01* |
|  | Coating Reference | 0.17±0.01* | 0.20±0.01* |
|  | Coating RA | 0.18±0.01* | 0.20±0.01* |
|  | Coating RB | 0.17±0.01* | 0.21±0.01* |
|  | Coating B77 | 0.17±0.01* | 0.21±0.01* |
|  | Coating Quidedur | 0.17±0.01* | 0.24±0.06* |
|  | Non coated | 0.38±0.01* | 0.35±0.01♠ |
| Diffusivity (mm2∙s-1) | Coating Reference | 0.36±0.02* | 0.32±0.01♠ |
|  | Coating RA | 0.36±0.02* | 0.32±0.01♠ |
|  | Coating RB | 0.35±0.01* | 0.33±0.02♠ |
|  | Coating B77 | 0.37±0.06* | 0.33±0.01♠ |
|  | Coating Quidedur | 0.33±0.06* | 0.33±0.01♠ |
| ANOVAOneWay: *The population means are not significantly different at the 0.05 level. ♠The population means are significantly different at the 0.05 level. Bonferroni and Tukey test among the same wood specie: No number in superscript indicates that the difference of the mean is not significant at the 0.05 level. |  |  |  |

The overall result of these properties were statistically explored by ANOVA test with a level of significance of 99%. The results of the ANOVA test are presented in tables D2 and D3 of Appendix D. It was confirmed that in the majority of the cases the values of the thermal conductivity and diffusivity for the control wood samples and the coated ones were not significantly different, since the mean values of both properties were statistically equal for each specie. Thereby  the deposition of the coating did not alter the properties of wood related to the heat transfer. This would be of interest for a future utilization of the coatings as a product in the wood industry for wood products and interior fittings. Hence, these elements would maintain their thermal properties intact (concerning the heat transfer) but with enhanced thermal resistance. The aforementioned tendency was observed, for both the biobased coating formulations and the commercial ones.

Likewise, the values of these parameters for the different coating formulations were not statistically different either. Thereby, it was corroborated that the effect displayed by both biobased coating formulations and commercial ones over the wood properties, was analogous.

Nevertheless, the results for the diffusivity between wood species did show statistical differences as proved by the ANOVA test. This was observed in the case of both the control and the coated wood samples. This proved that the features and properties inherent to the nature and anatomy of the wood species have meaningful influence over this thermal parameter of wood.

CONCLUSIONS

In the present work, the synthesis of several coating formulations by means of biobased phenolic resins was accomplished for the protection of wood against fire hazards. On the one side, it was seen that the resins displayed low values of the non-volatile content and viscosity, which would facilitate their application onto the wood surface.On the other side, the assessment of the coating structure highlighted the appearance of new bands associated to the reaction of the different components of the resins. Besides, the formulation of the coatings with inorganic nanoparticles displayed an enhanced thermal performance as shown by the TGA analysis. Concerning the protective effect of the biobased coating towards wood, it was observed that a reduction of the heat release during combustion was achieved. The biobased coatings also provided a protective effect respecting the integrity of the wood bulk (higher residue remaining after combustion). Moreover, they reduced significantly the flame propagation through the wood samples. The previous behaviors results were improved more significantly in the beech wood samples compared to the maritime pine ones. Furthermore, the biobased coatings with the inorganic nanoparticles (RA and RB) displayed a better performance compared to the Reference formulation. It was also seen that the application of the coatings over the wood surface did not substantially modify thermal parameters of wood, such as the conductivity and diffusivity. The other important remark of this work was that the results achieved by the biobased coatings, respecting the protection of wood against fire, were comparable to those of two top rank fireproofing commercial coating formulations (B77 and Quidedur). This is of considerable relevance, since it opens the way to the fabrication of a protective fireproofing product for wood, which is based on renewable compounds and more environmentally friendly.

REFERENCES

(1) 	de la Roche, I.; Dangerfield, J. A.; Karacabeyli, E. Wood Products And Sustainable Construction. New Zel.  Timber Des. J. 2003, 12 (1), 9–13.

(2) 	Woodard, A. C.; Milner, H. R. Sustainability of Timber and Wood in Construction. In Sustainability of Construction Materials; Woodhead Publishing, 2016; pp 129–157.

(3) 	Popescu, C.; Pfriem, A. Treatments and Modification to Improve the Reaction to Fire of Wood and Wood Based products—An Overview. Fire Mater. 2020, 44 (1), 100–111.

(4) 	Shaw, S. Halogenated Flame Retardants: Do the Fire Safety Benefits Justify the Risks? Rev. Environ. Health 2010, 25 (4), 261–306.

(5) 	Shen, K. K. Review of Recent Advances on the Use of Boron-Based Flame Retardants. In Polymer Green Flame Retardants; Elsevier Inc., 2014; pp 367–388.

(6) 	Laoutid, F.; Bonnaud, L.; Alexandre, M.; Lopez-Cuesta, J.-M.; Dubois, P. New Prospects in Flame Retardant Polymer Materials: From Fundamentals to Nanocomposites. Mater. Sci. Eng. R Reports 2009, 63 (3), 100–125.

(7) 	Song, R.; Wang, Z.; Meng, X.; Zhang, B.; Tang, T. Influences of Catalysis and Dispersion of Organically Modified Montmorillonite on Flame Retardancy of Polypropylene Nanocomposites. J. Appl. Polym. Sci. 2007, 106 (5), 3488–3494.

(8) 	Kashiwagi, T.; Gilman, J. Silicon Based Flame Retardants. In  Fire retardancy of polymeric materials; Marcel Dekker Inc.: New York, 2000; pp 353–389.

(9) 	Ayandele, E.; Sarkar, B.; Alexandridis, P. Polyhedral Oligomeric Silsesquioxane (POSS)-Containing Polymer Nanocomposites. Nanomaterials 2012, 2 (4), 445–475.

(10) 	Kuo, S.-W.; Chang, F.-C. POSS Related Polymer Nanocomposites. Prog. Polym. Sci. 2011, 36 (12), 1649–1696.

(11) 	Tang, S.; Wachtendorf, V.; Klack, P.; Qian, L.; Dong, Y.; Schartel, B. Enhanced Flame-Retardant Effect of a Montmorillonite/phosphaphenanthrene Compound in an Epoxy Thermoset. RSC Adv. 2017, 7 (2), 720–728.

(12) 	El-Sheikhy, R.; Al-Shamrani, M. On the Processing and Properties of Clay/Polymer Nanocomposites CPNC. Lat. Am. J. Solids Struct. 2015, 12 (2), 385–419.

(13) 	Nazir, M. S.; Mohamad Kassim, M. H.; Mohapatra, L.; Gilani, M. A.; Raza, M. R.; Majeed, K. Characteristic Properties of Nanoclays and Characterization of Nanoparticulates and Nanocomposites. In Nanoclay Reinforced Polymer Composites; Springer, Singapore, 2016; pp 35–55.

(14) 	Giudice, C. A.; Pereyra, A. M. Silica Nanoparticles in High Silica/alkali Molar Ratio Solutions as Fire-Retardant Impregnants for Woods. Fire Mater. 2009, 34 (4), n/a-n/a.

(15) 	Fu, S.; Song, P.; Liu, X. Thermal and Flame Retardancy Properties of Thermoplastics/natural Fiber Biocomposites. In Advanced High Strength Natural Fibre Composites in Construction; Elsevier Inc., 2017; pp 479–508.

(16) 	Ali, S. W.; Basak, S.; Shukla, A. Nanoparticles: A Potential Alternative to Classical Fire Retardants for Textile Substrates. In Handbook of Nanomaterials for Manufacturing Applications; Elsevier, 2020; pp 265–278.

(17) 	Kausar, A. Flame Retardant Potential of Clay Nanoparticles. In Clay Nanoparticles; Elsevier, 2020; pp 169–184.

(18) 	Li, P.; Zhang, Y.; Zuo, Y.; Lu, J.; Yuan, G.; Wu, Y. Preparation and Characterization of Sodium Silicate Impregnated Chinese Fir Wood with High Strength, Water Resistance, Flame Retardant and Smoke Suppression. Journal of Materials Research and Technology. Elsevier Editora Ltda January 1, 2020, pp 1043–1053.

(19) 	Huang, Y.; Ma, T.; Wang, Q.; Guo, C. Synthesis of Biobased Flame-Retardant Carboxylic Acid Curing Agent and Application in Wood Surface Coating. ACS Sustain. Chem. Eng. 2019, 7 (17), 14727–14738.

(20) 	Beh, J. H.; Yew, M. C.; Yew, M. K.; Saw, L. H. Fire Protection Performance and Thermal Behavior of Thin Film Intumescent Coating. Coatings 2019, 9 (8), 483.

(21) 	Qu, H.; Wu, W.; Zheng, Y.; Xie, J.; Xu, J. Synergistic Effects of Inorganic Tin Compounds and Sb2O3 on Thermal Properties and Flame Retardancy of Flexible Poly(vinyl Chloride). Fire Saf. J. 2011, 46 (7), 462–467.

(22) 	Prieto, J.; Kiene, J. Wood Coatings : Chemistry and Practice; European Coatings, 2018.

(23) 	Zauer, M.; Pfriem, A.; Wagenführ, A. Toward Improved Understanding of the Cell-Wall Density and Porosity of Wood Determined by Gas Pycnometry. Wood Sci. Technol. 2013, 47 (6), 1197–1211.

(24) 	Bulian, F.; Graystone, J. Wood Coatings : Theory and Practice; Elsevier Science, 2009.

(25) 	Langille, K. B.; Nguyen, D.; Bernt, J. O.; Veinot, D. E.; Murthy, M. K. Constitution and Properties of Phosphosilicate Coatings - Part I Influence of Sodium Phosphates on the Constitution of Sodium Silicate Coatings. J. Mater. Sci. 1993, 28 (15), 4175–4182.

(26) 	White, R. H.; Dietenberger, M. A. Fire Safety of Wood Construction. In Wood handbook: wood as an engineering material; US Dept. of Agriculture, Forest Service, Forest Products Laboratory, 2010; p 18.1-18.22.

(27) 	Weil, E. D. Fire-Protective and Flame-Retardant Coatings - A State-of-the-Art Review. J. Fire Sci. 2011, 29 (3), 259–296.

(28) 	Nelson, T. J.; Masaki, B.; Morseth, Z.; Webster, D. C. Highly Functional Biobased Polyols and Their Use in Melamine-Formaldehyde Coatings. J. Coatings Technol. Res. 2013, 10 (6), 757–767.

(29) 	Jimenez, M.; Duquesne, S.; Bourbigot, S. Characterization of the Performance of an Intumescent Fire Protective Coating. Surf. Coatings Technol. 2006, 201 (3–4), 979–987.

(30) 	Streitberger, H. J.; Goldschmidt, A. BASF Handbook Basics of Coating Technology, 3rd ed.; European Coatings, 2018.

(31) 	Sagar, S.; Iqbal, N.; Maqsood, A.; Javaid, U. Thermogravimetric, Differential Scanning Calorimetric and Experimental Thermal Transport Study of MWCNT/NBR Nanocomposites. J. Therm. Anal. Calorim. 2013, 114 (1), 161–167.

(32) 	Liu, R.; Wang, X. Synthesis, Characterization, Thermal Properties and Flame Retardancy of a Novel Nonflammable Phosphazene-Based Epoxy Resin. Polym. Degrad. Stab. 2009, 94 (4), 617–624.

(33) 	Hassan, M. A.; Kozlowski, R.; Obidzinski, B. New Fire-Protective Intumescent Coatings for Wood. J. Appl. Polym. Sci. 2008, 110 (1), 83–90.

(34) 	Pan, Y.; Pan, H.; Yuan, B.; Hong, N.; Zhan, J.; Wang, B.; Song, L.; Hu, Y. Construction of Organic-Inorganic Hybrid Nano-Coatings Containing α-Zirconium Phosphate with High Efficiency for Reducing Fire Hazards of Flexible Polyurethane Foam. Mater. Chem. Phys. 2015, 163, 107–115.

(35) 	Pas’ko, Y. V.; Machneva, O. P. A Technology for Producing Low-Toxicity Phenol—Formaldehyde Resins. Polym. Sci. - Ser. D 2019, 12 (3), 283–285.

(36) 	Younesi-Kordkheili, H.; Kazemi-Najafi, S.; Eshkiki, R. B.; Pizzi, A. Improving Urea Formaldehyde Resin Properties by Glyoxalated Soda Bagasse Lignin. Eur. J. Wood Wood Prod. 2015, 73 (1), 77–85.

(37) 	Koumba-Yoya, G.; Stevanovic, T. Study of Organosolv Lignins as Adhesives in Wood Panel Production. Polymers (Basel). 2017, 9 (12), 46.

(38) 	Pizzi, A. Biosourced Thermosets for Lignocellulosic Composites. In Thermoset Composites; Khan, A., Bhawani, S. A., Asiri, A. M., Khan, I., Eds.; Materials Research Foundation, 2018; pp 81–111.

(39) 	Li, C.; Zhang, J.; Yi, Z.; Yang, H.; Zhao, B.; Zhang, W.; Li, J. Preparation and Characterization of a Novel Environmentally Friendly Phenol-Formaldehyde Adhesive Modified with Tannin and Urea. Int. J. Adhes. Adhes. 2016, 66, 26–32.

(40) 	Shrotri, A.; Kobayashi, H.; Fukuoka, A. Catalytic Conversion of Structural Carbohydrates and Lignin to Chemicals. In Advances in Catalysis; Academic Press Inc., 2017; Vol. 60, pp 59–123.

(41) 	Laurichesse, S.; Avérous, L. Chemical Modification of Lignins: Towards Biobased Polymers. Prog. Polym. Sci. 2014, 39 (7), 1266–1290.

(42) 	Bele, A. A.; Jadhav, V. M.; Kadam, V. J. Potential of Tannnins: A Review. Asian J. Plant Sci. 2010, 9 (4), 209–214.

(43) 	Pizzi, A. Natural Phenolic Adhesives I: Tannin. In Handbook of Adhesive Technology, Revised and Expanded; Pizzi, A., Mittal, K. L., Eds.; CRC Press, 2003; pp 567–581.

(44) 	Faris, A. H.; Rahim, A. A.; Ibrahim, M. N. M.; Alkurdi, A. M.; Shah, I. Combination of Lignin Polyol-Tannin Adhesives and Polyethylenimine for the Preparation of Green Water-Resistant Adhesives. J. Appl. Polym. Sci. 2016, 133 (43437), 1–6.

(45) 	Lei, H.; Pizzi, A.; Du, G. Environmentally Friendly Mixed Tannin/lignin Wood Resins. J. Appl. Polym. Sci. 2008, 107 (1), 203–209.

(46) 	Mansouri, H. R.; Navarrete, P.; Pizzi, A.; Tapin-Lingua, S.; Benjelloun-Mlayah, B.; Pasch, H.; Rigolet, S. Synthetic-Resin-Free Wood Panel Adhesives from Mixed Low Molecular Mass Lignin and Tannin. Eur. J. Wood Wood Prod. 2011, 69 (2), 221–229.

(47) 	Chupin, L.; Charrier, B.; Pizzi, A.; Perdomo, A.; Charrier-El Bouhtoury, F. Study of Thermal Durability Properties of Tannin–lignosulfonate Adhesives. J. Therm. Anal. Calorim. 2015, 119 (3), 1577–1585.

(48) 	de Hoyos-Martínez, P. L.; Robles, E.; Khoukh, A.; Charrier-El Bouhtoury, F.; Labidi, J. Formulation of Multifunctional Materials Based on the Reaction of Glyoxalated Lignins and a Nanoclay/Nanosilicate. Biomacromolecules 2019, 20 (9), 3535–3546.

(49) 	Yazaki, Y.; Hillis, W. E. Molecular Size Distribution of Radiate Pine Bark Extracts and Its Effect on Properties. Holtzforschung 1998, 34, 125–130.

(50) 	Shahid, S. A.; Ali, M.; Zafar, Z. I. Characterization of Phenol-Formaldehyde Resins Modified with Crude Bio-Oil Prepared from Ziziphus Mauritiana Endocarps. BioResources 2014, 9 (3), 5362–5384.

(51) 	Çetin, N. S.; Özmen, N. Studies on Lignin-Based Adhesives for Particleboard Panels. Turkish J. Agric. Technol. 2003, 27, 183–189.

(52) 	Younesi-Kordkheili, H. Ionic Liquid Modified Lignin-Phenol-Glyoxal Resin: A Green Alternative Resin for Production of Particleboards. J. Adhes. 2018, 1–13.

(53) 	Lin, R.; Sun, J.; Yue, C.; Wang, X.; Tu, D.; Gao, Z. Study on Preparation and Properties of Phenol-Formaldehyde-Chinese Fir Liquefaction Copolymer Resin. Maderas. Cienc. y Tecnol. 2014, 16 (2), 159–174.

(54) 	Chaouch, M.; Diouf, P. N.; Laghdir, A.; Yin, S. Bio-Oil from Whole-Tree Feedstock in Resol-Type Phenolic Resins. J. Appl. Polym. Sci. 2014, 131 (40014), 1–6.

(55) 	Siddiqui, H.; Mahmood, N.; Yuan, Z.; Crapulli, F.; Dessbesell, L.; Rizkalla, A.; Ray, A.; Xu, C. (Charles). Sustainable Bio-Based Phenol-Formaldehyde Resoles Using Hydrolytically Depolymerized Kraft Lignin. Molecules 2017, 22 (11), 1850.

(56) 	Ammar, M.; Khiari, R.; Belgacem, M. N.; Elaloui, E. Thermal Characterization and Comparisons of Lignin-Formaldehyde and Lignin-Glyoxal Adhesives. Mediterr. J. Chem. 2014, 2 (6), 731–737.

(57) 	De Meijer, M.; Thurich, K.; Militz, H. Comparative Study on Penetration Characteristics of Modern Wood Coatings. Wood Sci. Technol. 1998, 32 (5), 347–365.

(58) 	Pizzi, A. Wood Products and Green Chemistry. Ann. For. Sci. Springer Verlag 2016, 73 (1), 185–23.

(59) 	Karunanayake, L.; Sumathirathne, L. Synthesis of Novel Porous Tannin-Phenol-Formaldehyde Cation Exchange Resin from Terminalia Arjuna (Kumbuk). J. Natl. Sci. Found. Sri Lanka 2017, 45 (3), 219–227.

(60) 	Brebu, M.; Vasile, C. Thermal Degradation of Lignin—a Review. Cellul. Chem. Technol. 2010, 44 (9), 353.

(61) 	Liu, Y.; Wang, J.-S.; Deng, C.-L.; Wang, D.-Y.; Song, Y.-P.; Wang, Y.-Z. The Synergistic Flame-Retardant Effect of O-MMT on the Intumescent Flame-Retardant PP/CA/APP Systems. Polym. Adv. Technol. 2010, 21 (11), 789–796.

(62) 	Rezakazemi, M.; Vatani, A.; Mohammadi, T. Synergistic Interactions between POSS and Fumed Silica and Their Effect on the Properties of Crosslinked PDMS Nanocomposite Membranes. RSC Adv. 2015, 5 (100), 82460–82470.

(63) 	De Meijer, M. A Review of Interfacial Aspects in Wood Coatings: Wetting, Surface Energy, Substrate Penetration and Adhesion. In COST E18 Final Seminar: High performance wood coatings; 2005; p 16.

(64) 	Kennedy, R. W. An Outlook for Basic Wood Anatomy Research . Wood Fiber Sci. 2007, 2 (3), 182–187.

(65) 	dos Santos Viana, H. F.; Rodrigues, A. M.; Godina, R.; Matias, J. C. de O.; Nunes, L. J. R. Evaluation of the Physical, Chemical and Thermal Properties of Portuguese Maritime Pine Biomass. Sustainability 2018, 10 (8), 1–15.

(66) 	White, R. H. Effect of the Lignin Content and Extractives on the Higher Heating Value of Wood. Wood Fiber Sci. 1983, 19 (4), 446–452.

(67) 	Demirbas, A. Relationships Between Heating Value and Lignin, Moisture, Ash and Extractive Contents of Biomass Fuels. Energy Exploration & Exploitation. Sage Publications, Ltd. 2002, pp 105–111.

(68) 	Griu, T.; Lunguleasa, A. The Use of the White Poplar (Populus Alba L.) Biomass as Fuel. J. For. Res. 2016, 27 (3), 719–725.

(69) 	Rodríguez-García, A.; Martín, J. A.; López, R.; Sanz, A.; Gil, L. Effect of Four Tapping Methods on Anatomical Traits and Resin Yield in Maritime Pine (Pinus Pinaster Ait.). Ind. Crops Prod. 2016, 86, 143–154.

(70) 	Demirbas, A. Higher Heating Values of Lignin Types from Wood and Non-Wood Lignocellulosic Biomasses. Energy Sources, Part A Recover. Util. Environ. Eff. 2017, 39 (6), 592–598.

(71) 	Telmo, C.; Lousada, J. The Explained Variation by Lignin and Extractive Contents on Higher Heating Value of Wood. Biomass and Bioenergy 2011, 35 (5), 1663–1667.

ACKNOWLEDGMENTS

The authors would like to thank to the University of the Basque Country UPV/EHU and the University of Pau and Pays de l’Adour UPPA (Predoctoral fellowship-PIFPAU15/01) for financially supporting this work. Furthermore, we would like to thank TANAC S.A for kindly providing the tannin extracts, Hybrid Plastic Inc. (USA) and Laviosa Advance Mineral Solutions (Italy) for kindly providing the nanosilicate and nanoclay respectively. On the other hand, we would also like to acknowledge the companies of the varnish and coating industry, BASMODEC (Gipuzkoa) and NAILAN Parquets-Barnices (Bizkaia) for providing us with the commercial formulation of the fireproofing coatings.

SUPPORTING INFORMATION

Appendix A: Substrate and Parameters set for the application of the coating.

Appendix A1: Properties of wood substrates used

- Table A1. Differences concerning the anatomy and intrinsic porperties of the wood species selected in this work

Appendix A2: Parameters set for the coating application

- Figure A1: Evolution of the weight percentage gain (WPG) of the coated samples after the addition of different amounts of resin.

Appendix B: Analyses for assessing the fireproofing properties of the coating (methods description)

Appendix B1: Analysis of the heat release during combustion

Appendix B2: Analysis of the heat transfer after the application of the coating

Appendix C: Characterization of the coatings

Appendix C1: Fourier transformed Infrared Spectroscopy Analysis (FTIR)

- Table C1: List of assignments of the main signals detected in the spectra of the cured resins and their components

Appendix C2: Thermogravimetric Analysis (TGA)

- Figure C1. Thermogravimetric and derivative thermogravimetric curves of the resins compared to their raw material: a) Reference resin, LMP: maritime pine lignin, LF: lignin functionalized (glyoxalated), MT: mimosa tannin; b) Resin formulation RA, LMP: maritime pine lignin, LFA: lignin functionalized (glyoxalated+hybridized with montmorillonite), MT: mimosa tannin and c) Resin formulation RB, LMP: maritime pine lignin, LFB: lignin functionalized (glyoxalated+hybridized with POSS), MT: mimosa tannin

Appendix D: Assessment of the performance of the coatings

Appendix D1: Analysis of the combustibility of the wood samples

- Table D1: Capacity of the coatings for reducing the combustibility of the wood samples.

Appendix D2: Analysis of the heat transfer properties of the coatings

- Table D2: Results of Bonferroni test for the comparison between the means of the different types of samples.

- Table D3: Results of the overall ANOVA test

FOR TABLE OF CONTENTS USE ONLY

SYNOPSIS:

Formulations of biobased phenolic resins based on lignin, tannins and inorganic nanoparticles were successfully applied as fireproofing coatings for wood