## Slide 1: Metal-Organic Frameworks polymeric composites for environmental remediation
A. Valverde, G. I. Tovar Jimenez, J. Perez Bravo, A. Fidalgo-Marijuan, L. Lezama, S. Lanceros-Méndez, G. Copello and R. Fernández de Luis
INDESMOF - MSCA/RISE

## Slide 2: Scope 1.- INDESMOF Project Aims 2.- Active Metal-Organic Frameworks modification 3.- MOF/Polymeric membranes for water remediation 4.- Acknowledgements

## Slide 3: Scope 1.- INDESMOF Project Aims 2.- Active Metal-Organic Frameworks modification 3.- MOF/Polymeric membranes for water remediation 4.- Acknowledgements
Notes: Hello, I will talk about Energy storage materials and devices that is one of the ongoing projects between BCMaterials and the University of the Basque Country, specifically with a research group of the inorganic chemistry department of which Idoia Ruiz de Larramendi is a member.

## Slide 4
Core Scientific Proposal of the Project
Arsenic Water Pollution
Hg Soil Pollution
Pb Soil Pollution

## Slide 5
Core Scientific Proposal of the Project

## Slide 6: Scope 1.- INDESMOF Project Aims 2.- Active Metal-Organic Frameworks modification 3.- MOF/Polymeric membranes for water remediation 4.- Acknowledgements
Notes: Hello, I will talk about Energy storage materials and devices that is one of the ongoing projects between BCMaterials and the University of the Basque Country, specifically with a research group of the inorganic chemistry department of which Idoia Ruiz de Larramendi is a member.

## Slide 7
Adsorption
Metal-Organic Frameworks chemical versatility

## Slide 8
Adsorption
Metal-Organic Frameworks chemical versatility

## Slide 9
Photo-catalysis

## Slide 10
Photo-catalysis

## Slide 11: Scope 1.- INDESMOF Project Aims 2.- Active Metal-Organic Frameworks modification 3.- MOF/Polymeric membranes for water remediation 4.- Acknowledgements
Notes: Hello, I will talk about Energy storage materials and devices that is one of the ongoing projects between BCMaterials and the University of the Basque Country, specifically with a research group of the inorganic chemistry department of which Idoia Ruiz de Larramendi is a member.

## Slide 12
Polymer and Metal-Organic Frameworks composites:
Are the characteristics and functions of their components retained?
Armstrong-Scale
Nano-Scale
Nano-Micro Scale
Macro Scale
Processing

## Slide 13
Polymer and Metal-Organic Frameworks composites:
Are the characteristics and functions of their components retained?
MOF-808
 Sorbent
Chitin

## Slide 14
Processing of CHITIN/MOF-808 composites
Wet-spinning
Freeze Drying
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 15
Corroboration of the MOF incorporation
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 16
Modulation of the pore-structure
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 17
Interaction of MOF nanoparticles and CHITIN Matrix
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 18
Synergic effects on CH/MOF-808 composites
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 19
Synergic effects on CH/MOF-808 composites
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 20
Polymer and Metal-Organic Frameworks composites:
Are the characteristics and functions of their components retained?
MIL-125-NH2
Photocatalyst
Chitin
Trimethoprim
Adsorption
Photo degradation
Mineralization

## Slide 21
Corroboration of the MOF incorporation
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 22
Modulation of the pore-structure
CH
CH-MIL-1%
CH-MIL-5%
CH-MIL-10%
Notes: Nowadays, energy storage systems are necessary to supply energy and power in portable electronic devices and electrical vehicles, among others. In particular, considering the advances in electronic miniaturization, there is a demand for smaller and lighter batteries with enhanced performance.
LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 23
Performance of the active material and CH/MOF composite
Notes: LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 24
Performance of the active material and CH/MOF composite
Notes: LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 25
Performance of the active material and CH/MOF composite
Notes: LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 26
Performance of the active material and CH/MOF composite
Notes: LIBs are build-up by positive and negative electrode components, which are electronically isolated by a porous polymeric separator wetted in liquid electrolyte 4. Until recently, the research community has paid less attention to the characteristics of the separators, considering them as passive elements of LIBs. Nevertheless, it has been duly demonstrated that the separator is an essential active barrier that strongly affects the fast, reversible and long-term stable ionic transport in LIBs during operation

## Slide 27
Conclusions and future perspectives
Blending Metal-Organic Frameworks and Polymeric systems enables merging the functionalities of both systems.
The MOF nanoparticles act as a modulator of the macro-mesoporous structure of the polymeric host, especially at the nanometer scale regime.
The pore space compartmentalization impact as well the adsorption capacity of intermediate-sized molecules by the composite filters.
The chitin matrix protect the MIL-125-NH2 from a partial degradation during the reactivation process of the sorbent/photocatalysts.

## Slide 28
Acknowledgements
The European Commission Research & Innovation H2020-MSCA-RISE-2017 (Ref.: 778412) INDESMOF project is also acknowledged.
The Basque Government under the ELKARTEK, HAZITEK and PIBA programs. A.V. thanks to the Basque Government Education department for her predoctoral grant.
Spanish Ministry of Economy and Competitiveness (ERAMIN-TAILING43GREEN, AEI/FEDER, UE: PID2020–15935RB-C42).

## Slide 29
Thank you!!!