Functional carbon nitride materials – design strategies for electrochemical devices.

Fabian K. Kessler1, Yun Zheng2, Dana Schwarz3, Christoph Merschjann4, Wolfgang Schnick1, Xinchen Wang2 and Michael J. Bojdys3,5

1 Department of Chemistry, University of Munich (LMU), Butenandtstraße 5−13, 81377 Munich, Germany.

2 State Key Laboratory of Photocatalysis on Energy and Environment, College of Chemistry, Fuzhou University, Fuzhou 350002, P. R. China.

3 Charles University in Prague, Faculty of Science, Department of Organic Chemistry, Hlavova 8, 128 43 Prague 2, Czech Republic.

4 Fachbereich Physik, Freie Universität Berlin, Arnimallee 14, 14195 Berlin , Germany.

5 Institute of Organic Chemistry and Biochemistry ASCR, v.v.i., Flemingovo nám. 2, 166 10 Prague 6, Czech Republic

Abstract | Carbon nitrides have been in the spotlight of the material science community over the last decade as metal-free semiconductors and promising materials for metal-free photocatalysis. This has caused a paradigm shift in the quest for artificial photosynthesis away from simple, inorganic semiconductors to more abundant, polymeric ones. Melon – a somewhat neglected polymer – and related carbon nitride materials represent desirable alternatives to industrially used catalysts since they are easily synthesised and can be obtained from abundant and inexpensive starting materials. Furthermore they are chemically benign since they contain no heavy metal ions, thereby facilitating handling and disposal. The chemistry of carbon nitrides dates back to the 19th century, yet it can still help us to consolidate the largely intuitive, empirical design-strategies that dominate the field. We look at structure-properties relationships for this material class, and showcase some exciting applications that are leading towards overall photocatalytic water-splitting and to “post silicon” electronics.

Materials research and development is propelled by a continuous rise in demand for clean energy and innovations in the digital economy1. For example, Europe is home to the world’s largest independent segments in semiconductor design industry, employing, directly or indirectly, around 250,000 people in 11,500 companies alone in the UK2. The importance of the energy and electronics sectors poses two challenges world-wide: (1) In the context of materials security, almost all modern electronics devices depend on small, yet indispensable quantities of critical raw materials (CRMs). (2) Manufacturing processes (that is, refinement of Si) require substantial amounts of energy. These two points become noteworthy even more so, given that as of 2015, the number of mobile phone subscriptions outstrips the number of people on earth3.

One further challenge for modern society arises in the context of energy security. A highly sought-after alternative for finite fossil fuels is direct water splitting using a semiconductor photocatalyst with visible light to produce hydrogen, thus converting sunlight into storable and transportable energy. Here, the position of the energy level of H+ to H2 reduction and the energy level of H2O to O2 oxidation should ideally be situated within the band gap of the photocatalyst, and the valence and the conduction states are required to have a different character (that is, location of the red-/ox-sites). This is to prevent the immediate recombination of electrons and holes, as well as hydrogen and oxygen to water. In addition, the band gap of the material should be in the region of the energy of visible light (1.2–3.0 eV). Hence, the challenges of materials and energy security revolve around the discovery of alternative semiconductors that are ideally produced in less energy-intensive ways, and that do not require critical raw materials (CRMs) or complicated post-synthetic modifications to tune electronic properties, such as the electronic band gap.

One such material that has been considered as a candidate for “post-silicon electronics” due to its advantageous combination of high electrical and thermal conductivity and stability is graphene. However, the (half-)metallic character of graphene and the resulting absence of an electronic band gap have frustrated the development of a graphene-based electronic switch. Strategies to widen graphene’s band gap revolve around post-synthetic deletions and insertions of heteroatoms4 – all these methods however are top-down, and very difficult to control with the tools of chemistry. In this review, we do away with mere modifications of graphene and present an overview of bottom-up synthetic approaches towards organic semiconductors using heteroatom-containing precursors. The design principles for these C/N/H-containing solids were laid out about 25 years ago when Liu and Cohen postulated that carbon(IV) nitrides – structurally analogous to carbon-only structures like diamond and graphite – should exist5. This sparked a plethora of attempts to synthesise carbon nitrides as well as numerous theoretical studies, continuously feeding into a body of now more than 6000 papers. Here, we will critically evaluate reports on synthetic approaches6, which later turned out to be wrong or based on incomplete analyses. Crystalline carbon nitrides based on s-triazine units are highlighted, as they go beyond the well-known amorphous carbon and nitrogen containing polymers7. These ordered solids are remarkable not only because of the many unsuccessful studies but more so due to the (predicted) properties and applications, and the close relation to graphene. On the polymer side, (C, N)-based materials like melon are examined owing to their highly interesting semiconducting and (photo)catalytic properties8. Using bottom-up modification of the same material class, overall water-splitting was achieved, paving the way towards a potentially clean and renewable source for hydrogen fuel. Finally, we present a realistic outlook on material performance in photocatalysis and semiconductor electronics based on the structure-properties relationships of the above-mentioned systems.

Supramolecular synthons and crystal engineering of carbon nitride materials

Melamine, Melam and Melem. The structures of all known carbon nitride materials as well as some hypothetically feasible ones are based on one of two characteristic building blocks: the triazine (1,3,5-triazine, C3N3) and the heptazine (1,3,4,6,7,9,9b-heptaazaphenalene, C6N7) core11. Both are aromatic ring systems with an alternating arrangement of C- and N-atoms. Triazine- and heptazine-based molecular compounds are important precursors and side-products in the synthesis of higher molecular weight polymers and solids (Figure 1). The most prominent of these compounds is melamine; it was named arbitrarily by 19th century chemist Justus von Liebig12, and it remains of industrial relevance as a cheap precursor for thermoset plastics13-15 and flame retardants.

Figure 1 | Synthons and networks. Overview of synthetic pathways from C- and N-containing molecules to extended carbon nitride materials (top), and the associated, thermally triggered condensation processes of cyanamide in the absence of a solvent as seen in differential scanning calorimetry (bottom). Steps include melting of cyanamide (1), reaction of cyanamide to dicyandiamide (2), melting of dicyandiamide (3), reaction of dicyandiamide to melamine (4), sublimation of melamine (5), condensation to melam (6), formation of melem (7), and finally, formation of melon (8). On the right-hand side, the only existing layered, crystalline carbon nitride materials to date: poly(heptazine imide) (PHI), poly(triazine imide) (PTI), and triazine based graphitic carbon nitride. The bottom panel is adapted with permission from Wiley-VCH7.

Heating melamine to temperatures of 317 °C and above induces a cascade of condensation reactions accompanied by the evolution of ammonia18. Initially, melamine forms a dimer called “melam” ([(H2N)2(C3N3)]2NH)19 that rapidly reacts to a heptazine-based compound called “melem”, (triamino-tri-s-triazine, triamino-heptazine, C6N7(NH2)3) at temperatures above 360 °C. Different mechanisms have been proposed for this interconversion. A conceivable explanation is that melem is formed from the reaction of melamine with residual cyanamide. This is supported by the finding of melamine-melem adduct phases, and it suggests that all three compounds co-exist at certain temperatures24. Bulk assemblies of melem and melam are dominated by π-π-interactions between these disk-shaped molecules18 and strong lateral hydrogen bridges lead to ordered molecular crystals25.

Melon. Melem condenses to 1D chains of amine-linked heptazine units at temperature above 520 °C. This poly(aminoimino heptazine) has the formula [C6N7(NH2)(NH)]n and is known as Liebig’s melon26. These poly-heptazines are often (and misleadingly) classed together as “graphitic carbon nitride” (g-C3N4) in literature, although polymeric carbon nitride (PCN) is becoming more widely used, and it is a more useful term (see Box 1). Melon exhibits a characteristic bright yellow color and an optical band gap of 2.7 eV8 which makes it stand out from other carbon nitride type materials (see Table 1). The structure of melon shows some characteristic features; individual polymer strands align in a zigzag-fashion via hydrogen bonding between the ring nitrogens of one strand and NH or NH2 groups of an adjacent strand. Perpendicular π-π stacking of these hydrogen-bonded layers is less directional. Heptazine rings from one galery eclipse the next layer27. Historically, melon has been often referred to as “graphitic CN”, “graphitic carbon nitride” or “g-C3N4” mainly so, because the powder X-ray diffraction pattern of melon seems to show a pseudo-graphitic peak. This is deceptive nomenclature, however, as the observed π-π stacking of melon’s heptazine-subunits is shared by all flat, aromatic molecules, as small as napthalene (see Box 1). For reasons of clarity we therefore strongly recommed to refer to melon either by its non-systematic name or alternatively as poly(aminoimino heptazine) or as polymeric carbon nitride (PCN)8. Clarifying nomenclature might be considered moot, however, in instances where exfoliation of allegedly “graphitic” carbon nitrides is attempted28, it is not only π-π stacking but also hydrogen-bonding that is disrupted in chemical and physical treatment of PCNs.

Poly(heptazine imide) and poly(triazine imide). Melon is thermally stable up to temperatures between 650 and 700 °C and does not undergo further condensation reactions at higher temperatures, even though it retains one NH2 group per repeat unit that could undergo further elimination of ammonia. Instead, melon decomposes at these temperatures.

One report combines high temperatures of 630 °C and autogenous ammonia pressure, to drive melon condensation one step further towards a 2D extended network29. The resulting product of these harsh reaction conditions is poly(heptazine imide) (PHI) (see Figure 1). PHI is a minority phase next to the bulk product melon, and it is comprised of rings of six heptazine units that are each linked by NH-bridges. The linking pattern gives rise to triangular holes, large enough to host at its centre an isolated melamine molecule closely coordinated via hydrogen bonds.

The example of PHI demonstrates that mere thermal treatment of C- and N-containing monomers and oligomers stops short of full condensation and deamination once melon aggregates of a certain size are achieved. This is thought to be a kinetic problem that can be addressed by the addition of a solvent that provides more mobility for reactants and in some cases also acts as a template that facilitates optimal self-assembly into the desired, layered structures. Note that selecting a suitable solvent is not trivial since the temperature range for poly-condensation reactions of melamine is between 350 and 600 °C far beyond any common organic solvent and out of reach of even the most stable ionic liquids. Salt melts – either as single-component, or as binary or ternary eutectics – can alleviate this problem, and indeed organic synthesis of molecular nitrides, carbides, cyanides, cyanates, and thiocyanates was successfully performed in a wide range of these inorganic solvents31-35. Later, this idea was extended to the synthesis of covalently bonded, triazine-based frameworks36-40.

Box 1 | Polymeric carbon nitride at a glance

The yellow to orange coloured powder obtained from the pyrolysis of urea, thiourea, cyanamide, dicyandiamide, melamine and other CN-containing, molecular compounds at temperatures above 525 °C is not “graphitic carbon nitride” or “g-C3N4” but a polymeric carbon nitride called “melon” – a name coined by Justus von Liebig in 1834. Melon is “graphitic” only insofar that it features discernible basal planes that, however, are held together by hydrogen bonding between individual strands of the 1D polymers that make them up and not by covalent bonds like graphite. Likewise, the chemical composition of melon deviates from C3N4: it is usually closer to C6H3N9 with a substantial hydrogen content of 1.5 wt% or more. The fingerprint features of melon that can be discerned in X-ray diffraction experiments (c) are the in-plane repeats between heptazine (C6N7) units (indicated with * in a) and the π-π stacking motif of the very same heptazines on top of each other (indicated with # in b). The infrared fingerprint of the material is complex, but it invariably shows strong N-H and N-H2 stretches (3400-3000 cm-1) alongside with the characteristic heptazine breathing mode (~804 cm-1) (d). The here-presented physical data should serve as a sanity-check to facilitate quick identification of melon-type samples and aid in phase identification even in tricky cases: e.g. melon is chemically and physically indistinguishable from Nicanite® that is marketed as a “high purity, graphitic carbon nitride”. Panels c – d are adapted from an internal report with permission from the University of Liverpool30.

Thermal treatment of dicyandiamide in eutectic salt melts such as LiX/KX (X = Cl, Br) yields poly(triazine imide) (PTI), a triazine-based, two-dimensional material with intercalation of Li+ and X-. PTIs feature fully delocalised π-electron systems via imide bridges. Similar to melon, PTI has an optical band gap and hence shows promising performance in photocatalytic applications. Likewise, it is one of very few crystalline carbon nitride materials that can be exfoliated chemically and physically into thin layers and bundles thanks to the strong covalent bonding within individual layers. PTI layers stack in an AB fashion and form 1D pore channels that run through the sheets along the principal c-axis. These channels are lined by Li+ and the respective halogen counter anions that were used in the reaction medium44. Intriguingly, the gallery height of the layered PTI materials can be tuned by intercalation of halogens, and it follows the same trend as the ionic radii of the incorporated guests F < Cl < Br48. Table 1 ¦ UV/Vis absorption edges of CN materials

Compound; Absorption edge; Ref.. Melamine; 235 nm; 41. Melam; 285 nm; 41. Melem; 296 nm; 41. Melon; 460 nm; 8. PTI/Li+Cl-; ~380 nm; 42.

Ionothermal treatment of dicyandiamide has been performed in the presence of metal cations such as Co, Sn, Zn, Cs, and Na49-51. However, in comparison with the binary salt eutectic of LiX and KX (X = F, Cl, Br) variation of the cations does not only change the interlayer stacking, but has a profound influence on the reaction mechanism as a whole. Salt melts of CoCl2/ZnCl2 lead to PTI, while CoCl2/SnCl2 favour the formation of a melon-based product51. One likely reason is the difference in Lewis acidity of Zn- compared to Sn-salts that leads to stabilisation of the C3N3 over the C6N7 core under ionothermal conditions.

Triazine-based graphitic carbon nitride. A recent addition to the exclusive club of “graphitic” compounds is constructed from nitrogen-linked triazine units (C3N3), and thus has been called “triazine-based graphitic carbon nitride” (TGCN)7. This structure was postulated as “graphitic carbon nitride” (shorthand: “g-C3N4”) in analogy to the structurally related graphite. Unlike graphite, it contains an alternating arrangement of covalently-linked, sp2-hybridised carbon and nitrogen atoms (Figure 1). This is accompanied by an opening of the band gap. Indeed, UV-visible measurements and the correlation of DFT and XPS results corroborate that TGCN has a band gap of between 1.6 and 2.0 eV. TGCN is obtained from the condensation of dicyandiamide in the eutectic salt-melt of LiBr/KBr at 600 °C in a quartz glass ampoule. Crystalline TGCN flakes form at the inherent gas-liquid interface in the reaction and also on the surfaces of a quartz glass reactor. Hence, it is surface-mediated synthesis that provides an appropriately confined reaction environment for molecular building blocks and is advantageous in the formation of a strictly 2D layered material. It is noteworthy that with the current reaction set-up overall yields of TGCN are poor (12.6 % yield), and all efforts to remedy that should be geared towards maximizing solid-liquid and liquid-gas interfaces.

No integrated devices based on TGCN semiconductors have been produced, yet. However, since this material grows interfacially, it could in principle be processed directly onto a planar substrate and thus presents interesting new possibilities for post-silicon electronic devices. The synthesis of TGCN is an example of bottom-up design of a 2D layered material, and while inherently challenging, it highlights the required level of sophistication in reaction- and reactor-design.

Carbon nitride photocatalysts

Synthesis and design of C/N/H photocatalysts. With the explosive growth of energy consumption, the development of highly efficient materials and devices for energy conversion and storage is becoming a pertinent challenge. An ubiquitous and obvious source of energy and bulk chemicals for conversion is sunlight and water. Several classes of inorganic semiconductors have been explored but the number of organic and polymeric photocatalysts for water splitting is very small. Recently, polymeric carbon nitrides (PCNs) featured as solar energy transducers for water splitting. The peculiar properties of these carbon nitrides include an optical band gap and hence semiconducting properties, high nitrogen content, outstanding thermal and chemical stability, as well as tuneable texture and structure. In 2009 polymeric carbon nitride was shown to catalyse both half-cell reactions in visible-light driven water splitting8 thanks to its advantageous band structure with an optical band gap of 2.7 eV, and positions of the conduction band (CB) and valence band (VB) at −1.4 and 1.3 eV vs. NHE at pH 7, respectively8. More importantly, PCN catalysed this process on its own without the addition of a noble metal co-catalyst.

The catalytic and electronic performance of pristine melon are relative low because of a fairly small, solvent accessible surface area, low electric conductivity, wide band-gap, high exciton binding energy, and rapid rate of charge-carrier recombination59. Therefore, various synthetic methods and modification techniques are discussed in the following sections to highlight avenues of synthetic and experimental design that seek to improve the catalytic and electronic performances of these carbon nitride materials.

Co-polymerisation and heteroatom doping. Overall π-conjugation of carbon nitride polymers can be tuned and enhanced by anchoring additional, structure-matching organic monomers into the molecular structure of melon. This co-polymerisation method has a pronounced effect on quantifiable properties of the material such as electronic structure, optical absorption, and photocatalytic activity. Suitable aromatic co-monomers can be classified into three organic anchoring groups, including (1) π-conjugated aromatic system such as benzene and its derivatives, (2) π-rich aromatic system such as thiophene and its derivatives, and (3) π-deficient aromatic system for example pyridine- type motifs. Phenylene groups were incorporated into carbon nitrides through co-polymerisation of 2-aminobenzonitrile (ABN) with dicyandiamide. The optical absorption edge red-shifted as ABN content increased from 460 nm for the pristine carbon nitride (CN-ABN0) to 700 nm for CN-ABN0.5. The sample CN-ABN0.05 with Pt co-catalyst shows the best photocatalytic evolution of hydrogen of up to 147 μmol h-1 at λ > 420 nm while the unmodified sample generates only 18 μmol h-1 . In contrast, π-deficient 2,4,6-triaminopyrimidine was also employed as a co-monomer in the co-polymerisation with the aim to introduce more carbon into binding motif of heptazine. This results in an overall decrease of the band gap energy to 2.4 eV.62 The material shows higher photocatalytic activity for the removal of NO gas pollutant62.

To date, there are a number of studies on the doping of anions (e.g., O, C, N, P, S, B, F, and I) and cations (e.g., Fe3+, Co2+, Ni2+, Cu2+, Zn2+, K+, Na+, and Li+) into the frameworks of carbon nitrides63-65. For example, phosphorus-doped, porous carbon nitride nanosheets were obtained from the co-polymerisation of melamine and 2-aminoethylphosphonic acid followed by thermal exfoliation.66 On the basis of density functional theory calculations the intrinsic band gap of P-doped carbon nitrides is decreased from 2.98 eV to 2.66 eV. Introduction of phosphorus into the periodic lattice of carbon nitrides gives rise to empty midgap states that originate from mixing of C 2s2p, N 2s2p, and P 3s3p orbitals and that are situated below the conduction band of melon66. Hence, the empty midgap states can accommodate photo-excited electrons with energies smaller than the band gap of the pristine material (c.f. Urbach tail)66. The as-synthesized phosphorus-doped carbon nitride nanosheets with Pt co-catalyst exhibit a significant improvement in photocatalytic hydrogen evolution under visible-light. Besides that, Fe species were also incorporated into the carbon nitride matrix by complexation forming Fe-N bonds. This is accompanied by a lowering of the band gap, expansion of absorption range across the visible spectrum, and overall improvement of photooxidation activity67. Excessive doping, however, is not favourable for photocatalytic reactivity of carbon nitrides due to the generation of further electron-hole recombination sites and due to potential side reactions that give rise to light-obstructive minority phases.

Sensitisation. Carbon nitride photocatalysts can be further sensitised with a variety of dyes, such as metal phthalocyanines68, Eosin Y, erythrosine B, fluorescein, and dibromofluorescein. The electron transfer cascade in Eosin Y sensitised nanoporous carbon nitride is thought to proceed from excited EY molecules to the carbon nitride catalyst that acts as transducer, eventually finishing at the co-catalyst e.g. Pt metal. Moreover, the increased, solvent accessible surface area and the open, nanoporous structure of the photocatalyst favour attachment of dye molecules and enhance overall mass transfer.

Nanostructure engineering: Physical tuning of photocatalytic properties. Properties of carbon nitride photocatalysts can be tuned by changes in their morphology as well as their makeup. Physical tuning methods play a vital role in modifying nanostructure, morphology, crystallinity, surface access, and electron-hole separation efficiency of carbon nitrides. Optical, electronic, mechanical, magnetic, and chemical properties of carbon nitride materials can be manipulated by changing the size, composition, dimension, and shape of their reactive (nano-)domains. There is an increasing number of these carbon nitride nanomaterials that are being reliably synthesised, and they have shown promising applications in branches of electronics and catalysis. Herein, we review the effects of hard and soft-templating methods, supramolecular pre-organisation of monomers, template-free methods, exfoliation strategies, and heterojunction construction on the photocatalytic performance of carbon nitride based photocatalysts.

Figure 2 | Overview of the different nanostructures of carbon nitride photocatalysts. a| HRTEM image of a PTI nanosheet edge viewed along [001] and simulation (inset)42. b| SEM image of carbon nitride sol thin-films synthesised by sol-processing73. c| TEM image of the carbon nitride nanorods synthesised by solvothermal method74. d| TEM image of carbon nitride nanospheres synthesised by hard-templating76. e| TEM image of a 3D porous carbon nitride monolith obtained via soft-templating by thermal polymerisation of urea in a melamine sponge78. The inset photograph shows that the monoliths supports the structural stress of a 100 g weight.

Hard and soft templating methods. Templating approaches offer a promising strategy to modify the structural and physical properties of semiconductor materials by varying the overall morphology and introducing porosity. Thus, larger guest-accessible surface areas, more active sites and more efficient charge separation can be achieved; all thought to benefit overall photocatalytic activity. Hard-templating is a multi-step process that involves filling a rigid template with a precursor, treatment of that precursor to generate the target material, and the removal of the template to yield a replica. The mesoporous carbon nitride photocatalyst was prepared by the replication of silica nanoparticles (Ludox HS40 with size of 12 nm) with melon obtained through the thermal condensation process of cyanamide precursors. The silica template is etched by NH4HF2 reagent79, and the resulting mesoporous PCN replica shows surface areas ranging from 8 to 373 m2 g-1 depending on the initial ratio of silica/cyanamide ranging from 0 to 1.5 (see Figure 2). Similarly, numerous porous or nanostructured carbon nitrides, including ordered mesoporous graphitic carbon nitride, nanospherical carbon nitride composed of nanosheets, nanorods, nanosheets, and diatom-based carbon nitrides have been prepared80-86. A more facile variation of hard-templating is a sol-gel approach in which silica (TEOS) and a C, N-containing molecular precursor (cyanamide) are simultaneously mixed and thermally condensed. Selective removal of the hard template affords a variety of mesoporous carbon nitrides, one of which outperforms all photocatalysts of this type with a hydrogen evolution rate of 75 µmol h-1 (CN-6).

In comparison, soft-templating offers an alternative, potentially greener route for the engineering of carbon nitride nanostructures. Soft structure-directing agents such as surfactants, amphiphilic block polymers, and ionic liquids are used to introduces porosity into a carbon nitride framework. Boron and fluorine co-doped carbon nitride, as well as phosphorus-doped nanomaterials were obtained using 1-butyl-3-methylimidazolium tetra-fluoroborate ([Bmim][BF4]) and 1-butyl-3-methylimidazolium hexaﬂuorophosphate ([Bmim][PF6]) ionic liquids91-93. The ionic liquids not only act as a reaction medium with reasonably high chemical and thermal stability, but they also serve as a structure-directing agent to confine the architecture of melon. Both of these B- and F-doped nanomaterails are reported to show much higher catalytic performance than that of pristine melon.

Thermal tempering and template-free methods. Vacancy sites in carbon nitride photocatalysts play an important role as they effectively introduce additional energy levels or act as reactive sites, and thus they profoundly change overall photocatalytic activity. In a post-synthetic modification step melon was reduced via heating in a hydrogen atmosphere. Compared to pristine melon with a band gap of 2.78 eV, reduced melon has a narrower band gap of 2.03 eV, a widened visible light absorption range and suppressed radiative recombination of photo-excited charge carriers as the reduction process effectively introduces vacancies into the polymer95. Reduced melon is superior at generating ·OH radicals for the photocatalytic degradation of organic dyes. Thermal tempering has also been employed as a tool to decrease the band gap of carbon nitride polymers. An amorphous carbon nitride with an optical band gap of 1.90 eV was synthesised by heating crystalline melon at 620 °C for 2 h under argon atmosphere96. The amorphous carbon nitride showed an improved photocatalytic activity in hydrogen evolution, presumably due to the wider light absorption range and quenched radiative recombination.

Melamine and cyanuric acid self-assemble into flower-like, spherical aggregates without the agency of an additional template77. Such pre-organisation makes use of well-defined non-covalent interactions97. Thermal treatment of these assemblies under nitrogen at 550 °C generates mesoporous hollow spheres comprised of melon. Again, the trend holds true that photocatalytic activity is enhanced by additional surface area. The structure, morphology, optical properties, and photocatalytic activity of carbon nitride nanomaterials is greatly affected by the ratio of monomers used for hydrogen bonding, precipitation temperature, and the solvent used for recrystallisation98. The choice of precursors for this self-assembly approach is limited only by the availability of hydrogen bonding motifs.

Nanostructuring of carbon nitride photocatalysts can also be realised by thermal tempering during the polymerisation process of melamine99. Distortions and defects were introduced into hydrogen-bonded nanosheets of melem by thermal treatment at temperatures exceeding 650 °C; i.e. temperatures beyond the thermal stability limit of ordinary melem. These defects facilitate additional n→π* transition pathways for photo-excited electrons, and the materials feature extended UV/Vis absorption ranges of up to 550 nm99. Another way how to obtain defect rich carbon nitride nanorods and nanoplates has been devised that employs infrared heating of dicyandiamide at different power intensities100. The photocatalytic hydrogen evolution activity of the carbon nitride nanorods prepared at 50 % power output (~600 W, 560 °C) is about 2.9 times higher than that of carbon nitride nanoplates.

Exfoliation strategy. Inspired by the delamination of 2D graphene from bulk graphite, various attempts have been published to produce free-standing sheets of carbon nitrides. Exfoliation of crystalline PTI is relatively simple via sonication and shearing due to strong in-plane covalent bonding. Exfoliation of so-called “g-C3N4” was attempted using protocols that were designed for layered materials. However, these efforts were hampered by the physical reality that so-called “graphitic” carbon nitride is in fact melon – a hydrogen bonded material (see Box 1). Hence, delamination of melon without simultaneous debonding is tricky, and was achieved – if at all – serendipitously rather than by design. Sonicated melon yields nanostructures of various sizes and thicknesses down to 2 nm in size and an optical band gap of 2.65 eV72. Both H2 evolution and quantum yield can be improved compared to bulk melon by such a physically induced break-up of the structure. Alternatively, a combination of thermal and chemical exfoliation of melon under H2 atmosphere was attempted, yielding nanosheets with average thickness of 2 nm. Not only did this exfoliation protocol succeed in breaking of hydrogen bonds and van der Waals stacking in the bulk of melon, further, it suppressed re-stacking of large aggregates via the formation of comparatively apolar C–H bonds at surfaces. A combination of heating, hydrothermal exfoliation and fragmentation via acid digestion was applied to produce carbon nitride “quantum dots” – tiny, ordered domains of melon down to 0.336 nm in diameter. These nanostructures show great potential in photocatalysis, bio-imaging and as invisible inks for data security103-105.

There are two principle ways of how to improve photocatalytic performance of carbon nitrides: (1) break-up of the bulk structure of carbon nitrides with the aim of making more active sites available for catalysis, and (2) chemical modification of active sites and the polymer backbone that strives to change the optical and electronic makeup of carbon nitrides. Rational deconvolution of these two methods is difficult, since morphological changes of carbon nitrides are usually accompanied by chemical changes on local scale, and there are very few studies to date that attempt to correlate these effects systematically. There is some evidence that there is weak, non-linear correlation between solvent accessible surface area and rate of hydrogen evolution across various types of carbon nitride materials106. Chemical modification of carbon nitrides outweighs this effect by an order of magnitude, though45. In other studies it was found that increasing the surface area of a carbon nitride photocatalyst is accompanied by fast trapping of separated electrons on the surface where they are available for subsequent reactions. In contrast, photo-excited electrons in bulk melon quickly return to the valence band, which is the reason for the relatively low catalytic activity of that photocatalyst.87

Composites and heterojunctions. We have seen in the previous examples that carbon nitrides including the hydrogen-bonded PCNs can be broken up, dispersed and re-deposited on various supports. It is hence that the concept of heterojunctions based on carbon nitrides originates, and it has been employed successfully to modulate the photocatalytic performance of these materials107. Heterojunctions between inorganic semiconductor and carbon nitrides can be divided into four types: traditional type-I heterojunctions, type-II heterojunctions, all-solid-state semiconductor-semiconductor Z-scheme heterojunctions and all-solid-state semiconductor-conductor-semiconductor Z-scheme heterojunctions108. A type-II heterojunction has been synthesised by combining melon and boron-doped carbon nitride109. Calculations of the band gap positions for simplified models of this heterojunction suggest that the electron transfers to the carbon nitride matrix while the hole migrates to the boron-doped carbon nitride. This heterojunction showed much higher photo-degradation activity and rates of H2 evolution than the pristine compounds109. Although the photoinduced electron-hole separation and transfer are promoted in type-II heterojunction, the redox ability of the photoexcited electron and holes is reduced in comparison with the individual materials. Solid-state Z-scheme heterojunctions provide an alternative pathway for both promoting electron-hole separation and enhancing redox activity110. In overall water-splitting reactions they offer the advantage of spatial separation of red/ox sites – and hence of nascent H2 and O2 gases – that would otherwise combine to explosive gas mixtures in single-component systems111. A Z-scheme Ag3PO4/carbon nitride composite was demonstrated to show superior photocatalytic activity in converting CO2 to fuels112 (Figure 4, c). An optimised Ag3PO4/CN heterojunction showed a CO2 conversion rate of 57.5 μmol h-1 gcat–1; an overall improvement by the factor of 6.1 and 10.4 compared to the model systems melon and pentyl trihydrogen diphosphate (P25), respectively.

In other examples, carbon nitrides have been coupled with metals, metal organic frameworks (MOFs), carbonaceous materials, conducting polymers and various mixtures thereof. For example, a multicomponent heterojunction of one-dimensional (1D) Ag@AgVO3 nanowires/2D reduced graphene oxide/protonated melon (Ag@AgVO3/rGO/PCN) was synthesised via an electrostatic self-assembly method and a photochemical reduction process113. Reduced graphene oxide serves as an electron mediator to improve the charge separation between Ag@AgVO3 and PCN to prevent the electron-hole recombination while the Ag@AgVO3 nanowires act as photosensitisers to harvest more photons and promoted the separation and migration of electron-hole pairs at the interface. As-prepared Ag@AgVO3/rGO/PCN heteroconjugates exhibited remarkably enhanced photocatalytic activity for pollutant degradation113. The observed effects in the examples above show promise, even though exfoliated carbon nitrides are difficult to produce in reliable quantity and quality, and sample homogeneity and cleanliness is a concern with current synthetic protocols.

Applications in electronics and catalysis. Emerging applications of carbon nitride materials are predominantly photocatalytic water splitting, activation of CO2, degradation of pollutants and bacteria disinfection, organic synthesis, as well as electronic materials and devices. In the following, we will highlight the most recent developments that make use of a variety of previously discussed modifications and synthetic protocols.

Figure 3 | Photocatalysts based on polymeric carbon nitride (PCN) and their efficiencies for hydrogen evolution from water. top | Summary of various modification strategies of PCNs. bottom | Apparent quantum efficiencies (AQE) of modified PCN-based photocatalysts (with UV/Vis adsorption edges given in nm and in bold).

Photocatalytic water splitting. Photocatalytic water splitting using carbon nitride materials is potentially an economically feasible technique for converting solar energy into hydrogen. Since its first discovery as a metal-free photocatalyst in 20098, the application of melon-based materials in photocatalytic water splitting has stimulated great research interest, and there is a published example of a continuously operating, large-scale reactor that uses melon and natural sunlight to produce hydrogen125 (Figure 4, a).

The photocatalytic H2 evolution activity of melon is greatly affected by pH, micro- and macroscopic structure of the photocatalyst, and finally by the choice of co-catalysts and sacrificial agents (see Table 2 and Figure 3). Nobel metal co-catalysts such as Pt, Pd, and Ru and their oxides raise the hydrogen evolution rate of pure melon over the baseline of 1 μmol h-1. There exist now a wide array of PCNs combined with MoS2, WS2, NiSx, Ni(OH)2, Ni@NiO core shell structures, CoOx, Co(OH)2, Co3(PO4)2, CoSx, CoSex68,127,128, Ag3PO4, BiVO4 on sulfur-doped melon, and NiFe-layered double hydroxides128-130, and combinations with molecular catalysts such as Ni-complexes, cobaloxime, and hydrogenases131-133. However, most of the noble and some of the transition metals are classified as critical raw materials by governmental bodies due to their low natural abundance and slow rates of recycling, hence it is of particular interest to develop noble metal-free strategies for H2 evolution.

Water oxidation is the other half-reaction of water splitting. It is not only a complex process of multi-electron/proton transfers, but it is also one of the main rate-determining steps in overall water splitting. It is widely believed that the major bottlenecks of photocatalytic water oxidation are poor charge separation efficiency and sluggish surface kinetics. Photocatalytic O2 evolution on melon in particular is limited by the relatively high position of the LUMO. Sulphur mediated condensation of PCN and co-polymerisation with electron-deficient pyromellitic dianhydride was employed to shift down the LUMO position and promote overall water oxidation activity.

The ultimate challenge of photocatalytic water splitting, however, is to develop a process that encompasses both half-cell reactions without the need for sacrificial reagents. One approach to realise this goal are Z-scheme water-splitting systems. They are comprised of two semiconductor photocatalysts that participate simultaneously in the redox processes through e.g. close spatial proximity. An overall water splitting system that uses visible light has been proposed involving Pt-carbon nitride/BiVO4 and Pt-carbon nitride/WO3. Both systems rely on a soluble redox mediator in the form of Fe3+/Fe2+ and IO3-/I- pairs138. Both H2 and O2 are evolved in a ratio of 2:1, leading to a stable and reproducible H2 and O2 evolution rates from water138. Similarly, other Z-scheme photocatalysts have been developed such as, TiO2/carbon nitride, β-Ni(OH)2/WO3(PtOx) with I−/IO3−139, as well as Pt-carbon nitride/WO3 with reduced graphene oxide140. Water splitting via a four-electron pathway to produce H2 and O2 in a stoichiometric molar ratio of 2:1 can be realised over carbon nitride nanosheets modified by Pt, PtOx, and CoOx co-catalysts that were photodeposited in situ9 (Figure 4, b). The optimal Co-Pt/carbon nitride nanocomposite exhibits a turnover number of 3.1 moles of H2 and O2 per mole of carbon nitride9. Higher efficiency for overall water splitting was recorded for a nanocomposite of carbon dots on carbon nitride in the absence of a metallic co-catalyst10.

Photocatalytic carbon dioxide reduction. Recently, the application of carbon nitrides for photocatalytic CO2 conversion has drawn keen interest. Melon and its modifications are uniquely suitable for this particular task: for one, we have ubiquitous NH and NH2 groups as Lewis basic sites at the surface that facilitate sorption of CO2 molecules, and the material behaves as a semiconductor that enables the formation of photoinduced charge carriers for the reduction of surface-bound CO2 species141. This particular application highlights the dangers of preconception regarding structure and chemical make-up of the carbon nitride catalyst: in fact, it is entirely inconceivable how the observed CO2 sorption on carbon nitride polymers should at all be rationalised, if it was – as oftentimes postulated – a fully condensed network of heptazine units, rather than a amine-rich polymer. Likewise, the concepts of delamination, fragmentation and induction of porosity in the carbon nitride matrix become much more relevant, since availability of surface functional groups will limit the CO2 sorption capacity of the photocatalyst, and indeed, bulk melon shows only moderate catalytic efficiency for CO2 conversion.

A heterogeneous photocatalyst that consists of a ruthenium complex and carbon nitride has been used for the reduction of CO2 to formic acid. Ru enhances electron transfer from the carbon nitride which in turn acts as the catalytic unit and light-harvester. The material reaches a turnover number exceeding 1000 and an AQE of 5.7 % at 400 nm142. A variation of this catalytic motif is the combination of carbon nitride and a cobalt complex that catalyses the conversion of CO2 to CO143. The melon backbone serves as a substrate to adsorb and activate CO2 while the cobalt species (Co(bpy)32+) acts as an electron mediator to accelerate charge-carrier separation and transfer kinetics143. The photosystem converts CO2 to CO via carboxyl anion radical intermediates with an apparent quantum yield of 0.25 % at 420 nm. This system can be further improved by addition of open framework carbon nitrides (nanosheets), or cobalt-containing zeolitic imidazolate framework (Co-ZIF-9) as a co-catalyst. Zirconium based MOFs (UiO-66) and carbon nitride nanosheet composites, Ag/Ag3PO4/carbon nitride, and AgBr/carbon nitride/nitrogen-doped graphene hybrids have been reported to achieve high efficiency and stable photocatalysis in CO2 reduction.

Photocatalytic degradation of pollutants and bacteria disinfection. A variation on the theme of photocatalysis is the end-application of carbon nitrides as sanitisers for the removal of contaminants including pollutants and pathogenic microorganisms from drinking water and air.

Polymeric carbon nitride has been successfully employed in proof-of-concept degradation of soluble dyes such as methyl orange, methylene blue and Rhodamine B147. Furthermore, PCNs can activate H2O2 to generate reactive oxy-radicals under visible light irradiation without the need for metal additives. In the presence of organic dyes and pollutants this leads to a fast degradation of the contaminant147. Heterojunction photocatalysts such as WO3/carbon nitride148, SnS2/carbon nitride149, and plasmonic Ag@AgBr/carbon nitride150 successfully remove NOx species from air under light irradiation. Melon that was hydrothermally treated with NaOH at temperatures up to 150 °C shows 8.6 times higher rates of photocatalytic oxidation of NO151. It is thought that the main reactive species for NO removal are ˙O2– radicals and photoinduced holes whereas ˙OH radicals played a minor role152. Additionally, carbon nitride polymers are an effective and recyclable bacteriocide in water under visible light irradiation.

Catalytic organic synthesis. Based on the concept of “green sustainable chemistry” design of highly selective, heterogeneous catalysts is highly desirable155. Melon and melon-based polymers hold great potential as metal-free catalysts or catalyst supports for catalytic oxidation and hydrogenation transformation. In particular, reactive structural defects, abundant nitrogen surface groups, strong Lewis basic sites, and semiconductivity have much to offer here. Mesoporous melon (denoted as mpg-C3N4 in literature) shows some activity in Friedel-Crafts acylation of benzene using hexanoyl chloride with an optimised conversion reaching 90 %. It has been proposed that donation of π-electrons from the ring nitrogen atoms activates the arene for subsequent addition of the electrophile8,143. In other examples, the same catalyst activates CO2, and it facilitates the oxidation of benzene158. In the process, CO2 is split into an oxygen diradical that oxidises benzene to phenol, and into CO158.

In addition, melon is able to reduce O2 to an active ˙O2− radical photochemically that is used in selective oxidation of benzene, aromatic alcohols, and aromatic amines159-161. A series of Fe-modified PCN materials have shown remarkably improved activity to convert benzene to phenol in the presence of H2O2 under visible-light irradiation as compared with the in-the-dark reaction. Ferrocene moieties were fixed to mesoporous carbon nitride by covalent –CN– or –N–CO– linkages164 (Figure 4, d). The addition of this dye to the surface of the carbon nitride improved the absorption cross-section of incident light, and it has been suggested that the donor-acceptor interaction between the carbon nitride matrix and Fc group promoted exciton splitting and enhanced photocatalytic performance for the synthesis of phenol from benzene164.

Electrocatalysis and devices. Electrocatalytic conversion of renewable resources is a key technology in realising the goals of clean energy production and environmental remediation167-169. One of the major challenges to melon-based materials in the field of electrocatalysis is the inherently poor electronic conductivity and the low surface area of bulk melon170-174. Thus, substantial effort has been invested to interface melon with conductive materials, be it via direct chemical modification or via assembly into heterostructures170-174. Further, fabrication of electronic and photoelectronic devices from PCNs is feasible since they can be deposited from solution on different electrodes. A flexible membrane has been obtained from porous melon and nitrogen-doped graphene sheets, and it has been successfully used as a stand-alone electrode in the hydrogen evolution reaction165 (Figure 4, e). This metal-free electrocatalyst shows outstanding HER activity with a positive onset-potential close to that of commercial Pt (8 mV vs. 0 mV of Pt/C, vs. RHE @ 0.5 mA cm–2), high exchange current density of 0.43 mA cm–2, and an excellent durability of more than 5000 cycles165. The remarkable HER performance of this hybrid system is attributed to the open, hierarchically porous structure.

Figure 4 | Overview of the applications of polymeric carbon nitride (PCN) in catalytic and electronic devices. a| Light promotes electron-hole separation in PCN via a direct bandgap125. b| Semiconductor junction of PCN decorated with PtOx and Pt nanoparticles used in overall water splitting9. c| PCN can be interfaced with bulk metal oxides (e.g. Ag3PO4) to form p-n heterojunctions (Z-scheme) and used for CO2 conversion112. d| Semiconductor heterojunctions using dye-sensitisation (e.g. ferrocene decorated PCN) for direct oxidation of benzene to phenol with visible light164. e| Bulk heterojunction between two semiconductors, PCN and N-doped graphene films are used as electrodes165. f| A sandwich assembly of PCN between layers of graphene oxide is patterned using laser light and used as a memory storage device166.

In addition, carbon nitride materials have been explored for their use of state-of-the-art applications such as non-volatile memory devices (Figure 4, f). A metal-free, flexible and rewritable memory device was partially processed from solution, and it consists of carbon nitride nanosheets as the insulating layer with graphene electrodes obtained via direct laser writing166. This memory device shows electrical bistability and a reliable ON/OFF ratio of about 105, higher than all the previously reported metal-free flexible memory diodes166.

Electrochemical properties of carbon nitride materials. Graphite anodes – though cheap and the favoured workhorse material in lithium-ion batteries (LIBs) with a high specific capacity of 372 mAh g-1 – suffer from surface passivation effects and slow intercalation kinetics177. Introduction of heteroatoms in particular nitrogen into the carbon can enhance the specific capacity of the anode material. For example, carbon nitride nanobelts with 10 at. % N show 480 mAh g-1 178, and nitrogen-doped carbon nanotubes with 16.4 at. % N have a capacity of 494 mAh g-1 179. We have seen in previous examples that carbon nitride networks such as poly(triazine imides) (PTIs) readily coordinate lithium cations into ordered, ion-lined pore channels44. This begs the question to what extent carbon nitride materials may be a useful substitute for silicon, tin, and graphite as anode in LIBs.

Before the development of electrochemical lithiation, high-temperature methods were used to intercalate metallic Li vapour into graphite to form LiC6 (stage 1) and LiC12 (stage 2) materials180. An analogous method has been applied to both melon and PTI/Li+Cl-181. Although, metallic Li species were still detectable within the polymer matrix, the majority of Li reacted readily with quaternary C3N species that resulted in the partial destruction of aromaticity and order of the carbon nitride materials. An alternative approach using cyclic voltammetry clearly shows oxidation/reduction cycles in the range 0.5–1.5 V indicating that electrochemical Li+ intercalates into melon prepared at various temperatures182. Curiously, the PCN material prepared at 550 °C – i.e. the material with the highest amount of NH and NH2 surface functional groups – showed the maximum initial capacity of 14 mAh g-1. This initial capacity, however, decreases to 6–8 mAh g-1 in subsequent cycles, and is far below that of commercially viable graphite. These findings spell bad news for carbon nitrides as anode materials, however, the jury is still out whether carbon nitrides are better at stabilising holes, or whether reactive electrons could potentially be transported away from the carbon nitride matrix onto metals or other electron catchers.

One such avenue explores the use of carbon nitrides as Pt-support in polymer electrolyte fuel cells (PEFCs)183. Here, three types of carbon nitrides were tested: melon, PTI/Li+Cl-, and boron-doped melon, and they were benchmarked against conventional carbon black (Vulcan XC-72R). Intriguingly, the crystalline Pt@PTI/Li+Cl- has the best durability after 2000 cycles with a loss of 19 % of electrochemical surface area. This is better than the carbon black reference that lost 36 % in the same test, and the B-doped sample that experienced a loss of 100 %. These findings are significant as they highlight the potential of the carbon nitride backbone be it comprised of triazine (C3N3) or heptazine (C6N7) units: (1) crystalline order seems to enhance electrochemical stability. In all instances, (2) electron doping into the carbon nitride backbone leads to undesired side-reactions and decomposition of the structure, while (3) generation of holes seems to be much more tolerable.

How to think about semiconducting carbon nitrides – a rational approach. Application of polymeric carbon nitrides as functional materials in (photo)catalysis or microelectronics is fundamentally determined by their electronic and optical properties. However, a thorough experimental validation, let alone quantification, is hindered by the grainy, powder-like morphology of the vast majority of materials of this class, with the sole exception to date of TGCN7. In practice, this means that direct determination of dark- and photoconductivity by means of electrical measurements is virtually impossible due to near-infinite resistance of macroscopic aggregates of polymeric carbon nitrides184.

It might be prudent to assume that carbon nitride powders are easier to access regarding their steady-state UV/Vis properties. However, the standard laboratory procedure of embedding the material within a KBr pellet is an abstract, non-quantitative measure of the absorbance of this mixture. Only the absorption coefficient of the pristine material enables us to determine the band gap and the proper spectral positioning of absorption bands185. Consequently, it is to some degree inaccurate to describe PCNs with the same vocabulary as one would describe classical semiconductors. Terms like conduction band, valence band, doping levels, band alignment, etc. are frequently used for the description and design of devices containing carbon nitrides, and – though helpful – should be taken with a grain of salt. In the following, we present an overview of the current state-of-the-art regarding the “true” optical and electronic properties of polymeric carbon nitrides – in particular of PCN materials – with a focus on optical investigations.

Steady-state measurements. Typically, the absorbance of melon is determined via diffuse UV/Vis measurements, and though these experiments do not yield accurate values of the material’s absorption coefficient, they enable a qualitative assessment and a surprising find: the apparent optical gap is closing with increasing synthesis temperatures. Likewise, increased synthesis temperatures lead to a more compact packing of the material as determined via X-ray diffraction. This solvatochromic effect is not untypical for other molecular solids188, and it was interpreted as a result of the increased mixing of π-orbitals of overlapping heptazine units186. This observation is corroborated by photoluminescence (PL) investigations that clearly show that the emission undergoes the same redshift as the onset of absorption189. Temperature-dependent PL measurements on melon show no thermal quenching in the range of 4 to 300 K that would typically be observed for covalent semiconductors189. This means that luminescence of melon is the consequence of molecular excitons located on the heptazine subunits, and hence, that photo-excited charge carriers are highly localised. A large activation energy is needed to yield free electron-hole pairs in melon, and indeed such high exciton binding energies of several hundred meV are typical for semiconducting polymers190.

Transient measurements. Until very recently, the only means to collect transient optical data on polymeric carbon nitrides was transient photoluminescence (TRPL). While this technique is comparably easy to apply it has two major draw-backs: firstly, it has a limited time-resolution (typically 50 ps), thus it is not useful for the ultrafast regime. Secondly, it is only sensitive to signals from recombining charge carriers, hence it gives no direct information on the kinetics of conduction-state electrons, and it cannot detect non-radiative recombination of those carriers. It turns out that in typical polymeric carbon nitrides the radiative quantum yield is quite low (usually a few percent). Moreover, it is those carriers not recombining that are doing the job in any catalytic application. Thus, TRPL can give only a very indirect view on the transient behavior of the charge carriers of interest. It is hence paramount to apply transient absorption (TA) spectroscopy. A first study of TA has been reported for dispersed melon in colloidal solution191, and measurement methods for solid samples are currently under development.

Overall, several reports manage to extract useful information about charge-transport in PCN from TRPL data. All share the common observation that the PL signals do not decay monoexponentially, as would be expected for a simple de-excitation processes in molecules or doped semiconductors. Most researchers attribute this behaviour either to a coexistence or a cascade of decay channels, and extract various carrier lifetimes in the range of less than one nanosecond to microseconds. These lifetimes become shorter for carbon nitrides synthesised at higher temperatures, and this is believed to be a consequence of more compact bulk packing189. TRPL analysis yields good fit results, however, there is no consensus on what these lifetimes actually refer to. A solid-state photoactive material requires spatial transport of excitations for its function, and hence, the assumption of localised “0D” decay processes is not helpful. To understand photocatalysis we need to include transport of excitons in our models, and hence, we have to look at the overall process of excitation-transport-recombination. Recently, one such attempt has been reported for TRPL data of melon synthesised at various temperatures167. The authors explain their findings by a hopping mechanism of small electron and hole polarons after fast splitting of initially generated singlet excitons on the heptazine units. The specifics of this hopping transport correlate with the observed decay kinetics in a concise way, and they hint at microscopic hopping rates and carrier mobilities. There is a very important conclusion from this study, namely that charge transport is not solely confined to the hydrogen-bonded planes of melon. Rather, carriers must be moving predominantly perpendicular to these planes, i.e., along 1D paths made up from stacked heptazine units167. Thus, transport in melon is complementing the 2D metallic transport in graphene. Commensurately, TRPL of dispersed melon shows monoexponential decay kinetics, indicating that charge separation and transport is hindered by the removal of heptazine stacks191. More sophisticated, theoretical calculations support these TRPL experiments, at least qualitatively. They show that excitons are indeed located at the heptazine monomer units194, as well as that electron and hole polarons play a decisive role in both steady-state and kinetic opto-electronic characteristics of the material195. It is remarkable that in-plane transport on 1D and 2D pathways along the melon backbone is seemingly strongly disfavoured196. Carriers are forced to move via thermally activated hopping perpendicular to the hydrogen-bonded planes at overall low mobilities (10-5 cm2 V-1 s-1)167. While such mobilities are comparable to those of undoped semiconducting polymers197, it remains to be seen whether PCNs can be pushed to significantly higher intrinsic mobility values via doping.

It is safe to say that PCN materials are best described by the terminology we use for semiconducting polymers, with the only caveat that – contrary to semiconducting polymers – transport along the covalent backbone of melon is severely inhibited. While this spells bad news for overall charge transport and thus device performance, it actually may open the way for applications that specifically exploit this apparent 1D conductivity along van der Waals stacks.

Conclusions and pointers for future development. The observable properties of carbon nitride materials are fantastic, and offer great promise for continuous developments in various fields such as electrocatalysis, photoelectrode applications, batteries, fuel and solar cells, light emitting devices, supercapacitors, sensors, etc. However, it becomes also increasingly clear that the basis of discussions about carbon nitrides has to move away from mere phenomenology and towards rational design and accurate descriptions of the systems at hand. One theory that presently hinders progress in carbon nitride research is that “graphitic carbon nitride (g-C3N4)” exists as a crystalline 2D lattice of covalently bonded heptazine units with no NH or NH2 end groups (see Box 1). In over 6000 published examples of carbon nitride materials to date there is no evidence whatsoever that such a compound was indeed achieved, and it is in the interest of ongoing experimental research, explanatory calculations and that one future paper claiming the actual synthesis that we should lay this unhelpful nomenclature to rest. The original seminal paper described the photocatalytic carbon nitride system in title, text and in the accompanying DFT calculations correctly as “polymeric carbon nitride”8, and we suggest that this nomenclature be observed for melon-based carbon nitride materials in the future.

In terms of synthetic design strategies, there are a couple of trends to note. Electron removal from PCN materials (i.e., p-doping) seems to be the conservative approach, while electron addition (i.e., n-doping) results in unpredictable side-reactions either with oxygen-rich air, or with themselves leading to structural and chemical disintegration. Likewise, many of the emerging (photo)catalytic applications that employ carbon nitrides rely on accessible surface functional groups. Here, hard- and soft-templating methods that break up the bulk melon structure seem to lead to enhancements. So-called exfoliation of carbon nitrides – in particular in hydrothermal and acidic media – is in fact debonding of the hydrogen bonded melon backbone. It should be noted, that particularly in the context of (photo)catalysis several published examples quote the need for a “reactivation of the catalyst” by e.g. acid or base washes for continuous operation. This is indicative of salt-formation or protonation and deprotonation events on the surface functional groups of the carbon nitride materials, and it clearly invalidates the ideal “g-C3N4” structural model that simply cannot account for any chemisorption. Finally, the emerging trend that just about any modification of the basic melon motif leads to a perceived or actual improvement of (photo)catalytic performance is in need of revision: polymeric carbon nitride is a very poor photocatalyst with a rate of hydrogen evolution of 3 µmol h-1 8. This bottom baseline serves as a poor reference given the state-of-the-art.

Our understanding of charge transport properties in melon and PCN materials and the underlying physics of these process is only at the very beginning. Unravelling these processes, however, may very well lead to a future of energy materials from ubiquitously abundant carbon and nitrogen precursors.

Acknowledgements

The authors thank A. Thomas, P. F. McMillan, E. Kroke, and B. V. Lotsch for illuminating discussions. M.J.B. thanks the Czech Science Foundation (GA ČR) for junior grant funding (CAMs – 16-21151Y) and the European Research Council (ERC) for funding under the Starting Grant scheme (BEGMAT – 678462). X.C.W thanks the financial supports from National Basic Research Program of China (2013CB632405), the National Natural Science Foundation of China (21425309) and the 111 Project. C.M. thanks the Deutsche Forschungsgemeinschaft (Grant No. ME 4387/1-1).

Competing interests

The authors declare no competing interests.

1	Blaney, K. in EPSRC Workshop Report   (ed EPSRC) (EPSRC, Manchester, 2010).

2	Innovation Opportunities and Materials Security. (Materials Knowledge Transfer Network, 2012).

3	Union, I. T. The World in 2014: ICT Facts and Figures. 8 (International Telecommunication Union, Switzerland, 2014).

4	Nevius, M. S. et al. Semiconducting Graphene from Highly Ordered Substrate Interactions. Phys. Rev. Lett. 115, 136802, doi:10.1103/PhysRevLett.115.136802 (2015).

5	Liu, A. Y. & Cohen, M. L. Prediction of New Low Compressibility Solids. Science 245, 841-842, doi:10.1126/science.245.4920.841 (1989).

6	Lotsch, B. V. & Schnick, W. New Light on an Old Story: Formation of Melam during Thermal Condensation of Melamine. Chem. Eur. J. 13, 4956-4968, doi:10.1002/chem.200601291 (2007).

7	Algara-Siller, G. et al. Triazine-Based Graphitic Carbon Nitride: a Two-Dimensional Semiconductor. Angew. Chem. Int. Ed. Engl. 53, 7450-7455, doi:10.1002/anie.201402191 (2014).

8	Wang, X. et al. A metal-free polymeric photocatalyst for hydrogen production from water under visible light. Nat. Mater. 8, 76-80, doi:10.1038/nmat2317 (2009).

9	Zhang, G. G., Lan, Z. A., Lin, L. H., Lin, S. & Wang, X. C. Overall water splitting by Pt/g-C3N4 photocatalysts without using sacrificial agents. Chem. Sci. 7, 3062-3066, doi:10.1039/c5sc04572j (2016).

10	Liu, J. et al. Water splitting. Metal-free efficient photocatalyst for stable visible water splitting via a two-electron pathway. Science 347, 970-974, doi:10.1126/science.aaa3145 (2015).

11	Kroke, E. et al. Tri-s-triazine derivatives. Part I. From trichloro-tri-s-triazine to graphitic C3N4 structures. New J. Chem. 26, 508-512, doi:10.1039/b111062b (2002).

12	Liebig, J. v. Ueber einige Stickstoff-Verbindungen. Ann. Pharm. 10, 1-47 (1834).

13	Diem, H. & Matthias, G. in Ullmann's encyclopedia of industrial chemistry Vol. A2  (ed W. Gerhartz) 115-141 (VCH, Weinheim, 1985).

14	Jurgens, B., Hoppe, H. A., Irran, E. & Schnick, W. Transformation of ammonium dicyanamide into dicyandiamide in the solid. Inorganic Chemistry 41, 4849-4851, doi:10.1021/ic025800k (2002).

15	Lotsch, B. V. & Schnick, W. Towards Novel C-N Materials: Crystal Structures and Thermal Properties of Two Polymorphs of Guanidinium Dicyanamide and Their Thermal Conversion into Melamine. New J. Chem. 28, 1129-1136 (2004).

16	Weil, E. D. Fire-Protective and Flame-Retardant Coatings - A State-of-the-Art Review. J. Fire Sci. 29, 259-296, doi:10.1177/0734904110395469 (2011).

17	Weil, E. D. & Levchik, S. V. Flame Retardants in Commercial Use or Development for Textiles. J. Fire Sci. 26, 243-281 (2009).

18	Jürgens, B. et al. Melem (2,5,8-Triamino-tri-s-triazine), an Important Intermediate During Condensation of Melamine Rings to Graphitic Carbon Nitride: Synthesis, Structure Determination by  X-ray Powder Diffraction, Solid-State NMR, and Theoretical Studies. J. Am. Chem. Soc. 125, 10288-10300 (2003).

19	Wirnhier, E., Mesch, M. B., Senker, J. & Schnick, W. Formation and characterization of melam, melam hydrate, and a melam-melem adduct. Chem. Eur. J. 19, 2041-2049, doi:10.1002/chem.201203340 (2013).

20	May, H. Pyrolysis of melamine. J. Appl. Chem. 9, 340-344, doi:10.1002/jctb.5010090608 (1959).

21	Holst, J. R. & Gillan, E. G. From Triazines to Heptazines: Deciphering the Local Structure of Amorphous Nitrogen-Rich Carbon Nitride Materials. J. Am. Chem. Soc. 130, 7373-7379, doi:10.1021/ja709992s (2008).

22	Miller, D. R., Swenson, D. C. & Gillan, E. G. Synthesis and Structure of 2,5,8-Triazido-s-Heptazine:  An Energetic and Luminescent Precursor to Nitrogen-Rich Carbon Nitrides. J. Am. Chem. Soc. 126, 5372-5373, doi:10.1021/ja048939y (2004).

23	Shahbaz, M. et al. Tri-s-triazine: synthesis, chemical behavior, and spectroscopic and theoretical probes of valence orbital structure. J. Am. Chem. Soc. 106, 2805-2811, doi:10.1021/ja00322a014 (1984).

24	Sattler, A. et al. Melamine-melem adduct phases: investigating the thermal condensation of melamine. Chem. Eur. J. 15, 13161-13170, doi:10.1002/chem.200901518 (2009).

25	Seyfarth, L. & Senker, J. An NMR crystallographic approach for the determination of the hydrogen substructure of nitrogen bonded protons. Phys. Chem. Chem. Phys. 11, 3522-3531, doi:10.1039/b819319c (2009).

26	Liebig, J. v. Ueber Mellon und Mellonverbindungen. Justus Liebigs Ann. Chem. 50, 337-363 (1844).

27	Seyfarth, L., Seyfarth, J., Lotsch, B. V., Schnick, W. & Senker, J. Tackling the stacking disorder of melon--structure elucidation in a semicrystalline material. Phys. Chem. Chem. Phys. 12, 2227-2237, doi:10.1039/b919918g (2010).

28	Zhang, X. D. et al. Enhanced Photoresponsive Ultrathin Graphitic-Phase C3N4 Nanosheets for Bioimaging. J. Am. Chem. Soc. 135, 18-21, doi:10.1021/ja308249k (2013).

29	Doblinger, M. et al. Structure elucidation of polyheptazine imide by electron diffraction--a templated 2D carbon nitride network. Chem. Commun., 1541-1543, doi:10.1039/b820032g (2009).

30	Bojdys, M. J. Analysis of Carbodeon’s Nicanite®. http://web.natur.cuni.cz/orgchem/funanomat/wp-content/uploads/2015/05/20130304_Nicanite.pdf (2013).

31	Sundermeyer, W. Fused Salts and Their Use as Reaction Media. Angew. Chem. Int. Ed. Engl. 4, 222-238, doi:10.1002/anie.196502221 (1965).

32	Sundermeyer, W. Chemische Reaktionen in geschmolzenen Salzen. Chem. Unserer Zeit 1, 150-157, doi:10.1002/ciuz.19670010504 (1967).

33	Stenzel, J. & Sundermeyer, W. Chemische Reaktionen in Salzschmelzen, XIV. Über die Darstellung von Bis-trimethylsilyl-carbodiimid und Bis-trimethylsilyl-acetylen. Chem. Ber. 100, 3368-3370, doi:10.1002/cber.19671001027 (1967).

34	Sundermeyer, W. Chemische Reaktionen in Salzschmelzen. IV. Neue Darstellungsmethode von Cyaniden, Cyanaten und Thiocyanaten des Siliciums und Kohlenstoffs. Z. Anorg. Allg. Chem. 313, 290-295, doi:10.1002/zaac.19623130508 (1962).

35	Verbeek, W. & Sunderme.W. Preparation of Carbonyl and Fluorocarbonyl Pseudohalides in Molten Salts. Angew. Chem. Int. Ed. Engl. 6, 871-872, doi:10.1002/anie.196708711 (1967).

36	Kuhn, P., Antonietti, M. & Thomas, A. Porous, Covalent Triazine-Based Frameworks Prepared by Ionothermal Synthesis. Angew. Chem. Int. Ed. Engl. 47, 3450-3453, doi:10.1002/anie.200705710 (2008).

37	Bojdys, M. J., Jeromenok, J., Thomas, A. & Antonietti, M. Rational Extension of the Family of Layered, Covalent, Triazine-Based Frameworks with Regular Porosity. Adv. Mater. 22, 2202-2205, doi:10.1002/adma.200903436 (2010).

38	Bojdys, M. J., Wohlgemuth, S. A., Thomas, A. & Antonietti, M. Ionothermal Route to Layered Two-Dimensional Polymer-Frameworks Based on Heptazine Linkers. Macromolecules 43, 6639-6645, doi:10.1021/ma101008c (2010).

39	Kuhn, P., Forget, A., Su, D., Thomas, A. & Antonietti, M. From Microporous Regular Frameworks to Mesoporous Materials with Ultrahigh Surface Area: Dynamic Reorganization of Porous Polymer Networks. J. Am. Chem. Soc. 130, 13333-13337, doi:10.1021/ja803708s (2008).

40	Kuhn, P., Thomas, A. & Antonietti, M. Toward Tailorable Porous Organic Polymer Networks: A High-Temperature Dynamic Polymerization Scheme Based on Aromatic Nitriles. Macromolecules 42, 319-326, doi:10.1021/ma802322j (2009).

41	Finkel'shtein, A. I. & Spiridonova, N. V. Chemical properties and molecular structure of derivatives of sym-heptazine [1,3,4,6,7,9,9b-heptaazaphenalene, tri-1,3,5-triazine]. Russ. Chem. Rev. 33, 400-405 (1964).

42	Schwinghammer, K. et al. Crystalline Carbon Nitride Nanosheets for Improved Visible-Light Hydrogen Evolution. J. Am. Chem. Soc. 136, 1730-1733, doi:10.1021/ja411321s (2014).

43	Bojdys, M. J., Muller, J. O., Antonietti, M. & Thomas, A. Ionothermal Synthesis of Crystalline, Condensed, Graphitic Carbon Nitride. Chem. Eur. J. 14, 8177-8182, doi:10.1002/chem.200800190 (2008).

44	Wirnhier, E. et al. Poly(triazine imide) with intercalation of lithium and chloride ions [(C3N3)2(NH(x)Li(1-x))3LiCl]: a crystalline 2D carbon nitride network. Chem. Eur. J. 17, 3213-3221, doi:10.1002/chem.201002462 (2011).

45	Schwinghammer, K. et al. Triazine-based Carbon Nitrides for Visible-Light-Driven Hydrogen Evolution. Angew. Chem. Int. Ed. Engl. 52, 2435-2439, doi:10.1002/anie.201206817 (2013).

46	McDermott, E. J. et al. Band Gap Tuning in Poly(triazine imide), a Nonmetallic Photocatalyst. J. Phys. Chem. C 117, 8806-8812, doi:10.1021/jp4002059 (2013).

47	Bojdys, M. J. et al. Exfoliation of Crystalline 2D Carbon Nitride: Thin Sheets, Scrolls and Bundles via Mechanical and Chemical Routes. Macromol. Rapid Commun. 34, 850-854, doi:10.1002/marc.201300086 (2013).

48	Chong, S. Y. et al. Tuning of gallery heights in a crystalline 2D carbon nitride network. J. Mater. Chem. A 1, 1102-1107, doi:10.1039/c2ta01068b (2013).

49	Fettkenhauer, C., Weber, J., Antonietti, M. & Dontsova, D. Novel carbon nitride composites with improved visible light absorption synthesized in ZnCl2-based salt melts. RSC Adv. 4, 40803-40811, doi:10.1039/c4ra08236b (2014).

50	Fettkenhauer, C., Clavel, G., Kailasam, K., Antoniettia, M. & Dontsova, D. Facile synthesis of new, highly efficient SnO2/carbon nitride composite photocatalysts for the hydrogen evolution reaction. Green Chem. 17, 3350-3361, doi:10.1039/c5gc00021a (2015).

51	Fettkenhauer, C., Wang, X. C., Kailasam, K., Antonietti, M. & Dontsova, D. Synthesis of efficient photocatalysts for water oxidation and dye degradation reactions using CoCl2 eutectics. J. Mater. Chem. A 3, 21227-21232, doi:10.1039/c5ta06304c (2015).

52	Ren, S. et al. Porous, Fluorescent, Covalent Triazine-Based Frameworks Via Room-Temperature and Microwave-Assisted Synthesis. Adv. Mater. 24, 2357-2361, doi:10.1002/adma.201200751 (2012).

53	Liu, A. Y. & Wentzcovitch, R. M. Stability of carbon nitride solids. Phys. Rev. B 50, 10362-10365, doi:10.1103/PhysRevB.50.10362 (1994).

54	Teter, D. M. & Hemley, R. J. Low-Compressibility Carbon Nitrides. Science 271, 53-55, doi:10.1126/science.271.5245.53 (1996).

55	Cai, J. et al. Graphene nanoribbon heterojunctions. Nat. Nanotechnol. 9, 896-900, doi:10.1038/nnano.2014.184 (2014).

56	Cai, J. et al. Atomically precise bottom-up fabrication of graphene nanoribbons. Nature 466, 470-473, doi:10.1038/nature09211 (2010).

57	Fujishima, A. & Honda, K. Electrochemical Photolysis of Water at a Semiconductor Electrode. Nature 238, 37-38, doi:10.1038/238037a0 (1972).

58	Maeda, K. et al. Photocatalyst releasing hydrogen from water. Nature 440, 295, doi:10.1038/440295a (2006).

59	Zheng, Y., Lin, L., Wang, B. & Wang, X. Graphitic Carbon Nitride Polymers toward Sustainable Photoredox Catalysis. Angew. Chem. Int. Ed. Engl. 54, 12868-12884, doi:10.1002/anie.201501788 (2015).

60	Zhang, J. et al. Co-Monomer Control of Carbon Nitride Semiconductors to Optimize Hydrogen Evolution with Visible Light. Angew. Chem. Int. Ed. Engl. 51, 3183-3187, doi:10.1002/anie.201106656 (2012).

61	Zhang, J. et al. Synthesis of a Carbon Nitride Structure for Visible-Light Catalysis by Copolymerization. Angew. Chem. Int. Ed. Engl. 49, 441-444, doi:10.1002/anie.200903886 (2010).

62	Ho, W. et al. Copolymerization with 2,4,6-Triaminopyrimidine for the Rolling-up the Layer Structure, Tunable Electronic Properties, and Photocatalysis of g-C3N4. ACS Appl. Mater. Interfaces 7, 5497-5505, doi:10.1021/am509213x (2015).

63	Lin, Z. & Wang, X. Nanostructure Engineering and Doping of Conjugated Carbon Nitride Semiconductors for Hydrogen Photosynthesis. Angew. Chem. Int. Ed. Engl. 52, 1735-1738, doi:10.1002/anie.201209017 (2013).

64	Zhang, G. et al. Iodine Modified Carbon Nitride Semiconductors as Visible Light Photocatalysts for Hydrogen Evolution. Adv. Mater. 26, 805-809, doi:10.1002/adma.201303611 (2014).

65	Ding, Z., Chen, X., Antonietti, M. & Wang, X. Synthesis of Transition Metal-Modified Carbon Nitride Polymers for Selective Hydrocarbon Oxidation. ChemSusChem 4, 274-281, doi:10.1002/cssc.201000149 (2011).

66	Ran, J., Ma, T. Y., Gao, G., Du, X.-W. & Qiao, S. Z. Porous P-doped graphitic carbon nitride nanosheets for synergistically enhanced visible-light photocatalytic H2 production Energy Environ. Sci. 8, 3708-3717, doi:10.1039/c5ee02650d (2015).

67	Wang, X., Chen, X., Thomas, A., Fu, X. & Antonietti, M. Metal‐Containing Carbon Nitride Compounds: A New Functional Organic–Metal Hybrid Material. Adv. Mater. 21, 1609-1612 (2009).

68	Takanabe, K. et al. Photocatalytic hydrogen evolution on dye-sensitized mesoporous carbon nitride photocatalyst with magnesium phthalocyanine. Phys. Chem. Chem. Phys. 12, 13020-13025, doi:10.1039/c0cp00611d (2010).

69	Min, S. X. & Lu, G. X. Enhanced Electron Transfer from the Excited Eosin Y to mpg-C3N4 for Highly Efficient Hydrogen Evolution under 550 nm Irradiation. J. Phys. Chem. C 116, 19644-19652, doi:10.1021/jp304022f (2012).

70	Wang, Y. B., Hong, J. D., Zhang, W. & Xu, R. Carbon nitride nanosheets for photocatalytic hydrogen evolution: remarkably enhanced activity by dye sensitization. Catal. Sci. Technol. 3, 1703-1711, doi:10.1039/c3cy20836b (2013).

71	Xu, J. Y., Li, Y. X. & Peng, S. Q. Photocatalytic hydrogen evolution over Erythrosin B-sensitized graphitic carbon nitride with in situ grown molybdenum sulfide cocatalyst. Int. J. Hydrogen Energy 40, 353-362, doi:10.1016/j.ijhydene.2014.10.150 (2015).

72	Yang, S. et al. Exfoliated Graphitic Carbon Nitride Nanosheets as Efficient Catalysts for Hydrogen Evolution Under Visible Light. Adv. Mater. 25, 2452-2456, doi:10.1002/adma.201204453 (2013).

73	Zhang, J., Zhang, M., Lin, L. & Wang, X. Sol Processing of Conjugated Carbon Nitride Powders for Thin-Film Fabrication. Angew. Chem. Int. Ed. Engl. 54, 6297-6301, doi:10.1002/anie.201501001 (2015).

74	Cui, Y., Ding, Z., Fu, X. & Wang, X. Construction of Conjugated Carbon Nitride Nanoarchitectures in Solution at Low Temperatures for Photoredox Catalysis. Angew. Chem. Int. Ed. Engl. 51, 11814-11818, doi:10.1002/anie.201206534 (2012).

75	Han, Q., Wang, B., Zhao, Y., Hu, C. & Qu, L. A Graphitic-C3N4 “Seaweed” Architecture for Enhanced Hydrogen Evolution. Angew. Chem. Int. Ed. Engl. 54, 11433-11437, doi:10.1002/anie.201504985 (2015).

76	Sun, J. H. et al. Bioinspired hollow semiconductor nanospheres as photosynthetic nanoparticles. Nat. Commun. 3, 1139, doi:10.1038/ncomms2152 (2012).

77	Jun, Y. S. et al. From Melamine-Cyanuric Acid Supramolecular Aggregates to Carbon Nitride Hollow Spheres. Adv. Funct. Mater. 23, 3661-3667, doi:10.1002/adfm.201203732 (2013).

78	Liang, Q. et al. Macroscopic 3D Porous Graphitic Carbon Nitride Monolith for Enhanced Photocatalytic Hydrogen Evolution. Adv. Mater. 27, 4634-4639, doi:10.1002/adma.201502057 (2015).

79	Groenewolt, M. & Antonietti, M. Synthesis of g-C3N4 Nanoparticles in Mesoporous Silica Host Matrices. Adv. Mater. 17, 1789-1792, doi:10.1002/adma.200401756 (2005).

80	Chen, X. F. et al. Ordered Mesoporous SBA-15 Type Graphitic Carbon Nitride: A Semiconductor Host Structure for Photocatalytic Hydrogen Evolution with Visible Light. Chem. Mater. 21, 4093-4095, doi:10.1021/cm902130z (2009).

81	Jiang, G. F. et al. Controllable preparation of graphitic carbon nitride nanosheets via confined interlayer nanospace of layered clays. Mater. Lett. 64, 2718-2721, doi:10.1016/j.matlet.2010.09.004 (2010).

82	Li, X. H. et al. Condensed Graphitic Carbon Nitride Nanorods by Nanoconfinement: Promotion of Crystallinity on Photocatalytic Conversion. Chem. Mater. 23, 4344-4348, doi:10.1021/cm201688v (2011).

83	Liu, J. & Antonietti, M. Bio-inspired NADH regeneration by carbon nitride photocatalysis using diatom templates. Energy Environ. Sci. 6, 1486-1493, doi:10.1039/c3ee40696b (2013).

84	Zhang, J., Zhang, M., Yang, C. & Wang, X. Nanospherical Carbon Nitride Frameworks with Sharp Edges Accelerating Charge Collection and Separation at a Soft Photocatalytic Interface. Adv. Mater. 26, 4121-4126, doi:10.1002/adma.201400573 (2014).

85	Zheng, Y., Lin, L., Ye, X., Guo, F. & Wang, X. Helical Graphitic Carbon Nitrides with Photocatalytic and Optical Activities. Angew. Chem. Int. Ed. Engl. 53, 11926-11930, doi:10.1002/anie.201407319 (2014).

86	Jun, Y.-S., Hong, W. H., Antonietti, M. & Thomas, A. Mesoporous, 2D Hexagonal Carbon Nitride and Titanium Nitride/Carbon Composites. Adv. Mater. 21, 4270-4274, doi:10.1002/adma.200803500 (2009).

87	Hollmann, D. et al. Structure–Activity Relationships in Bulk Polymeric and Sol–Gel-Derived Carbon Nitrides during Photocatalytic Hydrogen Production. Chem Mater 26, 1727-1733, doi:10.1021/cm500034p (2014).

88	Kailasam, K., Epping, J. D., Thomas, A., Losse, S. & Junge, H. Mesoporous carbon nitride-silica composites by a combined sol-gel/thermal condensation approach and their application as photocatalysts. Energy & Environmental Science 4, 4668-4674, doi:10.1039/c1ee02165f (2011).

89	Wang, Y., Wang, X., Antonietti, M. & Zhang, Y. Facile One-Pot Synthesis of Nanoporous Carbon Nitride Solids by Using Soft Templates. ChemSusChem 3, 435-439, doi:10.1002/cssc.200900284 (2010).

90	Yan, H. Soft-templating synthesis of mesoporous graphitic carbon nitride with enhanced photocatalytic H2 evolution under visible light. Chem. Commun. 48, 3430-3432, doi:10.1039/c2cc00001f (2012).

91	Wang, Y., Zhang, J., Wang, X., Antonietti, M. & Li, H. Boron- and Fluorine-Containing Mesoporous Carbon Nitride Polymers: Metal-Free Catalysts for Cyclohexane Oxidation. Angew. Chem. Int. Ed. Engl. 49, 3356-3359, doi:10.1002/anie.201000120 (2010).

92	Zhang, L. G. et al. Facile synthesis of phosphorus doped graphitic carbon nitride polymers with enhanced visible-light photocatalytic activity. Mater. Res. Bull. 48, 3485-3491, doi:10.1016/j.materresbull.2013.05.040 (2013).

93	Lin, Z. & Wang, X. Ionic Liquid Promoted Synthesis of Conjugated Carbon Nitride Photocatalysts from Urea. ChemSusChem 7, 1547-1550, doi:10.1002/cssc.201400016 (2014).

94	Liang, Q. H., Li, Z., Huang, Z. H., Kang, F. Y. & Yang, Q. H. Holey Graphitic Carbon Nitride Nanosheets with Carbon Vacancies for Highly Improved Photocatalytic Hydrogen Production. Adv. Funct. Mater. 25, 6885-6892, doi:10.1002/adfm.201503221 (2015).

95	Niu, P., Yin, L. C., Yang, Y. Q., Liu, G. & Cheng, H. M. Increasing the Visible Light Absorption of Graphitic Carbon Nitride (Melon) Photocatalysts by Homogeneous Self-Modification with Nitrogen Vacancies. Adv. Mater. 26, 8046-8052, doi:10.1002/adma.201404057 (2014).

96	Kang, Y. et al. An Amorphous Carbon Nitride Photocatalyst with Greatly Extended Visible-Light-Responsive Range for Photocatalytic Hydrogen Generation. Adv. Mater. 27, 4572-4577, doi:10.1002/adma.201501939 (2015).

97	Shalom, M., Inal, S., Fettkenhauer, C., Neher, D. & Antonietti, M. Improving Carbon Nitride Photocatalysis by Supramolecular Preorganization of Monomers. J. Am. Chem. Soc. 135, 7118-7121, doi:10.1021/ja402521s (2013).

98	Jun, Y. S. et al. Three-Dimensional Macroscopic Assemblies of Low-Dimensional Carbon Nitrides for Enhanced Hydrogen Evolution. Angew. Chem. Int. Ed. Engl. 52, 11083-11087, doi:10.1002/anie.201304034 (2013).

99	Chen, Y., Wang, B., Lin, S., Zhang, Y. & Wang, X. Activation of n → π* Transitions in Two-Dimensional Conjugated Polymers for Visible Light Photocatalysis. J. Phys. Chem. C 118, 29981-29989, doi:10.1021/jp510187c (2014).

100	Li, H. J., Qian, D. J. & Chen, M. Templateless Infrared Heating Process for Fabricating Carbon Nitride Nanorods with Efficient Photocatalytic H2 Evolution. ACS Appl. Mater. Interfaces 7, 25162-25170, doi:10.1021/acsami.5b06627 (2015).

101	Niu, P., Zhang, L. L., Liu, G. & Cheng, H. M. Graphene-Like Carbon Nitride Nanosheets for Improved Photocatalytic Activities. Adv. Funct. Mater. 22, 4763-4770, doi:10.1002/adfm.201200922 (2012).

102	Qiu, P. X. et al. Fabrication of an exfoliated graphitic carbon nitride as a highly active visible light photocatalyst. J. Mater. Chem. A 3, 24237-24244, doi:10.1039/c5ta08406g (2015).

103	Wang, W., Yu, J. C., Shen, Z., Chan, D. K. & Gu, T. g-C3N4 quantum dots: direct synthesis, upconversion properties and photocatalytic application. Chem. Commun. 50, 10148-10150, doi:10.1039/c4cc02543a (2014).

104	Song, Z. et al. Invisible Security Ink Based on Water-Soluble Graphitic Carbon Nitride Quantum Dots. Angew. Chem. Int. Ed. Engl. 55, 2773-2777, doi:10.1002/anie.201510945 (2016).

105	Cui, Q. et al. Phenyl-Modified Carbon Nitride Quantum Dots with Distinct Photoluminescence Behavior. Angew. Chem. Int. Ed. Engl. 55, 3672-3676, doi:10.1002/anie.201511217 (2016).

106	Schröder, M. et al. Impact of the reaction conditions on the photocatalytic reduction of water on mesoporous polymeric carbon nitride under sunlight irradiation. Int. J. Hydrogen Energy 39, 10108-10120, doi:10.1016/j.ijhydene.2014.04.164 (2014).

107	Zhang, J., Zhang, M., Sun, R. Q. & Wang, X. A Facile Band Alignment of Polymeric Carbon Nitride Semiconductors to Construct Isotype Heterojunctions. Angew. Chem. Int. Ed. Engl. 51, 10145-10149, doi:10.1002/anie.201205333 (2012).

108	Cao, S., Low, J., Yu, J. & Jaroniec, M. Polymeric Photocatalysts Based on Graphitic Carbon Nitride. Adv. Mater. 27, 2150-2176, doi:10.1002/adma.201500033 (2015).

109	Li, H., Liu, Y., Gao, X., Fu, C. & Wang, X. Facile Synthesis and Enhanced Visible-Light Photocatalysis of Graphitic Carbon Nitride Composite Semiconductors. ChemSusChem 8, 1189-1196, doi:10.1002/cssc.201500024 (2015).

110	Zheng, D., Pang, C. & Wang, X. The function-led design of Z-scheme photocatalytic systems based on hollow carbon nitride semiconductors. Chem. Commun. 51, 17467-17470, doi:10.1039/c5cc07867a (2015).

111	Maeda, K. Z-Scheme Water Splitting Using Two Different Semiconductor Photocatalysts. ACS Catalysis 3, 1486-1503, doi:10.1021/cs4002089 (2013).

112	He, Y., Zhang, L., Teng, B. & Fan, M. New Application of Z-Scheme Ag3PO4/g-C3N4 Composite in Converting CO2 to Fuel. Environ. Sci. Technol. 49, 649-656, doi:10.1021/es5046309 (2015).

113	Zhang, S. W. et al. Rationally designed 1D Ag@AgVO3 nanowire/graphene/protonated g-C3N4 nanosheet heterojunctions for enhanced photocatalysis via electrostatic self-assembly and photochemical reduction methods. J. Mater. Chem. A 3, 10119-10126, doi:10.1039/c5ta00635j (2015).

114	Zhang, X., Peng, B., Zhang, S. & Peng, T. Robust Wide Visible-Light-Responsive Photoactivity for H2 Production over a Polymer/Polymer Heterojunction Photocatalyst: The Significance of Sacrificial Reagent. ACS Sustainable Chem. Eng. 3, 1501-1509, doi:10.1021/acssuschemeng.5b00211 (2015).

115	Wang, X. X., Chen, J., Guan, X. J. & Guo, L. J. Enhanced efficiency and stability for visible light driven water splitting hydrogen production over Cd0.5Zn0.5S/g-C3N4 composite photocatalyst. Int. J. Hydrogen Energy 40, 7546-7552, doi:10.1016/j.ijhydene.2014.11.055 (2015).

116	Martin, D. J. et al. Highly Efficient Photocatalytic H2 Evolution from Water using Visible Light and Structure-Controlled Graphitic Carbon Nitride. Angew. Chem. Int. Ed. Engl. 53, 9240-9245, doi:10.1002/anie.201403375 (2014).

117	Liu, G. et al. Nature-Inspired Environmental "Phosphorylation" Boosts Photocatalytic H2 Production over Carbon Nitride Nanosheets under Visible-Light Irradiation. Angew. Chem. Int. Ed. Engl. 54, 13561-13565, doi:10.1002/anie.201505802 (2015).

118	Bhunia, M. K. et al. Dendritic Tip-on Polytriazine-Based Carbon Nitride Photocatalyst with High Hydrogen Evolution Activity. Chem. Mater. 27, 8237-8247, doi:10.1021/acs.chemmater.5b02974 (2015).

119	Xu, J., Li, Y., Peng, S., Lu, G. & Li, S. Eosin Y-sensitized graphitic carbon nitride fabricated by heating urea for visible light photocatalytic hydrogen evolution: the effect of the pyrolysis temperature of urea. Phys. Chem. Chem. Phys. 15, 7657-7665, doi:10.1039/c3cp44687e (2013).

120	Yan, Z., Sun, Z., Liu, X., Jia, H. & Du, P. Cadmium sulfide/graphitic carbon nitride heterostructure nanowire loading with a nickel hydroxide cocatalyst for highly efficient photocatalytic hydrogen production in water under visible light. Nanoscale 8, 4748-4756, doi:10.1039/c6nr00160b (2016).

121	Bhunia, M. K., Yamauchi, K. & Takanabe, K. Harvesting Solar Light with Crystalline Carbon Nitrides for Efficient Photocatalytic Hydrogen Evolution. Angew. Chem. Int. Ed. Engl. 53, 11001-11005, doi:10.1002/anie.201405161 (2014).

122	Zhang, M. W. & Wang, X. C. Two dimensional conjugated polymers with enhanced optical absorption and charge separation for photocatalytic hydrogen evolution. Energy Environ. Sci. 7, 1902-1906, doi:10.1039/c3ee44189j (2014).

123	Hu, S. Z. et al. Enhanced visible light photocatalytic performance of g-C3N4 photocatalysts co-doped with iron and phosphorus. Appl. Surf. Sci. 311, 164-171, doi:10.1016/j.apsusc.2014.05.036 (2014).

124	Huang, Z. F. et al. Carbon nitride with simultaneous porous network and O-doping for efficient solar-energy-driven hydrogen evolution. Nano Energy 12, 646-656, doi:10.1016/j.nanoen.2015.01.043 (2015).

125	Schröder, M. et al. Hydrogen Evolution Reaction in a Large-Scale Reactor using a Carbon Nitride Photocatalyst under Natural Sunlight Irradiation. Energy Technology 3, 1014-1017, doi:10.1002/ente.201500142 (2015).

126	Hou, Y. et al. Layered Nanojunctions for Hydrogen-Evolution Catalysis. Angew. Chem. Int. Ed. Engl. 52, 3621-3625, doi:10.1002/anie.201210294 (2013).

127	Zhang, G. G., Li, G. S. & Wang, X. C. Surface Modification of Carbon Nitride Polymers by Core-Shell Nickel/Nickel Oxide Cocatalysts for Hydrogen Evolution Photocatalysis. ChemCatChem 7, 2864-2870, doi:10.1002/cctc.201500069 (2015).

128	Yang, X. et al. Tuning the Morphology of g-C3N4 for Improvement of Z-Scheme Photocatalytic Water Oxidation. ACS Appl. Mater. Interfaces 7, 15285-15293, doi:10.1021/acsami.5b02649 (2015).

129	Yang, X., Tang, H., Xu, J., Antonietti, M. & Shalom, M. Silver Phosphate/Graphitic Carbon Nitride as an Efficient Photocatalytic Tandem System for Oxygen Evolution. ChemSusChem 8, 1350-1358, doi:10.1002/cssc.201403168 (2015).

130	Nayak, S., Mohapatra, L. & Parida, K. Visible light-driven novel g-C3N4/NiFe-LDH composite photocatalyst with enhanced photocatalytic activity towards water oxidation and reduction reaction. J. Mater. Chem. A 3, 18622-18635, doi:10.1039/c5ta05002b (2015).

131	Wang, D., Zhang, Y. & Chen, W. A novel nickel-thiourea-triethylamine complex adsorbed on graphitic C3N4 for low-cost solar hydrogen production. Chem. Commun. 50, 1754-1756, doi:10.1039/c3cc48141g (2014).

132	Song, X. W. et al. Efficient photocatalytic hydrogen evolution with end-group-functionalized cobaloxime catalysts in combination with graphite-like C3N4. RSC Adv. 4, 18853-18861, doi:10.1039/c4ra01413h (2014).

133	Caputo, C. A. et al. Photocatalytic Hydrogen Production using Polymeric Carbon Nitride with a Hydrogenase and a Bioinspired Synthetic Ni Catalyst. Angew. Chem. Int. Ed. Engl. 53, 11538-11542, doi:10.1002/anie.201406811 (2014).

134	Zhang, G. G., Zang, S. H. & Wang, X. C. Layered Co(OH)2 Deposited Polymeric Carbon Nitrides for Photocatalytic Water Oxidation. ACS Catal. 5, 941-947, doi:10.1021/cs502002u (2015).

135	Zhang, G. G. et al. Cobalt selenide: a versatile cocatalyst for photocatalytic water oxidation with visible light. J. Mater. Chem. A 3, 17946-17950, doi:10.1039/c5ta04767f (2015).

136	Zhang, J. S. et al. Sulfur-mediated synthesis of carbon nitride: Band-gap engineering and improved functions for photocatalysis. Energy Environ. Sci. 4, 675-678, doi:10.1039/c0ee00418a (2011).

137	Chu, S. et al. Band Structure Engineering of Carbon Nitride: In Search of a Polymer Photocatalyst with High Photooxidation Property. ACS Catal. 3, 912-919, doi:10.1021/cs4000624 (2013).

138	Martin, D. J., Reardon, P. J., Moniz, S. J. & Tang, J. Visible Light-Driven Pure Water Splitting by a Nature-Inspired Organic Semiconductor-Based System. J. Am. Chem. Soc. 136, 12568-12571, doi:10.1021/ja506386e (2014).

139	Yan, J. Q. et al. Fabrication of TiO2/C3N4 heterostructure for enhanced photocatalytic Z-scheme overall water splitting. Appl. Catal., B 191, 130-137, doi:10.1016/j.apcatb.2016.03.026 (2016).

140	Zhao, G. X., Huang, X. B., Fina, F., Zhang, G. & Irvine, J. T. S. Facile structure design based on C3N4 for mediator-free Z-scheme water splitting under visible light. Catal. Sci. Technol. 5, 3416-3422, doi:10.1039/c5cy00379b (2015).

141	Qin, J. N., Wang, S. B., Ren, H., Hou, Y. D. & Wang, X. C. Photocatalytic reduction of CO2 by graphitic carbon nitride polymers derived from urea and barbituric acid. Appl. Catal., B 179, 1-8, doi:10.1016/j.apcatb.2015.05.005 (2015).

142	Kuriki, R., Sekizawa, K., Ishitani, O. & Maeda, K. Visible-Light-Driven CO2 Reduction with Carbon Nitride: Enhancing the Activity of Ruthenium Catalysts. Angew. Chem. Int. Ed. Engl. 54, 2406-2409, doi:10.1002/anie.201411170 (2015).

143	Lin, J. L., Pan, Z. M. & Wang, X. C. Photochemical Reduction of CO2 by Graphitic Carbon Nitride Polymers. ACS Sustainable Chem. Eng. 2, 353-358, doi:10.1021/sc4004295 (2014).

144	Ye, X. J., Cui, Y. J., Qiu, X. Q. & Wang, X. C. Selective oxidation of benzene to phenol by Fe-CN/TS-1 catalysts under visible light irradiation. Appl. Catal., B 152, 383-389, doi:10.1016/j.apcatb.2014.01.050 (2014).

145	Li, H., Gan, S., Wang, H., Han, D. & Niu, L. Intercorrelated Superhybrid of AgBr Supported on Graphitic-C3N4-Decorated Nitrogen-Doped Graphene: High Engineering Photocatalytic Activities for Water Purification and CO2 Reduction. Adv. Mater. 27, 6906-6913, doi:10.1002/adma.201502755 (2015).

146	Shi, L., Wang, T., Zhang, H. B., Chang, K. & Ye, J. H. Electrostatic Self-Assembly of Nanosized Carbon Nitride Nanosheet onto a Zirconium Metal-Organic Framework for Enhanced Photocatalytic CO2 Reduction. Adv. Funct. Mater. 25, 5360-5367, doi:10.1002/adfm.201502253 (2015).

147	Cui, Y. et al. Metal-free activation of H2O2 by g-C3N4 under visible light irradiation for the degradation of organic pollutants. Phys. Chem. Chem. Phys. 14, 1455-1462, doi:10.1039/c1cp22820j (2012).

148	Chen, S. F., Hu, Y. F., Meng, S. G. & Fu, X. L. Study on the separation mechanisms of photogenerated electrons and holes for composite photocatalysts g-C3N4-WO3. Appl. Catal., B 150, 564-573, doi:10.1016/j.apcatb.2013.12.053 (2014).

149	Zhang, Z. Y., Huang, J. D., Zhang, M. Y., Yuan, L. & Dong, B. Ultrathin hexagonal SnS2 nanosheets coupled with g-C3N4 nanosheets as 2D/2D heterojunction photocatalysts toward high photocatalytic activity. Appl. Catal., B 163, 298-305, doi:10.1016/j.apcatb.2014.08.013 (2015).

150	Yang, Y. et al. Fabrication of Z-scheme plasmonic photocatalyst Ag@AgBr/g-C3N4 with enhanced visible-light photocatalytic activity. J. Hazard Mater. 271, 150-159, doi:10.1016/j.jhazmat.2014.02.023 (2014).

151	Sano, T. et al. Activation of graphitic carbon nitride (g-C3N4) by alkaline hydrothermal treatment for photocatalytic NO oxidation in gas phase. J. Mater. Chem. A 1, 6489-6496, doi:10.1039/c3ta10472a (2013).

152	Dong, F., Wang, Z., Li, Y., Ho, W. K. & Lee, S. C. Immobilization of Polymeric g-C3N4 on Structured Ceramic Foam for Efficient Visible Light Photocatalytic Air Purification with Real Indoor Illumination. Environ. Sci. Technol. 48, 10345-10353, doi:10.1021/es502290f (2014).

153	Wang, W., Yu, J. C., Xia, D., Wong, P. K. & Li, Y. Graphene and g-C3N4 nanosheets cowrapped elemental alpha-sulfur as a novel metal-free heterojunction photocatalyst for bacterial inactivation under visible-light. Environ Sci Technol 47, 8724-8732, doi:10.1021/es4013504 (2013).

154	Huang, J., Ho, W. & Wang, X. Metal-free disinfection effects induced by graphitic carbon nitride polymers under visible light illumination. Chem. Commun. 50, 4338-4340, doi:10.1039/c3cc48374f (2014).

155	Gong, Y. T., Li, M. M., Li, H. R. & Wang, Y. Graphitic carbon nitride polymers: promising catalysts or catalyst supports for heterogeneous oxidation and hydrogenation. Green Chem. 17, 715-736, doi:10.1039/c4gc01847h (2015).

156	Goettmann, F., Fischer, A., Antonietti, M. & Thomas, A. Chemical synthesis of mesoporous carbon nitrides using hard templates and their use as a metal-free catalyst for Friedel-Crafts reaction of benzene. Angew. Chem. Int. Ed. Engl. 45, 4467-4471, doi:10.1002/anie.200600412 (2006).

157	Hong, Y. et al. In-situ synthesis of direct solid-state Z-scheme V2O5/g-C3N4 heterojunctions with enhanced visible light efficiency in photocatalytic degradation of pollutants. Appl. Catal., B 180, 663-673 (2016).

158	Goettmann, F., Thomas, A. & Antonietti, M. Metal-Free Activation of CO2 by Mesoporous Graphitic Carbon Nitride. Angew. Chem. Int. Ed. Engl. 46, 2717-2720, doi:10.1002/anie.200603478 (2007).

159	Su, F. et al. mpg-C3N4-Catalyzed Selective Oxidation of Alcohols Using O2 and Visible Light. J. Am. Chem. Soc. 132, 16299-16301, doi:10.1021/ja102866p (2010).

160	Long, B., Ding, Z. & Wang, X. Carbon Nitride for the Selective Oxidation of Aromatic Alcohols in Water under Visible Light. ChemSusChem 6, 2074-2078, doi:10.1002/cssc.201300360 (2013).

161	Su, F. et al. Aerobic Oxidative Coupling of Amines by Carbon Nitride Photocatalysis with Visible Light. Angew. Chem. Int. Ed. Engl. 50, 657-660, doi:10.1002/anie.201004365 (2011).

162	Chen, X., Zhang, J., Fu, X., Antonietti, M. & Wang, X. Fe-g-C3N4-Catalyzed Oxidation of Benzene to Phenol Using Hydrogen Peroxide and Visible Light. J. Am. Chem. Soc. 131, 11658-11659, doi:10.1021/ja903923s (2009).

163	Zhang, P. F., Gong, Y. T., Li, H. R., Chen, Z. R. & Wang, Y. Selective oxidation of benzene to phenol by FeCl3/mpg-C3N4 hybrids. RSC Adv. 3, 5121-5126, doi:10.1039/c3ra23357j (2013).

164	Ye, X., Cui, Y. & Wang, X. Ferrocene-Modified Carbon Nitride for Direct Oxidation of Benzene to Phenol with Visible Light. ChemSusChem 7, 738-742, doi:10.1002/cssc.201301128 (2014).

165	Duan, J., Chen, S., Jaroniec, M. & Qiao, S. Z. Porous C3N4 Nanolayers@N-Graphene Films as Catalyst Electrodes for Highly Efficient Hydrogen Evolution. ACS Nano 9, 931-940, doi:10.1021/nn506701x (2015).

166	Zhao, F. et al. Functionalized Graphitic Carbon Nitride for Metal-free, Flexible and Rewritable Nonvolatile Memory Device via Direct Laser-Writing. Sci. Rep. 4, 5882, doi:10.1038/srep05882 (2014).

167	Merschjann, C. et al. Complementing Graphenes: 1D Interplanar Charge Transport in Polymeric Graphitic Carbon Nitrides. Adv. Mater. 27, 7993-7999, doi:10.1002/adma.201503448 (2015).

168	Mistry, H., Varela, A. S., Kuhl, S., Strasser, P. & Cuenya, B. R. Nanostructured electrocatalysts with tunable activity and selectivity. Nat. Rev. Mater. 1, 16009, doi:10.1038/natrevmats.2016.9 (2016).

169	Ma, T. Y., Cao, J. L., Jaroniec, M. & Qiao, S. Z. Interacting Carbon Nitride and Titanium Carbide Nanosheets for High-Performance Oxygen Evolution. Angew. Chem. Int. Ed. Engl. 55, 1138-1142, doi:10.1002/anie.201509758 (2016).

170	Ma, T. Y., Dai, S., Jaroniec, M. & Qiao, S. Z. Graphitic carbon nitride nanosheet-carbon nanotube three-dimensional porous composites as high-performance oxygen evolution electrocatalysts. Angew. Chem. Int. Ed. Engl. 53, 7281-7285, doi:10.1002/anie.201403946 (2014).

171	Zhao, Y. et al. Graphitic Carbon Nitride Nanoribbons: Graphene-Assisted Formation and Synergic Function for Highly Efficient Hydrogen Evolution. Angew. Chem. Int. Ed. Engl. 53, 13934-13939, doi:10.1002/anie.201409080 (2014).

172	Liang, J. et al. Facile Oxygen Reduction on a Three-Dimensionally Ordered Macroporous Graphitic C3N4/Carbon Composite Electrocatalyst. Angew. Chem. Int. Ed. Engl. 51, 3892-3896, doi:10.1002/anie.201107981 (2012).

173	Zheng, Y. et al. Nanoporous Graphitic-C3N4@Carbon Metal-Free Electrocatalysts for Highly Efficient Oxygen Reduction. J. Am. Chem. Soc. 133, 20116-20119, doi:10.1021/ja209206c (2011).

174	Hou, Y., Zuo, F., Dagg, A. P., Liu, J. & Feng, P. Branched WO3 Nanosheet Array with Layered C3N4 Heterojunctions and CoOx Nanoparticles as a Flexible Photoanode for Efficient Photoelectrochemical Water Oxidation. Adv. Mater. 26, 5043-5049, doi:10.1002/adma.201401032 (2014).

175	Shalom, M. et al. Controlled Carbon Nitride Growth on Surfaces for Hydrogen Evolution Electrodes. Angew. Chem. Int. Ed. Engl. 53, 3654-3658, doi:10.1002/anie.201309415 (2014).

176	Xu, J. et al. Liquid-Based Growth of Polymeric Carbon Nitride Layers and Their Use in a Mesostructured Polymer Solar Cell with Voc Exceeding 1 V. J. Am. Chem. Soc. 136, 13486-13489, doi:10.1021/ja508329c (2014).

177	Li, H., Wang, Z., Chen, L. & Huang, X. Research on Advanced Materials for Li-ion Batteries. Adv. Mater. 21, 4593-4607, doi:10.1002/adma.200901710 (2009).

178	Zhong, D. Y. et al. Lithium storage in polymerized carbon nitride nanobells. Appl. Phys. Lett. 79, 3500 (2001).

179	Li, X. et al. High concentration nitrogen doped carbon nanotube anodes with superior Li+ storage performance for lithium rechargeable battery application. J. Power Sources 197, 238-245, doi:10.1016/j.jpowsour.2011.09.024 (2012).

180	Guerard, D. & Herold, A. Intercalation of lithium into graphite and other carbons. Carbon 13, 337-345, doi:10.1016/0008-6223(75)90040-8 (1975).

181	Veith, G. M. et al. Electrochemical and Solid-State Lithiation of Graphitic C3N4. Chem. Mater. 25, 503-508, doi:10.1021/cm303870x (2013).

182	Jorge, A. B., Cora, F., Sella, A., McMillan, P. F. & Brett, D. J. L. Electrochemical properties of graphitic carbon nitrides. Int. J. Nanotechnol. 11, 737-746, doi:10.1504/ijnt.2014.063784 (2014).

183	Mansor, N. et al. Graphitic Carbon Nitride Supported Catalysts for Polymer Electrolyte Fuel Cells. J. Phys. Chem. C 118, 6831-6838, doi:10.1021/jp412501j (2014).

184	Zhang, Y., Mori, T., Ye, J. & Antonietti, M. Phosphorus-Doped Carbon Nitride Solid: Enhanced Electrical Conductivity and Photocurrent Generation. J. Am. Chem. Soc. 132, 6294-6295, doi:10.1021/ja101749y (2010).

185	Pankove, J. I. Optical Processes in Semiconductors.  448 (Dover Publications, 1975).

186	Tyborski, T. et al. Tunable optical transition in polymeric carbon nitrides synthesized via bulk thermal condensation. J. Phys.: Condens. Matter 24, 162201 (2012).

187	Thomas, A. et al. Graphitic carbon nitride materials: variation of structure and morphology and their use as metal-free catalysts. J. Mater. Chem. 18, 4893-4908, doi:10.1039/b800274f (2008).

188	Wolf, H. C. The Electronic Spectra of Aromatic Molecular Crystals.  (New York: Academic, 1959).

189	Merschjann, C. et al. Photophysics of polymeric carbon nitride: An optical quasimonomer. Phys. Rev. B 87, 205204 (2013).

190	Beljonne, D., Cornil, J., Silbey, R., Millie, P. & Bredas, J. L. Interchain interactions in conjugated materials: The exciton model versus the supermolecular approach. J. Chem. Phys. 112, 4749-4758, doi:10.1063/1.481031 (2000).

191	Zhang, H., Chen, Y., Lu, R., Li, R. & Yu, A. Charge carrier kinetics of carbon nitride colloid: a femtosecond transient absorption spectroscopy study. Phys. Chem. Chem. Phys. 18, 14904-14910, doi:10.1039/C6CP01600F (2016).

192	Shalom, M., Inal, S., Neher, D. & Antonietti, M. SiO2/carbon nitride composite materials: The role of surfaces for enhanced photocatalysis. Catal. Today 225, 185-190, doi:10.1016/j.cattod.2013.12.013 (2014).

193	Zhang, H. & Yu, A. Photophysics and Photocatalysis of Carbon Nitride Synthesized at Different Temperatures. J. Phys. Chem. C 118, 11628-11635, doi:10.1021/jp503477x (2014).

194	Wei, W. & Jacob, T. Electronic and optical properties of fluorinated graphene: A many-body perturbation theory study. Phys. Rev. B 87, 115431 (2013).

195	Meek, G. A., Baczewski, A. D., Little, D. J. & Levine, B. G. Polaronic Relaxation by Three-Electron Bond Formation in Graphitic Carbon Nitrides. J. Phys. Chem. C 118, 4023-4032, doi:10.1021/jp412305y (2014).

196	Huda, M. N. & Turner, J. A. Morphology-dependent optical absorption and conduction properties of photoelectrochemical photocatalysts for H-2 production: A case study. J. Appl. Phys. 107, 5, doi:10.1063/1.3428957 (2010).

197	Amorim, C. A. et al. Determination of carrier mobility in MEH-PPV thin-films by stationary and transient current techniques. J. Non-Cryst. Solids 358, 484-491, doi:10.1016/j.jnoncrysol.2011.11.001 (2012).