Construction of trifloaluminate ionic liquid catalyst on the silica surface dedicated for continuous flow Diels-Alder synthesis

Anna Wolnya, Piotr Latosa, Katarzyna Szymańskab, Sebastian Jurczykc, Anna Chroboka,*

a Department of Chemical Organic Technology and Petrochemistry, Faculty of Chemistry, Silesian University of Technology, Krzywoustego 4, PL-44100 Gliwice, Poland,

b Department of Chemical Engineering and Process Design, Faculty of Chemistry, Silesian University of Technology, Strzody 7, PL-44100 Gliwice, Poland

c Institute for Engineering of Polymer Materials and Dyes, Lukasiewicz Research Network, Sklodowskiej-Curie 55, PL-87100 Torun, Poland

* Corresponding author: anna.chrobok@polsl.pl

Abstract

Supported ionic liquid phases (SILP) are efficiently use for the construction of highly active, heterogeneous and recyclable catalysts. In this study, three strategies towards chemical immobilization of trifloaluminate ionic liquid catalyst into microporous/mesoporous silica support were investigated. The order of silica surface modification with trifloaluminate ILs components had crucial influence on the catalytic activity and stability which was tested in the model Diels-Alder reaction between isoprene and maleic anhydride in acetonitrile at room temperature. The best catalytic performance (maleic anhydride conversion > 97% in ten reaction cycles) was achieved for catalyst created through the synthesis of trifloaluminate ionic liquid in the first step with further bounding to the silica surface using 25 wt% of ionic liquid loading. The effective transformation of the Diels-Alder reaction to continuous flow synthesis led to 97% maleic anhydride conversion over 432 h with a TOF of 104.3 h-1 and significantly improved process sustainability.

Keywords: ionic liquids, supported ionic liquid phase, immobilization, Diels-Alder, flow chemistry

1. Introduction

Heterogeneous catalysts play an important role in chemical industry due to their robustness and easy separation resulting in lower operational cost. The proper design of heterogeneous catalysts is crucial affecting not only their activity but also selectivity and stability. The careful choice of the carrier and the active phase effects final characteristics of the catalyst. Recently, supported ionic liquid phase (SILP) became a powerful tool for the designing of heterogeneous catalysts meeting global green chemistry assumptions [1-3]. Diversity in the ionic liquids (IL) structures and properties makes them widely use as catalysts in organic synthesis, particularly as acidic catalysts [4].

SILP catalysts can be synthesized by chemical anchoring or physical adsorption of IL moieties on the surface of a carrier. Integration of IL with a solid matrix by covalent bonding prevents leaching of catalytic phase from the surface and provides catalyst durability in the process [5,6]. Two methods of chemical immobilization of ILs, via cation or anion, can be used [7,8]. Immobilization of the IL via cation involves the modification of IL structure with siliceous precursors, e.g. 3-(chloropropyl)triethoxysilane, or 3-mercaptopropyl-trimethoxysilane. The resulted IL modified with ethoxysilane groups can be directly attached to the hydroxyl groups of silica. The fixation of the IL through the anion was primarily observed for chlorometallate ILs, especially in the wet impregnation method, leading to the formation of -Si-O-M bonds [7]. Brønsted or Lewis acidity can be introduced to SILP catalyst to the structure of the cation through functional groups, like -SO3H, -B(OH)2 or via anion, e.g. [HSO4 ]-, [AlCl4]- of IL [8-10]. An alternative option involves the modification of the surface of carrier with neutral IL followed by subsequent immobilization of metal complexes or enzymes [10-13].

Incorporation of metal chlorides as Lewis acids in IL structure and formation of chlorometallates ILs prevents its leaching in organic synthesis and provides high product purity which is of particular importance for pharmaceutical applications. The heterogenization of chlorometallates ILs via chemical bound into the solid carrier was already described in several reports [7,14-19]. The low hydrolytic stability of these systems is the major drawback which influences the possibility of recycling of SILP catalysts. Chlorogallate(III) and chloroaluminate(III) ILs were bounded into mesoporous silica support and used as catalysis in Diels-Alder cycloaddition under solventless conditions. Chlorogallate(III) SILP catalysts were the most active causing the full conversion of substrates and high endo/exo selectivities for various adducts. The stability of SILP catalysts in at least five reaction cycles was achieved [14]. Chloroaluminate(III) silica based SILP catalysts were also used in Friedel–Crafts alkylation of benzene with olefins, production of alkylated gasoline and trimerization of isobutene with improved yield, selectivity, and catalyst recyclability compared to homogenous version [7, 15, 16]. Other more hydrolytically stable metals species, as chloroferrate(III) and chloroindate(III) ILs chemically anchored on silica were used in the synthesis of diphenylmethane and its derivatives as well. Exceptional selectivity up to 100%, complete conversion of substrate and stability of SILP catalyst for 10 cycles were observed [17, 18]. It was also reported that SnCl4 was integrated with quaternary ammonium chloride IL immobilized on various silicas. SILP catalyst enhanced selectivity (94%) and conversion (76%) in condensation of isobutene and formaldehyde [19].

Another possibility of introducing metal moieties into ILs structure is the formation of water tolerant triflometallates ILs, e.g. trifloaluminate ILs in contrary to hydrolytically unstable chlorometallates ILs. Trifloaluminate IL are based on trifluoromethanesulfonate (triflate) anion derived from, e.g. 1-ethyl-3-methylimidazolium triflate [C2mim][OTf] or 1-methyl-3-octylimidazolium triflate [C8mim][OTf] complexed with Al(OTf)3 in substoichiometric quantities χAl(OTf)3 = 0.15 and 0.25 forming homogenous liquids. During the synthesis of trifloaluminate ILs with increasing loading of Al(OTf)3 higher than 0.25, the suspended solid was visible in the product even in 85 oC. Lewis acidity of was measured using Gutmann acceptor number (AN) approach positioning trifloaluminate ILs as medium-strength Lewis acids (AN = ca. 65). Our previous studies showed that trifloaluminate systems consist of hexacoordinate aluminum in multiply charged, oligonuclear anionic complexes, exhibiting diverse triflate bridging modes [20]. Trifloaluminate ILs were embedded via adsorption on multi-walled carbon nanotubes and used for the synthesis of chromanes in several cycles. High conversions (94-99%) and selectivities (80-89%) were achieved under SILP conditions [20]. The same catalytic system was tested for levulinic acid esters synthesis from α-angelica lactone. High performance of trifloaluminate SILP catalyst remained constant for 5 reaction cycles achieving full conversion and 100% selectivity of the butyl levulinate [21]. Trifloaluminate IL was also chemically grafted to silica and hybrid silica materials (CaO-SiO2, MgO-SiO2), and use in the batch and continuous flow aminolysis of epoxides. High conversion 81.1% and selectivity 95.9% through 72 h under flow conditions were reached in the presence of SILP based on MgO-SiO2 [22].

It was confirmed that the order in which the silica surface is modified in the fabrication process of chloroaluminate SILP catalysts is crucial. Immobilization of ILs via triethoxysilyl groups located in the dialkylimidazolium cation, and subsequent complexation reaction of anion with AlCl3, leads to the deposition of free aluminum chloride species on/in the silica material [7]. To mitigate this adverse occurrence in our previous work the following sequence was applied for the fabrication of chlorometallates SILP catalysts: synthesis of 1-methyl-3-(triethoxysilylpropyl)imidazolium chloride, the addition of gallium chloride and formation of chlorogallate ILs, and then its chemical immobilization on the silica surface [14]. However, this phenomenon for trifloaluminate SILP catalysts remains poorly understood.

Summing up, immobilization of ILs on the solid support can offer high stability of the SILP materials allowing their application in the continuous flow synthesis. However, the application of SILP catalytic systems have received more interest for the processes carried out in the gas phase [23-27]. On the other hand, due to the low stability of chlorometallate ILs they were not applied for the flow synthesis and water tolerant trifloaluminate systems can overcome this drawback.

In this work, seeking for the best recycling strategy, taking advantage of water stable triflometallate ILs the influence of the order of silica surface modification with trifloaluminate ILs components on the catalytic activity was determined following a multi-technique speciation study. The curtail sequence of the immobilization of reagents was proposed. Next, the trifloaluminate SILP catalyst was used for the model Diels-Alder reaction in batch process. After optimisation of the reaction conditions an efficient upgrade from batch to flow was demonstrated.

2. Experimental

2.1. Materials

1-methylimidazole (≥99.0%), (3-chloropropyl)triethoxysilane (≥95.0%), aluminum trifluoromethanesulfonate (99.9%), lithium trifluoromethanesulfonate (96.0%), silver trifluoromethanesulfonate (	≥99.0%), polyethylene glycol (35.000 gmol-1), hexadecyltrimethylammonium bromide (≥98,0%), tetraethyl orthosilicate (98.0%), maleic anhydride, isoprene (99.0%), dicyclopentadiene, α-terpinene (≥85.0%), myrcene (≥90%.0), ocimene (≥90%) were purchased from Sigma Aldrich, Merck Group, Poland. Multimodal porous SiO2 [28,29], 1-methyl-3(triethoxysilylpropyl)imidazolium chloride ([tespmim]Cl) [7], 1-methyl-3(triethoxysilylpropyl)imidazolium triflate ([tespmim][OTf]) [22], 1-methyl-3(triethoxysilylpropyl)imidazolium triflate – aluminium triflate ([tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15) [22] were prepared according to the literature (Supplementary Materials).

2.2. Catalyst preparation

SILP SiO2-[tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15 catalysts preparation:

SILP (1): [tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15 (0.75 mmol) was added to the 25 mL round-bottomed flask and dissolved in toluene (10 mL) at 90°C, next SiO2 (0.50 g) was added. Reaction mixture was stirred for 24 h. After that, material was filtered off, washed using Soxhlet extraction for 24 h at 120°C, filtered off under vacuum, and dried on the Schlenk line (rt, 24 h) yielded 0.52 g of SILP (1) with [tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15 loading 25.3 wt% (determined by TGA).

SILP (2): [tespmim][OTf] (0.75 mmol) was added to the 25 mL round-bottomed flask and dissolved in toluene (10 mL) at 90°C, next SiO2 (0.50 g) was added. Reaction mixture was stirred for 24 h. After that, material was filtered off, washed using Soxhlet extraction for 24 h at 120 °C, filtered off under vacuum, and dried on the Schlenk line (rt, 24 h) yielded 0.51 g of product. Then, the obtained material (0.51 g) and the aluminium triflate (0.0217 g, molar ratio χAl(OTf)3 = 0.15) dissolved in acetonitrile (10 mL) were placed in 25 mL round-bottomed flask, and stirred for 24 h at 95°C. Next, material was filtered off, washed with acetonitrile (3 × 20 mL), and dried on the Schlenk line (rt, 24 h) yielded 0.5 g of SILP (2) with [tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15 loading 19.2 wt% (determined by TGA).

SILP (3): [tespmim]Cl (0.75 mmol) was added to the 25 mL round-bottomed flask and dissolved in toluene (10 mL) at 90°C, next SiO2 (0.50 g) was added. Reaction mixture was stirred for 24 h. After that, material was filtered off, washed using Soxhlet extraction for 24 h at 120 °C, filtered off under vacuum, and dried on the Schlenk line (rt, 24 h) yielded 0.5 g of product. Next, the obtained material (0.5 g) and lithium triflate (0.15 g, 30 mol% per [tespmim]Cl loaded on material) dissolved in ethyl acetate (10 mL) were placed in 25 mL round-bottomed flask, and stirred for 24 h at room temperature. Next, material was filtered off, washed with ethyl acetate (3 × 20 mL), and dried on the Schlenk line (rt, 24 h) yielded 0.5 g of product. Then, the obtained material (0.5 g) and the aluminium triflate (0.0218 g, molar ratio χAl(OTf)3 = 0.15) dissolved in acetonitrile (10 mL) were placed in 25 mL round-bottomed flask, and stirred for 24 h at 95°C. Next, material was filtered off, washed with acetonitrile (3 × 20 mL), and dried on the Schlenk line (rt, 24 h) yielded 0.5 g of SILP (3) with [tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15 loading 19.7 wt% (determined by TGA).

SiO2-Al(OTf)3: Aluminium triflate (0.75 mmol) was added to the 25 mL round-bottomed flask and dissolved in acetonitrile (10 mL) at 90°C, and next SiO2 (0.50 g) was added. Reaction mixture was stirred for 24 h. After that, material was filtered off, washed using Soxhlet extraction for 24 h at 120°C, filtered off under vacuum, and dried on the Schlenk line (rt, 24 h) yielded 0.5 g of SiO2-Al(OTf)3. SiO2-Al(OTf)3 loading was 36.5 wt% (determined by TGA).

2.3. General procedure of Diels-Alder reaction in batch system

The maleic anhydride (4 mmol) dissolved in acetonitrile (0.5 mL), n-decane (GC inert standard, 0.02 g), SILP(1-3) containing 0.1 mol% of Al(OTf)3 (recalculated for maleic anhydride) were placed in a round-bottomed flask, and then the diene (6 mmol) was added dropwise. The reaction was stirred (100 rpm) at room temperature for 1-180 min, and monitored by gas chromatography (GC). After the reaction, the catalyst was filtered off, the solvent was removed using rotary evaporator, and the product was purified applying column chromatography using chloroform as eluent (yield 95%) and characterised by 1H and 13C NMR spectroscopy.

1H NMR (400 MHz, cdcl3) δ 5.63 (s, 1H), 3.43 – 3.28 (m, 2H), 2.54 (m, J = 17.6, 15.7, 4.2 Hz, 2H), 2.26 (m, J = 15.8, 10.3, 4.5 Hz, 2H), 1.77 (s, 3H) (Supplementary Materials, Fig.S17).

13C NMR (101 MHz, cdcl3) δ 174.49 (s), 174.34 (s), 136.71 (s), 120.29 (s), 40.23 (s), 39.59 (s), 28.55 (s), 24.22 (s), 23.62 (s) (Supplementary Materials, Fig.S18).

2.4. SILP catalyst recycling

After the reaction, the SILP (1-3) were filtered off, washed with 30 mL of acetonitrile, dried under the vacuum on the Schlenk line (6 h, 20 °C) and reused.

2.5. General procedure of Diels-Alder reaction in flow system

The continuous-flow Diels-Alder reaction was performed in a fully automated Syrris Asia flow reactor with two pumps and four syringes. Pump A pumped maleic anhydride (2.0 M) in acetonitrile with flow 0.023 mLmin-1, and pump B pumped isoprene with flow 0.007 mLmin-1.

The combined steams were flowed through the column reactor filled with 0.3 g of SILP(1) catalyst for 48 h at room temperature. Reaction progress was monitored by gas chromatography after 6, 24 and 48 h.

2.6. Materials characterisation and analysis

Gas chromatography (GC) analyses were performed on a SHIMADZU GC-2010 Plus equipped with a Zebron ZB-5MSi column (30 m×0.32 mm; 0.25 μm). Thermogravimetric analyses (TGA) of all materials were carried out on a thermobalance (Mettler Toledo STAR851). Samples (10 mg) were heated with temperature ramp between 25-800 °C at 20 °C min-1 and nitrogen flow of 100 mLmin-1). BET surface area (SBET), average pore size (dp) and average pore volume (Vp) of all materials were measured on ASAP 2020 Plus Version 2.00 using low-temperature nitrogen sorption (–196 °C). SEM-EDX images of all materials were obtained on a Phenom Pro Desktop SEM instrument equipped with an EDS detector (15 kV) (Thermo Fischer Scientific). 29Si MAS NMR of trifloaluminate SILP (1) material was recorded at 59.517 MHz using a Bruker HP-WB high-speed MAS probe. 1H NMR and 13C NMR spectra were obtained on a Varian system (400 MHz and 101 MHz, respectively).

3. Results and discussion

3.1. Trifloaluminate SILP catalysts synthesis

Lewis acidic type triflometallate ILs became alternative for poorly stable and highly corrosive chlorometallate ILs [8, 10]. Superior moisture stability of ILs derived from triflate anions prolongs its catalytic performance and facilitate synthesis procedures. In this work, major studies are focused on trifloaluminate ILs due to a relatively low price of aluminium species. Until now, the application of trifloaluminate ILs as homogenous catalysts was described [20, 21] and recent findings have demonstrated their efficiency when chemically grafted to silica hybrid materials, as MgO-SiO2 and CaO-SiO2 as well [22]. During the immobilization of chloroaluminate ILs via triethoxysilyl groups situated in the cation, and subsequent addition of aluminium chloride for anion complexation, the creation of bonds between the aluminium and oxygen located on the silica surface and inside the pores can occurred as a side process which lower the activity of the final catalyst [7, 8]. Given this circumstance, the primary objective of this study was to determine the accurate sequence of steps employed in the synthesis of SILP systems utilizing triflometallate ILs.

A porous silica material with a hierarchical pore structure comprising micro-, meso-, and macropores was selected as a matrix for trifloaluminate SILP chemical immobilization. Such silica structure facilitates improved mass transport of organic reagents to and from active sites due to their unique design. The interconnected macropores serve as main transport pathways to smaller micro/mesopores, what play a crucial role in the activity of catalysts based on the matrix and selectivity of chemical reactions [14, 28, 29].

A silica porous material was created following a previously outlined method [14, 28, 29]. This involved employing porogens of varying sizes (such as polyethylene glycol and cetyltrimethylammonium bromide), along with inducing and freezing the transitional structures resulting from the phase separation process. The composition led to the formation of a porous, interconnected, open network with macropores of micrometer size (see Fig. S9-S12 SI). In addition to the macropores, the material also exhibited textural mesopores with an average diameter of approximately 19 nm, a BET surface area of 291.8 m2/g,  and a total pore volume of 1.14 cm3/g, (determined through low temperature nitrogen adsorption). Further modification of the surface structure with ionic liquid may improve their properties and application prospects.

To explore the influence of the sequence of silica surface modification with trifloaluminate IL, the three different approaches of the immobilization were studied. All applied methods started from the synthesis of [tespmim]Cl to provide triethoxysilyl functionality in to ILs structure as a linker with hydroxyl groups on silica surface [7, 14] as shown on Scheme 1. For all methods χAl(OTf)3 = 0.15 (molar fraction of Al(OTf)3 used for complexation of [OTf]- anion) was chosen to design catalyst with medium-strength Lewis acidity.

Method 1 for the synthesis of SILP (1) is based on synthesis of trifloaluminate IL ([tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15) in the first step, via anion exchange of [tespmim]Cl with silver triflate (1:1, n/n) [22], complexation reaction with aluminium triflate (χAl(OTf)3 = 0.15) at 95°C [17], and subsequent chemical immobilization on silica surface at 90°C in toluene [7] (loading of IL 25.3 wt%; Supplementary Materials Fig.S2). Next approach (Method 2 for the synthesis of SILP (2)) implies the synthesis of [tespmim][OTf], then chemical grafting to silica matrix (loading of IL 19.2 wt%; Supplementary Materials Fig.S3), and further addition of aluminium triflate (χAl(OTf)3 = 0.15) at 95°C in acetonitrile (loading of IL 19.2 wt%; Supplementary Materials Fig.S4). Method 3 for the synthesis of SILP (3) assumed direct bonding of [tespmim]Cl to the silica surface (loading of IL 19.7 wt%; Supplementary Materials Fig.S5), then anion exchange to aluminium triflate with LiOTf in ethyl acetate (loading of IL = 19.7 wt%; Supplementary Materials Fig.S6), ending with complexation with aluminium triflate (χAl(OTf)3 = 0.15) at 95°C in acetonitrile (loading of IL 19.7 wt%; Supplementary Materials Fig.S7). All three approaches are leading to SILP materials with catalytic properties. For comparison reasons SiO2-Al(OTf)3 was also fabricated using for the synthesis the same silica material and aluminium triflate dissolved in acetonitrile and stirred at 90°C (loading of Al(OTf)3 36.5 wt%; Supplementary Materials Fig.S8).

TGA, BET, SEM-EDX and 29Si MAS NMR analyses were performed to characterise the obtained SILP materials and determine the choice of the most preferable immobilization procedure. The loading of [tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15 on silica matrix for SILP(1-3) materials was measured by TGA (Table 1). The highest IL loading was achieved for SILP (1) 25.3 wt% (Supplementary Materials Fig.S2), while for the SILP(2) and SILP(3) reached 19.7 wt% and 19.2 wt% (Supplementary Materials Fig.S4,S7), respectively. The decreasing BET surface area after IL immobilization on the silica surface was observed for all the SILP materials, what confirms the presence of IL on the carrier (Table 1). Moreover, similar values of pore volumes and pore diameters size mean that IL immobilization process did not clog up the pores providing effortless reagents flow through the catalyst during the reaction. Determined high amount of IL loading on the silica mainly arises from well-defined hierarchical pore structure and availability of evenly distributed numerous hydroxyl groups that facilitate the effective binding of a substantial amount of IL.

Scheme 1. Synthesis of SILP (1-3) via three different methods.

The developed porosity of SILP (1-3) is also clearly visible at SEM images supplied with EDX analyses demonstrating presence of new elements, such as Al, C, N, S on the silica matrix (Supplementary Materials Fig.S9-S12). The chemical attachment of [tespmim][OTf-Al(OTf)3], χAl(OTf)3 = 0.15 to the silica surface was proven by 29Si MAS NMR (Supplementary Materials Fig.S13). The MAS-NMR spectra indicate the vanishing of signals related to (SiO)2Si-(OH)2 and (SiO)3Si-OH groups, alongside the emergence of a new signal at −66 ppm. This clearly demonstrates the IL was chemically grafted to the siliceous surface. The reference material SiO2-Al(OTf)3 was characterized by slightly lower value of surface area (161.7 m2g-1) in comparison with SILP (1-3) materials with similar pore’s size and 36.5 wt% of Al(OTf)3 loading on the surface (Supplementary Materials Fig.S8).

Table 1. Characterisation and catalytic activity of multimodal silica and catalysts based on Al(OTf)3.

| Material | SBET, m2g-1 | Vp, cm3g-1 | dp, nm | IL loading, wt% ±0.3a | MA conversion, % ±2.0 |
| --- | --- | --- | --- | --- | --- |
| SiO2 | 291.8 | 1.14 | 19.7 | - | - |
| SILP (1) | 225.1 | 1.10 | 19.4 | 25.3 | 97.45 |
| SILP (2) | 217.9 | 1.05 | 19.3 | 19.2 | 97.31 |
| SILP (3) | 218.6 | 0.98 | 19.2 | 19.7 | 97.45 |
| SiO2-Al(OTf)3 | 161.7 | 0.66 | 18.9 | 36.5b | 91.17c |

adetermined by TGA; the standard deviation of 3 replicate experiments bAl(OTf)3 wt%, cmeasured after 240 min

Reaction conditions: isoprene 3 mmol, maleic anhydride 2 mmol, acetonitrile 0.5 mL, SILP (1-3) or SiO2-Al(OTf)3 catalyst contains 0.1 mol% Al(OTf)3 per maleic anhydride, 20°C, 180 min. MA conversion was determined using GC.

3.2. Catalytic activity of trifloaluminate SILP catalysts in Diels-Alder reaction

Heterogeneous trifloaluminate SILP (1-3) materials were tested as catalysts in a model Diels-Alder reaction between maleic anhydride (MA) and isoprene (Scheme 2). The cycloadducts formed during the Diels-Alder reaction are mostly used as intermediates in the production of pharmaceuticals, agrochemicals, flavours, fragrances, surfactants, or bio-based polymers. [30, 31]. The Diels-Alder cycloaddition reaction is commonly conducted using harmful organic solvents, and often requires extended reaction times, occasionally even under elevated pressure. As an illustration, cycloaddition between maleic anhydride and isoprene was reported in hexane/nitrobenzene mixture for over 24 h [32]. Other studies presented benzene/CO2 system at 33°C, 7.5 MPa in the presence of AlCl3 catalyst for the same reaction [33].  Higher temperatures for this model reaction 65-75°C and reaction time up to 8 h for the reaction in cyclohexane were also applied [34]. Afresh report showed chlorogallate(III) SILP catalyst, that shorten the reaction time to 180 minutes under room temperature [14]. To overcome all drawbacks related to the presented literature reports concerning Diels-Alder cycloaddition, we offer water-tolerant trifloaluminate SILP catalyst as more ecologically friendly alternative to produce cycloadducts in more efficient way.

Scheme 2. Diels-Alder cycloaddition between maleic anhydride and isoprene in the presence of SILP catalyst.

The results of maleic anhydride and isoprene cycloaddition in the presence of SILP(1-3) catalysts containing 0.1 mol% of Al(OTf)3 per maleic anhydride are presented in Table 1 using 1.5 molar ratio of reactants and acetonitrile as solvent. The conversion of maleic anhydride was determined using GC and no other by products were detected (selectivity 100%).  SILP (1-3) exhibited high catalytic activity in this process enabling approximately 97.5% conversion of maleic anhydride. Additionally, a comparison in catalytic performance was undertaken between developed SILP catalysts and aluminium triflate chemically attached to the silica (SiO2-Al(OTf)3), and the results were shown in Table 1. Significantly reduced values of BET surface area 161.7 m2g-1, volume of pores 0.66 cm3g-1 and higher loading of Al(OTf)3 on the silica surface (36.5 wt%, Supplementary Materials Fig.S8) led to deterioration of free reagents flow through the material, and in consequence decline its catalytic performance.

At this stage of research, given the lack of differences in catalytic activity among the acquired SILP (1-3) materials, SILP(1) was selected for subsequent optimization of reaction conditions in the model process. The studies on the influence of a solvent amount on maleic anhydride conversion showed that 0.5 mL of acetonitrile is the optimum volume per 2 mmole of maleic anhydride (4 mmol/cm3) (Figure 1). Lower amounts hindered the effective mixing of reagents due to the high volume of catalyst. Next, the influence of maleic anhydride : isoprene molar ratio on maleic anhydride conversion was determined (Figure 2). The most beneficial result was obtained for 1:1.5 MA : isoprene molar ratio. A subsequent increase in the quantity of isoprene did not influence the enhancement of maleic anhydride conversion rates. Finally, the influence of catalyst loading on maleic anhydride conversion was examined and presented in Figure 3. The results showed that the 0.1 mol% of Al(OTf)3 per MA is enough for efficient catalysis. Lower amounts were not sufficient to obtained full conversion of substrate.

Figure 1. The influence of acetonitrile amount on MA conversion.

Reaction conditions: isoprene 3 mmol, maleic anhydride 2 mmol, acetonitrile 0.5-2.5 mL, SILP(1) catalyst with 0.1 mol% of Al(OTf)3 per maleic anhydride, 20°C. MA conversion was determined using GC.

Figure 2. The influence of maleic anhydride : isoprene molar ratio on MA conversion.

Reaction conditions: isoprene 2-5 mmol, maleic anhydride 2 mmol, acetonitrile 0.5 mL, SILP(1) catalyst with 0.1 mol% of Al(OTf)3 per maleic anhydride, 20°C. MA conversion was determined using GC.

Figure 3. The influence of catalyst loading on MA conversion.

Reaction conditions: isoprene 3 mmol, maleic anhydride 2 mmol, acetonitrile 0.5 mL, SILP (1) catalyst with 0.05-0.5 mol% of Al(OTf)3 per maleic anhydride, 20°C. MA conversion was determined using GC.

The next challenge was to demonstrate the stability of obtained SILP catalysts in consequent cycles of the reaction. And this time the differences in catalytic activity was clear revealing the importance of the sequence of silica surface modification steps.

Recycling of the SILP (1-3) and SiO2-Al(OTf)3 catalysts was studied over 10 reaction cycles under optimised conditions (Figure 4). All catalysts were used in the same amounts, calculating for active phase. The highest stability was determined for SILP (1) material with no decline in catalytic stability in all studied cycles. SILP (2) and SILP (3) started loss their activities in fifth reaction cycle, conversion of MA after 180 min dropped to 91% and 90% respectively). It is worth to underline that both materials were prepared with the addition of aluminium triflate after the immobilization of IL ([tespmim][OTf] for SILP (2) or [tespmim]Cl for SILP (3)) on the surface of silica.

It can indicate that some aluminium triflate species embedded straight to the silica surface and partially the complexation reaction did not occur or some moieties of [tespmim][OTf]-Al(OTf)3, χAl(OTf)3 = 0.15 leached from silica matrix (loading of IL 10.8 wt% SILP (2), 9.2 wt% SILP (3) after fourth cycle, Supplementary Materials Fig.S14,S15). According to TGA analysis (Supplementary Materials Fig.S16) it can be observed that SILP (1) catalyst remained almost the same quantity of ILs (25.1 wt%) as before the recycling runs (25.3 wt%). Generally, the incorporation of aluminium triflate into the ionic liquid structure ensures stability and prevents the leaching of the active phase from the material. This was confirmed by experiments involving the recycling of SiO2-Al(OTf)3 where the Al(OTf)3 is directly bounded to the surface what causing the lower activity expressed by only 82% conversion of MA after 180 minutes in third cycle.

Figure 4. The influence of IL immobilisation method on SILP (1-3) catalysts recycling; SILP (1) bue; SILP (2) purple; SILP (3) light purple; SiO2-Al(OTf)3 yellow.

Reaction conditions: isoprene 3 mmol, maleic anhydride 2 mmol, acetonitrile 0.5 mL, SILP (1-3) catalysts with 0.1 mol% of Al(OTf)3 per maleic anhydride, 20°C. MA conversion was determined using GC, reaction time 180min.

Summing up SILP (1) catalyst ensures great catalytic performance in cycloaddition of maleic anhydride and isoprene in comparison with SiO2-Al(OTf)3, and Al(OTf)3 (Table 2). Nearly full conversion of maleic anhydride after 180 min in the presence of SILP (1) with only of 0.1 mol% of Al(OTf)3 was gained. Major advantage above homogeneous form of catalyst [tespmim][OTf-Al(OTf)3)] is effortless and low-cost SILP(1) catalyst recycling and its extremely high stability under evaluated reaction conditions. Developed heterogeneous SILP catalytic system provides sustainability for studied process.

Table 2. The influence of the structure of Al(OTf)3-based catalysts on catalytic activity.

| Catalyst | Time, min | MA conversion, % |
| --- | --- | --- |
| SILP (1) | 180 | 97.45 |
| SiO2-Al(OTf)3 | 240 | 91.17 |
| [tespmim][OTf-Al(OTf)3)] | 180 | 95.57 |
| Al(OTf)3 | 240 | 84.01 |

Reaction conditions: isoprene 3 mmol, maleic anhydride 2 mmol, 0.5 mL acetonitrile, catalyst with 0.1 mol% of Al(OTf)3 per maleic anhydride, 20°C. MA conversion was determined using GC.

To prove the versatility of developed method for producing maleic anhydride cycloadducts in the presence of SILP (1) catalyst dienes, such as isoprene, cyclopentadiene, α-terpinene, myrcene and ocimene, were tested (Table 3). It was examined that the SILP (1) catalyst was active for all chosen dienes, and almost full conversions of maleic anhydride were achieved in short reaction times.

Table 3. Diels-Alder synthesis of maleic anhydride adducts in the presence of SILP (1) as a catalyst under evaluated batch conditions.

| Dienophile | Diene | Product | Time, min | MA conversion, % |
| --- | --- | --- | --- | --- |
|  |  |  | 180 | 97.5 |
|  |  |  | 1 | 99.9 |
|  |  |  | 60 | 97.9 |
|  |  |  | 60 | 98.7 |
|  |  |  | 60 | 98.2 |

Reaction conditions: diene 3 mmol, maleic anhydride 2 mmol, acetonitrile 0.5 mL, SILP (1) catalyst with 0.1 mol% for Al(OTf)3 per maleic anhydride, 20°C. MA conversion was determined using GC.

3.3. Trifloaluminate SILP catalysts in continuous flow Diels-Alder reaction

Based on the promising results obtained in the batch system, we decided to test the developed trifloaluminate SILP (1) catalyst for the continuous-flow synthesis. The catalytic activity experiments were performed in a fully automated Syrris Asia column flow reactor equipped with two pumps. Pump A was pumping a solution of maleic anhydride in acetonitrile, while pump B was utilized for isoprene.  The steams were merged in a standard T-mixer, and then flowed to the column reactor filled with 0.3 g of SILP (1) material.

Table 4. Catalytic activity of SILP (1) in Diels-Alder cycloaddition between maleic anhydride and isoprene under continuous flow conditions.

| Flow, pump A, mLmin-1 | Flow, pump B, mLmin-1 | A:B ratio (n:n) | Catalyst loading, g | Residence time, min | Time, h | Conv., % | TOF, h-1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0500 | 0.0100 | 1:1 | 0.3 | 18.3 | 6 | 57.7 | 134.7 |
|  |  |  |  |  | 24 | 58.5 | 136.6 |
|  |  |  |  |  | 48 | 58.1 | 135.6 |
| 0.0490 | 0.0110 | 1:1.12 | 0.3 | 18.3 | 6 | 67.8 | 155.1 |
|  |  |  |  |  | 24 | 68.5 | 156.7 |
|  |  |  |  |  | 48 | 67.7 | 154.9 |
| 0.0480 | 0.0120 | 1:1.25 | 0.3 | 18.3 | 6 | 71.2 | 159.6 |
|  |  |  |  |  | 24 | 71.6 | 160.5 |
|  |  |  |  |  | 48 | 71.3 | 159.8 |
|  |  |  |  |  | 6 | 79.4 | 170.5 |
| 0.0460 | 0.0140 | 1:1.5 | 0.3 | 18.3 | 24 | 78.6 | 168.8 |
|  |  |  |  |  | 48 | 78.9 | 169.5 |
| 0.0450 | 0.0150 | 1:1.67 | 0.3 | 18.3 | 6 | 77.7 | 163.3 |
|  |  |  |  |  | 24 | 77.8 | 163.5 |
|  |  |  |  |  | 48 | 76.9 | 161.6 |
|  |  | 1:2.5 | 0.3 |  | 6 | 78.6 | 146.8 |
| 0.0400 | 0.0200 |  |  | 18.3 | 24 | 77.6 | 144.9 |
|  |  |  |  |  | 48 | 78.1 | 145.9 |
|  |  |  |  |  | 6 | 82.9 | 148.3 |
| 0.0383 | 0.0113 | 1:1.5 | 0.3 | 22.0 | 24 | 83.0 | 148.4 |
|  |  |  |  |  | 48 | 82.8 | 148.1 |
|  |  |  |  |  | 6 | 88.6 | 127.0 |
| 0.0307 | 0.0093 | 1:1.5 | 0.3 | 27.5 | 24 | 89.0 | 127.6 |
|  |  |  |  |  | 48 | 88.8 | 127.3 |
|  |  |  |  |  | 6 | 96.8 | 103.6 |
| 0.0230 | 0.0070 | 1:1.5 | 0.3 | 36.7 | 24 | 97.2 | 104.4 |
|  |  |  |  |  | 48 | 97.3 | 104.5 |

Reaction conditions: pump A: maleic anhydride (2M in acetonitrile), pump B: isoprene, 20°C. MA conversion was determined using GC.

Experiments were carried out in various molar ratios of maleic anhydride to isoprene ranging from 1:1 to 1:2.5 and variable total flow rates ranging from 0.03 to 0.06 mLmin-1, the obtained results were collected in Table 4. To maintain the stable reagents flow through the whole system, the backpressure regulator was introduced after the reactor and set to 2 bar (Fig. 5).

The influence of the molar ratio of substrates on the maleic anhydride conversion was examined for 0.06 mLmin-1 of total reagents flow. The results obtained in continuous-flow system are quite compatible to those derived in batch. The conversion of maleic anhydride increased along with increasing molar ratio until it reached the 1:1.5 maleic anhydride to isoprene molar ratio. Further increasing the molar ratio of substrates did not lead to higher maleic anhydride conversion.

The influence of the residence time on the maleic anhydride conversion was determined for 1:1.5 maleic anhydride : isoprene molar ratio in total flow from 0.03 to 0.06 mLmin-1. As shown in Table 4, increasing the residence time from 18.3 to 36.7 minutes resulted in higher catalyst performance, with substrate conversion improving from approximately 78% to 97%. A direct comparison of the residence times for batch and continuous systems indicated better efficiency for flow synthesis. The same maleic anhydride conversion value 97% was achieved in 36.7 min in flow and 180 min in batch system. Through all conducted experiments stable catalytic activity for 48 h duration of each attempt could be observed.

Exceptional stability of trifloaluminate SILP (1) material in batch and continuous-flow tests prompted the studies on catalyst long-term stability. The experiment was carried out under optimised conditions, 1:1.5 maleic anhydride : isoprene molar ratio in total flow of 0.06          mLmin-1 at 20°C (Figure 5).

Figure 5. Catalytic stability of SILP (1) in a flow Diels-Alder cycloaddition between maleic anhydride and isoprene.

Reaction conditions: isoprene 0.007 mL/min, maleic anhydride 0.023 mL/min (2 M in acetonitrile), 0.3 g SILP (1) catalyst, 20°C. MA conversion was determined using GC.

The developed SILP (1) catalyst exhibited extremely stable activity, achieving a 97% maleic anhydride conversion over 432 h with a TOF of 104.3 h-1. Superactivity of trifloaluminate SILP (1) catalyst under flow conditions can be explain by the use of multimodal porous silica used as a support for IL. Advanced porous nature of silica intensified reagents mixing and flow through the material improving catalytic properties. The proposed continuous-flow system, utilizing trifloaluminate SILP (1) material, ensured efficient performance in the Diels-Alder reaction, resulting in high maleic anhydride conversion without the need for catalyst separation from the post-reaction mixture. The transformation of Diels-Alder synthesis to continuous-flow process significantly improved its sustainability.

4. Conclusions

In this study, the effective catalysis of in Diels-Alder reaction was reached after carful optimization of the catalyst preparation.Three approaches were explored for the chemical immobilization of trifloaluminate ionic liquid catalyst onto a microporous/mesoporous silica support. The most superior catalytic performance, attaining maleic anhydride conversion of over 97% in ten reaction cycles, was achieved by initially synthesizing the trifloaluminate ionic liquid. Subsequently, this was bound to the silica surface using a 25 wt% loading of the ionic liquid. This successful transformation of the Diels-Alder reaction into continuous flow synthesis resulted in a 97% conversion of maleic anhydride over 432 h, exhibiting a Turnover Frequency (TOF) of 104.3 h-1.

Table 5. The comparison of reaction conditions for continuous synthesis of Diels-Alder adducts.

| Catalyst | Diels-Alder model reaction | Reaction conditions | Parametersa | Lit. |
| --- | --- | --- | --- | --- |
| Zeolite H-Beta | Cyclopentadiene and methyl acrylate | 0.2 mLmin-1, τ=1.8 min, dichloromethane, 100°C | α=95%, 89:11 (endo/exo), (7 h) | [35] |
| Zeolite H-Beta | Isoprene and maleic anhydride | 0.1 mLmin-1, τ=40.6 min, acetonitrile, 80°C | y= 76%, (72 h) | [36] |
| MacMillan catalyst attached to silica | Cyclopentadiene and trans-cinnamaldehyde | 5 μLmin-1, τ=10 h, rt | y=95%, 83% (endo), (150 h) | [37,38] |
| MacMillan catalyst copolymerized with divinylbenzene | Cyclopentadiene and trans-cinnamaldehyde | 5 μLmin-1, τ=5h, acetonitrile:water (95:5; v/v), rt | y=61%, 90% (endo) | [39] |
| MnO2 | Cyclopentadiene and tert-butyl N-hydroxycarbamate | 0.03 mLmin-1, τ=30 min, dichloromethane, rt | y=99% | [40] |
| SILP(1) | Isoprene and maleic anhydride | 0.03 mLmin-1, τ=36.7 min, acetonitrile, rt | α=97%, (432 h) | This work |

aa- conversion; y - yield

In the literature, limited reports are available concerning the use of continuous flow technic for the synthesis of Diels-Alder cycloadducts (Table 5). Stevens et al. performed cycloaddition between cyclopentadiene and methyl acrylate in continuous system in the presence of various zeolites as Y, Ultrastable Y, ZSM-5, Beta and Mordenite. High conversion (>95%) and endo-selectivity (89:11) were obtained for this process. What is more, it was reported that flow synthesis achieved 14 times higher production in comparison to batch [35]. Kobayashi et al. used zeolite Beta in continuous cycloaddition of isoprene and acrolein. The catalyst was recyclable for 4 times and showed stability over 72 h [36]. Puglisi et al. investigated chiral MacMillan organocatalyst immobilized on silica for continuous cycloaddition between cyclopentadiene and unsaturated aldehydes. Catalyst assured high yields and satisfying selectivities for 150 h [37,38]. The same group presented chiral MacMillan catalyst grafted into polymer monolith in continuous flow Diels-Alder reaction. Again, high enantioselectivities (90%) and productivities at ambient temperature were reached [39]. Yamamoto et al. showed two catalytic systems for Diels-Alder continuous process. First was based on homogeneous CuCl/pyridine and the second one on heterogeneous MnO2 catalyst. During this studies, high yields (>99%) and methods versatility were reported [40].

The proposed in this work catalytic system SILP (1) is characterised with the highest efficiency among others. Mild reaction conditions at room temperature are sufficient to obtain high yield of cycloadduct versus 80-100oC required for zeolites. In this work due to the consistent design of  trifloaluminate SILP catalysts via various synthesis pathways the high catalytic performance was reached, with special emphasis on catalyst stability.

Credit Author Statement：

Anna Wolny: conceptualization, investigation, data curation, validation, writing - original draft, visualisation; Piotr Latos: formal analysis; Katarzyna Szymańska: investigation, validation, writing - original draft; Sebastian Jurczyk: formal analysis; Anna Chrobok: conceptualization, supervision, project administration, conceptualization, writing - review & editing.

Declaration of interests

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

Acknowledgements

This work was funded by the National Science Centre, Poland. Grant no. UMO-2020/37/B/ST8/00693.

5. References

[1] Scheldon, R.A. Green Chem. 19 (2017) 18–43. doi.org/10.1039/C6GC02157C

[2] De los Ríos, A.P.; Irabien, A.; Hollmann, F.; Fernández, F.J.H. J. Chem. 2013, (2013), 402172. doi.org/10.1155/2013/402172

[3] Ratti, R. SN Appl. Sci. 2 (2020) 263. doi.org/10.1007/s42452-020-2019-6

[4] Amarasekara, A.S. Chem. Rev. 116 (2016) 6133–6183. doi.org/10.1021/acs.chemrev.5b00763

[5] Giacalone, F.; Gruttadauria, M. ChemCatChem. 8 (2016) 664–684. doi.org/10.1002/cctc.201501086

[6] Schwieger, W.; Selvam, T.; Klumpp, M.; Hartmann, M., in: Fehrmann, R., Riisager, A., Haumann, M. (Eds.), Supported Ionic Liquids: Fundamental and Applications, Wiley-VCH Verlag GmbH: Berlin, Germany, 2014, pp. 37–74.

[7] Valkenberg, M.H.; deCastro, C.; Hölderich, W.F. Green Chem. 4 (2001) 88–93. doi.org/10.1039/B107946H

[8] Skoda-Földes, R. Molecules 19 (2014) 8840–8884. doi.org/10.3390/molecules19078840

[9] Vafaeezadeh, M.; Alinezhad, H. J. Mol. Liq. 218 (2016) 95–105. doi.org/10.1016/j.molliq.2016.02.017

[10] Wolny, A.; Chrobok, A. Molecules 27 (2022) 5900. doi.org/10.3390/molecules27185900

[11] Gu,Y. ;Li,G. Adv. Synth. Catal. 351 (2009) 817–847. doi.org/10.1002/adsc.200900043

[12] Wolny, A.; Chrobok, A. Nanomaterials 11 (2021) 2030. doi.org/10.3390/nano11082030

[13] Garcia-Verdugo, E.; Lozano, P.; Luis, S.V., in: Fehrmann, R., Riisager, A., Haumann, M., (Eds.), Supported Ionic Liquids: Fundamental and Applications, Wiley-VCH Verlag GmbH: Berlin, Germany, 2014, pp. 351–368.

[14] Matuszek, K.; Chrobok, A.; Latos, P.; Markiton, M.; Szymańska, K.; Jarzębski, A.; Swadźba-Kwaśny, M. Catal. Sci. Technol. 6 (2016) 8129–8137. doi.org/10.1039/C6CY01771A

[15] Kumar, P.; Vermeiren, W.; Dath, J.-P.; Hoelderich, W.F. Appl. Catal. A Gen. 304 (2006) 131–141. doi.org/10.1016/j.apcata.2006.02.030

[16] Liu, S.; Shang, J.; Zhang, S.; Yang, B.; Deng, Y. Catal. Today 200 (2013) 41–48. doi.org/10.1016/j.cattod.2012.06.023

[17] Wang, G.; Yu, N.; Peng, L.; Tan, R.; Zhao, H.; Yin, D.; Yin, D. Catal. Lett. 123 (2008) 252–258. doi.org/10.1007/s10562-008-9415-7

[18] Zhao, H.; Yu, N.; Wang, J.; Zhuang, D.; Ding, Y.; Tan, R.; Yin, D. Microporous Mesoporous Mater. 122 (2009) 240–246. doi.org/10.1016/j.micromeso.2009.03.006

[19] Jyothi, T.M.; Kaliya, M.L.; Herskowitz, M.; Landau, M.V. Chem. Commun. 11 (2001) 992–993. doi.org/10.1039/B101843O

[20] Latos, P., Culkin, A., Barteczko, N., Boncel, S., Jurczyk, S., Brown, L. C., Nockemann P., Chrobok A., Swadźba-Kwaśny, M. Frontiers in Chemistry, 6 (2018) doi:10.3389/fchem.2018.00535

[21] Latos, P.; Szelwicka, A.; Boncel, S.; Jurczyk, S.; Swadzba-Kwasny, M.; Chrobok, A. ACS Sustain. Chem. Eng., 7 (2019) 5184–5191. doi.org/10.1021/acssuschemeng.8b06066

[22] Latos, P.; Wolny, A.; Zdarta, J.; Ciesielczyk, F.; Jurczyk, S.; Jesionowski, T.; Chrobok, A. Environ. Technol. Innov. 31 (2023) 103164. doi.org/10.1016/j.eti.2023.103164

[23] Latos, P.; Wolny, A.; Chrobok, A. Materials 16 (2023) 2106. https://doi.org/10.3390/ma16052106

[24] Haumann, M., in: Shiflett, M.B. (Eds.), Commercial Applications of Ionic Liquids, Springer: Cham, Switzerland, 2020; pp. 49–67.

[25] Burguete, M.I.; García-Verdugo, E.; Karbass, N.; Luis, S.V.; Sans, V.; Sokolova, M. Pure Appl. Chem. 81 (2009) 1991–2000. doi.org/10.1351/PAC-CON-08-11-02

[26] Marinkovic, J.M.; Riisager, A.; Franke, R.; Wasserscheid, P.; Haumann, M. Ind. Eng. Chem. Res. 58 (2019) 2409–2420. doi.org/10.1021/acs.iecr.8b04010

[27] Lozano, P.; Cerón, S.N.; Serrano, J.; Pérez, J.; Sánchez, G.; Garcia-Verdugo, E.; Luis, S.V. Mini-Rev. Org. Chem. 14 (2017) 65–74. doi.org/10.2174/1570193X13666161103145723

[28] Drożdż, A.; Chrobok, A.; Baj, S.; Szymańska, K.; Mrowiec-Białoń, J.; Jarzębski, A. Appl. Catal. A, 467 (2013) 163. doi.org/10.1016/j.apcata.2013.07.009

[29] Chrobok, A.; Baj, S.; Pudło, W.; Jarzębski, Appl. Catal. A, 366 (2009) 22. doi.org/10.1016/j.apcata.2009.06.040

[30] Funel, J.A., Abele, S. Angew. Chem. 52 (2013) 3822 – 3863. doi.org/10.1002/anie.201201636

[31] Briou, B.; Améduri, B.; Boutevin, B. Chem. Soc. Rev. 50 (2021) 11055-11097. doi.org/10.1039/D0CS01382J

[32] Lv, X-C.; Tan, Z-C.; Shi, Q.; Zhang, H-T.; Sun, L-X.; Zhang, T. J. Chem. Eng. Data, 36 (2005) 932-935. doi.org/10.1016/j.jct.2004.05.008

[33] Tomotaka, N.; Yusuke, I.; Masaki, S.; Yoshio, I.; Yasuhiko, A. AIChE J., 44 (1998) 1706-1708. doi.org/10.1002/aic.690440723

[34] Ikushima, Y.; Saito, N.; Arat, M. Bull Chem. Soc Jpn., 64 (1990) 282-284. doi.org/10.1246/bcsj.64.282

[35] Seghers, S., Protasova, L., Mullens, S., Thybaut, J. W., Stevens, C. V. Green Chem. 19 (2017) 237–248. doi.org/10.1039/C6GC02334G

[36] Masuda, K., Agalave, S. G., Chen, W., Onozawa, S.-y., Shimada, S., Sato, K., Kobayashi, S., Asian J. Org. Chem. 12 (2023) e202200557. doi.org/10.1002/ajoc.202200557

[37] Porta, R., Benaglia, M., Chiroli, V., Coccia, F., Puglisi, A. Israel Journal of Chemistry, 54 (2014) 381–394. doi.org/10.1002/chin.201440033

[38] Chiroli, V., Benaglia, M., Cozzi, F., Puglisi, A., Annunziata, R., Celentano, G. Organic Letters, 15 (2013) 3590–3593. doi.org/10.1021/ol401390z

[39] Chiroli, V., Benaglia, M., Puglisi, A., Porta, R., Jumde, R. P., Mandoli, A. Green Chem. 16 (2014) 2798. doi.org/10.1039/C4GC00031E

[40] Nakashima, E., Yamamoto, H. Chem. Commun. 51 (2015) 12309–12312. doi.org/10.1039/C5CC03458B