## Slide 1: Realising growth of MoS2, WS2 and MoxW1-xS2 nano films for application in Photoelectrochemical Water-splitting
Vikas Jangra
Chair of Electronic Devices
RWTH Aachen

## Slide 2: What is Photoelectrochemical Water Splitting ?
Requirements for a semiconductor :
Bandgap ~ 1.5 – 2.4 eV
High Optical absorption
High electron Mobility
*Freehydrocells
P-type and n-type combination of TCOs and TMDs
Stability in strong electrolytes
Noncorrosive
High catalytic properties
HER
OER
*Jiajie Cen et al. Volume 2, Issue 2, 2017
Need :
Clean and sustainable
Solution to fossil fuels
Notes: H2 (cathode) at and O2 (anode) evolution reactions …….thermodinamically and kinetically challenging
Electrons and holes : charge carrier separations
Energy losses : rection barriers
Electrodes : good conductivity, non corrosive, large surface area
Maximum absorption : TCOs and TMDs
Just for questions : Conduction band : H2 redox reaction and valence band : O2 redox reaction
TiO2 very high band gap – UV range and high recombination rate.
Diffusion length should be less than recombination lifetime

## Slide 3: Why MoS2 and WS2?
5. Lee.J et.al.,Sci Rep 4, 7352 (2014)
1.H.F. Lui et al., CVD Growth of MoS2 based 2D materials
2.www.epfl.ch/labs/lanes/posters/mos2fet-2
3.Zhang, J. et.al.,P. Nat Electron 4
4.lnnano.cnpem.br
Energy band diagram of MoS2
Indirect
Direct
Mo, W
S
1
Semiconducting
High mobility
Lubricating
Photocatalysis
Mechanical strength
Unique properties
Transistors
Memory Devices
2
3
4
Hydrogen Generation
Biosensing
5
D
S
G
Notes: Molybdenum disulfide (MoS₂) has a layered, hexagonal crystal structure,
Molybdenum (Mo) atoms are sandwiched between two layers of sulfur (S) atoms.Each Mo atom is coordinated to six S atoms, forming a trigonal prismatic coordination geometry.
Memristors : defect migration and chage trapping.
This means an electron can directly jump from the valence band to the conduction band (or vice versa) without changing its momentum
Sensitive to environmental changes : Biosensors : proteins, glucose etc.

## Slide 4: MoS2 and WS2 TAC process (Thermally Assisted Conversion) and Growth Parameters
Substate : SiO2 and Sapphire
Sputtered : Molybdenum (Mo)
and Tungsten (W)
Growth Parameters :
Temperature : 600-800 °C
Pressure : 9x10-2 mBar
Notes: Large are Uniform growth : homogenous growth
Scalable : cost efficient

## Slide 5: Structural and Chemical Characterization (Si - 600°C)
x ~ 0.4
Raman
Optical
AFM
A1g and E2g peaks identified for MoS2 and WS2.
Combined signatures of peaks in MoxW1-xS2.
Bandgap evaluated (UV Visible spectra – Tauc Plot).
Surface morphology analysed using AFM.
Application in Photoelectrochemical water splitting in progress.
Si
(381.4)
(407.6)
(418.8)
(351.6)
~ 12.5 nm
~ 11.7 nm
~ 13.8 nm
(353.7)
(379.8)
(412.7)
12.5 nm MoxW1-xS2
Notes: Raman : Characteristic peaks of MoS2, WS2

## Slide 6: Appreciate your Attention !
1.Jiajie Cen et al. Volume 2, Issue 2, 2017
2.Freehydrocells