## Slide 1: 2019PROG702 – July 2022 https://nxtgenwood.ie/ https://twitter.com/NEXTGENWOOD1 https://www.linkedin.com/company/nxtgenwood/
NXTGENWOOD & TRANSLATE
Fabrication and Optimization of Ionic Nanofluidic Harvester
-Nano-wood for Sustainable Conversion of Heat to Electricity
ANJALI ASHOKAN
3rd Year PhD
Material Chemistry & Analysis Group
University College Cork
Supervised By
Prof. Justin Holmes

## Slide 2: TABLE OF CONTENT
Introduction
Functionalisation and Optimisation Cellulose Membranes
  Synthesis/Functionalisation
  Characterisation
  Ionic conductivity
  Thermoelectrics
Summary

## Slide 3: INTRODUCTION
70% of total energy - lost as heat into the atmosphere
An efficient TE device – most of the energy needs can be met.
Thermoelectrics - temperature difference is converted into electric voltages
The basic TEGs configuration
Our focus on the thermoelectric effect based on a nanochannel–electrolyte-based system
Electrolyte - the mobility difference of cations and anions used to enhance the thermoelectric energy generated.
Nanochannels - charged membrane can further affect the thermophoretic mobility of ions.
Charge carriers move or diffuse from the hot end to the cold end, producing electricity.

## Slide 4: Optimisation of Cellulose Membranes for enhancing thermovoltage output.

## Slide 5: 1. Regenerated Cellulose Membrane (RC)
RC – 200 nm pore size
Thickness – around 40 μm
Weight – around 60mg
RC – 450 nm pore size
Thickness – around 70 μm
Weight – around 70mg
RC – 1000 nm pore size
Thickness – around 40 μm
Weight – around 50mg

## Slide 6
Positively charged membrane – CHMAC reaction – (3-Chloro-2-hydroxypropyl)trimethylammonium chloride
Negatively charged membrane – TEMPO Oxidation – 2,2,6,6,-Tetramethylpiperdine 1-oxyl
TEMPO OXIDATION
ETHERIFICATION
CHMAC-RC
TEMPO-RC
RC
Functionalisation of RCs – Synthesis of Positive and Negatively charged membranes
Membrane | Z.P (mV)
200 | -16.9
450 | -14.5
1k | -13
Membrane | Z.P (mV)
200 | -30
450 | -28.9
1k | -22
Membrane | Z.P (mV)
200 | +11
450 | +12.7
1k | +13.4

## Slide 7
Characterisation of Pristine and Functionalised Membranes
Fourier-transform infrared spectroscopy (FT-IR)
a new C=O peak at 1727 cm-1 – Confirms oxidation.
a new peak at 1476 cm-1 corresponding to CH2 bending of methyl groups of cationic substituent – confirms attachment of ammonium group
Intense C=O peak at 1727cm-1 – successful oxidation
Contact Angle Measurements
RC_200 nm – 30.28°
TEMPO-RC_200 nm – 35.63°
CHMAC-RC_200 nm – 51.92°
Pristine membranes were more hydrophilic
Similar C.A values for Pristine and TEMPO-RCs
Increase in hydrophilicity of membranes with CHMAC Reaction – because of the addition of larger organic (2-hydroxypropyl)trimethylammonium group with etherification.

## Slide 8
Lab prepared Cellulose membrane from waste wood chips
Cellulose extracted from wood chips with NaOH, Na2SO3 and H2O2.
15 mg/ml solution used for making the membranes with Vacuum filtration.
2. Cellulose Membrane
Cellulose - Thickness – around 200 µm
Functionalisation
Cellulose
SILANISATION
SILANISATION
3-amino-Cellulose
3-COO--Cellulose
[(Trimethoxysilyl)propyl]ethylenediamine triacetic acid trisodium salt
3-[2-(2-aminoethylamino)ethylamino]propyltrimethoxysilane

## Slide 9
Cellulose Extracted from wood
NaOH/Na2SO3
H2O2
3. Nano-channeled Cellulose Membrane
Functionalisation to induce increases charge density
Charge separation with Temperature gradient
Pine wood
Cellulose
Reference
https://doi.org/10.1038/s41563-019-0315-6

## Slide 10: Effect of Functionalisation on Ionic conductance of Electrolyte

## Slide 11
Ionic Conductivity Measurements of RCs with HCl
Ionic conductivity Cell – Membranes embedded in Polymer Cell; Electrolyte chamber carved at two ends
Membranes |  | Ionic Conductivity (mS/cm)
RC-200 | Pristine | 0.0018
 | TEMPO | 0.51 (around 250 times)
 | CHMAC | 1.18 (around 600 times)
RC-450 | Pristine | 0.0017
 | TEMPO | 0.32 (around 180 times)
 | CHMAC | 0.54 (around 300 times)
RC-1k | Pristine | 0.0010
 | TEMPO | 0.12 (around 100 times)
 | CHMAC | 0.36 (around 350 times)
For each pore sizes - functionalisation has enhanced the ionic conductivity.
Ionic Conductivity Trend
RC-200 > RC-450 > RC-1K
CHMAC-RC-200 – highest conductivity of 1 mS/cm
Electrolyte – 10-4 M HCl
Electrode – Ag/AgCl

## Slide 12: Effect of Functionalisation on Thermovoltage

## Slide 13
Thermovoltage Measurements on RCs
Thermoelectric output measured with membranes infiltrated with 10-4 M HCl, with an increment of 2-degree temperature.
LinkedIn: https://www.linkedin.com/company/nxtgenwood/ Twitter: https://twitter.com/NEXTGENWOOD1 Web: https://biorbic.com/nxtgenwood/

## Slide 14
Thermovoltage Output
LinkedIn: https://www.linkedin.com/company/nxtgenwood/ Twitter: https://twitter.com/NEXTGENWOOD1 Web: https://biorbic.com/nxtgenwood/
Nature of charges
Cellulose and TEMPO-Cellulose – negative thermoelectric output – Membranes of similar charge density
CHMAC-Cellulose – Positive thermoelectric output - CHMAC has opposite charge as of TEMPO and pristine

## Slide 15
Membranes |  | Thermovoltage Output (mV/K)
RC-200 | Pristine | -0.35
 | TEMPO | -1.09
 | CHMAC | 3.68 (10 times enhancement)
RC-450 | Pristine | -0.145
 | TEMPO | -0.89
 | CHMAC | 1.22
RC-1k | Pristine | -0.096
 | TEMPO | -0.36
 | CHMAC | 0.92
With functionalisation, Ionic conductivity and thermoelectric output of the regenerated cellulose membranes have been successfully enhanced
Ionic Conductivity trend – CHMAC-RC-200 > CHMAC-RC-450 > TEMPO-RC-200 > CHMAC-RC-1k > TEMPO-RC-450 > TEMPO-RC-1K > RC-200 > RC-450 > RC-1k
Same trend observed for thermoelectrics – Higher ionic conductivity membranes showed higher thermoelectric output.
LinkedIn: https://www.linkedin.com/company/nxtgenwood/ Twitter: https://twitter.com/NEXTGENWOOD1 Web: https://biorbic.com/nxtgenwood/

## Slide 16: Summary
Cellulose membranes were functionalised with suitable functional groups to enhance the charge density of the membranes
An enhancement in charge density showed positive enhancement in ionic conductivity of electrolytes through the membrane.
- Regenerated cellulose membranes with CHMAC functionalisation enhanced the ionic conductivity around 600 times than of pristine
Increasing the charge density of the membranes can enhance the thermovoltage output as high as 10 times than of pristine
ACKNOWLEDGEMENTS
This research is supported by the European Union's Horizon 2020 research and innovation programme under grant agreement number 964251 (TRANSLATE) , and by Irish Government funding via the DAFM NXTGENWOOD research program (grant agreement: 2019PROG704).

## Slide 17: THANK YOU