Department of Organic Chemical Technology and Petrochemistry, Faculty of Chemistry, Silesian University of Technology, Bolesława Krzywoustego 4, 44-100 Gliwice, Poland. *E-mail: anna.chrobok@polsl.pl

Institute for Engineering of Polymer Materials and Dyes, Lukasiewicz Research Network, Sklodowskiej-Curie 55, PL-87100 Torun, Poland.

Address School of Chemistry, Monash University, Clayton, Victoria 3800, Australia.

The QUILL Research Centre, School of Chemistry and Chemical Engineering, Queen's University of Belfast, David Keir Building, Stranmillis Road, Belfast BT9 5AG, UK. *E-mail: m.swadzba-kwasny@qub.ac.uk

†Electronic supplementary information (ESI) available: Referenced data S1 and S2, detailed experimental information and TGA thermal curves. See DOI: 10.1039/x0xx00000x

Received 00th January 20xx,

Accepted 00th January 20xx

DOI: 10.1039/x0xx00000x

Al(III) and Ga(III) triflate complexes as solvate ionic liquids: speciation and application as recyclable Lewis acidic catalysts

Justyna Więcławik,a Alina Brzęczek-Szafran,a Sebastian Jurczyk,b Karolina Matuszek,c Małgorzata Swadźba-Kwaśny *d and Anna Chrobok *a

This work reports the on first solvate ionic liquids (SILs) based on aluminium(III) or gallium(III) triflate, M(OTf)3 and triglyme (G3). Liquid-phase speciation of these new SILs was studied by multinuclear NMR spectroscopy. Across compositional range of G3:M(OTf)3 mixtures, both metals were found to be in hexacoordinate environment, with both G3 and [OTf]- ligands present in the first coordination sphere, and apparently exchanging through a dynamic equilibrium. The Lewis acidity was quantified by Gutmann acceptor number (AN) and compared to the performance of SILs as Lewis acidic catalysts in model [3+3] cycloadditions. Despite saturated coordination, AN values were high (AN = 70.8 – 93.4), corroborating the dynamic nature of metal-ligand bonding. SILs were fully soluble in the reaction mixtures, in contrast to the corresponding triflate salts. Catalytic performance of SILs was better than that of the corresponding triflate salts, and Ga-SILs were more active than Al-SILs. In conclusion, the new Group 13 SILs can be considered as soluble and catalytically active form of their corresponding metal triflates, with potential uses in catalysis.

Introduction

The concept of functional liquids, in which a metal cation was solvated by L-type ligands, was firstly introduced by Angell in 1965.1 He described hydrates, such as Ca(NO3)2∙4H2O, as a ‘‘new class of molten salt mixtures’’, recognising that solvating the metal cation generates low-melting hydrates with high conductivities, potentially useful as electrolytes.2 In contrast to molten salts, however, thermal stability of such “molten salt mixtures” was limited by the aqua ligand.

A similar approach was used in the design of liquid coordination complexes (LCCs), in which metal halides were combined with sub-equimolar quantities of organic L-donors, e.g. AlCl3 and acetamide, or GaCl3 and trioctylphosphine oxide.3,4 LCCs (Figure 1b), developed as less expensive and more tuneable alternatives to chlorometallate ionic liquids (Figure 1a), were subsequently demonstrated to be Lewis acidic catalysts in an array of reactions: oligomerisation of olefins,5 Diels-Alder cycloaddition,4 and Friedel-Crafts alkylation,6 as well as co-catalysts in heterogenous catalysis through solid catalysts with ionic liquid layer (SCILL).7 However, most reported LCCs, like conventional chlorometallate ionic liquids, are highly corrosive due to high chloride content.

Figure 1. Examples of structures of metal-containing ionic liquids: a) chlorometallate ionic liquid, b) liquid coordination complex (LCC), c) trifloaluminate ionic liquid and d) solvate ionic liquid.

Salts of Lewis acidic metals (M = Al, Ga, Ln) and trifluoromethanesulfonic acid (known as triflates, OTf) are stable in aqueous media, chloride-free and catalytically active at low concentrations.8,9 However, they suffer from poor solubility in most solvents.10,11 In attempt to enhance their solubility, we have developed triflometallate ionic liquids, synthesised by the reaction of triflate ionic liquids and Group 13 triflates (Figure 1c).12 While catalytically active, these ILs were extremely viscous and very expensive. Seeking further alternatives, we have decided to explore the concept of solvate ionic liquids (SILs).

Watanabe and co-workers developed SILs,13–16 exemplified by equimolar mixtures of Li[NTf2] and triglyme (G3), or tetraglyme (G4), for energy storage applications  (Figure 1d). Mandai et al.14 provided formalised criteria for “good” SILs, combining flexible polydentate ligands, solvating a metal (typically from Group 1 or 2), and weakly basic anions, such as bis(trifluoromethanesulfonate)imide, [NTf2]-. These design principles yield long-lived robust cations, in which an alkali metal was solvated by the glyme, and in consequence – to ILs with physico-chemical behaviour different from concentrated electrolyte solutions. “Good” SILs are relatively simple to synthesise, thermally stable, electrically conductive and non-flammable, therefore make very good electrolytes.17–24

Since SILs have been developed in the context of energy storage applications, their uses in catalysis are scarce.25 Eyckens et al. used SILs in Diels-Alder and [2+2] cycloadditions, reporting that higher yields (up to 94%) and improved reaction safety can be achieved by replacing a solution of lithium salt in a molecular solvent with [Li(G3)][NTf2] or [Li(G4)][NTf2], in the formation of oxetanone.26 Obregón-Zúñiga et al. found improved yield and selectivity in asymmetric aldol reaction in the presence of SILs, also [Li(G3)][NTf2] or [Li(G4)][NTf2], due to their involvement in the catalytically active supramolecular aggregate formation.27 Other uses included Kabachnik-Fields reactions,28 stereo- and regioselective ring opening of epoxides,29 and catalytic additives for curing epoxy systems.30 Importantly for this work, all catalytic studies to date have been focussed on Li-based SILs, a weak Lewis acid. Although SILs based on Na, K, Mg and Al are known, they have only been used in energy storage applications.31,32

In this contribution, we combined our expertise in the design and study of Lewis acidic LCCs and ILs, with the potential offered by the solvate ionic liquids design, to report a series of solvate ionic liquids based on triflate salts of aluminium and gallium and triglyme (G3). We delved into the speciation of these materials using multinuclear NMR spectroscopy and probed their acidity with Gutmann Acceptor number (AN). Our investigation revealed intricate speciation patterns and strong Lewis acidity of these new Group 13 SILs, demonstrated directly through a catalytic application in a model [3+3] cycloaddition reaction. The study highlights notable differences in the coordination chemistry and Lewis acidity of Al-SILs and Ga-SILs, providing new insights into the chemistry of Group 13 metals.

Experimental

Materials

Aluminium(III) trifluoromethanesulfonate  (99.9%), triethylene glycol dimethyl ether (99%), triethylphosphine oxide (97%), decane (99%) and isoprene (99%, contains <1000 ppm p-tert-butylcatechol as inhibitor), trimethylaluminum solution 2.0M in toluene, anhydrous toluene (99.8%) were all purchased from Sigma Aldrich and used as received. Phosphoric(V) acid (85% in D2O) was also purchased from Sigma Aldrich. 2,4-Dimethylphenol (99%) and gallium(III) trifluoromethanesulfonate (99%) were purchased from Thermo Fisher Scientific.

General procedure for synthesis of SILs

The SILs were synthesized in a glovebox under an inert argon atmosphere (<0.6 ppm O2 and H2O). The triglyme (G3) and appropriate metal salt M(OTf)3 (Al(OTf)3 or Ga(OTf)3) were weighed into a vial at various molar ratios from 2:1 to 10:1 (χM(OTf)3 = 0.09 - 0.33). The mixture was allowed to react in a glovebox (40-45°C, 3 h), afterwards the heating was turned off and further stirred overnight.

The same procedure was used for Al(NTf2)3 and G3, with cAl(NTf2)3 = 0.09-0.50.

Multinuclear NMR spectroscopy

All NMR spectra (1H, 13C, 19F, 27Al, 31P and 71Ga) were recorded on a Bruker Avance DPX 400 MHz spectrometer. All samples were studied at 297 K, neat using a DMSO-d6 or D2O filled, sealed capillary as an external lock. In the case of 27Al NMR   solution of Al(NO3)3 hydrate in D2O was used as an external reference. In 71Ga NMR spectroscopy, a solution of Ga(NO3)3 hydrate in D2O was used as an external reference and in 19F NMR a fluorobenzene in acetone-d6 was an external reference.

Acceptor Number Determination

Every ionic liquid was sampled into three different NMR tubes and triethylphosphine oxide (TEPO) in the following concentration: 1 %wt, 2 %wt and 3 %wt. An 85% phosphoric(V) acid solution in D2O enclosed in a capillary was used as the external standard. After TEPO dissolved in the ionic liquid the 31P NMR spectra were recorded at room temperature, at 161.89 MHz and recorded at Agilent 400 MHz spectrometer.  Measured 31P NMR chemical shift for each ionic liquid-TEPO concentration arrangement, was extrapolated to infinite dilution of TEPO, δinf. The referential value was TEPO chemical shift in hexane extrapolated to infinite dilution, δinf hex = 0 ppm. For each ionic liquid the acceptor number was calculated based on the formula: AN = 2.348·δinf, as described in the lierature.33,34

General procedure for [3+3] Cycloaddition

All reactions were carried out under a protective atmosphere of argon. The catalyst (1-5 mol% per 1.00 mol of isoprene) was placed into the flask. Then 0.98 g of 2,4-dimethylphenol (8 mmol) and 0.27 g of isoprene (4 mmol) were added along with 0.10 g (0.7 mmol) of decane as internal standard. The reaction was carried out on a magnetic stirrer at various temperatures (20-40 °C). The progress of the reaction was monitored by gas chromatography. The GC analysis were prepared in anhydrous hexane storage over molecular sieves.

Results and discussion

Design of Group 13 SILs

Initial screening experiments included three Group 13 salts: aluminium trifluoromethanesulfonate, Al(OTf)3, gallium(III) trifluoromethanesulfonate, Ga(OTf)3, and aluminium bis(trifluoromethane)sulfonimide, Al(NTf2)3, combined with triethylene glycol dimethyl ether (triglyme, G3).

Considering that non-coordinating anions were reported to be the best candidates for generating “good” SILs, mixtures of Al(NTf2)3 and G3 were tested first. Combinations with high loadings of the metal salt, cAl(NTf2)3 = 0.33 and 0.50, where cAl(NTf2)3 is the molar ratio of Al(NTf2)3, were homogeneous and extremely viscous liquids. Decreasing the molar fraction of Al(NTf2)3 resulted in apparent autocatalytic decomposition: the mixtures darkened and dark-brown, insoluble solid precipitated from the liquid glyme. This explained the absence of literature data on Al(NTf2)3 and glyme mixtures, whereas there are several papers on Al(OTf)3 and diglyme,35–37 and on AlCl3 and various glymes.38–40

Subsequently, mixtures of G3:Al(OTf)3 and G3:Ga(OTf)3 were tested. Initially, it was anticipated that homogenous compounds could be synthesised from equimolar reactants ratios, cM(OTf)3 = 0.50 (Figure 2a). However, both G3:Al(OTf)3 and G3:Ga(OTf)3 systems formed homogenous liquids from very low metal triflate loadings, up to cM(OTf)3 = 0.33, which is equivalent to two moles of G3 per mole of M(OTf)3. This suggested possible formation of both ionic and charge-neutral complexes (exemplified in Figure 2b), but also significantly more complex species, with either triflates or glymes acting as bridging ligands. Apparent viscosity and yellow/orange colour of the formed SILs decreased with decreasing metal loading (Table 1).

Figure 2. Hypothetical speciation of Al-SILs synthesised at a) cM(OTf)3 = 0.50 (reaction did not proceed to completion), and b) cM(OTf)3 = 0.33 (reaction gave a homogenous liquid).

Acidity measurement by Gutmann acceptor number

There are several scales currently used to measure Lewis acidity by different research groups; each relies on a probe that interacts with a Lewis acid, and experimental or computational methods are used to quantify the strength of the interaction. Computational methods: Global Electrophilicity Index (GEI),41 Fluoride Ion Affinity (FIA) and Hydride Ion Affinity (HIA),42 gain increasing popularity, but they require detailed information on the structure of the investigated species to accurately perform electronic structure computations, optimise geometry, or evaluate enthalpy changes associated with fluoride/hydride coordination. Spectroscopic methods, proposed by Gutmann or Childs, are based on NMR spectroscopic probes. They offer less fundamental insights, but they can be used without knowing the speciation, and in some cases – they were successfully used to corroborate speciation studies.43,44 Since Gutmann acceptor number (AN) has been commonly used to measure acidity of Lewis acidic ionic liquids,4,12,45 including solvate ionic liquids,26 it has been selected for this study.

Following a standard procedure,4,12,33,34,46 AN values were determined from  31P NMR chemical shifts of an NMR probe, a weakly basic hard nucleophile, triethylphosphine oxide (TEPO). The probe has been dissolved in the G3:M(OTf)3 ionic liquids, across available compositional range, cM(OTf)3 = 0.09 - 0.33.

| Metal | M(OTf)3 | G3:M(OTf)3 molar ratio | Physical state | AN |
| --- | --- | --- | --- | --- |
| Al | 0.33 | 2:1 | Very viscous, yellow liquid | 70.9-82.7 |
|  | 0.25 | 3:1 | Viscous, light yellow liquid | 70.8-82.7 |
|  | 0.20 | 4:1 | Pale yellow liquid | 70.7-82.7 |
|  | 0.17 | 5:1 | Pale yellow liquid | 70.7-82.6 |
|  | 0.14 | 6:1 | Pale yellow liquid | 71.0-82.6 |
|  | 0.13 | 7:1 | Yellow hue liquid | 71.4-82.6 |
|  | 0.11 | 8:1 | Yellow hue liquid | 71.2-82.7 |
|  | 0.10 | 9:1 | Yellow hue liquid | 71.1-82.5 |
|  | 0.09 | 10:1 | Yellow hue liquid | 70.7-82.6 |
| Ga | 0.33 | 2:1 | Very viscous, orange liquid | 79.6-92.4 |
|  | 0.25 | 3:1 | Viscous, light orange liquid | 81.6-92.3 |
|  | 0.20 | 4:1 | Pale orange liquid | 80.4-92.3 |
|  | 0.17 | 5:1 | Pale orange liquid | 80.3-93.4 |
|  | 0.14 | 6:1 | Pale orange liquid | 80.3-92.8 |
|  | 0.13 | 7:1 | Orange hue liquid | 79.9-92.6 |
|  | 0.11 | 8:1 | Orange hue liquid | 79.6-93.4 |
|  | 0.10 | 9:1 | Orange hue liquid | 80.0-93.5 |
|  | 0.09 | 10:1 | Orange hue liquid | 80.1-93.3 |
| - | - | 1:0 (neat G3) | Colourless liquid | 9.6 |

Table 1. The composition, physical appearance and acceptor number (AN) values measured for the solvate ionic liquids in this study.

In all cases, there were several distinguishable signals, situated within a narrow range of ca. 8 ppm (Figure 3). This was in contrast to AN measurements for chlorometallate ionic liquids, characterised by a single 31P NMR signal,45 but similar to LCCs, in which multiple Lewis acidic complexes (or multiple potential modes of TEPO coordination) are reflected in several 31P NMR signals in AN measurements.3 In all cases, the pattern of signals was the same. There were three high-intensity signals: two relatively sharp and deshielded peaks, and one broader signal shifted upfield by ca. 5 ppm, in addition to at least two low intensity peaks. This suggests the existence of several Lewis acidic species capable of interacting with TEPO. The pattern of the 31P NMR signals was broadly the same for Ga-SILs and Al-SILs, but signals for Ga-SILs were deshielded by ca. 5 ppm with respect to those for Al-SILs, indicating a stronger interaction of TEPO (higher Lewis acidity) of Ga-SILs.

For the purpose of numerical quantification of Lewis acidity, instead of single AN values, a range of values were reported for each ionic liquid: ANAl-SILs = 70.7-82.7; ANGa-SILs = 79.6-93.5 (Table 1). Comparing these results with the literature, Lewis acidity of Al-SILs, χAl(OTf)3  = 0.33 and 0.25 (AN = 70.8-82.7) was higher than that of 1-octyl-3-methylimidazolium trifloaluminate ionic liquids, [C8mim][OTf]-Al(OTf)3, with the same molar ratio of aluminium triflate, χAl(OTf)3 = 0.33 and 0.25 (AN = 64.9-69.3),12 but lower than AN values of archetypal chloroaluminate ionic liquids (AN = 83.3-101.9),4,45,47 or AlCl3 (AN = 85.6-87.0).4 Lewis acidity of Ga-SILs (AN = 79.6-93.5) was higher than that of Al-SILs, approaching Lewis acidity of chlorogallate ionic liquids [C8mim]Cl-GaCl3 with excess of gallium chloride, χGaCl3 > 0.5 (AN = 87.7-107.3).4 Chlorogallate ionic liquids with sub-stoichiometric loading of gallium chloride (χGaCl3 = 0.33) were only mildly acidic, with AN = 21.7.45

Figure 3. 31P NMR comparison Al-SILs and Ga-SILs, studied across three compositions: cM(OTf)3 = 0.33, 0.25 and 0.09.

These results led to two questions: whether the difference in measured AN values translates to difference in catalytic performance, and how is Lewis acidity related to speciation, considering that in chlorometallate ILs there was a clear and direct link between anionic speciation and AN values.4,45

Speciation of Group 13 SILs

In contrast to Li-based SILs, very little is known about the speciation of Al-based SILs. A single FT-IR spectroscopic study of Al(OTf)3 and diglyme mixtures, across a range of concentrations: χAl(OTf)3 = 0.286, 0.130, 0.029 and 0.0015, suggested the presence of free triflate anions in the two most diluted samples, and the prevalence of Al-OTf coordination in the more concentrated samples.35

In this work, speciation of SILs was studied as a function of composition using multinuclear 1H, 13C, 27Al or 71Ga NMR spectroscopy. All SILs were studied neat; in NMR spectroscopy, a capillary with D2O was used as a lock and external reference.

The 1H NMR spectra of G3:M(OTf)3 systems have been compared to the 1H NMR spectrum of neat triglyme (Figure 4). Signals corresponding to both methylene and methyl groups of glyme in SILs (δH = 3.0 - 3.5 ppm) are more shielded than the corresponding signals in neat glyme (δH = 3.9 - 4.2 ppm), consistent with coordination of oxygens to the metal centre.48–50 As expected, upon increasing the glyme concentration from χM(OTf)3 = 0.33 to 0.09, the signals become slightly shielded, because more oxygens are competing for each atom of aluminium. Even at χM(OTf)3 = 0.09, which corresponds to ten G3 molecules to each M(OTf)3, all glyme molecules appear to be coordinated to the metal centres, and no signals corresponding to free glyme are visible.

Figure 4. 1H NMR spectra of neat glyme, G3, and solvate ionic liquids based on Al(OTf)3 or Ga(OTf)3, studied across three compositions: χM(OTf)3 = 0.33, 0.25 and 0.09.

13C NMR spectra of the neat glyme and selected SILs (Figure 5) present a slightly different image: in all SILs, signals corresponding to methylene carbon atoms (δ13C = 66-72 ppm) are deshielded when compared to neat glyme (δ13C = 70 - 72 ppm), but no changes are observed for the methyl group signals in neat glyme and in SILs (δ13C = 58 ppm). The same observation was made by Aldous and co-workers in their study of SILs based on Li[NTf2] and several glymes.49 Quartets in the 13C NMR spectra of SILs, arising from CF3 groups in triflates, are found at δ13C = ca. 119.5 ppm, which correspond to bound anions.51,52

Figure 5. 13C NMR spectra of neat glyme, G3, and solvate ionic liquids based on Al(OTf)3 or Ga(OTf)3, studied across three compositions: χM(OTf)3   = 0.33, 0.25 and 0.09.

27Al NMR spectra, recoded for Al-containing SILs (Figure 6), all featured a group of signals between -13 and 0 ppm corresponding to six-coordinate Al species, in oxygen coordination environment.53 Multiple signals suggest co-existence of several coordination environments of aluminium, in a manner resembling the coordination environment of trifloaluminate ionic liquids.12 There were no signals corresponding to tetrahedral (40 - 140 ppm), or pentacoordinate (25 - 60 ppm) aluminium environments,54–58 which is unsurprising given the excess of O-donors available in each sample. Samples with higher concentrations of 27Al featured in their spectra a broad signal at ca. 75 ppm, attributable to the NMR probe.12

Figure 6. 27Al NMR spectra of Al(NO3)3 in D2O, and a full series of Al-SILs compositions, χAl(OTf)3 = 0.33-0.09.

Ga-SILs (χGa(OTf)3 = 0.33 - 0.09) were studied by 71Ga NMR spectroscopy (Figure 7). Most spectra were flat, with signals indistinguishable from the baseline; this is commonly found in gallium-based ionic liquids with low-symmetry anions.59 It can be attributed to fast quadrupolar relaxation in these low-symmetry environments, combined with rapid exchanges between several species (as indicated by 1H NMR spectroscopy), all of which would contribute to the signal broadening. In the most concentrated samples (χGa(OTf)3 = 0.33, 0.25 and possibly 0.20), a  signal at -50 ppm was detected, attributable to octahedral environment of gallium (-50 to 50 ppm).60

Figure 7. 71Ga NMR spectrum of Ga(NO3)3 in D2O and full series of Ga-SILs compositions, χGa(OTf)3 = 0.33-0.09.

Finally, both Al-SILs and Ga- SILs were studied by 19F NMR spectroscopy across their entire compositional range (χM(OTf)3 = 0.33 - 0.09). 19F NMR spectra of Al-SILs exhibited multiple signals within the chemical shift range of -79.2 to -80.2 ppm (Figure 8), while 19F NMR signals for Ga-SILs were slightly more shielded on average, -78.9 to -79.6 ppm (Figure 9). To our knowledge, these are the most complicated patterns of 19F NMR signals from triflate anions reported in the IL literature.

Conventional ILs with free [OTf]- anions, measured in solution, all had single sharp 19F NMR signals within -76 to -79 ppm.61 Al-coordinated triflates in triflometallate ILs featured several merged 19F NMR signals, centred around -79 ppm, with minimal downfield shift with increasing χAl(OTf)3, whereas the parent metal-free IL, 1-octyl-3-methylimidazolium triflate, measured neat, had a singlet at -80.2 ppm.12

In this work, all 19F NMR signals shift upfield with increasing χM(OTf)3, although the pattern of signals did not change significantly with composition (aside from broadening due to viscosity change). Arguably, the upfield shift could be attributed to the solvent effect. At χM(OTf)3 = 0.09, the neat sample is a solution of M(OTf)3 in a molecular solvent (glyme). At higher χM(OTf)3 values, a significant proportion of glyme is coordinated to the metal centre, and the sample resembles a “good” SIL, with strong Coulombic interactions. In both Al-SILs and Ga- SILs, this transition from solution to SIL environment is observable for χM(OTf)3 ≥ 0.20.

Figure 8. 19F NMR spectra of full series of Al-SILs, χAl(OTf)3 = 0.33-0.09.

Figure 9. 19F NMR spectra of full series of Ga-SIls, χGa(OTf)3 = 0.33-0.09.

In conclusion, NMR spectroscopy points to both aluminium and gallium having octahedral coordination, with both [OTf]- and G3 ligands coordinated to the metal centre. It can be certainly stated that there is no single well-defined species in any sample, but there are multiple octahedral complexes, each characterised by a number of [OTf]- anions and specific numbers/hapticities of G3 ligands around the metal centre.

Comparing 19F NMR spectra of Al-SILs (Figure 8) and Ga-SILs (Figure 9), further conclusions could be cautiously proposed. Firstly, although there are multiple species, both in Al-SIL and in Ga-SIL, they do not seem to change as a function of χM(OTf)3 in either system. Rather, it could be envisaged that the χM(OTf)3 = 0.33 composition is the concentrated SIL and adding more glyme (towards χM(OTf)3 = 0.09) dilutes the metal species without affecting their coordination environments. AN measurements corroborate with this hypothesis, as the range of AN values appears constant for each family of SILs (Table 1). Secondly, 19F NMR spectra of Al-SILs and Ga-SILs are markedly different; there seems to be an additional deshielded signal in the Al-SILs spectra, which reaches -80.2 ppm for χAl(OTf)3 = 0.33 (more ionic nature, viz. Figure 2b). In Ga-SILs, all triflates appear to be bound, suggesting that the equilibrium in Figure 2b is right- shifted for gallium.

Notably, in all samples, there is excess of O-donors with respect to metal centres. Although no free glymes were detected by 1H or 13C NMR spectroscopy, it must be assumed that dynamic exchange of glyme ligands occurs.

Thermogravimetric analysis

Thermal stability of the solvate ionic liquids was studied by thermogravimetric analysis (TGA). TG curves are available in Figures S1 and S2 in the ESI.† In contrast to their thermally stable precursors: glyme (Td = 167 °C), Al(OTf)3 (Td = 221 °C) and Ga(OTf)3 (Td = 182 °C) thermal stability of the investigated systems was much lower with Td5% = 127 °C for Al-SILs and Td5% = 105 °C Ga-SILs, respectively. This unfortunately limits the span of operative conditions for these glymes, but also suggests that the metal centre is highly Lewis acidic, effectively catalysing decomposition of the glyme at much lower temperature.

Catalytic performance in [3+3] cycloaddition reaction

A [3+3] cycloaddition was selected as a test reaction for catalytic activity of the new SILs. The yield and selectivity of products in this reaction depend strongly both on the activity of the Lewis acidic catalyst and on the reaction conditions, which makes it sensitive to subtle changes and therefore a good model to distinguish between catalysts.62,63

The synthesis of chromane from 2,4-dimethylphenol and isoprene (Scheme 1) was chosen as a model [3+3] cycloaddition. Chromane is a part of a structure of more complicated compounds, including various forms of vitamin E and flavonoids,64 which makes it a common synthetic target. The reaction is typically catalysed by metal triflates, promoting high selectivity towards chromane (main product, Scheme 1).65

Scheme 1. Reaction between 2,4-dimethylphenol and isoprene.

All reactions were carried out solventless, at 35 °C, using liquid reactants (1:2 molar ratio of isoprene:2,4-dimethylphenol). Conversion of 2,4-dimethylphenol was monitored using GC, and each reaction was carried out until plateau of conversion has been reached. All SILs formed homogenous solutions when added to the reaction mixture, whereas their corresponding solid metal triflates, studied as comparators, were suspended in the reaction mixture.

Catalytic performance of Al(OTf)3, at 2 mol% loading of aluminium with respect to isoprene, was compared to Al-SIL (χAl(OTf)3 = 0.33), at 1, 2 and 5 mol% (Figure 10). While conversion for 2 mol% of Al(OTf)3 reached plateau at ca. 70%, the same loading of Al-SIL (χAl(OTf)3 = 0.33) gave ca. 99% conversion after 240 min, with the same selectivity to chromane of ca. 80%. Increasing the Al-SIL loading to 5 mol% resulted in improved reaction kinetics and selectivity; it gave full substrate conversion within 120 min, with selectivity reaching maximum of 90.7% after 180 min. Decreasing the Al-SIL loading to 1 mol% had the opposite effect, with performance lower than the benchmark catalyst, i.e. 2 mol% of Al(OTf)3.

Figure 10. Performance of various amounts of Al-SIL (χAl(OTf)3 = 0.33) in [3+3] cycloaddition of 2,4-dimethylphenol to isoprene, relative to metal triflate. Reaction conditions: 2,4-dimethylphenol (8 mmol), isoprene (4 mmol), 1000 rpm, T = 35 °C, S - selectivity to the main product.

In a series of analogous experiments, the performance of Ga(OTf)3, at 2 mol% loading, was compared to Ga-SIL (χGa(OTf)3 = 0.33), at 1, 2 and 5 mol% loadings (Figure 11). Reaction catalysed with 2 mol% of Ga(OTf)3 reached ca. 91% conversion after 240 min, with selectivity approaching 90%, whereas the same loading of Ga-SIL (χGa(OTf)3 = 0.33) gave full conversion after only 30 min. Extended reaction time increased the selectivity, from 86.8% after 30 min to 93.8% after 120 min.

Figure 11. Performance of various amounts of Ga-SIL (χGa(OTf)3 = 0.33) in [3+3] cycloaddition of 2,4-dimethylphenol to isoprene, relative to metal triflate. Reaction conditions: 2,4-dimethylphenol (8 mmol), isoprene (4 mmol), 1000 rpm, T = 35 °C, S - selectivity to the main product.

Both gallium triflate and Ga-SIL significantly outperformed their aluminium-based analogues, in keeping with higher AN values recorded for Ga-SIL (Table 1). The Ga-SIL (χGa(OTf)3 = 0.33, loading 2 mol%) gave full conversion in 120 min, whereas analogous Al-SIL required 240 min.

The best outcomes, in terms of conversion and selectivity, achieved with each tested catalyst, are given in Table 2, along with corresponding experimental conditions. Both Al-SIL and Ga-SIL outperformed their corresponding triflates at the same loadings of 2 mol%. Inferior reaction rates in M(OTf)3-catalysed reactions could be attributed to poor mass transport, as the triflate salts were suspended rather than dissolved. However, for both M(OTf)3 catalysts, conversions reached plateau values, whereas SILs enabled both full conversions and higher selectivities to chromane, which cannot not be attributed solely to mass transfer. We have therefore concluded that altering coordination around the metal centres, from triflate-only to mixed glyme/triflate complexes, had the dual benefit of (i) increased solubility in the organic phase and (ii) increased catalytic activity.

Following this reasoning, it was concluded that further altering of the coordination environment of Al(III) and Ga(III), from triflate to glyme ligands, could be beneficial. To test this hypothesis, both SILs were tested at χM(OTf)3 = 0.09, with vastly increased concentration of G3 with respect to metal. However, even at 5 mol% loading, the χM(OTf)3 = 0.09 SILs produced inferior results (Table 2, entries 4 and 8), when compared to χM(OTf)3 = 0.33 SILs (Table 2, entries 2, 3, 6 and 7). Most likely, liquids at χM(OTf)3 = 0.09 are merely solutions of SILs of certain fixed compositions in the excess of glyme; upon addition to the reaction mixture, excess glyme is simply washed away and acts as a dilutant to the system, decreasing overall concentration of reactants.

Table 2. Performance of SILs in [3 + 3] cycloaddition of 2,4-dimethylphenol to isoprene.

| No | Catalyst | χM(OTf)3 | Catalyst loading (mol%) | Time (min) | Conversion (%) | Selectivity (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | Al(OTf)3 | 1.00 | 2 | 180 | 70.3 | 80.3 |
| 2. | Al-SIL | 0.33 | 2 | 240 | 99.2 | 80.3 |
| 3. | Al-SIL | 0.33 | 5 | 180 | 100.0 | 90.7 |
| 4. | Al-SIL | 0.09 | 5 | 240 | 64.0 | 70.9 |
| 5. | Ga(OTf)3 | 1.00 | 2 | 240 | 91.4 | 83.2 |
| 6. | Ga-SIL | 0.33 | 2 | 120 | 100.0 | 82.8 |
| 7. | Ga-SIL | 0.33 | 5 | 120 | 100.0 | 93.8 |
| 8. | Ga-SIL | 0.09 | 5 | 240 | 92.6 | 84.3 |

Reaction conditions: 2,4-dimethylphenol (8 mmol), isoprene (4 mmol), 1000 rpm, T = 35 °C, amount of catalyst calculated in relation to isoprene.

Recyclability of the best-performing SIL, Ga-SIL (χGa(OTf)3 = 0.33) was tested by extracting the residual substrate and product with anhydrous hexane, after which the phase-separated catalyst layer was isolated, washed twice with hexene, concentrated and used in the next reaction cycle. Full conversion of substrate was maintained over 4 consecutive reaction cycles, with selectivities above 90% (Table 3).

Table 3. Recycling of Ga-SIL (χGa(OTf)3 = 0.33) in [3 + 3] cycloaddition of 2,4-dimethylphenol to isoprene.

| Cycle no | Conversion (%) | Selectivity (%) |
| --- | --- | --- |
| 1 | 100.0 | 93.8 |
| 2 | 100.0 | 94.0 |
| 3 | 100.0 | 92.6 |
| 4 | 100.0 | 91.5 |

Reaction conditions: 2,4-dimethylphenol (12-16 mmol), isoprene (6-8 mmol), 1000 rpm, T = 35 °C, 5 mol% of Ga-SIL (χGa(OTf)3 = 0.33) (amount of catalyst calculated in relation to isoprene), 120 min.

In conclusion, the G3:Ga(OTf)3, χGa(OTf)3  = 0.33 SIL was found to be an excellent catalyst for the synthesis of chromane, giving full conversion of isoprene within 2 h, with selectivity towards 2,2-dimethyl-6,8-dimethylchromane reaching 93.8%, slightly higher than previously reported catalytic systems, offering selectivities ranging from 80% to 92%.12,66,67 The catalytic performance of Al-SILs and Ga-SILs has followed the AN trend.

Conclusions

New solvate ionic liquids based on aluminium(III) and gallium(III) triflates, and G3, have been synthesised, characterised and used as Lewis acidic catalysts for the synthesis of chromane. Both triflate salts dissolved in G3 at low concentrations (χM(OTf)3 = 0.09) and formed homogenous liquids up to the metal triflate loading of χM(OTf)3 = 0.33. It was found that both metals were octahedral across the entire compositional range, and both G3 and [OTf]- were included in the first coordination sphere of the metal.

From multinuclear NMR spectroscopic experiments, it appeared that coordination environment remained similar across the compositional range, for each of the two metals. Furthermore, it was suggested that speciation of Al-SILs was different from that of Ga-SILs, potentially with more free triflate in the former. AN values (an experimental measure of Lewis acidity) were constant for each SIL family, across the entire compositional range: ca. 71-83 for Al-SILs and ca. 80-93 for Ga-SILs. These values lie within relatively high acidity range, despite fully occupied coordination shell.

Catalytic activity of SILs was tested in a model [3+3] cycloaddition, yielding 2,2-dimethyl-2,4-dimethylchromane. Both families of SILs were fully dissolved in the reaction mixtures, in contrast to the parent metal triflates, and their catalytic activity has been enhanced when compared at the same metal loading. Catalytic performance was aligned with AN measurements, with Ga-SILs outperforming Al-SILs. The best catalyst (Ga-SIL χM(OTf)3 = 0.33) gave full substrate conversion and a high selectivity of 93.8% after 2 h at 35˚C, and could be recycled four times, retaining consistently high conversion and selectivity.

Given the notorious difficulties in dissolving metal triflates, converting them to SILs may offer a broadly-applicable and robust approach to generate well-soluble metal triflate catalysts; this strategy is likely applicable beyond Group 13, to rare earth triflates and transition metal triflates. Further detailed studies on the structure and applications of Group 13 SILs are currently ongoing in our group.

Author Contributions

Justyna Więcławik: Data curation, Formal analysis, Investigation, Methodology, Validation, Visualization Writing – original draft; Alina Brzęczek-Szafran: Conceptualisation, Formal analysis, Methodology, Visualization, Writing – original draft, Writing – review & editing; Sebastian Jurczyk: Formal analysis, Methodology; Karolina Matuszek: Methodology, Validation, Writing – review & editing; Małgorzata Swadźba-Kwaśny: Conceptualisation, Funding acquisition, Supervision, Writing – original draft, Writing – review & editing; Anna Chrobok: Conceptualisation, Funding acquisition, Supervision, Writing – original draft, Writing – review & editing.

Conflicts of interest

There are no conflicts to declare.

Data availability

The data supporting this article have been included as part of the Supplementary Information.

Acknowledgements

The financial support from the National Science Centre, Poland (grant no. UMO-2020/39/B/ST8/00693) are gratefully acknowledged. The authors also express gratitude to the Polish Agency for Academic Exchange (under the Academic International Partnerships program, grant agreement PPI/APM/2018/1/00004) for financial support of the internship at The QUILL Research Centre, Queen’s University Belfast, which enabled a part of the speciation study, Polish National Agency for Academic Exchange and grant agreement BPI/PST/2021/1/00039 for enabling scientific discussions in a project funded within the Strategic Partnerships program that helped us interpret a phenomena described above.

Notes and references

Referenced data S1 – S4, detailed experimental information, IR spectra and TGA.

1	C. A. Angell, J. Electrochem. Soc., 1965, 112, 1224.

2	C. Austen Angell, Y. Ansari and Z. Zhao, Faraday Discuss., 2012, 154, 9–27.

3	F. Coleman, G. Srinivasan and M. Swadźba-Kwaśny, Angew. Chemie - Int. Ed., 2013, 52, 12582–12586.

4	J. M. Hogg, L. C. Brown, K. Matuszek, P. Latos, A. Chrobok and M. Swadźba-Kwaśny, Dalt. Trans., 2017, 46, 11561–11574.

5	J. M. Hogg, F. Coleman, A. Ferrer-Ugalde, M. P. Atkins and M. Swadźba-Kwas̈ny, Green Chem., 2015, 17, 1831–1841.

6	K. Matuszek, A. Chrobok, J. M. Hogg, F. Coleman and M. Swadźba-Kwaśny, Green Chem., 2015, 17, 4255–4262.

7	M. Lijewski, J. M. Hogg, M. Swadźba-Kwaśny, P. Wasserscheid and M. Haumann, RSC Adv., 2017, 7, 27558–27563.

8	S. Kobayashi, M. Sugiura, H. Kitagawa and W. W. L. Lam, Chem. Rev., 2002, 102, 2227–2302.

9	L. Massi, J. F. Gal and E. Duñach, Chempluschem, 2022, 87, e202200037.

10	G. A. Olah, O. Farooq, S. M. F. Farnia and J. A. Olah, J. Am. Chem. Soc., 1988, 110, 2560–2565.

11	M. Distaso and E. Quaranta, Tetrahedron, 2004, 60, 1531–1539.

12	P. Latos, A. Culkin, N. Barteczko, S. Boncel, S. Jurczyk, L. C. Brown, P. Nockemann, A. Chrobok and M. Swadźba-Kwaśny, Front. Chem., 2018, 6, 1–15.

13	T. Tamura, T. Hachida, K. Yoshida, N. Tachikawa, K. Dokko and M. Watanabe, J. Power Sources, 2010, 195, 6095–6100.

14	T. Mandai, K. Yoshida, K. Ueno, K. Dokko and M. Watanabe, Phys. Chem. Chem. Phys., 2014, 16, 8761–8772.

15	T. Mandai, K. Yoshida, S. Tsuzuki, R. Nozawa, H. Masu, K. Ueno, K. Dokko and M. Watanabe, J. Phys. Chem. B, 2015, 119, 1523–1534.

16	T. Tamura, K. Yoshida, T. Hachida, M. Tsuchiya, M. Nakamura, Y. Kazue, N. Tachikawa, K. Dokko and M. Watanabe, Chem. Lett., 2010, 39, 753–755.

17	C. Zhang, K. Ueno, A. Yamazaki, K. Yoshida, H. Moon, T. Mandai, Y. Umebayashi, K. Dokko and M. Watanabe, J. Phys. Chem. B, 2014, 118, 5144–5153.

18	C. Zhang, A. Yamazaki, J. Murai, J. W. Park, T. Mandai, K. Ueno, K. Dokko and M. Watanabe, J. Phys. Chem. C, 2014, 118, 17362–17373.

19	H. Hirayama, N. Tachikawa, K. Yoshii, M. Watanabe and Y. Katayama, Electrochemistry, 2015, 83, 824–827.

20	K. Ueno, J. Murai, K. Ikeda, S. Tsuzuki, M. Tsuchiya, R. Tatara, T. Mandai, Y. Umebayashi, K. Dokko and M. Watanabe, J. Phys. Chem. C, 2016, 120, 15792–15802.

21	M. Watanabe, K. Dokko, K. Ueno and M. L. Thomas, Bull. Chem. Soc. Jpn., 2018, 91, 1660–1682.

22	Z. Yu, C. Fang, J. Huang, B. G. Sumpter and R. Qiao, ACS Appl. Mater. Interfaces, 2018, 10, 32151–32161.

23	S. Terada, K. Ikeda, K. Ueno, K. Dokko and M. Watanabe, Aust. J. Chem., 2019, 72, 70–80.

24	S. Wei, Z. Li, K. Kimura, S. Inoue, L. Pandini, D. Di Lecce, Y. Tominaga and J. Hassoun, Electrochim. Acta, 2019, 306, 85–95.

25	D. J. Eyckens and L. C. Henderson, Front. Chem., 2019, 7, 1–15.

26	D. J. Eyckens, M. E. Champion, B. L. Fox, P. Yoganantharajah, Y. Gibert, T. Welton and L. C. Henderson, European J. Org. Chem., 2016, 2016, 913–917.

27	A. Obregón-Zúñiga, M. Milán and E. Juaristi, Org. Lett., 2017, 19, 1108–1111.

28	D. J. Eyckens and L. C. Henderson, RSC Adv., 2017, 7, 27900–27904.

29	S. Di Pietro, V. Bordoni, A. Mezzetta, C. Chiappe, G. Signore, L. Guazzelli and V. Di Bussolo, Molecules, 2019, 24, 1–9.

30	N. Hameed, D. J. Eyckens, B. M. Long, N. V. Salim, J. C. Capricho, L. Servinis, M. De Souza, M. D. Perus, R. J. Varley and L. C. Henderson, ACS Appl. Polym. Mater., 2020, 2, 2651–2657.

31	T. Mandai, K. Dokko and M. Watanabe, Chem. Rec., 2019, 19, 708–722.

32	Z. Ma, M. Forsyth, D. R. MacFarlane and M. Kar, Green Energy Environ., 2019, 4, 146–153.

33	K. Matuszek, A. Chrobok, F. Coleman, K. R. Seddon and M. Swadźba-Kwaśny, Green Chem., 2014, 16, 3463–3471.

34	A. Brzęczek-Szafran, J. Więcławik, N. Barteczko, A. Szelwicka, E. Byrne, A. Kolanowska, M. Swadźba Kwaśny and A. Chrobok, Green Chem., 2021, 23, 4421–4429.

35	L. D. Reed, A. Arteaga and E. J. Menke, J. Phys. Chem. B, 2015, 119, 12677–12681.

36	L. D. Reed, S. N. Ortiz, M. Xiong and E. J. Menke, Chem. Commun., 2015, 51, 14397–14400.

37	S. Gu, Y. Haoyi, Y. Yuan, Y. Gao, N. Zhu, F. Wu, Y. Bai and C. Wu, Energy Mater. Adv., 2022, 1, 1–10.

38	A. Kitada, K. Nakamura, K. Fukami and K. Murase, Electrochemistry, 2014, 82, 946–948.

39	A. Kitada, K. Nakamura, K. Fukami and K. Murase, Electrochim. Acta, 2016, 211, 561–567.

40	Z. Zhang, A. Kitada, S. Gao, K. Fukami, N. Tsuji, Z. Yao and K. Murase, ACS Appl. Mater. Interfaces, 2020, 12, 43289–43298.

41	A. R. Jupp, T. C. Johnstone and D. W. Stephan, Dalt. Trans., 2018, 47, 7029–7035.

42	P. Erdmann, J. Leitner, J. Schwarz and L. Greb, ChemPhysChem, 2020, 21, 987–994.

43	J. Estager, P. Nockemann, K. R. Seddon, M. Swadźba-Kwaśny and S. Tyrrell, Inorg. Chem., 2011, 50, 5258–5271.

44	M. Currie, J. Estager, P. Licence, S. Men, P. Nockemann, K. R. Seddon, M. Swadźba-Kwaśny and C. Terrade, Inorg. Chem., 2013, 52, 1710–1721.

45	J. Estager, A. A. Oliferenko, K. R. Seddon and M. Swadźba-Kwaśny, Dalt. Trans., 2010, 39, 11375–11382.

46	K. Matuszek, S. Coffie, A. Chrobok and M. Swadźba-Kwaśny, Catal. Sci. Technol., 2017, 7, 1045–1049.

47	M. Sakhalkar, R. P. Choudhury, V. Bhakthavatsalam, S. V. Lande, J. Pradhan and S. Chandra, J. Mol. Struct., 2020, 1222, 128936.

48	N. Peddagopu, P. Rossi, C. Bonaccorso, A. Bartasyte, P. Paoli and G. Malandrino, Dalt. Trans., 2020, 49, 1002–1006.

49	J. J. Black, A. Dolan, J. B. Harper and L. Aldous, Phys. Chem. Chem. Phys., 2018, 20, 16558–16567.

50	S. Sun, Y. Niu, Q. Xu, Z. Sun and X. Wei, RSC Adv., 2015, 5, 46564–46567.

51	L. L. Tolstikova, A. V. Bel’Skikh and B. A. Shainyan, Russ. J. Org. Chem., 2010, 46, 383–388.

52	P. Latos, A. Wolny, J. Zdarta, F. Ciesielczyk, S. Jurczyk, T. Jesionowski and A. Chrobok, Environ. Technol. Innov., 2023, 31, 103164.

53	M. M. Finnegan, S. J. Rettig and C. Orvig, J. Am. Chem. Soc., 1986, 108, 5033–5035.

54	G. A. Olah, O. Farooq, S. M. F. Farnia, M. R. Bruce, F. L. Clouet, P. R. Morton, G. K. Surya Prakash, R. C. Stevens, R. Bau, K. Lammertsma, S. Suzer and L. Andrews, J. Am. Chem. Soc., 1988, 110, 3231–3238.

55	D. A. Atwood, Coord. Chem. Rev., 1998, 176, 407–430.

56	M. Choi, K. Matsunaga, F. Oba and I. Tanaka, J. Phys. Chem. C, 2009, 113, 3869–3873.

57	A. W. Apblett, in Encyclopedia of Inorganic and Bioinorganic Chemistry, John Wiley & Sons, Ltd, 2012.

58	K. N. Tayade, M. Mishra, K. Munusamy and R. S. Somani, Catal. Sci. Technol., 2015, 5, 2427–2440.

59	K. R. Seddon, G. Srinivasan, M. Swadźba-Kwaśny and A. R. Wilson, Phys. Chem. Chem. Phys., 2013, 15, 4518–4526.

60	Z. L. Ma, K. M. Wentz, B. A. Hammann, I. Y. Chang, M. K. Kamunde-Devonish, P. H. Y. Cheong, D. W. Johnson, V. V. Terskikh and S. E. Hayes, Chem. Mater., 2014, 26, 4978–4983.

61	N. V. Ignat’ev, P. Barthen, A. Kucheryna, H. Willner and P. Sartori, Molecules, 2012, 17, 5319–5338.

62	P. Quadrelli, Modern applications of cycloaddition chemistry, Elsevier, 2019.

63	J. Deng, X. N. Wang and R. P. Hsung, in Wiley Blackwell 6, Wiley Blackwell, 2014, vol. 9781118299, pp. 283–354.

64	C. Schneider, Mol. Nutr. Food Res., 2005, 49, 7–30.

65	S. W. Youn and J. I. Eom, J. Org. Chem., 2006, 71, 6705–6707.

66	Y. Yamamoto and K. Itonaga, Org. Lett., 2009, 11, 717–720.

67	T. T. Dang, F. Boeck and L. Hintermann, J. Org. Chem., 2011, 76, 9353–9361.

Table of Contents

This first report on solvate ionic liquids (SILs) based on aluminium(III) or gallium(III) triflate and triglyme (G3) provides insights into their liquid-phase speciation, thermal stability, Lewis acidity and catalytic activity in [3+3] cycloaddition reactions.