Modulating the spin-flip rates and emission energies through ligand design in Cr(III) molecular rubies

Yating Ye,a Maxime Poncet,b Polina Yaltseva,c Pablo Salcedo-Abraira,a Antonio Rodríguez-Diéguez,a Javier Heredia Martín,a Laura Cuevas,a Carlos M. Cruz,d Benjamin Doistau,e Claude Piguet,b Oliver S. Wenger,c Juan Manuel Herrera,a and Juan-Ramón Jiménez*a

Department of Inorganic Chemistry. University of Granada and “Unidad de Excelencia en Química (UEQ)”, Avda. Fuente Nueva s/n, 18071, Granada, Spain.

Department of Analytical and Inorganic Chemistry. University of Geneva. 30 quai Ernest Ansermet, CH-1211 Geneva 4, Switzerland.

Department of Chemistry, University of Basel, St. Johanns-Ring 19, 4056, Basel, Switzerland

Department of Organic Chemistry. University of Granada and “Unidad de Excelencia en Química (UEQ)”, Avda. Fuente Nueva s/n, 18071, Granada, Spain.

Laboratoire de Chimie et de Biochimie Pharmacologiques et Toxicologiques, Université Paris Cité, CNRS, 45 rue des Saint-Pères  F-75006 Paris, France.

Supporting Information

(49 pages)

Experimental part

Elemental analyses were carried out on a Fisons-Carlo Erba analyser model EA 1108. 1H Nuclear Magnetic Resonance Spectroscopy (RMN) data were recorded on a 400 MHz BRUKER Nanobay Avance III HD High-Definition spectrometer and the spectra were internally referenced to solvent signals. Absorption spectra in acetonitrile solution were recorded using a Jasco Cary (Agilent Technologies) spectrometer (quartz cell path length 1 cm or 1 mm, 290-800 nm domain, 2×10−4 M and 650-800 nm domain, 7.7 mM). Emission and excitation spectra were measured on a UV-VIS-PTI QuantaMaster™ 8000 spectrofluorometer equipped with a Picosecond Photon Detector (230-850nm, PPD-850, HORIBA Scientific) and a continuous Xenon Short Arc Lamp (190-2000nm, USHIO). All the spectra (emission and excitation) were corrected with real-time correction functions. Time Correlated Single Photon Counting (TCSPC) lifetime measurements were performed using a 480 nm or 450 nm flash lamp (1 s pulse, HORIBA Scientific). Low temperature (77 K) was achieved using liquid quartz transparent Dewar filled with liquid N2 in the center of which samples were placed. Sample solutions in CH3CN, were introduced in quartz tube (4 mm interior diameter) and introduced into the sample holder of the Dewar. All emission quantum yields were measured according to an absolute method which makes use of an integration sphere. Mass spectrometry measurements have been recorded in a Compact Bruker QTOF with UHPLC Elute Ole Bruker. Using the relationship kq = 1/[O2] ⋅(1/air -1/Ar), where [O2] is the oxygen concentration (2.42 mM in CH3CN at 20 °C), air is the 2E/2T1 lifetime under aerated conditions and Ar the respective lifetime under deaerated condition, kq values for energy transfer from 2E/2T1 to O2 could be estimated (see main text). UV-vis transient absorption measurements on the nanosecond timescale were carried out on an LP920-KS instrument from Edinburgh Instruments. A frequency-tripled pulsed Nd:YAG laser (Quantel Q-smart 450, ca. 10 ns pulse width) with a beam expander (BE02-355 from Thorlabs) in the beam path was used for excitation at 355 nm (pulse energy of ~30 mJ) and a frequency-tripled  Nd:YAG laser (Quantel Brilliant, ca. 10 ns pulse width) equipped with OPO from Opotek and a beam expander (GBE02-A from Thorlabs) in the beam path was used for excitation at 450 nm (pulse energy of ~13 mJ). An iCCD camera from Andor was used to detect transient absorption spectra, and single-wavelength kinetics were recorded with a photomultiplier tube (Hamamatsu).

X-Ray Crystallography.

Suitable crystals of 1, 2 and 3 were mounted on a Bruker D8 Venture diffractometer. Details of the crystals, data collection and refinement parameters are given in Table S1. After data processing (raw data integration, merging of equivalent reflections and absorption correction), the structures were solved by direct or Patterson methods and refined using least squares minimization with the SHELX suite of programs[S] integrated in OLEX2.[S] Selected bonds and lengths are given in Tables S2 and S3. In 2, the iodine atom I1 is disordered over two sites and refined with site occupancies of 0.5/0.5. Carbon atoms C1S and C3S, which belong to a diethyl ether solvation molecule, are also disordered. The checkcif file of this structure contains two A-level alerts associated with residual peaks near a triflate counterion which is probably disordered and which we could not model. The CCDC numbers 2266702 (1), 2266703 (2) and (3) 2389781 contain the supplementary crystallographic data for this article. These data are provided free of charge by the Cambridge Crystallographic Data Centre.

Appendix. Experimental section.

Solvents and starting materials

All the chemicals were purchased from commercial suppliers and used without further purification.

Synthesis: Preparation of the ligands and complexes

Synthesis of 2,6-bis((3,5-dimethyl-1H-pyrazol-1-yl)methyl)pyridine (Mebipzp) and 2,6-bis((4-iodo-3,5-dimethyl-1H-pyrazol-1-yl)methyl)pyridine (IMebipzp) and 2,6-bis(indazol-2-ylmethyl)pyridine (bip).

In a 100 mL round-bottom flask containing 20 mL of toluene were added: 0.3050 g of 2,6-bis(chloromethyl)pyridine and 0.3345 g of 3,5-dimethylpyrazole for Mebipzp or 0.3060 of 3,5-dimetil-4-iodo-pyrazole for IMebipzp. On the other hand, a 40% NaOH solution was prepared, containing 4.8 g of NaOH dissolved in 12 mL of water, and 10 drops of TBAOH were added. This basic solution was added to the pyrazole containing solution which was subsequently refluxed at 110°C for 24 hours. After this period, the mixture was allowed to cool to room temperature, and a liquid-liquid extraction was performed to separate the organic phase (toluene). The organic phase was washed with 3x10 mL of water. The organic phase was then dried with MgSO4, filtered, and the solvent was removed under vaccum, resulting in the desired product in the form of a white solid. 1H-NMR (400 MHz, CDCl3, ppm) δ: 7.53-7.49 (t, J = 7.8 Hz, 1H), 6.64-6.62 (d, J = 7.8 Hz, 2H), 5.87 (s, 2H). 5.30 (s, 4H), 2.30 (s, 6H), 2.19 (s, 6H). 1H-NMR (400 MHz, CDCl3, ppm) δ: 7.55 (t, J = 7.8 Hz, 1H), 6.77 (d, J = 7.8 Hz 2H), 5.35 (s, 4H), 2.25 (s, 6H), 2.2 (s, 6H).

For the synthesis of 2,6-bis(indazol-2-ylmethyl)pyridine (bip), we use 2,6-bis(bromomethyl)pyridine (0.300 g, 1.132 mmol) instead of 2,6-bis(chloromethyl)pyridine with 1H-indazole (0.267 g, 2.264 mmol). The synthesis procedure is the same as Mebipzp and IMebipzp. 1H-NMR (400 MHz, CDCl3, ppm) δ: 8.04 (s, 2H), 7.79 – 7.64 (m, 4H), 7.60 – 7.44 (m, 1H), 7.30 (t, J = 1.1, 2H), 7.10 (t, J = 0.9, 2H), 6.97 (d, J = 7.8, 2H), 5.72 (s, 4H).

Synthesis of [Cr(IMebipzp)2](SO3CF3)3 (1) and [Cr(IMebipzp)2](SO3CF3)3 (2) [Cr(bip*)2](SO3CF3)3 (3)

In a glovebox 2 mmol of ligand suspended in 10 mL of anhydrous acetonitrile were added dropwise to a solution containing 1 mmol of Cr(CF3SO3)2·2H2O previously dissolved in 5 mL of anhydrous acetonitrile. The mixture was stirred for 2h at 35ºC resulting in a purple solution. Subsequent addition of 1 mmol of AgSO3CF3 led to a colour change from purple to orange with the apparition of a grey solid. The mixture was stirred for additional 4 h. The reaction was taken from the glovebox and filtered through a membrane of PTFE of 2 m. The volume of the orange solution was reduced under vacuum and diethyl ether was added to precipitate the solids which were filtered giving a pale pink solid for 1, an orange solid for 2 and an orange solid for 3 (reaction yields 90%). Elemental analysis for 1: C37H42CrF9N10O9S3P3·1.8H2O %, found: C: 39.75, N: 12.59, H: 3.75; calculated: C: 40.01, N: 12.61, H: 4.02. Elemental analysis for 2: C37H38CrF9I4N10O9S3P3·H2O, found %: C: 27.26, N: 8.53, H: 2.49; calculated: C: 27.33, N: 8.61, H: 2.58. Elemental analysis for 3: C45H34CrF9N10O9S3 · 0,9 H2O %, found: C: 45.13, H: 2.87, N: 11.63; calculated: C: 45.26, H: 3.02, N: 11.73.

Single crystals suitable for X-ray diffraction were obtained by slow diffusion of diethyl ether into a concentrated acetonitrile solution containing the complexes after 48h.

Figure S1. ESI-Mass spectrometry for complex 1 (top), 2 (medium) and 3 (bottom) and their respective assignation.

Table S1. Crystallographic data for complexes 1, 2 and 3

|  | 1 | 2 |
| --- | --- | --- |
| Empirical formula | C41H48CrF9N12O9S3 | C43H51CrF9I4N11O10S3 |
| Formula weight | 1172.09 | 1708.72 |
| Crystal system | monoclinic | monoclinic |
| Space group | P21/c | P21/n |
| a/Å | 21.2505(15) | 11.8195(5) |
| b/Å | 11.5885(7) | 22.8812(10) |
| c/Å | 20.6086(13) | 22.7016(10) |
| β/° | 92.210(2) | 100.6638(16) |
| Volume/Å3 | 5071.3(6) | 6033.5(5) |
| Z | 4 | 4 |
| ρcalcg/cm3 | 1.535 | 1.881 |
| μ/mm-1 | 0.447 | 2.428 |
| F(000) | 2412.0 | 3324.0 |
| Crystal size/mm3 | 0.243 × 0.216 × 0.026 | 0.247 × 0.101 × 0.051 |
| Radiation | MoKα (λ = 0.71073) | MoKα (λ = 0.71073) |
| 2Θ range for data collection/° | 3.956 to 56.726 | 3.932 to 56.606 |
| Index ranges | -28 ≤ h ≤ 28, -14 ≤ k ≤ 15, -27 ≤ l ≤ 27 | -15 ≤ h ≤ 15, -30 ≤ k ≤ 30, -28 ≤ l ≤ 30 |
| Reflections collected | 79343 | 92085 |
| Independent reflections | 12613 [Rint = 0.0398, Rsigma = 0.0284] | 14938 [Rint = 0.0548, Rsigma = 0.0369] |
| Data/restraints/parameters | 12613/0/686 | 14938/95/772 |
| Goodness-of-fit on F2 | 1.053 | 1.073 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0413, wR2 = 0.1091 | R1 = 0.0611, wR2 = 0.1405 |
| Final R indexes [all data] | R1 = 0.0500, wR2 = 0.1165 | R1 = 0.0816, wR2 = 0.1539 |
| Largest diff. peak/hole / e Å-3 | 1.26/-0.72 | 3.10/-1.54 |

|  | 3 |
| --- | --- |
| Empirical formula | C45H54CrF9N10O19S3 |
| Formula weight | 1358.16 |
| Temperature/K | 100.00 |
| Crystal system | orthorhombic |
| Space group | Pna21 |
| a/Å | 24.8078(9) |
| b/Å | 21.0257(10) |
| c/Å | 11.4987(5) |
| α/° | 90 |
| β/° | 90 |
| γ/° | 90 |
| Volume/Å3 | 5997.7(4) |
| Z | 4 |
| ρcalcg/cm3 | 1.504 |
| μ/mm-1 | 0.400 |
| F(000) | 2796.0 |
| Crystal size/mm3 | 0.246 × 0.221 × 0.216 |
| Radiation | MoKα (λ = 0.71073) |
| 2Θ range for data collection/° | 3.812 to 50.054 |
| Index ranges | -28 ≤ h ≤ 29, -25 ≤ k ≤ 25, -13 ≤ l ≤ 13 |
| Reflections collected | 49184 |
| Independent reflections | 10588 [Rint = 0.0473, Rsigma = 0.0293] |
| Data/restraints/parameters | 10588/1284/654 |
| Goodness-of-fit on F2 | 1.687 |
| Final R indexes [I>=2σ (I)] | R1 = 0.1037, wR2 = 0.3308 |
| Final R indexes [all data] | R1 = 0.1117, wR2 = 0.3517 |
| Largest diff. peak/hole / e Å-3 | 2.19/-1.23 |
| Flack parameter | 0.51(6) |

Figure S2. Molecular Structure of 1. Colour codes: Cr (orange), N (blue), C (grey).

Table S2. Selected bond distances (Å) and angles (º) for complex 1

|  | Bond distances (Å) |  | Bond angles (º) |
| --- | --- | --- | --- |
| Cr1-N1 Cr1-N3 Cr1-N5 Cr1-N6 Cr1-N8 Cr1-N10 | 2.0527(15) 2.0813(14) 2.0634(15) 2.0550(14) 2.0869(14) 2.0470(14) | N1-Cr1-N3 N1-Cr1-N5 N1-Cr1-N6 N1-Cr1-N8 N1-Cr1-N10 N3-Cr1-N5 N3-Cr1-N6 N3-Cr1-N8 N3-Cr1-N10 N5-Cr1-N6 N5-Cr1-N8 N5-Cr1-N10 N6-Cr1-N8 N6-Cr1-N10 N8-Cr1-N10 | 88.63(6) 176.25(6) 92.89(6) 93.38(6) 85.80(6) 87.82(6) 93.28(6) 177.28(6) 90.36(6) 86.11(6) 90.20(6) 95.43(6) 88.44(6) 176.10(6) 87.97(6) |

Figure S3. Molecular Structure of 2. Colour codes: Cr (orange), N (blue), C (grey), I (purple).

Table S3. Selected bond distances (Å) and angles (º) for complex 2

|  | Bond distances (Å) |  | Bond angles (º) |
| --- | --- | --- | --- |
| Cr1-N1 Cr1-N3 Cr1-N5 Cr1-N6 Cr1-N8 Cr1-N10 | 2.067(5) 2.091(5) 2.065(5) 2.065(5) 2.104(5) 2.069(5) | N1-Cr1-N3 N1-Cr1-N5 N1-Cr1-N6 N1-Cr1-N8 N1-Cr1-N10 N3-Cr1-N5 N3-Cr1-N6 N3-Cr1-N8 N3-Cr1-N10 N5-Cr1-N6 N5-Cr1-N8 N5-Cr1-N10 N6-Cr1-N8 N6-Cr1-N10 N8-Cr1-N10 | 87.28(18) 175.28(19) 93.53(19) 92.69(18) 86.51(19) 88.06(18) 92.80(19) 178.97(19) 91.38(18) 85.95(19) 91.99(18) 94.36(19) 88.23(19) 175.8(2) 87.59(18) |

Figure S4. Molecular Structure of 3. Colour codes: Cr (orange), N (blue), C (grey), I (purple).

Table S4. Selected bond distances (Å) and angles (º) for complex 3

|  | Bond distances (Å) |  | Bond angles (º) |
| --- | --- | --- | --- |
| Cr1-N3 | 2.079(7) | N3-Cr1-N8 | 178.5(2) |
| Cr1-N5 | 2.047(6) | N5-Cr1-N3 | 88.5(3) |
| Cr1-N10 | 2.030(7) | N5-Cr1-N8 | 90.0(2) |
| Cr1-N1 | 2.043(6) | N10-Cr1-N3 | 91.7(3) |
| Cr1-N8 | 2.098(4) | N10-Cr-N5 | 95.0(3) |
| Cr1-N6 | 1.999(7) | N10-Cr-N1 | 85.7(2) |
|  |  | N10-Cr1-N8 | 88.0(3) |
|  |  | N1-Cr1-N3 | 88.8(3) |
|  |  | N1-Cr1-N5 | 177.3(3) |
|  |  | N1-Cr1-N8 | 92.6(2) |
|  |  | N6-Cr1-N3 | 92.9(3) |
|  |  | N6-Cr1-N5 | 85.2(2) |
|  |  | N6-Cr1-N10 | 175.4(3) |
|  |  | N6-Cr1-N1 | 94.4(3) |
|  |  | N6-Cr-N8 | 87.3(3) |

Table S5. SHAPE analysis of the compounds [Cr(bpmp)2]3+, 1, 2 and 3

|  | JPPY-6 | TPR-6 | OC-6 | PPY-6 | HP-6 |
| --- | --- | --- | --- | --- | --- |
| [Cr(bpmp)2]3+ | 31.949 | 15.635 | 0.158 | 28.611 | 31.107 |
| [Cr(btmp)2]3+ | 32.182 | 15.898 | 0.151 | 28.855 | 30.753 |
| 1 | 31.175 | 14.327 | 0.186 | 27.654 | 31.836 |
| 2 | 31.272 | 14.843 | 0.183 | 27.77 | 31.885 |
| 3 | 31.075 | 14.859 | 0.208 | 27.818 | 31.59 |

JPPY-6 5 C5v Johnson pentagonal pyramid J2

TPR-6 4 D3h Trigonal prism

OC-6 3 Oh Octahedron

PPY-6 2 C5v Pentagonal pyramid

HP-6 1 D6h Hexagon

Figure S5. Molecular Structure of 1. Colour codes: Cr (orange), N (blue), C (grey), I (purple).

Figure S6. Molecular Structure of 2. Colour codes: Cr (orange), N (blue), C (grey), I (purple).

Figure S7. Molecular Structure of 3. Colour codes: Cr (orange), N (blue), C (grey), I (purple) highlighting the hydrogen bonding.

Figure S8. a) Solid state absorption spectra of [Cr(Mebipzp)2]3+ (1)  and [Cr(IMebipzp)2]3+ (2) and b) [Cr(bip*)2]3+ (3)

Figure S9. Comparison of emission spectra of 1, [Cr(dqp)2]3+ and [Cr(ddpd)2]3+ at room temperature (a) and 77 K in frozen solution (b).

Figure S10. Comparison of absorption and emission spectra at 77 K for complex 1 (a), 2 (b) and 3 (c).

Figure S11. Excitation spectra of 1 (a), 2 (b), upon monitoring em = 748 nm and 3 (c) monitored at em = 830 nm.

counts

Figure S12. Excited state lifetime and the best fit of the experimental data for the [Cr(Mebipzp)2]3+ complex (exc = 480 nm) in deaerated acetonitrile solution

counts

Figure S13. Excited state lifetime and the best fit of the experimental data for the [Cr(Mebipzp)2]3+ complex (exc = 480 nm) in aerated acetonitrile solution

counts

Figure S14. Excited state lifetime and the best fit of the experimental data for the [Cr(Mebipzp)2]3+ complex (exc = 480 nm) at 77 K in frozen acetonitrile

counts

Figure S15. Excited state lifetime and the best fit of the experimental data for the [Cr(IMebipzp)2]3+ complex (exc = 480 nm) in deaerated acetonitrile solution

counts

Figure S16. Excited state lifetime and the best fit of the experimental data for the [Cr(IMebipzp)2]3+ complex (exc = 480 nm) in aerated acetonitrile solution.

counts

Figure S17. Excited state lifetime and the best fit of the experimental data for the [Cr(IMebipzp)2]3+ complex (exc = 480 nm) at 77 K in frozen acetonitrile.

counts

Figure S18. Excited state lifetime and the best fit of the experimental data for the [Cr(bip*)2]3+ complex (exc = 450 nm) in deaerated acetonitrile solution at room temperature.

counts

Figure S19. Excited state lifetime and the best fit of the experimental data for the [Cr(bip*)2]3+ complex (exc = 450 nm) in aerated acetonitrile solution at room temperature.

counts

Figure S20. Excited state lifetime and the best fit of the experimental data for the [Cr(bip*)]3+ complex (exc = 450 nm) at 77 K in frozen acetonitrile.

Theoretical studies

The Orca[S3] (version 5.0.3) and Gaussian 16[S4] (revision A.03) software packages were used to investigate the structural and electronic properties of the studied complexes. Starting from the X-ray diffraction structures, the ground, 4A2 state, structure of the two complexes were obtained from DFT optimizations using the unrestricted version of the Becke three-parameters exchange function in combination with the Lee-Yang-Parr correlation functional (UB3LYP). The Ahlrichs’ polarized valence triple- basis set def2-TZVPP was used for these optimizations. The D3 version of Grimme’s dispersion with Becke-Johnson damping (GD3BJ) was applied. Solvent effects were included via the Conductor-like Polarizable Continuum Model (CPCM) as implemented in Orca 5.0.3 with the dielectric constant of acetonitrile. Optimized geometries were confirmed to be stationary points by analysis of their vibrational frequencies. Tight convergence criteria were selected for the optimization step. The resolution of identity approach for the Coulomb term in combination with the chain-of-spheres approximation for the exchange term (RIJCOSX) was applied. The zero-order relativistic approximation (ZORA) was used to describe relativistic effects. Spin density information was extracted from the optimized geometries.

Ab initio ligand field (AILF) analysis was performed over the optimized geometries using Orca version 5.0.3. The complete-active-space self-consistent field method (CASSCF) together with the fully internally contracted N-electron valence perturbation theory to second order (FIC-NEVPT2) was used, selecting only the 3d orbitals as active space (CASSCF(3,5)/FIC-NEVPT2) and using the def2-TZVPP basis set in combination with the RI-JK approximation (def2/JK as auxiliary base). 10 quartet and 40 doublet roots were computed for the AILF analysis.

To accurately model the ligand field, CASSCF together with FIC-NEVPT2 was used. Dominant bonding/antibonding orbitals formed between ligand and chromium and a second d shell were considered, creating an active space of 7 electrons and 12 orbitals (CASSCF(7,12)/FIC-NEVPT2). 10 quartet and 9 doublet roots were computed to calculate the energies of the excited states.

The 50 lowest energetic transitions were calculated by TD-DFT as implemented in Gaussian 16, using the unrestricted version of the Coulomb-attenuated B3LYP functional (UCAM-B3LYP), selecting the def2-TZVPP basis set and considering solvent effects. Electronic transitions were corrected by –0.3 eV to better fit experimental results. Charge transfer numbers were computed using TheoDORE 2.4.[S5] Electron density difference maps (EDDMs) were obtained using GaussSum,[S6] and visualized using UCSF Chimera (isoval=0.002).[S7]

Optimized Geometries

Figure S21. DFT optimized geometries of the quartet ground state of 1(left), 2 (middle) and 3 (right). Spin density at the Cr center: 3.162171, 3.143759 and 3.111739 (respectively).

Table S6. Bond lengths (Å) and angles (°) of 1 and 2 from XRD measurements and DFT calculations. and CASSCF(7,12)/FIC-NEVPT2 results of 1, 2 and 3. Energies in cm-1.

|  | 3 |  | 2 |  | 1 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | XRD | DFT | XRD | DFT | XRD | DFT |
| Cr-N1 | 2.0777 | 2.1313 | 2.1040 | 2.1169 | 2.0868 | 2.1137 |
| Cr–N2 | 2.0976 | 2.1314 | 2.0910 | 2.1168 | 2.0812 | 2.1136 |
| Cr–N3 | 1.9976 | 2.0572 | 2.0687 | 2.0819 | 2.0471 | 2.0764 |
| Cr–N4 | 2.0433 | 2.0564 | 2.0656 | 2.0788 | 2.0634 | 2.0765 |
| Cr–N5 | 2.0293 | 2.0564 | 2.0650 | 2.0837 | 2.0550 | 2.0765 |
| Cr–N6 | 2.0470 | 2.0572 | 2.0677 | 2.0802 | 2.0527 | 2.0764 |
| N1–Cr–N2 | 178.48 | 179.84 | 178.97 | 179.96 | 177.28 | 179.99 |
| N1–Cr–N3 | 92.93 | 87.14 | 87.60 | 87.72 | 87.97 | 88.24 |
| N1–Cr–N4 | 88.83 | 92.67 | 91.98 | 92.20 | 90.20 | 91.75 |
| N1–Cr–N5 | 91.69 | 87.22 | 88.24 | 87.92 | 88.44 | 88.24 |
| N1–Cr–N6 | 88.52 | 92.97 | 92.70 | 92.29 | 93.39 | 91.76 |
| N2–Cr–N3 | 87.31 | 92.97 | 91.37 | 92.32 | 90.36 | 91.75 |
| N2–Cr–N4 | 92.65 | 87.21 | 88.03 | 87.81 | 87.82 | 88.25 |
| N2–Cr–N5 | 88.07 | 92.67 | 92.79 | 92.04 | 93.29 | 91.77 |
| N2–Cr–N6 | 90.00 | 87.15 | 87.30 | 87.70 | 88.63 | 88.24 |
| N3–Cr–N4 | 94.41 | 94.20 | 94.32 | 93.64 | 95.43 | 93.72 |
| N3–Cr–N5 | 175.38 | 174.36 | 175.83 | 175.65 | 176.10 | 176.48 |
| N3–Cr–N6 | 85.15 | 86.05 | 86.55 | 86.48 | 85.80 | 86.39 |
| N4–Cr–N5 | 85.65 | 86.10 | 85.98 | 86.50 | 86.11 | 86.40 |
| N4–Cr–N6 | 177.29 | 174.36 | 175.27 | 175.51 | 176.25 | 176.49 |
| N5–Cr–N6 | 95.00 | 94.20 | 93.49 | 93.72 | 92.89 | 93.70 |

|  | 2E (1) | 2E (2) | 2T1 (1) | 2T1 (2) | 2T1 (3) | 2T2 (1) | 2T2 (2) | 2T2 (3) | 4T2 (1) | 4T2 (2) | 4T2 (3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 15557 | 16110 | 15247 | 15314 | 16019 | 23553 | 23700 | 23976 | 21386 | 21410 | 22690 |
| 2 | 15558 | 16104 | 15230 | 15377 | 16033 | 23490 | 23699 | 23924 | 21205 | 21244 | 22522 |
| 3 | 15342 | 15916 | 14741 | 14933 | 15722 | 23268 | 23410 | 23909 | 20486 | 21446 | 22129 |

Figure S22. Schematic representation of the energy levels for the calculated (CASSCF(7,12)/FIC-NEVPT2) excited states of 1 (left), 2 (middle) and 3 (right).

Table S7. Orbitals used in the CASSCF(7,12)/FIC-NEVPT2 calculations for 1 (isoval=0.04).

| # | E (hartrees) | Orbital | # | Energy | Orbital |
| --- | --- | --- | --- | --- | --- |
| 165 | -0.877399 |  | 171 | -0.205190 |  |
| 166 | -0.867665 |  | 172 | 0.730059 |  |
| 167 | -0.421046 |  | 173 | 0.753275 |  |
| 168 | -0.411074 |  | 174 | 0.755171 |  |
| 169 | -0.403576 |  | 175 | 1.365514 |  |
| 170 | -0.199660 |  | 176 | 1.405373 |  |

Table S8. Orbitals used in the CASSCF(7,12)/FIC-NEVPT2 calculations for 2 (isoval=0.04).

| # | E (hartrees) | Orbital | # | Energy | Orbital |
| --- | --- | --- | --- | --- | --- |
| 213 | -0.876005 |  | 219 | -0.209919 |  |
| 214 | -0.868147 |  | 220 | 0.728399 |  |
| 215 | -0.424772 |  | 221 | 0.750394 |  |
| 216 | -0.414683 |  | 222 | 0.749667 |  |
| 217 | -0.408243 |  | 223 | 1.356002 |  |
| 218 | -0.205755 |  | 224 | 1.387980 |  |

Table S9. Orbitals used in the CASSCF(7,12)/FIC-NEVPT2 calculations for 3 (isoval=0.04).

| # | Energy (Hartrees) | Orbital | # | Energy (Hartrees) | Orbital |
| --- | --- | --- | --- | --- | --- |
| 185 | -0.856996 |  | 191 | -0.180911 |  |
| 186 | -0.871802 |  | 192 | 0.758509 |  |
| 187 | -0.407756 |  | 193 | 0.741001 |  |
| 188 | -0.396342 |  | 194 | 0.771543 |  |
| 189 | -0.389943 |  | 195 | 1.355980 |  |
| 190 | -0.195714 |  | 196 | 1.427039 |  |

Electronic transitions

Table S10. Calculated 50 lowest electronic transitions for compound 1, their energies (in nm) and oscillatory strength (in cgs units).

| Transition number | Wavelength / nm | Osc. Strength / cgs | Transition number | Wavelength / nm | Osc. Strength / cgs |
| --- | --- | --- | --- | --- | --- |
| 1 | 511.75 | 0.0001 | 31 | 274.02 | 0.0019 |
| 2 | 504.50 | 0.0002 | 32 | 272.41 | <0.0001 |
| 3 | 475.65 | 0.0006 | 33 | 269.12 | 0.0067 |
| 4 | 433.23 | <0.0001 | 34 | 268.79 | <0.0001 |
| 5 | 388.10 | 0.0005 | 35 | 268.52 | 0.0027 |
| 6 | 371.89 | 0.0001 | 36 | 267.58 | 0.0025 |
| 7 | 353.32 | <0.0001 | 37 | 267.48 | 0.0162 |
| 8 | 353.29 | 0.0001 | 38 | 266.03 | 0.0505 |
| 9 | 344.68 | 0.0012 | 39 | 264.94 | <0.0001 |
| 10 | 343.92 | 0.0010 | 40 | 262.86 | 0.1052 |
| 11 | 337.99 | 0.0001 | 41 | 259.77 | 0.0227 |
| 12 | 334.34 | 0.0141 | 42 | 258.61 | 0.1918 |
| 13 | 330.27 | 0.0049 | 43 | 256.50 | 0.0013 |
| 14 | 325.80 | 0.0000 | 44 | 256.47 | 0.0007 |
| 15 | 306.46 | 0.0138 | 45 | 255.01 | <0.0001 |
| 16 | 306.43 | 0.0075 | 46 | 254.82 | 0.0429 |
| 17 | 305.30 | 0.0200 | 47 | 253.58 | 0.0076 |
| 18 | 304.50 | <0.0001 | 48 | 253.44 | 0.0091 |
| 19 | 299.12 | 0.0067 | 49 | 253.08 | 0.0081 |
| 20 | 290.03 | 0.0066 | 50 | 251.42 | 0.0165 |
| 21 | 285.02 | <0.0001 | 51 | 249.87 | 0.0169 |
| 22 | 282.93 | <0.0001 | 52 | 249.36 | 0.0012 |
| 23 | 281.65 | 0.0093 | 53 | 249.33 | 0.0373 |
| 24 | 279.00 | 0.0064 | 54 | 247.40 | 0.0436 |
| 25 | 275.98 | <0.0001 | 55 | 245.73 | 0.0082 |

Figure S23. TD-DFT charge transfer numbers of 1 defined from 0 to 1 of the first 50 electronic transitions.

| #1: 511.75 nm dxy → dx2− y2 | #2: 504.50 nm dxz → dz2 | #3: 475.65 nm dyz → dz2 |
| --- | --- | --- |
| #4: 433.23 nm dxy → dz2 | #5: 388.10 nm dxz → dx2− y2 | #6: 371.89 nm dyz → dx2− y2 |

Figure S24. Electron density difference maps (EDDM) of the first six electronic transitions calculated for 1 (isoval 0.002). Blue: density loss; Purple: density gain.

Figure S25. Experimental UV-Vis spectrum of compound 1 in acetonitrile and calculated oscillatory strength of the calculated electronic transitions. a) Full view; b) Zoom view.

Table S7. Calculated 100 lowest electronic transitions for compound 2, their energies (in nm) and oscillatory strength (in cgs units).

| Transition number | Wavelength / nm | Osc. Strength / cgs | Transition number | Wavelength / nm | Osc. Strength / cgs |
| --- | --- | --- | --- | --- | --- |
| 1 | 473.10 | 0.000108964 | 41 | 318.20 | 0.000263198 |
| 2 | 456.50 | 0.000452785 | 42 | 316.90 | 0.008250000 |
| 3 | 433.60 | 0.002120000 | 43 | 316.30 | 0.058120000 |
| 4 | 421.70 | 0.016060000 | 44 | 315.80 | 0.000985345 |
| 5 | 418.80 | 0.000068200 | 45 | 315.10 | 0.000107209 |
| 6 | 418.20 | 0.001340000 | 46 | 314.90 | 0.000030102 |
| 7 | 417.20 | 0.000016529 | 47 | 314.80 | 0.000192036 |
| 8 | 412.10 | 0.016820000 | 48 | 314.10 | 0.000598102 |
| 9 | 393.00 | 0.004440000 | 49 | 313.70 | 0.000030902 |
| 10 | 391.50 | 0.035680000 | 50 | 313.30 | 0.000015566 |
| 11 | 390.50 | 0.028460000 | 51 | 313.20 | 0.000275754 |
| 12 | 385.40 | 0.001030000 | 52 | 312.20 | 0.031220000 |
| 13 | 384.30 | 0.000661078 | 53 | 310.60 | 0.000008509 |
| 14 | 383.20 | 0.000032186 | 54 | 309.30 | 0.000037478 |
| 15 | 381.90 | 0.000000908 | 55 | 306.80 | 0.000039574 |
| 16 | 381.10 | 0.001170000 | 56 | 306.70 | 0.000757662 |
| 17 | 377.20 | 0.006460000 | 57 | 306.60 | 0.000260772 |
| 18 | 368.10 | 0.000055521 | 58 | 306.20 | 0.001170000 |
| 19 | 361.70 | 0.038660000 | 59 | 305.60 | 0.000515571 |
| 20 | 359.20 | 0.001340000 | 60 | 301.60 | 0.000104348 |
| 21 | 354.00 | 0.000060078 | 61 | 301.40 | 0.000234251 |
| 22 | 353.70 | 0.001060000 | 62 | 301.10 | 0.000031909 |
| 23 | 352.50 | 0.000393966 | 63 | 300.80 | 0.000012235 |
| 24 | 344.60 | 0.000040619 | 64 | 300.10 | 0.000014117 |
| 25 | 339.60 | 0.013930000 | 65 | 300.00 | 0.000349261 |
| 26 | 338.40 | 0.000355893 | 66 | 299.80 | 0.000059690 |
| 27 | 338.10 | 0.000377016 | 67 | 299.50 | 0.000052418 |
| 28 | 336.00 | 0.000003415 | 68 | 296.90 | 0.003600000 |
| 29 | 334.50 | 0.000046120 | 69 | 293.00 | 0.000007392 |
| 30 | 330.80 | 0.000196906 | 70 | 291.60 | 0.000393282 |
| 31 | 326.80 | 0.006340000 | 71 | 290.50 | 0.000752906 |
| 32 | 326.30 | 0.000424654 | 72 | 289.90 | 0.000006983 |
| 33 | 325.00 | 0.008490000 | 73 | 289.60 | 0.000008326 |
| 34 | 323.10 | 0.000030904 | 74 | 289.10 | 0.001010000 |
| 35 | 322.90 | 0.002350000 | 75 | 287.70 | 0.000320723 |
| 36 | 322.00 | 0.002180000 | 76 | 287.00 | 0.000187108 |
| 37 | 321.30 | 0.000376841 | 77 | 285.60 | 0.017430000 |
| 38 | 319.40 | 0.001310000 | 78 | 284.90 | 0.017870000 |
| 39 | 318.60 | 0.000213804 | 79 | 284.10 | 0.019970000 |
| 40 | 318.40 | 0.000317286 | 80 | 283.30 | 0.005930000 |

| Transition number | Wavelength / nm | Osc. Strength / cgs | Transition number | Wavelength / nm | Osc. Strength / cgs |
| --- | --- | --- | --- | --- | --- |
| 81 | 283.00 | 0.000121244 | 91 | 277.10 | 0.000200959 |
| 82 | 282.90 | 0.000757880 | 92 | 277.10 | 0.000194927 |
| 83 | 282.90 | 0.000597674 | 93 | 276.70 | 0.003830000 |
| 84 | 282.50 | 0.000952859 | 94 | 276.40 | 0.010510000 |
| 85 | 282.30 | 0.000178893 | 95 | 275.60 | 0.001890000 |
| 86 | 282.30 | 0.001010000 | 96 | 275.40 | 0.002880000 |
| 87 | 278.60 | 0.011260000 | 97 | 275.30 | 0.001330000 |
| 88 | 278.30 | 0.000042284 | 98 | 274.60 | 0.001930000 |
| 89 | 278.00 | 0.001410000 | 99 | 273.80 | 0.009130000 |
| 90 | 277.80 | 0.000243845 | 100 | 269.70 | 0.031430000 |

Figure S26. TD-DFT charge transfer numbers of 2 defined from 0 to 1 of the first 100 electronic transitions.

| #1: 473.10 nm dxy → dx2− y2 | #2: 456.50 nm dxz → dz2 | #3: 433.60 nm dyz → dx2− y2 |
| --- | --- | --- |
| #4: 421.70 nm LMCT | #5: 418.80 nm LMCT | #6: 418.20 nm LMCT |

Figure S27. Electron density difference maps (EDDM) of the first six electronic transitions calculated for 2 (isoval 0.002). Blue: density loss; Purple: density gain.

Figure S28. Experimental UV-Vis spectrum of compound 2 in acetonitrile and calculated oscillatory strength of the calculated electronic transitions. a) Full view; b) Zoom view.

Table S7. Calculated 50 lowest electronic transitions for compound 3, their energies (in nm) and oscillatory strength (in cgs units).

| Transition number | Wavelength / nm | Osc. Strength / cgs | Transition number | Wavelength / nm | Osc. Strength / cgs |
| --- | --- | --- | --- | --- | --- |
| 1 | 480.90 | 0.000502828 | 41 | 327.40 | 0.000419571 |
| 2 | 469.50 | 0.000072148 | 42 | 324.10 | 0.000002021 |
| 3 | 452.60 | 0.000002317 | 43 | 322.10 | 0.000448382 |
| 4 | 449.10 | 0.042220000 | 44 | 321.10 | 0.000000117 |
| 5 | 443.40 | 0.034090000 | 45 | 320.20 | 0.010290000 |
| 6 | 438.00 | 0.001590000 | 46 | 315.20 | 0.005560000 |
| 7 | 424.10 | 0.000000218 | 47 | 312.70 | 0.002310000 |
| 8 | 423.60 | 0.019750000 | 48 | 311.50 | 0.000901356 |
| 9 | 418.40 | 0.000014488 | 49 | 309.80 | 0.000005275 |
| 10 | 414.30 | 0.010280000 | 50 | 309.20 | 0.000060072 |
| 11 | 404.00 | 0.000000630 | 51 | 306.60 | 0.002170000 |
| 12 | 398.80 | 0.000001024 | 52 | 306.30 | 0.002850000 |
| 13 | 394.80 | 0.006230000 | 53 | 305.70 | 0.000376664 |
| 14 | 385.70 | 0.000451373 | 54 | 305.10 | 0.000948934 |
| 15 | 384.80 | 0.000019833 | 55 | 304.80 | 0.000618534 |
| 16 | 383.60 | 0.011100000 | 56 | 304.20 | 0.011410000 |
| 17 | 376.20 | 0.001330000 | 57 | 299.00 | 0.000338436 |
| 18 | 375.60 | 0.097690000 | 58 | 297.70 | 0.000262351 |
| 19 | 373.30 | 0.073920000 | 59 | 297.50 | 0.009260000 |
| 20 | 363.50 | 0.088430000 | 60 | 297.00 | 0.052430000 |
| 21 | 360.70 | 0.005600000 | 61 | 296.70 | 0.001060000 |
| 22 | 359.80 | 0.001540000 | 62 | 295.50 | 0.001140000 |
| 23 | 353.50 | 0.000003055 | 63 | 295.40 | 0.000032476 |
| 24 | 347.20 | 0.014470000 | 64 | 294.60 | 0.000262728 |
| 25 | 345.40 | 0.004540000 | 65 | 294.40 | 0.000066425 |
| 26 | 341.80 | 0.000007731 | 66 | 294.30 | 0.000439374 |
| 27 | 341.20 | 0.003760000 | 67 | 294.20 | 0.000348638 |
| 28 | 340.30 | 0.001190000 | 68 | 293.80 | 0.000009963 |
| 29 | 338.70 | 0.000026103 | 69 | 293.20 | 0.003590000 |
| 30 | 337.40 | 0.000305482 | 70 | 291.50 | 0.000000426 |
| 31 | 336.60 | 0.000129417 | 71 | 291.00 | 0.000000251 |
| 32 | 334.70 | 0.004950000 | 72 | 291.00 | 0.004640000 |
| 33 | 334.20 | 0.001630000 | 73 | 290.50 | 0.004660000 |
| 34 | 334.20 | 0.000095017 | 74 | 289.40 | 0.000539907 |
| 35 | 332.40 | 0.015170000 | 75 | 289.30 | 0.000158726 |
| 36 | 331.20 | 0.000176195 | 76 | 289.30 | 0.000105146 |
| 37 | 330.70 | 0.001130000 | 77 | 289.10 | 0.000002374 |
| 38 | 330.40 | 0.000588991 | 78 | 288.70 | 0.001650000 |
| 39 | 329.40 | 0.001860000 | 79 | 288.20 | 0.003640000 |
| 40 | 327.50 | 0.002100000 | 80 | 286.50 | 0.003540000 |

| Transition number | Wavelength / nm | Osc. Strength / cgs | Transition number | Wavelength / nm | Osc. Strength / cgs |
| --- | --- | --- | --- | --- | --- |
| 81 | 286.20 | 0.004070000 | 91 | 280.50 | 0.074520000 |
| 82 | 285.80 | 0.000378163 | 92 | 278.10 | 0.004930000 |
| 83 | 283.90 | 0.000553583 | 93 | 277.80 | 0.003430000 |
| 84 | 283.70 | 0.010230000 | 94 | 276.40 | 0.000233219 |
| 85 | 283.30 | 0.004560000 | 95 | 276.20 | 0.000844896 |
| 86 | 282.90 | 0.000234102 | 96 | 275.60 | 0.000359979 |
| 87 | 281.90 | 0.006860000 | 97 | 275.30 | 0.000024417 |
| 88 | 280.90 | 0.000001937 | 98 | 274.40 | 0.000685888 |
| 89 | 280.70 | 0.070110000 | 99 | 274.40 | 0.014700000 |
| 90 | 280.50 | 0.034560000 | 100 | 273.90 | 0.000135663 |

Figure S29. TD-DFT charge transfer numbers of 3 defined from 0 to 1 of the first 100 electronic transitions.

| #1: 480.90 nm dxz → dz2 | #2: 469.50 nm dxy → dx2− y2 | #3: 452.60 nm dxy → dz2 |
| --- | --- | --- |
| #4: 449.10 nm LMCT | #5: 443.40 nm dyz → dz2 | #6: 438.00 nm LMCT |

Figure S30. Electron density difference maps (EDDM) of the first six electronic transitions calculated for 3 (isoval 0.002). Blue: density loss; Purple: density gain.

Figure S31. Experimental UV-Vis spectrum of compound 3 in acetonitrile and calculated oscillatory strength of the calculated electronic transitions. a) Full view; b) Zoom view.

Geometries

1

Cr  0.00030435029453     -0.00017921823173     -0.00049039987500

N   -2.33690501176889      1.07453338641386      1.54343861201445

N   1.42021167754291      0.06641599046485     -1.51406696974597

N   1.42009516649813     -0.05722678341546      1.51370684643270

N   2.33652506414530     -1.07103247340930      1.54761055108532

N   -1.41905175054907     -0.07040328779766     -1.51430386441064

N   2.33061672107800      1.08568819930022     -1.54682149288553

N   -2.32947040999390     -1.08972189779818     -1.54509724965039

N   -0.00647124177198      2.11345029297479     -0.00295235841621

N   0.00761741825178     -2.11383361537157      0.00184572279727

N   -1.42036804250698      0.06072034091955      1.51274332120682

C   -1.60109726134686     -0.64270531968421      2.65426867191383

C   1.59954384398627      0.64853842038052      2.65398965361242

C   2.63618670704127     -0.05499484214087     -3.38803305902396

H   3.01234560254262     -0.38916785164203     -4.33860568049301

C   -1.17284506599860      4.18157141273865      0.26108791883780

H   -2.10188352231432      4.68766473434493      0.47601195629188

C   1.14653909533677     -2.79687123507452      0.25138153063932

C   -2.42757082910356      2.04425946984976      0.47137228721253

H   -3.20353732131943      2.74859879817172      0.74450134500887

H   -2.74683381802563      1.54738902558661     -0.44152987828438

C   -2.63537593970796     -0.06414620564550      3.38707700600673

H   -3.00958258512013     -0.39876062706591      4.33826301050327

C   1.12811020607375      2.80393628545001     -0.25186764848613

C   2.42841050279070     -2.04296016020391      0.47769556764389

H   3.20432323354385     -2.74650573711252      0.75300571907730

H   2.74834719876172     -1.54792093511288     -0.43595884483670

C   -1.60448252879049      0.63245104493416     -2.65542307916467

C   3.08335560452259     -1.02221077250337      2.66870787752026

C   -2.41372481780895     -2.06066483566597     -0.47361040587721

H   -3.18479294777447     -2.77014405618854     -0.74732000990819

H   -2.73659810859847     -1.56657667380639      0.43951704182228

C   1.60483290615673     -0.63783268619559     -2.65447341808929

C   -1.14529147768609      2.79735117639127      0.24462675956393

C   2.41508781490573      2.05842100232835     -0.47700576711007

H   3.18653784044103      2.76707063657466     -0.75177688404985

H   2.73749100429962      1.56577946553665      0.43707522117763

C   -1.12651324294178     -2.80522137800358     -0.24670917483573

C   -3.08466142870465      1.02831940756000      2.66403371607060

C   1.14704169436231      4.18827962576077     -0.27097099963382

H   2.07284330717151      4.69988337379384     -0.48684483230121

C   3.07901592847109      1.04145230787862     -2.66707550235465

C   -2.63539264039187      0.04785043812918     -3.38820359985458

H   -3.01195016547075      0.38059298864902     -4.33912100789813

C   -0.01509668298371      4.89187155024801     -0.00559337657824

H   -0.01844962864345      5.97260050973459     -0.00658961847157

C   -0.84166577166289      1.84806404540798     -3.05193483338164

H   -1.09753546491073      2.70368148526904     -2.42849422984877

H   -1.10013745211576      2.09956828565903     -4.07759567343375

H   0.23234353022277      1.70021304787845     -3.00153810038465

C   0.84071967412469     -1.85301431950943     -3.04978865826255

H   1.09623720950150     -2.70846300007124     -2.42600484237624

H   1.09840853256206     -2.10538391490192     -4.07543884751156

H   -0.23315847115887     -1.70425186635333     -2.99892797746669

C   1.17465998439909     -4.18105705575511      0.27013581616154

H   2.10376392455681     -4.68638733927216      0.48657282259070

C   -3.07779486728827     -1.04762593798348     -2.66548896540726

C   2.63336656369166      0.07183520010900      3.38889797664904

H   3.00654600335131      0.40846329963011      4.33977602594454

C   0.82812466232199      1.85955972838741      3.04793193642062

H   1.07819617953989      2.71573588119078      2.42294794202702

H   1.08443766921371      2.11480084021218      4.07321450813818

H   -0.24481833936402      1.70410974432391      2.99748179265814

C   -0.83047442932573     -1.85326121977666      3.05120271578389

H   -1.07919490427022     -2.71021311758443      2.42675526851216

H   -1.08876680821094     -2.10725336109809      4.07629149351362

H   0.24254985698938     -1.69772082748106      3.00260908087383

C   -4.15867218930084      2.00706719884704      2.97213904174765

H   -3.76866259207043      3.02557964592842      2.99496859781053

H   -4.58482705899344      1.77714883239494      3.94507912657256

H   -4.95392655953992      1.96684366053135      2.22628635747401

C   -1.14482294160243     -4.18959623400191     -0.26361810773028

H   -2.07025438961482     -4.70196811187958     -0.47925272566163

C   4.14726498837911      2.02590912703745     -2.97701487095687

H   3.75153381591643      3.04218814698547     -3.00058703249598

H   4.57398858562554      1.79736847431706     -3.95002900219650

H   4.94331034701031      1.99088842486725     -2.23173832924206

C   4.15703044325350     -2.00027853291341      2.98008786754460

H   3.76708196333500     -3.01878291376500      3.00430733632825

H   4.58183735630819     -1.76846747636099      3.95316959618664

H   4.95331063981987     -1.96138121243364      2.23525806866097

C   0.01743142371726     -4.89227035862705      0.00370314931439

H   0.02124591192511     -5.97299789588840      0.00441042443470

C   -4.14592155500946     -2.03278340108520     -2.97364641042079

H   -3.74987829862428     -3.04896293543716     -2.99625375815370

H   -4.57329168299908     -1.80554861102460     -3.94668229586976

H   -4.94152290859922     -1.99713971781796     -2.22792849875097

2

I   12.58196104507405      3.36399154591363      7.24531204989903

I   2.93564970014811     10.68078108987436      4.38389425417440

I   3.61493688681225      7.97824043210413     10.49047994459432

Cr  8.02182188157902      7.47593898995100      6.09193121485771

I   12.94404849298149      7.83352871509917      2.26333023871842

N   9.94533602215487      6.51007087022082      8.18730404998615

N   8.94095206370001      9.08857279591054      7.10952853981209

N   9.31647655366074      7.65025115138610      4.47313576461390

N   7.05476962896736     10.12524643833410      5.06476056543558

N   7.10189862346266      5.86433551651497      5.07335624031893

N   6.21587521580638      5.91199473189722      7.90406008048007

C   4.44534725552077      7.62460512221280      5.29728434641027

H   4.21969337614454      7.20464615496032      4.31476235420954

H   3.50099419255058      7.91746940924100      5.75221556149175

H   4.88857699104917      6.84899850716512      5.90411483049405

N   6.65322096717798      8.84337160088387      5.31824460789714

C   9.87516533212734      7.34335290963595      2.31936820541392

C   5.21555068431614      5.91700350497640      8.80562219840633

C   6.34191168722467      4.85992045038460      3.04394711677289

H   6.25375216633306      4.92068262162624      1.96954262250616

C   10.64941798013025      7.84314761560207      4.37290031862355

N   8.87007709240280      7.35082309140077      3.21631534233234

N   9.45724141764440      6.23013820382499      6.94164685080349

N   6.65844785475090      7.17613280866549      7.63225925949446

C   10.20216312706305      5.21410791249468      6.45495189114045

C   5.01114214238180      7.25258046537372      9.13483872359686

C   9.68185584681035      7.03924229470164      0.88117608947241

H   9.23921270758933      6.05133788832519      0.74734769610594

H   10.64252560101413      7.05922956200468      0.37410906911537

H   9.02693337371465      7.77412597358355      0.41095513227034

C   9.46507298979904      8.91585535347590      8.34316662727295

C   4.53590595219356      4.68513911467928      9.27392889799914

H   4.11976684490378      4.12719070432026      8.43440916192325

H   3.72691523971464      4.95008994923821      9.94888553033116

H   5.23047172544621      4.03366375091364      9.80633605773202

C   10.97996525644223      5.70906090443661      8.50865826770237

C   8.45105002305096     10.50771675840512      5.15562387860297

H   8.51420614546204     11.55763902935537      4.89868815552463

H   9.02396555783257      9.95645942748089      4.41502459403842

C   6.79770864131865      4.75413249706186      7.25135108714305

H   6.28998669224201      3.87918356842178      7.63733792391976

H   7.84449831569383      4.67394258825167      7.53136983876980

C   9.99730893744442      4.55032468483826      5.14223286441087

H   9.35382739284015      3.67589933667215      5.26071991467420

H   10.95484493380368      4.20420931849736      4.75966850688654

H   9.55148168724718      5.20155485843627      4.40438352717117

C   6.95805830164486      5.89231796838930      3.73044151277797

C   5.91739785505056      8.01489800818816      8.38815493320278

C   4.89005033371322     10.10392444187698      4.78606258003176

C   6.15716920228618     12.36331576136475      4.43504978429392

H   6.60848815731869     12.89704576711583      5.27245199916544

H   5.17820967029194     12.79128213839050      4.23867848504755

H   6.78552018568698     12.51385924971874      3.55602630338375

C   6.08539542943108      9.48947992403850      8.44489221412270

H   6.77844171102152      9.75864340112222      9.24483319059825

H   5.12807399182107      9.95394122272737      8.66981839681236

H   6.45735931319946      9.90705382759595      7.52003596306636

C   9.01621603315273     10.30880477306425      6.53433793141457

C   11.02353802204981      7.66116245021536      3.03619438814457

C   6.01488529556397     10.91985160883420      4.74421258472297

C   10.08000180270229      9.95318769912570      9.02304869986714

H   10.49380624616956      9.76944660167391     10.00333818108918

C   9.37286469690811      7.56651530796069      9.00078729042440

H   9.92600938398527      7.58989492865090      9.93162886078772

H   8.34372317140116      7.31438825596206      9.24149260733277

C   11.15807524646858      4.86658853273109      7.41680509866374

C   6.00557181607279      3.74169026045904      5.11914095588894

H   5.63784774972891      2.91304349296463      5.70575546601275

C   9.61168228200240     11.38091347718517      7.17633880580360

H   9.64118866090137     12.34026057302829      6.68172762773626

C   5.31342171496838      8.82057805330975      5.15189420707721

C   11.54858628413020      8.22835346924635      5.49005935937512

H   11.68032866073160      9.31226165151835      5.51018848182966

H   12.52870007896075      7.78293078443743      5.33401562384492

H   11.18116016157702      7.91383739468835      6.45594645110286

C   7.46975765927534      7.07549176411292      2.95654135188395

H   7.37648898856367      6.86653246383157      1.89804262314092

H   6.88112682297731      7.96544157514381      3.16370607378530

C   6.63353948285080      4.79705321103737      5.75757276528342

C   5.85492075232950      3.76869993066853      3.74296060685673

H   5.36823685464425      2.95431669388835      3.22524265897053

C   11.71067000261155      5.79780913055607      9.79621179536969

H   12.14627776859056      6.78902188277993      9.92826077084247

H   12.51058533171009      5.06291261879282      9.81317227367821

H   11.04347408352904      5.60429568959990     10.63732369079390

C   10.15520843128528     11.20549424798321      8.43736547015644

H   10.62811011696325     12.02872954726698      8.95386194206626

3

Cr  8.63122906146343      5.28589767904733      7.73899443009920

N   7.05006305530688      3.85668474538851      7.74187209266907

N   9.49230896166365      4.17736657732771      6.23506212914896

N   9.34637488484008      2.82308412769657      6.17962988037558

N   6.25773966649277      6.26160863590054      9.29323387038391

C   6.88887476692799      7.17868525875560     11.18899273706037

C   10.30242205452704      3.35878561226875      4.27383279036495

C   8.02918441542741      6.82157953229869     10.41612519763091

C   9.32369272274260      7.06580543162964     10.90333157180470

C   5.47578026099228      5.70273954319085      8.20235368726938

C   5.77545600191132      4.24448554106621      7.97266719114121

C   10.08257578590318      4.52774310916458      5.05492046103113

C   5.78616869789423      6.79029264418270     10.41941559889277

C   7.30509419589251      2.54730639045495      7.52386210924605

C   8.72152151883543      2.09920667683458      7.27435401514192

C   9.80665724913695      2.30189981678461      5.04540635148908

C   4.99105579653416      1.99325948653590      7.77354656233221

C   6.29615118351196      1.59921971382408      7.53339695973660

C   10.45921240670138      5.78995720725041      4.56699643625341

C   7.03046801083146      7.77924816680081     12.45452355796449

C   11.24769686440375      4.68121417522624      2.53397835151857

C   9.43376921811870      7.65021127826817     12.14341884323295

C   10.89322952703853      3.43956762755278      2.99841045754174

C   11.03031068509021      5.84120861304907      3.31682869001010

C   4.73208681269290      3.33497550591293      7.99561599487764

C   8.30230583131139      8.00605602598639     12.91747478163429

N   7.61959064473692      6.25905381494771      9.24167364083810

N   10.21239702882981      6.71510784295577      7.74186434958652

N   7.77014297327612      6.39443313070449      6.23507052256407

N   7.91607483010165      7.74871606106592      6.17964206940732

N   11.00472578641651      4.31017661018791      9.29321237096293

C   10.37360195600734      3.39310738404801     11.18897825674618

C   6.96001342294959      7.21302006650573      4.27385051035955

C   9.23328745003159      3.75021828540064     10.41612091810168

C   7.93878227952965      3.50600542934092     10.90334339847574

C   11.78667851861506      4.86904747170333      8.20232816416132

C   11.48700466069420      6.32730310265764      7.97264861875384

C   7.17986974335655      6.04405983327517      5.05493137126382

C   11.47630358259816      3.78149294945956     10.41939125182024

C   9.95736737881597      8.02448687689277      7.52385605197469

C   8.54093798769839      8.47258905454661      7.27436365393303

C   7.45578185727175      8.26990408945739      5.04542447372407

C   12.27140956463427      8.57852696762537      7.77352091667434

C   10.96631346420586      8.97257022347210      7.53338028586936

C   6.80324030427117      4.78184509447863      4.56700247135110

C   10.23201773834021      2.79255958006547     12.45451753553722

C   6.01473109741570      5.89059438819535      2.53399766707855

C   7.82871454776662      2.92161487927051     12.14343824077726

C   6.36919542294160      7.13224076807104      2.99843273517144

C   6.23213109045065      4.73059699226072      3.31684007751694

C   12.53037649200475      7.23681040760935      7.99558980299871

C   8.96018327397609      2.56576643322640     12.91748450119645

N   9.64287416940692      4.31273579466455      9.24166241673980

H   6.95034079700195      3.87898266968984      5.13392381622559

H   5.93831412389459      3.76964483162571      2.91715190320613

H   5.56156075303276      5.78721129605851      1.55816916332791

H   6.20633764059058      8.02478660519352      2.41098310290381

H   7.50977789281877      9.32858001584597      4.85875161149736

H   8.53734372776673      9.52174608669270      7.00023237063630

H   7.93192112369872      8.35319719040690      8.16672633075063

H   10.72114675378599     10.00768157126251      7.34953852430027

H   13.07255568894389      9.30357498992893      7.78687783343302

H   13.53343827697071      6.88741338271900      8.18992793187190

H   12.83009943151398      4.75114056305514      8.47214580282392

H   11.60192329345140      4.28608355372136      7.30342445221762

H   12.53522225752243      3.71794486240812     10.60198554167298

H   11.10307947420829      2.52428527995297     13.03542929570343

H   8.81058388942998      2.10869568169407     13.88547335920391

H   6.84246233935104      2.72712565390195     12.54217622291377

H   7.05637703953781      3.76218899853444     10.34317489797837

H   10.31211984894274      6.69281794882537      5.13392296146038

H   11.32412968342111      6.80216120978481      2.91714307247587

H   11.70085852723393      4.78459969395731      1.55814606835558

H   11.05607813935613      2.54702379773056      2.41095533600428

H   9.75265644731196      1.24322502494919      4.85872888317198

H   9.33054771765129      2.21859284141043      8.16671134123498

H   8.72511249954724      1.05005104526562      7.00021726933640

H   6.54131926900583      0.56410879181442      7.34955473065333

H   4.18991184514723      1.26820913615207      7.78691090040231

H   3.72902554319712      3.68436999285848      8.18996123875458

H   5.66052661229418      6.28570687981122      7.30345045111645

H   4.43236096753896      5.82064264388616      8.47217925427533

H   4.72725120573346      6.85383862181678     10.60201688248955

H   6.15940996783613      8.04752179113231     13.03544115235951

H   8.45191181895173      8.46313922610403     13.88545676095788

H   10.42002429522019      7.84471185845404     12.54214393900975

H   10.20609420555513      6.80962360886747     10.34315657483897

References

[S1] G. M. Sheldrick, Acta Crystallogr., Sect. A: Found. Crystallogr., 2008, 64, 112–122.

[S2] O. V. Dolomanov, L. J. Bourhis, R. J. Gildea, J. A. K. Howard and H. Puschmann, J. Appl. Crystallogr., 2009, 42, 339–341.

[S3]	a) F. Neese, WIREs Comput. Mol. Sci. 2012, 2, 73-78; b) F. Neese, WIREs Comput. Mol. Sci. 2022, e1606.

[S4]	Gaussian 16, Revision A.03, M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria, M. A. Robb, J. R. Cheeseman, G. Scalmani, V. Barone, G. A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A. V. Marenich, J. Bloino, B. G. Janesko, R. Gomperts, B. Mennucci, H. P. Hratchian, J. V. Ortiz, A. F. Izmaylov, J. L. Sonnenberg, D. Williams-Young, F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone, T. Henderson, D. Ranasinghe, V. G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J. A. Montgomery, Jr., J. E. Peralta, F. Ogliaro, M. J. Bearpark, J. J. Heyd, E. N. Brothers, K. N. Kudin, V. N. Staroverov, T. A. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A. P. Rendell, J. C. Burant, S. S. Iyengar, J. Tomasi, M. Cossi, J. M. Millam, M. Klene, C. Adamo, R. Cammi, J. W. Ochterski, R. L. Martin, K. Morokuma, O. Farkas, J. B. Foresman, and D. J. Fox, Gaussian, Inc., Wallingford CT, 2016.

[S5]	J. Plasser, J. Chem. Phys. 2020, 084108.

[S6]	N. M. O'Boyle, A. L. Tenderholt and K. M. Langner, J. Comput. Chem., 2008, 29, 839-845.

[S7]	E. F. Pettersen, T. D. Goddard, C. C. Huang, G. S. Couch, D. M. Greenblatt, E. C. Meng, T. E. Ferrin, J. Comput. Chem., 2004, 13, 1605-1612.