Department of Inorganic Chemistry. University of Granada and “Unidad de Excelencia en Química (UEQ)”, Avda. Fuente Nueva s/n, 18071, Granada, Spain.

Department of Analytical and Inorganic Chemistry. University of Geneva. 30 quai Ernest Ansermet, CH-1211 Geneva 4, Switzerland.

Department of Chemistry, University of Basel, St. Johanns-Ring 19, 4056, Basel, Switzerland

Department of Organic Chemistry. University of Granada and “Unidad de Excelencia en Química (UEQ)”, Avda. Fuente Nueva s/n, 18071, Granada, Spain.

Laboratoire de Chimie et de Biochimie Pharmacologiques et Toxicologiques, Université Paris Cité, CNRS, 45 rue des Saint-Pères  F-75006 Paris, France.

Electronic Supplementary Information (ESI) available: [details of any supplementary information available should be included here]. See DOI: 10.1039/x0xx00000x

Received 00th January 20xx,

Accepted 00th January 20xx

DOI: 10.1039/x0xx00000x

Modulating the spin-flip rates and emission energies through ligand design in chromium(III) molecular rubies

Yating Ye,a Maxime Poncet,b Polina Yaltseva,c Pablo Salcedo-Abraira,a Antonio Rodríguez-Diéguez,a Javier Heredia Martín,a Laura Cuevas,a Carlos M. Cruz,d Benjamin Doistau,e Claude Piguet,b Oliver S. Wenger,c Juan Manuel Herrera,a and Juan-Ramón Jiméneza*

Three homoleptic spin-flip (SF) emitters, namely [Cr(Mebipzp)2]3+ (1), [Cr(IMebipzp)2]3+ (2) and [Cr(bip*)2]3+ (3) have been successfully synthesized and characterized. The weak distortion compared to perfect octahedron imparts favourable structural properties in the three complexes which display SF luminescence at approximately 740 nm with quantum yields in the range of 9-11% for 1 and 2 in deaerated acetonitrile solutions at 25°C. Time-resolved luminescence and transient UV-Vis absorption experiments unveiled lifetimes for the lowest-lying 2MC (metal-centered) of 1.5 ms for 1 and 350 s for 2. The incorporation of iodine atoms onto the ligand scaffold in 2 accelerates the 2MC  4A2 relaxation process through simultaneous enhancements in the radiative and non-radiative rates constants. In agreement, the experimentally calculated absorption oscillator strength for the 2MC  4A2 transition amounts to 9.8·10-7 and 2.5·10-6 for 1 and 2, respectively. The 2.5 factor enhancement observed in the iodine derivative indicates a higher spin-flip transition probability, translating into higher values for radiative rate constant (krad). Interestingly, in compound 3, the substitution of the distal methyl-pyrazole with indazole rings causes an important bathochromic shift of the spin-flip emission energy to 12000 cm⁻¹ (830 nm). Likely, the extended  system and the more covalent bond character induced by the indazole decreases the interelectronic repulsion further stabilizing the SF excited states. The recorded excited state lifetime of 111 s in 3 remains among the longest for a molecular ruby emitting beyond 800 nm. These discoveries signify an underexplored avenue for modifying deactivation pathways and emission energy while retaining high quantum yields and long-lived excited states in molecular rubies.

Introduction

The increasing interest and need for a more sustainable photochemistry has challenged scientists to develop photoactive metal complexes based on earth-abundant metals such as CoIII, VIII, FeII, FeIII, MnI, Cr0 or CrIII.1–17 Among those, CrIII has garnered significant attention due to its appealing physicochemical properties associated with (i) its relative kinetic inertness, enabling the manipulation of CrIII chromophores under different experimental conditions (ii) the small excited-state distortions associated with the relevant spin-flip (SF) transition favouring radiative relaxation against non-radiative and (iii) the long-lived electric-dipole and spin forbidden SF emission.18–23 When surrounded by a strong near-octahedral ligand field, CrIII exhibits long-lived Cr(2T1, 2E) excited states showing lifetimes in the millisecond range with overall quantum yields () attaining 17% for non-deuterated samples and up to 30% for deuterated ones.3,17,24–26 These appealing properties have been exploited in molecular upconversion and downshifting,27–32 molecular thermometry,33 circularly polarized luminescence (CPL)17,30,34–37 and photocatalysis.38,39 Most reported polypyridyl CrIII complexes show radiative emission within the range of 700 - 800 nm (14300 cm-1 - 12500 cm-1)18,25 but recent examples demonstrated that increasing metal-ligand covalency favours the nephelauxetic effect (i.e. decreases the electron-electron repulsion) stabilizing the SF states and thus shifting the CrIII centered emission up to 1000-1067 nm (NIR-II region, ~ 9400 cm-1).40–43 Conversely, Heinze and coworkers harnessed weak π accepting ligands in the [Cr(bpmp)2]3+ complex (bpmp = 2,6-bis(2-pyridylmethyl)pyridine) which displays strong red emission ( = 709 nm) (Fig. 1a).44 Since CrIII coordination chemistry has been mainly limited to polypyridyl organic ligands, Scattergood and co-workers introduced a novel class of ligands in which a central pyridine is functionalized at the 2,6 positions with 1,2,3-triazoles donors.45  However, the photophysical properties of [Cr(btmp)2]3+ (btmp = 2,6-bis(4-phenyl-1,2,3-triazol-1-yl-methyl)-pyridine) remain comparatively modest ( = 0.27%; τ = 37.9 s) (Fig. 1b).

Boosting the overall luminescence quantum yield in this type of chromophores has traditionally been achieved by reducing high-energy oscillators (e.g., C-H, O-H, or N-H) near the metal center, thereby lowering non-radiative rates (knrad).26 However, beyond this common approach, other strategies such as  enhancing the radiative rate constant (krad)—which describes the intrinsic rate of spontaneous emission from an excited state in the absence of any other non-radiative deactivating processes, remain comparatively underexplored.46,47 The radiative rate lifetime, τrad (krad−1), is a key parameter that governs the luminescence quantum yield, as shown in Equation 1, where ηsens is the sensitization efficiency, τobs is the measured (observed) luminescence lifetime, and knrad represents non-radiative rates. This equation reveals that higher values of krad relative to knrad could, in principle, promote greater emission efficiencies. The luminescence quantum yields of CrIII spin-flip emitters are currently constrained by the low radiative rates, a consequence of the intrinsically doubly forbidden nature of this transition. Therefore, enhancing krad presents an especially appealing strategy for improving the performance of this class of compounds.

=sens τobsτrad = sens krad krad + knrad 	(eq. 1)

Figure 1. Structure, luminescence quantum yield, emission lifetime (deaerated CH3CN/HClO4 solution at 293 K), wavelength of the emission band maximum, full width at half maximum of emission band and radiative rate constant of some closely related emissive chromium(III) complexes: a) [Cr(bpmp)2]3+,[36] b) [Cr(btmp)2]3+,[37] c) [Cr(Mebipzp)2]3+ and d) [Cr(IMebipzp)2]3+ e) [Cr(bip*)2]3+ (this work).

In this work, we present the modulation of spin-flip transition rates and the adjustment of emission energy through precise tuning of the organic ligands. We demonstrate that substituting the distal pyridines at the 2 and 6 positions of the ligand bpmp (Fig. 1a) with functionalized pyrazolyl or indazole groups (Fig. 1c-e) significantly broadens the spin-flip emission bandwidth, tune the radiative rates and modify the emission energy while maintaining long excited-state lifetimes and relatively high luminescence quantum yields compared to the related [Cr(btmp)2]3+. The syntheses, crystal structures, theoretical calculations and photophysical properties of these three novel molecular rubies: [Cr(Mebipzp)2]3+ (1) (Mebipzp = 2,6-bis((3,5-dimethyl-1H-pyrazol-1-yl)methyl)pyridine; Fig. 1c), [Cr(IMebipzp)2]3+ (2) (IMebipzp = 2,6-bis((4-iodo-3,5-dimethyl-1H-pyrazol-1-yl)methyl)pyridine; Fig. 1d) and [Cr(bip*)2]3+ (3) (bip* = 2,6-bis(indazol-2-ylmethyl)pyridine; Fig. 1e) are discussed hereunder.

Results and discussion

Synthesis and structural properties

Reacting CrII(SO3CF3)2·2H2O48 with two equivalents of Mebipzp, IMebipzp or bip* ligands, followed by oxidation with silver triflate (AgSO3CF3) in acetonitrile led to the desired compounds in a 90-95% yield (Fig. S1, further synthetic details in SI). The alternative air oxidation resulted in undesirable redox reactions. Single crystals suitable for X-ray diffraction were obtained from slow diffusion of diethyl ether into concentrated acetonitrile solutions containing the CrIII complexes (Table S1). For the three compounds, the two tridentate ligands coordinate in a twisted and meridional fashion (Fig. 2a, Fig. S2-S4) around the central CrIII cation with dihedral angles of approximately 57° and 50° between the central pyridine ring and the flanking pyrazoles or indazoles units. Due to the distorted conformation adopted by the ligands, a decrease in the symmetry point group (D2d → D2) generates a pair of enantiomers (λλ and ; notation for the ligand disposition)49 that crystallize as racemic mixtures (PP and MM enantiomers). The four iodine atoms in 2 are in the equatorial plane of the molecule and the average Cr···I distance amounts to 6.22 Å. In all three compounds, the Cr–N(pyridine) bond lengths range from 2.0813(14) to 2.104(5) Å, consistent with those found in related polypyridyl-based molecular rubies and in the particular case of [Cr(bpmp)2]3+ with six coordinated pyridines (average Cr-N distance = 2.0731(13) Å). In contrast, the Cr–N(pyrazole) and Cr–N(indazole) bond lengths are shorter, spanning from 2.0470(15) to 2.069(5) Å in compounds 1 and 2, and reaching 1.999(7) Å in compound 3 (Fig. 2a and Table S2-S4). This reduction in bond length suggests a slightly greater covalent character compared to the Cr–N(pyridyne) bonds, with this effect being more pronounced for the indazole-based ligand. Similar findings have been observed in [Cr(btmp)₂]³⁺, where the Cr–N(triazole) bond are as short as 1.995(2) Å.45 This structural feature induces compression in the equatorial plane of the complexes, resulting in a non-negligible Jahn-Teller distortion in the ground state.

The N(terminal)-Cr-N(terminal) bite angles of 175°-177° are close to 180° expected for a perfect octahedron (Table S2-S4). A detailed geometrical analysis using ∑ =  ∑i=112|90−ϕi|, where ϕi are the cisoid N−Cr−N bond angles (Table S2-S4), shows ∑ = 31°, 33° and 33° for 1, 2 and 3, and 27° and 25° for [Cr(btmp)₂]³⁺ and [Cr(bpmp)2]3+ respectively. Slightly more distorted geometries are observed for compounds 1–3, which may be attributed to steric hindrance caused by the methyl groups and fused heterocycles. In any case, this represents a small geometric distortion with respect to the ideal CrN6 octahedron and ensures an efficient orbital overlap between the metal and the ligands, thus inducing strong ligand field splitting destabilizing the 4T2 state and preventing, in principle, back-intersystem crossing with the SF excited states. Additionally, the coordination geometry adopted by the CrIII ion in the three compounds has been evaluated through the SHAPE software, which is based on the continuous shape measurements method (CShMs).50 The coordination sphere of compounds 1–3 closely resembles an ideal octahedral geometry (OC-6), typical for CrIII complexes with six ligands symmetrically arranged around the metal centre. However, compound 3 exhibits slight deviations (Table S5), likely due to a more compressed octahedral structure resulting from the shortening of certain Cr–N bonds. In the solid state, CH···O hydrogen bonds are observed between the methylene bridges and the triflate anions (d(C··· O) = 2.9−3.2 Å), which highlights the acidity of the CH2 bridge units in the cationic complexes (Fig. S5-S7).44

Electronic absorption properties

The UV-Vis absorption spectra in acetonitrile (10-5 M) at room temperature shows maxima between 250 and 300 nm (ε > 8000 M−1·cm−1), which can be attributed to ligand-centered π* ← π

transitions, along with lower intensity bands between 300 and 550 nm (ε < 7000 M−1·cm−1) assigned to mixed metal-centered and ligand to metal charge transfer (MC/LMCT) transitions with a considerable red-shift for the iodine analog 2 and for compound 3 (Fig 2b). The band located at the lowest energy (450-480 nm) can be attributed to the 4T2←4A2 transition according to TD-DFT calculations (Fig. 2b, Fig. S23-S31). From this electronic transition, the value of the ligand field splitting is estimated at approximately 21500 cm-1 for the three compounds. This significant ligand-field splitting could potentially limit the thermally assisted back-intersystem crossing between the emissive excited states 2E/2T1 and 4T2.25

Figure 2. a) Crystal structures of complexes 1, 2 and 3 including their Cr-N bond distances. Triflate anions, solvent molecules and hydrogen atoms were omitted for clarity. Colour codes: Cr (orange), N (blue), C (grey), I (purple). b) Absorption and emission spectra at room temperature (solid line) and 77 K (dashed line) of complexes 1 (red), 2 (green) and 3 (blue) in acetonitrile. c) Excited state decays recorded em 741 nm (1), 748 nm (2) and 830 nm (3) at room temperature and under argon atmosphere upon irradiation with a flashlamp at 480 nm. d) comparison of the emission spectra at 298 K (solid line) and 77 K (dashed line) in compound 1-3.

At much lower energies (12300 – 14500 cm-1), in solution and in solid state, the absorption spectra displayed two main bands with maxima at  740 nm, with a molar extinction coefficient () of 0.58 M−1·cm−1 and 1.27 M−1·cm−1 for 1 and 2 respectively. For compound 3 the band maximum is red-shifted up to 773 with  = 0.6 M−1·cm−1 (Fig. 3 and Fig. S8). Weaker absorption bands at 690 nm with  = 0.1 – 0.2 M−1·cm−1 for 1 and 2, and 717 nm for 3 with  = 0.21 M−1·cm−1 have also been detected. These bands correspond to the spin-forbidden direct transitions from the quartet ground state (4A2) to the manifold low-lying doublet metal-centered excited states (2E and 2T1).

Figure 3. Spin-flip Absorption spectra of 1, 2 and 3 complexes in acetonitrile (c = 7.7 mM). Assignation band according to (CASSCF(7,12)/FIC-NEVPT2) calculations (see text and Fig. S22). The oscillator strength (f) has been calculated according to equation 2.

Concerning these spin-forbidden transitions, it is worth noticing that the decadic absorption coefficients  for the lowest energy band for the three compounds are on average one order of magnitude greater (and at least 3 fold greater) than those previously reported for related complexes (0.02 - 0.3 M-1·cm-1).17,22,51,52 The even larger value found for complex 2 (1.27 M−1·cm−1) is attributed to the heavy-atom effect caused by the iodine atoms in the ligand scaffold, boosting the spin-orbit coupling and so partially relaxing the spin selection rule. The associated oscillator strength (fexp) for the lowest energy transition has been calculated using the Strickler-Berg relationship (eq. 1), where m is the electron mass, c is the velocity of the light in vacuum, Na is Avogadro’s number, e is the electron charge, X = (n2+2)2/9n is the local field correction where n is the refractive index of the medium, v is the wavenumber of the relevant electronic transition and ε is the molar absorption coefficient.

fexp=2303 mc2Naπe2 1Xεvdv=3.63x 10-9εvdv eq. 2

The obtained value of 9.8·10-7, 2.5·10-6  and 9.0·10-7 for 1, 2 and 3 respectively, are larger compared to previous related Cr(III) compounds.17,53 The compound 2 containing four iodine atoms reflects an increased value by a factor 2.5 in agreement with the abovementioned difference in molar extinction coefficient at the absorption maxima. The fexp in 2 lies in the order of magnitude found in lanthanides ions such as Yb(III), which is well-known to act as a sensitizer in energy transfer upconversion processes (ETU).54 Although weak, the enhancement of the spin-flip transition cross-section (associated to fexp) would be keystone to harness inert Cr(III) as efficient NIR sensitizer for boosting ETU efficiency in (supra)molecular Cr(III)-Er(III) assemblies,27,32,55 and potentially also for enhancing the efficiency of red light-driven photoredox catalysis with Cr(III) complexes.56,57

Theoretical calculations

The geometries of [Cr(Mebipzp)2]3+, [Cr(IMebipzp)2]3+ and [Cr(bip*)2]3+ in their 4A2 ground states were optimized using unrestricted density functional theory (DFT) calculations at the UB3LYP/def2TZVPP level (SI for technical details and Fig. S21). The obtained geometries matched those obtained from the single-crystal diffraction, with minimal variations in their bite angles (Table S6). The excited state landscape was evaluated using the complete active space self-consistent field method (CASSCF(7,12)/FIC-NEVPT2) for the three complexes. The calculations revealed a similar distribution of the excited states in the three compounds, where the microstates 2T1(1) and 2T1(2) are the lowest energy excited states (Fig. S22). Similar results have been found in [Cr(bpmp)2]3+, [Cr(ddpd)2]3+, [Cr(btmp)2]3+ and [Cr(dqp)2]3+.17,44,45 Despite the admixture and small energy difference between the six microstates belonging to the 2T1 and 2E states, two distinguishable bands were experimentally observed in the absorption spectrum and were tentatively assigned to two different sets of doublet states (Fig. 3). Thus, according to the quantum chemical calculations and the experimental results, the band located at lower energy can be assigned to the [2E(1),2T1(2),2T1(1) ← 4A2] transitions and the higher one to [2E(2),2T1(3) ← 4A2] which result in the Jablonski diagram depicted in Fig. S22. Fifty spin-allowed vertical electronic transitions were computed using time dependent DFT (TD-DFT, Table S7-S9) at the UCAM-B3LYP/def2TZVP level of theory. The decomposition of these transitions suggested that the six lowest energetic electronic transitions have a mainly metal centered (MC) character (Fig. S23, S26 and S29), as expected. Those transitions can be divided into two groups, three transitions falling under the observed band between 450 and 550 nm and three transitions between 370 and 450 nm (Fig. 2b). Electron density difference maps (EDDM) assigned the orbitals involved in each transition, confirming their 4T2 ← 4A2 character (Fig S24, S27 and S30). In all cases, the calculated oscillator strengths are lower than 0.0006, expected for parity-forbidden metal centered electric dipole transitions in chromium(III) complexes. According to the TD-DFT results, the observed band between 300 and 400 nm is composed of transitions with a strong intra-ligand charge transfer (ILCT) character, while the higher energetic transitions show a ligand-metal charge transfer (LMCT) character.

Emission properties

At ambient temperature and after light excitation at 480 nm (4T2←4A2 transition), the three complexes exhibit a broad SF emission band with FWHM ranging from 590 cm-1 (for 1 and 2) to 1070 cm-1 (for 3), and maxima located at 741 nm (13495 cm-1), 748 nm (13368 cm−1) and 830 nm (12000 cm-1) for 1, 2 and 3 respectively (Fig. 2b). The excitation spectra recorded upon monitoring the emission band coincide with the absorption spectra, demonstrating the participation of the 4T2 and 4LMCT excited states in the population of the emissive excited states of 1, 2 and 3 (Fig. S11). Interestingly, the FWHM value is four times larger compared to the archetypal [Cr(ddpd)2]3+, [Cr(dqp)2]3+ complexes (Fig. S9a), and comparable to the analog [Cr(btmp)2]3+,45 which can be a benefit for Förster type energy transfer to low-energy acceptors in supramolecular assemblies. At 77 K, the emission bands are more structured, as expected, but remains broad (dashed line in Fig. 2b and Fig. 2d), which is in stark contrast with the sharper bands found at low temperature in the related [Cr(ddpd)2]3+, [Cr(dqp)2]3+ and [Cr(bpmp)2]3+ complexes (Fig. S9b).44 The broad emission bands observed at both room temperature and low temperature are consistent with important vibronic structure as a consequence of misalignments of the ground and excited potential wells (Fig. 4). The origin of this misalignment is in part due to the inhomogeneity of Cr-N bonds due to the presence of two different binding sites (pyrazole/indazole and pyridine), as similarly observed in fac-Cr(ppy)3 (ppy =2-phenylpyridine) and [Cr(btmp)2]3+.45,58 Indeed, the compression of the octahedral geometry, resulting from the shorter Cr–N(pyrazole) and Cr-N(indazole) bond distances in the equatorial plane of the complexes, leads to a noticeable Jahn-Teller distortion. This compressed distortion causes a splitting of the t2 orbitals, which in turn contributes to the broadening of the emission. The associated increase of covalence of the t2 orbitals as stated before (in O point group) can also be incriminated in the unusual Stokes shift of the spin flip transition reaching 340 cm-1 and 410 cm-1 respectively for 1 and 2 and a even larger value of 820 cm-1 for compound 3 (Fig. 4 and Fig. S10). The latter Stokes shift reflected by the low temperature shifting of the emission band maxima, as also observed in [Cr(btmp)2]3+,45 is particularly uncommon for CrIII spin flip transitions and mirrors misalignment between the potential wells of the excited 2MC and ground 4A2 states (Fig. 2d and Fig. 4). In addition, compared to the analogue [Cr(bpmp)2]3+, which features six pyridine ligands in the first coordination sphere around the CrIII with a SF emission at 709 nm, the incorporation of pyrazole and indazole results in a shift of the emission bands to  740 nm (for 1 and 2) and 830 nm (for 3). This bathochromic shift aligns with an increase in covalency., It might be due to enhanced electronic delocalization of the metal-centered t2 electrons in the five membered aromatic heterocycle pyrazole and indazole in comparison to the six membered pyridine, altogether, stabilizing the SF states.

The overall luminescence quantum yield () at room temperature in non-acidified acetonitrile after excitation at 480 nm reaches (i) 9.2% (under Ar) and 0.7% (under air) for 1, (ii) 9.0% (under Ar) and 1.2% (under air) for 2 and 1.5% (under Ar) and 0.7% (under air) for 3. The obtained values for 1 and 2 represent substantial improvements compared to [Cr(bpmp)2]3+ ( = 0.8%) which experiences quenching due to ground state deprotonation of the -CH2- moieties in pure acetonitrile.44 In acidic medium, complexes show a slight increase in luminescence quantum yields, in contrast to [Cr(bpmp)2]3+, where a luminescence quantum yield of 11.4% is measured (Table 1). This highlights the weaker acidic nature of the CH2 bridges upon replacing the lateral pyridine substituents in bpmp with pyrazole or indazole rings. For 1 and 2, the luminescence quantum yield is one order of magnitude higher compared to the structurally most closely related [Cr(btmp)2]3+ complex in both non-acidic and acidic media (Table 1). The freely rotating peripheral phenyl ring in the latter compound can likely activate additional nonradiative decay channels and could be responsible for its luminescence quenching.59

Figure 4. Schematic representation of the SF absorption and emission at 77K (right-hand side) and potential energy curves for the quartet ground and excited state, 4A and 4T2, and the doublet excited state 2E and 2T1.

The excited state lifetimes under argon in neat acetonitrile at room temperature are 1231 μs for 1, 313 μs for 2 and 111 μs for 3 (Fig. 2d, Fig. S12, S15 and S18), becoming slightly longer in acidic medium (Table 1). Under an ambient (aerated) atmosphere, the excited state lifetimes for the three complexes are considerably shortened (Fig. S13, S16 and S19), due to the quenching by atmospheric 3O2, which generates the reactive 1O2 species. kq values for energy transfer from doublet excited states to 3O2 of 3.8⋅107 M-1·s-1, 5.6⋅107 M-1·s-1 and 6.4⋅107 M-1·s-1 have been estimated for 1, 2 and 3 respectively (see SI for details). These values are in line with those reported for related complexes.3,38,44,45 The efficient 1O2 generation has been demonstrated to be very useful in catalysis and for photodynamic therapy.25,38,39,60 In a rigid medium at 77 K (frozen acetonitrile solution), the excited-state lifetimes of 1500 μs for compound 1 and 145 μs for compound 3 are approximately 20% longer than the lifetimes observed at room temperature under deaerated conditions (Table 1, Fig. S14 and S20). For compound 2, the excited state lifetime of 1064 μs at 77K represents a threefold increase relative to 293 K (Fig. S17), suggesting a significant and distinct thermally activated non- radiative relaxation mechanism compared to the structurally similar compound 1. This may be attributed to notable room temperature back-intersystem crossing, 2MC→4T2, facilitated by the presence of heavy iodine atoms. This has been already observed in organic dyes and recently reported in chromium (III) complexes.61,62The similar luminescence quantum yields of the compounds 1 and 2 ( 9.0% in non-acidic media) contrast with the shorter excited-state lifetime measured, in going from 1 to 2, highlighting a concomitant increase of the deactivation rate constants for the spin-flip emission in complex 2 (Fig. 2d). The radiative rate for the low energy 2MC excited state, kCr,rad, has been estimated assuming that the intersystem crossing between the 4MC and 2MC states is close to unity (i.e. =1 in Eq.1).44,45,63 The computed values of 74 s−1 and 135 s-1 for 1 and 3 are larger than those found in [Cr(tpe)2]3+ (kCr,rad = 23-18 s-1), [Cr(CN)6]3- (kCr,rad = 25 s-1) and [Cr(phen)3]3+ (kCr,rad = 32-43 s-1), and similar to the related complexes such as [Cr(dqp)2]3+ (kCr,rad = 29-98 s-1) and [Cr(ddpd)2]3+ (kCr,rad = 135 s-1). For 2, a value of 271 s−1 has been calculated, which is significantly larger compared to the  [Cr(dqp)2]3+ and [Cr(ddpd)2]3+ and the closet structurally related [Cr(bpmp)2]3+ (131 s-1) and [Cr(btmp)2]3+ (88 s-1) complexes as well as in compounds 1 and 2. This observable increase of the radiative excited-state decay rate constant is consistent with the increased oscillator strength of the spin-flip transition in 2 in solution and solid state (Fig. 3 and Fig. S8). The non-radiative de-excitation pathways of 2MC are independently evaluated by the non-radiative rate constants (knonrad) amounting in deaerated solutions to 738(50) s−1 and 2900(250) s−1 for 1 and 2 respectively.

Thus, the positive effect of heavy atoms on the radiative excited-state decay rate constant is balanced by a concomitant increase of the non-radiative de-excitation pathways, such as the thermally assisted back intersystem crossing. Moreover, the enhanced spin-orbit coupling will also favour vibrationally-induced nonradiative decay between strongly coupled potential energy surfaces, in other words, between the excited state and ground state.64

Table 1. Photophysical parameters of the 1, 2 and 3.

| Complex | abs/E(2MC) (nm/cm-1) | em/E(2MC) (nm/cm-1) | (%) | obs (μs)[b] | obs (μs) 77K | krade/knrad (s-1) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 - [Cr(Mebipzp)2]3+ 1 - acidic conditions | 738/13550 | 741/13500 | 9.2a 11.0a | 1231b,c/1264d 1500 | 1500 | 74/738 |
| 2 - [Cr(IMebipzp)2]3+ 2 - acidic conditions | 742/13477 | 746/13404 | 9.0a 9.5a | 313b,c/380d 350 | 1063 | 287/2900 |
| 3 - [Cr(bip*)2]3+ 3 - acidic conditions | 773/12940 | 830/12048 | 1.5a 1.5a | 111b,c/110d 110 | 145 | 135/8873 |
| [Cr(bpmp)2]3+ (3)36 3 - acidic conditions | 706/14164 | 709/14100 | 0.8 11.4 | 840 1290 | - | 88/686 |
| [Cr(btmp)2]3+ (4)37 4 - acidic conditions | - | 760/13157 | 0.27 0.54 | 37.9 41.5 | 782 | 131/24000 |

[a] Emission quantum yield measured by using an integration sphere upon excitation at 480 nm in deaerated acetonitrile at room temperature. [b] Emission lifetime measured in deaerated acetonitrile solution at r.t and upon excitation at 480 nm. [c] Excited state lifetime obtained by time-correlated single photon counting (TCSPC) technique. [d] Excited state lifetime obtained through the transient absorption experiments [e] krad=Φ/obs assuming the ISC = 1.

Nanosecond UV-vis transient absorption (TA) spectroscopy was further used to probe the photophysical properties of the doublet spin-flip excited states. Spectra for 1 and 2 were recorded in acetonitrile at room temperature following excitation at 355 nm (30 mJ pulses, ca. 10 ns duration) and for 3 at 450 nm (13 mJ per pulse). The TA spectrum of complex 1 features broad excited state absorption (ESA) bands with maxima at 410 nm and 515 nm and a ground state bleach (GSB) of the charge transfer band at 300 nm. Similarly, for complex 2, excited state absorption bands at 450 nm and 650 nm, as well as a ground state bleach at 350 nm, are observed. In compound 3, the ESA bands at 510 and 660 nm, and the ground state bleach at 380 nm. In all cases, the ESA bands are tentatively attributed to electronic transitions from the 2E/2T1 states to higher-lying doublet excited states, most likely of charge transfer character. ESA lifetimes are consistent with the observed luminescence lifetimes (Table 1, Figure 4). Complex 2, with iodine-substituents, exhibits a three-fold decrease in the lifetime relative to 1, consistent with the luminescence lifetime experiments performed under identical conditions. Collectively, the photoluminescence decay and transient UV-Vis absorption data support the hypothesis of a heavy atom effect, which accelerates radiative 2MC excited state decay.

Figure 4. a) and b) Transient absorption spectra of compounds 1, 2 and 3 upon excitation at 355 nm (30 mJ pulses, ca. 10 ns duration) for 1 and 2, and at 450 nm (13 mJ per pulse) for 3 with nanosecond pulses in deaerated acetonitrile solution at room temperature, time-integrated over 1 μs.  c) 410 nm, d) 450 nm and e) 520 nm decays of the normalized ESA bands for the three compounds.

Conclusions

In conclusion, the straightforward synthesis of the [Cr(Mebipzp)₂]³⁺ (1), [Cr(IMebipzp)₂]³⁺ (2), and [Cr(bip*)₂]³⁺ (3) complexes provides a simple route to substitute widely used saturated pyridine ligands with more versatile pyrazole and indazole heterocycles. The distinct bonding interactions introduced by the pyrazole/indazole and pyridine moieties induce significant energetic splitting of the lowest-lying doublet excited states, leading to a more pronounced distortion of the 2MC states relative to the electronic ground state. This results in broader emission profiles and unusually large Stokes shifts for the spin-flip transitions. Despite the broader emission spectrum, the luminescence quantum yields of compounds 1 and 2 (9-11% in deaerated solution), are among the largest reported for Cr(III) molecular rubies. Notably, the incorporation of iodine substituents in complex 2 improves the spin-orbit coupling via the heavy atom effect. This significantly increases (i) the oscillator strength (f), (ii) both the radiative and non-radiative rate constants for the 2MC ↔4A2 transition and (iii) facilitates the room temperature back-intersystem crossing. Finally, the substitution of distal methyl-pyrazole rings with indazole in compound 3 induces a significant bathochromic shift in the spin-flip emission to 830 nm (12000 cm⁻¹), highlighting the impact of the extended π-system and increased covalent bond character of the indazole ligand. These findings reveal an underexplored approach for tuning deactivation pathways and emission energies while maintaining high quantum yields and long-lived excited states, offering exciting opportunities for the development of advanced molecular rubies with tailored photophysical properties.

Author Contributions

Acknowledgements

The authors acknowledge the funding received from the grant TED2021.129598A.I00 funded by MCIN/ AEI/10.13039/501100011033 and by European Union NextGenerationEU/PRTR and Junta de Andalucía. This work was financially supported by Ministerio de Ciencia e Innovación (PGC2018 102052-B-C21) MCIN/AEI/10.13039/501100011033/ FEDER ‘‘Una manera de hacer Europa’’, Junta de Andalucía (FQM-195, projects I + D + i A-FQM-172-UGR18 and B.FQM.328.UGR20) and the University of Granada. J. R. J. acknowledge the Juan de la Cierva Incorporation grant IJC2020-044040-I funded by MCIN/AEI/10.13039/501100011033 and by European Union NextGenerationEU/PRTR. P.S.-A. thanks Juan de la Cierva Grant JDC2022-048964-I funded by MICIU/AEI/10.13039/501100011033 and by “European Union NextGenerationEU/PRTR”. We thank Centro de Servicios de Informática y Redes de Comunicaciones (CSIRC), Universidad de Granada, for providing the computing time. This work made use of the infrastructure services provided by S3IT (www.s3it.uzh.ch), the Service and Support for Science IT team at the University of Zurich. The authors would like to thank the S3IT team for their support. M.P., B.D., J.R.J and C.P. were supported through grants from the Swiss National Science Foundation (grant 200020_207313).

References

1	C. Förster and K. Heinze, Chem. Soc. Rev., 2020, 49, 1057–1070.

2	O. S. Wenger, J. Am. Chem. Soc., 2018, 140, 13522–13533.

3	S. Otto, M. Grabolle, C. Förster, C. Kreitner, U. Resch-Genger and K. Heinze, Angew. Chem. Int. Ed., 2015, 54, 11572–11576.

4	J. Steube, A. Kruse, O. S. Bokareva, T. Reuter, S. Demeshko, R. Schoch, M. A. Argüello Cordero, A. Krishna, S. Hohloch, F. Meyer, K. Heinze, O. Kühn, S. Lochbrunner and M. Bauer, Nat. Chem., , DOI:10.1038/s41557-023-01137-w.

5	K. S. Kjær, N. Kaul, O. Prakash, P. Chábera, N. W. Rosemann, A. Honarfar, O. Gordivska, L. A. Fredin, K. E. Bergquist, L. Häggström, T. Ericsson, L. Lindh, A. Yartsev, S. Styring, P. Huang, J. Uhlig, J. Bendix, D. Strand, V. Sundström, P. Persson, R. Lomoth and K. Wärnmark, Science (80-. )., 2019, 363, 249–253.

6	P. Chábera, Y. Liu, O. Prakash, E. Thyrhaug, A. El Nahhas, A. Honarfar, S. Essén, L. A. Fredin, T. C. B. Harlang, K. S. Kjær, K. Handrup, F. Ericson, H. Tatsuno, K. Morgan, J. Schnadt, L. Häggström, T. Ericsson, A. Sobkowiak, S. Lidin, P. Huang, S. Styring, J. Uhlig, J. Bendix, R. Lomoth, V. Sundström, P. Persson and K. Wärnmark, Nature, 2017, 543, 695–699.

7	Y. Ye, P. Garrido-Barros, J. Wellauer, C. M. Cruz, R. Lescouëzec, O. S. Wenger, J. M. Herrera and J.-R. Jiménez, J. Am. Chem. Soc., 2024, 146, 954–960.

8	N. Sinha, C. Wegeberg, D. Häussinger, A. Prescimone and O. S. Wenger, Nat. Chem., 2023, 15, 1730–1736.

9	N. Sinha and O. S. Wenger, J. Am. Chem. Soc., 2023, 145, 4903–4920.

10	C. Wegeberg and O. S. Wenger, JACS Au, 2021, 1, 1860–1876.

11	S. Kaufhold, N. W. Rosemann, P. Chábera, L. Lindh, I. Bolaño Losada, J. Uhlig, T. Pascher, D. Strand, K. Wärnmark, A. Yartsev and P. Persson, J. Am. Chem. Soc., 2021, 143, 1307–1312.

12	A. K. Pal, C. Li, G. S. Hanan and E. Zysman‐Colman, Angew. Chemie, 2018, 130, 8159–8163.

13	M. Dorn, J. Kalmbach, P. Boden, A. Päpcke, S. Gómez, C. Förster, F. Kuczelinis, L. M. Carrella, L. A. Büldt, N. H. Bings, E. Rentschler, S. Lochbrunner, L. González, M. Gerhards, M. Seitz and K. Heinze, J. Am. Chem. Soc., 2020, 142, 7947–7955.

14	P. Herr, C. Kerzig, C. B. Larsen, D. Häussinger and O. S. Wenger, Nat. Chem., 2021, 13, 956–962.

15	L. A. Büldt, X. Guo, R. Vogel, A. Prescimone and O. S. Wenger, J. Am. Chem. Soc., 2017, 139, 985–992.

16	B. C. Paulus, K. C. Nielsen, C. R. Tichnell, M. C. Carey and J. K. McCusker, J. Am. Chem. Soc., 2021, 143, 8086–8098.

17	J. R. Jiménez, B. Doistau, C. M. Cruz, C. Besnard, J. M. Cuerva, A. G. Campaña and C. Piguet, J. Am. Chem. Soc., 2019, 141, 13244–13252.

18	J. R. Jiménez, B. Doistau, M. Poncet and C. Piguet, Coord. Chem. Rev., 2021, 434.

19	E. C. Constable, C. E. Housecroft, M. Neuburger, J. Schönle and J. A. Zampese, Dalt. Trans., 2014, 43, 7227–7235.

20	T. H. Maiman, Nature, 1960, 187, 493–494.

21	W. R. Kitzmann, J. Moll and K. Heinze, Photochem. Photobiol. Sci., 2022, 21, 1309–1331.

22	B. Doistau, J. R. Jiménez, S. Guerra, C. Besnard and C. Piguet, Inorg. Chem., 2020, 59, 1424–1435.

23	J. Chong, C. Besnard, C. M. Cruz, C. Piguet and J. R. Jiménez, Dalt. Trans., 2022, 51, 4297–4309.

24	J.-R. Jiménez, M. Poncet, S. Miguez-Lago, S. Grass, J. Lacour, C. Besnard, J. M. Cuerva, A. G. Campaña and C. Piguet, Angew. Chem. Int. Ed., 2021, 60, 10095–10102.

25	S. Otto, M. Dorn, C. Förster, M. Bauer, M. Seitz and K. Heinze, Coord. Chem. Rev., 2018, 359, 102–111.

26	C. Wang, S. Otto, M. Dorn, E. Kreidt, J. Lebon, L. Sršan, P. Di Martino-Fumo, M. Gerhards, U. Resch-Genger, M. Seitz and K. Heinze, Angew. Chem. Int. Ed., 2018, 57, 1112–1116.

27	L. Aboshyan-Sorgho, C. Besnard, P. Pattison, K. R. Kittilstved, A. Aebischer, J. C. G. Bünzli, A. Hauser and C. Piguet, Angew. Chem. Int. Ed., 2011, 50, 4108–4112.

28	Y. Suffren, D. Zare, S. V. Eliseeva, L. Guénée, H. Nozary, T. Lathion, L. Aboshyan-Sorgho, S. Petoud, A. Hauser and C. Piguet, J. Phys. Chem. C, 2013, 117, 26957–26963.

29	B. Golesorkhi, H. Bolvin and C. Piguet, Dalt. Trans., 2021, 50, 7955–7968.

30	C. Dee, F. Zinna, W. R. Kitzmann, G. Pescitelli, K. Heinze, L. Di Bari and M. Seitz, Chem. Commun., 2019, 55, 13078–13081.

31	J. Kalmbach, C. Wang, Y. You, C. Förster, H. Schubert, K. Heinze, U. Resch-Genger and M. Seitz, Angew. Chem. Int. Ed., 2020, 59, 18804–18808.

32	M. Poncet, C. Besnard, J. R. Jiménez and C. Piguet, Inorg. Chem., , DOI:10.1021/acs.inorgchem.4c02397.

33	S. Otto, N. Scholz, T. Behnke, U. Resch-Genger and K. Heinze, Chem. - A Eur. J., 2017, 23, 12131–12135.

34	B. Doistau, J. R. Jiménez and C. Piguet, Front. Chem., 2020, 8, 1–27.

35	J. R. Jiménez, S. Míguez-Lago, M. Poncet, Y. Ye, C. Lopez, C. M. Cruz, A. G. Campaña, E. Colacio, C. Piguet and J. M. Herrera, J. Mater. Chem. C, 2023, 2582–2590.

36	Y. Cheng, J. He, W. Zou, X. Chang, Q. Yang and W. Lu, Chem. Commun., 2023, 59, 1781–1784.

37	A. Gabbani, M. Poncet, G. Pescitelli, L. Carbonaro, J. Krzystek, E. Colacio, C. Piguet, F. Pineider, L. Di Bari, J.-R. Jiménez and F. Zinna, Chem. Sci., , DOI:10.1039/d4sc04718d.

38	T. H. Bürgin, F. Glaser and O. S. Wenger, J. Am. Chem. Soc., 2022, 144, 14181–14194.

39	S. Sittel, R. Naumann and K. Heinze, Front. Chem., 2022, 10, 340.

40	N. Sinha, J. R. Jiménez, B. Pfund, A. Prescimone, C. Piguet and O. S. Wenger, Angew. Chem. Int. Ed., 2021, 60, 23722–23728.

41	N. Sawicka, C. J. Craze, P. N. Horton, S. J. Coles, E. Richards and S. J. A. Pope, Chem. Commun., 2022, 58, 5733.

42	Y. Cheng, Q. Yang, J. He, W. Zou, K. Liao, X. Chang, C. Zou and W. Lu, Dalt. Trans., , DOI:10.1039/d2dt02872g.

43	N. Sinha, P. Yaltseva and O. S. Wenger, Angew. Chem. Int. Ed. 2023, 62, e202303864

44	F. Reichenauer, C. Wang, F. Christoph, P. Boden, N. Ugur, B. Ricardo, J. Kalmbach, L. M. Carrella, E. Rentschler, C. Ramanan, G. Niedner-schatteburg, M. Gerhards, M. Seitz, U. Resch-genger and K. Heinze, J. Am. Chem. Soc, , DOI:10.1021/jacs.1c05971.

45	R. W. Jones, A. J. Auty, G. Wu, P. Persson, M. V Appleby, D. Chekulaev, C. R. Rice, J. A. Weinstein, P. I. P. Elliott and P. A. Scattergood, J. Am. Chem. Soc., 2023, 145, 12081–12092.

46	E. A. Juban and J. K. McCusker, J. Am. Chem. Soc., 2005, 127, 6857–6865.

47	J. N. Schrauben, K. L. Dillman, W. F. Beck and J. K. Mc Cusker, Chem. Sci., 2010, 1, 405–410.

48	M. Cantuel, G. Bernardinelli, D. Imbert, J. C. G. Bünzli, G. Hopfgartnerd and C. Piguet, J. Chem. Soc. Dalt. Trans., 2002, 1929–1940.

49	M. Poncet, A. Benchohra, J. R. Jiménez and C. Piguet, ChemPhotoChem, 2021, 5, 880–892.

50	M. Llunell, D. Casanova, J. Cirera, P. A. And and S. Alvarez, 2013.

51	B. Golesorkhi, I. Taarit, H. Bolvin, H. Nozary, J. R. Jiménez, C. Besnard, L. Guénée, A. Fürstenberg and C. Piguet, Dalt. Trans., 2021, 50, 7955–7968.

52	S. Treiling, C. Wang, C. Förster, F. Reichenauer, J. Kalmbach, P. Boden, J. P. Harris, L. M. Carrella, E. Rentschler, U. Resch-Genger, C. Reber, M. Seitz, M. Gerhards and K. Heinze, Angew. Chem. Int. Ed., 2019, 58, 18075–18085.

53	K. DeArmond and L. S. Forster, Spectrochim. Acta, 1963, 19, 1687–1693.

54	W. T. Carnall, P. R. Fields and B. G. Wybourne, J. Chem. Phys., 1965, 42, 3797–3806.

55	I. Taarit, F. Alves, A. Benchohra, L. Guénée, B. Golesorkhi, A. Rosspeintner, A. Fürstenberg and C. Piguet, J. Am. Chem. Soc., 2023, 145, 8621–8633.

56	B. D. Ravetz, A. B. Pun, E. M. Churchill, D. N. Congreve, T. Rovis and L. M. Campos, Nature, 2019, 565, 343–346.

57	F. Glaser and O. S. Wenger, JACS Au, 2022, 2, 1488–1503.

58	L. Stein, P. Boden, R. Naumann, C. Förster, G. Niedner-Schatteburg and K. Heinze, Chem. Commun., 2022, 58, 3701–3704.

59	Z. Lou, Y. Hou, K. Chen, J. Zhao, S. Ji, F. Zhong, Y. Dede and B. Dick, J. Phys. Chem. C, 2018, 122, 185–193.

60	L. Gourdon, K. Cariou and G. Gasser, Chem. Soc. Rev., 2022, 51, 1167–1195.

61	B. Pfund, V. Hutskalova, C. Sparr and O. S. Wenger, Chem. Sci., 2023, 14, 11180–11191.

62	F. Reichenauer, R. Naumann, C. Förster, W. R. Kitzmann, A.-P. M. Reponen,  b S. Feldmannb and K. Heinze, Chem. Sci., , DOI:10.1038/scientificamerican10271883-6511csupp.

63	J. P. Zobel, H. Radatz and L. González, Molecules, , DOI:10.3390/molecules28041668.

64	C.-H. Ting, Photochem. Photobiol., 1969, 9, 17–31.

We strongly encourage authors to include author contributions and recommend using CRediT for standardised contribution descriptions. Please refer to our general author guidelines for more information about authorship.

Conflicts of interest

In accordance with our policy on Conflicts of interest please ensure that a conflicts of interest statement is included in your manuscript here.  Please note that this statement is required for all submitted manuscripts.  If no conflicts exist, please state that “There are no conflicts to declare”.7