Geometry‑Harmonized Fly‑Ash based Alkali‑Activated Concrete Dataset for Data‑Driven Modelling

Amine el Mahdi SAFHI1*, Shima PILEHVAR1,2, Mahdi KIOUMARSI1,2

1Østfold University College, Faculty of Engineering, Halden, Norway

2OsloMet – Oslo Metropolitan University, Department of Built Environment, Oslo, Norway

Version v1.0 · CC-BY 4.0 Licence

Overview

This repository contains a harmonized compilation of 799 fly-ash alkali-activated concrete (FA-AAC) mix designs extracted from 67 peer-reviewed publications & the open-access parent dataset created by Torres et al. (1 630 mixes, ref. [70-71] in the bibliography.

- Single precursor & activator: Only fly ash as binder precursor & NaOH(aq) as activator.

- Geometry‑normalized strengths: All compressive strengths have been converted to the equivalent 150 × 300 mm cylinder value using ACI 318‑19 & CEB‑FIP factors; raw values are preserved for traceability.

- Rich feature set: Binder oxide chemistry, activator properties, mix proportions, fresh & hardened properties, curing regime, & CO2 footprint. A statistical overview is also provided.

- Bibliographic traceability: Complete bibliography of the 67 papers included.

- Deliverables: Tidy CSV & README—ready for ML modelling, meta-analysis, & low-carbon mix benchmarking.

Keywords: Fly-Ash, Alkali-Activated Concrete, Machine Learning Dataset, Geopolymer.

Value of the Data

- Provides the first openly shared, geometry-harmonized collection of FA-AAC mixes, eliminating specimen-geometry bias via size normalization.

- Serves researchers developing machine-learning or optimization models by pairing full mix parameters with cylinder-equivalent compressive strengths. Supply a ready-to-model table of mix designs & properties.

- Offers industry professionals an objective benchmark for screening low-carbon, FA-only AAC formulations.

- Fulfils FAIR principles by supplying tidy CSV file & a complete bibliography—facilitating reproducibility, reuse, & future extensions.

Data description (Features)

- Statistical overview (7 features): Number of data, minimum & maximum value, 10th & 90th percentile, average value, & standard deviation.

- Identification features (3 features): number of the mixture, references, & the mixture code.

- Fly ash properties (18 features): the dosage, specific density, & the chemical composition including the sum of the pozzolanic oxides (silica, alumina, & ferrite), the Si/Al ratio.

- Aggregate properties (7 features): Content & density of fine & coarse aggregates, the total aggregate, the fine-to-total-aggregate ratio, & the binder-to-total-aggregate ratio.

- Alkali-activator content & concentration (18 features): Properties of Na2SiO3 & NaOH including content, composition, concentration & specific density. Besides, some significant ratio such as Na₂O/SiO₂ ratio, liquid/solid ratio, activator-to-binder ratio, etc.

- Workability features (8 features): including those related to mix design such as water, superplasticizer, & the water-to-binder ratio; & slump flow, flow-table, & setting time.

- Curing features (4 features): including initial & final curing time, initial & final curing temperature.

- Hardened properties (39 features): this includes the sample dimensions, the original mechanical strengths for different cube & cylinder size, then the converted strengths to the equivalent 150 × 300 mm cylinder, the young modulus, & porosity.

- CO2 footprint feature: in kg emission per 1m3 of samples produced & cured based on [68-69].

Limitations

- Literature coverage stops at December 2023; newer FA‑AAC studies are not yet included.

- Size‑effect factors are derived from OPC concrete; validation for very high‑Ca or ultra‑high‑strength mixes is advised.

- Non‑strength properties (workability, durability) appear only when reported by the original authors, resulting in sparse coverage.

Ethics & competing interests

The authors declare no competing financial interests.