## Slide 1: Explosion during an electrolysis experiment in an open cell mass flow calorimeter
Jean-Paul Biberian
Faculté des Sciences de Luminy, CNRS-CRMCN
Université d’Aix-Marseille II
Tél: + 33 660 14 04 85
Email: biberian@crmcn.univ-mrs.fr

## Slide 2: Experimental set-up
Dewar
Palladium
Platinum
Thermistor in
Thermistor out
100 ml/min distilled water at constant temperature
Pump

## Slide 3: Experimenal conditions
Cathode : Palladium tube length:10 cm, diameter 2mm
Anode :Platinum wire
Electrolyte : LiOD 0.1N
Maximum gas volume 120 ml
DC current
Calorimeter efficiency 95%

## Slide 4: The cell

## Slide 5: The cell after!

## Slide 6: Electrode after explosion

## Slide 7: Pin-Pout

## Slide 8: Last two days

## Slide 9: Conclusion
The explosion occurred during an endothermic phase
Open cell calorimetry
Maximum available gas: 120 ml
Don’t seems to be a deuterium-oxygen explosion
What then?