## Slide 1: EXCESS HEAT IN ELECTROLYSIS EXPERIMENTS AT ENERGETICS TECHNOLOGIES
I. Dardik, T. Zilov, H. Branover, A. El-Boher, E. Greenspan, B. Khachaturov,
V. Krakov, S. Lesin and M. Tsirlin
Energetics Technologies
P.O.Box 3026
Omer Industrial Park
Omer, Israel
E-mail: lesin@energetics.il.co
Presented at the
6th International Workshop on Anomalies in Hydrogen / Deuterium loaded Metals
13-16 May 2005
Sienna - Italy

## Slide 2
Abstract
Energetics Technologies (ET) is investigating intensification of Low Energy Nuclear Reactions (LENR) using excitation by SuperWaves©.
Using the electrolytic cells described in our ICCF-10 and 11 papers driven with Dardik’s modified SuperWaves, significant amounts of excess heat were obtained in a number of experiments.
New experimental approach is being pursued: Ultra Sound (US) cavitation, focused on cathode surface during electrolytic loading.
Excess heat generation has been observed in 2 US experiments out of 5.
Qualitative estimation 70% and 1800%.

## Slide 3
A
A
C
T4
T5
Teflon
Alumina
Aluminum
Recombiner
Electrolyte
Cell description:
Teflon beaker, placed into isoperibolic calorimeter, that dipped into constant temperature +2.50C water bath
ELECTROLYTIC CELL OVERVIEW

## Slide 4
    Measured parameters:
    Resistance of cathode for loading
    monitoring (four probe AC method)
    Input Current
    Input Voltage
    Wall Temperatures T4 and T5
ELECTROLYTIC CELL

## Slide 5: ELECTROLYTIC CELL
Electrolytic Cell and System Assembly

## Slide 6
Target Description:
Pd foil 50 µm, prepared by Dr. Vittorio Violante (ENEA Frascatti, Italy) or home-made
Annealed at 8700C in vacuum during 1h
Etched:
in Nitric Acid 65-67% 1 min
in Aqua Regia 1:1 water solution 1 min
Rinsed:
D2O four times
Ethanol 95% twice
Ethanol Absolute once
Dried:
in vacuum at amb. temperature 24 h
Electrolyte:
0.1M LiOD in D2O Low Tritium Content 230 ml
80 mm
7 mm
ELECTROLYTIC CELL

## Slide 7
Excess Power; Exp. # 56
Excess Power of up to ~3.5 watts; Average ~2.7 watts for ~300 h
300 h
Average Pout ~6.9 watts
Average Pinet ~3.9 watts
COPE=(Pout-Pinet):Pinet ≈ (6.9-3.9):3.9 ≈ 0.8

## Slide 8
Excess Power; Exp. # 64a
Pout=KΔT
Pinet=Iin*Vin – P dis
Excess Power of up to 34 watts; Average ~20 watts for 17 h
17 h
Average Pinet ~0.74 watts
Average Pout ~20 watts
COPE=(Pout-Pinet):Pinet ≈ (20-0.74):0.74 ≈ 25

## Slide 9
Excess Power; Exp. # 64b
Excess Power of up to 32 watts; Average ~12 watts for 80 h
COPE=(Pout-Pinet):Pinet ≈ (12-0.72):0.72 ≈ 15
Average Pout ~12 watts
Average Pinet ~0.72 watts
80 h

## Slide 10
ENERGETICS TECHNOLOGIES LTD.

## Slide 11
ENERGETICS TECHNOLOGIES LTD.

## Slide 12
Plasma Etching of Pd cathode
Pd foil in alumina holder (cathode)
Molybdenum anode
Application of Plasma etching with different gases (deuterium, argon, helium, argon – oxygen, deuterium – argon, deuterium – helium) of Pd foil before electrolytic loading, gave excess heat generation ( 10 – 73%) in 5 experiments out of 19
Quartz chamber

## Slide 13
Plasma Etching of Pd cathode
Pd surface after Ar plasma bombardment
Pd surface after D2 plasma bombardment

## Slide 14
50-55 mm
2.5-3.0 mm
Ultra Sound – Electrolytic Cell
Target Description:
Pd foil 30-35 µm, prepared by rolling of 0.5 mm Pd wire
Annealed at 8700C in vacuum during 1h
Etched:
in Nitric Acid 65-67% 1 min
in Aqua Regia 1:1 water solution 1 min
Rinsed:
D2O four times
Ethanol 95% twice
Ethanol Absolute once
Dried:
in vacuum at amb. temperature 24 h
Electrolyte:
0.3M LiOD in D2O Low Tritium Content 35 ml

## Slide 15
Ultra Sound – Electrolytic Cell
Quartz Beaker
Axial Centered Cathode
Teflon Support
Helical Pt anode

## Slide 16
Schematic View of Ultra Sound Cell
Ultrasound Cylindrical Transmitter
Electrolyte
Cathode (Pd wire)
Anode (Pt Helix)
Cooling Jacket
Cooling Water inlet
Cooling Water outlet
Tcell
Tjacket
Ultra Sound – Electrolytic Cell overview

## Slide 17
SuperWave applied in US –Electrolytic experiment.
Average current density J=11 mA/cm2
Ultra Sound – Electrolytic Cell

## Slide 18
R/R0=1.5277 (D/Pd≈0.95)
Relatively high loading achieved with low (11 mA/cm2) current density
Application of US
Ultra Sound – Electrolytic Cell

## Slide 19
Ultra Sound – Electrolytic Cell
Δ(ΔT)=4.50C
ΔT=T4-T5
Cell Temperature T4
Jacket Temperature T5
Application of US
Ultra Sound cell ETE -6-201 : Δ(ΔT)=4.50C
( 18 times higher, than Δ(ΔT)=0.250C corresponds to Pinet=0.1W )

## Slide 20
Ultra Sound – Electrolytic Cell
Ambient Temperature
Ambient Temperature behavior during Excess Heat generation

## Slide 21
US off
US on
US 20%
US full power
Tcell
Tjacket
ΔT=Tcell-TJacket
Tambient
Estimation of US influence on temperature in the cell & jacket
Ultra Sound – Electrolytic Cell

## Slide 22
Ultra Sound Cell
Increasing of ΔT caused by increasing of electric power input, but not US input
Tcell
ΔT=Tcell-Tjacket
Tjacket
Pinet=0
US off
Pinet=0.27W
US off
Pinet=0.27W
US=20%
Pinet=1.47W
US=20%.
Pinet=2.9W
US=20%
Pinet=2.9W
US off
Pinet=1.47W
US off

## Slide 23
Ultra Sound – Electrolytic Cell
ΔT and Δ(ΔT) as function of Pinet, measured in reference cell with Pt cathode and Pt anode
Δ(ΔT)=4.50C corresponds to 3.75W
(extrapolation)

## Slide 24
Ambient Temperature
Regular temperature behavior Pinet = constant
Cell Temperature
Jacket Temperature
US off
US on
ΔT=T4-T5
US=max
US=max, higher cooling rate
US off
Ambient Temperature
Ultra Sound – Electrolytic Cell

## Slide 25
Pd surface after loading
No.92 Electrolysis + US
No.135 Electrolysis

## Slide 26
Pd surface after loading
No.201 Electrolysis + US
No.64 Electrolysis

## Slide 27
Pd foil No.201 after Electrolytic-US loading
Cavitation tracks (half-octahedral shape) on cathode surface

## Slide 28
Pd foil No.162 after Electrolytic-US loading
Groups of Cavitation tracks on cathode surface

## Slide 29
ACKNOWLEDGMENT
We wish to thank Dr. Vittorio Violante and his group from ENEA FRASCATTI for their cooperation in preparatioin of the Pd cathods.

## Slide 30
CONCLUDING REMARKS
Using SuperWaves ( SW ) in Electrolytic Cells allows to achieve high Excess Heat rates ( up to 2500 % ) at relatively low current densities ( 7- 11 mA/ cm2 ) and at relatively low D/Pd loading rates ( 0.75- 0.85 ) .
When applaying US waves in addition to the SuperWaves the reproducibilty rate improves ( 40 % ) .
When applying GD etching to the Pd cathode before electrolysis reproducibility also improves ( 25 % ), however the Excess Heat rate is not exceeding 72 % as compared to 2500 % achieved with Pd cathodes prepared by Dr. Vittorio Violante .
The promising qualitative experimental results achieved using a combination of SW and US waves requires accurate calorimetry, which is underway .
In order to achieve high reproducibilty rates the following has to be done:
- Further optimizatin of the SW in combination with the US .
- Thorough investigation of the controlling parameters of
the Pd cathodes in order to achieve large amount of
active sites.