## Slide 1
Nuclear transmutations in D-Pd films induced
by low power He-Ne laser beams
U. Mastromatteo
STMicroelectronics, via Tolomeo, 1 200010 Cornaredo Milano-I
V. Nassisi, A. Lorusso, G. Caretto
Applied Electronics Laboratory, Department of Physics, University of Lecce, I.N.F.N., C.P. 193, 73100 Lecce– I
A. Buccolieri, G. Buccolieri, D. Manno, L. Famà
Department of Material Science, University of Lecce, C.P. 193, 73100 Lecce-I
Department of Physics
Department of Physics
University of Lecce
University of Lecce

## Slide 2
Contents:
Nuclear transmutations in D-Pd films induced
by low power He-Ne laser beams
Samples
Experimental apparatus
Analysis and results

## Slide 3
Evidence of elements transmutation
Samples of silicon with thin Pd layer implanted with B ions
Samples loaded with deuterium gas and exposed to He-Ne laser beams
SEM, EDX analysis of samples after 76 treatment days
Evidence of presence of “new” elements inexistent in samples not processed

## Slide 4
Samples
Implanted with:
B at 150 keV
Atomic weight :
B= 11
Substrate Si
1st layer 50 nm Ti
2nd layer 500 nm Pd
Nuclear transmutations in D-Pd films induced
by low power He-Ne laser beams

## Slide 5
Samples
B implantation were done in order to try to force only specific nuclear reactions
Nuclear transmutations in D-Pd films induced
by low power He-Ne laser beams

## Slide 6
Samples
B Implanted Pd
Energy = 150 keV
Nuclear transmutations in D-Pd film and induced
by low power He-Ne laser beams
Fig. 1: Boron ions distributions vs. target depth

## Slide 7
Experimental apparatus
Apparatus Sketch
D2: Deuterium gas
pressure up to 4 bar
T: Target
W: Quartz window
L: Convergent lens

## Slide 8
Experimental apparatus
Type: CW He-Ne λ=648 nm
Laser power density: 2mW/cm2

## Slide 9
SEM and EDX analysis of sample irradiated in air atmosphere
SEM micrograph of virgin sample
EDX analysis of virgin sample

## Slide 10
SEM micrograph of sample processed with D2 gas and He-Ne laser
SEM analysis of samples loaded with D2 gas irradiated by He-Ne laser

## Slide 11
SEM analysis of samples loaded with D2 gas irradiated by He-Ne laser
SEM micrograph of sample processed with D2 gas and He-Ne laser

## Slide 12
SEM analysis of samples loaded with D2 gas irradiated by He-Ne laser
SEM micrograph of sample processed with D2 gas and He-Ne laser

## Slide 13
SEM analysis of samples loaded with D2 gas irradiated by He-Ne laser
SEM micrograph of sample processed with D2 gas and He-Ne laser

## Slide 14
X-Ray spectrum of sample loaded with D2
EDX Analysis
EDX spectra of samples loaded with D2 gas and irradiated by He-Ne laser
Semiquantitative analysis
Elements %
C 8.71
O 43.04
Na 3.41
Mg 0.35
Al 0.78
Si 3.95
S 0.49
Cl 1.83
K 2.37
Ca 3.88
Pd 31.18

## Slide 15
X-Ray spectrum of sample loaded with D2
EDX Analysis
EDX spectra of samples loaded with D2 gas and irradiated by He-Ne laser

## Slide 16
Conclusions
As in previous works, Pd samples irradiated
with lasers beams show clear effect of nuclear
transmutations. These samples were implanted
with specific elements in order to highlight the
activated nuclear channel.