## Slide 1: Hydrogen loading of Nickel and related phenomena
S. Focardi
  Department of Physics - University of Bologna - Italy
V. Montalbano, F. Piantelli
  Centro I.M.O. - Department of Physics - University of Siena - Italy
S. Veronesi
  Istituto Nazionale Fisica della Materia – UdR Siena - Italy
  Centro I.M.O. - Department of Physics - University of Siena - Italy
6th International Workshop on
Anomalies in Hydrogen / Deuterium loaded Metals
ISCMNS
Siena, Certosa di Pontignano
14/5/2005

## Slide 2: Summary
The experiment
  Hydrogen loading of pure Ni. No electrolysis
  New cell designed for laminar flow of gas
  Quantitative determination of loading
  Loading dynamic
  Primer and energy production
  Photon emission
  laboratory Energy from Hydrogen:
  setup for production of well-characterized metallic surfaces still in progress

## Slide 3
AMBE

## Slide 4
Experimental program
4 programmed experiments
2 with cylindrical samples (in progress; one working, the other outgassing)
2 with planar samples (in preparation)
Goals
Check of the effect of an applied magnetic field (among 0 -except for the Earth field- up to more than 2T)
Check of the behaviour homogeneity for different samples after annealing at 900°C and cooling down to ~200°C by step of 10°C
Evaluation of the absorption process:
fast for 110°C<T<140°C
slow for 220°C<T<260°C and 340°C<T<380°C
it is sufficient an absorption of x0.05 to have the primer

## Slide 5
Goals (continued)
Primer and energy production:
fast primer starting from ~180°C by temperature step
slow primer starting from >350°C (auto excitation)
primer by pressure step
Photon and particle emission

## Slide 6
We study cylindrical and planar rod
        Pure Ni
Cleaning: chemical and physical (out gassing)
Annealing cycles
    in vacuum TMAX < 550 °C
    in Hydrogen TMAX < 450 °C
Loaded with Hydrogen
pressure 100 mbar < PH < 1000 mbar
temperature 150 °C < TS < 450 °C

## Slide 7: Experimental setups
Cell for a cylindrical sample
Pt 100
T1
T2

## Slide 8: Experimental setups
Cell for 3 plane samples

## Slide 9: Experimental setups
Cell for a cylindrical sample
Gas flow

## Slide 10: experimental setup
Schematic layout
PRESSURE SENSORS
EXP. CELL
NaI(Tl)
detector
Vacuum
turbo-pump
H2
Power
supply

## Slide 11: Hydrogen Loading
Example of slow loading

## Slide 12: Hydrogen Loading
  Examples of slow loading

## Slide 13: Hydrogen Loading
Example of fast loading

## Slide 14: Primers
Fast primer by pressure step
Slow primer by temperature step

## Slide 15
Absorption and slow primer by temperature step

## Slide 16
Sequence of excitation by temperature step

## Slide 17: Energy production in planar sample

## Slide 18: Experiment in progress

## Slide 19
Preliminery data

## Slide 20
Preliminary data

## Slide 21
Preliminery data

## Slide 22
Preliminery data

## Slide 23: Correlation between temp1 and pt100

## Slide 24: Correlation between temp1 and temp2

## Slide 25: Gamma emission in previous experiments
Cell with planar samples

## Slide 26: Photon emission

## Slide 27
Photon emission
137Cs source
Cell with cylindrical samples

## Slide 28: Conclusions and perspectives
*We are very close to the auto-sustenance (less than 20W introduced and 71W produced = 91W)(t=260°C) => we want to evaluate the possibility to increase the produced power to more than 100W
**We have seen that the energy production can be obtained between 200°C and 400°C => we want to evaluate the best temperature interval inside that region
***We want to evaluate the effect of a magnetic field on the absorption and on the primer of the energy emission
****We have indication that the phenomenon takes place at the surface of the sample; we have seen in previous experiments a transmutation effect => we want to evaluate the residue by means of SEM-EDAX and SIMS technique
*****As already done in previous experiments, we want to investigate the decay of the samples extracted from the 4 cells (about 2 months) and the particle emissions by means of a Ge and Si detector and Wilson chamber