## Slide 1: ISCMNS-2 at Siena (13-16 May 2005) a Poster on “An overview of experimental studies about H/Pd over-loading with thin Pd wires and several different electrolytic solutions. ”
by
--- Prof. Antonio Spallone:
[Antonio.Spallone@LNF.INFN.IT]
Ricercatore Associato ai Laboratori Nazionali di Frascati dell’Istituto Nazionale di Fisica Nucleare (LNF-INFN) [WWW.LNF.INFN.IT]
and
Docente di Matematica e Fisica al Liceo “Edoardo Amaldi” di Roma [HTTP://Utenti.RomaScuola.Net/Liceo_Amaldi]
in Collaboration with
F.CELANI(1), P.MARINI(2), V.di STEFANO(2) (1) INFN-LNF, Via E.Fermi 40, 00044 Frascati, (Italy)
(2) EURESYS, Via Lero 30, 00129 Roma, (Italy)

## Slide 2: INDEX
Introduction (D/Pd threshold)
The method (H/Pd over-loading)
Electrolysis Protocol (OFF/L/H current)
Measurements:
  Loadings (H/Pd=1)
  Temp. Resistance coeff. (KTR)
Conclusions

## Slide 3
Introduction
Since March 1989, after M.Fleishmann and S.Pons claimed to produce a big amount of hentalpy in excess from an electrolytic cell of D2O+LiOD (0.1 N) using a Pd cathode absorbing high concentration of Deuterium, the main critical point was to achieve high D/Pd values (around 1:1). Many researchers spent a lot of efforts to reach to this goal but the difficulties were much more than expected and the high absorption reproducibility very poor.
Our group from many years has studied the Pd cathode over-loading achieving at D/Pd around at 1 with Pd tick plates using a own high voltage, short time, electrolytic pulsed technique. But working at this very unstable condition, the heat in excess reproducibility was very poor. So that we substitute bulk Pd plate (very difficult to over-load in homogeneous way) to long thin wires and instead of high frequency pulse electrolysis (very difficult to study loading parameters, because high electric noise) we used direct current electrolysis.
Motivations
In order to determinate H(D)/Pd loading value, we can refer to H(D)-Pd resistance curve, so that, to have accurate measurements we need to solve these questions:
a) high Pd resistance  long and thin wire;
b) low influence of electrolyte on Pd resistance measurement  very diluted solution and distant electrodes;
c) no uncontrolled metallic deposition on cathode  acidic solution (instead of basic) using very pure solvent water;
d) addition of a very low amount of known elements into the solution and production of a quite controlled Pd surface deposition layer.

## Slide 4: The D/Pd threshold
The Pd lattice:
The Pd lattice is a fcc (face centred cubic)
H or D atoms are formerly located into the lattice centre (phase ), further interstitial sites of lattice are occupied ( + phase ); finally when the whole of Pd lattice available sites are saturated, we achieve H/Pd or D/Pd=1 (named as phase )
It has been experimentally verified (M. McKubre) that the threshold D/Pd 0.84 must be overcome to record heat in excess!
Pd
D

## Slide 5
Normalised Palladium resistance versus Hydrogen (Deuterium) molar fraction of Pd. Peak value is: H/Pd=0.75, R/Ro=1.78 (Hydrogen) and D/Pd=0.75, R/Ro=2.0 (Deuterium). Max known loading is H(D)/Pd=0.95 at R/Ro=1.4 (1.6)
The electrolytic cell is a glass beaker filled by about 400 cm3 of H2O+HCl solution (2 cm3 of HCl at 10 M/cc) in which are located two parallel (1.5 2 cm distant) thin long (19 cm length) wire electrodes (cathode: Pd, 50 um diameter; anode: Pt, 0.5 mm diameter). The cell is located into a thermostatic water bath set at room temperature (22 °C). Cell, bath and room temperature are continuously recorded.

## Slide 6: The Loading Tests
The Pd wire cathode:
We tested 50 and 100 m (10cm long) wires
The electrolyte solution:
BASE: H2O (400cc) + HCl (or H2SO4) at 50 M
Loading-supporter: kation elements addition (Ca, Sr, Li) at 50 M
Loading-catalyzer: Hg (50-> 500-> 1000 nM)
The electrolysis Protocol:
Electrolysis current cycles were performed: OFF/High=50mA and/or Low/High/Low=5mA
Kation-Hg deposition on Pd surface is supposed to be formed (width 20-> 200 nm)

## Slide 7
Fig. – Calcium loading trend.
Loading trend curve (R/Ro vs log time) occurred when Ca ions (70*10-6 M) have been added to the electrolyte; in about 300s resistivity peak was achieved. It is visible a shoulder lasting for about a hour after the peak; the highest loading (R/Ro=1.28 for “up” and 1.38 for “down” at 23 °C) reached stable valurs in about one day.
(“up” and “down” labels are corresponding to up (EF) and down (DE) Pd wire segments, see Fig. 4).
Fig. – Strontium loading trend.
Loading trend curve (R/Ro vs log time) occurred when Sr ions (35*10-6 M) have been added to the electrolyte; in about 300s resistivity peak was achieved. The shoulder occurring lasts about half hour; loading higher than Ca test (R/Ro=1.13 for “up” and 1.15 for “down” at 27 °C) were reached in less than one day.
Ca
Sr

## Slide 8
Fig. – Deloading trend.
The plot shows Hydrogen deloading versus time. Electrolysis current has been switch off (“OFF” condition) after “ON” condition (R/Ro=1.13 at 23 °C) and in about one hour loading peak was achieved (R/Ro=1.77 at 23 °C). A visible deloading shoulder lasts, about half hour, at R/Ro=1.65; full deloading process requires about 16 hours: both “up” and “down” wire segments return to their initial Ro resistance values.
Fig. – Fast re-loading test.
Typical test of OFF/ON current cycle: starting from a high loading condition (R/Ro=1.10 at 22 °C), after about half hour of de-loading (near the resistivity peak) because current disconnected (“OFF”), current was switched on (“ON”) again. In this condition, reloading is quite fast (less than half hour) and wire reached the previous R/Ro value. Sometimes this procedure, operated cyclically, can be useful to achieve high loading values.
Sr: OFF-deload
Sr: OFF/ON cycle

## Slide 9
Loading tests with electrolytic solution composed by bi-distilled water + HCl:
A) loading protocol: in 2 days best loading at R/Ro=1.6 .
Loading tests with electrolytic solution composed by bi-distilled water + HCl:
B) a further detail of loading protocol (low/high+off/on+low current): a much higher loading improvement (R/Ro= 1.48) occurs at low current (about 5 mA) for long time; at high current (100mA) R/Ro= 1.42 is achieved. Test has finishes with a long time electrolysis-off operation to verify loading calibration (peak at R/Ro= 1.78, a shoulder at R/Ro=1.70 and return to R/Ro= 1.02 initial condition).
HCl - only
Begin
run
End
run

## Slide 10
Loading tests with electrolytic solution composed by bi-distilled water + HCl +Sr:
The beginning of loading is quite similar to only-HCl loading (R/Ro= 1.7); but, after the several times repetition of off/on current cycles, loading value achieves R/Ro=1.5 at low current (4 mA).
Loading tests with electrolytic solution composed by bi-distilled water + HCl+ Sr:
The final conclusion of this procedure is up to now R/Ro= 1.15 at 5 mA; in this condition loading state is stable in the time. Increasing the current up to 100 mA (high current) a sort of “Tafel effect” increases the loading at R/Ro= 1.08 (not reported in this plot). During the same test, it has been possible to repeat again this values.
Sr - only
Begin
run
End
run

## Slide 11
Loading tests with electrolytic solution composed by bi-distilled water + Sr + Hg:
The beginning of loading is operated with SrSO4 and no interesting loading effect has occurred, even changing H2SO4 solute to HCl and operating low/high current cycles; then adding HgCl2 (10-5 Moles) (at time 7500 s) and increasing current to 150 mA, loading increases in 1 hour up to R/Ro= 1.15 and remaining stable (even reducing current to 100 mA).
Loading tests with electrolytic solution composed by bi-distilled water + HCl + Hg:
In this test no Sr has been added but only Hg (10-7 Moles) and loading effect occurs and in 2 days R/Ro= 1.35 (at 5 mA) has been achieved; further, increasing the current to 75 mA, R/Ro= 1.3 has been achieved (not shown in the plot) and at off-current Pd deloads quickly. Following tests with much more Hg (10-5 Moles) have shown no high loading (R/Ro 1.7) and no deloading occurs when current is off even after many hours.
Hg-tests
Sr+Hg
Hg-only

## Slide 12
Loading tests with electrolytic solution composed by Alcohol:
After the first loading, a OFF/ON=high current protocol is operated; then a OFF/ON=low current is left for long time. Slowly Pd wire over-charged up to R/Ro= 1.15, at room temperature and 2.5 mA, 11V.
Etil-Alcohol + Hg (+Sr)

## Slide 13
After addition of HgCl2=5cc (10-7 M/cc), at I=5mA (5V) loading slowly reached R/Ro= 1,43(up) and 1.23(down); furthermore at I=40mA(40V), achieved R/Ro=1.36(u) and 1.16(d); (up) loaded upto 1.27 and down deloaded to 1.32; achieving a plateau...
After anodic current (-5mA), a similar restarting got a good over-loading R/Ro= 1,07(up) and 1.05(down) with a L/H cycle at I=45mA (45V) ! Following cycle H/L shows up reaching a plataeau at R/Ro= 1.10 for long time…
Sr+Hg
begin
run
Sr+Hg
L/H/L
test

## Slide 14
Fig. – Slow high loading at Low-current: [I=5mA, V=10V] (R/Ro=1.33) and then applying a L/High-current cycle: [34mA,48V] (R/Ro=1.21) the loading is increased; a further H/L cycle shows a better value reached at Low-current.
- It seems that Li addition in the electrolytic solution is effective as well as Sr, even with a very small amount of Hg.
NEW Li+Hg (test-L/H/L)
(small Hg)

## Slide 15
NEW Li+Hg (test-L/H/L)
(big Hg)
Fig. – Test with a big amount of Hg:
Start up and slow loading at Low-current: [I=6mA, V=8V] (R/Ro=1.45); Pd locked by Hg.
After anodic current, again start up and slow loading at High-current: [36mA,45V] (R/Ro=1.20); Pd locked.
 It is quite evident that when Hg is in high quantity it is important to use high current before Hg fully cover the Pd-cathode.

## Slide 16
Loading tests with electrolytic solution composed by purified D2O + Sr:
After a loading, R/Ro= 1.6 (I= 6mA, V= 11V); OFF/ON current cycles are operated. Finally Pd wire slowly discharges in OFF current condition
Loading tests with electrolytic solution composed by Metil-Alcohol in D2O:
After a long term OFF-deloading, a new loading is operated reaching a value of R/Ro= 1.6 (I= 8mA, V= 11V);
D2O tests with Sr-only
pure
D2O
D2O
in
Metil
alcohol

## Slide 17
D2O tests with Li+Hg
Fig.: - Loading tests with electrolytic solution: D2O + Li + Hg=4cc (10-7/M/cc):
No enough loading: R/Ro= 1.90 (I= 6mA, V= 12V); L/H current cycles are operated with no loading increasing.
Fig.: - Loading tests with electrolytic solution: D2O + Li + Hg=8cc (10-7/M/cc):
A better loading: R/Ro= 1.83 (I= 6mA, V= 12V); L/H:32mA current cycles are operated showing a loading increasing up to R/Ro= 1.73

## Slide 19
Fig. - H/Pd resistance temperature coefficient.
According to the literature data (Baranowsky et al.) this coefficient almost linearly decreases from 4.1.10-3 K-1 (end of  phase) to 1.8.10-3 K-1 (end of + phase) because H loading. At H/Pd >0.70 no data are allowable.
Resistance Temperature coefficient: kT

## Slide 20
Fig. – Hg coated wire, high temperature measurements. After achieving R/Ro=1.1, the Pd surface has been coated with Hg (by HgCl2 electrolysis) and a cycle of “high temperature test” was performed.Only a weak de-loading occurred at 100 °C (2 hours at ebullition state). In this experiment the temperature coefficient (T w )was estimated to be 3.2.10-3 °C-1.
Fig. – Hg coated wire, test at very low temperatures. After achieving R/Ro=1.1, the Pd surface was coated with Hg and a cycle of low temperature test (up to liquid nitrogen) was performed. For sector “up” both high and low temperatures data are available: they are roughly on the same line. In the range 77÷300 K the temperature coefficient, T, was estimated to be 3.3 ÷ 3.4.10-3 °C-1.
kT tests
(100°C)
(77 K)

## Slide 22: CONCLUSIONs
To achieve a H/Pd over-loading:
Kations elements addition to acid solution (Li, Sr, Ca and maybe others…)
Very low Hg ions concentration (and low power supply electrolysis of tenth of mW)
A proper metallic structure deposited onto Pd surface (by peculiar electrolysis current protocol)
and many tests to optimize the effect…