## Slide 1
Revealing restricted organic cation geometry in the low temperature phase of FAPbI3 via solid state nuclear magnetic resonance spectroscopy at 100 K
Benny Gallant, Dominik Kubicki
14/02/2025
b.gallant@bham.ac.uk
Notes: I’m going to talk today about MOF glasses, and present a strategy by which they can be modified to make them easier to process, at substantially lower temperatures, whilst also opening up a new route to tailor the properties of MOF glasses (optical, mechanical, as well as thermal)

## Slide 2
13C CPMAS NMR (100 K)
2
Three freeze-thaw cycles were conducted.
In each cycle α-FAPbI3 single crystals were rapidly cooled (order of ~2000 K/min) from 298 K to 100 K and both 13C and 15N cross polarisation (CP) magic angle spinning (MAS) NMR conducted.
The sample was then warmed rapidly to 298 K, and the process repeated.
13C CPMAS measurements produced identical spectra each time the sample was quenched. Two 13C environments are apparent (only the spectrum from the third freeze cycle is shown fitted in the figure). These spectra should not be considered quantitative.

## Slide 3
15N CPMAS NMR (100 K)
3
In contrast to 13C CPMAS NMR measurements, there are some variation between the 15N CPMAS NMR spectra acquired on the sample during each sequential freezing event.
As shown more clearly on the following slide, these differences can be accounted for by varying the relative populations of ~8 distinct 15N environments, each with its own characteristic 15N chemical shift.
This result is consistent with multiple, but far from an infinite number, of possible FA+ cation orientations in the low temperature phase of FAPbI3 when cation reorientation is stymied (at least to a first approximation).
That the ratio of the different populations does not remain constant between freeze-thaw cycles suggests that there may be two
It’s worth noting, anecdotally, that – although it is labelled “Freeze 1” – the sample had already been frozen and thawed multiple times before this spectrum was measured. This is notably as, given this 15N spectrum is appreciably different to that observed for the second and third freezing events, it would otherwise be tempting to infer that there may be some degree of uncontrolled sample evolution over the course of the course of the three freeze-thaw cycles. Indeed, it’s reassuring that the crystals were still black even after multiple (perhaps as many as 10!) freeze-thaw cycles!

## Slide 4
15N CPMAS NMR (100 K)
4
It is possible to fit the 15N CPMAS NMR spectra of each freezing event with 8 characteristic signals.
During fitting, the peak centres, the Gaussian broadening and the Lorentzian broadening for each fitted peak were permitted to vary by only up to ±0.1 ppm between each freeze-thaw cycle (fits carried out sequentially in order starting with Freeze 1). Some variation was permitted to account for spectral noise distorting the peak positions and shapes.
It is worth noting that, even with these limitations applied to the fitting, there is a very real danger of an overparametrised fit here, and thus I’d suggest that these fittings should only be taken as indicative that the 15N spectra “are consistent with approximately eight distinct 15N environments”, and thus are consistent with limited number of FA+ orientations with respect to the surround haloplumbate network.
Note: Colours shown are an aid to the eye only.