## Slide 1: Isotopic and Elemental Composition of Substance in Nickel-Hydrogen Heat Generators
K.A. Alabin1, S.N. Andreev1, S.N. Zabavin3,
A.G. Parkhomov3, A.G. Sobolev2 T.R. Timerbulatov3
1Prokhorov General Physics Institute, Russian Academy of Sciences
2Lebedev Physical Institute, Russian Academy of Sciences
3R & D laboratory K.I.T.
<number>

## Slide 2
At the present time, many devices have been created that produce energy comparable to energy release in nuclear reactions, but not accompanied by harmful radiation and radioactivity. The nature of this surprising effect remains unclear. The study of elemental and isotopic changes in the operation of reactors is of paramount importance for solving this problem.
<number>

## Slide 3
Estimates show that if the anomalous heat release is really associated with changes at the nuclear level, the appearance of nuclides originally absent from the fuel can be detected with excess energy of about 1 MJ per gram of fuel.
To reliably detect changes in the ratios of isotopes in elements that originally form part of the fuel, excess energy is required to exceed 100 MJ / g. It is natural that even a thorough analysis of the fuel of reactors with insufficient development of excess energy does not reveal any changes.
Excess energy in the high-temperature heat-generator of Rossi was 5800 MJ / g. This is quite sufficient for radical changes in the isotopic composition of both nickel and lithium.
This report provides information on the results of the analysis of changes in fuel and in structural materials that occurred in several nickel-hydrogen reactors created by our team.
<number>

## Slide 4: Reactor AP2
Reactor was charged with a fuel mixture of 640 mg Ni + 60 mg LiAlH4. It worked on March 16-22, 2015, producing about 150 MJ of excess heat.
Elemental composition analysis using an electronic scanning microscope (Prokhorov General Physics Institute, Russian Academy of Sciences)
<number>

## Slide 5
Elemental composition of fuel before and after work in the reactor AP2, determined by a laser atomic-emission spectrometer (Kurnakov Institute of General and Inorganic Chemistry RAS)
Isotopic composition of fuel before and after work in reactor AP2. The analysis is made by ICP-MS in Vernadsky Institute of Geochemistry and Analytical Chemistry RAS
<number>

## Slide 6: ICP-MS Isotopic analysis of fuel at the AP2 reactor
Vernadsky Institute
Uppsala University, Sweden
<number>

## Slide 7
Heat dissipation power W = c (dm /dt) (T-To) (1 + )
c is the specific heat of water,
(dm /dt) is the mass of water flowing per second,
 - correction for heat loss,
To is the temperature at the entrance to the calorimeter,
T is the outlet temperature.
Design of a water flow calorimeter
<number>

## Slide 8: Design of reactors tested in a water flow calorimeter
One of reactors tested in conjunction with water flow calorimeter "Protok-6" worked continuously from April 11 to May 29, 2016, with excess heat output from 20 to 65 watts. The integrated excess energy in this reactor is about 100 MJ.
This reactor had a heater of tungsten wire, located inside of sealed ceramic pipe. The fuel (1.8 g of nickel powder mixed with 0.2 g of lithium aluminum hydride) was in a ceramic tube wrapped in a tungsten heater.
<number>

## Slide 9
After opening the reactor, it was found that the inner surface of the outer tube near the heater was covered with a gray, hilly, glassy coating. Fuel has became to vitreous mass with impregnations of metal balls about 0.1 mm in size. Several balls had diameter of up to 1 mm. At the ends of the filling, the fuel took the form of a sintered mass containing small metal balls. In addition, a powder was formed, one of whose fractions had ferromagnetic properties.
The initial fuel mixture, the metal ball from the spent fuel, the fuel at the edge of the core, the formed powder, the coating on the inner surface of the outer tube were subjected to ICP-MS analysis in Vernadsky Institute
Reactor "Protok-6" after destruction
<number>

## Slide 10
Relative content of nuclides (atomic%) in fuel and near the core of the reactor "Protok-6" before and after reactor operation.
Nuclides with a content > 0.1% are shown.
<number>

## Slide 11: Ratio of nickel isotopes in the fuel and near the core of the "Protok-6" reactor before and after the reactor operation.
Since the data on 64Ni is unreliable due to the uncontrolled additive 64Zn, when preparing the table for the 64Ni fraction, the natural value was assigned
Obvious result of isotopic analysis is the increase in the content of many nuclides in comparison with their content in the initial fuel and structural materials. The content of boron, iron, gallium, cerium, zirconium, strontium, bismuth increased greatly. The most significant anomalies are found in the powder accumulated in the space between the inner and outer tubes. Especially many appeared 140Ce: 6.3% (in the initial fuel <0.0001%). A significant amount of tungsten found in the samples after being in the reactor is probably due to the migration of this element from the incandescent tungsten helix
<number>

## Slide 12
Reactor VV3
Reactor VV3 differs from the "Protok 6" reactor with a different heater design and the absence of a calorimeter. A mixture of nickel powder with lithium aluminum hydride weighing 1.5 g was used as fuel. The fuel contained pieces of tungsten wire with a total mass of 0.77 g. The reactor operated from June 14 to July 24, 2016, producing excess power up to 330 W. A total of 790 MJ of excess heat was generated.
ICP-MS analysis of fuel was done In Vernadsky Institute, with separate analyzes of the surface and deeper layers. Partially, the results of the analysis are shown in Table 4. In addition to the data for the samples recovered from the reactor after its operation, information on the content of isotopes in the initial fuel, including tungsten wires embedded in it, is given.
Fuel after operation in the VV3 reactor
<number>

## Slide 13
The content of nuclides (atomic%) in the fuel of the reactor VV3 before and after the operation of the reactor. Isotopes with a content > 0.1% are shown.
The content of nuclides in fuel as a result of being in the reactor has changed markedly.
The content of boron, copper, cerium, and silver increased especially.
<number>

## Slide 14
Ratio of nickel isotopes in fuel VV3 before and after operation of the reactor
Data on the investigated samples, although slightly different from the natural ratio, differ slightly among themselves.
<number>

## Slide 15
Reactor KV3
Reactor KV3 at the beginning of work
Reactor KV3 opened after completion of work.
Fuel: a nickel powder weighing 1.8 grams without admixture of lithium aluminum hydride. Saturation with hydrogen was carried out by aging in hydrogen gas. The reactor had not a ceramic but a quartz outer tube. The heater was made of tungsten-rhenium alloy.
The KV3 reactor operated from December 20, 2016 until January 31, 2017, with an excess power of 100-200 watts. Integral excess heat generation is about 400 MJ.
<number>

## Slide 16
Comparing fuel before and after work in the reactor, you can see a decrease in the content of sodium, potassium and iron.
The appearance of a significant amount of copper is noteworthy.
The content of nuclides (atomic%) in the fuel and near the core of the KV3 reactor before and after the reactor operation. Isotopes with a content > 0.1% are shown. ICP-MS analysis is made in Vernadsky Institute
In space between inner and outer tubes a lot of tungsten, as well as iron, sodium, potassium, nickel, silicon, calcium, scandium and a number of other elements appeared.
<number>

## Slide 17
Relative content of nuclides (atomic%) in the ceramic tube before and after the operation of the KV3 reactor. Nuclides are shown whose content has increased more than 10 times.
In addition to tungsten and rhenium, the appearance of which can be explained by migration from the helix of the heater, the content of boron has greatly increased in the ceramic tube, as well as nuclides with atomic masses of 43-53, 64-83, 107-130, 198-208.
<number>

## Slide 18
The ratio of nickel isotopes in fuel and near the core of the KV3 reactor before and after reactor operation.
The isotopic composition of nickel in fuel before and after work in the reactor remained practically unchanged. Some differences are noticeable in the results obtained for the ceramic tube and the substance between the tubes. But these results can not be considered accurate, since the concentration of nickel in the samples studied is not high enough for reliable analysis.
<number>

## Slide 19
CONCLUSIONS
The analysis of the isotopic and elemental composition of the substance in four nickel-hydrogen reactors of various designs with the development of excess energy from 100 to 790 MJ was done. Not only the changes in fuel, but also in materials adjacent to the core have been investigated. In addition, the composition of the substance accumulating in the cavity of the reactor near the core has been studied.
There were no significant changes in the isotopic composition of nickel and lithium, except for the analysis of the fuel of the AP2 reactor at Uppsala University (Sweden).
Significant increase in the concentration of impurities in a number of nuclides has been observed not only in fuel, but also in structural elements adjacent to the active zones of the reactors. In addition to tungsten and rhenium, the appearance of which can be explained by migration from the helix of the heater, the content of boron increases greatly in them, as well as nuclides with atomic masses of 43-53, 64-83, 107-130, 198-208.
In substance accumulated in the cavity of the reactor near the core, in addition to tungsten, a lot of iron, sodium, potassium, nickel, silicon, calcium, scandium and a number of other elements accumulated.
<number>

## Slide 20
References
Levi G., Foschi E, Höistad B. Observation of abundant heat production from a reactor device and of isotopic changes in the fuel. − http://www.sifferkoll.se/sifferkoll/wp-content/uploads/2014/10/LuganoReportSubmit.pdf
2. Parkhomov A.G. Report of the international commission on the test of high-temperature heat generator Rossi. − IJUS, 2014, v.2, № 6, pp. 57-61 (in Russian). http://www.unconv-science.org/pdf/6/parkhomov2-ru.pdf
3. Parkhomov A.G. Nickel-hydrogen reactors created after publication of the report on experiment in Lugano (in Russian). − IJUS, 2016, v.4 № 11, pp.58–62, http://www.unconv-science.org/pdf/11/parkhomov-ru.pdf
4. Alabin K.A., Andreev S.N., Parkhomov A.G. Results of analysis of isotopic and elemental composition of the fuel of nickel-hydrogen reactors. − IJUS, 2015, v. 3, №10, pp. 49-53 (in Russian). http://www.unconv-science.org/pdf/10/alabin-ru.pdf
5. Parkhomov A.G. Investigation of new version of the device similar to high-temperature Rossi heat generator. -IJUS, 8(3), pp. 34-38, 2015. http://www.unconv-science.org/pdf/8/parkhomov-en.pdf
6. Parkhomov A.G. Long-term tests of nickel-hydrogen heat generators in an water flow calorimeter. − IJUS, 2016, v. 4, №12-13, pp. 74-79 (in Russian). http://www.unconv-science.org/pdf/12/parkhomov-ru.pdf
<number>