## Slide 1
LEAP: The LENRIA Experiment and Analysis Program
Steven B. Katinsky, David J. Nagel LENRIA Corporation
Melvin H. Miles, M. Ashraf Imam
12th International Workshop on Anomalies in Hydrogen Loaded Metals
5-9 June 2017
Hotel Langhe e Monferrato, Via Contessa di Castiglione, 14055 Costigliole d'Asti (AT), Italy
Introduction and Progress Report

## Slide 2
LEAP: The LENRIA Experiment and Analysis Program
Strategy
Perform the same LENR experiment that has been qualified to produce excess heat, at multiple major laboratories.
Produce reports on the conduct and results of the experiments at each laboratory.
Coordinate simultaneous publication of the reports in a major scientific journal.
Goal is a change of perception of LENR by the scientific community, for ‘very important people,’ government agencies and the public.

## Slide 3
LEAP: The LENRIA Experiment and Analysis Program
History
The multi-lab program, now called LEAP, was conceived in 2013.
Since then, we have examined experimental options for the program.
Last year, in 2016, we decided to base the program on the electrochemical loading of Pd-Boron alloys.
In recent months we have been acquiring and testing equipment to produce a modern, turn-key, automated system.

## Slide 4
LEAP: The LENRIA Experiment and Analysis Program

## Slide 5
Rothwell, J., Introduction to the Cold Fusion Experiments of Dr. Melvin Miles. Infinite Energy, 1997. 3(15/16): p. 27. Revised and updated, 2004.
LEAP: The LENRIA Experiment and Analysis Program
Consideration of experimental candidates for the LEAP Program

## Slide 6: LEAP: The LENRIA Experiment and Analysis Program
Rothwell, J., Introduction to the Cold Fusion Experiments of Dr. Melvin Miles. Infinite Energy, 1997. 3(15/16): p. 27. Revised and updated, 2004.
Introduction to the Cold Fusion
Experiments of Melvin Miles Jed Rothwell

## Slide 7
LEAP: The LENRIA Experiment and Analysis Program
Rothwell, J., Introduction to the Cold Fusion Experiments of Dr. Melvin Miles. Infinite Energy, 1997. 3(15/16): p. 27. Revised and updated, 2004.
8/9 with NHE Japan in Sapporo

## Slide 8
LEAP: The LENRIA Experiment and Analysis Program
ANOMALOUS EFFECTS IN DEUTERATED SYSTEMS
Melvin H. Miles, Benjamin F. Bush, Kendall B. Johnson
Naval Air Warfare Center, China Lake 09/96

## Slide 9
LEAP: The LENRIA Experiment and Analysis Program
ANOMALOUS EFFECTS IN DEUTERATED SYSTEMS
Melvin H. Miles, Benjamin F. Bush, Kendall B. Johnson
Naval Air Warfare Center, China Lake 09/96
1/1 NHE Japan
1/1 NRL
1/1 Miles Ridgecrest
10/11 Aggregate Pd-B
*
**
** Excess heat measured before calorimeter failure
* Non-performing cathode was observed to have defect
Solid experimental base behind the experiment we chose.

## Slide 10
ANOMALOUS EFFECTS IN DEUTERATED SYSTEMS
Melvin H. Miles, Benjamin F. Bush, Kendall B. Johnson
Naval Air Warfare Center, China Lake 09/96

## Slide 11: New Hydrogen Energy Laboratory (NHE) Sponsored by New Energy Development Organization (NEDO)
Dr. Melvin H. Miles visits Japan as a NEDO
Guest Researcher
Location: NHE Laboratory, Sapporo, Japan
Dates: October 23, 1997 to March 31, 1998
Included is a Pd-B Alloy Experiment

## Slide 12
LEAP: The LENRIA Experiment and Analysis Program

## Slide 13
LEAP: The LENRIA Experiment and Analysis Program
NEDO Final Report, Electrochemical and Calorimetric Studies of Palladium and Palladium Alloys in Heavy Water. Dr. Melvin H. Miles. 1998.

## Slide 14
LEAP: The LENRIA Experiment and Analysis Program
NEDO Final Report, Electrochemical and Calorimetric Studies of Palladium and Palladium Alloys in Heavy Water. Dr. Melvin H. Miles. 1998.

## Slide 15
LEAP: The LENRIA Experiment and Analysis Program
NEDO Final Report, Electrochemical and Calorimetric Studies of Palladium and Palladium Alloys in Heavy Water. Dr. Melvin H. Miles. 1998.

## Slide 16
LEAP: The LENRIA Experiment and Analysis Program
NEDO Final Report, Electrochemical and Calorimetric Studies of Palladium and Palladium Alloys in Heavy Water. Dr. Melvin H. Miles. 1998.

## Slide 17
LEAP: The LENRIA Experiment and Analysis Program
NEDO Final Report, Electrochemical and Calorimetric Studies of Palladium and Palladium Alloys in Heavy Water. Dr. Melvin H. Miles. 1998.

## Slide 18: Off to See Mel Assist Mel in looking for Pd-B A2 NHE Cathode
Mel extended an Invitation to come visit him in Ridgecrest, CA
About 2.5 hours and 154 miles north of
Los Angeles.
Home of China Lake Naval Air
Weapons Station
Mel worked as an electrochemist and researcher at the China Lake labs

## Slide 21: Search for A2 Cathode
Two days of searching with Mel
Checked attic, garage, closets, file cabinets, boxes, every storage space we could find
Found an empty vial labeled Pd-B 0.5
Made one last effort an hour before leaving
Found A1, A2 and A3 NHE cathodes on shelf

## Slide 35: Dr. Melvin Miles Ridgecrest Lab Bench
Heater/circulator for water bath
Techne, TE-10D Tempette, 1000 W, Model # FTE10DPC.
Thermistor thermometer 5 channel
Cole Parmer Model 8502 Series displays the temperatures to 0.01 C.
Potentiostat/Galvanostat
PAR (Princeton Applied Research) Model 362 Scanning Potentiostat.
Digital Multimeter (DMM)
GW Digital Multimeter, Model GDM-8145.
Waterbath
Aqua Culture 10 Gallon Glass Aquarium, Walmart #: 0008022662

## Slide 41
The Fleischmann-Pons Calorimetric Methods And Equations
Melvin H. Miles SSICCF20 Xiamen, China
Mathematical Modeling and Calorimeter Equations

## Slide 42
Chart: Pd - 0.5 B 2017
| 1.0 | 2.0 | 3.0 | 4.0 | 4.5 | 5.0 | 6.0 | 7.0 | 7.5 | 8.0 | 9.0 | 10.0 | 11.0 | 12.0 | 13.0 | 14.0 | 15.0 | 16.0 | 17.0 | 18.0
 | 0.4 | 1.5 | 1.6 | 7.3 | 20.8 | 14.1 | 14.7 | 20.1 | 21.7 | 15.5 | 26.5 | 35.9 | 17.8 | 15.5 | 28.9 | 25.4 | 22.5 | 9.6 | 12.9 | 20.1
Does not include power due to the gases exiting the cell. This is anticipated to add up to 20 mW excess power at the highest currents used. Currents used in increasing order: 0.150A, 0.300A, 0.500A.
Preliminary Results LEAP PdB Qualification Experiment #1

## Slide 43
Bubbles observed due to new design of cathode platform.
Validates institutionalization of replication of experimental instances.
Very minor details can effect experimental outcome or performance.

## Slide 44: “Dr. Imam's Pd-B cathodes have now shown excess heat using four different calorimeters”
China Lake with insulation ±20 mW
NRL Seebeck ±2 mW
F-P Dewar at NHE ±0.1 mW
Ridgecrest Copper Calorimeter ±3 mW
Mel Miles
Note: SRI International also measured a small excess heat with one of Dr. Imam’s Pd-B cathodes using their own Seebeck Calorimeter accurate to ±2-3 mW.

## Slide 45: LENRIA (Los Angeles) Development Lab Bench
Heater/Circulator for Water Bath
Techne, TE-10D, 1000 W
HP/Agilent 34970A Data Acquisition and Data Logger Switch Unit
HP/Agilent E34901A 20 Channel Multiplexer Module
HP/Agilent E34901A Multifunction Module
Built-in DMM Module
Keysight E36104A DC Power Supply
Accurate 35V, 1A, 35W DC power supply
Hewlett Packard All-in-One PC
23” Display LED Core i3 4170T 3.2GHz 4GB RAM - 23-q116
Waterbath
15 Gallon Glass Aquarium
(Washington, D.C. development work is going on in David Nagel’s GWU LENR Lab)

## Slide 51
BenchVue
Virtual Instrument Interface
Test Flow
Automation Sequences

## Slide 52
PdB 0.75% Ingot
84.6 grams Elliptical Shape
Created by Dr. Ashraf Imam
Circa ~1993 - 1995
To be swaged and annealed
into 4.7mm and/or 3mm rod

## Slide 53: Cathode Yield Pd-B 0.75% Ingot 84.6 grams
Diameter 4.7mm
X 20mm
Diameter 3.0 mm
X 20mm
= ~20 units
= ~49 units

## Slide 54: Four Quadrants of Performance
Input Power W
Excess Power (Gain %)
Low Power, Low Gain
High Power, Low Gain
Low Power, High Gain
High Power, High Gain
Best
Very Good
Pretty Good
Good
LEAP

## Slide 55
Calorimetric Analysis of a Heavy Water Electrolysis Experiment Using a Pd-B Alloy Cathode
M.H. MILES, M. FLEISCHMANN, M.A. IMAM

## Slide 56
Dave Nagel in San Leandro 1970’s

## Slide 57
LEAP: The LENRIA Experiment and Analysis Program
Progress
Conceived of the program.
Identified the experiment on which to base the program.
Completed the first qualification experiment.
Began the process of equipment modernization.

## Slide 58
LEAP: The LENRIA Experiment and Analysis Program
Plans
Complete all aspects of the system: Hardware, Software, Materials and Protocol.
Once we have everything in hand, we shall seek funding to clone the system.
In parallel we shall seek agreements with major laboratories to perform and document the experiment on a specified time scale.

## Slide 59
Steven B. Katinsky, David J. Nagel LENRIA Corporation
Melvin H. Miles, M. Ashraf Imam
12th International Workshop on Anomalies in Hydrogen Loaded Metals
5-9 June 2017
Hotel Langhe e Monferrato, Via Contessa di Castiglione, 14055 Costigliole d'Asti (AT), Italy
LEAP: The LENRIA Experiment and Analysis Program