Grant Agreement No: 101004761

AIDAinnova

Advancement and Innovation for Detectors at Accelerators

Horizon 2020 Research Infrastructures project AIDAINNOVA

deliverable report

Completion of Common Productions

Deliverable: D6.1

| Document identifier: | AIDAinnova-Del 6.1 |
| --- | --- |
| Due date of deliverable: | M 54 (September 2025) |
| Report release date: | 30/09/2025 |
| Work package: | WP6: Hybrid Pixel Sensors for 4D Tracking and Interconnection Technologies |
| Lead beneficiary: | FBK, CNM |
| Document status: |  |

Abstract:

WP6 has as main deliverables the production and qualification of Hybrid Pixel sensors for excellent tracking and timing performance in future HEP experiments. LGAD and 3D sensors with optimized design have been chosen as best candidates.  Production has been organized by sharing it over two vendors, FBK and CNM, for a total of four common productions. Status and quality of the deliverables is summarized.

AIDAinnova Consortium, 2025

For more information on AIDAinnova, its partners and contributors please see http://aidainnova.web.cern.ch/

The Advancement and Innovation for Detectors at Accelerators (AIDAinnova) project has received funding from the European Union’s Horizon 2020 Research and Innovation programme under Grant Agreement no. 101004761. AIDAinnova began in April 2021 and will run for 4 years.

Delivery Slip

|  | Name | Partner | Date |
| --- | --- | --- | --- |
| Authored by | Anna Macchiolo Claudia Gemme Giulio Pellegrini | U. Zurich INFN Genova | dd/mm/yy |
| Edited by | Anna Macchiolo Claudia Gemme | U. Zurich INFN Genova | 30/09/2025 |
| Reviewed by | Giovanni Calderini [Scientific coordinator] | [CNRS] | 20/10/2025 |
| Approved by | Giovanni Calderini [Scientific coordinator] Steering Committee |  | 7/11/2025 |

Table of Contents

1.	Introduction	4

2.	COMMON PRODUCTIONS IN FBK	4

2.1.	Trench-3d production at FBK	4

2.2.	TI-LGAD production at FBK	6

3.	Common productions at CNM	7

3.1.	Design and fabrication of iLGAD devices at IMB-CNM	8

3.2.	3D sensors productions at CNM	12

4.	FUTURE PLANS / Conclusion / relation to other AIDAInnova work	15

Executive summary

WP6 has as main deliverables the production and qualification of Hybrid Pixel sensors for excellent tracking and timing performance in future HEP experiments. One of the main goals has been the production of LGAD and 3D sensors, with runs both at FBK and CNM. The design and technological choices were based on simulations, and previous experiences, as well as future uses of the produced parts.

FBK has produced 3D and LGAD with very encouraging results. Due to contingent problems in the cleanroom, CNM has produced engineering runs only.

# Introduction

WP6 has as main deliverables the production and qualification of Hybrid Pixel sensors for excellent tracking and timing performance in future HEP experiments. One of the main goals has been the production of LGAD and 3D sensors, with runs both at FBK and CNM. The design and technological choices were based on simulations, and previous experiences, as well as future uses of the produced parts.

FBK has produced 3D and LGAD with very encouraging results. Due to contingent problems in the cleanroom, CNM has produced engineering runs only.

The results of the characterization are discussed in the report of D6.2 on the validation of the WP6 common productions. In the following the description is primarily focussed on what has been produced.

# COMMON PRODUCTIONS IN FBK

## Trench-3d production at FBK

3D silicon sensors with trenched electrodes have been fabricated by Fondazione Bruno Kessler (FBK) within the framework of Work Package 6 (WP6) of the AIDAInnova project. The main objective of this production was to realize a batch of 3D sensors featuring trenched electrodes, designed for high timing and spatial resolution in hybrid pixel detectors for future high-energy physics experiments.

Following the completion of the design and layout definition in 2022 [1], the fabrication run was executed and finalized in May 2024. The main goals of the production were to validate the technological process for 3D-trench sensors, to fabricate structures compatible with upcoming 28nm readout ASICs such as IGNITE and Picopix, and to produce a complete set of test structures for detailed electrical and timing characterization.

The fabrication employed stepper lithography with a reticle area of approximately 4 cm². 14 wafers were produced with the sparse layout, including 18 reticle shots, and 4 wafers were processed with the full layout, with 29 shot exposures. The two layouts are sketched in Fig 1a. The device density is therefore largely increased with respect to previous experiences. Different trenches poly filling techniques have been tested at wafer level as detailed in Fig.1b.

Fig. 1: Left: Sparse and full layout implemented in the FBK 3D production, Right: List of wafers splitting.

Fig. 2: Sketch of different 3D-trench pixels: a) continuous ohmic trench, b) dashed ohmic trench (gap between the read-out trenches=15 μm, gap between the ohmic trenches=10 μm).

Two different options have been implemented for the ohmic trenches, either continuous (STD) or dashed (DSH). The two concepts are sketched in Figure 2.

The baseline pixel size is 55 μm x 55 μm and a few matrixes have been implemented: 32x32, 64x64 and 128x128 pixels. Additionally, device test structures, with groups of individual pixels, strips or diodes, have been implemented, with pitch of 55 and 42 μm, and STD and DSH trenches. The individual reticle with all these structures is shown in Figure 3.

Fig. 3: Layout of the single reticle

While more results will be reported in the D6.2 report, the main results of this production are that the wafer bow is well below 20 μm for the splits (this was one of the main concerns after the TimeSPOT production) and the yield is pretty large, ranging from 80-90% on the smaller matrixes to 35% on the largest ones, in general slightly larger for the dashed with respect to the standard trenches. Few wafers have been sent to IZM for bump deposition, while a few have been cut in FBK to provide dice for first tests, irradiation and test beam activities.

## TI-LGAD production at FBK

The TI-LGAD fabrication employs a process flow on high-resistivity p-type silicon substrates with active thicknesses of 45 and 55 μm. The process integrates etching of shallow trenches to achieve electrical isolation between pixels. The trench design minimizes the no-gain region between pixels to values as low as 2–10 μm, corresponding to fill factors greater than 80%. A sketch of this sensor is shown in Figure 4. The production used stepper lithography with a reticle area of approximately 2×2 cm², shown in Figure 5, repeated across the wafer surface. The processing sequence includes trench etching, filled with dielectrics. Carbon co-implantation in the gain layer was applied in a fraction of the wafers, to enhance radiation hardness and improve performance by suppressing the diffusion of the gain layer and preventing acceptor removal under irradiation.

Fig. 4: Sketch of Trench-Isolated LGADs

The TI-LGAD production includes multiple pixel matrix geometries and test structures. The baseline design features pixels with 55 μm × 55 μm pitch arranged in matrices compatible with various readout ASICs. The main matrix configurations are: 1×1 cm² arrays for Timepix4 compatibility, 32×32 and 64×64 pixel arrays compatible with IGNITE and Picopix chips, and simpler pad structures designed for wire-bonding. A 5×5 matrix of 1.3×1.3 mm² pads was implemented for compatibility with the existing timing ASICs, ALTIROC and ETROC, for the HGTD and ETL sub-detectors in CMS and ATLAS.

Figure 5: Layout of the ~2x2 cm2 reticule in the FBK TI-LGAD production

Several technological splits were included in the production, as summarized in Table 1. Variations were introduced in the trench depth and process (D1–D3 options) and in the use of carbon co-implantation in the gain layer.

Table 1: Process splits for the TI-LGAD production

The production was completed in October 2023 with a very good yield. Three wafers have been diced without UBM deposition and the structures distributed among several AIDAInnova groups.

The remaining 9 wafers have been sent to IZM Berlin for processing of the Under Bump Metallization and then diced. The structures of these wafers have been distributed, characterized stand alone or connected to Timepix3 and Timepix4 chips. Further structures will be connected to the IGNITE prototype chips.

# Common productions at CNM

## Design and fabrication of iLGAD devices at IMB-CNM

IMB-CNM has designed and fabricated a new mask-set for inverted LGAD (iLGAD) sensors. This technology has been optimized with Sentaurus TCAD simulation toolkit. The sensor has a 100% fill factor and the active area can be maximized thanks to the trench isolation technique. The technology and the mask-set are shown in the following image.

Figure 6: Technological sketch and Layout of the wafer

In an iLGAD, the multiplication layer is fabricated over a thick (> 250 µm) low resistivity n-type handle wafer, as shown in Figure 6. Unlike the standard LGAD, the JTE is replaced by a deep trench etched from the pixelated side of the wafer, enabling single-sided photolithography processes and the reduction of the device active thickness, set by the thickness of the high resistivity p-type layer, for timing applications while maintaining a 100% fill factor.

iLGAD sensors were first manufactured at IMB-CNM on 100 mm and 50 μm active thickness Si-Si and epitaxial wafers. This fabrication aimed, among other goals, to develop pixelated detectors for tracking and timing applications with small pixel pitches (<55 μm).

Figure 7: On the left it is shown the top view of a filled trench while on the right the photo of the first iLGAD wafer fabricated at CNM.

The first results of this fabrication were that the trench width (in Figure 7) played a key role in the periphery’s stability. The wider the trench, the higher the breakdown voltage of the device, which is a direct consequence of having a larger amount of dielectric material smoothing the electric field at the core edge. Nevertheless, wider trenches present a drawback from a technological standpoint, as they are more difficult to fully fill with deposited SiO2 and polysilicon. Additionally, they complicate subsequent photolithography processes, as the photoresist would slip through partially filled trenches.

The CNM mask was modified to include trenches with a width of 8 μm, which would theoretically ensure a breakdown voltage over 300 V, enough for operating the device, while maintaining a sufficiently narrow trench to try to avoid the technological issue. On the other hand, it was found that the trench would necessarily need to be in direct contact with the P++ layer, otherwise, edge electric field effects would cause an earlier breakdown at the gap between it and the trench. Two types of wafers (Si-Si and epitaxial) were used to manufacture the first iLGAD prototypes, each requiring a different design approach.

Si-Si wafers were obtained by metallurgically bonding two 300 μm FZ wafers: an n-type low-resistivity wafer (phosphorus-doped) that serves as the handle wafer, and a p-type high-resistivity wafer (boron-doped). The latter was implanted with boron prior to the bonding process to create a deep multiplication layer. The manufacturing process for epitaxial wafers differs significantly from that for Si-Si wafers. In this process, two epitaxial layers are tailored onto a low-resistivity n-type substrate. First, the multiplication layer is created via epitaxial growth onto the 450 μm thick n-type low-resistivity substrate (arsenic-doped). Subsequently, a high-resistivity epitaxial p-type layer is grown onto the multiplication layer. A complete set of simulations was carried out with Sentaurus TCAD to find the optimum parameters for the fabrication as shown in Figure 8.

Figure 8: Sentaurus TCAD parameter optimization

iLGAD detectors were investigated for their gain response when exposed to IR light of 1064 nm. The result shows the signal response of both the iLGAD and the reference PiN at reverse biases of 20, 21, and 22 V.  Figure 9 presents the gain response of the iLGAD over the voltage range. The results indicate a clear Geiger behaviour of the studied ILGAD, as the gain response is boosted from 0 to 50 in less than one volt.

Figure 9: Signal (A) and gain (B) responses to TCT IR light of 1064 nm wavelength for a iLGAD device and a reference PiN

Figure 10: 2D map of the average TCT signal amplitude for the iLGAD at 20.5 and 22 V.

Figure 10 shows a 2D map of the average TCT signal amplitude for the iLGAD at reverse biases of 20.5 V and 22 V. At 20.5 V, the average gain for IR light is ≈2.5, indicating that the device is operating in linear (LGAD) mode. The 2D scan demonstrates that, while in linear mode, the trenches effectively serve their isolating purpose, as no signal is detected at the device periphery. In contrast, at 22 V, the average gain exceeds 50, and the device operates in Geiger mode. At this voltage, charge injection is observable from all areas of the device, even when the laser beam is projected on the reflecting metal layer. Moreover, the 2D map clearly shows that breakdown occurs at the trenches, where the amplitude of the signals is even higher than the photo-generated signals at the core.

The second fabrication of iLGAD included Timepix4 large area sensors as shown in figure 11. This run focused on finding a better thermal process, for both wafers, to obtain LGAD behaviour rather than APD or PiN.  Although there was an improvement of the breakdown voltage, going from 20 to 40V, as shown in Figure 12, this may not be enough to operate detectors under high irradiation fluences.

Figure 11: left leakage current measurements of the second iLGAD fabrication. Right, photo of the fabricated wafer.

Figure 12: TCT Laser Measurements of the second iLGAD fabrication obtained with a blue 404 nm laser. On the left it is shown the wafer mapping in the metal opening, on the right the signal amplitude at different bias voltages.

Finally, a new mask set was designed at CNM to solve the limitation of the Geiger mode regime of the iLGAD which includes detectors with the following geometries, as shown in Figure 13:

- TimePix4. 55x55 µm pitch, 448x512 pixels: total 2

- TimePix3. 55x55 µm pitch, 256x256 pixels: total 4.

- iStrip. 80 µm pitch, 20 strips

- Pad. 1300x1300 µm, 3000x3000 µm

The fabrication of this new run has been delayed by the supplier of the wafers. At the moment, CNM still has not received the epitaxial wafers with the multiplication layer optimized reduce the Geiger mode regime and operate as predicted by simulation.

Figure 13: CNM1225 Mask set for Timepix4 and Timepix3 iLGAD third fabrication run

## 3D sensors productions at CNM

IMB-CNM 3D timing detectors were fabricated using a double-sided process that improved yield and simplified processing. Wafers were high-resistivity float-zone p-type silicon with resistivity above 5 kΩ·cm and a nominal thickness of 285 µm ±10 µm, as shown in figure 14. The sensors employed columnar 3D electrodes etched through the wafer with hole diameters of 8–10 µm, and used p-stop isolation between pixel implants to control inter-pixel leakage and isolation. The back side included a metal opening to facilitate contact and routing, delivering fast charge collection, radiation tolerance, and processing reliability suited for timing applications.

Figure 14: Left: cross section of a 3D double sided detector. Right: Mask design of the fabricated detectors.

Two different pixel geometries—orthogonal and hexagonal—were investigated to study the timing performance of 3D detectors after irradiation. A complete set of Sentaurus TCAD simulations was carried out to analyse the electric field distribution within each design, with the results of the three-dimensional simulations shown in figure 15. The hexagonal configuration consisted of two pixels, while the orthogonal design featured a single pixel. In the 3D detectors strong electric fields are seen near the n-columns and comparatively lower fields between the pixels. Various design parameters were explored to optimize the uniformity of the electric field across the active area. Since full Monte Carlo simulations are required to estimate the time resolution, the comparison between designs was based on the fraction of the pixel area exhibiting an electric field above a defined threshold. Across the entire threshold range, the hexagonal geometry consistently showed a higher percentage of area above the threshold, indicating a more uniform electric field distribution.

Figure 15: Left: cross section of a 3D double sided detector with a hexagonal columnar structure and an inter column distance of 30µm; Middle: cross section of a 3D double sided detector with a hexagonal columnar structure and an inter column distance

Figure 16: Time resolution versus bias voltage of 3D detectors and LGADs before and after irradiation

The characterization of the 3D detectors focused on assessing their timing performance before and after irradiation. Measurements of time resolution as a function of bias voltage were performed on orthogonal-pixel sensors irradiated to fluences of 1x1015neq/cm2and 5x1015neq/cm2. The studies were carried out with a 90Sr set-up, with a LGAD detector and a scintillator as timing references. The results, shown in figure 16, show that the irradiated 3D detectors maintain excellent timing capability, achieving time resolutions comparable to those of unirradiated LGADs when operated at optimal bias. This demonstrates the strong radiation hardness of the 3D design and its potential for operation in high-luminosity environments.

Time-of-arrival (ToA) studies were performed using the two-photon absorption (TPA) technique to investigate the spatial uniformity of the timing response. Due to the intrinsic geometry of the 3D electrodes, the timing resolution exhibits position dependence, making the ToA analysis a key factor to understand the detector performance. The TOA plots for both designs are shown in figure 17. The orthogonal pixel structure shows a narrower ToA spread of approximately 75 ps, compared to around 175 ps for the hexagonal design. It should be noted that the hexagonal structure features a larger active area, which likely contributes to the broader distribution.

Figure 17: Left: TOA vs position map of an orthogonal pixel; Right TOA vs position map of a hexagonal pixel

A new mask has been designed to include the new timing chips that are designed for future experiments (Picopix and Velopix, Timespot and Timepix4)). The fabrication of this new run has started and will be ready in 2026.

# FUTURE PLANS / Conclusion / relation to other AIDAInnova work

Beyond the results summarized here, more details on the sensor performance will be provided in the D6.2 report.

For the FBK wafers, so far, the tests have been concentrated on the test structures with a few diodes/pixels/strips. More tests will be possible as soon as new readout chips matching the pitch and matrix sizes and providing excellent timing performance will be available.

For CNM, the experience collected with the engineering runs, will support new productions with the same pixel matrices used in FBK to be hybridized to the same new generation of readout  chips.

Fast hybridization with ACF techniques as developped inWP6 will also be pursued, as they allow a fast-track dice to dice, that is optimal at this stage of the R&D programs.