Synthesis, XRD, EMR, magnetic, and optical studies of trigonal and triclinic dinuclear MNM-analogous Gd3+ complexes

Dawid Marcinkowski,a# Marta Fik-Jaskółka,a# Adam Gorczyński,a Violetta Patroniak,a Maciej Kubicki,a Ireneusz Stefaniuk,b Magdalena Wencka,c Muhammed Açıkgöz,d* Maria Korabik,e Mirosław Karbowiak,e Czesław Rudowicz,a*

a Faculty of Chemistry, Adam Mickiewicz University, Uniwersytetu Poznańskiego 8, 61-614 Poznań, Poland.

b Institute of Materials Enginering, College of Natural Sciences, University of Rzeszow, Rejtana 16a, 35-310 Rzeszów, Poland

c Institute of Molecular Physics, Polish Academy of Sciences, Mariana Smoluchowskiego 17, 60-179 Poznań, Poland

d Department of Science, The State University of New York (SUNY) Maritime College, New York 10465, USA.

e Faculty of Chemistry, University of Wrocław, F. Joliot-Curie 14, 50-383 Wrocław, Poland

* Corresponding authors’ e-mails: <czeslaw.rudowicz@amu.edu.pl> (C. Rudowicz); <macikgoz@sunymaritime.edu> (M. Açıkgöz)

#Equal contribution of the two authors

ABSTRACT:

Two structurally similar dinuclear Gd3+ complexes are newly synthesized as potential molecular nanomagnets (MNMs): [Gd2(L1)3](NO3)3 (1 symmetric) and [Gd2(L2)3(NO3)3] (2 dissymmetric). Characterization by variety of experimental techniques: XRD, EMR, magnetic measurements, and optical spectroscopy was carried out. The EMR and magnetic measurements reveal that the two Gd3+ complexes show very weak exchange interactions. Hence these complexes can be classified as the MNM-analogous complexes. The zero-field splitting (ZFS) parameters bkq were fitted from EMR spectra using the forms of the zero-field splitting Hamiltonian (HZFS) suitable for Gd3+ ions at various symmetry sites. This enabled exposing the role of site symmetry for proper interpretation of spectroscopic and magnetic properties of these Gd3+ complexes. Several fitting schemes were employed to investigate the role of each k-rank bkq's for Gd3+ ions. The distinction between actual (low/high) site symmetry and apparent (lower/higher) site symmetry was introduced. Since for triclinic site symmetry (complex 2), infinite number of physically equivalent ZFSP sets exist, to assess equivalence of independently obtained sets, we utilize the invariant quantities and standardization. Our findings clearly demonstrate the importance of the low and high symmetry aspects in EMR studies. This paper prepares grounds for an in-depth study of the symmetry aspects inherent in the modelled ZFSP sets. Elucidation of these aspects may help to improve understanding of these crucial aspects, which are frequently overlooked in literature, thus potentially yielding erroneous interpretations of compounds’ properties.

Keywords: EMR/EPR; XRD; magnetic measurements; zero-field splitting; dinuclear Gd3+ complexes; molecular nanomagnets; symmetry aspects.

1. Introduction

In the last decades molecular nanomagnets (MNMs) containing transition ions have been extensively investigated [,,,,,], including examinations by electron magnetic resonance (EMR), equivalently named electron paramagnetic resonance (EPR), techniques. MNMs display unique magnetic properties, which are particularly suitable for potential applications in quantum computing and spintronics [,,,,,,,,,]. Since, the classification of MNMs in the literature is still somewhat ambiguous, we adopt a clear distinction between three nominal groups of MNM compounds [], namely, (i) single molecule magnets (SMMs) and (ii) single chain magnets (SCMs), which both are formed by polynuclear clusters assembled from mononuclear coordination complexes, and thus belong to the large class of the exchange coupled systems (ECSs) [], (iii) single ion magnets (SIMs), which are formed by mononuclear complexes where transition ions are not coupled by exchange interactions. Often the SIM complexes are labelled as SMM ones, thus leading to terminological confusions as well as misinterpretations of MNM properties. The proposed classification of MNMs may alleviate such deficiencies.

Two distinct subgroups of SIM: A and B, should also be distinguished [17], since they are described by Hamiltonians having different physical origin [,,,], namely, the zero-field splitting (HZFS) and crystal field (HCF), respectively. This distinction is not well understood in literature, thus resulting in confusion concerning the meaning of associated Hamiltonians’ parameters [17]. The subgroup A SIMs encompass either (i) transition metal 3dN ions exhibiting an orbital singlet ground state with the spin S (equal 1, 3/2, 2, or 5/2), or (ii) the lanthanide 4f7 ions (Eu2+, Gd3+, Tb4+) exhibiting the ground spin multiplet 8S7/2 being an orbital singlet L = 0 with spin S = 7/2. Hence, the single-ion HZFS with spin S applies for the SIMs in the subgroup A. The subgroup B SIMs encompass other lanthanide 4fN ions with 2S+1LJ ground multiplet, hence HCF (HLF) applies. The subgroup A SIMs may be investigated by various EMR (EPR) techniques, whereas for the subgroup B SIMs only a few transitions are observable in the usual EMR frequency ranges. Importantly, unlike in the SMMs and the subgroup A SIM, the EMR transitions in the subgroup B SIMs occur between the lowest J-multiplet CF states and not between the spin states. Such transitions as well as mixing of the J-states by lower symmetry CF terms have been considered in several studies in the SIM/SMM area, see, Refs [,,]. The significant energy separation between the ground spin multiplet 8S7/2 of Gd3+ and the higher 2S+1LJ  multiplets is responsible for rather small magnitude of the zero-field splitting (ZFS) [,,,,,], i.e. the separation between the spin (mS) levels without an applied magnetic field, which is quantified by the ZFS parameters (ZFSPs) [19-22]. This weakness of ZFS affects the relaxation properties of Gd3+-based SMMs and SIMs. Computational modelling is also essential for understanding these properties, and thus the magnetostructural correlations. Knowledge of the ZFSPs enables relating the ground spin multiplets with magnetic and relaxation properties of MNMs [,,].

Gd3+ complexes have been investigated for prospective applications in quantum algorithms. To name a few examples: polyoxometalate-assemblies (POM) [,], metal-organic frameworks [] or asymmetric dimeric assemblies [,,,]. Mayans et al. [] suggested that the SIM behavior observed in Gd3+ ions could be associated with small conventional [19,20] ZFSP D ∼ 0.1 cm−1. Experimental and theoretical studies of ZFSPs in Gd3+ SIMs could shed light on magnetic relaxation processes, which may involve weak axial ZFS along with spin–lattice relaxation or phonon-bottleneck processes [37,39,40]. Gompa et al. [] using high-frequency and-field EMR determined ZFSPs (D, E) for 4f7 ions Eu2+, Gd3+, and Tb4+ in four homoleptic compounds at sites with approximate orthorhombic symmetry, whereas the actual site symmetry of the compounds is triclinic C1. Taran et al. [] determined several 'ligand field parameters’ (actually, the genuine ZFS parameters [19,20]) for Gd3+ in the SMMs complex Et4N[160GdPc2] using a combined µSQUID-EPR technique. Xu et al. [] investigated Gd(III) crystal as a candidate for a high-dimensional spin-qudit system with addressable transitions. Single crystal of the complex [Gd0.02Y1.98(pydc)6(H2pip)3]·20 H2O with Gd3+ (S = 7/2) ions at the C3 symmetry sites  was characterized by X-band EMR. Several 'crystal field parameters' (actually, the genuine ZFS parameters [19,20]) Bkq associated with the extended Stevens operators (ESO) Okq(S) defined in [,] were determined in [45]. To explain the effect of chemical modification in trigonal Gd(III) molecular qubits, Hansen et al. [] investigated EPR and the ‘CF splitting’ (actually, the genuine ZFS splitting [19,20]) of the ground multiplet of Gd(III) ion in Gd(trenovan) and Gd(trenpvan). They determined all ZFSPs Bkq admissible in HZFS for the C3 symmetry.

Motivation for this study stems from our ongoing research aimed at rational design of lanthanide-based MNMs and investigations of their properties [,,,,,,]. Hence, we synthesized and characterized two dinuclear Gd3+ complexes, intended as potential MNM, which display distinct site symmetry: trigonal C3 (complex 1) and triclinic C1 (complex 2). This study integrates a variety of experimental techniques, including crystallographic X-ray diffraction (XRD), X- and Q-band EMR, magnetic measurements, and optical spectroscopy (see, Appendix, Section SI). This paper prepares grounds for an in-depth study (in the forthcoming paper []) of the symmetry aspects inherent in the modelled ZFSP sets, which are frequently overlooked in literature. The EMR and magnetic measurements have revealed that the two Gd3+ complexes show very weak exchange interactions. This finding has been corroborated by the ab initio computations [56]. These complexes exhibit neither the magnetic relaxation observed in SMMs [1-6, 7-16], nor the slow magnetic relaxation, which is a characteristic feature of Ln-based SIMs [42,51,52]. Hence, the studied complexes 1 and 2 belong to a subgroup of polynuclear ECSs that sits in between SMMs and SIMs. We propose to classify this subgroup as the MNM-analogous complexes. Nominally, they may be classified under SMMs but their magnetic behavior is more akin to typical paramagnets.

2. X-ray structural characterization of Gd3+ complexes

While both complexes [Gd2(L1)3](NO3)3 (1) and {[Gd2(L2)3(NO3)3}2 (2) can be termed as dinuclear helicate architectures, their structural character is fundamentally different. In the highly symmetrical complex 1, three deprotonated L1 ligand molecules coordinate the two Gd3+ centers to form the C3-symmetrical [Gd2(L1)3]3+ complex cation, where two gadolinium ions lie on a threefold axis that coincides with one of the crystallographic axis. The metal-to-ligand ratio is 2:3 (asymmetric unit contains one ligand molecule and two one-thirds of the Gd3+ cations), each symmetry-generated ligand wraps around both gadolinium ions by two nitrogen atoms – from hydrazine and benzimidazole groups - and by bridging phenolate oxygen atom (Fig. 1a). In consequence, each lanthanide ion is nine-coordinated in a face-sharing distorted tricapped trigonal prismatic geometry (Fig. 1b), with nearly the same structural parameters, i.e. bond lengths and angles (see, Appendix, Section SII). The ligand molecules are significantly folded, in order to coordinate two relatively close metal centers (the Gd - Gd distance is 3.5733(7) Å), thus forming dinuclear triple-stranded helicates. The helicate charge is balanced by three non-coordinating NO3- anions(Fig. 1b). Benzimidazole amine protons do not dissociate, therefore, N-H···O and relatively short and linear C-H···O hydrogen bonds can be found in the crystal lattice, which join both cations and anions, thus resulting in creation of highly symmetric three-dimensional network described by R-3c space group (Fig. 1c). Inherent helical character of the system [] results in two sets of chiral isomers: right-) and  (left-handed) [Gd2(L1)3]3+ entities.

Fig. 1. a) Crystal structure of [Gd2(L1)3]3+ cation; b) Local enlarged view of coordination centre of complex 1; c) Crystal packing of complex 1 as seen along the threefold axis (z direction); d) Crystal structure of [Gd2(L2)3(NO3)3] complex 2; e) Local enlarged view of coordination centre of complex 2; f) Crystal packing of complex 2 as seen along the threefold axis (z direction).

They are adjacently distributed along the z axis to form quartets of columnar assemblies in a doublet i.e. fashion, thus forming a racemic mixture. Of interest is the fact that the structurally similar Robson type ligands [] crystallized in the monoclinic space group and only the pseudo-C3-symmetric environment could have been established therein [,]. The complex 2 can be termed as dissymmetric, because three deprotonated L2 ligand molecules bind the two Gd3+ cations in the dissimilar fashion, resulting in structurally different geometrical surrounding of each metal ion. So formed helical architecture can be described as [Gd2(L2)3(NO3)3] or more accurately as [(2-NO3)Gd(3-L2)2(3-L2)Gd(2-NO3)2] in which additional coordination of bidentate NO3- counterions is needed to maintain the 9-fold coordination of Gd3+ ions in the edge sharing fashion and distorted tricapped trigonal prismatic geometry (Fig. 1d and Fig. 1e). The dissymmetric character of the system is also observed in the asymmetric unit, where both  (right-) and  (left-handed) [Gd2(L2)3(NO3)3] enantiomers constitute crystallographically inequivalent entities (Fig. 1e). Three phenolic oxygen atoms are bridging two gadolinium centers (Gd···Gd distance is 3.4899(3) in the  and 3.4934(3) in the isomer. The coordination is completed by nitrogen atoms from L2 ligand (from hydrazine and benzoxazole moieties) and oxygens from nitrate anions: 4N/2O and 2N/4O for respective Gd3+ ion. Short contacts between molecules of the complex and additional acetonitrile and diethyl ether solvent molecules result in 3D supramolecular network and P-1 space group (Fig. 1f). The most important structural parameters for both complexes are provided in Appendix (Section SIII). The ligands L1 and L2 have different number of coordinating subunits and dissimilar donor atom compositions, which affects the symmetric/dissymmetric character of complexes and the symmetry around each Gd3+ cation.

3. EMR spectra and analysis

3.1. EMR spectra

Continuous wave EMR spectra were recorded in X- and Q-band frequencies at temperatures from 296 K down to 5 K. The experimental details concerning EMR measurements are provided in Appendix (Section SI). The EMR spectra recorded under varying conditions for complex 1 and 2 as well as the simulated spectra are presented in Appendix (Section SV.1.A and SV.1.B, respectively).

Complex 1:

Analysis of the recorded EMR spectra of Gd3+ ions in complex 1 in Fig. 2 and those provided in Appendix (Section SV.1.A) reveals specific spectral features. A double EMR line can be observed, which may be resolved into the main (i.e. narrow) component and a weaker (i.e. broad) one. However, the weaker component becomes more visible only at near helium temperatures 10K and 5K, since the intensity of the main component is significantly reduced. This finding is consistent with the crystallographic structure of complex 1 (see, Appendix, Section SIII).

Analysis of the temperature dependencies of the linewidth of the main and weaker components in Fig. S13 and Fig. S14, respectively, indicates presence of weak antiferromagnetic exchange interactions in complex 1. The weaker component behaves in accordance with the Boltzmann distribution, which is characteristic of isolated paramagnetic centers. In the low temperature range below 10 K the characteristics of the EMR spectrum changes significantly - instead of one strong line with accompanying weaker lines, some of which may originate from the ZFS terms, only the weaker lines appear in this range. Moreover, the nature and position of these lines agree with the simulated spectra provided in Appendix (Section SV.1.A). The appearance of seven lines indicates the spectrum of the fine structure from the isolated (weakly bound) Gd3+ (S = 7/2) ion. However, due to the overlapping of the lines and low intensity, it is not feasible to resolve the hyperfine structure of the spectra.

Fig. 2. Q-band EMR spectra of Gd3+ ions in complexes 1 (up) and 2 (bottom) measured in the temperature range 5 – 296 K.

Complex 2:

Analysis of the recorded EMR spectra of Gd3+ ions in complex 2 in Fig. 2 and those provided in Appendix (Section SV.1.B) reveals specific spectral features. The X-band spectra (Fig. S8 and Fig. S9) correlate well with the Q-band spectra (Fig. 2 and Fig. S17). In addition to the lines characteristic for Gd3+ ions, we observed additionally the so-called low-field microwave absorption (LFMA) lines. Generally, LFMA lines may be due either to non-resonant microwave absorption or resonant one that is related to magnetic properties. In the case of long range ordering of magnetic moments in the two antiferromagnetic sublattices of Yafet-Kittel type [,] the changes in the LFMA signal phase and those in the line shape may be considered as an indicator of antiferromagnetic interactions, see, Refs [,,,] and references therein. The temperature dependence of Q-band EMR spectra of complex 2 above 10 K reveals that the phase change of the LFMA-like signal is observed at 60K and then above 170K (see, Fig. S17). This suggests that this signal is most likely due to non-resonant absorption. In both complexes the exchange interactions determined by magnetic measurements are very weak, so that no long range order would be expected. However, at helium temperatures we clearly observe an increase in the intensity of the LFMA line for complex 2. This suggests that the lines below 10 K, see, Fig. S16, may be due to resonant absorption, thus indicating antiferromagnetic interactions. This is in agreement with the Curie-Weiss temperature determined by magnetic studies (see, Section 4). Detailed analysis of the LFMA line is beyond the scope of this study.

Comparison of EMR spectra for both complexes reveals that for complex 2 we observe a similar change in the character of the EMR spectrum as in complex 1. The fine structure of the spectrum at 5 K, which may originate from the weakly bound Gd3+ ion, is also visible in Fig. 2. However, in complex 2 a strong line is visible with g ≈ 2.00, which may suggest that only some of the ions are magnetically isolated, while others remain coupled by antiferromagnetic interactions.

3.2. Notations used for spin Hamiltonian parameters

For description of EMR (EPR) spectra [,,,] and the energy levels of the ground spin (S) state of paramagnetic transition ions exhibiting an orbital singlet ground state in crystals the effective spin Hamiltonian (SH) [19-22] is utilized. The prevailing SH notation, including the Zeeman electronic (Ze) terms (S  1/2), and the zero-field splitting (ZFS) terms (S  1), used for higher spin systems is:

HSH=HZe+HZFS=μBB∙g∙S+k=2,4,6q=-k+kBkqOkqSx,Sy,Sz=μBB∙g∙S+k=2,4,6q=-k+kfkbkqOkqSx,Sy,Sz, 							(1)

where g is the spectroscopic splitting factor (dimensionless),  - Bohr magneton, B - the applied magnetic field (in fact the magnetic induction (or the magnetic field intensity [,,], denoted for short: B-field or B), S - the effective spin operator, whereas Bkq and bkq are the ZFSPs associated with Okq(S) - the extended Stevens operators (ESO) [46,47]. The scaling factors [19-22] are fk = 1/3 , 1/60, and 1/1260 for k = 2, 4, and 6, respectively. The limit to the even ranks k (k  2S) for the operators acting within the ground spin S multiplet yields for Gd3+ (4f7, 8S7/2) centers: k = 2, 4, and 6. Eq. (1) including all q components: -k  q  +k is suitable for triclinic symmetry, whereas specific limits on the non-zero components q for higher symmetry cases are governed by the group theory. Explicit HZFS forms for all 32 point symmetry groups describing possible local site symmetries in crystals may be found in Misra [,70].

For the S  1 centers at orthorhombic symmetry sites the Ze g-tensor comprises three gi factors: (gx, gy. gz). The same applies for lower symmetry sites if the g-tensor is expressed in its principal axis system (PAS-g). The orthorhombic 2nd-rank ZFS term contains only two ZFSPs:

HZFS=B20O20+B22O22=13b20O20+b22O22=DSz2-13SS+1+ESx2-Sy2,		(2)

The same applies for lower symmetry sites if the D-tensor (S.D.S) is expressed in its principal axis system (PAS-D). The third form Eq. (2) represents the orthorhombic-like 2nd-rank ZFS terms in the conventional notation [19-22]. The conversions between the 2nd-rank ZFSPs expressed in different notations are:

D=3B20=b20, E=B22=1/3b22. 							(3)

The notation bkq is adopted as the reference notation for presentation of the ZFSP sets in this study.

For the trigonal C3 site symmetry around the two Gd3+ centers in complex 1 the only non-zero ZFPs in Eq. (1) are: ; , , ; , , , , , whereas for the approximated symmetry C3v the ZFPs bkq with negative q components vanish. The explicit forms of HZFS in Eq. (1) for monoclinic and triclinic symmetry are given in Appendix (Section SIV.1). For analysis of EMR spectra for the four Gd3+ centers in complex 2, we use the monoclinic form of HZFS with C2||Oz.

3.3. Fitting and simulations of EMR spectra

The fitting and simulations were performed using the program EasySpin [,], whereas for verification the program Visual-EPR [,] was also used. The general procedures used for both complexes 1 and 2 are outlined in Appendix (Section SV.1). In view of the large number of the fitted ZFSP sets, here we provide the partial Tables listing only selected ZFSP sets with rank k = 2 and 4. The full Tables containing all fitted ZFSP sets for complex 1 and 2 are listed in Appendix (Section SV.1.A and SV.1.B, respectively). This ensures succinct presentation of datasets herein as well as facilitates analysis of the results. The selected sets of the Zeeman gi factors and ZFSPs fitted using HZFS of specified symmetry are listed in Table 1 (extracted from Table S6) and Table 2 (Table S8 and S9) for Gd3+ ions in complex 1 and 2, respectively.

Table 1

The selected trigonal (C3 symmetry) SHPs fitted to the main component of the Q-band EMR line for Gd3+ ions in complex 1: gi factors and ZFSPs bkq (in 10-4 cm-1); two fitting schemes are utilized with bkq: (a) k = 2, 4, 6 and (b) k = 2 and 4 only, using as starting parameters ZFSP values close to zero.

| T [K] | 295 | 295 | 10 | 10 |
| --- | --- | --- | --- | --- |
| Set | C3 (a) | C3 (b) | C3 (a) | C3 (b) |
| g1 | 1.991 | 2.019 | 2.036 | 2.035 |
| g2 | 1.992 | 1.935 | 2.08 | 2.08 |
| b20 | 161.73 | 153.20 | 161.29 | 146.00 |
| b40 | 6.02 | 25.99 | -13.35 | -31.87 |
| b43 | 19.86 | 22.41 | 4.01 | 16.01 |
| b4-3 | 0.62 | 12.10 | 13.52 | 2.00 |

Attempts to fit for Gd3+ ions in complex 2 all ZFSPs for triclinic symmetry have failed yielding unreliable ZFSPs due to convergence problems arising from large number of ZFSPs. Hence, we used HZFS for the approximated higher monoclinic symmetry with C2||Oz [21,22] and orthorhombic, see, Table 2 (Tables S20, S21, and S22). For the orthorhombic ZFSPs we also provide the rhombicity ratio λ'=  b22/b20 [] calculated using the package CST [,]. All values of λ’ are in the standard range, thus adhering to the convention implicitly used in EMR area [67-74]: 0 < λ = E/D < 1/3, i.e. equivalently 0 < λ’ < 1.

Table 2

The selected SHPs fitted to the EMR X- and Q-band spectra for Gd3+ ions in complex 2: orthorhombic gi factors, monoclinic and orthorhombic ZFSPs bkq (in 10-4 cm-1); two fitting schemes are utilized with bkq: (a) k = 2, 4, 6 and (b) k = 2 and 4 only, using as starting parameters ZFSP values close to zero.

| Complex 2 – monoclinic ZFSPs |  |  |  |  |  | Complex 2 – orthorhombic ZFSPs |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| T [K] | 300 | 300 | 10 | 10 |  | 300 | 300 | 10 | 10 |
| Set | X (a) | X (b) | Q (a) | Q (b) |  | X (a) | X (b) | Q (a) | Q (b) |
| g1 | 1.958 | 1.950 | 1.923 | 1.923 |  | 1.95 | 1.98 | 1.92 | 1.92 |
| g2 | 1.983 | 1.987 | 2.002 | 2.002 |  | 1.99 | 1.98 | 2.0 | 2.0 |
| g3 | 1.985 | 1.989 | 2.002 | 2.002 |  | 1.99 | 1.96 | 2.0 | 2.0 |
| b20 | 153.05 | 149.82 | 154.69 | 158.23 |  | 111.28 | 155.84 | 160.21 | 148.65 |
| b22 | -30.02 | -30.31 | -28.71 | -27.35 |  | -62.67 | -56.91 | -28.67 | -28.29 |
| b2-2 | 26.35 | 28.48 | 27.38 | 24.79 |  | - | - | - | - |
| b40 | 5.51 | 4.70 | 4.59 | 4.52 |  | 2.68 | 2.8 | 4.33 | 4.26 |
| b42 | -6.22 | -6.45 | -6.16 | -6.40 |  | -6.42 | -6.46 | -6.49 | -6.76 |
| b4-2 | 4.79 | 4.60 | 4.93 | 4.30 |  | - | - | - | - |
| b44 | 9.67 | 9.75 | 10.16 | 9.95 |  | 10.57 | 9.74 | 9.59 | 9.78 |
| b4-4 | 9.14 | 8.78 | 9.11 | 8.52 |  | - | - | - | - |
| λ’ | - | - | - | - |  | -0.563 | -0.365 | -0.179 | -0.190 |

An in-depth discussion of the results of fitting and simulations of EMR spectra for Gd3+ ions in complex 1 and 2 is provided in Appendix (Section SV.1.A and SV.1.B, respectively). This includes, e.g. the following issues [56]: (i) the role of each k-rank ZFSPs bkq for Gd3+ ions in the two complexes; (ii) the orthorhombic and monoclinic [,], as well as triclinic [], standardization of ZFSP sets; (iii) the invariant quantities [,]. The issues (ii) and (iii) are crucial for proper interpretation and analysis of experimental and computed ZFSP sets for low site symmetry EPR centers in crystals, which were obtained by various methods or taken from various sources. The importance of the issue (ii) resides in the fact that proper standardization [79-84] must be performed to enable direct comparison of the low symmetry ZFSP sets, like those in Table 2 (and Table S8 in Appendix). The usefulness of the issue (iii) resides in the fact that the invariant quantities [83-86]: Sk and Ei (k = 2, 4, 6), enable to assess the degree of physical equivalence of the various ZFSP sets determined by various methods for high and low symmetry cases. Sk measure indirectly the magnitude of ZFS of a given rank k, whereas Ei are the ZFS energies within the ground spin multiplet (like the S = 7/2 multiplet of Gd3+ ion)

Comparison of the fitted ZFSPs in Table 1 and 2 with the ZFSPs reported for Gd3+ ions in selected Gd3+–O2− complexes collected in Appendix (Section SV.2) as well as with the experimental ZFSPs compiled in EMR reviews [26-31] indicates their mutual compatibility, especially for ZFSPs obtained from EMR spectra at room temperature. Our survey of recent experimental and theoretical studies of Gd3+ compounds has revealed several SHP sets determined for potential MNMs. These ZFSP sets were converted from the original notation (and units)  to that used here, i.e. bkq (in 10-4 cm-1), and are collected in Table 3. For conversion from the original Bkq’s we apply the scaling factors fk given in Eq. (1). Comparison of the magnitudes of the ZFSPs in Table 1 and 2 with those in Table 3 indicates that the fitted ZFSPs are well comparable with the reported ones, albeit overall somewhat lower.

Table 3

The gi and ZFSP values, recently reported for Gd3+ complexes studied as potential MNM, converted to bkq (in 10-4 cm-1).

| Compound [Ref.] | Site symmetry | gi | b2q | b4q | b6q |
| --- | --- | --- | --- | --- | --- |
| [NiGd(L)(NO3)3] (1), [NiGd0.15Eu0.85(L)(NO3)3] (2) Mayans et al. [42] | - | 2.00 | b20=1100 | - | - |
| C64H148GdKN16O2P4 Gompa, et al. [43] | triclinic C1 | 1.990 | b20= 860 b22= 180 | - | - |
| C296H656Gd4K4N72O24P16 Gompa, et al. [43] | triclinic C1 | 1.990 | b20= 180 b22= 50 |  |  |
| Et4N[160GdPc2] Taran, et al. [44* | D4d | 1.96 | b20= -681 b22= -275 | b40= -31.4 b44= 67.6 | b60= -0.067 |
| [Gd0.02Y1.98(pydc)6(H2pip)3]·20 H2O Xu, et al. [45]* | C3 | gꞱ =1.985 g¦¦ =1.975 | b20= ±315 | b40= ∓1 b43= ±160 b4-3= ∓160 | b60= ∓0.28 |
| Gd0.005Y0.995 (trenovan) Hansen, et al. [48] | C3 | 2.00 | b20= 642 | b40= 25.2 b43= -410 b4-3= -35 | - |
| Gd0.005Y0.995 (trenpvan) Hansen, et al. [48] | C3 | 2.00 | b20= 269 | b40= 27.8 b43= -464 b4-3= -38 | b60= 7.72x10-2 b6-3= 4.088 b66= 3.71 |

* The values in Hz are converted using 29.9792458 GHz/cm−1 conversion factor.

The high degree of compatibility of the SHPs obtained for Gd3+ ions in complex 1 and 2 with pertinent SHP sets identified due to extensive literature survey in Table 3 and in Appendix (Section SV.2) corroborates the reliability of the fitted ZFSP values in Table 1 and 2.

3.4. Symmetry aspects inherent in the fitted ZFSP sets

For the sake of lucidity, an outline of key notions pertinent for the low symmetry aspects [22,56] are presented in Appendix (Section SIV.2). This includes [22,56]: the notions of low and high actual site symmetry, the distinction between the actual site symmetry cases and the apparent site symmetry cases, and the axis systems appropriate for the MLn polyhedra. Utilizing the experimental results obtained herein, an in-depth study of the symmetry aspects inherent in the ZFSP sets modelled for the Gd3+ complexes 1 and 2 is carried out in [56] employing semiempirical approaches and the ab initio methods.

Analysis of the results presented in Sections 3.1 and 3.3 and in Appendix (Section SV) allows to draw the following observations. The close match between the experimental Q-band EMR spectra for Gd3+ ions in complex 1 and the spectra simulated using the fitted trigonal ZFSP sets indicates that the actual C3 or approximated C3v site symmetry is appropriate.

Discrepancies between the symmetry reflected by fitted ZFSP sets and the actual site symmetry may imply an apparent site symmetry. The valid apparent site symmetry cases may emerge from judicious application of an approximated HZFS with a smaller subset of ZFSPs then admissible by PSG. In EMR studies, the actual site symmetry is often approximated by a higher site symmetry for computational convenience. In our case, for complex 2, due to large number of triclinic ZFSPs, fitting using the actual C1 symmetry yielded unreliable ZFSPs. Hence, in the subsequent fitting rounds for Gd3+ centers in complex 2, instead of triclinic HZFS, we utilized the approximated monoclinic (Table S8) and orthorhombic (Table S9) ZFSP sets. Such approximations do not compromise interpretation of structural data, provided that they are transparently stated.

However, using an incorrect fitting procedure may result in invalid apparent site symmetry cases. In EMR studies, HZFS form used for fitting is sometimes selected based on the crystal's space group symmetry [22]. Hence, the Cartesian crystallographic axis system (CAS) or modified CAS (CAS*) is adopted without giving consideration to the symmetry-adapted axis system (SAAS) (or limited SAAS) suitable for the actual site symmetry. However, the simplest forms of HZFS (HCF), i.e. with the minimal number of physically independent adjustable ZFS (CF) parameters, are obtained in SAAS (limited SAAS) suitable for a paramagnetic center [19-22]. Hence, this selection is justified only if CAS (or CAS*) coincides with SAAS (or limited SAAS). If this condition is not satisfied, then for complexes with the high actual site symmetry the fitted ZFSP sets may reflect the triclinic-like symmetry, which would be merely apparent and not genuine. Comparative analysis of the apparent site symmetry cases reflected by the fitted and modelled ZFSP sets for Gd centers in complexes 1 and 2 will be provided in [56].

3.5. Temperature dependencies of EMR spectra

The major parameters characterizing EMR lines, i.e. the peak-peak linewidth (Bpp), EMR line intensity (I), and the resonance field (Br), were determined from the recorded EMR spectra for complex 1 and 2 in Appendix (Section SV.1.A and SV.1.B, respectively). The temperature dependence of Bpp for complex 1 measured for the main and weaker components of the Q-band EMR line, whereas for complex 2 measured for one EMR line are presented in Appendix (Section SV.3). The analysis of temperature dependencies of the reciprocal of the total EMR spectrum intensity, and thus magnetic properties, was performed based on double integration of the EMR spectrum and the Curie-Weiss law [,]:

χ=CT-								(4)

In Eq. (4), C is the Curie constant, T - temperature, the constant   (called also the paramagnetic Curie point [82,83]) depends on the type of magnetic material and indicates either ferromagnetic interactions for  > 0 or antiferromagnetic interactions for  < 0. In nearly whole temperature range both complexes are paramagnetic, but broadening of the EMR linewidth indicates presence of weak antiferromagnetic exchange interactions. This is corroborated by DC magnetic measurements in Section 4. Below 10K magnetic behavior depends slightly on site symmetry. In complex 1 (symmetric) magnetically isolated Gd3+ centers are well observed, whereas in complex 2 (dissymmetric) it is less visible.

These measurements allowed us to determine the EMR line broadening (ΔB), i.e. the spin-phonon part of the EMR linewidth. Using Eqs. (S4) and (S5) in Appendix (Section SV.3), derived based on the Orbach process [], the temperature dependence of the spin-lattice relaxation times T1 were determined in complex 1 and 2 (see, Fig. S12). The best fit yields the energy splitting between the ground Gd3+ state and the first excited state δ = 179 cm-1 and the constant characteristic of the Orbach process A = 0.42x1010 [s-1] for 1, whereas δ = 168 cm-1 and A = 0.49x1010 [s-1] for 2.

4. DC magnetic measurements

For the S-state Gd3+ (4f7) ions the orbital angular momentum L is completely quenched, thus yielding the ground S = 7/2 multiplet 8S7/2 with 8-fold spin degeneracy. The first excited state is about 104 cm-1 above and is only slightly affected by the crystal field [27-30, 43]. For Gd3+ ions in axial or lower symmetry sites the ground spin state is split into four Kramers doublets |S = 7/2, ±MS> even in the absence of applied magnetic field, which removes the Kramers degeneracy yielding eight Zeeman levels [13, 14]. Moreover, two of the six stable Gd isotopes (155Gd and 157Gd) have a nuclear spin of I = 3/2 and together account for about 30% of the total natural content. Nuclear gyromagnetic ratios for these isotopes are about 25 times lower than for hydrogen, which results in a very weak hyperfine interaction between electron spin and nuclear spin, and is therefore often omitted in the interpretation of EMR spectra of Gd3+ ions. Hence, the ZFS originates from higher-order spin-orbit coupling effects within the excited CF states.

The experimental magnetic susceptibility data χmT, calculated per Gd3+ centre, for complex 1 and 2 reveal constant value: 14.56 and 15.86 in cm3Kmol-1 (calculated per one Gd3+ centre:7.25 and 7.88 in cm3Kmol-1, μeff = 7.61 and 7.95 B.M.), respectively, from the room temperature to about 50 K. Below 50 K χmT decreases (see, Appendix, Fig. S10) in a similar way for both complexes, and at 1.8 K 5.86 and 5.68 cm3Kmol-1 (calculated per one Gd3+ centre :2.93 and 2.84 in cm3Kmol-1, μeff = 4.85 and 4.77 B.M.) for complex 1 and 2, respectively. In the free-ion approximation, the χmT product for Gd3+ should be constant at 7.88 cm3Kmol-1 down to about 4.2 K, whereas below only a small decrease is observed due to weak ZFS [26-31]. The fitting of χm−1 vs T in Fig. 3 to the Curie-Weiss law yields the Curie constant C as 7.28 and 7.93 (in cm3·K·mol-1) and the Weiss constant  as -1.64 K and -1.25 K for complex 1 and 2, respectively. Small negative values of  confirm weak antiferromagnetic interactions between Gd3+ ions in dimeric units. The experimental magnetic data were also fitted using the program PHI []. The best fit yields the Heisenberg exchange interactions constant (with the convention H ≡ --JSS) [20] as J = -0.2 and -0.16 (in cm-1) for complex 1 and 2, respectively.

Fig. 3. Temperature dependence of χmT for complex 1 (•) and 2 (•), calculated per one Gd3+ ion (left). Solid red lines represent calculated using the program PHI [85] with the input parameters given in text. The χm−1 vs T plots for complex 1 (•) and 2 (•), calculated per one Gd3+ ion. Solid red lines are the linear fits of the experimental data to Curie-Weiss law (right).

The negative J signs further confirm weak antiferromagnetic nature of the exchange interactions. However, our experimental results do not allow for determination of the ZFS parameters for Gd3+ ions. The Gd-based dinuclear complexes 1 and 2 do not exhibit the magnetic behavior characteristic for the SMMs [1-6,49,55] reported for some Gd-based complexes, see, Refs [53,,,]. We have also not observed the slow magnetic relaxation as in some Ln-based SIMs [42,51,52]. Such subgroup of polynuclear ECS, which sits in between SMMs and SIMs, may be classified as MNM-analogous complexes.

5. Optical spectroscopy

The synthesized compounds show an extended absorption in the UV-vis range. The characteristics of the observed absorption bands indicate that spectra are due to intra-ligand transitions. Such transitions obscure the low-intensity 4f-4f transitions of Gd3+ ion that are expected at the UV wavelength region above 300 nm [62]. Consequently, no specific information on the CF energy levels can be extracted from the spectra recorded at RT. Note that measurements in low temperatures would not provide any additional information on Gd levels. Photoluminescence spectra indicate that both compounds are luminescent at RT. The observed photoluminescence transitions can be assigned as originating from intra-ligand n-* or -* transitions. The absorption and photoluminescence spectra for the synthesized compounds are presented in Appendix (Section SVI).

Emission spectra of the Gd3+ complex isostructural to the linear trinuclear Zn-Dy-Zn single-molecule magnet [(LZn(H2O))2Dy(H2O)](CF3SO3)3 has been observed by Costes et al. []. Similarly, as in our case, the observed emission is due to intra-ligand transitions because the lowest excited state for Gd3+ is so high in energy that transfer from the ligand is forbidden.

6. Summary, conclusions, and outlook

We have synthesized two new dinuclear helical Gd3+ complexes: 1 ([Gd2(L1)3](NO3)3 and 2 ({[Gd2(L2)3(NO3)3}2) with the actual trigonal C3 and triclinic C1 site symmetry, respectively. The initial selection of these complexes was driven by the pursuit of potential molecular nanomagnets (MNMs). An extensive characterization of the two complexes was conducted using a variety of techniques, including crystallographic XRD, EMR, magnetic measurements, and optical spectroscopy. These experimental efforts are complemented by computational modelling of ZFSPs [56] using semiempirical approaches: SHAPE [,] and superposition model [21] analysis, as well as the ab initio methods incorporated in the package MOLCAS [,]. Our EMR and magnetic measurements reveal that across nearly the entire temperature range, both complexes behave as paramagnets and do not exhibit slow magnetic relaxation. However, the broadening of the EMR linewidth indicates weak antiferromagnetic exchange interactions. Below 10 K, magnetic behavior is slightly influenced by site symmetry: in complex 1 (symmetric), magnetically isolated Gd3+ centers are additionally observed, while in complex 2 (dissymmetric), such centers are less evident. These features have been corroborated by the ab initio computational modelling [56].

The following conclusions may be drawn.

Specific conclusions:

(a) The 2nd-rank ZFSPs bkq are dominant, whereas the 4th-rank ZFSPs are next in importance for Gd3+ ions in each complex. The 6th-rank ZFSPs are rather negligible, albeit were found more significant for the trigonal complex 1, whereas less significant for the triclinic complex 2. This may be due to the smaller (complex 1) and significantly larger (complex 2) number of the lower-rank (k = 2, 4) ZFSPs, since during fitting process these ZFSPs must incorporate the effect of the omitted 6th-rank ZFSPs.

(b) The results evidently show that, in the case of orthorhombic and lower symmetry ZFSP sets, a prior standardization of sets is indispensable for proper interpretation of the experimental ZFSP sets taken from various sources as well as meaningful comparison of ZFSP sets obtained by various methods.

(c) For complexes exhibiting triclinic (like complex 2) as well as monoclinic site symmetry, an infinite number of physically equivalent ZFSP sets exist. Hence, to assess physical equivalence of independently obtained sets, utilizing the invariant quantities and standardization is crucial for low site symmetry EPR centers.

(d) Elucidation of symmetry aspects inherent in the fitted ZFSP sets for Gd3+ ions in complex 1 and 2, which includes the notions of the apparent and actual low and high symmetry reflected by the ZFSP sets obtained by various methods, may help to improve understanding of these crucial aspects, which are frequently overlooked in literature [56].

General conclusions: (1) The value added was acquired by integrating various experimental characterization techniques. This has enabled us to classify the newly synthesized Gd3+ complexes 1 and 2 as belonging to the subgroup of the exchange coupled systems (ECS) named the MNM-analogous complexes. (2) The systematic classification of various groups of molecular nanomagnets and the distinction between the two subgroups of SIM as well as introduction of the category of MNM-analogous complexes may help preventing proliferation of semantic misunderstandings arising from ambiguous terminology being still utilized in literature.

In the way of outlook, we comment that the experimental investigations presented herein prepare grounds for an in-depth study of the symmetry aspects in the forthcoming paper [56]. Combining the experimental results with the computational modelling of ZFSPs, which employs semiempirical approaches and the ab initio methods, will enable comprehensive elucidation of the low and high site symmetry aspects inherent in the fitted and modelled ZFSP sets for two Gd3+ complexes. This elucidation may have profound impact for the studies of other transition ions in various coordination compounds, especially MNM.

Declaration of Competing Interest

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

Acknowledgments

This work was primarily supported by the grant: (PI: CZR): OPUS UMO-2016/21/B/ST4/02064 and to a lesser extent: (PI: DM): PRELUDIUM UMO-2022/45/N/ST4/00344; (PI: AG): SONATA UMO-2020/39/D/ST4/01182, from Polish National Science Centre. C. Rudowicz acknowledges partial support from the internal research grant from the Faculty of Chemistry, Adam Mickiewicz University. Thanks are due to Prof. Henry S. La Pierre for useful explanations on the actual site symmetry of their compounds (Gompa et al, Inorg. Chem. 60, 9064 (2021).

Appendix A. Supplementary material

Supplementary data associated with this article can be found, in the online version, at http://dx.doi.org/     .

References

[] D. Gatteschi, R. Sessoli, and J. Villain, Molecular Nanomagnets, Oxford University Press, Oxford, 2006.

[] J. Bartolomé, F. Luis, and J. F. Fernández (Eds.), Molecular Nanomagnets: Physics and Applications, Springer-Verlag Berlin Heidelberg, 2014.

[] C. Benelli and D. Gatteschi, Introduction to Molecular Magnetism: From Transition Metals to Lanthanides, Wiley-VCH, 2015.

[] R. A. Layfield and M. Murugesu, Lanthanides and Actinides in Molecular Magnetism, Wiley-VCH, 2015.

[] J. Tang and P. Zhang, Lanthanide Single Molecule Magnets, Springer-Verlag Berlin Heidelberg, 2015.

[] S. Gao (Ed.), Molecular Nanomagnets and Related Phenomena, Structure and Bonding, vol. 164, Springer-Verlag Berlin Heidelberg, 2015.

[] M. S. Fataftah, J. M. Zadrozny, S. C. Coste, M. J. Graham, D. M. Rogers, and D. E. Freedman, Employing forbidden transitions as qubits in a nuclear spin-free chromium complex, J. Am. Chem. Soc. 138 (2016) 1344.

[] Y.-S. Ding, Y.-F. Deng, and Y.-Z. Zheng, The rise of single-ion magnets as spin qubits, Magnetochemistry 2 (2016) 40.

[] M. Shiddiq, D. Komijani, Y. Duan, A. Gaita-Ariño, E. Coronado, and S. Hill, Enhancing coherence in molecular spin qubits via atomic clock transitions, Nature 531 (2016) 348.

[] J. Ferrando-Soria, J. Vallejo, M. Castellano, J. Martínez-Lillo, E. Pardo, J. Cano, I. Castro, F. Lloret, R. Ruiz-García, and M. Julve, Molecular magnetism, quo vadis? A historical perspective from a coordination chemist viewpoint, Coord. Chem. Rev. 339 (2017) 17.

[] S. G. McAdams, A.-M. Ariciu, A. K. Kostopoulos, J. P. Walsh, and F. Tuna, Molecular single-ion magnets based on lanthanides and actinides: Design considerations and new advances in the context of quantum technologies, Coord. Chem. Rev. 346 (2017) 216.

[] F. Pointillart, O. Cador, B. Le Guennic, and L. Ouahab, Uncommon lanthanide ions in purely 4f Single Molecule Magnets, Coord. Chem. Rev. 346 (2017) 150.

[] Y.-S. Ding, Y.-F. Deng, and Y.-Z. Zheng, The Rise of Single-Ion Magnets as Spin Qubits Magnetochemistry 2 (2016) 1.

[] S. Sanvito, Molecular spintronics, Chem. Soc. Rev. 40 (2011) 3336.

[] L. Bogani and W. Wernsdorfer, Molecular spintronics using single-molecule magnets, Nat. Mater. 7 (2008) 179.

[] M. N. Leuenberger and D. Loss, Quantum computing in molecular magnets, Nature 410 (2001) 789.

[] C. Rudowicz, P. Cecot, and M. Krasowski, Selection rules in electron magnetic resonance (EMR) spectroscopy and related techniques: fundamentals and applications to modern case systems, Physica B 608 (2021) 412863.

[] A. Bencini and D. Gatteschi, Electron Paramagnetic Resonance of Exchange-Coupled Systems, Springer, Berlin, 1990.

[] C. Rudowicz and S. K. Misra, Spin-Hamiltonian formalisms in electron magnetic resonance (EMR) and related spectroscopies, Appl. Spectrosc. Rev. 36 (2001) 11.

[] C. Rudowicz and M. Karbowiak, Disentangling intricate web of interrelated notions at the interface between the physical (crystal field) Hamiltonians and the effective (spin) Hamiltonians, Coord. Chem. Rev. 287 (2015) 28.

[] C. Rudowicz, P. Gnutek, and M. Açikgöz, Superposition model in electron magnetic resonance spectroscopy–a primer for experimentalists with illustrative applications and literature database, Appl. Spectrosc. Rev. 54 (2019) 673.

[] C. Rudowicz, M. Açıkgöz, and M. Karbowiak, Low symmetry aspects in electron magnetic resonance (EMR) spectroscopy of coordination compounds of transition ions: crucial notions and issues, literature survey and database, Coord. Chem. Rev. 512 (2024) 215865.

[] S. Hino, M. Maeda, K. Yamashita, Y. Kataoka, M. Nakano, T. Yamamura, H. Nojiri, M. Kofu, O. Yamamuro, and T. Kajiwara, T. Linear trinuclear Zn(II)Ce(III)Zn(II) complex which behaves as a single-molecule magnet Dalton Trans. 42 (2013) 2683.

[] M. Vonci, M. J. Giansiracusa, W. Van den Heuvel, R. W. Gable, B. Moubaraki, K. S. Murray, D. Yu, R. A. Mole, A. Soncini, and C. Boskovic, Magnetic Excitations in Polyoxotungstate-Supported Lanthanoid Single-Molecule Magnets: An Inelastic Neutron Scattering and ab Initio Study, Inorg. Chem. 56 (2017) 378.

[] T. Fukuda, N. Shigeyoshi, T. Yamamura, and N. Ishikawa, Magnetic relaxations arising from spin phonon interactions in the nonthermally activated temperature range for a double-decker terbium phthalocyanine single molecule magnet, Inorg. Chem. 53 (2014) 9080.

[] S. K. Misra, Electron paramagnetic resonance studies of Gd3+, Magn. Reson. Rev. 10 (1986) 333.

[] S. K. Misra and X. Li, Gd3+ EPR study of structural phase transition in NH_4La(SO)_2.4H_2O single crystal: a superposition-model calculation of zero-field splitting parameters, J. Phys.: Condens. Matter 2 (1990) 9613.

[] S. K. Misra, in Handbook of Electron Spin Resonance, edited by C. P. Pool Jr. and H. A. Farach, Vol. 2, AIP, New York, 1999, Vol. 2, Chap. VII.

[] H. A. Buckmaster and Y. H. Shing, A survey of the EPR spectra of Gd3+ in single crystals, Phys. Status Solidi A 12 (1972) 325.

[] G. L. McPherson and L. M. Henling, EPR spectrum of coupled pairs of Gd3+ ions in single crystals of CsCdBr_3, Phys. Rev. B 16 (1977) 1889.

[] C. Benelli and D. Gatteschi, Magnetism of lanthanides in molecular materials with transition-metal ions and organic radicals, Chem. Rev. 102 (2002) 2369.

[] A. Lunghi, Toward exact predictions of spin-phonon relaxation times: An ab initio implementation of open quantum systems theory, Sci. Adv. 8 (2022) eabn7880.

[] J. A. Clayton, K. Keller, M. Qi, J. Wegner, V. Koch, H. Hintz, A. Godt, S. Han, G. Jeschke, and M. S. Sherwin, Quantitative analysis of zero-field splitting parameter distributions in Gd(III) complexes, Phys. Chem. Chem. Phys. 20 (2018) 10470.

[] J. B. Petersen, Y.-S. Ding, S. Gupta, A. Borah, E. J. L. McInnes, Y.-Z. Zheng, R. Murugavel, and R. E. P. Winpenny, Electron Paramagnetic Resonance Spectra of Pentagonal Bipyramidal Gadolinium Complexes, Inorg. Chem. 62 (2023) 8435.

[] M. J. Martínez-Pérez, S. Cardona-Serra, C. Schlegel, F. Moro, P. J. Alonso, H. Prima-García, J. M. Clemente-Juan, M. Evangelisti, A. Gaita-Ariño, J. Sesé, J. van Slageren, E. Coronado, and F. Luis, Gd-Based Single-Ion Magnets with Tunable Magnetic Anisotropy: Molecular Design of Spin Qubits, Phys. Rev. Lett. 108 (2012) 247213.

[] J. J. Baldoví, S. Cardona-Serra, J. M. Clemente-Juan, E. Coronado, A. Gaita-Ariño, and H. Prima-García, Coherent Manipulation of Spin Qubits Based on Polyoxometalates: The Case of the Single Ion Magnet [GdW₃₀P₅O₁₁₀]¹⁴⁻, Chem. Commun. 49 (2013) 8922.

[] J. López-Cabrelles, L. Escalera-Moreno, Z. Hu, H. Prima-García, G. M. Espallargas, A. Gaita-Ariño, and E. Coronado, Near Isotropic D₄d Spin Qubits as Nodes of a Gd(III)-Based Metal–Organic Framework, Inorg. Chem. 60 (2021) 8575.

[] D. Aguilà, L. A. Barrios, F. Luis, A. Repollés, O. Roubeau, S. J. Teat, and G. Aromí, Synthesis and Properties of a Family of Unsymmetric Dinuclear Complexes of LnIII (Ln = Eu, Gd, Tb), Inorg. Chem. 49 (2010) 6784.

[] D. Aguilà, L. A. Barrios, V. Velasco, L. Arnedo, N. Aliaga-Alcalde, M. Menelaou, S. J. Teat, O. Roubeau, F. Luis, and G. Aromí, Lanthanide Contraction within a Series of Asymmetric Dinuclear [Ln₂] Complexes, Chem. Eur. J. 19 (2013) 5881.

[] D. Aguilà, V. Velasco, L. A. Barrios, J. González-Fabra, C. Bo, S. J. Teat, O. Roubeau, and G. Aromí, Selective Lanthanide Distribution within a Comprehensive Series of Heterometallic [LnPr] Complexes, Inorg. Chem. 57 (2018) 8429.

[] T. J. Clough, L. Jiang, K.-L. Wong, and N. J. Long, Ligand Design Strategies to Increase Stability of Gadolinium-Based Magnetic Resonance Imaging Contrast Agents, Nat. Commun. 10 (2019) 1420.

[] J. Mayans and A. Escuer, Correlating the Axial Zero Field Splitting with the Slow Magnetic Relaxation in GdIII SIMs, Chem. Commun. 57 (2021) 721.

[] T. P. Gompa, S. M. Greer, N. T. Rice, N. Jiang, J. Telser, A. Ozarowski, B. W. Stein, and H. S. La Pierre, High-Frequency and -Field Electron Paramagnetic Resonance Spectroscopic Analysis of Metal–Ligand Covalency in a 4f⁷ Valence Series (Eu²⁺, Gd³⁺, and Tb⁴⁺), Inorg. Chem. 60 (2021) 9064.

[] G. Taran, E. Moreno-Pineda, M. Schulze, E. Bonet, M. Ruben, and W. Wernsdorfer, Direct Determination of High-Order Transverse Ligand Field Parameters via μSQUID-EPR in a Et₄N[160GdPc₂] SMM, Nat. Commun. 14 (2023) 3361.

[] X-N. Xu, Y-S.Zhang, J-M. Song, Q-S. Deng, Y-Q. Liao, J-Y. Yuan, S. Gao, S. Zhou, S-D. Jiang, A high-dimensional spin-qudit candidate of Gd (III) center complex crystal with addressable transitions, CCS Chemistry, accepted paper, on-line October 2024.

[] C. Rudowicz, Journal of Physics C: Solid State Physics 18 (1985) 1415.

[] C. Rudowicz and C. Chung, Journal of Physics: Condensed Matter. 16 (2004) 5825.

[] S. H. Hansen, C. D. Buch, H. Weihe, S. Piligkos, Effect of chemical modification in trigonal Gd(III) molecular qubits, ChemRxiv, paper r7ld5, November 2024.

[] A. Gorczyński, M. Kubicki, D. Pinkowicz, R. Pełka, V. Patroniak, and R. Podgajny, The first example of erbium triple-stranded helicates displaying SMMs behaviour, Dalton Trans. 44 (2015) 16833.

[] A. Gorczyński, D. Marcinkowski, M. Kubicki, M. Löffler, M. Korabik, M. Karbowiak, P. Wiśniewski, C. Rudowicz, and V. Patroniak, New field-induced single ion magnets based on prolate Er(III) and Yb(III) ions: tuning the energy barrier U_eff by the choice of counterions within an N3-tridentate Schiff-base scaffold, Inorg. Chem. Front. 5 (2018) 605.

[] D. Marcinkowski, M. Kubicki, V. Patroniak, T. Muzioł, S. Chorazy, L. Shi, M. Zychowicz, A. M. Majcher-Fitas, R. Podgajny, and A. Gorczyński, Trityl-based lanthanide-supramolecular assemblies exhibiting slow magnetic relaxation, Chem. Eur. J., 29 (2023) e202300695.

[] D. Marcinkowski, A. Adamski, M. Kubicki, G. Consiglio, V. Patroniak, T. Ślusarski, M. Açıkgöz, D. Szeliga, N. Vadra, M. Karbowiak, I. Stefaniuk, C. Rudowicz, A. Gorczyński, and M. Korabik, Understanding the effect of structural changes on slow magnetic relaxation in mononuclear octahedral copper(II) complexes, Dalton Trans. 51 (2022) 12041.

[] Y. H. Pham, V. A. Trush, A. N. C. Neto, M. Korabik, J. Sokolnicki, M. Weselski, O. L. Malta, V. Amirkhanov, and P. Gawryszewska, Lanthanide complexes with N-phosphorylated carboxamide as UV converters with excellent emission quantum yield and single-ion magnet behavior, J. Mater. Chem. C 8 (2020) 9993.

[] M. Açıkgöz and C. Rudowicz, Temperature and pressure dependence of local structural changes around Gd3+ centers in RAl3(BO3)4 crystals: Modeling zero-field splitting parameters, Polyhedron 150 (2018) 15.

[] I. Pospieszna-Markiewicz, M. A. Fik-Jaskółka, Z. Hnatejko, V. Patroniak, and M. Kubicki, Synthesis and characterization of lanthanide metal ion complexes of new polydentate hydrazone Schiff base ligand, Molecules 27 (2022) 8390.

[] Forthcoming paper, in preparation (2025).

[] S. F. Mason, Molecular optical activity and the chiral discriminations, Cambridge University Press, 1982.

[] R. Robson, Complexes of binucleating ligands. II. Geometrical models for potential nitrogen fixing systems, Aust. J. Chem. 23 (1970) 2217.

[] F. B. Tamboura, O. Diouf, A. H. Barry, M. Gaye, and A. S. Sall, Dinuclear lanthanide(III) complexes with large-bite Schiff bases derived from 2, 6-diformyl-4-chlorophenol and hydrazides: Synthesis, structural characterization and spectroscopic studies, Polyhedron, 43 (2012) 97.

[] S.-Y. Lin, G.-F. Xu, L. Zhao, Y.-N. Guo, Y. Guo, and J. Tang, Observation of slow magnetic relaxation in triple-stranded lanthanide helicates, Dalton Trans., 40 (2011) 8213.

[] O. Yalçın, Ferromagnetic Resonance: Theory and Applications, BoD–Books on Demand, 2013.

[] Y. Yafet and C. Kittel, Antiferromagnetic arrangements in ferrites, Phys. Rev. 87 (1952) 290.

[] S. Bhat, P. Ganguly, T. Ramakrishnan, and C. Rao, Absorption of electromagnetic radiation by superconducting YBa₂Cu₃O₇: An oxygen-induced phenomenon, J. Phys. C: Solid State Phys. 20 (1987) L559.

[] V. Srinivasu, S. Lofland, S. Bhagat, K. Ghosh, and S. Tyagi, Temperature and field dependence of microwave losses in manganite powders, J. Appl. Phys. 86 (1999)1067.

[] H. Montiel, G. Alvarez, I. Betancourt, R. Zamorano, and R. Valenzuela, Correlations between low-field microwave absorption and magnetoimpedance in Co-based amorphous ribbons, Appl. Phys. Lett. 86 (2005) 072503.

[] G. Alvarez and R. Zamorano, Characteristics of the magnetosensitive non-resonant power absorption of microwave by magnetic materials, J. Alloys Compd. 369 (2004) 231.

[] J. R. Pilbrow, Transition-Ion Electron Paramagnetic Resonance, Clarendon Press, Oxford, 1990.

[] F. E. Mabbs and D. Collison, Electron Paramagnetic Resonance of d Transition-Metal Compounds, Elsevier, Amsterdam, 1992.

[] J. A. Weil and J. R. Bolton, Electron Paramagnetic Resonance, Elemental Theory and Practical Applications, Wiley, New York, 2007.

[] S. K. Misra (Ed.), Multifrequency Electron Paramagnetic Resonance, Wiley-VCH, Weinheim, 2011; Erratum, S. K. Misra and C. Rudowicz, [http://www.wiley-vch.de/publish/dt/books/ISBN3-527-40779-0/].

[] E.E. Schneider, B not H in Magnetic Resonance, in: P.S. Allen, E.R. Andrew, C.A. Bates (Eds.), Magnetic Resonance and Related Phenomena, Proceedings of 18th Congress Ampere, Nottingham, England, 1974, North-Holland, Amsterdam, 1975, Vol. 2., pp. 569-570.

[] F.J. Lowes, Geophys. J. R. Astr. Soc. 37 (1974) 151-155.

[] C. Rudowicz, H.W.F. Sung, Am. J. Phys. 71 (2003) 1080-1083.

[] S. Misra, C. Poole and H. Farach, Applied Magnetic Resonance 11 (1996) 29-46.

[] S. Stoll and A. Schweiger, EasySpin, a comprehensive software package for spectral simulation and analysis in EPR, J. Magn. Reson. 178 (2006) 42.

[] S. Stoll, EasySpin: An EPR Toolbox for Matlab—version 3.0.0, available from the website: http://www.easyspin.org, 2008.

[] V. Grachev, see www.visual-epr.com (for all details and light version to download).

[] V. Grachev, R. Petersen, E. Kokanyan, O. Schirmer, and G. Malovichko, Structural analysis of the dominant axial Fe³⁺ center in LiNbO₃ crystal by electron nuclear double resonance, J. Appl. Phys. 120 (2016) 193901.

[] C. Rudowicz and R. Bramley, On standardization of the spin Hamiltonian and the ligand field Hamiltonian for orthorhombic symmetry, J. Chem. Phys., 83 (1985) 5192.

[] C. Rudowicz, Computer package CST, in: D. J. Newman, B. K. C. Ng (Eds), Crystal Field Handbook, Cambridge University Press, Cambridge, 2000, p. 259-268.

[] C. Rudowicz and Q. Jian, The extended version of the computer package CST for conversions, standardization and transformations of the spin Hamiltonian and the crystal-field Hamiltonian, Comput. Chem. 26 (2002) 149.

[] C. Rudowicz in, B. Ng and D. J. Newman, Computer package CST: conversions, standardization and transformations, Cambridge University Press Cambridge, 2000.

[] C. Rudowicz and Q. Jian, Computers & chemistry, 2002, 26, 149-157.

[] P. Gnutek and C. Rudowicz, Optical Materials, 2008, 31, 391-400.

[] C. Rudowicz and J. Qin, Noether’s theorem and conserved quantities for the crystal-and ligand-field Hamiltonians invariant under continuous rotational symmetry, Phys. Rev. B 67, 174420 (2003).

[] C. Rudowicz and J. Qin, Can the low symmetry crystal (ligand) field parameters be considered compatible and reliable?, J. Lumin. 110, 39 (2004).

[] O. Kahn, Molecular Magnetism 4th ed., Wiley-VCH, New York, 2001.

[] B. D. Cullity and C. D. Graham, Introduction to Magnetic Materials, John Wiley & Sons, 2011.

[] A. Abragam and B. Bleaney, Electron Paramagnetic Resonance of Transition Ions, OUP Oxford, 2012.

[] N. F. Chilton, R. P. Anderson, L. D. Turner, A. Soncini, and K. S. Murray, PHI: A powerful new program for the analysis of anisotropic monomeric and exchange-coupled polynuclear d- and f-block complexes, J. Comput. Chem. 34 (2013) 1164.

[] F. Luis, P. J. Alonso, O. Roubeau, V. Velasco, D. Zueco, D. Aguilà, J. I. Martínez, L. A. Barrios, and G. Aromí, A dissymmetric [Gd₂] coordination molecular dimer hosting six addressable spin qubits, Commun. Chem. 3 (2020) 1.

[] F. Habib and M. Murugesu, Lessons learned from dinuclear lanthanide nano-magnets, Chem. Soc. Rev. 42 (2013) 3278.

[] G. Handzlik, M. Magott, M. Arczyński, A. M. Sheveleva, F. Tuna, M. Sarewicz, A. Osyczka, M. Rams, V. Vieru, and L. F. Chibotaru, Magnetization dynamics and coherent spin manipulation of a propeller Gd(III) complex with the smallest helicene ligand, J. Phys. Chem. Lett. 11 (2020) 1508.

[] J. P. Costes, S. Titos-Padilla, I. Oyarzabal, T. Gupta, C. Duhayon, G. Rajaraman and E. Colacio, Chemistry – A European J. 21 (2015) 15785-15796.

[] S. Alvarez, P. Alemany, D. Casanova, J. Cirera, M. Llunell, and D. Avnir, Shape maps and polyhedral interconversion paths in transition metal chemistry, Coord. Chem. Rev. 249 (2005) 1693.

[] M. Llunell, D. Casanova, J. Cirera, P. Alemany, and S. Alvarez, SHAPE v. 2.1, University of Barcelona, Barcelona, Spain, 2013.

[] F. Aquilante, J. Autschbach, R. K. Carlson, L. F. Chibotaru, M. G. Delcey, L. De Vico, I. Fdez Galván, N. Ferré, L. M. Frutos, and L. Gagliardi, Molcas 8: New capabilities for multiconfigurational quantum chemical calculations across the periodic table, J. Comput. Chem. 37 (2016) 506.

[] F. Aquilante, et al. Modern quantum chemistry with [Open] Molcas, J. Chem. Phys. 152 (2020) 214117.