SUPPLEMENTAL INFORMATION FOR

Suppressing part warpage in large-area Digital Light Processing (DLP) printing A structure-process co-optimisation strategy

1 Mesh generation and convergence analysis

To ensure numerical accuracy and robustness of the curing–thermal–mechanical (CTM) multiphysics simulations, a mesh convergence analysis was performed using a sequence of progressively refined finite element meshes. Six mesh configurations with increasing spatial resolution (Mesh 1–Mesh 6) were evaluated, as summarised in Table 1. Convergence was assessed by monitoring the temperature response at representative locations within the printed structure. The results indicate that the predicted temperature field converges between Mesh 5 and Mesh 6, with variations below 0.01%, demonstrating that Mesh 6 provides sufficient spatial resolution for accurately capturing thermal transport and heat accumulation. Further mesh refinement led to numerical instability, attributed to the strong nonlinearity arising from the tight coupling between curing kinetics, exothermic heat generation, and thermo-mechanical interactions.

Table 1. Mesh convergence study

| Mesh | Temperature (˚C) | Difference (%) | Displacement (mm) | Difference (%) |
| --- | --- | --- | --- | --- |
| 1 | 117.32 | - | -0.0195 | - |
| 2 | 117.81 | 0.42 | -0.0198 | 1.56 |
| 3 | 117.32 | 0.42 | -0.0195 | 1.58 |
| 4 | 106.12 | 10.55 | -0.0158 | 23.29 |
| 5 | 107.7 | 1.47 | -0.0167 | 5.32 |
| 6 | 107.71 | 0.01 | -0.0061 | 172.93 |
| 7 | 79.547 | 35.40 | -0.0004 | 1285.40 |

In contrast to the thermal response, displacement predictions exhibit pronounced mesh sensitivity, particularly in regions characterised by steep temperature gradients and localised stress concentrations. Such behaviour is inherent to multiphysics simulations of curing-induced deformation and reflects the highly localised nature of thermo-mechanical coupling during stepwise DLP printing. As the primary objective of this work is to elucidate the thermal and reaction-kinetic mechanisms governing stress evolution, Mesh 6 (Fig. 1) was adopted to ensure converged and reliable thermal predictions.

Figure 1. Finite element mesh (Mesh 6) adopted for all simulations after a mesh sensitivity study. The mesh ensures adequate resolution of the temperature field and stable numerical performance for the coupled thermo-mechanical model.

2 Polymerisation lumped rate constant P

The polymerisation lumped rate constant P was determined directly from the experimentally calibrated critical exposure condition of the Phrozen 8K acrylate resin. Under a constant ultraviolet irradiance I0, defined as the incident UV power per unit area, the critical exposure time  Tc represents the minimum irradiation duration required for the resin surface to reach the gel point and form a mechanically stable solid network. The corresponding critical radiant exposure Ec  is defined as:

Ec=I0 ∙ Tc

which provides a direct link between the experimentally determined exposure threshold and the curing kinetics adopted in the numerical model.

To describe the curing behaviour in the CTM model, the degree of cure α(t) was introduced as a dimensionless state variable representing the fraction of reacted polymerisable double bonds at time t, with α=0 corresponding to the uncured liquid state and α=1 to complete conversion. The temporal evolution of α(t) under constant irradiation was approximated using a first-order lumped kinetic formulation.

dα(t)dt=P ∙[1-α(t)]

Subject to the initial condition alpha(0) = 0. The analytical solution of this equation is given by:

αt=1-e(-P∙t)

The experimentally determined critical exposure time Tc marks the gelation threshold. In the present model, this condition was represented by assigning a gel-point degree of cure αgel such that

αTc= αgel

According to classical Flory–Stockmayer gelation theory[1], the critical gel-point conversion decreases markedly with increasing monomer functionality, allowing the formation of a percolated crosslinked network at relatively low degrees of conversion. Consistent with these theoretical predictions, experimental studies on UV-curable multifunctional (meth)acrylate systems have demonstrated that gelation typically occurs at conversion levels of 5–8% under photopolymerisation conditions [2-4]. On this basis, a single gel-point conversion αgel=0.073 was adopted to map the experimentally observed solidification threshold to the lumped kinetic model.

By enforcing the condition αTc= αgel, the polymerisation lumped rate constant can be expressed as

P= ln(1- αgel)Tc

Substituting the experimentally calibrated value of Tc and the selected αgel yields

P= 0.163

This value was used as the polymerisation lumped rate constant in the CTM model, as summarised in Table 1.

3 Initial monomer concentration [M]0

[M]0 is defined as the initial molar concentration of polymerisable, acrylate-type reactive monomers in the resin. According to the Safety Data Sheet (SDS) of Phrozen Aqua-Grey 8K, the formulation explicitly lists two components as reactive acrylate monomers: oxybis(methyl-2,1-ethanediyl) diacrylate (CAS 57472-68-1, 30–50 wt%) and 4-(1-oxo-2-propenyl)-morpholine (CAS 5117-12-4, 15–30 wt%). Other proprietary components reported as “Additives” are not chemically specified and were therefore not treated as quantifiable reactive monomers in the conversion of [M]0

To convert the SDS-reported mass-fraction intervals into a single deterministic input for model parameterisation, the upper-bound mass fractions of the two listed reactive monomers were used ωDPGDA=0.50,ωAM=0.30 . The resin density ρ was taken directly from the SDS (25 °C). The conversion from mass fractions to molar concentration is:

[M]0= ρ ∙ ωDPGDAMDPGDA + ωAMMAM

Where ωi​ denotes the mass fraction and Mi​ the molar mass of component i; DPGDA denotes oxybis(methyl-2,1-ethanediyl) diacrylate and AM denotes 4-(1-oxo-2-propenyl)-morpholine. Molar masses were taken from PubChem MDPGDA=242.27,MAM=141.17  Substituting ρSDS and the selected mass fractions give

[M]0= 4.94 mol/L

This value was used for “Initial monomer concentration, [M]0 in Table 1.

4 Maximum chemical strain, εch,max

Polymerisation shrinkage was incorporated into the coupled curing–thermal–mechanical model as an isotropic chemical eigenstrain linked to the degree of conversion α\alphaα, reaching a maximum magnitude at full cure, εch,max. Here, α denotes the fractional conversion of reactive double bonds 0≤α≤1, and εch,max​ is defined as the maximum isotropic linear shrinkage strain from the liquid resin to the crosslinked polymer network.

For isotropic shrinkage, the commonly reported volumetric shrinkage Sv​ can be converted into the corresponding linear eigenstrain through.

1-Sv= VcuredVliquid= λ3

εch,max=λ-1=1-Sv13-1

where λ is the isotropic linear shrinkage ratio. For acrylate- and urethane–acrylate-based photocurable resins employed in Digital Light Processing (DLP) and stereolithography (SLA), volumetric polymerisation shrinkage varies with monomer structure, functionality, and network crosslink density, and is typically reported in the range of 4–10%. For example, Deng et al.[5]. reported a volumetric shrinkage of Sv=4.15% for a urethane–acrylate photosensitive resin used in stereolithographic 3D printing, representing a conservative lower-bound value within this material class. In contrast, higher shrinkage levels are commonly observed in multifunctional acrylate systems that develop higher crosslink density and achieve higher effective conversion, which are representative of many commercial DLP resins. Considering the acrylate-rich composition and rapid crosslinking characteristics of the Phrozen 8K resin, a representative volumetric shrinkage of  Sv≈8.7% was adopted to characterise the maximum chemical contraction associated with full network formation. Substitution into the isotropic shrinkage relation yields.

εch,max=1-0.0871/3-1=0.03

Accordingly, the magnitude εch,max=0.03 was employed as the maximum linear chemical shrinkage eigenstrain in the CTM model. This value lies within the experimentally established range for acrylate-based photocurable networks and can be used for quantitative modelling of polymerisation-shrinkage-induced residual stress and structural deformation during DLP printing based on Phrozen 8K resin.

5 Poisson’s ratio

Phrozen 8K is a UV-curable acrylate photopolymer resin. After curing, such materials are appropriately treated as densely crosslinked polymer networks, for which Poisson’s ratio is commonly modelled as a constant in small-strain mechanics.

Across the UV-resin/UV-curable resist mechanics literature, υ=0.35 is repeatedly used as a representative value for cured photopolymer networks. For example, a Poisson’s ratio of 0.35 was adopted in the mechanical analysis of UV-cured resist deformation and demoulding behaviour [6]. Importantly, independent static material testing has reported a fully cured UV resin exhibiting υ=0.35, providing direct experimental support for this assignment [7], accordingly, Poisson’s ratio for Phrozen 8K resin was set to: υ=0.35.

6 Initial multiplication factor for Epol

In the DLP curing–mechanical model, the Young’s modulus is defined as a conversion-dependent quantity.

Ep=ηp∙ Epol

where Epol​ denotes the Young’s modulus of the fully polymerised network and ηp is a dimensionless scaling function of the degree of conversion p. At the initial stage of curing (p), a finite value.

η0=E0

η0 is prescribed to represent the effective stiffness assigned to the uncured resin prior to gelation. The same modulus-evolution formulation and parameter order have been adopted in previously reported multiphysics models of vat photopolymerisation processes and are employed here for consistency [8, 9]. Considering that the elastic modulus of a liquid photopolymer before gelation is several orders of magnitude lower than that of the fully crosslinked polymer network, the initial multiplication factor was set to

Epol=1.0 × 10-3

This order-of-magnitude separation ensures that the pre-gel resin contributes negligibly to stress development while allowing a continuous, well-posed evolution as curing proceeds.

7 Conversion gel-point pgel

The conversion gel-point, pgel​, represents the critical extent of double-bond conversion at which a percolated polymer network first emerges during multifunctional acrylate photopolymerisation, marking the transition from a predominantly viscous liquid to an elastic, stress-bearing gel. In the present curing–thermal–mechanical framework, pgel​​ is introduced as the conversion threshold governing the activation of mechanically effective modulus development, such that elastic stress accumulation is suppressed prior to network percolation and enabled only after the formation of a connected polymer network.

Experimental and modelling studies on acrylate photopolymerisation have demonstrated that gelation occurs at comparatively low conversion in multifunctional systems and shifts to lower values with increasing effective functionality. In particular, microrheology-assisted kinetic analyses have reported critical gel-point conversions of approximately 0.14 for tetrafunctional acrylate networks and around 0.20 for trifunctional systems, reflecting accelerated network formation associated with higher crosslink density[10, 11]. Given that the Phrozen 8K resin comprises difunctional acrylate monomers together with multifunctional acrylated oligomeric components, the onset of a percolated, stress-bearing network is expected to be governed primarily by the multifunctional crosslinking fraction rather than by the difunctional diluents. Consequently, the effective functionality controlling network percolation is closer to tetrafunctional behaviour within the conversion regime reported above. Accordingly, the conversion gel-point was set to  pgel=0.14.​

8 Heat capacity, cp

The heat capacity at constant pressure, cp characterises the thermal inertia of the photopolymer resin and governs the coupling between volumetric heat generation and transient temperature evolution in the energy-balance equation of the curing–thermal–mechanical framework. In the present formulation, cp directly controls the magnitude and temporal evolution of temperature rise induced by photopolymerisation exotherm and absorbed irradiation, thereby influencing both the peak thermal accumulation during exposure and the subsequent cooling behaviour.

For acrylate-based UV-curable resins (such as the Phrozen 8K resin), the specific heat capacity has been reported for both cured and partially cured states. Representative thermophysical characterisations of UV-curable acrylate systems, including technical datasheets for cured acrylate resin films such as the Addison Clear Wave BD218D resin, report specific heat capacities on the order of  1.2×103Jkg-1K-1, while thermal analyses and process-scale modelling studies commonly employ values up to 1.34×103Jkg-1K-1 to describe irradiation-induced heating in similar resin chemistries[12]. Within this convergent range, and consistent with the chemical composition and polymer network density of the present acrylate resin, the heat capacity was set to

cp=1.3×103Jkg-1K-1

9 Thermal conductivity, k

The thermal conductivity k governs conductive heat transport within the photopolymer during exposure and post-exposure cooling and therefore sets the degree to which spatially non-uniform heat generation can be redistributed by diffusion. In the present heat-transfer formulation, k directly controls the smoothing of localised temperature gradients and the characteristic thermal diffusion length over the relevant exposure and cooling timescales.

For acrylate-based vat-photopolymerisation resins(Phrozen 8K resin), manufacturer-provided thermophysical data for representative DLP resin families indicate that unfilled photopolymer resins typically exhibit k in the range of 0.25-0.35Wm-1K-1[13]. Independent experimental measurements of stereolithography photopolymer resins using a dedicated conductivity test bench yield values of the same order, including 0.314 ±0.087Wm-1K-1 and 0.343 ±0.061Wm-1K-1 for two commercial resins[14]. Consistent with these convergent literature ranges for insulating acrylate photopolymers, the thermal conductivity of Phrozen 8K resin was set:

k=0.3 Wm-1K-1

10 Monomer thermal expansion coefficient, αth,mono

The thermal strain associated with the pre-gel liquid phase was modelled by introducing an effective volumetric thermal expansion coefficient representative of an acrylate monomer mixture. Prior to gelation, the resin remains in a monomer-rich, fluid state, in which temperature changes primarily affect the free volume and give rise to thermoelastic expansion rather than network-constrained deformation. To capture this behaviour within multiphysics curing–thermal formulations for DLP, a monomer-mixture expansion coefficient αM is commonly employed to describe the temperature dependence of the liquid-phase volume before network formation. For acrylate-based photosensitive systems, a representative value of αM=200×10-6K-1 has been widely adopted in previous DLP thermokinetic models [15]. Accordingly, the monomer thermal expansion coefficient for the present resin was set to

αth,mono= 2.0×10-4K-1

This value reflects the higher thermal expansivity of the liquid, monomer-rich phase relative to the solidified polymer network, while remaining consistent with established parameter ranges used in multiphysics simulations of acrylate-based photopolymerisation processes.

11 Polymerisation heat, ∆H

In the curing–thermal formulation, the coupling between photopolymerisation kinetics and heat transfer is introduced via a volumetric heat-generation term. The local rate of heat generation associated with polymerisation is written as：

q=∆HR

where q denotes the volumetric heat generation rate arising from the exothermic polymerisation reactio. The parameter ∆H represents the reaction enthalpy released per mole of polymerisable acrylate functionalities (C=C) consumed during photopolymerisation, while R denotes the molar consumption rate of these reactive functionalities as defined by the kinetic mode. This formulation ensures direct energetic consistency between the chemical reaction kinetics and the thermal field, as the product of the molar reaction enthalpy and the local reaction rate yields the rate of heat generation per unit volume. By integrating the volumetric heat generation rate over time, the total heat released within the conversion window relevant to stepwise DLP exposure can be expressed as：

Qtot=q dt=C0∆HΔα

where C0 is the initial concentration of polymerisable acrylate functionalities defined by the kinetic model, and Δα denotes the effective increment of double-bond conversion attained within the timescale associated with a single exposure step. This definition explicitly accounts for the fact that, under stepwise DLP printing conditions, only a fraction of the total available reactive functionalities contributes to heat release within each exposure window.

For acrylate-based photopolymer systems, the intrinsic polymerisation enthalpy associated with complete double-bond conversionΔH0, has been extensively characterised in calorimetric studies and is commonly taken to be approximately 78 KJmol-1 [16]. In practical DLP printing, however, the effective heat release is expected to be lower than this intrinsic value due to oxygen inhibition, rapid network formation, and diffusion-limited propagation following gelation, particularly near exposed surfaces[17, 18]. To account for these effects in a physically transparent manner, an effective conversion fraction feff​ is introduced, such that

ΔH=ΔHeff=feff∙ΔH0​

and consequently

Qtot=C0∙ΔH0∙eff

under the present definition of the effective conversion window.For the Phrozen 8K resin, the liquid density is taken as ρ=1.1g cm-3. The initial concentration of reactive functionalities C0​ is constrained by the formulation composition, which comprises diacrylate monomers (30–50 wt%), multifunctional acrylated oligomers (10–30 wt%), and a substantial fraction of 4-(1-oxo-2-propenyl)-morpholine (15–30 wt%, monofunctional). These components collectively define a reactive-function inventory on the order of C0≈1.0×104molm3 within the kinetic framework. Guided by the experimentally established conversion ranges of multifunctional acrylate systems and the expected suppression of effective conversion under ambient oxygen-inhibited curing conditions, an effective conversion fraction of  feff=0.5 is adopted as a conservative and representative value for stepwise DLP exposure[19]. This yields an effective polymerisation heat of

ΔHeff=3.9×104Jmol-1

which is employed in the coupled curing–thermal simulations to ensure energetic consistency between the kinetic consumption of reactive functionalities and the macroscopic thermal response of the printed structures.

References

[1].	Flory, P.J., Principles of Polymer Chemistry. 1953, Cornell university press.

[2].	Stockmayer, W.H., Theory of molecular size distribution and gel formation in branched polymers II. General cross linking. The Journal of Chemical Physics, 1944. 12(4): p. 125-131

[3].	Bowman, C.N., and Christopher J. Kloxin, Toward an enhanced understanding and implementation of photopolymerization reactions. AIChE Journal 2008. 54(11): p. 2775-2795

[4].	Decker, C., Kinetic study and new applications of UV radiation curing. Macromolecular Rapid Communications, 2002. 23(18): p. 1067-1093

[5].	Deng, Y., Jie Li, Zuhan He, Jiang Hong, and Jianjun Bao, Urethane acrylate‐based photosensitive resin for three‐dimensional printing of stereolithographic elastomer. Journal of Applied Polymer Science, 2020. 137(42): p. 49294

[6].	Tochino, T., Takahiro Shiotsu, Kimiaki Uemura, Masaaki Yasuda, Hiroaki Kawata, and Yoshihiko Hirai., Impact of resist shrinkage on the template release process in nanoimprint lithography. Journal of Vacuum Science & Technology B, 2014. 32(6)

[7].	Onishi, Y., Ryunosuke Yamashita, Kenji Amaya, and Yoshihiko Hirai, Numerical analysis of pattern shape deformation in UV imprint considering thermal deformation with UV shrinkage and curing. Journal of Vacuum Science & Technology B, 2021. 39(2)

[8].	Classens, K., et al., Multiphysical modeling and optimal control of material properties for photopolymerization processes. Additive Manufacturing, 2021. 38.DOI: 10.1016/j.addma.2020.101520

[9].	Brighenti, R., et al., Multiphysics modelling of the mechanical properties in polymers obtained via photo-induced polymerization. The International Journal of Advanced Manufacturing Technology, 2021. 117(1-2): p. 481-499.DOI: 10.1007/s00170-021-07273-2

[10].	Bowman, C.N., and Nikolaos A. Peppas., Coupling of kinetics and volume relaxation during polymerizations of multiacrylates and multimethacrylates. Macromolecules, 1991. 24: p. 1914-1920

[11].	Anseth, K.S., Cynthia M. Wang, and Christopher N. Bowman, Reaction behaviour and kinetic constants for photopolymerizations of multi (meth) acrylate monomers. Polymer, 1994. 35(15): p. 3243-3250

[12].	竹下, 一.福.久.酒.昭.西.等.大.崇.宮.篤.石.知., Sheet-transporting apparatus and printing apparatus. 2022.

[13].	Formlabs. Thermal properties of selected Formlabs SLA resins. 2025.

[14].	Oval-Trujillo, A., et al., Experimental measurement of thermal conductivity of stereolithography photopolymer resins. SN Applied Sciences, 2022. 4(8).DOI: 10.1007/s42452-022-05087-9

[15].	Blyweert, P., et al., Numerical simulation model for the curing of photosensitive acrylate resin in a stereolithography process. The International Journal of Advanced Manufacturing Technology, 2024. 135(11-12): p. 5157-5172.DOI: 10.1007/s00170-024-14744-9

[16].	Broer, D.J., G.N. Mol, and G. Challa, Temperature effects on the kinetics of photoinitiated polymerization of dimethacrylates. Polymer, 1991. 32(4): p. 690-695.DOI: 10.1016/0032-3861(91)90482-x

[17].	Iedema, P.D., et al., Photocuring of di-acrylate. Chemical Engineering Science, 2018. 176: p. 491-502.DOI: 10.1016/j.ces.2017.11.009

[18].	Decker, C., Photoinitiated crosslinking polymerisation. Progress in polymer science, 1996. 21(4): p. 593-650

[19].	Bagheri, A. and J. Jin, Photopolymerization in 3D Printing. ACS Applied Polymer Materials, 2019. 1(4): p. 593-611.DOI: 10.1021/acsapm.8b00165