mm019

R1=5.91%

Crystal Data and Experimental

Experimental. Single clear pale yellow prism-shaped crystals of mm019 were used as supplied. A suitable crystal with dimensions 0.10 × 0.08 × 0.07 mm3 was selected and mounted on a XtaLAB Synergy R, DW system, HyPix-Arc 150 diffractometer. The crystal was kept at a steady T = 170(40) K during data collection. The structure was solved with the ShelXT (Sheldrick, 2015) solution program using dual methods and by using Olex2 1.5 (Dolomanov et al., 2009) as the graphical interface. The model was refined with ShelXL 2019/3 (Sheldrick, 2015) using full matrix least squares minimisation on F2.

Crystal Data. C108N24O32Zr6, Mr = 2692.64, cubic, Fm-3m (No. 225), a = 32.3755(6) Å, b = 32.3755(6) Å, c = 32.3755(6) Å,  =  =  = 90°, V = 33935.2(18) Å3, T = 170(40) K, Z = 4, Z' = 0.020833, (Cu K) = 1.714, 10637 reflections measured, 1668 unique (Rint = 0.0300) which were used in all calculations. The final wR2 was 0.1718 (all data) and R1 was 0.0591 (I≥2 (I)).

| Compound | mm019 |
| --- | --- |
| Formula | C108N24O32Zr6 |
| Dcalc./ g cm-3 | 0.527 |
| /mm-1 | 1.714 |
| Formula Weight | 2692.64 |
| Colour | clear pale yellow |
| Shape | prism-shaped |
| Size/mm3 | 0.10×0.08×0.07 |
| T/K | 170(40) |
| Crystal System | cubic |
| Space Group | Fm-3m |
| a/Å | 32.3755(6) |
| b/Å | 32.3755(6) |
| c/Å | 32.3755(6) |
| /° | 90 |
| /° | 90 |
| /° | 90 |
| V/Å3 | 33935.2(18) |
| Z | 4 |
| Z' | 0.020833 |
| Wavelength/Å | 1.54184 |
| Radiation type | Cu K |
| min/° | 2.364 |
| max/° | 74.645 |
| Measured Refl's. | 10637 |
| Indep't Refl's | 1668 |
| Refl's I≥2 (I) | 1342 |
| Rint | 0.0300 |
| Parameters | 54 |
| Restraints | 109 |
| Largest Peak | 1.103 |
| Deepest Hole | -0.504 |
| GooF | 1.101 |
| wR2 (all data) | 0.1718 |
| wR2 | 0.1646 |
| R1 (all data) | 0.0655 |
| R1 | 0.0591 |

Structure Quality Indicators

| Reflections: |  |
| --- | --- |
| Refinement: |  |

A clear pale yellow prism-shaped crystal with dimensions 0.10 × 0.08 × 0.07 mm3 was mounted. Data were collected using a XtaLAB Synergy R, DW system, HyPix-Arc 150 diffractometer operating at T = 170(40) K.

Data were measured using  scans with Cu K radiation. The diffraction pattern was indexed and the total number of runs and images was based on the strategy calculation from the program CrysAlisPro 1.171.42.93a (Rigaku OD, 2023). The maximum resolution that was achieved was  = 74.645° (0.80 Å).

The unit cell was refined using CrysAlisPro 1.171.42.93a (Rigaku OD, 2023) on 3326 reflections, 31% of the observed reflections.

Data reduction, scaling and absorption corrections were performed using CrysAlisPro 1.171.42.93a (Rigaku OD, 2023). The final completeness is 98.60 % out to 74.645° in . An analytical absorption correction was performed using CrysAlisPro 1.171.42.93a (Rigaku Oxford Diffraction, 2023). The analytical numeric absorption correction was done using a multifaceted crystal model based on expressions derived by R.C. Clark & J.S. Reid. (Clark, R. C. & Reid, J. S. (1995). Acta Cryst. A51, 887-897). The empirical absorption correction was carried out using spherical harmonics, implemented in SCALE3 ABSPACK scaling algorithm. The absorption coefficient  of this crystal is 1.714 mm-1 at this wavelength ( = 1.54184Å) and the minimum and maximum transmissions are 0.886 and 0.908.

The structure was solved and the space group Fm-3m (# 225) determined by the ShelXT (Sheldrick, 2015) structure solution program using dual methods and refined by full matrix least squares minimisation on F2 using version 2019/3 of ShelXL (Sheldrick, 2015). All non-hydrogen atoms were refined anisotropically. Hydrogen atom positions were not included in the model.

_smtbx_masks_special_details: A solvent mask was calculated and 5622 electrons were found in a volume of 25977Å3 in 1 void per unit cell. This is consistent with the presence of 36[C3H7NO] per Asymmetric Unit which account for 5760 electrons per unit cell.

The value of Z' is 0.020833. The moiety formula is C108 N24 O32 Zr6.

Data Plots: Diffraction Data

Data Plots: Refinement and Data

Reflection Statistics

| Total reflections (after filtering) | 10637 | Unique reflections | 1668 |
| --- | --- | --- | --- |
| Completeness | 0.938 | Mean I/ | 30.81 |
| hklmax collected | (23, 34, 35) | hklmin collected | (-26, -13, -38) |
| hklmax used | (22, 27, 38) | hklmin used | (0, 0, 1) |
| Lim dmax collected | 100.0 | Lim dmin collected | 0.77 |
| dmax used | 18.69 | dmin used | 0.8 |
| Friedel pairs | 146 | Friedel pairs merged | 1 |
| Inconsistent equivalents | 0 | Rint | 0.03 |
| Rsigma | 0.0219 | Intensity transformed | 0 |
| Omitted reflections | 0 | Omitted by user (OMIT hkl) | 0 |
| Multiplicity | (6745, 1943, 2) | Maximum multiplicity | 24 |
| Removed systematic absences | 0 | Filtered off (Shel/OMIT) | 0 |

Table 1: Fractional Atomic Coordinates (×104) and Equivalent Isotropic Displacement Parameters (Å2×103) for mm019. Ueq is defined as 1/3 of the trace of the orthogonalised Uij.

| Atom | x | y | z | Ueq |
| --- | --- | --- | --- | --- |
| Zr1 | 5000 | 4240.0(2) | 5000 | 50.7(3) |
| O1 | 5371.8(12) | 4628.2(12) | 5371.8(12) | 95(2) |
| O2 | 4406.2(12) | 3907.6(10) | 5000 | 102.5(12) |
| N1 | 2569(4) | 3631(6) | 5000 | 354(8) |
| N2 | 2782(2) | 2782(2) | 5000 | 374(6) |
| C1 | 4031.2(15) | 4031.2(15) | 5000 | 172(4) |
| C2 | 3708.3(17) | 3708.3(17) | 5000 | 217(4) |
| C3 | 3302(2) | 3831(3) | 5000 | 258(4) |
| C4 | 3002(3) | 3516(2) | 5000 | 308(4) |
| C5 | 3110(3) | 3110(3) | 5000 | 341(5) |
| C6 | 2341(3) | 2995(3) | 5000 | 395(6) |

Table 2: Anisotropic Displacement Parameters (×104) for mm019. The anisotropic displacement factor exponent takes the form: -22[h2a*2 × U11+ ... +2hka* × b* × U12]

| Atom | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- |
| Zr1 | 61.7(3) | 28.8(3) | 61.7(3) | 0 | 0 | 0 |
| O1 | 95(2) | 95(2) | 95(2) | -41(2) | 41(2) | -41(2) |
| O2 | 100(2) | 65(2) | 142(3) | 0 | 0 | -39.9(19) |
| N1 | 138(5) | 250(11) | 670(20) | 0 | 0 | -123(6) |
| N2 | 198(5) | 198(5) | 727(15) | 0 | 0 | -142(7) |
| C1 | 87(2) | 87(2) | 341(11) | 0 | 0 | -56(3) |
| C2 | 120(3) | 120(3) | 413(10) | 0 | 0 | -87(4) |
| C3 | 115(3) | 162(5) | 498(10) | 0 | 0 | -94(4) |
| C4 | 143(4) | 192(5) | 589(11) | 0 | 0 | -122(5) |
| C5 | 183(4) | 183(4) | 655(13) | 0 | 0 | -132(6) |
| C6 | 203(6) | 212(8) | 768(17) | 0 | 0 | -132(8) |

Table 3: Bond Lengths in Å for mm019.

| Atom | Atom | Length/Å |  |
| --- | --- | --- | --- |
| Zr1 | Zr11 | 3.4798(7) |
| Zr1 | Zr12 | 3.4798(7) |
| Zr1 | Zr13 | 3.4798(7) |
| Zr1 | Zr14 | 3.4798(7) |
| Zr1 | O15 | 2.116(2) |
| Zr1 | O16 | 2.116(2) |
| Zr1 | O17 | 2.116(2) |
| Zr1 | O1 | 2.116(2) |
| Zr1 | O27 | 2.203(3) |
| Zr1 | O28 | 2.203(3) |
| Zr1 | O29 | 2.203(3) |
| Zr1 | O2 | 2.203(3) |
| O2 | C1 | 1.278(5) |
| N1 | C4 | 1.450(15) |
| N2 | C5 | 1.502(15) |
| N2 | C610 | 1.585(11) |
| N2 | C6 | 1.585(11) |
| C1 | C2 | 1.478(9) |
| C2 | C310 | 1.374(8) |
| C2 | C3 | 1.374(8) |
| C3 | C4 | 1.408(8) |
| C4 | C5 | 1.361(7) |
| C6 | C611 | 1.541(14) |

––––

11-z,1-x,1-y; 2+z,+x,+y; 3+y,+z,+x; 41-y,1-z,1-x; 5+x,+y,1-z; 61-x,+y,+z; 71-x,+y,1-z; 81-z,+y,+x; 9+z,+y,1-x; 10+y,+x,1-z; 111/2-y,1/2-x,+z

Table 4: Bond Angles in ° for mm019.

| Atom | Atom | Atom | Angle/° |  |
| --- | --- | --- | --- | --- |
| Zr11 | Zr1 | Zr12 | 60.002(1) |
| Zr13 | Zr1 | Zr14 | 60.0 |
| Zr11 | Zr1 | Zr14 | 60.0 |
| Zr11 | Zr1 | Zr13 | 90.003(1) |
| Zr12 | Zr1 | Zr13 | 60.0 |
| Zr12 | Zr1 | Zr14 | 90.0 |
| O15 | Zr1 | Zr11 | 88.98(15) |
| O15 | Zr1 | Zr13 | 34.69(8) |
| O15 | Zr1 | Zr14 | 88.98(15) |
| O16 | Zr1 | Zr11 | 34.69(8) |
| O17 | Zr1 | Zr13 | 34.69(8) |
| O1 | Zr1 | Zr14 | 88.98(15) |
| O17 | Zr1 | Zr14 | 34.69(8) |
| O1 | Zr1 | Zr11 | 34.69(8) |
| O16 | Zr1 | Zr13 | 88.98(15) |
| O15 | Zr1 | Zr12 | 34.69(8) |
| O1 | Zr1 | Zr13 | 88.98(15) |
| O16 | Zr1 | Zr12 | 88.98(15) |
| O16 | Zr1 | Zr14 | 34.69(8) |
| O17 | Zr1 | Zr12 | 88.98(15) |
| O1 | Zr1 | Zr12 | 34.69(8) |
| O17 | Zr1 | Zr11 | 88.98(15) |
| O16 | Zr1 | O17 | 69.34(18) |
| O16 | Zr1 | O1 | 69.34(18) |
| O15 | Zr1 | O1 | 69.34(18) |
| O17 | Zr1 | O1 | 107.1(4) |
| O15 | Zr1 | O16 | 107.1(4) |
| O15 | Zr1 | O17 | 69.34(18) |
| O17 | Zr1 | O28 | 141.86(4) |
| O16 | Zr1 | O28 | 141.86(4) |
| O1 | Zr1 | O27 | 78.09(16) |
| O16 | Zr1 | O29 | 78.10(16) |
| O17 | Zr1 | O27 | 141.86(4) |
| O17 | Zr1 | O29 | 78.10(16) |
| O15 | Zr1 | O29 | 141.86(4) |
| O1 | Zr1 | O29 | 141.86(4) |
| O1 | Zr1 | O2 | 141.86(4) |
| O1 | Zr1 | O28 | 78.09(16) |
| O15 | Zr1 | O2 | 78.10(16) |
| O15 | Zr1 | O28 | 78.10(16) |
| O17 | Zr1 | O2 | 78.10(16) |
| O15 | Zr1 | O27 | 141.86(4) |
| O16 | Zr1 | O27 | 78.10(16) |
| O16 | Zr1 | O2 | 141.86(4) |
| O28 | Zr1 | Zr13 | 110.20(7) |
| O29 | Zr1 | Zr14 | 74.23(10) |
| O28 | Zr1 | Zr12 | 74.23(10) |
| O27 | Zr1 | Zr12 | 110.20(7) |
| O27 | Zr1 | Zr14 | 110.20(7) |
| O2 | Zr1 | Zr12 | 110.20(7) |
| O29 | Zr1 | Zr12 | 164.24(10) |
| O29 | Zr1 | Zr11 | 110.20(7) |
| O28 | Zr1 | Zr14 | 164.24(10) |
| O28 | Zr1 | Zr11 | 110.20(7) |
| O2 | Zr1 | Zr14 | 110.20(7) |
| O27 | Zr1 | Zr11 | 74.23(10) |
| O2 | Zr1 | Zr11 | 164.24(10) |
| O29 | Zr1 | Zr13 | 110.20(7) |
| O2 | Zr1 | Zr13 | 74.24(10) |
| O27 | Zr1 | Zr13 | 164.24(10) |
| O29 | Zr1 | O27 | 76.20(9) |
| O28 | Zr1 | O2 | 76.20(9) |
| O27 | Zr1 | O2 | 121.5(2) |
| O28 | Zr1 | O27 | 76.20(9) |
| O29 | Zr1 | O28 | 121.5(2) |
| O29 | Zr1 | O2 | 76.20(9) |
| Zr1 | O1 | Zr12 | 110.62(17) |
| Zr11 | O1 | Zr12 | 110.62(17) |
| Zr1 | O1 | Zr11 | 110.62(17) |
| C1 | O2 | Zr1 | 132.5(4) |
| C5 | N2 | C6 | 109.2(5) |
| C5 | N2 | C610 | 109.2(5) |
| C610 | N2 | C6 | 141.6(11) |
| O210 | C1 | O2 | 126.5(6) |
| O2 | C1 | C2 | 116.8(3) |
| O210 | C1 | C2 | 116.8(3) |
| C3 | C2 | C1 | 118.2(5) |
| C310 | C2 | C1 | 118.2(5) |
| C310 | C2 | C3 | 123.6(9) |
| C2 | C3 | C4 | 116.8(9) |
| C3 | C4 | N1 | 118.8(10) |
| C5 | C4 | N1 | 119.8(10) |
| C5 | C4 | C3 | 121.4(10) |
| C4 | C5 | N2 | 120.0(6) |
| C410 | C5 | N2 | 120.0(6) |
| C4 | C5 | C410 | 119.9(13) |
| C611 | C6 | N2 | 109.2(5) |

––––

11-y,1-z,1-x; 21-z,1-x,1-y; 3+y,+z,+x; 4+z,+x,+y; 51-x,+y,+z; 6+x,+y,1-z; 71-x,+y,1-z; 8+z,+y,1-x; 91-z,+y,+x; 10+y,+x,1-z; 111/2-y,1/2-x,+z

Table 5: Torsion Angles in ° for mm019.

| Atom | Atom | Atom | Atom | Angle/° |
| --- | --- | --- | --- | --- |
| Zr1 | O2 | C1 | O21 | 0.0 |  |
| Zr1 | O2 | C1 | C2 | 180.0 |  |
| O21 | C1 | C2 | C3 | 0.0 |  |
| O2 | C1 | C2 | C31 | 0.0 |  |
| O21 | C1 | C2 | C31 | 180.0 |  |
| O2 | C1 | C2 | C3 | 180.0 |  |
| N1 | C4 | C5 | N2 | 0.0 |  |
| N1 | C4 | C5 | C41 | 180.0 |  |
| C1 | C2 | C3 | C4 | 180.0 |  |
| C2 | C3 | C4 | N1 | 180.0 |  |
| C2 | C3 | C4 | C5 | 0.0 |  |
| C31 | C2 | C3 | C4 | 0.0 |  |
| C3 | C4 | C5 | N2 | 180.0 |  |
| C3 | C4 | C5 | C41 | 0.0 |  |
| C5 | N2 | C6 | C62 | 180.0 |  |
| C6 | N2 | C5 | C41 | 180.0 |  |
| C61 | N2 | C5 | C4 | 180.0 |  |
| C6 | N2 | C5 | C4 | 0.0 |  |
| C61 | N2 | C5 | C41 | 0.0 |  |
| C61 | N2 | C6 | C62 | 0.0 |  |

––––

1+y,+x,1-z; 21/2-y,1/2-x,+z

Table 6: Atomic Occupancies for all atoms that are not fully occupied in mm019.

| Atom | Occupancy |
| --- | --- |
| N1 | 0.5 |

Table 7: Solvent masking (PLATON/SQUEEZE) information for mm019.

| No | x | y | z | V | e | Content |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | -0.527 | -0.012 | -0.775 | 25977.0 | 5622.4 | 144DMF |

Citations

CrysAlisPro Software System, Rigaku Oxford Diffraction, (2023).

O.V. Dolomanov and L.J. Bourhis and R.J. Gildea and J.A.K. Howard and H. Puschmann, Olex2: A complete structure solution, refinement and analysis program, J. Appl. Cryst., (2009), 42, 339-341.

Sheldrick, G.M., Crystal structure refinement with ShelXL, Acta Cryst., (2015), C71, 3-8.

Sheldrick, G.M., ShelXT-Integrated space-group and crystal-structure determination, Acta Cryst., (2015), A71, 3-8.