## Slide 1
Graphite surface functionalisation in water medium using pulsed plasma:
Romain Chevigny
MRM 2025 Yokohama, Japan
Influence of liquid matrix and gas atmosphere

## Slide 2: European Pathfinder project WoundSens
Consortium between 3 laboratories – 3 expertise – 3 countries: Multidisciplinarity (Startup, academic lab, hybrid lab)
Development of smart bandages for the real-time early detection of wound infections
Obtaining enzyme-loaded conductive hollow polymer fibres

## Slide 3: European Pathfinder project WoundSens
Uric acid
Uric acid is produced infected wounds
Uricase is tasked to decompose it into hydrogen peroxide, generating electrons through redox reactions
Integrated sensor to detect the electrical signal conducted by the carbon material
Uricase
Electrospinning

## Slide 4: European Pathfinder project WoundSens
Aims of the Jean Lamour Institute :
Conductive carbon materials (electrical percolation)
Surface functionalisation (dispersion within the polymer)
antagonist: precise control of the process
Uric acid
Uricase

## Slide 5: Plasma-assisted treatment in aqueous media
Atmosphere: air
Voltage: 6 kV
Frequency: 6 kHz
Pulse duration: 1000 ns
Treatment duration: 60 min
Concentration: 0.3 mg.mL-1
1000 ns
Plasma arc 22 s
Joint project 201 & 205 teams
Technological maturation project ExFoGraP funded by Satt Sayens

## Slide 6: Plasma-assisted treatment in aqueous media
Stabilisation around 9 – 10 A
Transition to a stable power after ~ 30 min treatment
Stable regime
~ 15 kW
Transient regime

## Slide 7: Plasma-assisted treatment in aqueous media
Transmission electron microscopy
Before treatment
Treatment 1 h, 6 kHz, 1 µs
no amorphous carbon
signs of partial exfoliation
HR-TEM in progress using EELS spectroscopy
Treatment 2 h, 6 kHz, 1 µs
Treatment 1 h, 600 Hz, 10 µs
Natural
expanded graphite
Commercial
synthetic graphite

## Slide 8: Plasma-assisted treatment in aqueous media
Raman spectroscopy (λ = 633 nm)
D
G
2D
ID/IG = 0.04  0.16
 few induced structural defects
SFG
SFG_1a
Wavenumber (cm-1)
Intensity (counts)

## Slide 9: Plasma-assisted treatment in aqueous media
Thermogravimetric analysis in air

## Slide 10: Plasma-assisted treatment in aqueous media
Thermogravimetric analysis in helium coupled with mass spectrometry
CO
CO2
 presence of oxygen functions on the surface
pristine
SFG_1a
SFG_1af
SFG_2a

## Slide 11: Plasma-assisted treatment in aqueous media
CO
CO2
pristine
 presence of oxygen functions on the surface
Thermogravimetric analysis in helium coupled with mass spectrometry

## Slide 12: Plasma-assisted treatment in aqueous media
X-ray photoelectron spectroscopy
C1s
O1s
W4f
 increase of the oxygen content
O1s
Sample | C 1s (At%) | O 1s (At%)
SFG | 97 | 3
SFG_1a | 94 | 6
SFG_1af | 91 | 9
SFG_2a | 90 | 10
Na 1s

## Slide 13: Plasma-assisted treatment in aqueous media
Electrical conductivity measurements of elaborated materials
Van de Pauw method (conductive materials)
Electrometer (resistive materials)

## Slide 14: Plasma-assisted treatment in aqueous media
Dispersion within the polymer matrix and measure of the bulk electrical conductivity (non electrospun)
Polycaprolactone (PCL)
Electrical conductivity measurements of elaborated materials
SFG
EG
Percolation not reached
1 wt%
3 wt%
5 wt%
5 wt%
Inhomogeneous

## Slide 15: Ongoing and future research
Studies on the composite fibres behaviour
  Electrical conductivity
  Porosity
  Stability and activity of the enzyme after electrospinning