Trimodal Nanoparticle Contrast Agent for CT, MRI and SPECT imaging: Synthesis and Characterization of Radiolabeled Core/Shell Iron Oxide@Gold Nanoparticles

Menachem Motiei, #1 Tamar Dreifuss, #1 Tamar Sadan, 1 Noam Omer, 2 Tamar B. Katzir, 2 Eirini Fragogeorgi, 3 George Loudos, 3,4 Rachela Popovtzer, *1 and Noam Ben-Eliezer 2,5,6

1Faculty of Engineering and the Institutes of Nanotechnology and Advanced Materials, Bar-Ilan University, Ramat-Gan, Israel

2Department of Biomedical Engineering, Tel Aviv University, Tel Aviv, Israel

3Institute of Nuclear & Radiological Sciences, Technology, Energy & Safety, NCSR ‘‘Demokritos”, Ag. Paraskevi 15310, Athens, Greece

4Bioemission Technology Solutions, Alexandras Avenue 116, 11472, Athens, Greece / Lefkippos Attica Technology Park NCSR “Demokritos”Ag. Paraskevi 15310, Athens, Greece

5Sagol School of Neuroscience, Tel Aviv University, Tel Aviv, Israel

6Center for Advanced Imaging Innovation and Research (CAI2R), New-York University Langone Medical Center, New York, NY, USA

E-mail: Rachela.Popovtzer@biu.ac.il

Recently, nanoparticles have emerged as promising contrast agents for various imaging applications. In this paper, we present the synthesis and characterization of a novel hybrid nano-structure, consisting of an iron oxide@gold nanoparticle, labeled with technetium-99m, for trimodal SPECT/CT/MRI imaging.  The particles showed efficient capabilities as CT/MRI imaging agent and high radiochemical yield, indicating a potential single hybrid material for multimodal SPECT/CT/MRI.

Keywords: Multimodal imaging, nanoparticle contrast agents, core/shell nanoparticles

The idea of multimodal imaging, integrating two or more imaging modalities, has been emerging as a promising strategy for improving clinical and preclinical imaging1–3. Among the various clinically-used imaging techniques, computed tomography (CT), magnetic resonance imaging (MRI), and nuclear imaging are widely used for disease diagnosis, each providing different and complementary information about the patient. CT offers sensitivity to electron-dense elements such as bones, and delivers detailed anatomic information of the musculoskeletal system. However, it is limited in soft-tissue imaging applications. MRI enables detailed delineation of soft-tissue structures but it is less efficient in detecting lesions of bony structures4. Nuclear imaging, in particular single photon emission computed tomography (SPECT) and positron emission tomography (PET), offer the ability to track radiolabeled biomarkers with a very high detection sensitivity reaching below the picomolar range5. Yet, it suffers from poor spatial resolution, which led to the development of integrated SPECT or PET/CT and SPECT or PET/MRI scanners.  The combination of these technologies allows each technique to recompense the limitations of the other, and provide complementary information with higher accuracy.

To further improve the sensitivity and specificity of the above imaging modalities, various types of contrast agents have been developed. Nanoparticles have emerged as a promising class of contrast agents for in vivo imaging applications, providing improved imaging and targeting capabilities compared to the commonly used contrast compounds6–8. Moreover, nanoparticles offer an efficient platform for multimodal imaging, by facilitating the combination of different imaging agents into one hybrid material9.

In the current study, we present a novel core/shell iron oxide@gold nanoparticle design (Fig. 1A), with potential to be radiolabeled, and, as preliminary results indicate, suitable for CT, MRI, and SPECT imaging. While the magnetic iron oxide core serves to enhance MRI signal, the gold shell produces strong CT contrast. Although some Au and iron oxide hybrid nanoparticles were reported as CT/MRI contrast agents10–14, our new design offers higher Au mass ratio, precise control of the Fe/Au ratio, and ability to easily bind a variety of biological molecules to the particle surface. Moreover, our core/shell design further enables radiolabeling with various metal isotopes, thereby opening the door to trimodal CT-SPECT-MR imaging.

First, dextran T1-coated iron oxide nanoparticles were prepared according to previously published method15. Briefly, a mixture of ferric chloride hexahydrate (3 gr) and ferrous chloride tetrahydrate (1.5 gr) in 32 ml deionized water was mixed with dextran T1 (Mw=41 KDa) solution (1.7 gr in 20 ml deionized water) for 30 min, at room temperature under nitrogen flow. The mixture was cooled to 5 °C, and ammonium hydroxide (28%, 12.7 gr) was added under stirring over 2 min. Then, the mixture was heated to 60 °C for 40 min, and to 80 °C for 2 h. To allow coating of the particles with a gold shell in the next steps, the dextran coating was removed and replaced by a citrate layer. This was done by washing the solid phase twice with 10% sodium citrate solution followed by centrifugation (4000 rpm, 20 min).

Figure 1. (A) Scheme of radiolabeled glucose-coated Fe3O4@Au nanoparticle. Iron oxide core (center, grey) is surrounded by a gold shell, coated with a polyethylene glycol linker (black curved lines), conjugated to glucose molecules (red-white), or to 1,4,7,10-tetraazacyclododecane-1,4,7,10-tetraacetic acid (DOTA) molecules, as a chelating agent for the radioisotope (black-yellow, within DOTA). (B,C) Representative TEM images of (B) -Fe3O4 core nanoparticles, with a mean diameter of 8±2 nm; scale bar=100 nm (C) Final Fe3O4@Au nanoparticles; mean diameter 27 nm. Scale bar=20 nm.

After purification, the iron oxide particles pellet was dissolved in 10% sodium citrate solution to yield a final Fe concentration of 4 mg/ml, as measured by flame atomic absorption spectroscopy (FAAS). The size and shape of the obtained iron oxide nanoparticles (IONPs) were determined using transmission electron microscopy (TEM), which indicated uniformly distributed, spherical nanoparticles, with a mean diameter of 8±2 nm (Fig. 1B).

To form a gold shell on the IONPs, an Au solution (414 μl of 50% w/V HAuCl4 in 200 ml purified water) was heated until boiling, and 4.04 ml of the as-prepared IONP solution were added under stirring (10 min), yielding core-shell Fe3O4@Au nanoparticles. After cooling to room temperature, SH-PEG-COOH (1000 Da) solution (80 µl, 36.5 mg/ml) was added and stirred for 3 hrs. The PEG molecules surround the particle surface via thiol–gold interactions, providing stability in physiological solutions and external active carboxylic group for further surface modifications. Next, the particles were coated by both glucose molecules and tetraazacyclododecane tetraacetic acid (DOTA) chelator. DOTA was used to enable radiolabeling, and the glucose coating was chosen as we have previously shown that it allows effective nanoparticle uptake by cells, in vitro, for cell tracking applications, and in vivo, for cancer diagnosis16–21. D-(β)-glucosamine hydrochloride (30 µl, 25 mg/ml) was added to the solution together with N-ethyl-N-(3-(dimethylamino)-propyl) carbodiimide (EDC, 200µl, 10 mg/ml)  and N-hydroxysuccinimide (NHS, 200 µl, 10 mg/ml), followed by 3h stirring at room temperature, to yield glucose-coated Fe3O4@Au nanoparticles. After purification, DOTA-NH2 (1.3 mg) was added followed by 3h stirring at room temperature. Finally, the solution was centrifuged to purify the nanoparticles. For the radioactive study, the particles were labeled with Technetium-99m (99mTc), due to its relatively long half-life, and its extensive use in clinics. Characterization was conducted using TEM, energy dispersive X-ray (EDAX), UV-Vis spectroscopy and dynamic light scattering (DLS), and radio TLC for the radiolabeled particles.

TEM image of the Fe3O4@Au nanoparticles (Fig. 1C) demonstrated spherical nanoparticles, with a total mean diameter of 27 nm, indicating gold shell thickness of ~9.5 nm. The hydrodynamic diameter was ~140 nm, as measured by DLS. UV-vis spectra of Fe3O4@Au nanoparticles (Fig. S1) demonstrated a surface plasmon resonance peak at 522 nm, corresponding to the typical peak of gold nanoparticles with similar size.

EDAX analysis, performed to analyze the composition of Fe3O4@Au nanoparticles and determine the Fe:Au ratio, confirmed the presence of both Fe and Au in the final nanoparticle, and indicated weight percentages of 3.8% and 96.2% for Fe and Au, respectively (Fig. S2). This difference arises from the significantly larger mass of gold in the particle, together with the higher density of gold as compared to the iron oxide (19.32 gr/ml vs. 5.24 gr/ml, respectively). CT is limited by its low sensitivity to contrast agents, as compared with MRI and nuclear techniques22. X-ray attenuation of gold nanoparticles increases linearly with mass concentration, thus delivery of a greater mass concentration to sites of interest in vivo enables greater contrast enhancement23. The high gold-to-iron oxide mass ratio of our nanoparticle is thus critically important for allowing efficient and simultaneous CT and MRI detection.

To evaluate the Fe3O4@Au nanoparticles as contrast agents for MRI, solutions at different Fe concentrations, ranging from 2.5 µg/ml to 75 µg/ml, were scanned on a 3 Tesla clinical MRI scanner (Siemens Prisma). Image contrast, evaluated using standard MRI protocols (see Supporting Information (SI)), showed an effective MR contrast for the assayed range of nanoparticle concentrations. Qualitative T2* weighted MRI images (Fig. 2A) show the nanoparticles’ effectiveness in changing the image contrast compared to pure water and a manganese chloride (MnCl2) solution, which reduces the water relaxation values to a physiological range. Quantitative experiments were carried out to determine the accurate MR relaxation values of Fe3O4@Au nanoparticles in free-state.

All relaxation values decreased with an increasing nanoparticle concentration (Fig. 2B), yielding the following range of values for the nanoparticle solutions: T2=9…82 ms, T2*=4…34 ms, and T1=330…1742 ms. These match the typical values used in human MRI scans, covering both healthy and pathological tissue values24.

Figure 2. MRI dynamic contrast range of Fe3O4@Au nanoparticles. (A) MRI image of Fe3O4@Au nanoparticles at different Fe concentrations, #1-#6: 0.07, 0.14, 0.28, 0.70, 1.4, 2.1 mM. A positive contrast effect is seen with the increase of Fe3O4@Au nanoparticle concentration. (B) Quantification of Fe3O4@Au nanoparticle MR relaxation values in free-state. (I) R2 (=1/T2) relaxation. (II) R2* (=1/T2*) relaxation, (III) R1 (=1/T1) relaxation. Fe conc. shown up to 0.70 mM, as above this produced extremely rapid relaxation and very low signal at later echoes, preventing quantitative estimation of relaxation values.

Relaxivity values (in [mM-1 sec-1]) were R1= 3.86, R2=154.7, and R2*=346.6 (calculation in SI). Additionally, the concentration range of the MRI-active Fe compound is in accord with values reported in literature for in vitro models25; taken together with the relaxation values, this suggests that these Fe3O4@Au nanoparticles can generate contrast and enhance SNR in MR weighted imaging in vivo, even at low concentrations, which are more favorable for clinical use.

Next, the feasibility of Fe3O4@Au nanoparticles to be further used as CT contrast agents was assessed by scanning

the same nanoparticle samples used for the MRI experiment

in a micro-CT scanner (Skyscan High Resolution 1176; specifications in SI). Both Fe and Au concentrations of the samples were measured using FAAS (Fig. 3). The slight difference between the weight percentages obtained by EDAX and FAAS is attributed to the different measurement technologies and their deviations. Fig. 3 shows a clear visible contrast for nanoparticle samples with an Au concentration starting from 1 mg/ml. Quantification of the mean greyscale values demonstrated, as expected, a linear correlation between the observed CT contrast and the nanoparticle concentration. The lower sensitivity of the CT compared to the MRI to detect nanoparticles in small concentrations, highlights the importance of our large-thick-shell design, in which the Au volume is much higher than that of the Fe3O4 core.

Figure 3. Fe3O4@Au nanoparticles as CT contrast agent. (A) CT images of Fe3O4@Au nanoparticles at different Au concentrations, ranging from 0.1 mg/ml to 3 mg/ml. (B) Summary of nanoparticle concentrations in the samples. (C) Correlation between CT signal intensity and gold concentration.

Preliminary experiments on radiolabeling of the DOTA-glucose-coated Fe3O4@Au nanoparticles were conducted, by radiolabeling with 99mTc using the direct labelling approach26,27, in the presence of stannous chloride used as a reducing agent. This approach achieved a labelling incorporation as high as 98%.

The two-strip Instant Thin Layer Chromatography Silica Gel (ITLC-SG) method for analysis of [99mTc]Τc-DOTA-glucose-coated Fe3O4@Au nanoparticles ([99mTc]Tc-trimodal particle) showed that no amount of either pertechnetate ([99mTc]TcO4-) (Fig. 4A) or colloidal ([99mTc]TcO2) (Fig. 4B) was present. Free pertechnetate was not determined when developed on acetone as eluent, as if there was any, it would migrate to the front of the ITLC- SG strip (retardation factor (Rf)=0.8–1.0), while leaving the reduced/hydrolyzed [99mTc]TcO2 ([99mTc]99mTc-colloids) and the [99mTc]Tc-trimodal particle at the origin (Rf=0.0).

Colloid formation was also undetected (Rf=0.0) by using the same stationary phase (ITLC-SG), but a mobile phase of pyridine/acetic acid/water (3/5/1.5), where the [99mTc]Tc- trimodal particle migrated to the front along with [99mTc] 99mTcO4- (Rf=1.0). With the combination of these two solvent systems, the percentage of the [99mTc]Tc-trimodal particle derived and the radiochemical yield was higher than 98%, providing a single radioactive species. Stability tests showed stability up to 24h post preparation.

Figure 4. Radio TLC of [99mTc]Tc-DOTA-glucose-coated Fe3O4@Au nanoparticles ([99mTc]Tc-trimodal particle) developed on ITLC-SG chromatography paper with (A) aceton and (B) pyridine/acetic acid/water (3/5/1.5) as mobile phases.

DOTA-modified nanoparticles were radiolabeled by a straightforward methodology26,27, leading to a high complexation rate of 99mTc.  It is also notable that there was no need for further purification of the radiolabeled nanoparticles via a size exclusion column, a method previously used in a study based on a Fe3O4-Au particle28 coated with various ligands and complexed with 99mTc(I) via the organometallic, tri-carbonyl chemistry, where the radiolabeling yield ranged between 24% to 52%28 (which is lower than our result of >98%). Moreover, MRI and CT abilities of the above particle28, and of many other iron oxide core-gold shell nanoparticles (reviewed in29) were not examined, possibly due to a relatively thin gold shell (ranging between 0.54 nm28,30) that likely would not enable CT imaging, due to the lower CT sensitivity to contrast agents22, necessitating a higher gold mass23. Composite dual-modal Fe3O4-Au particles31,32 have been imaged, yet they lack the simpler spherical structure of our particles.

Others have shown multi-modal nanoparticles for CT, MRI and near-infrared imaging33–35; yet the latter modality has limited tissue penetration (<1-4 cm)36. Using our approach, a single nanoparticle enables use of three different imaging modalities, all with deep tissue imaging abilities. Future studies will investigate the imaging efficacy in vivo.  The variability in required concentrations between SPECT, CT and MRI can be easily circumvented by radioactively tagging only a fraction of the nanoparticles and creating mixtures with different relative amounts.

Altogether, the results demonstrate a highly effective nanoparticle, with a mean diameter of 27 nm, composed of a 8 nm-iron oxide core and a 9.5 nm-thick gold shell, with a proven efficacy as a dual-modal CT/MRI imaging agent and potential multimodal SPECT/CT/MRI. The combination of these clinically-available imaging modalities in one system can enable scanning patients with all three systems on the same day, and following a single injection; it can also provide improved spatial, temporal and functional information. This particle is in the size range that we have previously shown to be optimal for theranostics - combined treatment and diagnostics37,38. We have previously designed gold nanoparticles conjugated to various moieties20,38 for tumor targeting; moreover, the glucose coating enhances uptake by various cell types both in vitro and in vivo16,20,39, suggesting that the trimodal particles presented herein have potential to serve as a unique platform for precision imaging.

References and Notes

1.	Dreifuss, T., Barnoy, E., Motiei, M. & Popovtzer, R. Theranostic Gold Nanoparticles for CT Imaging. in Design and Applications of Nanoparticles in Biomedical Imaging (eds. Bulte, J. W. M. & Modo, M. M. J.) 403–427 (Springer International Publishing, 2017). doi:10.1007/978-3-319-42169-8_19

2.	Poß, M. et al. Multimodal [GdO] + [ICG] − Nanoparticles for Optical, Photoacoustic, and Magnetic Resonance Imaging. Chem. Mater. 29, 3547–3554 (2017).

3.	Gálisová, A. et al. Multimodal Imaging Reveals Improvement of Blood Supply to an Artificial Cell Transplant Site Induced by Bioluminescent Mesenchymal Stem Cells. Mol. Imaging Biol. 19, 15–23 (2017).

4.	Hou, W. et al. Nanoparticles for multi-modality cancer diagnosis: Simple protocol for self-assembly of gold nanoclusters mediated by gadolinium ions. (2017). doi:10.1016/j.biomaterials.2016.12.027

5.	Judenhofer, M. S. et al. Simultaneous PET-MRI: a new approach for functional and morphological imaging. Nat. Med. 14, 459–465 (2008).

6.	Na, H. Bin, Song, I. C. & Hyeon, T. Inorganic Nanoparticles for MRI Contrast Agents. Adv. Mater. 21, 2133–2148 (2009).

7.	Hainfeld, J. F., Slatkin, D. N., Focella, T. M. & Smilowitz, H. M. Gold nanoparticles: a new X-ray contrast agent. Br. J. Radiol. 79, 248–253 (2006).

8.	Hahn, M. A., Singh, A. K., Sharma, P., Brown, S. C. & Moudgil, B. M. Nanoparticles as contrast agents for in-vivo bioimaging: current status and future perspectives. Anal. Bioanal. Chem. 399, 3–27 (2011).

9.	Li, X., Zhang, X.-N., Li, X.-D. & Chang, J. Multimodality imaging in nanomedicine and nanotheranostics. Cancer Biol. Med. 13, 339–348 (2016).

10.	Cai, H. et al. Facile assembly of Fe 3 O 4 @Au nanocomposite particles for dual mode magnetic resonance and computed tomography imaging applications. J. Mater. Chem. 22, 15110–15120 (2012).

11.	Yang, M. et al. Affibody modified and radiolabeled gold–Iron oxide hetero-nanostructures for tumor PET, optical and MR imaging. Biomaterials 34, 2796–2806 (2013).

12.	Narayanan, S. et al. Biocompatible magnetite/gold nanohybrid contrast agents via green chemistry for MRI and CT bioimaging. ACS Appl. Mater. Interfaces 4, 251–60 (2012).

13.	Zhu, J. et al. Synthesis of Au–Fe 3 O 4 heterostructured nanoparticles for in vivo computed tomography and magnetic resonance dual model imaging. Nanoscale 6, 199–202 (2014).

14.	Kim, D. et al. Amphiphilic polymer-coated hybrid nanoparticles as CT/MRI dual contrast agents. Nanotechnology 22, 155101 (2011).

15.	Paul, K. G., Frigo, T. B., Jesse Y. Groman, A. & Groman, E. V. Synthesis of Ultrasmall Superparamagnetic Iron Oxides Using Reduced Polysaccharides. Bioconjug. Chem. 15, 394–401 (2004).

16.	Betzer, O. et al. In-vitro Optimization of Nanoparticle-Cell Labeling Protocols for In-vivo Cell Tracking Applications. Sci. Rep. 5, 15400 (2015).

17.	Meir, R. et al. Design principles for noninvasive, longitudinal and quantitative cell tracking with nanoparticle-based CT imaging. Nanomedicine Nanotechnology, Biol. Med. 13, 421–429 (2017).

18.	Betzer, O. et al. Nanoparticle-Based CT Imaging Technique for Longitudinal and Quantitative Stem Cell Tracking within the Brain: Application in Neuropsychiatric Disorders. ACS Nano 8, 9274–9285 (2014).

19.	Meir, R. et al. Nanomedicine for Cancer Immunotherapy: Tracking Cancer-Specific T-Cells in Vivo with Gold Nanoparticles and CT Imaging. ACS Nano 9, 6363–72 (2015).

20.	Motiei, M. et al. Differentiating between Cancer and Inflammation: A Metabolic-Based Method for Functional Computed Tomography Imaging. ACS Nano 10, 3469–77 (2016).

21.	Dreifuss, T. et al. Uptake mechanism of metabolic-targeted gold nanoparticles. Nanomedicine 13, 1535–1549 (2018).

22.	Cormode, D. P., Naha, P. C. & Fayad, Z. A. Nanoparticle contrast agents for computed tomography: a focus on micelles. Contrast Media Mol. Imaging 9, 37–52 (2014).

23.	Cole, L. E., Ross, R. D., Tilley, J. M., Vargo-Gogola, T. & Roeder, R. K. Gold nanoparticles as contrast agents in x-ray imaging and computed tomography. Nanomedicine 10, 321–341 (2015).

24.	Stanisz, G. J. et al. T1, T2 relaxation and magnetization transfer in tissue at 3T. Magn. Reson. Med. 54, 507–512 (2005).

25.	Vithanarachchi, S. M. & Allen, M. J. Strategies for Target-Specific Contrast Agents for Magnetic Resonance Imaging. Curr. Mol. Imaging 1, 12–25 (2012).

26.	Psimadas, D. et al. Radiolabeling approaches of nanoparticles with 99m Tc. Contrast Media Mol. Imaging 8, 333–339 (2013).

27.	Kostopoulou, A. et al. Iron Oxide Colloidal Nanoclusters as Theranostic Vehicles and Their Interactions at the Cellular Level. Nanomaterials 8, 315 (2018).

28.	Felber, M. & Alberto, R. 99m Tc radiolabelling of Fe 3 O 4 –Au core–shell and Au–Fe 3 O 4 dumbbell-like nanoparticles. Nanoscale 7, 6653–6660 (2015).

29.	Salihov, S. V. et al. Recent advances in the synthesis of Fe3O4@AU core/shell nanoparticles. J. Magn. Magn. Mater. 394, 173–178 (2015).

30.	Recent advances in the development of nanomaterials for DC-based immunotherapy. Sci. Bull. 61, 514–523 (2016).

31.	Li, J. et al. Facile One-Pot Synthesis of Fe 3 O 4 @Au Composite Nanoparticles for Dual-Mode MR/CT Imaging Applications. (2013). doi:10.1021/am4034526

32.	Cai, H. et al. Dendrimer-Assisted Formation of Fe 3 O 4 /Au Nanocomposite Particles for Targeted Dual Mode CT/MR Imaging of Tumors. Small 11, 4584–4593 (2015).

33.	van Schooneveld, M. M. et al. A fluorescent, paramagnetic and PEGylated gold/silica nanoparticle for MRI, CT and fluorescence imaging. Contrast Media Mol. Imaging 5, 231–236 (2010).

34.	Li, J. et al. Hyaluronic acid-modified Fe3O4@Au core/shell nanostars for multimodal imaging and photothermal therapy of tumors. Biomaterials 38, 10–21 (2015).

35.	Hsu, J. C. et al. An all-in-one nanoparticle (AION) contrast agent for breast cancer screening with DEM-CT-MRI-NIRF imaging. Nanoscale 10, 17236–17248 (2018).

36.	Zhu, B. & Sevick-Muraca, E. M. A review of performance of near-infrared fluorescence imaging devices used in clinical studies. Br. J. Radiol. 88, 20140547 (2015).

37.	Davidi, E. S. et al. Cisplatin-conjugated gold nanoparticles as a theranostic agent for head and neck cancer. Head Neck 40, 70–78 (2018).

38.	Meir, R. et al. Fast Image-Guided Stratification Using Anti-Programmed Death Ligand 1 Gold Nanoparticles for Cancer Immunotherapy. ACS Nano 11, 11127–11134 (2017).

39.	Hazkani, I. et al. Can molecular profiling enhance radiotherapy? Impact of personalized targeted gold nanoparticles on radiosensitivity and imaging of adenoid cystic carcinoma. Theranostics 7, 3962–3971 (2017).

This project received funding from the European Union’s Horizon 2020 research and innovation program under grant agreement #761031. This publication reflects only the author’s views and the European Union is not liable for any use that may be made of the information contained herein. We thank the Ministry of Science and Technology, Israel for T.D.’s scholarship, and partial support by Stavros Niarchos Foundation Industrial Scholarships, enhancing research in Greece. We thank Dr. Penelope Bouziotis, Research Director at the Radiochemical Studies Lab, for the radiolabeling studies at the National Center of Scientific Research “Demokritos”; and Chen Zror-Azankot for assistance with scheme creation.  #M.M. and T.D. contributed equally to this work.

Additional information included in the Supplementary Section.

NOTE   The diagram is acceptable in a colored form. Publication of the colored G.A. is free of charge.

For publication, electronic data of the colored G.A. should be submitted. Preferred data format is EPS, PS, CDX, PPT, and TIFF.

If the data of your G.A. is "bit-mapped image" data (not "vector data"), note that its print-resolution should be 300 dpi.

You are requested to put a brief abstract (50-60words, one paragraph style) with the graphical abstract you provided, so that readers can easily understand what the graphic shows.

| Graphical Abstract |  |
| --- | --- |
| Textual Information |  |
| A brief abstract (required) | This paper presents the synthesis and characterization of a novel hybrid nano-structure, consisting of iron oxide@gold nanoparticle, labeled with technetium-99m, for trimodal SPECT/CT/MRI imaging. |
| Title(required) | Trimodal Nanoparticle Contrast Agent for CT, MRI and SPECT imaging: Synthesis and Characterization of Radiolabeled Core/Shell Iron Oxide@Gold Nanoparticles |
| Authors’ Names(required) | Menachem Motiei, Tamar Dreifuss, Tamar Sadan, Noam Omer, Tamar B. Katzir, Eirini Fragogeorgi, George Loudos, Rachela Popovtzer, and Noam Ben-Eliezer |
| Graphical Information |  |