The Boron Oxide Glasses and Nanocomposites: Synthetic, Structural and Statistical Approach

Hristo Hristov1, Miroslava Nedialkova1*, Sergio Madurga2 and Vasil Simeonov1

1,1*Faculty of Chemistry and Pharmacy, University of Sofia, Sofia 1164, Bulgaria

2Physical Chemistry Department and Research Institute of Theoretical and Computational Chemistry (IQTCUB) of the University of Barcelona (UB), Barcelona 08028, Catalonia, Spain

* Corresponding author. Ph.D.; Tel.: +359 2 81 61 214.

E-mail address: mici345@yahoo.com (Miroslava Nedyalkova).

Three different precursors boron-aqua and glycerol solutions of boric acid and ethanol solution of trimethyl borate are used for the preparation of organic-inorganic advanced materials. The films and bulk materials samples are heat treated at 100oC, 400oC, 800oC for 2h. The hybrid samples are stable and transparent until 100oC. The further increase of temperature to 400oC is leading to samples destruction, and at 800oC, they are molten. The structural changes during the pyrolysis are studied by Fourier transform infrared spectroscopy, Differential Thermal analyzes, and X-ray diffraction. Details of surface morphology were observed by scanning electron microscopy. The obtained BO3 and BO4 groups are identified in the molten materials after pyrolysis. The quantities and order of borate structural units as well as residual carbon in the networks depend on boron precursor type. PVA/PEG/B2O3 hybrid materials are proved to be appropriate precursors for synthesizing borate and carboborate glass and carbon/borate glass nanocomposites. To access the impact of the experimental conditions on the structural changes of the nanocomposites, cluster analysis of the IR-spectral data was used as a classification method.

Key words: Organic-Inorganic Hybrid Materials; Borate glass; Nanocomposites; Cluster Analysis

- Introduction

Pure borate glass is made up of a random network including boroxol rings (B3O6) and threefold coordinate boron (BO3). The addition of modifiers (such as alkaline etc.,) supports the formation of BO4 groups in the glass structure. The structuring role of the network modifier is determined by its size, charge and network forming agent of the glass. Through sol-gel processing, homogeneous, high-purity inorganic oxide glasses can be made at ambient temperatures rather than at the very high temperatures as required in conventional approaches. The sol-gel process is a useful technique for processing a large number of technologically important glasses, glass-ceramics and crystalline ceramics, mainly because of its ability to generate stoichiometric materials with good control over final amount of compositions.

Significantly, less number of borate compositions is modified by low-temperature sol-gel technology. Special attention has been given to the effect of the ionic conductivity of alkali-borate glasses, especially of lithium-borate, and possibility of applications for solid state batteries and energy storage devices.[1-3] The hybrid borate hydrogel materials obtained by sol-gel technology with a combination of aqua soluble polymers, like polyvinyl alcohol (PVA) and polyethylene glycol (PEG), may have potential applications. Such materials are hybrids of borate esters applied as an electrolyte in lithium-ion batteries[4-8] and materials for medical and biotechnological applications.[9-11] Incorporations of boron in the polymer backbone are used for reinforcing carbon/carbon composite materials. As a result, carbon, active sites are blocked because it generates an oxygen diffusion barrier on the surface of the materials avoiding oxygen to reach the carbon surface[12-15]. Ceramic fiber [16], boron carbide [17-20] and boron nitride ceramics 21 are produced using only PVA-В2О3 hybrid precursors. For borate glasses, data exist only for the cases of metal counterions for anions borate units’ compensation. In this work we have prepared PVA/PEG/B2O3 precursors for boron doped carbon, materials are provided. The polymer pyrolysis is a simple processing route to produce multicomponent nanostructured materials. According to this method, organic/inorganic materials are converted to the borate and carboborate glass and carbon/borate glass nanocomposites.

The objective of the present study is to probe the structure of the hybrid borate hydrogel materials. The crosslinking is achieved by a combination of PVA and PEG in different solutions of borate species. The study is relevant because the new findings will provide information about the basic units forming this multicomponent glass structure. Additionally, multivariate statistical interpretation of infrared spectral data (hierarchical cluster analysis) was used to determine specific experimental conditions impacting the procedure of synthesis.

- Experimental

By the sol-gel process at ambient temperature, homogeneous and transparent organic-inorganic gel materials are obtained with mass ratio PVA/PEG/B2O3=10/7/1, by the method, referred in the literature[22-24]. All chemicals were used without any further purification: polyvinyl alcohol 72000 (PVA) 98 % hydrolyzed, polyethylene glycol 400 (PEG), trimethyl borate (CH3O)3B, boric acid (H3BO3) from Sigma-Aldrich Chemie, Germany. A stock solution of 4 wt% PVA was prepared by dissolving of PVA in distilled water by heating. Three precursor solutions of boron are used: 4 wt% H3BO3 in distilled water, 4 wt% H3BO3 prepared in glycerol and 4 wt% (CH3O)3B in ethanol.

The hybrid gels were maded by initially mixing and homogenizing PEG and different stock boron solutions. After that, the blend solution is added to the PVA under constant stirring. For obtaining self-standing films, and bulk material samples the hybrid gels are cast onto a glass plate or in a beaker for producing two types of samples for the next steps. The obtained films with 40 µm thicknesses and bulk material samples are dried at ambient temperature for one week. The next phase in the experimental procedure is heat treatment at 100 oC, 400 oC, 800 oC for 2h. Structural changes during the pyrolysis was studied by Fourier transform infrared spectroscopy (FTIR) - (Perkin Elmer SPECTRUM 1000), Differential Thermal analyzes  (TG/DTA) - (SETRAM LABYS TG/DTA),  X-ray diffraction (XRD) - (DRON-UN Cu Kα). The surface morphology is observed by scanning electron microscopy (SEM) - (JEOL JSM 5300).

Cluster analysis (CA) is well-known and widely used data mining approach for various purposes with its hierarchical and non-hierarchical algorithms[25-26]. Experimental samples (objects) could be characterized by a set of variables and cluster analysis allows to determine their similarity and to define cluster objects both for objects and variables. A preliminary step of data scaling is necessary (auto scaling or z – transform) to normalized dimensionless numbers replace the real data values. Thus, important differences in absolute values could be reduced to close numbers. Then, the similarity (or more strictly, the distance) between the objects in the variable space has to be determined. Very often the Euclidean distance is used for clustering purposes. Different approach of measuring similarity is the calculation of the correlation coefficient between the objects. Thus, from the input matrix (raw data) a similarity matrix could be constructed. There is a wide variability of hierarchical algorithms of objects linkage, but the typical ones include the single linkage, the complete linkage, and the average linkage methods. We have used The Ward’s linkage method was used. The representation of the results of the cluster analysis is performed by a tree-like scheme called dendrogram comprising a hierarchical structure (large groups are divided into small ones).

- Results and discussion

All obtained hybrid materials are transparent and thermally stable up to 100 oC, and over 400 oC they are converted into black powder. The final pyrolyzed products are obtained at 800 oC as transparent borate glasses, or black melt carbon/borate glass nanocomposites. Structural changes that are visually observed are gained as a function of the borate solutions type. In Fig. 1. to 4. are shown the FTIR spectra for hybrid precursors during pyrolysis for PVA/PEG/В2О3.

Fig. 1                                  Fig. 2                                  Fig. 3                                           Fig. 4

The absorption bands presented at 100 oC are assigned to: 3700-3100 cm-1 (νsН-ОН, νsC-ОН, νsB-ОН, hydrogen bonds), 2940-2870 cm-1 (νsC-H of СН2, CH3), 2300-1900 cm-1 (δ hydrogen bonds), 1720-1710 cm-1 (νsC=O), (1650-1640 cm-1 (O-H of H2О, C-C), 1460-1425 cm-1 (νasO–H, δC-H of CH2 and C-C), 1370-1350 cm-1 (δаsСН3 and C-C), 1370-1220 cm-1 (δC-OH, νO-C-C), 1120-1080 cm-1 (νС-ОН of secondary alcohol PVA, Glycerol), 1065-1020 cm-1 (νС-ОН of primary alcohol PEG, Glycerol), 1100-1000 cm-1 (δC-O-C of esters), 1200-970 cm-1 (δC–O), 940-920 cm-1 (γС-ОН and δC-C), 700-670 (δC-H and C-C) [16-21, 30-31]. The bands in region 1500-1200 cm-1 are allied to (νВ-О of ВО3), 1200-850 cm-1 to (νВ-О of ВО4) and 800-600 cm-1 (bending vibrations for various borate segments) [32-33]. The characteristic frequency for B-O-C bond has occurred at 1030 cm-1[16-19].

The major changes of vibration frequencies for O-H and C-OH (3700-3100 cm-1) and C-H (2940-2870 cm-1) bonds are observed in FTIR spectra at 400 oC. The effects of water evaporation and burning of polymers leads to decreasing of widths and intensities of these bands [29]. The spectral changes depicted in Fig. 1. and Fig. 2. are connected to the simultaneous disappearance of the absorptions bands in region 2940-2870 cm-1 and 1720 cm-1. The presence of new bands at 700 cm-1, 460 cm-1, 550 cm-1 indicates the presence of BO3 groups [16,19,32,33]. The network of the PVA-H3BO3 hybrid precursor at 400 oC is destroyed, and typical bands of BO3 group in boric acid are observed Fig. 1b. FTIR spectrum of pyrolysed to 400 oC hybrid precursor produced by a glycerol solution of boric acid is presented in Fig. 2b. The bands intensities are increased in regions 1425-1345 cm-1 (BO3) and 1060-900 cm-1 (BO4). That can be linked to the rearrangement of initially cross-linked borate groups. Fig. 3. and Fig. 4. shows the IR spectra of pyrolysed to 400 oC hybrid precursor prepared by an aqueous solution of boric acid and ethanol solution of boron methoxide. The observed changes are the increase of frequency intensities at wavenumbers range of 1400-1200 cm-1 (BO3) and decreasing of 1100-900 cm-1 (BO4). The IR spectra revealed a diminishing trend of the BO4/BO3 ratio. The occurrence of new bands 1030 cm-1 and 800 cm-1 can be assigned respectively to B-O-C bonds and BO4 groups while the absorptions bands at 1200 cm-1, 700 cm-1, 645 cm-1, 550 cm-1 are typical of boric acid Fig. 4b. The changes of absorption bands at wavenumbers regions 3200-2900 cm-1, 1700-1400 cm-1, 1000-600 cm-1 can be assigned according [34-35] to the vibrations frequencies of unsaturated hydrocarbons: 3100–3000 cm-1 (νs =C–H), 1730–1700 cm-1 (νC=O of aldehydes and ketones), 1680–1600 cm-1 (νsC=C), 1400 (δ =C–H), 1000–600 cm-1 (δ =C–H). The observed structural changes for all samples at 400-800 oC show two opposite tendencies: the simultaneous decomposition of hybrid networks and polymerization of BO3 and BO4 in borate glass networks. From IR analysis, it can be concluded that thermal stability of PVA-B2O3 hybrid precursor is the lowest one. The IR spectrum at 800 oC corresponding to molten H3BO3 Fig. 1c. and Fig. 1d., and no structural changes occur compared to that at 400 oC. The final product is transparent borate glass, containing only BO3 groups. Regarding the three component systems, the hybrid PVA/PEG/B2O3 precursor prepared by glycerol solution of boric acid show the lowest thermal stability. Structural decomposition at 400 oC has occurred without formation of secondary boric acid. The absorption peaks at wavenumber 1390 cm-1, 1080-990 cm-1, 770 cm-1  (Fig. 2c), were observed after pyrolysis at 800 oC. These absorption bands occurred due to the polymerization of BO3 and BO4 groups to diborate and triborate glass structures [32-33]. IR studies of pyrolyzed to 800 oC organic-inorganic precursors prepared by H3BO3 and (CH3O3)B consist broad and sharp spectral bands in the different region as shown in Fig. 3c. and Fig. 4c.. Secondary H3BO3 crystallization supplements pyrolysis to 400 оС of hybrid PVA/PEG/B2O3 precursors obtained by aqua solution of boric acid and ethanol solution of boron trimethoxide. The IR spectra show absorptions bands of hydrocarbon residue and BO3 and BO4 groups involved in tetraborate glass network (1390 cm-1, 1240 cm-1, 1100-950 cm-1, 695 cm-1). The final product is an amorphous carbon/borate glass nanocomposite. Structural changes after pyrolysis investigated by FTIR show that BO4 structural units are produced only by precursors containing PEG. The presence of BO4 tetrahedra in the structure without metal counter ion can be attendant on electron deficit nature of boron which takes part in redistributions of π electrons of carbohydrate residues [13,14]. Differential thermal analysis (DTA) technique was used for thermal characterization of the PVA/PEG/B2O3 precursor obtained by ethanol solutions of (CH3O3)B. The extent of the degradation process is usually estimated from measurements of mass losses (TGA). Thus, the evaluation of the effect of crosslinking on the degradation behavior of the hybrid materials was performed by measuring the mass loss of samples. TG/DTA curves are given in Fig. 5a. and Fig. 5b..

Fig. 5

In interval 70-350 oC, the hybrid precursor is losing 55 % from its weight. The particular weight loss are between 220-350 оC, followed by a further weight loss from 350-480 оC. The thermal degradation after 500 oC is would not influence the with weight losses obviously. Other authors observe a similar tendency [20,36,37]. The most profound endothermic effect at 123 оС can be assigned to the dehydratation of adsorbed water molecules and hydrogen bonded cross-linked groups. The next endothermic peak which appears at 320 оС seems to indicate decomposition of the hybrid structure. The pyrolysis processes can be associated with elimination and scission type reactions of polymer terminal groups, obtaining volatile byproducts, such as water, acetic acid, saturated and unsaturated aldehydes and ketones also. The appearance of exothermic effects at 387 oC and 670 оС can be explained by steppe mechanism starting with dehydratation of H3BO3 and transformations to the metaboric (HBO2), followed by the tetraboric acid (H2B4O7). The endothermic effect is observed at 820 оС for the melted boron oxide (B2O3)[20,36]. XRD results, presented in Fig. 6.a), b), c) confirms that PVA/PEG/B2O3 precursor is amorphous at 100 oC. Then, the crystallization of boric acid is observed at 400-700 оС. After that, at 800 oC, the sample is converted to the amorphous molten material.

Fig. 6

The presence of carbon nanoparticles may explain the visible changes of the sample in black glass composite [38]. The results by SEM are given in Fig. 7. The surface of hybrid films at 100 oC is homogeneous, amorphous without microcracks. The sample at 400 oC consists of particles with a size of 0.1-0.7 μm and their micro-aggregates are about 1.5 μm. Decreasing of particles size and agglomeration can be observed at 800 oC.

Fig. 7

The data set subject to hierarchical cluster analysis had dimension of [12x14] where the objects of the study were twelve IR frequencies which describe 14 experimentally different composites. The Ward’s method was used for linkage after applying squared Euclidean distance as similarity measure. The cluster significance was determined by the Sneath’s index (1/3 and 2/3Dmax). The hierarchical dendrogram is presented, showing the clustering of the composites in Fig. 8. The 14 experimentally different composites are labeled in the dendrogram and also in the text with the abbreviations. Here is the list of abbreviations in the same order like in the dendrogram:

PB400 and PB800 (binary system PVA/B2O3 pyrolysed at 400 and 800 oC); PPB(aq.)800 , PPB(aq.)25, PPB(aq.)100, PPB(aq.)400 (aqua solution of H3BO3  pyrolysed at 800 оС , 25 оС ,100 оС , 400оС); PPB(et.)400, PPB(et.)25, PPB(et.)100, PPB(et.)800 (ethanol solution of trimethyl borate (CH3O)3B) pyrolyzed at 400 оС, 25 оС, 100 оС, 800 оС); PPB(gl.)25, PPB(gl.)100, PPB(gl.)400, PPB(gl.)800 (glycerol solutions of H3BO3 pyrolysed at 25 оС ,100 оС , 400оС 800 оС).

Fig. 8

Four major clusters could be identified. The first one includes composites synthesized at temperature interval 25-100 оС for three types of hybrids for the system PVA/PEG/B2O3. This clustering confirms the conclusions in that the thermal stability of the composites up to 100 оС does not depend on the initial hybrid structure or the type of the precursor solutions used. The other three groups refer to pyrolysed at 400 and 800 oC products.

Among the rest of the groups, the linkage including PPB-gl objects (PPB (gl) 25 and PPB (gl) 100) is well defined. Here the similarity is related to the system composition and specificity – the lowest thermal stability is found exactly for this composite structure. At 400 oC it is completely degraded, and the inorganic components are represented by groups BO3 and BO4 which is kept even at 800 оС in a structure of transparent diborate glass.

The linkage for compositions PPB-aq and PPB-et (at 400 and 800 oC) is assumed to be due to the similarity in the thermal aspect which does not follow the composition similarity. The thermal stability is a function of the hybrid structure type. Due to its lower thermal stability, the hybrid structure of PPB-et at 400 oC reveals much stronger degradation. The reason seems to be structurally as depending on the type of borate solutions; the cross-linking mechanism has to be different. In the same way, the respective В-О structural groups included in the glass nanocomposite (PPB-aq at 800 oC) are present in the powder composition obtained from PPB-et at 400 oC. The primary reason for the lack of structural similarity as it is in the previous case. The last group of linkage for PB –aq (at 400 and 800 oC) concerns proposed hybrid structures obtained by cross-linking of water solutions of PVA and H3BO3. The thermal behavior is related to the system composition. After pyrolisis at 400 oC, only BO3 structural groups are present being the only structural units of the transparent at 800 оС glass. The reason for the different location of this linkage (an outlier) is due to the different composition of the system.

- Conclusions:

The focus of this work is preparation of In this work we have prepared PVA/PEG/B2O3 precursors for boron doped carbon materials. The quantities and order of borate structural units, residual carbon in networks depend on boron precursor type. After pyrolysis BO3 and BO4 structural groups are obtained in the molten materials like glass or nanocomposite, based on the kind of implementation of boron precursor solution. Glass structures involving polymerized BO3 and BO4 groups can be formed in the simultaneous presence of PVA and PEG only. To access the impact of the experimental conditions on the structural changes after pyrolysis of the nanocomposites cluster analysis of the IR-spectral data was used successfully as the proper classification method.

The clustering reveals new aspects of interpretation of results for boron contained hybrid nanocomposite systems by creating groups of similarity between the organic-inorganic materials independence of specific experimental conditions which could serve as “fingerprints” for a particular type or nanocomposite.

Acknowledgements

This work was supported by the Spanish Ministry of Education and Science (Project CTM2012-39183) and the Generalitat de Catalunya (Grup Consolidat 2014SGR1017).

References

[1] C. William Lepry, N. Showan Nazhat, Chem. Mater. 27 (2015) 4821–4831

[2] A. Chandra, A. Bhatt, A. Chandra, J. Mater. Sci. Technol. 29  (2013) 193-208

[3] H. Doweidar, Y. Moustafa, G. El-Damrawi and R. Ramadan, J. Phys.: Condens.                    Matter. 20 (2008) 035107- 035112

[4] F. Margha1, A. Abdelghany, Processing and Application of Ceramics 6 (2012) 183–192

[5] P. Pennarun, P. Jannasch, S. Papaefthimiou, N. Skarpentzos, P. Yianoulis, Thin Solid Films 514 (2006) 258–266

[6] Z.Xue, D. He, X.Xie, J. Mater. Chem. A. 3 (2015) 19218-19253

[7] C. Chiappe, F. Signori, G. Valentini, L. Marchetti, C. Pomelli, F. Bellina, J. Phys. Chem. B. 114 (2010) 5082–5088

[8] J. Luo, Ch. Pardin, X. Zhu, W. Lubell, J. Comb. Chem. 9 (2007) 582-591

[9] B. Pappin, M. Kiefel, T. Houston: "Boron-Carbohydrate Interactions", Carbohydrates - Comprehensive Studies on Glycobiology and Glycotechnology, ed. Chuan-Fa Chang, ISBN 978-953-51-0864-1, 37-54, 2012

[10] H. Costa, A.Mansur, M. Pereira, H. Mansur, Journal of Nanomaterials 2012 (2012) 1-16

[11] S. Morris,  T. Hawkins, P. Foy,  J. Ballato,  S. W. Martin, and R. Rice, Int. J. Appl. Glass Sci. 3 (2012) 144–153

[12] Y. Lee, H. Joob, L. Radovica, Carbon 41 (2003) 2591–2600

[13] R. Siqueira, I. Yoshida, L. Pardini, M. Schiavon, Materials Research 10 (2007) 147-151

[14] S. Labruquère, H. Blanchard, R. Pailler, R. Naslain, J. Eur. Ceram. Soc. 22 (2002) 1001–1009

[15] S. Labruquère, Blanchard, H.; Pailler, R.; Naslain, R., J. Eur. Ceram. Soc. 22 (2002) 1011- 1021

[16] I. Uslu, H. Daştan, A. Altaş, A. Yayli, O. Atakol, ML. Aksu, e-Polymers 7 (2007) 1568-1573

[17] S. Mondal, A. Banthia, J. Europ. Ceram. Soc. 25 (2005) 287–291

[18] A. Fathi, N. Ehsani, M. Rashidzadeh, H. Baharvandi, A. Rahimnejad, Ceramics– Silikáty 56 (2012) 32-35

[19] I. Uslu, T. Tunc, J Inorg Organomet Polym. 22 (2012) 183–189

[20] P. Barrosa, I. Yoshida, M. Schiavon, J. Non-Crystall. Sol. 352 (2006) 3444–3450

[21] M. Das, S. Ghatak, Bull. Mater. Sci. 35 (2012)  99–102

[22] H. Hristov, P. Vasileva, N. Riskov, C. Dushkin, J. Optoelectr. Adv. Mater. 11 (2009) 1343-1346

[23] P. Vasileva, H. Hristov, N. Riskov, C. Dushkin, Nanoscience and Nanotechnology 10 (2010) 201-205

[24] H. Hristov, P. Vasileva, M. Nedialkova, Nanoscience and Nanotechnology 12 (2012) 47-51

[25] D. L.Massart, L.Kaufman, "The Interpretation of Analytical Chemical Data by the Use of Cluster Analysis", Wiley-Interscience, New York,   USA, 1983.

[26] D. L Massart, B. G. M Vandeginste,  L. M. C. Buydens, "Handbook of Chemometrics and Qualimetrics: Data Handling in Science and Technology ", Parts A and B,  Data Handling in Science and Technology, eds., D.L. Massart, B.G.M. Vandeginste, L.M.C. Buydens, S. De Jong, P.J. Lewi and J. Smeyers-Verbeke, Elsevier, Amsterdam, Nederland, 1-867 1998

[27] H. Hristov, M. Nedialkova. Nanoscience and Nanotechnology, (2013), 13 147 - 151

[28] H. Hristov, M.Nedialkova: Nanoscience and Nanotechnology, 13 (2013) 152- 155

[29]  Ch. Liu, F. Ye, R. Xia, L. Zhang, Y. Zhou, Y. Huang, J. Mater. Sci. Technol. 29    (2013) 983-988

[30] M. Rozenberg, A. Loewenschuss, Y. Marcus, Spectrochimica Acta A 54 (1998) 1819–1826

[31] S.Gunasekaran, R. Arun Balaji, S. Kumaresan, G. Anand, M. Anand, Intern. J. Chem. Tech Research. 1 (2009) 1109-1124

[32] C. Gautam, A. Kumar Yadav, and A. Kumar Singh, ISRN Ceramics 2012 (2012) 1-17

[33] G. Padmaja and P. Kistaiah, J. Phys. Chem. A. 113 (2009) 2397–2404

[34] B. Stuart, Infrared spectroscopy: Fundamentals and applications, 2004, Wiley 1-76,

[35] I. Prosanov, A Matvienko, Physics of the Solid State 52 (2010) 2203- 2206

[36] C. Nyambo, E Kandare, C.Wilkie, Polymer Degradation and Stability 94 (2009) 513 - 520

[37] C. Gervais, F. Babonneau, N. Dallabonna, D. Soraru, J. Amer. Ceram. Soc. 84 [10] 2160 – 2164  (2001)

[38] I.Kottegoda, X.Gao, L.Nayanajith, Ch.Manorathne, J. Wang, J. Wang, H. Liu, Y. Gofer,  J. Mater. Sci. Technol.  31 (2015) 907-912

Figure captions

Fig. 1. Fourier transform infrared (FTIR) spectra (spectra are vertically shifted) of pyrolysed hybrid precursor PVA/B2O3: a) 100 oC, b) 400 oC, c) 800 oC, d) H3BO3 molten of 800 oC.

Fig. 2. Fourier transform infrared (FTIR) spectra (spectra are vertically shifted) of pyrolysed PVA/PEG/B2O3 hybrid precursor, prepared from glycerol solution of H3BO3: a) 100 oC, b) 400 oC, c) 800 oC.

Fig. 3. Fourier transform infrared (FTIR) spectra (spectra are vertically shifted)  of pyrolysed PVA/PEG/B2O3 hybrid precursor, prepared from aqueous solution of H3BO3: a) 100 oC, b) 400 oC, c) 800 oC.

Fig. 4. Fourier transform infrared (FTIR) spectra (spectra are vertically shifted) of pyrolysed PVA/PEG/ B2O3 hybrid precursor, prepared from ethanol solution of (CH3O)3B: a) 100 oC, b) 400 oC, c) 800 oC.

Fig. 5. Thermal analyses of PVA/PEG/B2O3 hybrid precursor, prepared from ethanol solution of (CH3O)3B: a) TG curve, b) DTA curve.

Fig. 6. XRD of PVA/PEG/B2O3 hybrid precursor, prepared from ethanol solution of (CH3O)3B: a) 100 oC, b) 600 oC, c) 800 oC.

Fig. 7. SEM images of PVA/PEG/B2O3 hybrid precursor, prepared from ethanol solution of (CH3O)3B: a) 100 oC, b) 400 oC, c) 800 oC.

Fig. 8. Hierarchical dendrogram for 14 experimentally different composites.