## Slide 1
EMMC International Workshop 2019
Session 16 - Innovation hubs: next generation collaboration and services on marketplaces
Feb. 27th 2019
Open Innovation Environment in materials characterisation: the example from H2020 project OYSTER
(Marco Sebastiani – coordinator)

## Slide 2
EMCC paradigm for product innovation
In the triangle of manufacturing, modelling, and experimentation, the projects should develop an open innovation environment for the optimisation of materials, materials behaviour and/or nano-device manufacturing processes, and for the validation of materials models based on experimental characterisation.
Image from EMCC 2017 roadmap, www.characterisation.eu

## Slide 3
www.oyster-project.eu
H2020 – OYSTER (www.oyster-project.eu)
H2020 Oyster Project – G.A. 760827
Notes: Then the possibility for high-frequency (100 kHz) displacement data acquisition (due to the acquisition of the new iNano) opened the way for unprecedented adhesion experiments to investigate surface free energy modifications on a nano-scale in advanced nanostructured materials and/or architecture surfaces.
This image reports a typical load-unload curve obtained by high-frequency nanoindentation, where the snap-in and pull-off adhesion events are highlighted.
By using 100 kHz data acquisition frequency, the snap-in and pull-off adhesion events are fully captured and can be effectively used for work of adhesion and surface free energy calculations.
From the new high frequency data, it was possible to observe a non-linear trend of the force during the snap-in and consequently the needing to re-elaborate the old linear analytical model.

## Slide 4
Enhancing of the heat transfer coefficient
Improvements of glass performances for optronic devices
Anti-icing performances
Applications of LFE surfaces
Self-cleaning properties
Improving the contact lens resistance
Friction reduction
Zhang, P. et al. Energy 82 (2015): 1068-1087.
H2020 – OYSTER WIDER IMPACT

## Slide 5
The Open Innovation Environment in Oyster
The platform is designed to be fully compatible with the one developed within the MARKETPLACE project.

## Slide 6
Where to start from: HARMONIZATION
Our proposal for a strategy is to pursue the concept of an Open Characterization Platform based on a semantic footing and open standards.
This is basically one step removed from an actual common platform implementation, but provides the interoperability standards for it.
On this basis, different platform implementation can exist, but would be highly interoperable if the same standard is used (starting from CHADA and ontology);
The main step to start this is the development and wide adoption of CHADA

## Slide 7: Where we start from: the MODA (EMMC)
Model 1
raw output
Model 2
processed output
raw output
processed output
user case input
Model 3
user case input
user case input
Consecutive workflow: linked models

## Slide 8: Visual representation of a general Characterisation Experiment
Medium (environment)
Specimen
Detector
Sample Pre-processing
Raw Data
Calibration
Property
Data Analysis
Elaborated data
Post- processing
User (operator)
Sample/Probe Physics of interaction
Equipment setup
Probe
Signal

## Slide 9: Visual representation of a general Characterisation exp. with keywords (and colors)
Medium (environment)
Specimen
Detector
Sample Pre-processing
Raw Data
Calibration
Property
Data Analysis
Elaborated data
Post- processing
User (operator)
Sample/Probe Physics of interaction
Equipment setup
Probe
Signal
Sample
Raw Data
Method
Data processing
2019, Submitted for publication

## Slide 10
Method
Raw data
CHADA Workflow materials characterisation: template 1
Sample -1
Workflow for a standalone method
First draft for CHADA workflow
Post-processing
Property

## Slide 11
Method
Raw data
Raw data
method
Post-processing
Workflow materials characterisation: template 2
Sample -1
Sample-2
Consecutive workflow: linked characterisation methods
First draft for CHADA workflow
Post-processing
method
Sample-3

## Slide 12
Method 1
Method 2
Post processing
Iterative workflow
Sample 1
Sample 2
Post-processing
Workflow materials Characterisation: template 3
Raw data 1
Raw data 2
First draft for CHADA workflow

## Slide 13
tightly coupled characterisations
Method-1
Tightly coupled characterisations
Workflow materials Characterisation: template 4
Raw data
Method-3
Method-2
Processed data
Sample
The final arrow is to be used of there is a next characterisation in a chain with

## Slide 14
Method
Calibration Raw Data
Raw data
method
Data analysis
Workflow materials characterisation: EXAMPLE with machine calibration
Sample -1
Sample-2
Characterisation method made of a machine calibration process ona reference sample, followed by the actual measurement
First draft for CHADA workflow
Level 1:
Machine calibration
Level 2:
Raw data acquisition
Calibration Data analysis
Property
Post-processing

## Slide 15
Method: Selection of the test recipe (loading sequence)
Sample 1
Raw data
Method: Test Execution
Data analysis
Sample--1
Sample-1
Level 1:
Test Preparation
Level 2:
Raw data acquisition
Level 3:
Machine Calibration
(it can be done before OR after raw data acauisition)
Level 3:
Machine Calibration
Method: Selection of the input parameters
Method: Video Calibration and selection of the test locations
Reference Sample
Method: Selection of the calibration test recipe
Method: Selection of the input parameters
Method: Selection of the test locations
Reference Sample
Reference Sample
Raw data
Method: Test Execution
EXAMPLE-1: Nanoindentation
Level 4:
Data PostProcessing
Property
Post-processing

## Slide 16
Keyword | Description
User (operator) | Human Operator (different levels of automation are available)
User case (sample specifications) | Sample dimensions (1 inch diam. – 5 mm thick.). Surface flat and polished. Sample embedding on sample-holder (hot glue or acrylic glue). Optical sample surface alignment with reference sample (SiO2) surface.
Specimen | Bulk material, coatings, heterogeneus materials, bio-material.
Medium (environment) | Equipment Box: Air, Temperature, Pressure, Humidity, Noise, Vibrations (Acoustic or mechanical).
Sample/Probe Physics of interaction | Detection of the surface by the tip (stiffness triggering value based) – Penetration of the tip inside the sample using a prescribed load function – Hold of the maximum load (or the load for the prescribed depth – unloading of the tip by steps – tip removal from the sample.
Equipment setup | Optical aligment of the sample. Method selection and Input parameters for the test (Sample Poisson’s Ratio, Prescribed Depth or Load, number of tests, locations of the tests, Engage options).
Calibration | Standard CSM tests on reference sample.
Probe | Selected Tip for the test (Berkovich, Cube Corner, Flat Punch..).
Detector | Electronic controllers and capacitive gauges.
Signal | Electrical current in a coil -> Force (Load)
Data Analysis | Check of the surface detection, check of the Load vs depth quadratic curve trend, check of the slope of the unloading curve, removal of the not significative tests.

## Slide 17
Keyword | Description
Raw Data | Hardware and software channels graphs (Raw Load, Raw displacement, Stiffness, Load, Depth…).
Raw Data Analysis | Application of the Oliver-Pharr method (or other data analysis methods)
Post-processing | Raw data calibration using tests on reference sample, check of the results (see data analysis), Selection of the load (or depth) range to evaluate the mechanical properties, Graphs or hystograms of interest.
Properties (elaborated data) | Elastic Modulus, Hardness, Yeld Stress, Residual Stress, Creep parameters, Fracture toughness, mechanical maps, etc.

## Slide 18
EXAMPLE-2: Scanning Electron Microscopy (SEM)
Images
Composition

## Slide 19
Workflow materials characterisation: Scanning Electron Microscopy (SEM)
First draft for CHADA workflow

## Slide 20: Keywords
Keyword | Description
User (operator) | Human Operator
Medium (environment) | High vacuum (typically) or low vacuum (environmental SEM)
Specimen | Solid and dry materials with good electron conductibility (Metals, ceramics, biological and polimers. If electron conductibility is not enough, sample have to be metallised or carbon coated
Specimen requirements | Sample dimensions (Typically 30mm x 30mm with thickness less than 10mm). Sample have to be flat, clean and dry.
Sample/Probe Physics of interaction | Energetic electrons in the microscope strike the sample and various reactions can occur in a restricted volume with a consequent generation of secondary electrons, backscattered electrons and X ray photons (for elastic and anaelastic interactions). The probe rasters the sample pixel by pixel
Equipment setup | Probe alignment and setup, sample positioning,
Calibration | Generally only during instrument maintenance
Probe | Energized electron beam (0,1 -30 keV)
Detector | Solid state or photomultiplier to detect secondary signal emitted by the sample
Signal | Electrons and X-ray

## Slide 21: Keywords
Keyword | Description
Raw Data | Morphological or compositional images. X-ray counts/energy spectrum.
Data Analysis | Image quality evaluation (noise, focus, astigmatism, etc.) and X-ray energy data identification
Post-processing | Image analysis and X-ray energy data quantification using models
Property | Topography, morphology, particles metrology (dimensions and shape) etc.

## Slide 22
EXAMPLE-3: Scanning Probe Microscopy
Measurement capabilities:
Topography
Roughness
Height
Friction
Magnetism
Mechanical Properties
Surface energy
Phase identification
www.bruker.com

## Slide 23
Workflow materials characterisation: Scanning probe microscopy (SPM)
First draft for CHADA workflow

## Slide 24: Keywords (colors corresponding to the four classes)
Keyword | Description
User (operator) | Human Operator
User case (sample specifications) | Sample dimensions (Typically 8mm x 8mm with thickness less than 4mm). Surface of the sample should be flat and smooth (usually, max z-excursion for AFMs is +/- 5 µm).
Specimen | Metals, Polymers, fibres (nanotube, hair, synthetic fibers), particles (micro-nano, quantum dots), Proteins, bacteria, cells, Viruses, Minerals, ceramics, plant surfaces, paper etc.
Medium (environment) | Mostly in air, special accessories for scanning and imaging in liquids
Sample/Probe Physics of interaction | Detection of the surface by the tip – Depending upon the mode selection, tip may (contact) or may not (Tapping, Non-contact etc.) touch the sample surface. The tip is mounted on a reflective cantilever (the cantilever and tip together are known as the probe). The deflection of the tip is measured by laser, reflected off the cantilever onto a split photodiode. This allows vertical and horizontal measurement of the cantilever bending. The vertical deflection data tells us about the interaction between the tip and the sample.
Probe | Selected Tip for the test (Contact, non-contact, tapping, PFM etc.)
Detector | Scanner which also controls the probe movement.
Signal | Cantilever deflection (monitored through laser deflection ) as it scan the sample surface .
Equipment setup | Optical alignment of the sample. Method selection and alignment of the laser on the cantilever.
Calibration | Standard SPM samples with known features.
Data Analysis | Scanning of the sample surface (selection of scan size, speed)
Post-processing | Image Flattening, different filters

## Slide 25: Keywords (colors corresponding to the four classes)
Keyword | Description
Raw Data | Wide range of interactions can be monitored e.g. Height, Amplitude, Phase, Stiffness etc. Largely depend upon the sample, probe and method.
Property | Topography, Roughness, Mechanical properties (stiffness and modulus), Number of Phases, size of the particles (height and diameter) etc.

## Slide 26
EXAMPLE-4: X-ray diffraction
(Conventional) Measurement capabilities:
Phase composition
Crystal structure
Epitaxy/texture/orientation
Crystallite size
Residual stresses measurement

## Slide 27
Workflow materials characterisation: X-ray diffraction (XRD)
First draft for CHADA workflow

## Slide 28: Keywords
Keyword | Description
User | Human Operator
Standard sample | Corundum, Silicon single crystal
Specimen requirements | Samples can include thin films on wafers or dense pieces up to 6” in diameter (maximum thickness of 3 mm), powders in top-loaded sample holders or in capillaries, dense pieces up to 60mm x 50mm x 15mm (and maybe even larger).
Medium (environment) | Mostly in air, but it can be done in different atmospheres and at different temperatures.
Specimen | Metals, Polymers, composites, ceramics etc. Samples can be powder, sintered pellets, coatings on substrates.
Sample/Probe Physics of interaction | Detection of the surface by the interaction of x-rays with sample (Diffraction) – Depending upon the diffraction geometries (Bragg Brentano or Grazing incidence) and input parameters (incidence angle, scan mode, scan type and increment ratio etc.). Primary optics (Goebel Mirror for parallel x-ray beam and Paraphocal block for divergent or nonparallel beam), secondary optics (Equatorial slits) and other slits are used to filter the x-ray radiations.
Equipment setup | Z- scan and rocking curve method is performed to adjust the height of the sample.
Calibration | Standard XRD samples with known diffraction pattern.
Probe | The characteristic x-rays are generated by using cooper (Cu) anode.
Detector | LYNEX XE is a high-resolution energy-dispersive detector for 0D, 1D and 2D diffraction.
Signal | Signals are generated by diffraction which occurs due to constructive interference if it follows the bragg’s law (nλ = 2dhkl sinθ).

## Slide 29: Keywords
Keyword | Description
Data Analysis | Scanning of the sample surface (selection of scan type, scan mode and speed)
Post-processing | Powder diffraction data consists of a record of photon intensity versus detector angle 2θ. The acquired pattern is then compared with the material database in order to identify the hkl planes and phases corresponding to the diffraction peaks.
Raw Data | Obtained diffraction pattern provides the information of peak position, peak intensity, peak broadening of certain hkl planes.
Property | Phase composition, crystal structure, epitaxy/texture/orientation, crystallite size and residual stresses can be measured by XRD.

## Slide 30
This project has received funding from the European Union’s Horizon research and innovation programme under gran agreement No 760827.
THANK U!
Contact details:
Seba@uniroma3.it