Figure S1. Changes of pH value measured in solutions of As(III) (a) and As(V) (b) before and after sorption experiment carrying out onto diverse initial pH value of raw and modified vermiculite.

Figure S2. Changes of pH value measured in solutions of As(III) (a) and As(V) (b) before and after sorption experiment carrying out onto diverse initial concentration of raw, HDTMA and HDBA modified vermiculite.

Figure S3. Changes of pH value measured in solutions of As(III) (a) and As(V) (b) before and after sorption experiment carrying out onto diverse dosage of raw, HDTMA and HDBA modified vermiculite.

Figure S4. Linearization of Freundlich and Langmuir model for sorption of As(III) (a), As(V) onto raw vermiculite (b); sorption of As(III) (c),  As(V) onto 0.5 HDTMA (d) and As (III) (e), As(V) onto 0.5 HDBA (f); As(III) (g) , As(V) onto 1.0 HDTMA (h) and As(III) (i), As(V) onto 1.0 HDBA (j); sorption of As(III) (k), As(V) onto 2.0 HDTMA (l) and As(III) (m), As(V) onto 2.0 HDBA (n).

Table S1. Freundlich and Langmuir model coefficients for sorption of As(III) and As(V) onto raw, HDTMA and HDBA modified vermiculite.

|  | Freundlich |  |  |  |  |  |  |  | Langmuir |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1/n |  | KF [mmol/kg] |  | R2 |  |  |  | Q [mmol/kg] |  | KL [L/mmol] |  | R2 |  |
| VER- As(III) | 0,563 |  | 3,803 |  | 0,7807 |  |  |  | 13,04 |  | 0,558 |  | 0,9594 |  |
| VER- As(V) | 0,897 |  | 6,978 |  | 0,9048 |  |  |  | 625 |  | 0,003 |  | 0,0338 |  |
| 0.5 HDTMA- As(III) | 0,559 |  | 7,815 |  | 0,9697 |  |  |  | 49,02 |  | 0,151 |  | 0,6981 |  |
| 0.5 HDTMA- As(V) | 0,752 |  | 6,671 |  | 0,8185 |  |  |  | 80 |  | 0,076 |  | 0,4929 |  |
| 1.0 HDTMA- As(III) | 0,601 |  | 8,054 |  | 0,9634 |  |  |  | 59,17 |  | 0,143 |  | 0,9232 |  |
| 1.0 HDTMA- As(V) | 0,594 |  | 12,700 |  | 0,9143 |  |  |  | 80 |  | 0,188 |  | 0,9338 |  |
| 2.0 HDTMA- As(III) | 0,995 |  | 12,806 |  | 0,9633 |  |  |  | 1428,57 |  | 0,008 |  | 0,1300 |  |
| 2.0 HDTMA- As(V) | 0,870 |  | 20,291 |  | 0,9641 |  |  |  | 769,231 |  | 0,015 |  | 0,5255 |  |
|  |  | Freundlich |  |  |  |  |  |  |  | Langmuir |  |  |  |  |
|  |  | 1/n |  | KF [mmol/kg] |  | R2 |  |  |  | Q [mmol/kg] |  | KL [L/mmol] |  | R2 |
| 0.5 HDBA- As(III) |  | 0,729 |  | 5,477 |  | 0,9837 |  |  |  | 49,02 |  | 0,129 |  | 0,9863 |
| 0.5 HDBA- As(V) |  | 0,691 |  | 12,598 |  | 0,8820 |  |  |  | 217,39 |  | 0,019 |  | 0,3637 |
| 1.0 HDBA- As(III) |  | 0,589 |  | 6,038 |  | 0,9493 |  |  |  | 51,02 |  | 0,143 |  | 0,9042 |
| 1.0 HDBA- As(V) |  | 0,739 |  | 13,677 |  | 0,9393 |  |  |  | 156,25 |  | 0,096 |  | 0,7872 |
| 2.0 HDBA- As(III) |  | 0,991 |  | 8,972 |  | 0,9928 |  |  |  | 1428,57 |  | 0,006 |  | 0,1055 |
| 2.0 HDBA- As(V) |  | 0,902 |  | 12,226 |  | 0,9061 |  |  |  | 277,78 |  | 0,040 |  | 0,1027 |