Journal of GEOPHYSICAL  RESEARCH

Supporting Information for

High Pressure-Temperature Study on the Thermal Equations of State of Seifertite and the CaCl2-type SiO2

Ningyu Sun1, Weigang Shi1, Zhu Mao1,2,*, Cijin Zhou1, Vitali B. Prakapenka3

1Laboratory of Seismology and Physics of Earth’s Interior, School of Earth and Planetary Sciences, University of Science and Technology of China, Hefei, Anhui 230026, China

2CAS Center for Excellence in Comparative Planetology, China

3Center for Advanced Radiation Sources, University of Chicago, Chicago, IL 60637, USA

Contents of this file

Figure S1 to S3

Dataset S1 and S2

Additional Supporting Information

Captions for Figure S1 to S3

Captions for Dataset S1 and S2

Figure S1. Representative XRD patterns of SiO2 at high pressures and temperatures. Green ticks: NaCl B2 phase; blue ticks: Pt; orange ticks: Stv; red ticks: CaCl2-type phase. The right panels show that the 211 and 121 peaks in the CaCl2-type phase gradually merge to the Stv 211 peak with increasing temperature.

Figure S2. Representative XRD patterns of SiO2 at Mbar pressures.  a) 113 GPa and 2400 K; b) 135 GPa and 2200 K. Green ticks: NaCl B2 phase; blue ticks: Pt; purple ticks: seifertite; red ticks: CaCl2-type phase.

Figure S3. The high-temperature data points with calculated isotherms from the thermal equations of state. Selected high-temperature data for the CaCl2-type SiO2 along a given isotherms. Blue: 300 K; purple: 1200 K; yellow: 1500 K; magenta: 1700 K; orange: 1900 K; red: 2100 K. The isothermal lines were calculated using our obtained thermal parameters.

| P (GPa) | T (K) | V (Å3) |
| --- | --- | --- |
| 64.8(8) | 300 | 40.28(4) |
| 68.1(6) | 300 | 40.00(5) |
| 79.5(6) | 300 | 38.91(6) |
| 81.8(8) | 300 | 38.73(4) |
| 87.7(12) | 300 | 38.49(4) |
| 89.8(18) | 300 | 38.22(3) |
| 91.1(18) | 300 | 38.17(6) |
| 102.1(14) | 300 | 37.29(4) |
| 103.1(14) | 300 | 37.16(7) |
| 109.5(16) | 300 | 36.87(5) |
| 119.7(13) | 300 | 36.33(4) |
| 126.8(26) | 300 | 36.09(4) |
| 139.4(18) | 300 | 35.68(5) |
| 83.4(16) | 1150(120) | 38.85(6) |
| 116.0(22) | 1150(120) | 36.82(5) |
| 64.4(14) | 1180(120) | 40.46(4) |
| 95.7(18) | 1230(120) | 38.21(3) |
| 108.0(22) | 1200(120) | 37.24(5) |
| 127.3(26) | 1200(120) | 36.23(10) |
| 65.1(8) | 1580(160) | 40.56(3) |
| 85.6(9) | 1450(150) | 38.88(4) |
| 92.7(9) | 1550(160) | 38.21(5) |
| 109.9(9) | 1500(150) | 37.19(3) |
| 127.3(26) | 1500(150) | 36.28(6) |
| 141.2(28) | 1600(160) | 35.73(7) |
| 65.7(14) | 1700(170) | 40.65(3) |
| 71.8(14) | 1750(180) | 40.16(3) |
| 92.8(18) | 1800(180) | 38.45(4) |
| 96.9(18) | 1700(170) | 38.21(5) |
| 117.8(24) | 1730(170) | 36.89(6) |
| 128.3(26) | 1720(170) | 36.28(8) |
| 142.0(28) | 1700(170) | 35.73(10) |
| 86.8(18) | 1900(190) | 38.95(3) |
| 87.0(18) | 1900(190) | 38.92(3) |
| 97.5(20) | 1900(190) | 38.21(5) |
| 97.6(20) | 1920(190) | 38.27(5) |
| 117.9(24) | 1930(190) | 37.02(5) |
| 128.9(26) | 1900(190) | 36.30(6) |
| 143(28) | 1900(190) | 35.92(9) |
| 73.9(14) | 2100(210) | 40.30(3) |
| 90.6(18) | 2120(210) | 38.89(3) |
| 96.6(20) | 2100(210) | 38.31(4) |
| 97.7(20) | 2250(230) | 38.29(5) |
| 98.3(20) | 2130(210) | 38.25(5) |
| 114.7(24) | 2100(210) | 37.33(7) |
| 119.5(24) | 2100(210) | 37.00(7) |
| 128.5(26) | 2200(220) | 36.38(4) |
| 131.1(26) | 2200(220) | 36.34(9) |

Data Set S1. Pressure-temperature-volume data of CaCl2-type phase SiO2 at high pressures and temperatures

| P (GPa) | T (K) | V (Å3) |
| --- | --- | --- |
| 124.1(36) | 300 | 71.5(8) |
| 129.5(38) | 300 | 71.1(12) |
| 135.4(32) | 300 | 70.7(9) |
| 114.1(34) | 300 | 72.4(10) |
| 111.8(28) | 300 | 72.7(8) |
| 116.7(22) | 300 | 72.2(12) |
| 123.0(36) | 2400(250) | 73.0(9) |
| 123.1(30) | 2300(250) | 73.0(7) |
| 123.2(42) | 2500(250) | 73.1(5) |
| 127.4(44) | 2250(250) | 72.5(7) |
| 130.4(32) | 2200(250) | 72.0(7) |
| 140.5(42) | 2200(250) | 71.1(5) |
| 135.6(38) | 2260(250) | 71.6(7) |
| 128.0(26) | 1950(200) | 72.2(10) |
| 138.8(40) | 2000(200) | 70.9(8) |
| 126.2(34) | 1320(200) | 71.8(12) |
| 126.2(28) | 1800(200) | 72.0(9) |
| 139.8(28) | 1660(200) | 70.7(7) |
| 134.7(38) | 3030(250) | 72.2(12) |
| 135.9(38) | 2700(250) | 71.9(11) |

Data Set S2. Pressure-temperature-volume data of seifertite at high pressures and temperatures

*Not all the data in Figure 1 were used to determine the thermal EoS of seifertite because some of the XRD patterns contain less than 7-10 useful peaks. These XRD patterns were excluded when determining the thermal EoS of seifertite.