# Supplementary Materials

# to

# Melt-Spinning of an Intrinsically Flame-Retardant Polyacrylonitrile Copolymer

Simon König1, Philipp Kreis1, Christian Herbert3, Andreas Wego3, Mark Steinmann1, Dongren Wang2, Erik Frank1, Michael R. Buchmeiser*1,2

1German Institutes of Textile and Fiber Research, Körschtalstr. 26, D-73770 Denkendorf, Germany, 2Institute of Polymer Chemistry, University of Stuttgart, Pfaffenwaldring 55, D-70569 Stuttgart, Germany; 3Dralon GmbH, Chempark Dormagen, Postfach 10 04 85, 41522 Dormagen

2

1

5

3

4

Figure S1. 1H NMR spectrum of DPA after vacuum distillation.

Figure S2. 31P NMR spectrum of DPA after vacuum distillation.

Figure S3. Example of a PAN film made of PAN F3.

Figure S4. DSC measurements in air of PAN samples F1-F5 applying a heating rate of 10 °C/min.

Figure S5. Temperature sweep from 150 to 190 °C of PAN sample F1 (8.1 mol-% DPA,  = 43 000 g/mol, Đ = 5.5), mixed with 22.5 wt.-% PC. γ = 0.5 %, ω = 10 rad/s, heating rate = 1 K/min.

Figure S6. Temperature sweep from 150 to 190 °C of PAN sample F2 (8.1 mol-% DPA,  = 35 000 g/mol, Đ = 5.3), mixed with 22.5 wt.-% PC. γ = 0.5 %, ω = 10 rad/s, heating rate = 1 K/min.

Figure S7. Temperature sweep from 150 to 190 °C of PAN sample F4 (6.1 mol-% DPA, 3.7 mol-% MA,  = 57 000 g/mol, Đ = 5.5), mixed with 22.5 wt.-% PC. γ = 0.5 %, ω = 10 rad/s, heating rate = 1 K/min.

Figure S8. Stress-strain diagram (tensile test) of PAN F5 fibers (8.2 mol-% DPA, 3.8 mol-% MA,  = 43 000 g/mol, Đ = 5.1) containing 22.5 wt.% PC wound at a winding speed of 30 m/min.

Figure S9. Stress-strain diagram (tensile test) of PAN F5 fibers spun (8.2 mol-% DPA, 3.8 mol-% MA,  = 43 000 g/mol, Đ = 5.1), spun with 22.5 wt.% PC at a winding speed of 30 m/min. PC was washed out in demineralized water at 90 °C over 5 minutes.

Figure S10. Photograph of PAN F5 (8.2 mol-% DPA, 3.8 mol-% MA,  = 43 000 g/mol, Đ = 5.1) fibers containing 22.5 wt.% PC. Fibers were wound at a winding speed of 30 m/min.