Natt Makul, Advanced smart concrete - A review of current progress, benefits and challenges, Journal of Cleaner Production, Volume 274, 2020, 122899, ISSN 0959-6526,

https://doi.org/10.1016/j.jclepro.2020.122899.

Advanced smart concrete - A review of current progress, benefits and challenges

- Natt Makul

Department of Building Technology, Faculty of Industrial Technology, Phranakhon Rajabhat University, Changwattana Road, Bangkhen, Bangkok 10220, Thailand

Corresponding author. Tel. Fax.: (+662) 544-8614

E-mail address: shinomomo7@gmail.com

- Abstract

Concrete is the second most globally consumed material in the world after water and the most used construction material. Yet, its benefits are masked with many ecological setbacks through the way it is produced, transported, or used. Concrete occurs in a brittle state characterized by low tensile strength, weak resistance to crack formation, and strain properties. Recent studies have focused on improving concrete properties by integrating it with innovative solutions such as fibers, admixtures, and supplementary cementitious components. The infrastructure of modern structures demands components with greater durability, and higher mechanical strength. This solution can only be achieved through the addition of nanomaterials to cement-based products, thus, enhancing their mechanical features. Examples of nanomaterials include carbon nanotubes (CNTs), nano-ferric oxide (nano - Fe2O3), and grapheme oxide. Nanomaterials can be added to cement with the addition of other reinforcements such as glass, steel fibers, fly ash and rice hull powder. With optimum dosages, the compressive, tensile, and flexural strength of cement-based materials, workability and water absorption are improved. The use of nanomaterials enhances the performance and life cycle of concrete structures. This study looks at some of the recent concrete improvisations, analyzing them on the spectrum of technical performance, durability, ecological sustainability, and economic benefits.

Keywords: Smart concrete; Ultra-durability; Smart materials; 3D printing; Additive manufacturing; Fiber-reinforced concrete; Nanomaterials; Cracks

- Contents

1. 	Introduction										x

2. 	Background										x

2.1 	Sustainable solutions for the construction industry				x

3. 	The emergence of smart concrete such as graphene					x

3.1 	Applications and opportunities of smart-cementation materials		x

3.2 	Technology potential and impacts						x

3.3 	Benefits									x

3.4 	Challenges									x

4. 	Self-healing concrete									x

4.1 	Experiment									x

4.2 	Application benefits								x

5. 	Self-curing concrete									x

5.1 	Benefits									x

5.2 	Challenges									x

6. 	Ultra-high performance concrete (UHPC)						x

6.1 	Mixture design of UHPC							x

6.2 	Models for mixture design of UHPC						x

6.3 	Optimization of water and high-range-water reducer (HRWR)		x

6.4 	Challenges facing UHPC							x

6.5 	Benefits and applications							x

7. 	Steel fibre reinforced concrete (SFRC)						x

7.1 	Recycling aggregates in concrete						x

7.2 	Challenges									x

8. 	Additive manufacturing (AM)							x

8.1 	Background to AM’s technology						x

8.2 	Types of 3D printing								x

8.3 	Opportunities for AM of cement-based materials				x

8.4 	AM Technology advantages							x

8.5 	AM Techonogy challenges							x

8.6 	AM Potential transformative impact						x

9. 	Conclusion										x

Acknowledgments										x

References											x

- 1. Introduction

The construction industry demands the adoption of those materials that maintain the mechanical properties of cement and other related components for modern concrete infrastructure. Ideally, this means that the tensile, compressive, and flexural strengths of concrete materials need to be improved. Advances in smart concrete have seen the establishment of nanomaterials that can be mixed with cementitious to come up with those with high mechanical strength (Bautista-Gutierrez et al., 2019). Research has established that nanomaterials have contributed to the establishment of nanomaterials that have been added to cement and concrete in order to step up the mechanical strengths, thereby aiding in reducing environmental impacts. Carbon dioxide produced during the production of cement accounts for about 7% of the world’s total emissions (Moser et al., 2012). Therefore, the main issue with the production of this construction material is how to reduce carbon dioxide emissions. One of such alternatives would be the adoption of those construction materials with high mechanical strengths and high durability. With this advancement, it is expected that concrete structures will have require less quantity of cement-based materials for construction due to their thin nature (Moser et al., 2012). Cement-based materials can be mixed with the so-called nanomaterials such as nano-silica (na-SiO2), nano-ferric oxide (nano-Fe2O3) and carbon nanotubes (CNTs). For a very long time, research has prioritized the adoption of nanomaterials in cement. The mixture of nano materials and cementitious can improve the mechanical strength of the resulting concrete. Thus, the life cycle (duration) of these structures can be increased while the amount of concrete material required is reduced significantly. A good example of a nano-material incorporated in cement is nano-silica. This material speeds up the hydration of cement due to the production of calcium silicate hydrate and dissolution of calcium silicates. Owing to research gathered globally, considerable improvements have been realized in concrete-based construction materials. As explained by Moser et al., the construction industry has been slow to implement these breath-taking improvements (Moser et al., 2012). Cost of adoption, the longevity of materials, and their functional properties are some of the aspects that make engineers and architects slow down the adoption of such techniques. The smart materials recently created including self-healing concrete or hydroceramics have laid the framework for revolutions in the construction industry. Digital technologies including 3D printing and brick molding are among the procedures that enhance smart cementitious concrete properties. While attention is placed on technology improvisations, the high costs of extraction have made many to adopt the eco-friendly techniques. Recent research reveals that new materials, enhanced automation, and digitization are inevitable and have paved the way in the construction industry. Despite this, advances in smart concrete is still a new and young area that requires alot of research to be conducted. Many engineers understand that concrete materials are the best for construction, not realizing that there is the need for improving the strength, tensile and compressive power of cement. There exists gaps in the available information concerning how to improve these properties of cement while ensuring that the amount of CO2 is kept within minimum levels.

This paper seeks to contribute to the list of existing literature studies in several ways. First, a review of smart concrete in terms of the current progress, benefits and challenges from 2015 to 2020 is expect to offer effective measures that can be used to improve the structural properties of the typical concrete. The different types of smart concrete have been developed to meet varied needs such as self-sensing, self-diagnosis concrete, self-heating, self-healing among others. However, the study will be limited to three types of smart concrete, namely self-healing concrete, self-curing concrete, and ultra-high performance. A review of these smart concrete is expected to provide how they have improved the properties of the typical concrete using different functions. Second, this study will contribute to the available knowledge about adoption of smart materials that can improve the strength, tensile, and compressive charcteristics of concrete while safegurading the environment. Third, the outcome of this research is expected to provide critical information on the development of concrete at the nano-scale. This is attributed to the fact that the atomic level of the concrete provides an opportunity that can be used for manipulating the individual atoms and molecules, which ensure that improvement on the concrete structure can be performed at the nano level. A review of existing studies indicate that more emphasis has been placed on understanding the atomic scale in construction materials, the mixture between water and other solutes combined with cement pastes (Adu-Amankwah, 2016; Biernacki et al., 2017). Additionally, the examination of the mechanical performance and the bonding of the concrete structure contribute to understanding how the graphene influences the cementitious materials.

- 2. Background

Concrete is the second most globally material in the world after water, and the most used construction material (Al-Tabbaa, 2016; Watts, 2019). Yet, its benefits are masked with many ecological disadvantages through the way it is produced, transported, or used (Ghosal, 2019; Papanikolaou et al., 2019). Regardless of its relevance, it occurs in the brittle state owing to its low tensile strength, weak resistance to crack formation, and strain properties. Initiatives have been made to improve concrete's properties by integrating it with many fibers, admixtures, and supplementary cementitious components (Rutigliano, 2019). The objective of such approaches has been to reduce the costs of construction and increase the sustainability of the environment.

It is widely accepted that fiber-reinforced concrete guarantees more tensile strength and toughness. Additionally, these fibers may substitute huge cracks with a dense network of microcracks (Chalioris et al., 2019; Yang et al., 2019). Nonetheless, as Alrekabi et al. explain, fibers cannot effectively curb all crack initiation at the nanoscale (Alrekabi et al., 2017). Rutigliano suggests that many scientists acknowledge that concrete has to be engineered at the nanoscale (Rutigliano, 2019). This is because such an improvisation allows for the changing of the mechanical and chemical composition of concrete. Concrete materials have to demonstrate improved longevity and mechanical performance as well as to integrate properties that satisfy multiple applications to match with future emerging structural projects. Thus, the nanoscale improvisation deals with the integration of nanomaterials that occur in crystalline and chemical composition forms. Those characterized based on electron movement and mode of shapes include the 0D nanoparticles, 1D nanofibers and 2D nanosheets (Jeevanandam et al., 2018). Examples of the recently manufactured and used nanomaterials include "nano-silica, nano titanium oxide, nano iron oxide, carbon nanotubes (CNTs), graphene oxide (GO) and graphene sheets” (Barrios et al., 2019; Rutigliano, 2019). Just as the name suggests, improvisation is based on their electrical properties.

The primary aim of the paper is to contribute to the available knowledge about smart construction materials (concrete) that are tensile, have greater strength and compressive power. The emphasis is in the adoption of nanomaterials, which have all these characteristics besides posseing self-cleansing features that could significantly reduce the emission of CO2 gas into the environment. A systematic review of relevant studies were solicited from Google and PubMed as the sole databases that could be used to develop a meaningful review of existing studies on smart concrete. In this case, an iterative search strategy was adopted to ensure that there was a completeness of the search for the relevant studies. Search terms and keywords  included “advances in smart concrete, nanomaterials, ultra-durability, smart materials, fiber-reinforced concrete and 3D printing.” This was facilitated by Boolean expressions and truncations that provided an effective way of searching the databases.  The selected studies were screened and only the papers that satisfied the inclusion criteria were selected for further review.

The inclusion criteria consisted of two measures that were intended to assist in reducing the number of the selected studies to a manageable number. First, it was important that the selected studies were related to development of smart concrete, which had been published between 2015 and 2020 to achieve a high level of internal validity. Second, the studies selected were scientific papers and available online. The exclusion criteria consisted of related studies that emphasized on improving the properties of the concrete structure such as durability, strength, elasticity among other properties.

By emphasizing on the inclusion criteria more strictly, a narrow scope of the study was developed which concentrate on identifying how specific smart concrete has been developed, its properties, benefits, and challenges. This was limited to cementitious materials that had been combined with various materials such as graphene, engineering cementitious composites, self cleaning concrete, self heating concretes and ultra high performance powder reactive concretes.

2.1 An overview on smart concrete

A review of existing studies indicates that smart concrete has been perceived as an intelligent system that has different structural properties as compared to the typical concrete construction from cement and natural aggregates. For instance, the self-sensing and self-healing concrete have been associated with the capacity to respond to the environment through temperature, stress or an external stimulus. The concept of “smartness” in the concrete has been achieved using the four main methods, namely material design composition, special processing, introducing other efficient components, and alteration of the microstructure. The selection of these methods has been tailored to achieve specific needs by improving on the properties of the concrete, such as the durability, strength, serviceability, reliability, cost, among other properties (Baoguo et al., 2015).Over time, the construction of concrete production has changed to achieve desirable properties that are environmentally friendly, durable and safety.

Advancement in nanotechnology has offered tools that can support the fabrication and development of materials that can enhance the functionality of the traditional cement-based materials. Scientific literature conducted in the last few decades demonstrates that interest in the use of nano-materials in the construction sector has been increased, especially the use of nanoparticles characterized by smart properties (Jeevanandam et al., 2018). Based on the findings that were presented in the Carbon Disclosure Project, it was noted that cement accounted for approximately 6% of carbon emissions while using a lot of energy during the production of concrete (Harvey, 2018). From a traditional perspective, concrete is developed based on a set of prescribed specifications, which includes the degradation of a material over a particular duration. Mitigating against the inevitable degradation calls for the use of a costly maintenance regime and in some cases, the use of a completely new approach (Rutigliano, 2019).

Concrete forms a critical component in the construction sector that is characterized as cheap, readily available and suited for casting. Despite the fact that is generally accepted in the construction sector, it has been associated with various drawbacks that affect its application. One of the main features associated with the concrete is that the cementitious materials can easily break under extreme loading and aggressive environmental agents (Khalil et al., 2015). This has significantly affects the structure of the concrete as a result of the materials that are used to develop the concrete. This in turn affects the durability of the concrete negatively. Other drawbacks that are associated with the typical concrete include reduced tensile strength and strain capabilities. Some of the remedies that have been proposed in existing literature to address these drawbacks are synthetic materials such as epoxies. However, they are not cost-effective, not compatible, diminish the aesthetic of the concrete and regularly require maintenance. To address this shortcoming, the bacterial induced Calcium Carbonate (Calcite) precipitation was also developed as an alternative that can be used as a remedy for cracks in self-healing concrete. The outcome from the use of Calcite improved on the strength of the cementitious materials.  Another approach that has been used to address the mediating the cracks and fissures in the typical concrete is the Microbiologically Induced Calcite Precipitation (MICP) method, which heavily depends on microbial activities that are autonomous from any pollution. Two benefits that have been derived from the use of the MICP method include enhance compressive strength and a reduction in the cracking as a result of stiffness in the concrete sample.

A review of existing studies indicates that several attempts have been made towards improving the performance of concrete by improving on the properties of cement composites using various materials such as admixtures, fibres or even complementary cement-based materials. Early development of carbon fibre and glass in improving the self-monitoring properties of concrete was achieved involved the application of carbon fibre and glass, which improved on the bonding features of the concrete (Krzywon et al., 2016). From this application, it was observed that the carbon fibre was a suitable cementitious material that can replace the natural aggregates when it is combined with the admixtures. Three main benefits that noted from the use of fibre to reinforce concrete included enhanced toughness, improved tensile strength, and blocking of large cracks using a dense system that is made up of microcracks. However, a wide range of studies has acknowledged that fibre has failed to prevent cracks at the nanoscale level (Gong et al., 2015; Alrekabi et al., 2017).

D’Alessandro et al. (2015) compared the sensitivity of cementitious materials that had been reinforced with carbon fibre to the typical concrete.  For uniform dispersion of fibre, silica fume and latex were utilized. The results indicated that the electrical resistance of the cement-based material differed based on the cracking. Improved conductivity in the composite was observed when the quantity of nanoparticles was less than the percolation threshold, which increased the degree of dispersion in the fibres. Dispersion of the nano-tubes in the cementitious material is a critical factor that needs to be considered to achieve improved electrical properties in the composite. In comparison, Yoo et al. (2017) examined the electrical properties and sensitivity of cementitious materials that was mixed with varying additives and the results indicated that the electrical resistivity of the cement varied during the compression cycles, which were overshadowed by the formation, opening and closure of cracks.

Zou et al. (2015) have held the notion that concrete is engineered at the nanoscale level, where the chemical and mechanical properties can be enhanced.  The cementitious materials need to exhibit improved durability, enhanced mechanical performance, and extended functionalities that apply to different uses suitable for emerging structural applications (Dimov et al., 2018). On the other hand, cement-based materials are suitable for nano-modifications as a result of its microscopic features (Ahmed et al., 2020). Some of the specific nano-materials that have been examined in recent studies include nano-silica, nano titanium oxide, nano iron oxide, carbon nanotubes (CNTs), graphene oxide (GO) and graphene sheets (Chuah et al., 2014).  For instance, the inclusion of CNTs in cementitious materials characterised by nano-metric size and high surface area, has resulted in a significant improvement in the mechanical and electrical properties (Bai et al., 2018). This is attributed to nano-particles, which support the fabrication of the composites with a high level of sensitivity. However, these factors account for low solubility and dispersion in the nanotubes that are combined in the admixture. This difficulty is associated with an increase in the surface area and the van der Waals attraction forces in the aggregates (Kharisov et al., 2016).

A study was conducted by Dimov et al. (2018) to incorporate graphene in the traditional production of concrete using nanotechnology. This was achieved through the inclusion of a water-based graphene dispersion that was characterized by high yields, cost-effective, and well-tuned for large-scale manufacturing. From their study, several outcomes were discovered concerning the improvement in the properties of the typical concrete. First, it was discovered that there was an increase in the compressive and flexural strength of the concrete by 146 and 79.5% respectively. A reduced displacement of approximately 78% was attributed to an increase in the compressive strength. Second, the study noted that the electrical and thermal properties of the graphene-based concrete had improved by 88%. Third, they discovered that there was a significant reduction in water permeability by approximately 400% as compared to the typical concrete.  This is considered as a desirable quality that is associated with the durability performance of the concrete structure, especially during the construction of flood-prone areas. Finally, the researchers demonstrated the inclusion of graphene in the concrete contributed to a significant reduction in concrete material by half while achieving the loading requirements for construction. This has, in turn, contributed to a reduction in carbon emission attributed to increased use of cement in concrete production.

2.2 Classification of smart concrete

Smart concrete represents a building material that is associated with modern technology and the typical concrete construction in an effort to improve its structural properties. However, the application of this type of concrete is still in laboratory stages of development and is quite far from enterprise-wide use. In the previous section, the historical account on how it has been developed has been presented based on the use of different admixtures that were intended to address several drawbacks that were encountered.

A review of existing literature indicates that several materials and criteria have been used to create the different types of smart concrete. Han et al. (2017) provide two main methods (criteria) that have been used for categorising concrete namely matrix and function-based methods. A summary of the classification of the smart concrete based on the behavior and matrix is presented in Table 29 as presented by Han et al. (2017). However, the focus of the sudy is limited to the construction of smart concrete using graphene, self-healing concrete, self-curing concrete, and ultra-high performance. Additionally, the study reviews recycling aggregates in concrete and additive manufacturing.

The typical concrete has first-rated properties; however, it is faced with numerous challenges that affect its structure. One of the drawbacks is reduced tensile strength, which makes it more susceptible to cracks. This, in turn, permits the flow of chemical and water, degrading its performance and requires a costly maintenance regime. However, the smart concrete is considered to possess better structural and functional behaviours, making the concrete to become a multifunctional material by inducing properties such as self-perception, self-adaptation, status retention, and self-healing (Mishra et al., 2018). This is based on the association between the composition, processing, structure and properties of the cementitious materials. These features tend to influence the internal structure of the concrete by providing techniques that can be used to anticipate the self-safety measures as well as avert the brittleness of the concrete structure (Ackermann, 2018; Mishra et al., 2018). Additionally, these features can be used to repair the concrete based on the testing result, which can improve on the safety and durability performance of the concrete structure. Despite the improvement on the typical concrete structure, it is still impossible to prepare the smart concrete using several functions and matrices based on the different technology (Mishra et al., 2018).

Using the typical concrete, several development trends have been used to classify the smart concrete into different types that are address different functions such as engineering cementitious composites, self-sensing concrete, self-diagnosis concrete, the temperature self-heating concrete, the bionic self-healing concrete, and ultra high performance powder reactive concretes, among others that have emerged to form the foundation of smart concrete.

For instance, the self-diagnosis concrete is associated with a self-sensing capability that uses pressure and temperature functions. As opposed to the typical concrete, this concrete is combined with other composite materials to introduce the self-sensor function such as the polymer type, carbon type, metal, and fibre. This type of concrete has further been sub-divided into the carbon fibre and optical fibre sensor smart concrete. On the other hand, the self-healing concrete can emulate the biological aspects, which secrete certain substances, while the self-repairing concrete is used to address the cracks in concrete.  From a critical look at these concretes, it can be noted that each serves different functions.

- 2.3 Sustainable solutions for the construction industry

Based on the Concrete Industry Sustainability Performance Report that was published in 2017, it was noted that regulating the ecological effects of production and procuring resources contributed significantly to sustainable development. Besides, it was also noted that the materials were considered more sustainable as long as the different functions were achieved. Otherwise, the cementitious materials become less sustainable when the typical concrete production is used for construction.

As explained by the Association of Equipment Manufacturers, many firms now aim at limiting the ecological effects of concrete (Association of Equipment Manufacturers, 2018). Great Britain developed the Concrete Industry Sustainable Construction Strategy in 2008 to provide a unified the wastage, thus, reducing costs of construction. Improvisation also enhances concrete performance, longevity, consistency, performance, and applicability.

The international pressure for sustainability has also affected the cement and construction industry. Most of the concrete industries are focused not only on achieving environmental sustainability but also to make their concrete solutions adaptable and with a wide offering. As explained by the CEO of Solidia, Tom Schuler states that companies are now concentrated on mixing concrete with secondary cementitious materials (SCMs) such as fly ash and slag. They also work towards achieving alternative fuels and improving kiln's performance.

The increased use of cement for the construction of concrete around the globe has drawn a lot of interest from scholars and experts in the construction sector in an effort to develop better alternative materials that improve the properties of the versatile concrete.  From the review of existing studies, it was noted that concrete has evolved immensely over the passage of time. This study envisage some of the latest smart development of concrete ranging from the typical concrete that is considered brittle,  reduced tensile strength and strain capabilities to the concrete with improved properties such as self-healing concrete, self-curing concrete,  and ultra-high performance powder reactive concretes. Each of these smart concrete are examined individually in terms of the applications and opportunities it offers, technology used and its potential, benefits, and  challenges that are encountered in the construction.

- 3. The emergence of smart concrete such as graphene

The review by the Association of Equipment Manufacturers (Association of Equipment Manufacturers, 2018) shows that smart options are another growing trend for concrete improvisation. The cement market is focused on attaining multifunctional concretes. These types of concrete are characterized by some functional and intelligent properties. Since cement in dry conditions cannot conduct electricity appropriately, experts had to explore other alternatives since the aim has been to find concrete with high electrical conductivity. The process of degredation in structures that have been reinforced by concrete will affect the durability of the material. Ions posses charges, and therefore, the ability of concrete to transfer ions is a product of its electrical resistivity (Sofi, 2016; Azarsa, 2017). It is due to this that there is a connection between the deterioration process and electrical resistivity. It should not be forgotten that electrical conductivity is one of the significant indicator of impermeability, and durability of materials. It is also one of the best measures for some special cement-based materials, for instance, insulating concrete (Liang, 2017; Cordon, 2020). Whereas previous initiatives integrated large quantities of steel fibers, magnetite, and carbonated forms both natural and synthetic, it could not achieve high electrical conductivity. Besides, the loading of active ingredients attracted many issues including corrosion, cost, compressive strength, weight and maintenance expenses, and abrasion resistance (Rutigliano, 2019). Such reasons made scientists integrate graphene into concrete to increase electrical conductivity capability.

As the Berkeley Lab reports, graphene “has been touted as the strongest material known to exist, [and it’s] 200 times stronger than steel [and] lighter than paper” (Berkeley Lab, 2016). Such incredible innovations could promote "greener" concrete alternatives. Nanotech study presents an experiment by Monica Craciun, the professor of nanoscience from the University of Exeter. Monica experimented with this greener approach by immersing graphene into water. She then utilized this water solution as a complementary element for concrete aggregates. After testing this concrete, experts found out that "the concrete was two times stronger than usual, four times more water-resistant, and far more elastic." Such is a remarkable and unexpected improvisation (Nanotech Real Estate, 2018). This implies that half the material can be utilized while still gaining more durability than traditional concrete.

Wang et al. define smart concretes and structures as intelligent systems whose behaviors differ from traditional cement (Han et al., 2015). For example, they have self-healing and self-sensing characteristics. Others may positively respond to external stimuli, such as pressure, heat, or stress. Through concrete’s smartness ability, they can respond to the stimuli without human intervention. The self-healing properties allow concrete to respond to air and water restoring the physical and mechanical properties damaged by exposure to such elements (Li, 2019). Thus, they promote longevity and resilience.

Construction firms attain concrete’s “smartness” by combining with other functional elements, through special processing, transforming the microstructure, or changing composition design. Smartness processes transform their properties to enhance safety, serviceability, durability, long-term performance, safety, and cutting life-cycle expenses. These high-performance characteristics also make concrete resilient and sustainable. As cement becomes more sustainable, quality of life also improves. Examples of high-performance cement properties include “greenness” of cement, autogenous crack-width control, and tensile ductility. Digital improvisation also contributes to high-performance characteristics of cement. Thus, concrete smartness is a combination of multifunctional concrete based on technological advancement and physical and mechanical properties.

Chung discusses that the need for “Multifunctional concretes that serve both structural and nonstructural functions have evolved from concretes that are purely structural materials … For example, self-sensing concrete can sense its condition (stress, strain, damage, etc.) without any embedded or attached sensor” (Association of Equipment Manufacturers, 2018). However, achieving multifunctional properties is a tedious process that calls for experience in the functional elements. Manufacturers must, therefore, understand electrical and other properties of cement (Association of Equipment Manufacturers, 2018). Nonetheless, most experts do not have significant information in functional properties but because of the relevance of smart concrete, the expectation is most of these blocks of cement are to be produced.

Production of cement is changing and important for various reasons. Traditionally, cement production has been seen as an easy, straightforward, and cheap process. A research conducted by Abir Al-Tabbaa for World Economic Forum shows a changing perception in the manufacture of cement (Al-Tabbaa, 2016). Firstly, the production capacity of cement is almost three metric tons for every individual on earth. Lim et al. (2018) reveals that concrete companies are the leading emitters of carbon dioxide across the globe. Cement contributes up to 8% of all anthropogenic carbon dioxide emissions (Andrew, 2018). Research suggests that nearly one tonne of cement manufactured produces 0.471 tonne of CO2 (Andrew, 2018). Secondly, besides contributing to automatic repair and monitoring, it is a useful resource for infrastructural development (Xu et al., 2015; Erdenebat et al., 2017; Association of Equipment Manufactures, 2018; Bonnet et al., 2019a; Bonnet et al., 2019b). Thus, the future is brighter for cement concerning improvisations only when various aggregates (self-cleaners) are incorporated. Cement is the major raw material for construction industries. Even though this research has established significant enevironmental impacts, the inclusion of nanomaterials will see the production of an environmental friendlycement with greater strengths and compressive index.

Other than Solidia, Giatech Scientific Inc. is another company that manufactures smart cement. Pouria Ghods and Aali Alizadeh, Canadian experts, founded the company. They use technology that can evaluate different cement properties such as corrosion and hardening in real-time (Association of Equipment Manufacturers, 2018). This technology integrates mobile applications and cement sensors that convey important data to contractors. Such data deals with construction projects such as cement composition, properties, or related updates. Giatech Scientific Inc. also established non-destructive testing technologies, which enables experts to control civil infrastructure through automated scheduling maintenance, rehabilitation, and replacement operations more efficiently. Whereas smart concrete is cheap, the embedded technology of sensors and mobile applications costs more.

Many transformations are taking place in the concrete industry that would fully transform it. While some aim at changing the material composition, others embed technological components to promote monitoring. Each of these contributions promotes smart and sustainable concrete that can detect structural faults before they become detrimental (Association of Equipment Manufacturers, 2018). Accordingly, this is transforming the mode and type of operations at job sites. Engineers currently interrelate with advanced technologies and new materials that are improving the mode of operations at construction sites.

There are different types of “Smart” materials such as piezoelectric, magneto-restrictive, pH-sensitive, chromogenic systems, and shape memory alloys (Bhatnagar, 2016; Heggade et al., 2016; Sivakumar and Naseem, 2016; Jain et al., 2017; Lakshmi et al., 2017; Sadiku et al., 2017; Gupta, 2018; Smart Materials and Structure, 2019). The manifestation of each of these elements differs.

- 3.1 Applications and opportunities of smart-cementation materials

Using smart concretes such as graphene limits the discharge of carbon dioxide by half and the same time creates sustainable construction resources for roads, houses, bridges, dams, and other structures (Augustyniak et al., 2018; Gibb et al., 2018; Díaz-Soler et al., 2019). The nanotech study quotes Professor Monica Craciun who states, "Our cities face growing pressure from global challenges on pollution, sustainable urbanization, and resilience to catastrophic natural events.” Such an invention completely revolutionizes the construction industry. It reinforces conventional concrete to achieve construction needs. Since support infrastructures including walls will only need half the concrete they currently use, not only does this create more avenues for architecture and design, but it also hastens building duration while also reducing pollution. Such nanotechnology benefits add to ecological sustainability.

Smart materials can also be used to manufacture different types of sensors, which is linked to signal transmission and diagnostic monitoring. The role of such sensors is to monitor the strain and stress of the health of structures. They can detect damages, cracks, or even determine early age curing behaviors. Therefore, sensing is an integral component of smart cementitious materials. Carbon nanofibers and nanotubes can be used as reinforcement materials. Residual cement made from such carbon elements exhibits high compressive strength with improved mechanical properties such as the chemical and electronic constituents. Additionally, concrete based elements with self-sensing or piezoelectric sensors can provide actual tracking of vehicles that appropriate for smart traffic control. Most of these elements tracking elements are composed of multi-walled carbon nanotubes. Another application of smart cement comes with the integration of iron oxide nanoparticles. The resulting aggregate has improved piezoresistive properties that equally contribute to actual tracking. At the same time, it improved the modulus of elasticity and strength for oil well structures. The benefit with tracking and real-time data collecting using smart objects, particularly in large-scale applications, will allow and promote present “big data” approaches such as multi-resolution and sampling.

- 3.2 Technology potential and impacts

The use of smart cementitious materials is based on their ability to detect cracks, moisture content and transportation capabilities, and stress-strains behaviors. These characteristics are important since they determine the safety and reliability of concrete for energy, transport, and civil infrastructural uses. Furthermore, they detect aging behaviors of complex structures. With sense, it is possible to detect and control aging and degradation of materials to avoid further calamities and loss. These operations are possible with the use of smart cementitious materials such as cement and concrete improvised using modern technologies. They also promote real-time response to situations. In other incidences, self-healing can promote efficiency and safety of operations. Actual tracking of infrastructure using “smart” cementitious composites can enhance the existing design capabilities.

According to recent trends in the construction industry, many customers have a propensity towards structured and unstructured data as shown in Table 1. For example, the overreliance on ad hoc interfaces, full-filed imaging, and mobile computing will make sensors attractive in the construction industry.

[Insert Table 1]

- 3.3 Benefits

According to Rutigliano’s article, graphene is a carbon atom with remarkable electrical, optical, thermal, and mechanical properties (Rutigliano, 2019). Graphene is a single carbon element that is already in use in various nano-engineering applications due to its energy storage capability, sensory ability, flexible electronics, and thermal management. It can also perform liquid filtration alongside other nano-composite characteristics. Owing to such properties, many engineering firms have considered integrating it alongside conventional concrete manufacturing.

Concrete manufactured via this mode of reinforcement occurs under an environment of water‐stabilized graphene dispersions. This improvisation has is largely affordable and complies with the large‐scale cement production and construction. As explained by Rutigliano, graphene-reinforced concrete exhibited an outstanding increase in compressive strength of 146 % (Rutigliano, 2019). Similarly, flexural strength increased by 79.5% with a reduction of maximum displacement because of a 78% rate of compressive loading. The final concrete also had improved electrical and thermal properties with an 88 % rise in heat capacity. The rise in healt capacity meant that cement became resistant to change in tempearature and could connect electrical currents.

Besides, the study confirmed an almost 400% decline in water permeability in contrast to traditional concrete. Water permeability is a largely desired characteristic and agents with such a considerable capability are demanded since they promote the long-term performance of concrete projects and can effectively apply locations exposed to flooding or for construction of bridges. Lastly, the study demonstrated that the integration of graphene in currently used concrete would cut concrete material requirements by 50%. Regardless of the reduction in the quantity of concrete, graphene reinforced concrete would still achieve the loading specifications for structures. As Dimov et al. (2018) explain, eventually, more than 446 kg per tonne of the carbon dioxide emissions emanating from concrete production would be controlled, thus, contributing to environmental sustainability. The Journal of Cleaner Production will serve as an interdisciplinary in exchange of information on concepts, technologies and policies designed to ensure progress towards societal sustainability (Severo et al., 2015). There is the need for industrial renovation in the construction industry to bring about the production of cleaner products and services.

- 3.4 Challenges

Cost and toughness are issues that graphene concrete currently faces. While its possibilities are exciting, not everyone is persuaded about its commercial viability. Whereas graphene concrete makes the construction process simple and quick, it is very expensive, which might discourage most contractors. Berkeley Lab report doubts the ability of graphene concrete in withstanding toughness compared with concrete using other improvisations such as steel. Berkeley’s University laboratory successfully produced a statistical theory for the toughness of polycrystalline graphene. This solution is manufactured by depositing chemical vapor. Whereas polycrystalline graphene was perceived to have high strength, it did not have toughness exhibited in other concrete techniques (Berkeley Lab, 2016). While it was tougher than graphite, it was less tough than diamond. Ritchie, Berkeley Laboratory scientist suggested that “It is extremely high strength is very impressive, but we can’t necessarily utilize that strength unless it has resistance to fracture.” The scientist further revealed that this polycrystalline graphene is “a mathematical model that takes into account the nanostructure of the material … We find that the strength varies with the grain size up to a certain extent, but most importantly this is a model that defines graphene’s fracture resistance” (Berkeley Lab, 2016). Irrespective of such bottlenecks, graphene will define the future of smart concrete.

Graphene material is yet to gain confidence in the supply chain. As Pollard explains, finding graphene suppliers is a barrier in itself as the material is not yet readily found on shelves. Many firms seeking to develop graphene-based products do not always establish reliable suppliers because of batch-to-batch variability. Such a challenge can worsen when neither the supplier nor end-user does not recognize the mechanical or chemical characteristics of graphene. Besides, most suppliers have issues in measuring a proportionate representation of the number of nanoscale flakes using tons. Rutigliano also notes that being a new approach, graphene producers must learn to how to raise graphene’s concentration in solutions alongside increasing volumes of production (Rutigliano, 2019). Since this solution’s concentration is normally 1g/L, transportation may not be environmentally attractive or economically convenient.

- 4. Self-healing concrete

Senthil et al. describe self-healing material as elements that can achieve self-repair and return to the original condition (Senthil et al., 2019). Self-healing is done to reduce cracks, reduce maintenance expenses, and increasing strength and durability (Devgire, 2019) as shown in Table 2. An experiment by Prabahar et Al. shows that there are different types of self-healing improvisations that include "bacterial encapsulation, self-healing with self-controlled tight crack width, chemical encapsulation, the chemical in glass tubes and mineral admixtures" (Prabahar et al., 2017).

[Insert Table 2]

The construction industry seeks to utilize self-healing concrete due to its sustainability benefits and long-term performance (Park and Choi, 2019; Reddy and Ravitheja, 2019). The study by Ackermann examines the self- healing properties of structural and early age cracks (Ackermann, 2018). This experiment utilizes crystalline admixture (CA) as an improvisation tool. Concrete is exposed to four different environments. Final testing seeks to evaluate concrete's regained mechanical properties. Energy-dispersive spectroscopy (EDS) is used to study the chemical properties. On the other hand, Fourier transforms infrared spectroscopy (FTIR) analyzes the physical characteristics. Findings revealed that in all the exposure environments, the concrete gained both the split tensile and compressive strengths. This after the mixture (Table 3) was treated with crystalline admixture (CCA) following structural and early age cracks. CCA solution increased calcite content present in concretes. Calcium carbonate has been used for a very long time as a cementitious composite that affects the properties of concrete such as nucleation and dilution effect (Jo et al., 2017; Özcan and Kaymak, 2018; Cao et al., 2019). Calcite content fills the viod between cement grains, increasing the hydration process, durability, mechanical properties, and chemical efefcts.

[Insert Table 3]

- 4.1 Experiment

Reddy and Ravitheja describe the four stages adopted for analyzing self-healing concrete’s impact includes the following (Reddy and Ravitheja, 2019). First is the determining mechanical property of conventional cement and one with CA at 28 days. The second stage involves creating control damage in the sample that includes early age and structural cracks. The third stage involves exposing the aggregate to a solution, then lastly, measuring the regained mechanical properties.

- Compressive strength (CS). The study determined whether the concrete regained some of its strength after exposure to minor damage. After 42 days of testing, concrete with CCA had 11.46% compressive strengths. This is because the pores were filled by CSH and calcite solution due to normal hydration process of cement. Additionally, compressive strength for cement with early age cracks under 42 days of curing declined by 36.07% for AE2, 15.29% for WD2, 4.47% for WC2, and 7.18% for WI2. This level of decrease was more as compared with that of CCA after 28 days curing. The reason for this reduction is the inadequate calcite that builds up within the cracks.

Accordingly, after CCA was exposed to 42 days of structural crack curing in WI28 (water immersion), it gained strength by 13.98% and 7.72% for WI28 and WC28 (water contact) compared with 28 days of curing, and this was more than conventional concrete. The compressive strength for structural crack reduced by 9.79% for WD28 (wet-dry) and declined by 23.82% for AE28 (air exposure) after 28 days of curing. These findings are as shown in the tables 4, 5 and 6. Compressive strength recovery was defined by the self-healing of the current micro cracks. The activating effect of the crystalline admixture caused the pores to hydrate.

[Insert Table 4]

[Insert Table 5]

[Insert Table 6]

- Split tensile strength (STS) analysis. STS is the tensile stresses created due to the application of the compressive load, which may expose concrete aggregates to cracks. For this experiment, after CA was exposed to 28 days of water curing, it gained strength by 35% more than conventional concrete. Additionally, STS for cement with early age cracks under 42 days of curing declined by 50.13% for AE2, 26.50% for WD2, 25.98% for WC2, and 14.43% for WI2. This level of decrease was more as compared with that of CCA after 28 days curing, which remained high. Accordingly, after CCA was exposed to 42 days of structural crack curing in WI28, it gained strength by 2.88% more compared with 28 days of curing, and this was more than conventional concrete. For instance, STS for cement with structural cracks under 28 days of curing declined by 26.02% for AE28, 3.67%, for WD28, and 16.83% for WC28. STS recovery CCA after healing of structural and early age cracks for CCA in WI (80–105%), WC (70–100%), WD (70–90%), and AE (45–80%) are shown in tables 7, 8 and 9.

[Insert Table 7]

[Insert Table 8]

[Insert Table 9]

- Load displacement (LD) curve. Concrete materials that should work in infrastructural construction should demonstrate high-energy dissipation and deformation capacity. This is as represented in the Figs. 1 and 2. The addition of CA to the mixture contributes to more deformation. This is because hydrated products start to develop rapidly. The Figs.1 and 2 also show that concrete healed both for 2 and 28 days for each crack recaptured their deformation capacity.

[Insert Fig. 1]

[Insert Fig. 2]

- 4.2 Application benefits

Another experiment by Momin et al. using bacteria and steam curing established that these methods contributed to positive strength recapturing by concretes (Momin et al., 2018). Steam curing was preferred since most of the bacteria could only survive up to 350 - 550 0C yet lime formation could still exist over the cracks. Strength was improved further when curing was integrated with artificial chemical admixtures. Self-healing was determined by various factors and is not limited to bacteria effect alone. CA is a reliable solution that can absorb moisture content from the atmosphere and promote self-healing of concrete. They have hydrophilic properties that make this process possible. The water and exposure to dry-wet conditions further constitute self-healing of both structural and early cracks of concrete. Ensuring hydration eventually improves the mechanical properties of concrete, which improves the compressive and tensile strength of concrete.

- 5. Self-curing concrete

This is another established method for producing smart concretes, which deals with the application of curing elements on surfaces of concretes. The commonly used solutions include polyethylene glycol or pre-saturated lightweight aggregates. A self-curing approach is an approach that counteracts autogenous shrinking and self-desiccation. Self-desiccation is the shrinkage of concrete due to a decrease in relative humidity, while autogenous shrinking is the decrease in volume of concretes due to internal structural and chemical processes (Ambily and Rajamane, 2019). As Nduka et al. discuss, self-curing is an important technique required for the construction of tall apartments and bridges (Nduka er al., 2018). Such conditions require restoration and protection of concrete from extremities of dehydration.

In their experiment, Mousa et al. compared various concretes (Table 10) cured using silica (Table 11) and other admixtures for 28 days (Mousa et al., 2015). The concrete was exposed at different temperatures (25 0C and 50 0C). Leca and polyethylene glycol (Ch) (Table 12) were the main self-curing elements. Factors determined included compressive and tensile strengths, water absorption rate, and mass loss.

[Insert Table 10]

[Insert Table 11]

[Insert Table 12]

After exposure to 25 °C air curing for 28 days, the compressive strength increased steadily as shown in Figs. 3 and 4. Self-curing with silica had the highest strength (26.5%) followed by Ch (20.6%), leca (8.8%,), relative to traditional concrete. Silica, Ch, and leca were applied in respective percentages of 15%, 2%, and 15%. An increase in temperature to 50°C slowed down the compressive strength. This rate was still higher than conventional concrete as shown in Table 13.

[Insert Fig. 3]

[Insert Fig. 4]

[Insert Table 13]

As indicated in the table above, an increase in temperature raised the strength of self-curing concretes compared with the conventional 25 0C as shown in Table 14.

[Insert Table 14]

After 28 days of testing, the concrete with 2% Ch and 15% silica fume had the leading improvement of compressive strength by almost 37.8%, 44 %. This rate was higher relative to concrete in conventional temperature.

After exposure to 25 °C air curing for 28 days, tensile strength increased steadily. Self-curing with silica had the highest strength (29.8%) followed by Ch (14.3%), leca (9.1%), relative to traditional concrete. Silica, Ch, and leca were applied in respective percentages of 15%, 2%, and 15% as shown in Figs. 5 and 6.

[Insert Fig. 5]

[Insert Fig. 6]

Results from Mousa et al. indicate that incorporation of 15% silica fume and other self-curing agents enhance the performance of concretes across all curing regimes (Mousa et al., 2015). These agents reduce water permeability thus promoting strong bonding of aggregates and cement paste.

Another study by Poovizhiselvi and Karthik examined different strengths of M20 (Table 15) and M30 (Table 16) grade after 28 days to determine their properties and self-curing capacity (Poovizhiselvi and Karthik, 2017). Mechanical properties analyzed were the CS, STS, and flexural strengths. Testing was done using Compression Testing Machine (CTM). For a compressive strength test, aggregates of 150 mm length by 150 mm width by 150 mm height were measured using IS 516-1959 test. Samples were marked and taken out of the molds and then immersed in water after which testing was done. By placing samples of a 2000 KN load capacity CTM, a 140 kg/cm2/min load is applied. CTM then shows the sample's load failure. For the split tensile strength (STS) Test, a 3000 KN CTM was used to assess the sample's STS. The load capacity was continuously applied at a steady pace until the sample's resistance wears down and no further sustenance was observed. In measuring the flexural strength, samples were placed on CTM, which exerted a 180 kg/min load alongside 13.3 cm double lines on the mold. The load was increased until the specimen failed.

[Insert Table 15]

[Insert Table 16]

Table 17 provides percentages of different mixtures ages, which are “NM, PEG 0.5%, PEG 1%, PEG 1.5%, and PEG 2%” (Poovizhiselvi and Karthik, 2017). The CS for each of these solutions at 28 days is tested for M20 and M30. The workability of such aggregates is sustained with an increase in the rate of superplasticizer.

[Insert Table 17]

Table 18 provides percentages of different mixtures ages, which are “NM (mix designations), PEG 0.5%, PEG 1%, PEG 1.5%, and PEG 2%” (Poovizhiselvi and Karthik, 2017). The STS for each of these solutions at 28 days is tested for M20 and M30.

[Insert Table 18]

Table 19 provides percentages of different mixtures ages, which are “NM, PEG 0.5%, PEG 1%, PEG 1.5%, and PEG 2%” (Poovizhiselvi and Karthik, 2017). The FS for each of these solutions at 28 days is tested for M20 and M30 as shown above. The above experiment shows that the maximum strength of the specimen was 1% for M20 and 0.5% for M30 samples. Internally cured concrete has more long-term performance and strength than those cured externally. Additionally, internal curing is cheaper compared with the external alternative.

[Insert Table 19]

- 5.1 Benefits

Among the benefits that come with this practice, Gopala and Putturu (Gopala and Putturu, 2018) suggest that it enhances concrete’s hydration, promotes compressive strength, limit cracks, and autogenous shrinking. The study by Udhanyan and Rajamane also established that self-curing reduced permeability and enhanced concrete’s longevity (Udhanyan and Rajamane, 2017). Similarly, the appropriate curing approach implemented on the course of concrete mixing is an important option that curbs the deficit of traditional curing practices. Among cement improvisation analyses, many scholars have intimated that internal curing has significant effects on concrete performance. Some of the findings revealed that less desiccation, more hydrated cement, and high water retention capability in self-curing concrete contributed to improved longevity and mechanical composition of cement.

The study by Nduka et al. (2018) summarized the following as befits accruing from the use of the self-curing technique as shown in Table 20. Justs et al. study sought to limit self-desiccation in UHPC. The authors also determined that since autogenous shrinkage contributed to low performance, they reduced it alongside the dehydration improvisation of the UHPC (Justs et al., 2015). Using the self-curing method, results indicated improved mechanical properties and reduced internal relative humidity. Additionally, Olawuyi and Boshoff experiment integrated SAP as a curing solution (Olawuyi and Boshoff, 2017). Employing various curing regimes that include air void distribution using the micro-CT analyzer, final concrete demonstrated improved mechanical properties. Accordingly, different tests by Afifi and later of Rahman (Afifi, 2016) exhibited related findings in reducing autogenous shrinkage, providing better mechanical properties, and enhancing long-term performance by adopting lightweight aggregates for the self-curing process.

[Insert Table 20]

- 5.2 Challenges

As discussed by Poovizhiselvi and Karthik, efficiency of self-curing agents may be determined by mix proportions (Poovizhiselvi and Karthik, 2017). For instance, water and concrete ratio and content of the cement may inhibit the effectiveness of these solutions, especially when the mixture is overdiluted. Moreover, the application of these self-curing methods may not guarantee better results among stakeholders without sufficient knowledge of each technique and factors associated with them.

- 6. Ultra-high performance concrete (UHPC)

Sidodikromo et al. investigated recent progress in concrete engineering and technology, including the UHPC (Sidodikromo et al., 2019). They established that UHPC is one of the recent methods of concrete improvisation, whose functionality and flowability can increase by adopting optimum grading of particles. They found that UHPC is a cement-based composite that portrays durable properties and mechanical features of high compressive strength above 150 MPa. The material also has a high tensile strength averaging 7 MPa (Azmee and Shafiq, 2020). As stated by Kusumawardaningsih et al. (2015), compared with conventional cement, UHPC has high compressive strength and durability. They found out that the benefits of such cement characteristics have made many scholars manufacture UHPC with advanced engineering properties. Most of the UHPC has ultra-high strength and durability. Some come with fiber reinforcement while others do not. Average UHPC demonstrates a 28-day compressive strength with at least 150 MPa (Lim et al., 2018). Nonetheless, the more the compression strength increases, the less ductile cement becomes. Hence, synthetic or steel fibers are usually blended in UHPC manufacturing. Thus, this integration leads to “ultra-high-performance fiber-reinforced concrete (UHPFC) with ductile behavior and enhanced mechanical properties” (Lim et al., 2018). Most of the mechanical properties improve with the integration of UHPC compared with conventional concrete.

Common UHPFCs distributed globally include “Lafarge-patented Ductal, CorTUF by US Army Corps of Engineers, and BSI and Densit in Europe.” The applicability of UHPC is determined by quality control of the materials and their consistency. These materials are largely applied in bridge construction in America. In such a case, the composition of UHPC is more sophisticated compared with traditional cement. Production of UHPC is a blend of several constituents. Approximately ten different elements are combined to produce UHPC. Since it has different ingredients, the final UHPC solution varies based on original mixing solutions. The resulting UHPC must be placed under a special mix design and curing regime to eliminate unwanted composition.

Part of the special mixing design integrates supplementary cementitious components including granulated blast-furnace slag, silica fume, and fly ash. Residual cement design with these components will gain more longevity compared with the ordinary Portland cement (OPC). Granulated blast-furnace slag and fly ash are the commonly used replacing ingredients. Fly ash replaces up to 30% of the cement composition, which contributes to high compression strength and toughness (Golewski, 2017). On the other hand, up to 70% of granulated blast furnace slag is required to improve compressive strength in the future and is appropriate for large scale concreting applications. The utilization of slag in concrete as a partial replacement material shows that these aggregates have better workability that could improve the tensile, compressive, and flexural strengths (Palod et al., 2017). It is this ability to improve in strength that slag is utilized on large scale concentrating applications.

- 6.1 Mixture design of UHPC

As discussed by Meng, UHPC’s constituents should be less costly and sustainable to attain a high packing density, to minimize porosity, and enhance internal microstructure (Meng, 2017). These characteristics guarantee outstanding longevity and improved mechanical properties. Meng’s study corroborates the above findings, indicating that high strength and long-lasting UHPC can be produced by reducing composite porosity. It should also integrate a denser matrix by determining the appropriate particle size distribution of aggregate elements. Minimising water-to-binder ratio (w/b) is achieved with the integration of high-range water reducer (HRWR). Most of the ingredients for the production of UHPC are under three-component premixes. These include organic fibers, powders, and superplasticizer. Examples are silica fumes, organic fibers or steel, quartz flour, water, Portland cement, fine silica sand, and high range water reducer.

- 6.2 Models for mixture design of UHPC

There are different models recommended for the mixture design of UHPC. Berry et al. (2017), developed the response surface methodology (RSM) that comprises sophisticated regression equations that can track and foretell the properties of an element in the UHPC aggregate (Berry et al., 2017). Whereas this model provides precise information on the reactions and properties of elements, there is a need for trial batches. The integration of trial batches into this method makes the whole process not feasible. Therefore, other approaches are required for the improvement of the elements.

Soliman and Tagnit-Hamou recommend a linear packing density model (LPDM) for the mixture design of UHPC (Soliman and Tagnit-Hamou, 2018). Nonetheless, this model does not concentrate on the interactions of aggregate ration and packing density because of the linear nature of this method. Thus, the approach was enhanced taking into account the virtual density theory. This improvisation prompted the emergence of a new model called the solid suspension model (SSM). Hoang et al. proposed a stepwise optimization model, whose functionality is based on UHPC’s particle packing density (Hoang et al., 2016). Initially, the superplasticizer-water solution analysis approach was utilized to establish the compatibility of aggregates including superplasticizers, quartz powders, and silica fumes (Table 21). It also measured the compressive strength and packing density of each of these elements. This measurement established appropriate elements and optimum cementitious pastes. Accordingly, there was a mixing of these pastes with stable volumes with aggregate produced from sand, quartz, or ground basalts. Suitable concrete ratios were established considering the plastic viscosity and highest self-flowability rates. These rates were based on the aggregates blended with cementitious pastes.

In another experiment, Ghafari et al. utilized a statistical mixture design (SMD) method in improving the aggregate composition and design of ultra-high performance concrete (Ghafari et al., 2015). They evaluated the impact of individual elements and their reactions and relations to foretell UHPC’s compressive strength of UHPC under minimal content of concrete. The researchers further utilized another mode, the artificial neural network (ANN) in forecasting UHPC’s functionality under various treatment environments. One of the ANN’s models, the polynomial regression, could provide accurate predictions of the required UHPC aggregate behaviors. The suitable quantity (volume) of silica fume and concrete required was 9% and 24% correspondingly. According to the final remarks, the ANN model was preferred over the SMD model. This is because it provided more optimized results regarding UHPC aggregate properties and characterization.

[Insert Table 21]

- 6.3 Optimization of water and high-range-water reducer (HRWR)

Considering the important function that water and HRWR have in regulating the UHPC workability, and the remarkable effect of water/binder ratio in the UHPC compressive strength (Fig. 7), production of Group #1 UHPC aggregates as shown in Table 22 encourages reduction of the water/binder ratio to optimize strength, which guarantees reliable fresh mix workability. Considering the results initial trials as seen in the Fig. 8, hooked steel fibers with 30 mm height and 0.5 mm diameter were utilized in the aggregates first at 1.0 vol% (“UHPC-B2” & “UHPC-B3”). Later, they were utilized in aggregates at 1.5 vol% in (“UHPC-B4a” & “UHPC-4b”). The need for the use of the second mixture was because the workability of the initial fresh aggregates was admirable.

Considerable results followed the utilization of HRWR at 25 % of water. There was a high flowability at 0.16 water/binder ratio. Nonetheless, compressive strengths across the different days attained through thermal treatment were not much raised. It still was within the brackets of 100 - 115 MPa. The expected compressive strength is 150 MPa, which calls for further improvisation. Furthermore, the approach taken for mixing UHPC constituents is as represented in the Fig. 10.

[Insert Table 22]

[Insert Fig. 7]

[Insert Fig. 8]

- 6.4 Challenges facing UHPC

Whereas UHPC is already in use in various applications globally, it encounters many constraints for wider implementation, particularly in the United States and Canada. The gains of this intuitive material are yet to be fully established. Setbacks to address before providing reliable UHPC are as follows. First, there is a need to establish a rationale for the maximization of UHPC elements and mixture design (instead of depending on trial mixes) to guarantee effective manufacture and implementation. Secondly, owing to the low w/b of UHPC, there is a need for high-energy mixers for the appropriate blending of its aggregates. Besides, modifications should be made in precast site mixers to maximize precast constituents.

Thirdly, UHPC flexural characteristics are affected by the orientation of fibers. Hence, creating a stable approach that permits the successful distribution of fibers within the aggregate solution with requisite orientation is needed, particularly for casting slender components. Four, blends of UHPC have high shrinkage strains compared with those in normal concrete. Thus, uniquely designed admixtures or protective approaches are necessary to avoid risks connected with dimensional stability, especially for full-scale infrastructural projects. The fifth challenge is that UHPC’s high strength and longevity characteristics are determined by thermal improvisation. Hence, there is a need for uniquely designed plans for thermal treatment for on-site manufacturing and at precast projects. Lastly, globally recognized, simple and feasible design plans should be created for UHPC (for both non-reinforced and reinforced) to guarantee users of the stability and reliability of successfully using the long-lasting and high strength UHPC.

- 6.5 Benefits and applications

Whereas the flexural strength of UHCP is determined by the curing regime and other properties, it nonetheless commands up to 48 MPa FS. Abbas et al. (2016) state that “horizontally cast beam specimens achieved nearly five times higher flexural strength compared to that of vertically cast beam specimens due to improved fiber orientation. “ This strength increases with a corresponding increase in fiber on a linear arrangement as well as with the decrease of specimen size. The intense micro- and macro-structures gives UHPC higher bonding capacity. These characteristics also promote durability, which eventually reduces the need for stronger reinforcing aids. It is also an economic use of concrete due to the limited cross-sectional dimension. Since it has an overall less structural weight, UHPC has been recommended for high-rise structures and applications in areas prone to earthquakes. Additionally, this concrete performs better on impact loading, which makes it appropriate concrete for military projects (Abbas et al., 2016). This is because infrastructure from the military has high exposure to blast loading. UHPC is a durable alternative since it reduces the volume and size of orifices. This mixture has a dense microstructure that reduces water absorption, which eventually reduces the effect of corrosion. UHPC limits porosity by eliminating water contents and attached air, which was also found to have reduced diffusion of chloride.

- 7. Steel fibre reinforced concrete (SFRC)

Another recent improvement has led to the production of steel fiber reinforced concrete (SFRC), which has gained much traction because of the advantages that fibers provide that enhance the cement’s longevity, resistance to cracks and fatigue, force, anchorage, ductility, and tensile strength (Oliari et al., 2019). “The use of macro fibers, such as steel fibers, as reinforcement in concrete is well-established in applications such as industrial pavements, precast structural elements, tunnel lining" (Błaszczyński and Przybylska-Fałek, 2015) Using SFRC as a compound matter, the cementitious matrix is blended under a discontinuous reinforcement. Steel fiber is the main material for reinforcement that is unevenly inserted in the mixture. The study by Marcos-Meson et al. utilized Portland cement binders as substitutes for steel reinforcement (Marcos-Meson et al., 2018). They placed concrete into a solution with elastic mechanical properties in specific mixture proportions. That is, in the non-cracked condition just as the traditional cement.

Constructors have increasingly embraced SFRC for prefabricated and in-situ concrete applications. For instance, it is widely adopted as auxiliary reinforcement for semi-permanent loads. Examples include reducing exposure to transportation cracks, arresting shrinkage fractures, and installation of precast concrete structures. SFRC can as well serve as a partial replacement of the traditional reinforcement. In this case, it is used in blended reinforcement structures. Additionally, it can serve as a complete substitution of the traditional reinforcement in components to compressive strength. Examples of complete replacement applications include thin-shell projects, basements, ground-supported slabs, and tunnel linings.

The experiment by Błaszczyński and Przybylska-Fałek assessed the impact of destruction on steel-reinforced concrete using two approaches, the deformation, and acoustic emission (Błaszczyński and Przybylska-Fałek, 2015). Both the critical initiating stress (i) level and the critical stress (cr,i) level were determined. Each of these was to establish the compression stress effect of load on fiber-reinforced concrete. Three tests concrete whose maximum size of 16 mm was prepared namely, BZS, BZ1, and BZ3. They comprised aggregates from sand, Portland cement, water, superplasticizer, and gravel. They had a similar composition except for the amount of steel reinforcement deposited in them as indicated in the Table 23.

Tests concrete BZ1 and BZ3 were reinforced with a 1 mm by 50 mm steel fibers. The amount of steel for BZ1 was 1% while 13 had 3% of steel. Test concrete of BZS would serve as the "witness" concrete. Therefore, it was not reinforced with steel fiber. For the first two concrete tests, steel fibers were immersed during the last phases of blending. The final aggregate was kept for 28 days in a room temperature of 18˚C (±1˚C) with an average humidity of 95% (± 5%). After 28 days of storage, the samples were placed in a dry-air environment up to the final test.

Using an acoustic emission method, rectangular blocks of 50 mm length by 50 mm width by 100 mm height were extracted from larger test elements. They were then placed under compression stress, which was timed based on AE descriptors. Non-friction compression was done at the sample's interface. Polishing and lubrication of the samples' surface were done such that they were mutually parallel with 0.05 mm accuracy. The choice of acoustic compressors was the "Vallen-Systeme AMS3 acoustic emission measuring set and two VS 150-M sensors with a 100-450 kHz transmission band" (Błaszczyński and Przybylska-Fałek, 2015). The signal effective value RMS and events rate Nzd were the recorded descriptors when compression began.

[Insert Table 23]

Findings from acoustic emission tests of the registered AE events rate Nzd are as indicated in the Table 24 and Figs. 9 - 11. Both critical stresses cr and cracking initiating stresses were measured. Values-based on concretes BZS, BZ1 and BZ3 are as shown in the Table 25. Similarly, the levels of deformation after critical (cr,i) and cracking initiation stresses (i) are as shown in the Table 26.

[Insert Fig. 9]

[Insert Fig. 10]

[Insert Fig. 11]

[Insert Table 24]

[Insert Table 25]

[Insert Table 26]

Fig. 12 indicates that along when the amount of steel fiber reinforcement increases, the optimal stress attain by concrete increases as well. Besides, increased steel reinforcement reduces the deformation effect that arises from destruction.

[Insert Fig. 12]

BZS, which was the witness concrete, did not have any steel fiber reinforcement (0%). It had an optimum stress of 37.52 MPa. On the other hand, concrete BZ1 with 0.5% of steel reinforcement had 37.62 MPa stress. Concrete BZ3 with 3% of steel reinforcement had 41.99 MPa. As more steel was dosed into the mixture, there was more resistance to destruction. This is because more areas under the curve increased thus more energy required to tear it down. The cr stresses for BZ1 and BZ3 were more than the BZS’s stress. The experiments also showed that BZ1 and BZ3 aggregates had respective 0, 80 c/fc and 0.81c/fc, which is a higher than BZS (Witness) 0.78c/fc.

Steel reinforced fiber prevents the propagation of micro-cracks thus limiting the effect of destruction stress along lines of the defect (Khan et al., 2017). According to The Masterbuilder’s report (The Masterbuilder, 2016), fiber eventually bolsters the bonding of the cement matrix reducing the effect of destruction. Thus, steel fiber makes concrete stronger and ductile. Additionally, Canzac (2019) discusses that steel-reinforced concrete eases the speed of construction cutting related expenses and saving time. It also simplifies the construction process considering that such concrete has simpler joints that are less prone to fabric positioning (Fiberecon, 2019). Moreover, steel fiber increases flexural strength such that thinner slabs can be used in place of larger and space-consuming bars.

- 7.1 Recycling aggregates in concrete

The CDW (Construction and Demolition Waste) came into existence after the reproduction of other materials such as metals. Various factor influenced this process, including the economy and availability of natural materials (Vázquez, 2016; Taffese, 2018; Ben Nakhi and Alhumoud, 2019). The research suggests that after the Second World War, CDW aggregates were used in concretes of low quality. Currently, predominant volumes of CDW contain mixed compositions of sand, concrete elements and masonry. Ceramic aggregates are being used in new concrete because of their elastic module and compressive strength when compared to those obtained from natural materials (Lynch, 2017; Khalil, 2018). With the vital change in the structure, higher porosity influences the physical property of durability of concrete (Khalil, 2018). This research agrees with the findings given by the author. The adoption ceramic agreegates in concrete will improve the durability of concrete used in the construction industry.

- 7.2 Challenges

Whereas steel fibers can replace all reinforcement materials in all structural projects, nonetheless, eventually the design economies and alternative costs will decline. It also requires stringent management of wastes since as more is wasted, it means a lot of fiber is lost. While steel-reinforced concrete cannot float on a slab’s surface, those slabs exposed to adverse conditions such as rain may uncover both the fiber and concrete to poor aesthetic conditions.

The use of steel-reinforced fibers as substitutes for normal concrete has gained traction because of their overall longevity and compressive strength (Lee et al., 2017). Nonetheless, many contractors are objected to total substitution since this reinforcement is yet to address challenges related to exposure of carbonation and chloride.

- 8. Additive manufacturing (AM)

Also called 3-dimensional (3D) printing, additive manufacturing will probably revolutionize the future of concrete infrastructure technology (Thompson et al., 2016). AM has the advantage of reducing construction costs and time while also increasing the safety, productivity, and reliability of projects (Huang et al., 2015). With AM, engineers manufacture concrete through 3D objects. This recent development not only transforms how concrete projects are developed but also the material design and their composition or properties.

- 8.1 Background to AM’s technology

Advancements in technology have made this process easy and achievable. Automated construction allows large-scale production of concrete using AM technology. Among such advancements is the Contour Crafting initiated by the University of Southern California. D-Shape and Concrete Printing are the other two methods initiated by the respective Monolite UK Ltd and Loughborough University. Contour Crafting and Concrete Printing deal with the extraction of concrete-related elements using a nozzle. On the other hand, D-Shape Printing casts some powder (grain aggregates) that selectively blend with cementations ink. Each of these approaches works with both concrete and mortar. Presently, AM manufacturing attracts engineers because it allows for the production of concrete with intuitive designs and shapes with lucrative architectural components.

AM manufacturing is still limited to size. Therefore, it mostly takes a modular approach of smaller size aggregates, which can then be combined for large-scale applications. Irrespective of this, AM manufacturing is a proven technique for both small- to full-scale applications and proofs-of-concept. This technology now makes it easy for architects to print bridges, homes, artistic structures, and buildings. Examples of structures developed from 3D technology include first, a complete AM-based two-story house by a Chinese manufacturing firm. This structure was set up within 45 days on single-go and on-site. This house can withstand an 8.0 magnitude earthquake. Secondly, the 5 m concrete castles set up using this technology was build using 3 cm by 1 cm layers depth (Tarhan and Şahin, 2019). The United States entrepreneur was the one responsible for its construction. Thirdly, the latest 10.5 m by 12.5 m and 3.0 m height structure constructed from traditional elements. Using materials such as volcanic ash, this hotel structure was built under five days in the Philippines.

There is increasing momentum for the adoption of 3D printing by the European Space Agency (ESA) and NASA for space exploration structures. Whereas this technology is attractive and relevant for extraterrestrial and space exploration, transportation expenses are likely to limit its adoption. Transporting bulk aggregates from the earth into space-sites is an expensive process that might limit its effectiveness. Irrespective of these constraints, the European Space Agency has manufactured 1.5-ton aggregates from synthetic lunar soil. Accordingly, NASA has collaborated with its Additive Construction for Mobile Emplacement (ACME) agency to construct similar 3D Printing concretes for space. They used feedstock concrete aggregates with planetary simulants to manufacture curved and straight wall structures. By 2016, NASA, alongside Bradley University, Caterpillar, and Bechtel, declared an Additive Manufacturing retreat. The focus of this retreat was to encourage the development of sustainable concrete using 3D technology. This challenge was to spur people to use locally found traditional or recycled resource matter. Irrespective of this recent progress, 3D Printing is still in infant stages. It does not allow full-scale manufacture of cement. Applications for this technology are limited to small architectural structures and blended designs. They are used as minor extensions of the already present concrete technology.

- 8.2 Types of 3D printing

The different types of 3D printing include extrusion-based technique and powder-based technique as shown Table 27. Examples of extrusion-based techniques are Contour Crafting (CC), Concrete Printing, Contour Crafting, and Concrete Printing, large-scale 3DCP using UHCP. The study by Nematollah, Xia, and Sanjayan gives examples of powder-based techniques are Powder-based 3DCP using Geopolymer, D-shape technology, and Emerging Objects technology (Nematollahi et al., 2017). Whereas 3DCP is still in the development stage, there is a possibility that these techniques will significantly change the future of concrete production by facilitating the printing of large-scale concrete infrastructures as shown some of the categories of additive manufacturing in Table 28.

[Insert Table 27]

[Insert Table 28]

Based on the experiment by Marchment, constituents used for the production of 3D UHCP are as discussed below (Marchment, 2017). Two sand variants (washed sand, which is Type 1, and silica fine sand, which is Type II) were used as aggregates alongside an ordinary Portland cement (OPC). Type II sand comprised not more than 300 µm size of granules while Type I had not more than 500 µm granule size.

The process of blending sought to attain the prerequisites for an extrusion-based 3D printing process. Thus, the focus was on concrete’s buildability, workability, and extrudability. First, the researchers employed a baseline trial aggregate solution whose ration was based on conventional cement elements and a regular mixing process. They began by combining cement with Sand Type I at a rate of 1:3. They used 0.5. water to cement ratio for this matrix. After preparation, the matrix was placed into a 3D printing machine as shown in Figs. 13 and 14.

[Insert Fig. 13]

[Insert Fig. 14]

[Insert Fig. 15]

The researchers determined compressive strength using a universal testing machine with load regulation of 20 MPa/min. Aggregates were ground into tiny pieces of 50 mm length by 25 mm width by 60 mm height. They were inserted into the machine in two directions. The first was a parallel direction (for testing front) and second perpendicular direction (for testin top as shown in fig 16).

[Insert Fig. 16]

The researchers determined the flexural strength using a universal testing apparatus regulating displacement at 1 mm/min. The mixture was placed at 250 mm length by 25 mm width by 60 mm height. Each solution was measured using a 3-point. A suitable setup for this setup was a 150 mm rate. Testing was two-directional similar to compressive strength as shown in Fig. 17.

[Insert Fig. 17]

For Inter-layer bonding strength test, 250 mm length by 25 mm width by 30 mm height specimen dimension was chosen. A displacement interval of 1 mm/min was chosen. Figs. 18 - 20 are the results of compressive, Inter-layer bonding, and flexural strengths of the specimens after undergoing a 3D Printing process.

[Insert Fig. 18]

[Insert Fig. 19]

[Insert Fig. 20]

- 8.3 Opportunities for AM of cement-based materials

Globally, the pressure is towards attaining more sustainable and greener concrete solutions. Besides, many architects also demand attractive and high-end designs for their structures. Civil infrastructure is turning towards the use of concrete that has adaptability, longevity, resilience, high mechanical abilities, and constructability. The economy is another factor driving the construction industry. Nonetheless, existing traditional cement do not possess most of these characteristics, as some require high costs of repair over a short period. The current cement relies upon the precast and casting technologies, which do not have significant improvement. Therefore, 3D printing is one of the best options that engineers, designers, and architects can look forward to revolutionizing the construction industry.

With 3D, there is high adaptability and longevity of concrete. It avails a new opportunity for unique prospects and regulation of structural design, functionality, shape, composition, and embedment of elements. For example, it incorporates additives including nanomaterials, sensors, and fibers, which are indispensable for durable and flexible concrete options. Nano-materials are those cementitious components derived from nanotechnology. Nanomaterials are known to have high tensile strength, fire resistance, and self-cleaning capacities. When other elements are integrated into nanomaterials, they increase the cement durability, reduce the force of wear and tear, increase permeability, and make them lighter. These elements have a tremendous contribution to roofing and facade solutions. As the world moves towards environment conservation, nano-insulating materials provide the much-needed sustainability to the ecosystem. The amount of cement used in the construction industry will decrease significantly, thereby limiting the production of CO2. Nanomaterials are enevironmental friendly. It is anticipated that the adoption of these cleaner materials is essential in enhancing sustainable productions.

Such unprecedented characteristics have opened a new avenue for aggregate formations that were not attained before while also developing durable solutions that can bind with several elements and adjust to different shapes, forms, and materials. The potential that 3D technology has on the construction industry was recently discussed by the United States-Based National Science Foundation (NSF). This session comprised 30 professionals in a body they called Multiscale/3D Cement Printing. They all revealed that the adoption of Additive Manufacturing is likely to revolutionize the future of the concrete industry due to reduced costs, high resilience, durability, and improved mechanical properties of cement.

- 8.4 AM technology advantages

Other than allowing architects to model various shapes and designs from the printed concrete, it also closes the gap between conventional cement and masonry placement techniques. It abolishes the need for traditional formwork and molding processes. Therefore, designers and engineers have the freedom to construct structures without depending on formwork. For instance, formwork and molds account for respective 60 to 30 % of the expenses of the cement structure. Therefore, abolishing molds and formwork significantly reduces expenses of construction and delays, while increasing productivity and efficiency.

Conventional concrete and other improvisation methods may not provide high optimization of binders compared with 3D printing, which optimizes the cementation binder using non-Portland matter. It also makes use of mineral-based, non-hydraulic aggregates, or inorganic matter to optimize the cementitious binder. Improvisations that do not depend on the water have a high significance to space exploration structures. This is because imported water can be stored for other relevant projects. For instance, water from a traditional form, based on the planetary surface, can be more challenging to extract. Chances of eliminating carbon dioxide emission as well as to use aggregates that do not comprise waste mater or limestone-based residues will have remarkable ecological effects.

Since this technology has proved useful in the extraction and formulation of waste substances, it can contribute to environmental conservation and reduced costs of production. Aggregates from sulfur wastes, magnesium oxides, iron oxide-free Portland cement-polymer materials, have been extracted and tested for 3D printing. These substances have been particularly useful for proof-of-concept structures and architectural buildings. Additionally, Additive Manufacturing concrete with extraterrestrial use can be relevant for resupplying of materials in regions with many constraints. The recyclable feedstock matter can serve this purpose of resupplying, which eventually promotes mission logistics, reduces cases of mission failure, which will ultimately enhance planetary explorations. Additive Manufacturing also integrates more functionality into the existing building or project by adding holes or spaces post-printing insertion activities. That is, it allows conduits for electrification purposes, plumbing, and other reinforcement such as tendon tensioning.

From the microstructural basis, 3D printing allows for localized management of the chemistry and micro-scale architectures. It also facilitates the integration of different types of co-printed reinforcements. The approach is relevant because it allows the incorporation of technologies into the microstructure of concrete that is not achievable using conventional extrusion or casting tactics. For instance, the nanoparticle method would not achieve such a feat. Additive Manufacturing blends both the fabrication and design processes. It starts with a 3-dimensional design digital design that imagines a structure that would incorporate all of the artistic, structural, and functional structure captured. This process concludes with a mere sliding of a button using the quick fabrication and constructing of the real project from the printer. This process is automated and remotely controlled. It has high significance for space operations that require less labor and time. This method was envisioned for planetary use considering that it will depend on robotic actions to set up structures in the space. For instance, NASA already initiated the AM construction project in 2014 in the Zero-G mission. This global agency exhibited the prowess of up linking a file to a three-dimensional printer into the International Space Station. It autonomously controlled this construction process with minimal aid of crews.

Engineers and architects will most probably construct multi-material structures with varying properties and functional characteristics using Additive Manufacturing capabilities. Examples of such structures may include those with self-healing and energy harvesting capabilities, as well as those that withstand seismic waves and with ability to sense, and bear heavyweights. Achieving these construction projects will be cost-effective and less time-consuming. Furthermore, 3D contributes towards sustainability as more and more companies seek to make good use of the ecosystem. The extraction of raw materials will decline as well as construction wastes due to improvised cement production techniques.

- 8.5 AM technology challenges

Whereas the benefits that 3D brings to concrete-based aggregates and its structures are ostensibly many, there are several drawbacks associated with large –scale industrial application of this technology. Additive technology is not yet embraced in many learning institutes yet it draws on several traditional disciplines. This challenge might hinder effective integration and transmission of knowledge into creative and desirable projects (Go and Hart, 2016; Pinkerton, 2016). AM proves futile in the setting up of large to mega-scale structures such as sophisticated houses and buildings, dams, bridges, and road networks. Those who pioneer AM technologies do so for few-metered buildings. Besides, these aggregates are in the form of assembled prefabrications. There is no on-site printing for a layer-by-layer complete infrastructure. Therefore, AM must address each of these reliability, sustainability, scalability, and commercialization challenges to increase adoption.

Moreover, layer thickness or the resolution of the powder deposition-based aggregates are relatively low. There is a need for blocks with large structures and sizes that do not require assemblage. This is because when the size remains low, it might interfere with the shape, productivity, and strength of these concrete during construction and blending. For instance, the admixture process involves various mechanics as more fibers and additives are integrated into the concrete, which might wear down the shape and strength of the residual cement. The blending process requires an understanding of the printed component scale, rate of deposition, bonding process, and structural layering.

Regardless of the recent progress in Additive Manufacturing, a major bottleneck is printing material itself. Due to the complexity and flexibility of concrete-related matter, aggregates can hardly adapt to 3D printing. Therefore, aggregates for 3D-based construction must have reliable thixotropy. Thixotropy is where concrete materials must be flexible, be hydrated, and allow for easy extrusion following deposition. They should allow for maximum flow and workability for easy insertion into layers. Additionally, their shape should be stable enough even after these processes. The concrete ink must demonstrate high resistance to adhesion and such a printing ink should set as quickly as possible. However, it is hard to achieve this process unless with the help of binders that can serve as reinforcement.

Concrete improvised through Additive Manufacturing has issues of longevity, bonding, and deposition of successive layers. Among other things, ecological effects adversely affect the adoption of this method of improvisation. Additionally, the development of appropriate 3D printing software is another drawback that hinders its adoption. It is not easy to come up with software that can allow the seamless blending of the architectural and hierarchical components of concrete. Moreover, capturing and conveying such information to printers is more difficult. The existing AM software can only generate the 3D geometry but fails to capture or relay sophisticated and relevant structural information from a hierarchical basis. Thus, more is expected in this field, especially in developing software that can extend the 3D model that can capture intricate details and relay them across a hierarchical basis including the integrated sensors, binders, and other components.

- 8.6 AM potential transformative impact

Concrete is the widely used building resource, so improvisation on its application and performance receives a wide appeal from the construction industry, which will also influence the world’s economy. Adoption of additive manufacturing technology is mired with debates as some suggest it is disruptive to the economy and the construction world. Others state that full adoption will take long periods before it becomes accepted. Whereas predicting the exact effects of additive manufacturing on cement and concrete, however, it avails new opportunities for the construction world. This technology is poised to transform how engineers, designers, and architects will use cement. Researchers and engineers have an opportunity to develop concrete that constitutes paradigm-shifting characteristics, attaining feat not previously achieved current materials (Paoletti and Ceccon, 2018; Yin et al., 2018; Chavanic, 2019). Therefore, it will avail more application opportunities in areas previously regarded as uncompetitive.

Forecasts on potential impacts often mentioned include:

- Improving efficiency and safety of the construction industry3D technology will reduce the duration used for mold building, inspection, and rebar placement. Construction will become cheaper, easier, and faster. AM will significantly enhance efficiency, promote adaptability, and encourage reliability of labor flow, alongside the transformation of project planning (Biernacki et al., 2017; Asprone et al., 2018; Howell, 2019). Since AM encourages automated construction, labor demographics will be transformed towards technology-based production, which will limit cases of injuries and deaths emerging from construction sites. For instance, more than 900 deaths occurred from construction sites in the United States in 2014. Construction is the field with the highest rate of death compared with other fields, thus, automating the process is desirable.

- A more durable and resilient infrastructureResource exhaustion and deterioration of cement-based aggregates is a leading challenge facing the construction world. Different countries, states, and local agencies have to spend significant sums on repairing, protecting, and reinforcing cement structures. Globally, $552 billion is spent on concrete repairs. The United States alone has to use over $20 billion yearly for these repairs while the £40 billion (Bureau of Reclamation, 2015; Energyskeptic, 2016). 3D technology comes with new opportunities as it enhances the longevity and performance of concrete. It transforms the resilience of concrete-based matter by eliminating human error, injuries, and promoting reproducibility. AM contributes to flaw tolerant and high-performance concrete-based aggregates more than the conventional cement. Therefore, it bypasses the limitations of resilience, durability, and performance of infrastructures.

- Transforming cities and homesArchitects and designers have an opportunity to utilize AM to specify and construct intuitive and sophisticated geometric structures. They can take advantage of the concrete’s suitability, aesthetics, and functionality to promote low-cost housing solutions and modern structures, which conventional cement could not achieve (3D Printing, 2019; Jose, 2019; Tilton and Holdowsky, 2019). This technology makes it possible to construct resilient large-scale structures for natural disaster-stricken regions.

- Environmental impactthe landfills comprising construction wastes threaten environment safety. These wastes also attract high financial costs for deposition as well as renovation. Therefore, AM technology eliminates most of these wastages through the precise management of aggregate resources and limitations in material usage.

- 9. Conclusion

The incorporation of smart concrete, for instance nano materials can improve the tensile, compressive, and flexural strengths. Studies have prioritized theconsideration of nanomaterials such as nano-titania, nano-silica, CNT, and GO. The addition of these materials to concrete has led to the coming up with concrete that has denser microstructures, thereby decreasing the rate of water absorption. The working ability of concrete can be improved through the addition of these materials. Nano-TiO2 is a modified concrete that has self-cleaning properties and other benefits that can help to keep the environment clean. Similarly, it has the ability to allow for the photocatalytic degredation of pollutants produced. Cement-based composites reinforced by CNTs have self-sensing abilities for detection of health hazards or damages. Additionally, GO and grapheme can be added to cement-based materials to improve durability and mechanical strengths. The study has demonstrated that cement-based composites can produce high amount of CO2 gas into the atmosphere. To address this problem, the solution is the addition of nanomaterials to these composites, thereby providing structural components that have great durability and mechanical strength. The replacement frequency as well as maintenance requirements of cement-based structures can be decreased subsequently. Such benefits can as well contribute to the reduction in the amount of cement used in the construction industry, an ideal case for curbing CO2 emissions caused by cement fabrication processes. Most of the recent advances in concrete improvisation examine mechanical and chemical properties to attain smart concretes and structures. Self-healing, self-curing, and self-sensing are some of the properties of smart materials that improve durability, strength, and performance of cementitious materials. Concrete smartness can be attained through special processing, change of the microstructure, integration of admixtures and functional components, and composition design. Such properties contribute to improved reliability, longevity, serviceability, and safety of the infrastructures while also cutting the life-cycle expenses.

Many scientists acknowledge that concrete has to be engineered at the nanoscale. This is because such an improvisation allows for the changing of the mechanical and chemical composition of concrete. Concrete materials have to demonstrate improved longevity and mechanical performance as well as to integrate properties that satisfy multiple applications to match with future emerging structural projects. Thus, the nanoscale improvisation deals with the integration of nanomaterials that subsist in crystalline and chemical composition as well as in electron movement forms. For this reason, this study regards graphene reinforcement and additive manufacturing as some of the best recent advancements in concrete production.

- Acknowledgements

This paper is part of a project supported by funding from the European Union’s Horizon 2020 Research and Innovation Programme under grant agreement no. 777823.

- References

3D Printing, 2019. What is 3D Printing? How Does a 3D Printer Work? Learn 3D Printing. 3D Printing. https://3dprinting.com/what-is-3d-printing/ (Accessed on Nov 1st, 2019)

Abbas, S., Nehdi, M. L., Saleem, M. A., 2016. Ultra-high performance concrete: Mechanical performance, durability, sustainability, and implementation challenges. IJCSM. 10 (3), 271.

Ackermann, K.C., 2018. Self-sensing concrete for structural health monitoring of smart infrastructures. University of Rhodes Island. https://digitalcommons.uri.edu/cgi/viewcontent.cgi?article=2268&context=theses (Accessed on Nov 1st, 2019)

Aditazz. Transforming engineering and construction by applying design-automation principles from the semiconductor Industry. Geneva: World Economic Forum, n.d. https://futureofconstruction.org/case/aditazz/download/ (Accessed on Nov 1st, 2019)

Adu-Amankwah, S. (2016). Relationship between Microstructure, Durability and Performance of CEM X Composite Cements (Doctoral dissertation, University of Leeds).

Afifi, M., 2016. Internal curing of high-performance concrete using lightweight and recycled aggregates.” https://pdfs.semanticscholar.org/8cef/2d3662b548bbf57772611f5f927834525f1c.pdf (Accessed on Nov 1st, 2019)

Ahmed, W., Baloch, W. L., & Khushnood, R. A. 2020. Fire performance of concrete containing nano-fibers and graphite nano-particles. In Smart Nanoconcretes and Cement-Based Materials (pp. 297-311). Elsevier.

Alrekabi, S., Cundy, A. B., Lampropoulos, A., Whitby, R. L. D., & Savina, I. 2017. Mechanical performance of novel cement-based composites prepared with nano-fibres, and hybrid nano-and micro-fibres. Composite Structures, 178, 145-156.

Alrekabi, S., Cundy, A. B., Lampropoulos, A., Whitby, R. L., Savina, I., 2017.  Mechanical performance of novel cement-based composites prepared with nano-fibers, and hybrid nano-and micro-fibers. Compos. Struct. 178, 145-156.

Al-Tabbaa, A., 2016. The concrete that heals its own cracks. World Economic Forum. https://www.weforum.org/agenda/2016/01/the-concrete-that-heals-its-own-cracks/. (Accessed on Nov 1st, 2019)

Ambily, P., Rajamane, N., 2019. Self-curing concrete an introduction. Home. https://www.nbmcw.com/tech-articles/concrete/563-self-curing-concrete-an-introduction.html. (Accessed on Nov 1st, 2019)

Andrew, R. M., 2018. Global CO2 emissions from cement production. Earth System Science Data. 10 (1), 195.

Asprone, D., Auricchio, F., Menna, C., Mercuri, V., 2018. 3D printing of reinforced concrete elements: Technology and design approach. Constr. Build. Mater. 165, 218-31.

Association of Equipment Manufacturers, 2018. New concrete developments for smart, sustainable building. Conexpoconagg, Association of Equipment Manufacturers. www.conexpoconagg.com/news/new-concrete-developments-for-smart-sustainable-bu (Accessed on Nov 1st, 2019)

Augustyniak, A., Sikora, P., Cendrowski, K., Nawrotek, P., Mijowska, E., Stephan, D., 2018. Challenges in studying the incorporation of nanomaterials to building materials on microbiological models. International Conference on Nanotechnology and Nanomaterials. 285-303.

Azarsa, P., Gupta, R., 2017. Electrical resistivity of concrete for durability evaluation: a review. Adv. Mater. Sci. Eng. 2017.

Azmee, N. M., Shafiq, N., 2019. Preparation of low cement ultra-high performance concrete. Lecture Notes in Civil Engineering, 54, 331-336.

Bai, S., Jiang, L., Xu, N., Jin, M., & Jiang, S. 2018. Enhancement of mechanical and electrical properties of graphene/cement composite due to improved dispersion of graphene by addition of silica fume. Construction and Building Materials, 164, 433-441.

Baoguo, H., Yunyang, W., Dong, S., Liqing, Z., Siqi, D., Xun, Y., & Jinping, O.2015, July. Smart concretes and structures: A review. Journal of Intelligent Material Systems and Structures. Vol. 26 (11): 1303-1345.

Barrios, E., Fox, D., Li Sip,Y., Catarata, R., Calderon, J. E., Azim, N., Afrin, S., Zhang, Z., Zhai, L., 2019. Nanomaterials in advanced, high-performance aerogel composites: A review. Polymers. 11 (4), 726.

Bautista-Gutierrez, K. P., Herrera-May, A. L., Santamaría-López, J. M., Honorato-Moreno, A., Zamora-Castro, S. A., 2019. Recent progress in nanomaterials for modern concrete infrastructure: Advantages and challenges. Materials. 12 (21), 3548.

Beglarigale, A., Seki, Y., Demir, N.Y., Yazıcı, H., 2018. Sodium silicate/polyurethane microcapsules used for self-healing in cementitious materials: Monomer optimization, characterization, and fracture behavior. Constr. Build. Mater. 162, 57-64.

Ben Nakhi, A., Alhumoud, J. M., 2019. Effects of recycled aggregate on concrete mix and exposure to chloride. Adv. Mater. Sci. Eng. 2019.

Berkeley Lab, 2016. Graphene is strong, but is it tough? News Center. Last modified. https://newscenter.lbl.gov/2016/02/08/graphene-is-strong-but-is-it-tough/ (Accessed on Nov 1st, 2019)

Berry, M., Snidarich, R., Wood, C., 2017. Development of non-proprietary ultra-high performance concrete. Montana Department of Transportation. Research Programs.  https://pdfs.semanticscholar.org/8647/7d4f30825fc85a144360cd3e425077aa9a80.pdf (Accessed on Nov 1st, 2019)

Bhatnagar, A., Wagh, S., Singh, B., Agarwal, R., Khan, F., 2016. Smart materials–A review. Annals of Dental Specialty. 4 (1), 10.

Biernacki, J. J., Bullard, J. W., Sant, G., Brown, K., Glasser, F. P., Jones, S., ... & Sanchez, F. (2017). Cements in the 21st century: challenges, perspectives, and opportunities. Journal of the American Ceramic Society, 100(7), 2746-2773.

Biernacki, J. J., Bullard, J. W., Sant, G., Brown, K., Glasser, F.P., Jones, S., Ley, T., Livingston, R., Nicoleau, L., Olek, J., Sanchez,  F., 2017. Cements in the 21st century: challenges, perspectives, and opportunities. J. Am. Ceram. Soc. 100 (7), 2746-2773.

Błaszczyński, T., Przybylska-Fałek, M., 2015. Steel fiber reinforced concrete as a structural material. Procedia Eng. 122, 282-9.

Bonnet, C., Carcanague, S., Hache, E., Jabberi, A., Gondia Sokhna, S. E. C. K., Simoën, M., 2019a. The impact of future generation on cement demand: An assessment based on climate scenarios.

Bonnet, C., Hache, E., Jabberi, A., Seck, G. S., Simoen, M., Carcanague, S., 2019b. The impact of future generation on cement demand: An assessment based on climate scenarios.

Broad Sustainable Building, 2016. Broad sustainable building. Future of Construction. Last modified December 5, 2016. https://futureofconstruction.org/case/broad-sustainable-building/ (Accessed on Nov 1st, 2019)

Building Ventures, 2018. May 2018. Building Ventures. https://www.buildingventures.com/whitepaper/may-2018.html.(Accessed on Nov 1st, 2019)

Bureau of Reclamation, 2015. Guide to energy repair. Bureau of Reclamation. https://www.usbr.gov/tsc/techreferences/mands/mands-pdfs/Guide2ConcreteRepair2015_Final.pdf. (Accessed on Nov 1st, 2019)

Canzac, 2019. Fibre reinforced concrete - What you need to know before you buy » Canzac. Home » Canzac. http://www.canzac.com/knowledge-centre/steel-fibres-advantages-and-disadvantages/ (Accessed on Nov 1st, 2019)

Cao, M., Ming, X., He, K., Li, L., Shen, S., 2019. Effect of macro-, micro-and nano-calcium carbonate on properties of cementitious composites—A review. Materials, 12 (5), 781.

Chalioris, C. E., Kosmidou, P. M., Karayannis, C., 2019. Cyclic response of steel fiber reinforced concrete slender beams; an experimental study. Mater. 12 (9), 1398.

Chavanic, S., 2019. Research team receives grant to commercialize 3D-printed concrete system. Penn State University. https://news.psu.edu/story/583678/2019/08/13/research/research-team-receives-grant-commercialize-3d-printed-concrete (Accessed on Nov 1st, 2019)

Chuah, S., Pan, Z., Sanjayan, J. G., Wang, C. M., & Duan, W. H. 2014. Nano reinforced cement and concrete composites and new perspective from graphene oxide. Construction and Building Materials, 73, 113-124.

City University, 2019. Tsing ma bridge. City University of Hong Kong. http://www.cityu.edu.hk/CIVCAL/book/bridge.html (Accessed on Nov 1st, 2019)

Cordon, H. C. F., Tadini, F. B., Akiyama, G. A., de Andrade, V. O., da Silva, R. C., 2020. Development of electrically conductive concrete. Cerâmica, 66 (377), 88-92.

D’Alessandro A., Ubertini F., Laflamme S., & Annibale, L.M. 2015. Towards smart concrete for smart cities: Recent results and future application of strain-sensing nanocomposites. Journal of Smart Cities, vol.1(1): 3–14.

Devgire, M., 2019. An experimental study of self-healing concrete by adding pseudomonas fluorescent bacteria.  IJAST, 6, 421-424.

Díaz-Soler, B., López-Alonso, M., Martínez-Aires, M. D., 2019. Nano-enabled products applied on construction sector. New risks for workers. International Congress on Engineering and Sustainability in the XXI Century. 1000-1007.

Dimov, D., Amit, I., Gorrie, O., Barnes, M. D., N. Townsend, J., Neves, A. I., Withers, Russo F.S., Craciun, M., 2018. Ultrahigh performance nanoengineered graphene–concrete composites for multifunctional applications. Adv. Funct. Mater. 28 (23), 1705183. https://ore.exeter.ac.uk/repository/bitstream/handle/10871/32568 (Accessed on Nov 1st, 2019)

Duarte, V. R., 2016. Additive manufacturing of high resistance steel by MIG/MAG. Ph.D. Diss. https://pdfs.semanticscholar.org/03d4/ eb63049e8bb44180f46d19eeec66f480ba67.pdf (Accessed on Nov 1st, 2019)

Electronic Design, 2019. 3D-Printed smart bridge leads MX3D to the construction industry's future. Electronic Design. https://www.electronicdesign.com/industrial-automation/3d-printed-smart-bridge-leads-mx3d-construction-industry-s-future. (Accessed on Nov 1st, 2019)

Energyskeptic, 2016. Corrosion Eats $552 Billion Infrastructure a Year (6% of GDP). Peak Energy & Resources, Climate Change, and the Preservation of Knowledge. http://energyskeptic.com/2016/corrosion-eats-552-billion-infrastructure-per-year-6-pct-of-gdp-billion-cost-per-year-6-of-gdp/ (Accessed on Nov 1st, 2019)

Erdenebat, T., Otgonlham, J., Oyunzul, E., Sanjaasuren, R., 2017. Recent and future of cement and concrete industries-a root of our development. Mongolian J. Chem. 12, 123-125.

Expotrade, 2016. UPDATED: How the Burj Khalifa Was built (including Design, Foundations, Cladding and Urban Myths). Skyscrapers Summit Dubai - UAE | 23-24 April 2018 | High Rise Buildings Conference. https://www.smartskyscrapers.com/news-detail:2caf9ede-8d6f-1890-eab8-597ed0c74529.html (Accessed on Nov 1st, 2019)

Feiteira, J., Gruyaert, E., De Belie, N., 2016. Self-healing of moving cracks in concrete by means of encapsulated polymer precursors. Constr. Build. Mater. 102, 671-8.

Feiteira, J., Tsangouri, E., Gruyaert, E., Lors, C., Louis, G., De Belie, N., 2017. Monitoring crack movement in polymer-based self-healing concrete through digital image correlation, acoustic emission analysis, and SEM in-situ loading. Mater. Design. 115, 238-246.

Ferrara, L., 2018. Self-healing cement-based materials: An asset for the sustainable construction industry. Mater. Sci. Eng. 442 (1), 012007.

Ferrara, L., Van Mullem, T., Alonso, M.C., Antonaci, P., Borg, R.P., Cuenca, E., Jefferson, A., Ng, P.L., Peled A., Roig-Flores, M., Sanchez, M., 2018. Experimental characterization of the self-healing capacity of cement-based materials and its effects on the material performance: a state of the art report by COST Action SARCOS WG2. Constr. Build. Mater. 167, 115-42.

Fiberecon, 2019. Slabs. Fibercon – Solutions That Work for Our Customers. http://fibercon.com.au/products/slabs/ (Accessed on Nov 1st, 2019)

Ghafari, E., Arezoumandi, M., Costa, H., Julio, E., 2015. Influence of nano-silica addition on the durability of UHPC. Constr. Build. Mater. 94, 181-8.

Ghosal, M., 2019. Mitigating the unknown-risks in construction and demolition (I). Safety and Security In Planning, Design and Construction. https://www.academia.edu/40705631/Mitigating_The_Unknown_-_Risks_In_Construction_and_Demolition_I_(Accessed on Nov 1st, 2019)

Gibb, A., Jones, W., Goodier, C., Bust, P., Song, M., Jin, J., 2018. Nanotechnology in construction and demolition: What we know, what we don’t. Constr. Res. Innov. 9 (2), 55-8.

Go, J., Hart, A. J., 2016. A framework for teaching the fundamentals of additive manufacturing and enabling rapid innovation. Addit. Manu. 10, 76-87.

Golewski, G., 2017. Generalized fracture toughness and compressive strength of sustainable concrete including low calcium fly ash. Mater. 10(12), 1393.

Gong, K., Pan, Z., Korayem, A. H., Qiu, L., Li, D., Collins, F., ... & Duan, W. H. 2015. Reinforcing effects of graphene oxide on portland cement paste. Journal of Materials in Civil Engineering, 27(2), A4014010.

Gopala, K. V., Putturu, M. K., 2018. Self-curing concrete with different self-curing agents. Mater. Sci. Eng. 330, 012120.

Gupta, V., 2018. Smart materials in dentistry: A review. Int. J. Adv. Res. Dev. 3, 89-96.

Han, B., Wang, Y., Dong, S., Zhang, L., Ding, S., Yu, X., Ou, J., 2015. Smart concretes and structures a review. J. Intel. Mater. Syst. Struct. 26(11), 1303-45.

Han, B., Zhang, L., & Ou, J. (2017). Smart and multifunctional concrete toward sustainable infrastructures (pp. 369-377). Singapore:: Springer.

Harvey, F. 2018. Cement Industry Urged to Reduce ‘Invisible’Global Emissions. The Guardian.

Heggade, V., Bhandary, S., Naik, R., Damda, A., 2016. Intelligent material: The essence of smart materials. Int. J. Appl. Dent. Sci. 2, 7-10.

Hoang, K. H, Hadl, P., Nguyen, V.T., 2016. A new mix design method for UHPC based on stepwise optimization of particle packing density. First International Interactive Symposium on UHPC 2016. https://www.extension.iastate.edu/registration/events/UHPCPapers/UHPC_ID66.pdf (Accessed on Nov 1st, 2019)

Howell, H. A., 2019. 3D-printed precast concrete molds for redeveloped NYC landmark a first. Construction Dive. https://www.constructiondive.com/news/3d-printed-precast-concrete-molds-for-redeveloped-nyc-landmark-a-first/551903 (Accessed on Nov 1st, 2019)

Huang, Y., Leu, M. C., Mazumder, J., Donmez, A., 2015. Additive manufacturing: Current state, future potential, gaps and needs, and recommendations. J. Manuf. Sci. 137 (1), 014001.

Jain, P., Kaul, R., Saha, S., Sarkar, S., 2017. Smart materials-making pediatric dentistry bio-smart. Int. J. Pedod. Reh. 2(2), 55.

Jeevanandam, J., Barhoum, A., Chan, Y. S., Dufresne, A., Danquah, M. K., 2018.  Review of nanoparticles and nanostructured materials: history, sources, toxicity, and regulations. Beilstein J. Nanotech. 9 (1), 1050-1074.

Jo, B. W., Sikandar, M. A., Chakraborty, S., Baloch, Z., 2017. Strength and durability assessment of Portland cement mortars formulated from hydrogen-rich water. Adv. Mater. Sci. Eng. 2017.

Jose, T. F., 2019. Layered Architecture: What is Additive Manufacturing? Arch Daily. https://www.archdaily.com/926587/layered-architecture-what-is-additive-manufacturing (Accessed on Nov 1st, 2019)

Justs, J., Wyrzykowski, M., Bajare, D., Lura, P., 2015. Internal curing by superabsorbent polymers in ultra-high performance concrete. Cem. Concr. Res. 76, 82-90.

Khalil, A. L., Hassan, M., Hamzah, A. K., Zaidi, K., ALI, A., 2018. Study the recycling and use of construction waste in concrete mixtures in yemen.

Khalil, E., Abd-Elmohsen, M., & Anwar, A. M. 2015. Impact resistance of rubberized self-compacting concrete. Water Science, 29(1), 45-53.

Khan, M. I., Abbas, Y. M., Fares, G., 2017. Review of high and ultrahigh performance cementitious composites incorporating various combinations of fibers and ultrafine. JKSUES. 29 (4), 339-47.

Kharisov, B. I., Kharissova, O. V., & Dimas, A. V. (2016). The dispersion, solubilization and stabilization in “solution” of single-walled carbon nanotubes. RSC advances, 6(73), 68760-68787.

Krzywon, R., Gorski, M., Dawczynski, S., Szojda, L., Castro Gomes, J., & Salvado, R. (2016). Self-monitoring strengthening system based on carbon fiber laminate. Journal of Sensors, 2016.

Kusumawardaningsih, Y., Fehling, E., Ismail, M., Aboubakr, A.A., 2015. Tensile strength behavior of UHPC and UHPFRC. Procedia Eng. 125, 1081-6.

Lakshmi, K. A., Rao, G., Arthiseethalakshmi, S., Padmapriya, M., 2017. Smart materials-astute aspects of dentistry-A review. RGUHS J. Med. Sci. 7 (2), 68-70.

Lansard, M., 2019. List of 3D Printing technologies - Guide on All 3D Printing technologies. Aniwaa. https://www.aniwaa.com/3d-printing-technologies/ (Accessed on Nov 1st, 2019)

Lee, S. K., Jeon, M. J., Cha, S. S., Park, G. G., 2017. Mechanical and permeability characteristics of latex-modified fiber-reinforced roller-compacted rapid-hardening-cement concrete for pavement repair. Appl. Sci. 7 (7), 694

Li, V. C., 2019. High-Performance and Multifunctional Cement-Based Composite Material. Eng. 5 (2), 250-60.

Liang, K., Zeng, X., Zhou, X., Qu, F., Wang, P., 2017. A new model for the electrical conductivity of cement-based material by considering pore size distribution. Mag. Concr. Res. 69 (20), 1067-1078.

Lim, J. L., Raman, S. N., Lai, F. C., Zain, M. F., Hamid, R., 2018. Synthesis of nano cementitious additives from agricultural wastes for the production of sustainable concrete. J. Clean. Prod. 171, 1150-60.

Lynch, C. M., 2017. Recyclable Waste Material as Substitute Aggregate in Concrete.

Marchment, T., Xia, M., Dodd, E., Sanjayan, J., Nematollahi, B., 2017. Effect of delay time on the mechanical properties of extrusion-based 3D printed concrete. In Proceedings of the International Symposium on Automation and Robotics in Construction, Taipei, Taiwan. 28.

Marcos-Meson, V., Michel, A., Solgaard, A., Edvardsen, F.G., Skovhus, T. L., 2018. The corrosion resistance of steel fiber reinforced concrete-A literature review. Cem. Concr. Res. 103, 1-20.

Meng, W., 2017. Design and performance of cost-effective ultra-high performance concrete for prefabricated elements. Missouri Sci. Tech. (Accessed on Nov 1st, 2019)

Mishra, D. K., Yu, J., Das, A. K., & Leung, C. K. Y. (2018). A Review of Self-Sensing and Self-Healing ‘Smart’Cement Based Materials–Bridging the Gap between Research & Application.

Mishra, D. Yu J., Leung, C. K. Y., 2018. Self-sensing and self-healing ‘smart’cement-based materials–A review of the state of the art.  https://www.researchgate.net/publication/327362456_A_Review_of_Self-Sensing_and_Self-Healing_'Smart'_Cement_Based_Materials_-_Bridging_the_Gap_between_Research_Application (Accessed on Nov 1st, 2019)

Momin, R. R., Adil, M. R., Jamal, M., 2018. An experimental study on self-healing concrete using bacillus subtilis bacteria. Intl. J. Innov. Knowl. Conc. 6(2), 178-82.

Moser, R. D., Singh, P. M., Kahn, L. F., Kurtis, K., 2012. The chloride-induced corrosion resistance of high-strength stainless steels in simulated alkaline and carbonated concrete pore solutions. Corros. Sci., 57(2), 41-53.

Mostavi, E., Asadi, S., Hassan, M., Alansari, M., 2015. Evaluation of self-healing mechanisms in concrete with double-walled sodium silicate microcapsules. Mater. Civ. Eng. 27 (12), 04015035.

Mousa, M. I., Mahdy, M. G., Abdel-Reheem, H., Yehia, A., 2015. Self-curing concrete types; water retention and durability. Alex. Eng. J. 54(3), 565-75.

Nanotech, Real Estate, 2018. Revolutionary graphene-concrete could be an absolute game changer for construction - and the Planet. Richard Van Hooijdonk Blog. https://richardvanhooijdonk.com/blog/en/revolutionary-graphene-concrete-could-be-an-absolute-game-changer-for-construction-and-the-planet/ (Accessed on Nov 1st, 2019)

Nduka, D., Ameh, J., Joshua, O., Ojelabi, R., 2018. Awareness and benefits of self-curing concrete in construction projects: Builders and Civil Engineers Perceptions. Build. 8(8), 109.

Nematollahi, B., Xia, M., Sanjayan, J., 2017. Current progress of 3D concrete printing technologies. InISARC. Proceedings of the International Symposium on Automation and Robotics in Construction 2017 (Vol. 34). Vilnius Gediminas Technical University, Department of Construction Economics & Property.

Olawuyi, B. J., Boshoff, W. P., 2017. Influence of SAP content and curing age on air void distribution of high-performance concrete using 3D volume analysis. Constr. Build. Mater. 135, 580-9.

Oliari Garcez, E., Ikramul Kabir, M., MacLeod, A., Subhani, M., Ghabraie, K., 2019. Self-Compacting Concrete Reinforced with Twisted-Bundle Macro-Synthetic Fiber. Appl. Sci. 9 (12), 2543.

Özcan, F., Kaymak, H., 2018. Utilization of Metakaolin and Calcite: Working Reversely in Workability Aspect—As Mineral Admixture in Self-Compacting Concrete. Adv. Civ. Eng. 2018.

Palod, R., Deo, S. V., Ramtekkar, G. D., 2017. Review and Suggestions on use of Steel Slag in Concrete and its Potential use as Cementitious Component Combined with GGBS. Int. J. Civ. Eng. Technol. 8 (4), 1026-1035.

Paoletti, I., Ceccon, L., 2018. The Evolution of 3D Printing in AEC: From Experimental to Consolidated Techniques. 3D Printing. 39. (Accessed on Nov 1st, 2019)

Papanikolaou, I., Al-Tabbaa, A., Goisis, M., 2019. An industry survey on the use of graphene-reinforced concrete for self-sensing applications. In International Conference on Smart Infrastructure and Construction 2019 (ICSIC) Driving data-informed decision-making. ICE Publishing., 613-622.

Park, B., Choi, C., 2019. Prediction of Self-Healing Potential of Cementitious Materials Incorporating Crystalline Admixture by Isothermal Calorimetry. Int. J. Concr. Struct. 13 (1), 36.

Perez, G., Erkizia, E., Gaitero, J., Kaltzakorta, I., Guerrero, J. A., 2015. Synthesis and characterization of epoxy encapsulating silica microcapsules and amine-functionalized silica nanoparticles for development of an innovative self-healing concrete. Mater. Chem. Phys. 165, 39-48.

Pinkerton, A. J., 2016. Lasers in additive manufacturing. Optics & Laser Technology. 78, 25-32.

Poovizhiselvi, M., Karthik, D., 2017. Experimental Investigation of Self Curing Concrete. Int. Res. J. Eng. Tech. (IRJET). 4 (1), 2395-0056.

Prabahar, A., Dhanya, R., Ramasamy, N., Dhanasekar, 2017. An experimental study of self-healing of cracks in concrete using sodium silicate capsule. Rasayan J. Chem. 10 (102), 577-83. http://rasayanjournal.co.in/admin/php/upload/183_pdf.pdf (Accessed on Nov 1st, 2019)

Reddy, T. C., Ravitheja, A., 2019. Macro mechanical properties of self-healing concrete with crystalline admixture under different environments. Ain. Shams. Eng. J. 10(1), 23-32.

Rutigliano, S., 2019. Graphene-reinforced concrete, the future of sustainable cities? Materials Blog - Matmatch. https://matmatch.com/blog/graphene-reinforced-concrete-the-future-of-sustainable-cities/. (Accessed on Nov 1st, 2019)

Sadiku, M., Tembely, M., Musa, M., 2017. Smart materials: A Primer. Intl. J. 7(3).

Sbia, L.A., Peyvandi, A. Lu, A.J., Abideen, S., Weerasiri, R. R., Balachandra, A., Soroushian, M. P., 2017. Production methods for reliable construction of ultra-high-performance concrete (UHPC) structures. Mater. Struct. 50(1), 7.

Senthil, M. V., Balamurugan, B., Navaneetha, B., 2019. Experimental study on self-healing concrete by using bacteria (Escherichia coli). Int. J. Sci. Eng. Res. 10(3).

Severo, E. A., de Guimarães, J. C. F., Dorion, E. C. H., Nodari, C. H., 2015. Cleaner production, environmental sustainability and organizational performance: an empirical study in the Brazilian Metal-Mechanic industry. J. Cleaner Produc. 96, 118-125.

Sidodikromo, E. P., Chen, Z., Habib, M., 2019. Review of the Cement-Based Composite Ultra-High-Performance Concrete (UHPC). The Open Civ. Eng. J. 13(1).

Sivakumar, P., Naseem, I., 2016. Biosmart materials the future of dentistry: A review. Res. J. Pharm. Technol. 9 (10), 1737.

Smart Materials and Structure, 2019. Smart Materials and Structures. Smart Materials and Structure. https://smartmaterialscongress.euroscicon.com/call-for-abstracts. (Accessed on Nov 1st, 2019)

Snoeck, D., Van den Heede, P., Van Mullem, T., De Belie, N., 2018. Water penetration through cracks in self-healing cementitious materials with superabsorbent polymers studied by neutron radiography. Cem. Concr. Res. 113, 86-98.

Sofi, A. A., Iqbal, S. M., Mir, S. A., Wani, M. V., Masoodi, E. A., 2016. Electrically Conductive Concrete Formed By Using Waste Coke Proving Beneficial For Grounding.

Soliman, N. A., Tagnit-Hamou, A., 2018. Using particle packing and statistical approach to optimize eco-efficient ultra-high-performance concrete. ACI Mater. J. 115(5), 795-7.

Taffese, W. Z., 2018. Suitability investigation of recycled concrete aggregates for concrete production: an experimental case study. Adv. Civ. Eng. 2018.

Tarhan, Y., Şahin, R., 2019. Developments of 3d Concrete Printing Process. J. Int. Civ. Eng. Arch. 7(23).

The Masterbuilder, 2016. SFRC As a structural material. The Masterbuilder. https://www.masterbuilder.co.in/sfrc-structural-material/. (Accessed on Nov 1st, 2019)

Thompson, M. K., Moroni, G., Vaneker, T., Fadel, G., Campbell, R.I., Gibson, I., Bernard, A., Schulz, J., Graf, P., Martina, A.B., 2016. Design for Additive Manufacturing: Trends, opportunities, considerations, and constraints. CIRP. Annals. 65(2), 737-60.

Tilton, B., Holdowsky, J., 2019. 3D Opportunity for standards. Deloitte Insights. https://www2.deloitte.com/us/en/insights/focus/3d-opportunity/additive-manufacturing-standards-for-3d-printed-products.html. (Accessed on Nov 1st, 2019)

Udhanyan, R., Rajamane, N. P., 2017. Experimental study of self-compacting self-curing concrete. Int. J. Civ. Eng. Technol. 8, 638-643.

Van Belleghem, B., Montoya, R., Dewanckele, J., Van den Steen, N., De Graeve, I., Deconinck, J., Cnudde, V., Tittelboom, V., De Belie, K., 2016. Capillary water absorption in cracked and uncracked mortar–A comparison between experimental study and finite element analysis. Constr. Build. Mater. 110, 154-62.

Van den Heede, P., Van Belleghem, B., Alderete, N., Van Tittelboom, K., De Belie, N., 2016. Neutron radiography based visualization and profiling of water uptake in (un) cracked and autonomously healed cementitious materials. Mater. 9 (5), 311.

Van Tittelboom, K., Tsangouri, E., Van Hemelrijck, D., De Belie, N., 2015. The efficiency of self-healing concrete using alternative manufacturing procedures and more realistic crack patterns. Cem. Concr. Compos. 57, 142-52.

Van Tittelboom, K., Wang, J., Araújo, M., Snoeck, D., Gruyaert, E., Debbaut, B., Derluyn, H., Tsangouri, C.V., Hemelrijck, D.V., De Belie, N., 2016. Comparison of different approaches for self-healing concrete in a large-scale lab test. Constr. Build. Mater. 107, 125-37.

Vázquez, E., 2016. Recycled aggregates for concrete: problems and possible solutions. Int. J. Earth Environ. Sci. 2016.

Watts, J., 2019. Concrete: the most destructive material on earth. The Guardian. https://www.theguardian.com/cities/2019/feb/25/concrete-the-most-destructive-material-on-earth. (Accessed on Nov 1st, 2019)

Xu, D., Cui, Y., Li, H., Yang, K., Xu, W., Chen, Y., 2015. On the future of Chinese cement industry. Cem. Concr. Res. 78, 2-13.

Xue, C., Li, W., Li, J., Wang, K., 2019. Numerical investigation on interface crack initiation and propagation behavior of self-healing cementitious materials. Cem. Concr. Res. 122, 1-6.

Yalcinkaya, G., 2018. World's First 3D-printed Steel Bridge Unveiled at Dutch Design Week. Dezeen. https://www.dezeen.com/2018/10/22/worlds-first-3d-printed-steel-bridge-completed-mx3d-technology/. (Accessed on Nov 1st, 2019)

Yang, G., Wei, J., Yu, Q., Huang, H., Li, F., 2019. Investigation of the match relation between steel fiber and high-strength concrete matrix in reactive powder concrete. Mater. 12(11), 1751.

Yin, H., Qu, M., Zhang, H., Lim. Y., 2018. 3D printing and buildings: A technology review and future outlook. Technol. Architec. Des. 2(1), 94-111.

Yoo, D. Y., You, I., & Lee, S. J. (2017). Electrical properties of cement-based composites with carbon nanotubes, graphene, and graphite nanofibers. Sensors, 17(5), 1064.

Zou, B., Chen, S. J., Korayem, A. H., Collins, F., Wang, C. M., & Duan, W. H. (2015). Effect of ultrasonication energy on engineering properties of carbon nanotube reinforced cement pastes. Carbon, 85, 212-220.

Natt Makul is a senior lecturer at Phranakhon Rajabhat University, Thailand. He received his Ph.D. in Civil Engineering from Thammasat University. His research interests include the microwave heating of cement-based materials, the utilization of waste materials as concrete materials, such as fly ash, rice husk ash, limestone powder, steel powder, foundry sand, and dry powder sludge ash, the behaviors of Portland cement-based materials, the microstructural characteristics of concrete, and the special testing and analysis of concrete structures.

Tables

- Table 1

Examples of Recent Cases of Smart Technology (Mishra et al., 2018).

| Project | Innovation | References |
| --- | --- | --- |
| Mx3D Smart Bridge | 3D Printing | Yalcinkaya (2018); Electronic Design (2019) |
| Tsing Ma Suspension Bridge | Longest Suspension Bridge, SHM | City University (2019) |
| Burj Khalifa Tower | Tallest Building, Vision | Expotrade (2016) |
| BROAD Sustainable Building (BSB) | Industrial-scale prefabrication of building systems | Broad Sustainable Building (2016); Building Ventures (2018) |
| Aditazz Automation | Automated Building Information system | Aditazz (2019) |

- Table 2

Categories of Tests for Self Healing Cement (Xue et al., 2019).

| Items | Mechanical tests | References |
| --- | --- | --- |
| Launching of the self‐healing process | Four‐point bending test | Van Tittelboom et al. (2016); Xue et al. (2019) |
|  | Three-point bending test | Mostavi et al. (2015); Feiteira et al. (2017); Beglarigale et al. (2018) |
| Measuring self‐healing efficiency | Four-point bending test | Van Tittelboom et al. (2016); Xue et al. (2019) |
|  | Three-point bending test | Feiteira et al. (2016); Feiteira et al. (2017) |
|  | Tensile test | Van Tittelboom et al. (2015) |
|  | Capillary water uptake | Huang et al. (2016) Van Belleghem et al. (2016) |
|  | Water permeability | Mostavi et al. (2015); Feiteira et al. (2016); Van Tittelboom et al. (2016) |
|  | Digital image correlation | Feiteira et al. (2017) |
|  | X‐ray computed tomography | Feiteira et al. (2017) |
|  | Micrograph | Feiteira et al. (2017) |
|  | Florescent microscopy | Van Tittelboom et al. (2015) |
|  | Infrared analysis | Perez et al. (2015); Ferrara (2018) |
|  | Neutron radiography | Snoeck et al. (2018) |
| Monitoring of self‐healing process | Piezoelectric transducers | Ferrara et al. (2018) |
|  | Acoustic emission analysis | Van Tittelboom et al. (2017) |

- Table 3

Aggregate Ratio of CCA Concrete (Reddy and Ravitheja, 2019).

| Material | Gravel (kg) (20–12.5 mm) | Cement (kg) | Gravel (kg) (12.5–4.75 mm) | Steel fibers (kg) | Sand (kg) | W/C | Crystalline admixture (kg) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CCA | 599 | 425.5 | 599 | 40 | 666.5 | 0.45 | 4.68 |

- Table 4

CCA’s CS Early Age Cracks Healing Exposed to Various Environments (Reddy and Ravitheja, 2019).

| Curing environment | CS (MPa) |
| --- | --- |
| CCA | 47 |
| WI2 | 45 |
| WD2 | 42 |
| WC2 | 35 |
| AE2 | 20 |

- Table 5

CCA’s CS Structural Cracks Healing Exposed to Various Environments (Reddy and Ravitheja, 2019).

| Curing environment | CS (MPa) |
| --- | --- |
| CCA | 47 |
| WI28 | 52 |
| WD28 | 50 |
| WC28 | 42 |
| AE28 | 37 |

- Table 6

Percentage of CCA’s CS Recovery for Both Structural and Early Age Cracks Healing Exposed to Various Environments (Reddy and Ravitheja, 2019).

| Curing environment | Compressive strength (MPa) |  |
| --- | --- | --- |
|  | Early-stage cracks | Structural cracks |
| WI | 98 | 120 |
| WD | 90 | 115 |
| WC | 70 | 90 |
| AE28 | 30 | 78 |

- Table 7

STS Of CCA after Early Age Cracks Healing in Various Environments (Reddy and Ravitheja, 2019).

| Curing environment | Split tensile strength (MPa) |
| --- | --- |
| CCA | 3.8 |
| WI28 | 3.4 |
| WD28 | 2.7 |
| WC28 | 2.8 |
| AE28 | 1.7 |

- Table 8

STS Of CCA after Structural Cracks Healing in Various Environments (Reddy and Ravitheja, 2019).

| Curing environment | Splint strength (MPa) |
| --- | --- |
| CCA | 3.8 |
| WI28 | 4.0 |
| WD28 | 3.5 |
| WC28 | 3.4 |
| AE28 | 2.7 |

Table 9

Percentage STS Recovery Of CCA Structural And After Early Age Cracks Healing in Various Environments (Reddy and Ravitheja, 2019).

| Curing environment | Split tensile strength (MPa) |  |
| --- | --- | --- |
|  | Early-stage cracks | Structural cracks |
| WI | 80 | 100 |
| WD | 75 | 95 |
| WC | 75 | 80 |
| AE28 | 45 | 70 |

- Table 10

Composition of Concretes (Kg/M3) (Mousa et al., 2015).

| Concrete mix | Gravel (20 mm) | Cement (C) | Silica fume (SF) | Super-plasticizer (SP) | Water (W) | W+Ch/C+SF | Self-curing agent (SCUA |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | Leca | Ch. |
| M6 (SF + Leca) | 1096 |  | - | 2.8 | 184 | 0.4 | 34(15%) | - |
| M5 (SF + Ch) | 1102 |  | 60(15%) | 2.8 | 175 | 0.4 | − | 9.2(2%) |
| M4 (15% leca) | 1190 |  | - | 4 | 160 | 0.4 | 37(15%) | - |
| M3 (2% Ch.) | 1189 |  | - | 4 | 152 | 0.4 | − | 8(2%) |
| M2 (15% SF.) | 1102 |  | 60(15%) | 2.8 | 184 | 0.4 | − | - |
| M1 (Ref.) | 1189 | 400 | 60(15%) | 2.8 | 160 | 0.4 | - | - |

- Table 11

Chemical Ingredients of Silica and Portland Cement (Mousa et al., 2015).

| Chemical composition (%) | SO3 | MgO | CaO | Fe2O3 | Al2O3 | C4AF | C3A | SiO2 | LOI | C2S | C3S |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Silica fume | 0.3 | 0.4 | 0.2 | 0.6 | 0.6 | - | - | 0.3 | 1.0 | - | - |
| Portland cement | 2.4 | 3.7 | 62.51 | 2.68 | 7.36 | 8.15 | 11.73 | 19.49 | 1.36 | 33.6 | 37.17 |

- Table 12

Properties of Polyethylene-Glycol (Mousa et al., 2015).

| Type | Functional group |  | Maximum solubility at 20 °C (mass fraction %) | Molecular weight |
| --- | --- | --- | --- | --- |
|  | Ether |  |  |  |
| Synthetic | Hydroxyl | Yes | 100 | 200 |

- Table 10

Comparing 50 °C Increase and The Conventional 25 °C Concrete at 28 Days (Mousa et al., 2015).

| Concrete mix | Indirect tensile strength (MPa) |  |  |  |  | Compressive strength (MPa) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Curing at 25 °C | Variance (a)% | Curing at 50 °C | Variance (b)% | Variance(c)% | Curing at 25 °C | Variance (a)% | Curing at 50 °C | Variance (b)% | Variance (c)% |
| M6 (SF + Leca) | – | – | 3.56 | +29.5 | – | 47 | +38.2 | 46 | +24.3 | −2.1 |
| M5 (SF + Ch) | – | – | 3.78 | +37.5 | – | 49 | +44.1 | 51 | +37.8 | +4.1 |
| M4 (15% leca) | 2.75 | +9.13 | 3.06 | +11.3 | +11.3 | 37 | +8.8 | 40 | +8.1 | +8.1 |
| M3 (2% Ch.) | 2.88 | +14.3 | 3.15 | +14.6 | +9.4 | 41 | +20.6 | 43 | +16.2 | +4.9 |
| M2 (15% SF.) | 3.27 | +29.8 | 3.32 | +20.7 | +1.5 | 43 | +26.5 | 45 | +21.6 | +4.7 |
| M1 (Ref.) | 2.52 | 0.0 | 2.75 | 0.0 | +9.1 | 34 | 0.0 | 37 | 0.0 | +8.8 |

- Table 11

Comparing 50 °C Increase and The Conventional 25 °C Concrete At 28 Days (Mousa et al., 2015).

| Concrete mix | Mass Loss (g) |  |  |  |  | V.W.A. (g/L) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Air Curing at 25 °C | Variance (a)% | Air Curing at 50 °C | Variance (b)% | Variance (c)% | Air Curing at 25 °C | Variance (a)% | Air Curing at 50 °C | Variance (b)% | Variance (c)% |
| M6(SF+Leca) | – | – | 110 | −20.3 | – | 42 | −26.3 | 48 | −35.5 | +11.11 |
| M5 (SF + Ch) | – | – | 102 | −26.1 | – | 49 | −36.8 | 40 | −35.5 | +11.11 |
| M4 (15%leca) | 2.75 | −4.8 | 122 | −11.6 | +107 | 55 | −3.5 | 60 | −3.2 | +9.1 |
| M3 (2% Ch.) | 50 | −19.4 | 115 | −16.7 | +130 | 49 | −14.0 | 55 | −11.3 | +12.3 |
| M2 (15% SF.) | 48 | −22.6 | 110 | +20.3 | +129 | 40 | −29.8 | 45 | −27.4 | +12.5 |
| M1 (Ref.) | 62 | 0.0 | 138 | 0.0 | 123 | 57 | 0.0 | 62 | 0.0 | +8.8 |

- Table 12

Blended Ratio per M3 for M20 Solution (Poovizhiselvi and Karthik, 2017).

| PEG (Polyethylene Glycol) -% of cement | Cement (kg) | PEG (kg) | Coarse aggregate (kg) | Fine aggregate (kg) | Water (lite) |
| --- | --- | --- | --- | --- | --- |
| 2.0 | 383 | 0.20 | 1188 | 546 | 270.6 |
| 1.5 | 383 | 0.15 | 1188 | 546 | 255 |
| 1.0 | 383 | 0.10 | 1188 | 546 | 239.3 |
| 0.5 | 383 | 0.05 | 1188 | 546 | 223.5 |
| 0 | 383 | 0.00 | 1188 | 546 | 192 |

- Table 13

Blended Ratio per M3 for M30 Solution (Poovizhiselvi and Karthik, 2017).

| PEG -% of cement | Cement (kg) | PEG (kg) | Coarse aggregate (kg) | Fine aggregate (kg) | Water (lite) |
| --- | --- | --- | --- | --- | --- |
| 2.0 | 413 | 0.20 | 1140 | 662 | 264.6 |
| 1.5 | 413 | 0.15 | 1140 | 662 | 249 |
| 1.0 | 413 | 0.10 | 1140 | 662 | 233.3 |
| 0.5 | 413 | 0.05 | 1140 | 662 | 217.5 |
| 0 | 413 | 0.00 | 1140 | 662 | 186 |

- Table 14

Results Showing CS at 28 Days (Poovizhiselvi and Karthik, 2017).

| PEG -% of cement | CS at 28 days for M20 (N/mm2) | CS at 28 days for M30 (N/mm2) |
| --- | --- | --- |
| 2.0% | 25.06 | 46.79 |
| 1.5% | 26.79 | 48.63 |
| 1.0% | 28.50 | 45.17 |
| 0.5% | 27.61 | 40.17 |
| 0% | 26.60 | 38.33 |

- Table 15

Results Showing STS at 28 Days (Poovizhiselvi and Karthik, 2017).

| PEG -% of cement | STS at 28 days for M20 (N/mm2) | STS at 28 days for M30 (N/mm2) |
| --- | --- | --- |
| 2.0% | 1.83 | 3.18 |
| 1.5% | 1.96 | 3.37 |
| 1.0% | 2.05 | 3.54 |
| 0.5% | 1.94 | 3.68 |
| 0% | 1.81 | 3.32 |

- Table 16

Results Showing FS at 28 Days (Poovizhiselvi and Karthik, 2017).

| PEG -% of cement | FS at 28 days for M20 (N/mm2) | FS at 28 days for M30 (N/mm2) |
| --- | --- | --- |
| 2.0% | 4.9 | 6.3 |
| 1.5% | 4.8 | 6.8 |
| 1.0% | 5.1 | 7.0 |
| 0.5% | 4.7 | 7.5 |
| 0% | 4.5 | 6.6 |

- Table 17

Benefits of Self-Curing According To an Experiment by Nduka Et Al. (Papanikolaou et al., 2019).

| Benefit | Rank | Std. Deviation | Mean |
| --- | --- | --- | --- |
| Increased strength and durability | 10 | 0.972 | 1.93 |
| Reduced autogenous shrinkage and cracking | 9 | 0.964 | 1.95 |
| Satisfactory impact resistance | 8 | 1.042 | 2.00 |
| Increased cement hydration | 7 | 1.112 | 2.02 |
| The improved interfacial transition zone | 6 | 1.086 |  |
| Higher stiffness and reduced creep | 5 | 1.202 | 2.25 |
| Reduced moisture evaporation | 4 | 1.200 | 2.32 |
| The improved microstructure of the cementitious paste | 3 | 1.075 | 2.38 |
| Reduced coefficient of thermal expansion | 2 | 1.095 | 2.43 |
| Lower permeability | 1 | 1.032 | 2.45 |

- Table 18

Constituents of UHPC (Abbas et al., 2016).

| UHPC ingredients | Range (% by weight) |
| --- | --- |
| Sand | 35–45 |
| Quartz powder | 7–14 |
| Water | 4–10 |
| Superplasticizer | 0.5–3 |
| Silica fume | 6–12 |
| Cement | 27–40 |

- Table 19

Appropriate UHPC Composition Ratio (Kg/M3) As Discussed in Previous Studies and the Experiment’S Initial Trial Mixture (‘UHPC-B1’) (Sbia et al., 2017).

| Mix elements | Wang et al. (2012) | Ma and Schneider (1200) | ‘UHPC-B1’ | Maruyama et al. (2013) |
| --- | --- | --- | --- | --- |
| Natural sand | 616.0 | 304.1 | 610.6 | 451.0 |
| Aggregate | 1539.0 | 1020.0 | 1383.0 | 1383.0 |
| Coarse aggregates | 923.0 | 715.2 | 772.4 | 932.0 |
| Cement | 450.0 | 465.0 | 623.0 | 930.0 |
| Cementitious materials | 900.0 | 804.9 | 933.0 | 1033.0 |
| Silica fume | 90.0 | 140.0 | 207.0 | 103.0 |
| Slag/fly ash | 180.0 | - | 103.0 | - |
| Water | 144.0 | 124.2 | 149.2 | 155.0 |
| Limestone (L)/quartz (Q) flour | 180.0 | 199.0 | - | - |
| Water/binder ratio | 0.18 | 0.16 | 0.16 | 0.15 |
| HRWR | 18.0 | 16.3 | 39.4 | 26.9 |
| Compressive strength (MPa) (28 day | 174.5 | 149.2 | - | 173.2 |
| Compressive strength (MPa) (365 days) | 180.0 | 155.8 | - | 180.0 |

- Table 23

Composition of Concrete Specimens BZS, BZI and BZ3 (Błaszczyński and Przybylska-Fałek, 2015).

| Composition | Quantity [kg/m3 ] |
| --- | --- |
| Multi-fraction gravel | 2-8 527 |
| Sand 0-2 mm | 630 |
| Single-fraction gravel | 8-16 724 |
| Water | 162 |
| Cement CEM II/BS-32.5R | 325 |
| Steel dispersed fiber | Based on assumption |
| Superplasticizer CHRYSO® Fluid CE 30 | 3.25 |

- Table 24

Concrete Increase in Relative CS for the Three Samples (BZS, BZI, BZ3) (Błaszczyński and Przybylska-Fałek, 2015).

| Compression | BZS |  | BZ1 |  | BZ3 |  |
| --- | --- | --- | --- | --- | --- | --- |
| Time | AE |  | AE |  | AE |  |
| 50 | 2 | 1 | 2 | 1 | 1 | 0.5 |
| 100 | 3 | 2 | 6 | 4 | 1 | 1 |
| 150 | 6 | 4 | 15 | 7 | 4 | 2.5 |
| 200 | 8 | 6 | 22 | 6 | 6.5 | 6 |
| 300 | 18 | 6 | 32 | 8 | 13 | 7 |
| 400 | 28 | 23 | 45 | 24 | 23 | 13 |
| 500 | 36 | 36 | 50 | 45 | 28 | 25 |
| 600 | 40 | 30 | 54 | 16 | 33 | 27 |

- Table 25

Composition Specification and Stress Levels for BZS, BZ1, and BZ3 (Błaszczyński and Przybylska-Fałek, 2015).

| Stress Levels |  |  |  |  |
| --- | --- | --- | --- | --- |
| Concrete | [-] | Variation factor | [-] | Variation factor |
| BZ3 | 0.81 | 1.30 | not observed | - |
| BZI | 0.80 | 1.32 | not observed | - |
| BZS | 0.78 | 1.15 | 0.33 | 1.92 |

- Table 26

Levels Of Deformation for Critical () and Cracking Initiation Stresses () BZS, BZ1 and BZ3 (Błaszczyński and Przybylska-Fałek, 2015).

| Stress Levels |  |  |  |  |
| --- | --- | --- | --- | --- |
| Concrete | [-] | Variation factor | [-] | Variation factor |
| BZ3 | 0.81 | 1.50 | not observed | - |
| BZI | 0.80 | 1.84 | not observed | - |
| BZS | 0.78 | 1.78 | 0.33 | 2.45 |

- Table 27

3D Printing Technologies (Lansard, 2019).

| Materials | Jetting | Fusion | Polymerization | Deposition |
| --- | --- | --- | --- | --- |
| Metal | Material or binder jetting | Powered bed fusion |  | Extrusion |
| Plastic | Material or binder jetting | Powered bed fusion | Photopolymerization | Extrusion or directed energy deposition |
| Ceramic | Material or binder jetting | Powered bed fusion |  |  |
| Sand | Material or binder jetting |  |  |  |
| Paper |  |  |  | Lamination |
| Liver cells |  |  |  | 3D Bioprinting |
| Plastic |  |  |  |  |
| Wax | Material or binder jetting | Powered bed fusion | Photopolymerization | Extrusion or directed energy deposition |

- Table 28

Additive Manufacturing Categories and Definition (Duarte, 2016).

| Category | Definition |
| --- | --- |
| Material jetting | This process involves selective deposition of droplets of building material |
| Binder jetting | Selective deposition of liquid bonding agent to join powder materials |
| Material extrusion | Involves selective dispensing of materials through an orifice |
| Directed energy deposition | Focused energy fuses materials through melting |
| Sheet lamination | Material sheets are bonded to form an object |
| Powder-bed fusion | Thermal energy fuses regions to form a powder bed |
| Photopolymerization | It is the curing of a liquid photopolymer via light activation |

- Table 29

Classification of smart concrete using different criteria as presented by Han, Zhang & Ou, (2017).

| Criteria | Classification |  |
| --- | --- | --- |
| Matrix materials | Cement-based materials |  |
|  | Asphalt-based materials |  |
|  | Polymer-based materials |  |
| Smartness or function | Self-compacting | Smartness |
|  | Self-expanding |  |
|  | Self-curing |  |
|  | Self-shaping |  |
|  | Self-sensing |  |
|  | Self-healing |  |
|  | Self-adjusting |  |
|  | Self-cleaning |  |
|  | Self-damping |  |
|  | Self-heating |  |
|  | Self-light-emiting |  |
|  | Damping | Mechanical function |
|  | Anti-spalling |  |
|  | Water-resisting |  |
|  | Aircraft arresting |  |
|  | Electrical conductive | Electrical function |
|  | Electrothermal |  |

Figures

Fig. 1. CCA's LD curves after early age crack healing in various environments (Reddy and Ravitheja, 2019).

Fig. 2. CCA's LD curves after early age crack healing in various environments (Reddy and Ravitheja, 2019).

- Fig. 3. Air curing at 25 °C and effect on compressive strength (Mousa et al., 2015).

- Fig. 4. Air curing at 50 °C and effect on compressive strength (Mousa et al., 2015).

Fig. 5. Air curing at 25 °C and effect on tensile strength (Mousa et al., 2015).

- Fig. 6. Air curing at 50 °C and effect on tensile strength (Mousa et al., 2015).

Compressive strength (MPa)

Fig. 7. Findings of UHPC compressive strength test from initial lab researches (means and standard errors) (Sbia et al., 2017).

Water, cement, superplasticizer silica fume, fly ash, slag, and powder

The largest size of granules and grading

Uniaxial CS, abrasion resistance, porosity, and density

Optimizing the packing density of granules (theory and practice)

Workability

Packing density, workability, compressive strength, hydration

Compressive strength

Improving granule ratio

Calculation of binder volume fraction

Improving the binder ingredients

UHPC formulation: fine and coarse granules, cement, water, fume, slag, superplasticizer, and silica

Test results

Choosing coarse and fine aggregates

Local availability

- Fig. 8. Flowchart outlining the approach to UHPC mix design (Sbia et al., 2017).

1.0

0.8

0.4

0

t [s]

Fig. 9. BZS Concrete increase in relative compressive stress (Błaszczyński and Przybylska-Fałek, 2015).

0.8

0.2

t [s]

Fig. 10. BZ1 Concrete increase in relative compressive stress (Błaszczyński and Przybylska-Fałek, 2015).

t [s]

Fig. 11. BZ3 Concrete increase in relative compressive stress (Błaszczyński and Przybylska-Fałek, 2015).

(MPa)

(%)

Fig. 12. Comparing sigma for compressed cements BZ1, BZ3 and BZS (Błaszczyński and Przybylska-Fałek, 2015).

Fig. 13. Schematic explanation of the extrusion-based three-dimensional printing technique (Marchment et al., 2017).

- Fig. 14. Showing 45° angle extrusion nozzle (Marchment et al., 2017).

Fig. 15. Showing a single layer of extruded concrete (250 mm length by 25 mm width by 15 mm height) (Marchment et al., 2017).

- Fig. 16. Directions for loading specimen (Marchment et al., 2017).

Fig. 17. Directions for loading specimen for flexural strength testing (Marchment et al., 2017).

Compressive strength (MPa)

Delay time (min)

- Fig. 18. Compressive strength vs. delay time (Marchment et al., 2017).

Flexural strength (MPa)

Delay time (min)

- Fig. 19. Flexural strength vs. delay time (Marchment et al., 2017).

Inter-bonding strength (MPa)

Delay time (min)

Fig. 20. Inter-layer bonding strength vs. delay time (Marchment et al., 2017).

Fig. 21. Model of materials (Han et al., 2017).