SARCOS – Interlaboratory Testing

# RRT2

# Concrete with MgO

# Introduction

Compatible supplementary minerals can improve the self-healing capacity of traditional cement and concrete materials through increasing the formation of healing products. Depending on the mineral type, these additions can remain considerably unhydrated after the initial mixing stage, and/or produce compatible expansive hydrated compounds that can heal cracks. Suitable minerals are required to remain substantially unhydrated after the initial concrete production. Three types of expansive minerals, magnesium oxide (MgO), bentonite clay, and hydrated lime, are used to produce a composite mix of healing additives to be added supplementing part of the cement. The MgO is a moderate reactive (lightburned) grade magnesia calcined from magnesite. This type of MgO contains 93.18% of MgO and was neutralized at 145 seconds in an accelerated acidic reactivity test. The bentonite is a Montmorillonite clay principally containing ~54.2% SiO2 and 18.8% Al2O3 in altering layers. Hydrated lime was used instead of the initial suggested quicklime due material safety restrictions in the producing laboratory. The final mineral, hydrated/slaked lime, at a content of about 93.9% and is provided as a dry white powder. The chemical composition and physical properties are presented in Table 1.

Table 1. Chemical composition and physical characteristics of mineral additions

|  | MgO (M) | Bentonite clay (B) | Slaked lime (L) |
| --- | --- | --- | --- |
| Chemical composition |  |  |  |
| SiO2 (%) | 2.25 | 54.20 | 2.00 |
| Al2O3 (%) | 0.22 | 18.80 | 0.80 |
| CaO (%) | 0.87 | 4.90 | 88.00 |
| Fe2O3 (%) | 0.53 | 5.00 | 0.40 |
| MgO (%) | 93.18 | 3.70 | 2.00 |
| SO3 (%) | - | - | 0.30 |
| Na2O (%) | - | 3.00 | - |
| K2O (%) | - | 0.60 | - |
| TiO2 (%) | - | 0.70 | - |
| CaCO3 (%) | - | - | - |
| LOI (%) | 2.59 | - | - |
| Physical properties |  |  |  |
| Avg. Particle size (μm) | 30-40 | 4.75-75 | - |
| Density (g/cm3) | 3.02 | 2.80 | 2.24 |
| S.Surface area (m2/g) | 16-20 | 0.48 | 20-25 |
| Bulk density (g/cm3) | - | - | 0.3-0.45 |
| Reactivity | 145 s | - | - |

# Mix design

Base material: Concrete with mineral admixtures as self-healing agent, with steel fibers

Table 1. Mix design

| kg / m3 | Reference | Self-healing |
| --- | --- | --- |
| CEM I 42.5 N | 360 | 315 |
| Water | 180 | 198 |
| Natural sand 0/4 | 930 | 980 |
| Crushed dolomite gravel 4/8 | 530 | 910 |
| Crushed dolomite gravel 8/16 | 365 |  |
| Steel fibers | 40 | 40 |
| Plasticizer SIKA | ~3lt/m3 | ~3-3.2lt/m3 |
| Hydrated lime (L) | - | 18 |
| MgO (M) | - | 18 |
| Bentonite (B) | - | 9 |

Mix design previously investigated by [1,2] considered only cement paste mixes with CEMI 42.5N w/c=0.35 (+0.3% plasticizer by weight of binder) and 2.5%, 5% and 5% cement substitution with bentonite, MgO and quicklime respectively.

## Specific comments:

- Grading and cement content for high workability and easy casting relatively small specimens

- CEM I 42.5N – Mainly clinker –

- Fibers: Dramix 65/35 BN from Bekaert (adapted to the specimen’s size)

- Calcareous aggregates, max size 16 mm – Natural sand and crushed coarse aggregate

- Expansive minerals: M5L5B2.5 ratio of cement substitution by weight (12.5% total cement substitution)

- Mixing process:

Minerals are mixed with the cement and aggregates in dry conditions (minimum of 3min), then 70% of the water will be added followed by further mixing (3min). The material will be scraped from the sides and stirred manually. Then the plasticizer and the 25% of the water will be added and mixed thoroughly for further 2 min (minimum). And finally the rest of the mixing water (5%) will be added in mixed for final 2min to ensure optimum dispersion.

## Responsibilities:

- Prepare guidelines for RRT2 (UCAM/RigaTU)

- Characterisation of minerals (UCAM)

- Shipping (MgO and Bentonite) materials to producer laboratory (UCAM)

- RigaTU will source the hydrated lime required.

- Samples’ casting and shipping to the different laboratories involved in RRT2 (RigaTU)

- Coordinate and collect the information of RRT2 (UCAM/RigaTU)

UCAM will ship to producer laboratory:

- MgO		10 kg

- Bentonite	5 kg

RigaTU will ship to each tester laboratory:

- Reference concrete:

  - 6, size 100x100x500 mm3 beams

  - 4, size Ø100XH200 mm cylinders (to be further cut)

- Self-healing concrete:

  - 6, size 100x100x500 mm3 beams

  - 4, size Ø100XH200 mm cylinders (to be further cut)

Specimens will be stored in in water for 14 days until shipping.

# Sample preparation

Before starting with the self-healing tests, all the samples will be stored in humidity chamber at 20°C, 95±5% relative humidity, or alternatively under water immersion, depending on the availability at each laboratory (but this should be clearly indicated by each lab).

discarded ends

Disks for self-healing tests

Notch all prismatic specimens (10 mm notch height, width depending on the saw), and pre-crack 3 prisms from each concrete type in 3PBT until reaching a crack width of 0.2±0.05mm after unloading (around 0.30mm in loaded state). Testing procedure is adapted from [1,2] where residual cracks of 0.20±0.03mm were considered.

From all the long cylindrical specimens cut 3 disks Ø 100mm × 50mm height, discarding the ends of the cylinder (see diagram). Pre-crack all disks by splitting test reaching a crack width of 0.2±0.05 mm after unloading (around 0.30 mm in loaded state). Testing procedure is adapted from [1,2] where residual cracks of 0.20±0.03mm were considered.

The starting testing time for self-healing will be coordinated inside RRT2 (minor adjustments expected if delays are produced in the deliveries). In this way, all data can be adjusted accordingly.

Table 3: Testing program to evaluate self-healing.

| Self-healing test | Sample | Time test (after 28 days) |
| --- | --- | --- |
| Water Permeability | All Disks | 0 /1/ 3/ 6 months |
| Chlorides | Disks from water perm (max 3 per age) | After WP, if water does not pass |
| Sorptivity | All Prisms | 0 /1/ 3/ 6 months |

After initial pre-cracking (before healing), and between tests, all the samples are stored in waterproof containers submerged in deionized water to promote the self-healing reactions during 1, 3 and 6 months. The same samples will be tested before healing, and at the defined 3 monitoring periods to monitor the healing process.

The reference and the self-healing samples should be kept in different water containers. The disks will be stored vertically. All prisms will be stored with the crack facing downwards to avoid further crack opening. Crack width will be observed macroscopically through optical microscopy and the crack width calculated thereafter.

## Precracking of prisms

Concrete specimens with a dimension of 100x100x500 mm³ are provided. 6 Reference without additions and 6 reference with additions. The notch should have a depth of 10 mm notch height and is inserted at least 1 day prior to cracking. Three reference and six with additions specimens are cracked in a crack width controlled three point bending test with an LVDT or CMOD which is mounted at the bottom of the specimen (similarly as prescribed by healCON to perform water absorption tests), see below. The span is equal to 30 cm. The specimens are to be loaded until a certain crack width of W around 0.30 is achieved at a loading speed of 0.7 μm/s. They are then unloaded manually or by a programmed rate. In an unloaded state the crack width (at the crack mouth) should be around 200 μm. The age at cracking will be 35±1 days (or 70±1 days). The three reference/control specimens are kept uncracked for reference testing. Samples will be kept in water till cracking date, once they are received.

The crack width is then recorded by optical microscopy at 4 different locations (5 measurements per location). The average crack width is the average of all these (20) measurements.

Crack width controlled three point bending test using LVDT (from healCON).

Crack width controlled three point bending test using CMOD

.

## Precracking of disks

Concrete cylinders with a dimension of Ø 100x200 mm³ are provided. From all the long cylindrical specimens 3 disks Ø 100mm × 50mm height will be cut, discarding the ends of the cylinder. Two notches, symmetrically on either side, about 3 and 5mm depth should be introduced in the middle of discs. All samples should be laterally restricted (by fastening with adhesive tape to minimize damage or crumbling of the sides). The specimens are to be loaded until a certain crack width of W around 0.30 is achieved at a loading speed of 0.7 μm/s. They are then unloaded manually or by a programmed rate. In an unloaded state the crack width (at the crack mouth) should be around 200 μm. The age at cracking will be 35±1 days (or 70±1 days). Samples will be kept in water till cracking date, once they are received.

Crack measure

Crack width will be measured with an optical microscope in 6 equidistant points of the length of the crack. The average crack width will be calculated.

Example of Cylindrical disc setup and crack width controlled three point bending test using CMOD

## Self-healing test // Water Permeability

Per lab:

- 9 cracked REF

- 9 cracked ADD self-healing with healing addition

Preparation

Prior to performing the water permeability test for samples healing for 1, 3 and 6 months, they will be preconditioned for 24 hours at laboratory conditions (or 24 hours drying at 40°C). Labs need to specify the preconditioning environments adopted. This will allow sufficient drying for the disks.

Permeability

PVC tubes of at least 200 mm (or 400 mm, 500 mm…) height will be glued on the top of the disks using a resin. Allow the resin to dry for 24 hours. Silicon glue can be used instead. The  tubes can remain glued on the samples, provided enough space is available in the container for storage. The tubes will be filled with 1.5 liters (or 3 liters, 3.80 liters…depending on the size of the tube) of tap water (beginning of filling the tube = time 0, filling time of 1 min approx.). The first 60s of testing are not recorded in order not to measure the error which is caused by air bubbles removed by the flow of water through the crack and to be sure that only a stable fully developed water flow is studied. Water is topped up to the initial volume (1.5litres or 3 litres or 3.8) and then the test is started, and the time needed to empty the tube is measured with a timer. The data collected is the time needed for the 1.5 litres to flow through once a constant flow has been achieved. If the time exceeds 20 minutes, then complete the test and measure the drop of water level at 30 minutes from the start of the test. The output of the test will be a water flow measure (litres / minute).

Sealing efficiency to be calculated by the formula:

By this test the sealing efficiency of the healing method can be calculated by applying the following formula:

SE=Wunhealed(t)-Whealed(t)Wunhealed(t)x 100%SE=Wunhealed(t)-Whealed(t)Wunhealed(t)x 100%

Where,

SESE	sealing efficiency calculated at test time (t)

Wunhealed(t)Wunhealed(to)	amount of water that has passed through the specimen’s unhealed crack at cracked time (to)

Whealed(t)Whealed(t)	amount of water that has passed through the specimen’s healed crack at test time (t)

## Self-healing test through chlorides penetration

Proposed test

This test will be performed only to healed samples through water permeability test. After the first month of healing, disks of ADD (with healing additions) that showed complete healing will be used. Since there are 9 disks, maximum 3 disks will be tested to chlorides after 1 month of healing, and maximum 3 disks at 3 months of healing. In this way, a minimum of 3 disks will continue healing until 6 months. The 3 best performing REF disks (reference without healing additions) will be selected for chloride testing to be compared to the ADD samples. The method is as follows:

- Use healed samples from the water permeability test.

- Use the same PVC tube sealed again with resin. Fill the tube with tap water + NaCl (33gr/l). Leave it for 3 days.

- Afterwards, cut the disks in the direction perpendicular to the crack and apply silver nitrate to the section. Leave the samples in an oven at 50°C for 1 day and analyze the output afterwards.

- Visual qualitative analysis of the area of Cl- ingress will be registered.

## Self-healing test through water sorptivity

For each concrete

Per lab:

- 3 cracked REF without healing additions

- 3 uncracked REF without healing additions

- 6 cracked with the healing addition

Preparation

All specimens are dried in an oven of 40°C for a minimum of 14 days until constant weight is achieved. Samples can be air dried in ambient lab conditions provided at the end of 14 days the constant weight is achieved when the change in mass over a period of 2h is less than 0.2%. Labs should record and repord their adopted drying and preconditioning environment. The specimens are subsequently stored for 1 day at 20°C and 60% RH. They are placed on spacers in order to prevent damage to the cracks and to prevent dust from entering the crack.  Placed back facing downwards.

Water sorption

Prior to testing the specimens are partially waterproofed using Aluminium tape (we use Buffalo Aluminium Foil Tape). The bottom of the specimens is completely waterproofed except for a zone of of 14 mm x 100 mm centred on the crack. The sides of the specimens are also sealed up to a height of 30 mm. Also the sides of the specimen where the crack is located are to be waterproofed (this to prevent the influence of small waves when specimens are removed or placed back in the water).

For each specimen the dry weight (with waterproofing) is recorded and subsequently the specimen is placed in the water. The bottom and lateral surfaces will be protected with adhesive aluminum foil, and the top covered with transparent plastic film (cling film) to avoid surface evaporation while leaving only the notch area free for both, cracked and uncracked prisms. The water level in the container shall not exceed by more than 5 mm the specimen’s surface exposed to water. The mass of the samples will be measured at time 0 and after the minutes: 1, 4, 9, 16, 25, 36, 49, 64, 81, 100, 121, 144, 169, 196, 225, 256, 476, 1448 (during 24 hours in total). The test shall be carried out in a waterproof container.

Water level

2-3mm above the notuch

Self-sealing ability is evaluated with this method on a minimum of 3 specimens per category (uncracked, cracked and unhealed, and cracked and healed) as follows:

SE=SCunhealed-SChealedSCunhealed-SCSoundx 100% SE=SCreference-SCADDSCreference-SCuncrackedx 100%	(C.1)

where,

SESCunhealedSE	sealing efficiency

SCunhealedSCreference	sorption coefficient for the reference/control cracked specimens

SCADD	sorption coefficient for the self-healing specimens with additions

SCsoundSCuncracked	sorption coefficient for the uncracked reference/control specimen

# Timetable of testing

## Monitoring times for prisms

| Time 0 | Time 1 | Time 2 | Time 3 | Time 4 | Time 5 | Time 6 | Time 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pre-cracking | 14 days conditioning at 40oC + 1 day at ambient conditions + 1 day test | First water curing (for 28 days) | 14 days conditioning at 40oC + 1 day at ambient conditions + 1 day test | Second water curing (for 2 months) | 14 days conditioning at 40oC + 1 day at ambient conditions + 1 day test | Third water curing (for 3 months) | 14 days conditioning at 40oC + 1 day at ambient conditions + 1 day test |
| Crack width monitoring | Sorptivity testing 1 (24hours) | Crack width monitoring | Sorptivity testing 2 (24hours) | Crack width monitoring | Sorptivity testing 3 (24hours) | Crack width monitoring | Final Sorptivity testing (24hours) |

Example: Pre cracking 1st of July->16th of July start sorptivity test->17th of July complete->28 days curing 14th of August (crack width monitoring)->29th August start of sorptivity test->30th of August finish sorptivity test (Cycle 1)->second water curing 56 days 27th of October (crack width monitoring)->….

## Monitoring times for disks

| Time 0 | Time 1 | Time 2 | Time 3 | Time 4 | Time 5 | Time 6 | Time 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pre-cracking | 1 day conditioning at 40oC + | First water curing (for 28 days) | 1 day conditioning at 40oC + | Second water curing (for 2 months) | 1 day conditioning at 40oC + | Third water curing (for 3 months) | 1 day conditioning at 40oC + |
| Crack width monitoring | Water passing test | Crack width monitoring | Water passing test | Crack width monitoring | Water passing test 2 | Crack width monitoring | Final Water passing test |

Example: Pre cracking 1st of July (crack width monitoring)->2nd of July water passing test->30th of July first water curing completed (crack width monitoring) -> 31st water passing test

# Preliminary results

Update of testing progress is given in Table 4. Tests progress has been disrupted by COVID 19 lockdown.

Table 4. Production date and test progress (updates pending from labs)

| Production date | 28d day | LAB | 1 month |  | 3 month | 6 month |
| --- | --- | --- | --- | --- | --- | --- |
| 29.05.19. | 26.06.19. | 2 | X |  | X |  |
| 31.05.19. | 28.06.19. | 9 | X |  | - | X |
| 03.06.19. | 01.07.19. | 6 | X |  | X | X |
| 07.06.19. | 05.07.19. | 7 | X |  | X (4 months) | X (10 months) |
| 10.06.19. | 08.07.19. | 5 | X |  | X | X |
| 30.06.19 | 27.07.19 | 3 | X |  | X | X(9months sorptivity) |
| 12.06.19. | 10.07.19. | 4 | X |  | X | X (13 months) |
| 14.06.19. | 12.07.19. | 1 | X |  | X | ? |
| 17-19.06.19. (planned) | 15-17.07.19. | 7 | X(1.5month) |  | X (4 months) | X (7months) |