An injectable Chitosan-based self-healable hydrogel system as an antibacterial wound dressing

Xiaoyu Wang#, Rijian Song#, Melissa Johnson, Sigen A, Zhonglei He, Cameron Milne, Xianqing Wang, Irene Lara-Sáez, Qian Xu*, and Wenxin Wang*

The Charles Institute of Dermatology, School of Medicine, University College Dublin, Dublin 4, Ireland.

* Corresponding authors:

wenxin.wang@ucd.ie; qian.xu@ucd.ie

# Co-first author

Contents

Supplementary tables 1-2

Supplementary figures 1-2

Supplementary references

## Table S1. Element analysis results of CTS-CHO.

| Sample | C (%) | N (%) | H (%) | OD (%) |
| --- | --- | --- | --- | --- |
| CTS | 41.77 | 7.12 | 6.73 | N/A |
| CTS-CHO | 38.88 | 5.32 | 6.09 | 14.75% |

Figure S1. Images of bacterial growth inhibition profile at different concentrations: A: 10 mg/mL; B: 30 mg/mL; C: 50 mg/mL. Scale bar: 8 mm.

## Figure S2. Bacterial growth inhibition zone at different concentrations: A: 10 mg/mL; B: 30 mg/mL; C: 50 mg/mL (n=3).

## Table S2. Inhibitory zone of CTS-CHO at different concentrations (n=3).

| ## Concentration (mg/mL) | ## Average inhibitory zone (mm) |
| --- | --- |
| ## 10 | ## 8 |
| ## 30 | ## 13.5 |
| ## 50 | ## 15.0 |

References

(1) 	Suarato, G.; Bertorelli, R.; Athanassiou, A. Borrowing from Nature: Biopolymers and Biocomposites as Smart Wound Care Materials. Front. Bioeng. Biotechnol. 2018, 6 (OCT), 1–11. https://doi.org/10.3389/fbioe.2018.00137.

(2) 	Zhang, X.; Qin, M.; Xu, M.; Miao, F.; Merzougui, C.; Zhang, X.; Wei, Y.; Chen, W.; Huang, D. The Fabrication of Antibacterial Hydrogels for Wound Healing. Eur. Polym. J. 2021, 146 (January), 110268. https://doi.org/10.1016/j.eurpolymj.2021.110268.

(3) 	Nomura, K.; Terwilliger, P. Self-Dual Leonard Pairs Long-Term Durability a Pair A , A Antibacterial Chinese Nutgall and Their Applications in Wound Dressing. 2019, 268–276.

(4) 	Sharma, P. K.; Halder, M.; Srivastava, U.; Singh, Y. Antibacterial PEG-Chitosan Hydrogels for Controlled Antibiotic/Protein Delivery. ACS Appl. Bio Mater. 2019. https://doi.org/10.1021/acsabm.9b00570.

(5) 	Cook, L.; Ousey, K. Demystifying Wound Infection: Identification and Management. Pract. Nurs. 2011, 22 (8), 424–428. https://doi.org/10.12968/pnur.2011.22.8.424.

(6) 	Li, S.; Dong, S.; Xu, W.; Tu, S.; Yan, L.; Zhao, C.; Ding, J.; Chen, X. Antibacterial Hydrogels. Adv. Sci. 2018, 5 (5). https://doi.org/10.1002/advs.201700527.

(7) 	Balakrishnan, B.; Mohanty, M.; Umashankar, P. R.; Jayakrishnan, A. Evaluation of an in Situ Forming Hydrogel Wound Dressing Based on Oxidized Alginate and Gelatin. Biomaterials 2005, 26 (32), 6335–6342. https://doi.org/10.1016/j.biomaterials.2005.04.012.

(8) 	El-banna, F. S.; Mahfouz, M. E. Chitosan as a Natural Copolymer with Unique Properties for the Development of Hydrogels. Appl. Sci. 2019, 9 (2193), 1–11.

(9) 	Sahariah, P.; Másson, M. Antimicrobial Chitosan and Chitosan Derivatives: A Review of the Structure-Activity Relationship. Biomacromolecules 2017, 18 (11), 3846–3868. https://doi.org/10.1021/acs.biomac.7b01058.

(10) 	Díez-Pascual, A. M.; Díez-Vicente, A. L. Wound Healing Bionanocomposites Based on Castor Oil Polymeric Films Reinforced with Chitosan-Modified ZnO Nanoparticles. Biomacromolecules 2015, 16 (9), 2631–2644. https://doi.org/10.1021/acs.biomac.5b00447.

(11) 	Kong, M.; Chen, X. G.; Xing, K.; Park, H. J. Antimicrobial Properties of Chitosan and Mode of Action: A State of the Art Review. Int. J. Food Microbiol. 2010, 144 (1), 51–63. https://doi.org/10.1016/j.ijfoodmicro.2010.09.012.

(12) 	Wegrzynowska-Drzymalska, K.; Grebicka, P.; Mlynarczyk, D. T.; Chelminiak-Dudkiewicz, D.; Kaczmarek, H.; Goslinski, T.; Ziegler-Borowska, M. Crosslinking of Chitosan with Dialdehyde Chitosan as a New Approach for Biomedical Applications. Materials (Basel). 2020, 13 (15), 1–27. https://doi.org/10.3390/ma13153413.

(13) 	Jiang, X.; Yang, Z.; Peng, Y.; Han, B.; Li, Z.; Li, X.; Liu, W. Preparation, Characterization and Feasibility Study of Dialdehyde Carboxymethyl Cellulose as a Novel Crosslinking Reagent. Carbohydr. Polym. 2016, 137 (November 2015), 632–641. https://doi.org/10.1016/j.carbpol.2015.10.078.

(14) 	Mahdavinia, G. R.; Pourjavadi, A.; Zohuriaan-Mehr, M. J. Synthesis and Properties of Highly Swelling PAAm/Chitosan Semi-IPN Hydrogels. Macromol. Symp. 2008, 274 (1), 171–176. https://doi.org/10.1002/masy.200851423.

(15) 	Zhang, W.; Yu, Z.; Qian, Q.; Zhang, Z.; Wang, X. Improving the Pervaporation Performance of the Glutaraldehyde Crosslinked Chitosan Membrane by Simultaneously Changing Its Surface and Bulk Structure. J. Memb. Sci. 2010, 348 (1–2), 213–223. https://doi.org/10.1016/j.memsci.2009.11.003.

(16) 	Jin, J.; Song, M.; Hourston, D. J. Novel Chitosan-Based Films Cross-Linked by Genipin with Improved Physical Properties. Biomacromolecules 2004, 5 (1), 162–168. https://doi.org/10.1021/bm034286m.

(17) 	Capáková, Z.; Fi, M.; Ku, I.; Vícha, J. Cited by Biocompatible Dialdehyde Cellulose / Poly ( Vinyl Alcohol ) Hydrogels with Tunable Properties. 2019, No. 6, 549.

(18) 	Hafezi, F.; Scoutaris, N.; Douroumis, D.; Boateng, J. 3D Printed Chitosan Dressing Crosslinked with Genipin for Potential Healing of Chronic Wounds. Int. J. Pharm. 2019, 560 (9), 406–415. https://doi.org/10.1016/j.ijpharm.2019.02.020.

(19) 	Charhouf, I.; Bennamara, A.; Abdelmjid, A.; Berrada, M. Characterization of a Dialdehyde Chitosan Generated by Periodate Oxidation International Journal of Sciences : Basic and Applied Research Characterization of a Dialdehyde Chitosan Generated by Periodate Oxidation. 2014, No. November.

(20) 	Lv, Y.; Long, Z.; Song, C.; Dai, L.; He, H.; Wang, P. Preparation of Dialdehyde Chitosan and Its Application in Green Synthesis of Silver Nanoparticles. BioResources 2013, 8 (4), 6161–6172. https://doi.org/10.15376/biores.8.4.6161-6172.

(21) 	Vold, I. M. N.; Christensen, B. E. Periodate Oxidation of Chitosans with Different Chemical Compositions. Carbohydr. Res. 2005, 340 (4), 679–684. https://doi.org/10.1016/j.carres.2005.01.002.

(22) 	Liu, X.; Dan, N.; Dan, W.; Gong, J. Feasibility Study of the Natural Derived Chitosan Dialdehyde for Chemical Modification of Collagen. Int. J. Biol. Macromol. 2016, 82, 989–997. https://doi.org/10.1016/j.ijbiomac.2015.11.015.

(23) 	Bam, P.; Bhatta, A.; Krishnamoorthy, G. Design of Biostable Scaffold Based on Collagen Crosslinked by Dialdehyde Chitosan with Presence of Gallic Acid. Int. J. Biol. Macromol. 2019, 130, 836–844. https://doi.org/10.1016/j.ijbiomac.2019.03.017.

(24) 	Yin, M.; Wang, Y.; Zhang, Y.; Ren, X.; Qiu, Y.; Huang, T. S. Novel Quaternarized N-Halamine Chitosan and Polyvinyl Alcohol Nanofibrous Membranes as Hemostatic Materials with Excellent Antibacterial Properties. Carbohydr. Polym. 2020, 232 (7), 10. https://doi.org/10.1016/j.carbpol.2019.115823.

(25) 	Kumar, S.; Koh, J. Physiochemical, Optical and Biological Activity of Chitosan-Chromone Derivative for Biomedical Applications. Int. J. Mol. Sci. 2012, 13 (5), 6103–6116. https://doi.org/10.3390/ijms13056102.

(26) 	Lv, Y.; Long, Z.; Song, C.; Dai, L.; He, H.; Wang, P. Preparation of Dialdehyde Chitosan and Its Application in Green Synthesis of Silver Nanoparticles. BioResources 2013, 8 (4), 6161–6172. https://doi.org/10.15376/biores.8.4.6161-6172.

(27) 	Wei, D.; Sun, W.; Qian, W.; Ye, Y.; Ma, X. The Synthesis of Chitosan-Based Silver Nanoparticles and Their Antibacterial Activity. Carbohydr. Res. 2009, 344 (17), 2375–2382. https://doi.org/10.1016/j.carres.2009.09.001.

(28) 	Mozafari, M.; Moztarzadeh; Jalali; Alhosseini, N.; Asgari; Dodel; Samadikuchaksaraei; Kargozar. Synthesis and Characterization of Electrospun Polyvinyl Alcohol Nanofibrous Scaffolds Modified by Blending with Chitosan for Neural Tissue Engineering. Int. J. Nanomedicine 2012, No. May 2014, 25. https://doi.org/10.2147/ijn.s25376.

(29) 	Jeong, Y. Il; Kim, D. G.; Jang, M. K.; Nah, J. W. Preparation and Spectroscopic Characterization of Methoxy Poly(Ethylene Glycol)-Grafted Water-Soluble Chitosan. Carbohydr. Res. 2008, 343 (2), 282–289. https://doi.org/10.1016/j.carres.2007.10.025.

(30) 	Mahmoudzadeh, M.; Fassihi, A.; Emami, J.; Davies, N. M.; Dorkoosh, F. Physicochemical, Pharmaceutical and Biological Approaches toward Designing Optimized and Efficient Hydrophobically Modified Chitosan-Based Polymeric Micelles as a Nanocarrier System for Targeted Delivery of Anticancer Drugs. J. Drug Target. 2013, 21 (8), 693–709. https://doi.org/10.3109/1061186X.2013.824455.

(31) 	Hoque, J.; Bhattacharjee, B.; Prakash, R. G.; Paramanandham, K.; Haldar, J. Dual Function Injectable Hydrogel for Controlled Release of Antibiotic and Local Antibacterial Therapy. Biomacromolecules 2018, 19 (2), 267–278. https://doi.org/10.1021/acs.biomac.7b00979.

(32) 	Hozumi, T.; Kageyama, T.; Ohta, S.; Fukuda, J.; Ito, T. Injectable Hydrogel with Slow Degradability Composed of Gelatin and Hyaluronic Acid Cross-Linked by Schiff’s Base Formation. Biomacromolecules 2018, 19 (2), 288–297. https://doi.org/10.1021/acs.biomac.7b01133.

(33) 	Jennings, J. A. Controlling Chitosan Degradation Properties in Vitro and in Vivo; Elsevier, 2017; Vol. 1. https://doi.org/10.1016/B978-0-08-100230-8.00007-8.

(34) 	Gong, Z.; Yang, Y.; Ren, Q.; Chen, X.; Shao, Z. Injectable Thixotropic Hydrogel Comprising Regenerated Silk Fibroin and Hydroxypropylcellulose. Soft Matter 2012, 8 (10), 2875–2883. https://doi.org/10.1039/c2sm06984a.