Mixed Metal Oxide Electrodes and the Chlorine Evolution Reaction

Heng Dong1, Weilai Yu2, and Michael R. Hoffmann1*

1Linde Laboratories and 2Division of Chemistry and Chemical Engineering

California Institute of Technology, Pasadena, California 91125, USA

E-mail: mrh@caltech.edu

Abstract: The Chlorine Evolution Reaction (CER) has practical applications in the chlor-alkali industry and electrochemical wastewater treatment. Efficient, stable, and cost-effective electrodes are critical for energy efficient chlorine production, water disinfection, and wastewater treatment. These practical applications require an in-depth understanding of the catalytic mechanism of chlorine evolution, the need for lower-cost electrode materials, and improvements in electrode design at the atomic scale. Herein, we examine factors controlling activity, selectivity, and stability of alternative CER electrodes, and provide mechanistic insights for achieving improvements in performance and durability. Steric effects of crystal structure and intermetallic electron polarization provide insight for understanding and tuning the electrode activity and selectivity. Additional insight into electrode deactivation mechanisms is gained by employing model material systems under controlled conditions. Herein, we explore viable strategies for the development of more efficient noble-metal-free CER electrodes for use in a variety of practical applications.

1. Introduction

Chlorine gas (Cl2) is a commodity chemical that is widely used in construction materials, plastics, organic synthesis, metallurgy, and water disinfection along with many other applications.1 In the chlor-alkali industry, Cl2(g) is produced via the chlorine evolution reaction (CER, Equation 1) in acidic NaCl aqueous electrolyte solutions at concentrations of 200 g L-1 (3.42 M) NaCl in the anolyte1. The oxygen evolution reaction (OER, Equation 2) is a competitive side reaction. Given that 150 TWh of electricity is consumed by chlor-alkali industry per year,2 optimization of the anodic processes can result in improved economic and environmental benefits. Seawater, a low cost source of chloride, is now considered to be an alternative electrolyte for CER.3–5 In addition, CER plays a key role in the onsite electrochemical oxidation (EO) of wastewater in decentralized facilities.6 In the latter case, chloride in wastewater is anodically oxidized into free reactive chlorine (Cl2, HOCl and OCl-), which contributes to organic matter oxidation and wastewater disinfection. In multiple practical cases, EO has been shown to be relatively efficient for the onsite treatment of household wastewater7–11 as well as trace pharmaceutical and personal care products (PPCPs).12

|  | 2Cl-⇌Cl2+2e- | (1) |
| --- | --- | --- |
|  | 2H2O⇌O2+4H++4e- | (2) |

The anode is a key for both chlor-alkali and EO systems. An ideal anode catalyzes the CER with fast kinetics and high selectivity, therefore increasing the efficiency while saving on operational costs. Dimensionally stable anodes (DSAs), which often consist of a Ti base metal plate as the conductive substrate and one or more metal oxide coatings as the active electrocatalyst, are traditionally employed in the chlor-alkali industry for CER. Beer13 proposed the use of oxides of the platinum group metals (PGMs, including Ru, Rh, Pd, Os, Ir and Pt) as the active catalyst layer. However, early generations of DSAs were often compromised by dissolution under high applied potentials and acidic conditions. The PGM oxides are also susceptible to reductive dissolution upon polarity reversal.  To overcome these problems, IVB and VB group transition metals such as Ti, Ta, Nb and Zr, also known as valve metals, were used to form mixed metal oxides (MMO) to stabilize the PGM oxides. For example, RuO2-TiO2 (RTO) electrodes exhibited enhanced catalytic activity as well as improved stability, enabling their use in the chlor-alkali industry.13 The performance of RTO electrodes was further improved by IrO2 doping. Thus, the family of  RuO2-IrO2-TiO2 electrodes can be considered ‘state-of-art’ for the CER in the chlor-alkali industry and for onsite wastewater electrolysis.14 Considering the scarcity and high price of Ru and Ir, anode stability and lifetime are directly related to the capital cost.

Optimization of MMO electrodes (e.g., RTO and RuO2-IrO2-TiO2) has been explored by controlling annealing temperature,15 elemental composition16,17, and particle size18. Comninellis and Vercesi investigated the DSAs with various “PGM + valve metal” binary coatings prepared by thermal deposition procedure. Low thermal deposition yields were noticed for SnO2 and Pt, as opposed to the almost 100% yield for IrO2, RuO2 and Ta2O5.19 A Pt-Ta2O5 electrode produced the largest electrochemically active surface area as quantified by integration of the cyclic voltammograms, while the IrO2-Ta2O5 electrode had the longest service lifetime with respect to the catalyst loading.20 At the same time, numerous factors have been identified to influence the apparent (practical) electrode performance, including electrode morphology, porosity, catalyst loading, gas bubble formation and removal as well as electrolyte pH and ionic composition.21 Brian et al. studied the influence of chloride concentration on CER kinetics over Pt electrodes and concluded that the reaction kinetics were controlled by the recombination of Cl· instead of mass transfer.22

However, after 60 years of research, the underlying catalytic mechanism of CER on MMO electrodes remains poorly understood. Moreover, RTO and RuO2-IrO2-TiO2 electrodes have lower CER selectivity in wastewater with typical chloride concentrations of ~30 mM.6,23,24 Lower chloride concentrations often reduce electrode lifetimes as the concurrent OER compromises electrode stability.25 For industrial applications, the use of PGMs increases capital costs and thus limits wide implementation of electrochemical technology for wastewater treatment in developing countries. In this regard, PGM-free electrodes that have high activity, long-term stability, and preferential selectivity for the CER are critical for developing practical electrochemical applications that are more efficient and economical. To achieve these goals, detailed mechanistic insights into CER catalysis at the atomic scale are essential. In this perspective, we focus on summarizing recent developments in the design, fabrication, and evaluation of CER anodes.

2. Evaluation of electrodes

The objective assessment of the performances of CER anodes requires standardized experimental protocols to properly evaluate activity, selectivity, and stability (Table 1). Electrochemical activity, as quantified by CER overpotential, and selectivity, as quantified by the Faradaic Efficiency (FE) or the current efficiency, need to be clearly defined. FE is defined as

|  | FE=QCERQoverall=iCERdtioveralldt | (3) |
| --- | --- | --- |

where Q is the charge passed and I is the current at an arbitrary time = t. At lower applied potentials in a NaCl solution, OER is the only primary side reaction competing with CER, giving an FE as follows:

|  | FE=iCERdtioveralldt≈iCERdt(iCER+iOER)dt | (4) |
| --- | --- | --- |

With no mass transfer limitations, the Tafel equation can be applied

|  | η=RTαCERFlni0,CER+RTαCERFlniCER | (5) |
| --- | --- | --- |

where i0 represents the exchange current, 𝛼 represents the transfer coefficient, 𝜂 represents overpotential and F = 96,485 C mol-1. For a system with two competing reactions, Tilak et al.26 developed an expression for FE as follows:

|  | FE=11+δFE-ϵI-ϵ | (6) |
| --- | --- | --- |

where

|  | δ=i0,1i0,2exp⁡(k2∆E)i0,1ϵ | (7) |
| --- | --- | --- |
|  | ϵ=k1-k2k1 | (8) |

The subscripts 1 and 2 in Equation 7 and 8 are the two reactions, the CER and OER, and I represents the overall current density, 𝛥E is the difference between the Nernst potentials of the two reactions, and k is the inverse of Tafel slopes for each reaction (Equation 9).

|  | k=αCERFRT | (9) |
| --- | --- | --- |

Based on Equation 5-9, the kinetics of the CER are reflected in both the overpotential and the Faradaic Efficiency. However, the FE also includes the kinetics of OER. Thus, activity and selectivity should not be used interchangeably.

Table 1. Key aspects and caveats in evaluating the overall performance of CER anodes.

| Aspects | Caveats | Refs |
| --- | --- | --- |
| Activity (overpotential) | Qualitative techniques: CV&LSV | 29-34 |
|  | Concentrated, acidified chloride solution to suppress OER | 27, 28 |
|  | Quantitative techniques: Tafel plots | 29, 35-38 |
|  | Gaseous Cl2 saturation for Nernstian potential calculation | 39 |
| Selectivity (Faradaic efficiency) | Gaseous Cl2 & O2 detection: DEMS, OLEMS | 27, 37, 42, 43 |
|  | Aqueous Cl2 detection: DPD reagent, iodometry | 6, 23, 32 |
|  | Different Cl- concentrations correspond to different applications | 23, 27 |
| Stability (service lifetime) | NaCl, KClO4, H2SO4 and HClO4 often used for ALT | 6, 15, 32, 51-54, 57-59, |
|  | CV and EIS coupled with ALT to understand deactivation mechanism | 15, 51-58 |
|  | Chronoamperometry may be helpful for understanding the deterioration of catalytic sites | 55 |
|  | Well-controlled nanoparticles used to unravel the intrinsic degradation of pure metal oxides | 55 |

Activity evaluation. Overpotential plays a key role in the screening of anodes for use in the traditional chlor-alkali industry. For measurements of electrode activity or overpotential, increasing the CER selectivity is essential to minimize interference due to competition with the OER. This can be achieved by increasing the chloride concentration and acidifying the electrolyte.27,28. However, the FE of the CER often drops below 50% in circum-neutral dilute chloride solutions such as found in wastewater.6,23 Therefore, quantifying electrode selectivity under the conditions related to wastewater is essential for evaluating the performance of an electrode for practical environmental applications.

|  | E=Eθ+RT2Flna(Cl2)a(Cl-)2 | (10) |
| --- | --- | --- |

In practice, it is challenging to determine the overpotential of the CER due to the difficulty of determining the Nernst potential (Eq. Equation 10) due to a constantly changing chloride activity and chlorine fugacity (i.e., evolution of Cl2 vs. time) during an electrochemical reaction. Therefore, potential sweeping techniques such as cyclic voltammetry (CV) and linear sweep voltammetry (LSV) are often used as convenient ways to compare the overpotential of CER anodes.29–34 Although these methods are easy to implement, it is often difficult to compare results between different studies, since the reported results are sensitive to various experimental factors, including electrolyte composition, electrochemical setup, and scan rate. To overcome these limitations, polarization curves and Tafel plots obtained using steady-state chronoamperometry (CA) or quasi-steady potential sweeping methods at low scan rates29,35–38 are often used for electrode evaluation and inter-comparison. Analogously, chronopotentiometry (CP) was also employed to compare the overpotential of electrodes at a fixed current density,39,40 which is more convenient but gives less kinetic insights compared to Tafel analysis.

To calculate the CER overpotential of a given electrode, the thermodynamic equilibrium potential of CER under standard-state conditions must be subtracted from the data obtained from the Tafel plots. The thermodynamic potential of the CER has been measured by Sohrabnejad-Eskan et al.,37 and Finke et al.39 In one study,37 the equilibrium CER potential was estimated by extrapolating the polarization curve to yield an approximate thermodynamic potential value of 1.26 V in a 5 M NaCl solution adjusted to pH = 2.  On the other hand, Finke et al.,39 determined the thermodynamic equilibrium potential of CER by pre-saturating a 5 M NaCl solution with 1.0 atm Cl2(g) while controlling the pH at 2.  Under these conditions, a thermodynamic potential was determined as 1.288 V at 25 °C. In the scenario of CP measurements, a concentrated NaCl electrolyte, minimized the competition from OER and changes in the thermodynamic equilibrium potential of CER by the continuous consumption of chloride ion. Saturation of the electrolyte with Cl2(g) also allows for the free chlorine fugacity to remain constant during the reaction, thereby allowing for a more reliable and precise determination of the actual thermodynamic potential.

Selectivity evaluation. Selectivity, as reflected by the FE, is often evaluated by measuring the ratio of anodically generated Cl2(g) to that of O2(g) or by comparing the generated Cl2(g) to the total charge passed. Given the 2-electron nature of the CER as opposed to the 4-electron OER, selectivity is influenced by the kinetics of both reactions at electrode surface.1

Chronopotentiometry is most often used for determination of selectivity.5,6,23,40,41 The production rate of dissolved Cl2 in solution is determined using traditional analytical methods that using N,N-diethyl-p-phenylenediamine (DPD)6,23,32 colorimetry or iodometry.40 The production rate of Cl2(g) in gas-phase can be determined using differential electrochemical mass spectroscopy (DEMS)27,42,43 or online electrochemical mass spectrometry (OLEMS),37 where O2(g) can be analyzed in parallel. It is worth noting that the formed chlorine is usually quantified by the HCl signal (m/z = 36 or 38) in mass spectrometers due to the easy breakage of Cl-Cl bond.37 Considering the evaporation from acidified chloride solution, the signal should be carefully calibrated. Due to the moderate solubility of Cl2 in water given a Henry’s law constant of 9.5 × 10-2 M atm-1 at 25 ˚C44, the partitioning of Cl2 between the aqueous and gaseous phases must be taken into account when determining the overall selectivity between Cl2 and O2. For example, a faster rate of the CER leads to a more rapid saturation of Cl2 in the aqueous phase coupled with a large fraction of Cl2 released into the gaseous phase. On the other hand, if the CER proceeds at a slower rate, a larger fraction of the evolved Cl2 will remain in the aqueous electrolyte.

Based on Henry’s law considerations, the release of Cl2(g) from acidic solution into gas phase is expected to occur regardless of its aqueous-phase concentration. However, the water-to-air gas transfer can be relatively slow depending on the concentration gradient near the water-air interface as well as the turbulence within the reactor. Similar concerns are relevant for large-scale CER applications. The apparent Faradaic Efficiencies obtained from measuring only the aqueous-phase Cl2 concentration could be considered sufficient for anode evaluation.  However, it should also be noted that the partitioning of Cl2 into the gas phase matters in practical applications (e.g., the chlor-alkali industry or municipal water disinfection). Thus, the partitioning of Cl2 between the gaseous and aqueous phases should be considered in calculating the electrode selectivity. Furthermore, the selectivity measurement is also influenced by a variety of experimental parameters including electrolysis time, applied current, and total electrolyte volume. As a consequence, aqueous-phase measurements are preferred in cases involving dilute chloride solutions with short electrolysis times and low currents,23 while gas-phase measurements are more suitable when concentrated chloride solutions with longer electrolysis times and larger applied currents are employed.27

The electrochemically generated chlorine may also be lost due to further anodic oxidation to chlorate (Equation 11). Different stoichiometries have been proposed by Kuhn and Mortimer,45 Rius and Llopis,46 and Jasper et al.,9 respectively. Although this reaction is valuable for chlorate production, it results in not only parasitic oxygen release in industrial chlorine production, but also chlorate formed as a toxic by-product in water treatment.6,9 The reaction is especially significant at relatively high temperature (e.g. 70 °C) and low chloride activity.45 For measurement of CER selectivity, formation of chlorate consumes a fraction of chlorine but adds to the oxygen production, leading to an underestimation of CER selectivity. Rotating ring-disk electrodes (RRDE) can be employed to mitigate the interference since it prevents the further contact of formed ClO- with the anode.47 However, it is worth noting that since this reaction is inevitable under most hydraulic conditions, evaluating the “chlorate formation corrected” CER selectivity is still reasonable for practical applications.

|  | aClO-+bH2O⇌cClO3-+dCl-+xH++yO2+ze- | (11) |
| --- | --- | --- |

Even though quantifying chlorine in only one phase may be sufficient for a rough comparison between different CER anodes, this approach will result in an underestimation of the chlorine production rate and the FE. Thus, to accurately determine the FE of CER for a given electrode formulation, measurements in both aqueous and gaseous phases should be made simultaneously to access the total yield of Cl2 (e.g., {Cl2}T  = {Cl2}aq + {Cl2}g). Uncontrolled losses in the quantification of total chlorine activity, {Cl2}T, is likely to account for some of the discrepancies in reported FEs.32,48

Apparent electrode selectivity is impacted by numerous factors other than the intrinsic properties of a specific electrode. In addition to the different electron transfer numbers and chloride concentrations, another pronounced difference lies in the different pH-dependent kinetics of the CER and OER (Equation 1 and 2). Acidification has been widely used to increase CER selectivity in chlor-alkali industry.1 This approach is also useful in tests of CER activity of electrodes to minimize the interference from the OER.39,40  In addition, anions  such as  F-, SO42-, NO3-, PO43- are also know to affect CER selectivity most likely due competitive surface binding.1 In particular, bidentate ligands have been shown to bind strongly to RTO electrode surfaces leading to a lower CER selectivity1, while F- deactivates RTO electrodes by forming TiF62-,49,50 or more likely, by replacement of surface hydroxy sites, >TiOH and >RuOH, with >TiF and >RuF, where “ > ” denotes a specific surface binding site. Thus, competitive surface complexation by F- and HSO4-, SO42- can block key surficial binding sites (e.g., >RuOH), for Cl- substitution. Furthermore, formation of radicals such as Cl2·-, ·OH, and HO2· are usually neglected in calculation of the FE due to their low steady-state concentrations, in spite of their important role in oxidative wastewater treatment.

Stability evaluation. Considering the high cost of PGMs like Ir and Ru, conventional MMO electrodes require sufficiently high catalytic activities, high FE’s, and long service lifetimes to be economically feasible for practical application. Oxidative dissolution and the growth of an insulating interlayer between the substrate and active catalyst layer are the two main deactivation mechanisms for MMO-type electrodes.14 Since conventional DSAs need to have lifetimes on the order of years, the stability of anodes is most often estimated using accelerated life tests (ALT). In a typical ALT, anodes are tested using chronopotentiometry under at high current densities in very acidic electrolytes.15,51–55 Electrode lifetime is estimated by the amount of time taken for the applied potential to exhibit a sharp increase, or to increase to a set value. Other techniques such as CV and electrochemical impedance spectroscopy (EIS) are also used along with ALT to monitor the changes in the electrochemical properties of electrode during long-term tests.15,51–58 Methods used for material characterization include scanning electron microscopy (SEM),53,54 X-ray diffraction (XRD)15,54, and X-ray photoelectron (XPS)55 to reveal microstructural and compositional changes after the electrochemical tests.

NaCl solutions are traditionally used as the electrolyte to simulate the working conditions of chlor-alkali industry.51,58 As the dissolution of PGMs has been shown to be closely correlated with the OER, sulfuric acid and perchloric acid are often used as electrolytes with concentration ranging from 0.1 N to 2 N.15,51–54,57,59 Perchlorate solutions are often used in environmental studies to better estimate electrode lifetimes in wastewater media.6,32 However, given the complicated electrolyte composition, the actual service lifetimes of electrodes used in wastewater treatment may vary substantially from the estimated lifetime by ALT. For example, organic compounds such as CH3OH, HCHO and HCOOH at concentrations as high as 0.5 M have been shown to substantially reduce the service lifetime of Ir-Ta electrodes in Na2SO4 solutions.60 These results indicate that different deactivation mechanisms are likely to co-exist for aqueous-phase species traditionally considered as unimportant in terms of CER electrode lifetime, even though the chlorine radical species may react with a wide array of organic and inorganic species in surface water, groundwater water, or wastewater. Thus, in order to fully understand the stability of electrodes in wastewater, it is necessary to fundamentally unravel the effects of different solutes as they may impact the deactivation of electrodes.

In absence of an accepted protocol to conveniently and rapidly screen electrodes, the time-intensive ALT methods of DSA-type electrodes provide a limited insight into the properties of surface catalytic sites (e.g., valence state, stoichiometry, and crystallinity) during the electrode dissolution. This is most likely due to the inhomogeneity of electrodes prepared by brush or spray coating techniques. Moreover, the loss of electrode activity may be due to a reductions in conductivity, electrochemically-active surface area (ECSA), or electrode-specific activity as measured in terms of catalytic activity per surface area. Although changes in electrode conductivity can be characterized using EIS, the conventional ALT protocol, even when coupled with CV and other characterization techniques, often fails to distinguish between the loss of ECSA and a decrease in specific activity.

To overcome inhomogeneity issues, several model electrodes based on well-defined nanostructures or nanoparticles of iridium oxide have been studied to understand its deactivation mechanism for the OER. For example, Tan et al.55 combined LSV, Tafel plots, and EIS to monitor the activity of the IrO2 anodes over time, while the dissolved Ir species in the aqueous solution were measured by inductively coupled plasma mass spectrometry (ICP-MS). Amorphous IrOx was found to have a higher catalytic activity, but lower stability compared with crystalline-phase IrO2. Tan et al.55 proposed a mechanism for Ir(III) dissolution to explain this apparent discrepancy. The deactivation of highly crystalline IrO2 was attributed to the loss in specific activity of the catalytic sites, whereas the deactivation of amorphous IrOx was due to the dissolution and loss of ECSA. In their study, the current density per geometric surface area was taken as the apparent catalytic activity summed over all catalytic sites. ECSA was determined by integral of the CV voltammograms to monitor the changes in the number of catalytic active sites. Specific activity was then quantified using the current density normalized to ECSA as determined by intermittent chronoamperometry experiments over the course of electrode deactivation. In this way, the decrease in the number of active sites and the deterioration of each site was uncoupled by the loss in ECSA and the decrease in specific activity, respectively. However, constant potential conditions were required by this approach to reasonably compare the specific activities. In conventional ALT protocols, the loss of ECSA usually leads to an increasing potential, which accelerates the changes in the specific activity of the catalytic sites.

ICP-MS measurements are used with ALT to monitor the real-time ionic leaching from electrode surfaces. However, detection and quantification of gaseous corrosion products such as RuO4(g) requires the use of online GC-MS. Electrochemical quartz crystal microbalance (EQCM) weight measurements versus time provide an alternative method to monitor dissolution of thin-film electrodes under electrochemical conditions.61–63 EQCM has been used to investigate the dissolution of various metal oxides used for the OER.64–66 Extending EQCM to research on the CER could provide additional mechanistic insight in to electrode stability under controlled operating conditions.

3. Activity & Selectivity

Various experimental factors, including electrolyte pH and composition, specific adsorption of ions, bubble formation and removal, and passivation of the substrate can influence the catalytic CER kinetics. Early studies of these factors has been comprehensively reviewed by Trasatti.21 With the advancement of fabrication and characterization techniques, more attention has been paid toward screening next-generation electrode materials with high intrinsic chemical properties. The Sabatier principle has played an important role in connecting the material properties to the CER catalytic performance.67 According to the Sabatier principle, the adsorption energy of reactive species near catalyst surfaces should be optimized to allow for facile sorption of the substrate and equally facile desorption of the product. This principle leads to the “volcano plot” relationship between catalytic activity and the surface properties of heterogenous catalysts (Figure 1 2).68 As mentioned above, the oxides of the PGMs are found near the apex of a volcano plot with RuO2 serving as the benchmark for the CER69,70 although IrO2, PtO2 and CoOx are also considered to be suitable CER catalysts.1

Figure 1. Volcano plot for CER catalysis reproduced with permission from Zeradjanin et al.68 Copyright 2012 WILEY-VCH Verlag GmbH & Co. KGaA, Weinheim. The overpotentials of CER on various catalysts at the same current density were plotted against the characteristic Raman shifts. The top of the plot marked with Cl-O represented the Raman shift of Cl-O vibration of HOCl in aqueous solution.

The CER activity of the MMO electrodes primarily relies on the use of PGMs, although Ru is most used. The effect of various metal ion dopants on the catalytic performance of RuO2 has been reviewed by Karlsson and Cornell.1 The metal dopants can be categorized into: (1) valve metals (e.g. Ti, Zr, Ta and Sn );5,34,36,43,68,71–77 (2) non-valve first-row transition metals (Zn, Co, Ni, Zn);26,42,78–85 and (3) other metals such as Ce and Mg.36,86 Iridium, which is more expensive than Ru, is often used as a dopant to prolong the service lifetime of the other PGM oxides.13,73,87–91 Valve metals are traditionally viewed as intrinsically inactive electrode stabilizers that are used solely for increasing electrode lifetimes. However, this argument has been challenged by the enhanced activities exhibited by Ti- or Sn-containing electrodes that enhance the CER selectivity of RuO2.26,77 In the case of RTO electrodes prepared by thermal deposition using homogenous precursor solutions, Ti has been shown by Rutherford backscattering spectrometry and XPS to preferentially segregate at the electrode surface to “cover” Ru sites.92 Moreover, Tafel plots were used to show that a RTO electrode made with 35 wt% RuO2 had a similar CER activity as an electrode made with 80 wt% RuO2.16 This result implies that Ti (e.g., >TiOH) also functions as catalytically active sites on the surface of RTO electrodes.

Transition metals such as Fe, Co and Ni can be incorporated into the rutile lattice of RuO2 to form a single-phase mixture,42,78,79,82,84 although Co and Ni dopants form new phases at high annealing temperatures.72,74 At an atomic percentage of  <20%, cobalt forms a single-phase binary nanocrystalline catalyst with RuO2 with a mean size of 20-60 nm that results in both enhanced OER activity and increased selectivity.84 Iron was shown to increase the OER activity and while suppressing the CER.78 Nickel was shown to be enriched at the surface upon doping into the rutile RuO2 matrix without forming a distinct phase.80 This resulted in an increase in both the CER selectivity and activity. The optimal CER selectivity was achieved at 10% Ni doping, whereas the highest activity was observed at 20% Ni doping for both CER and OER.42 In contrast, doping RuO2 with Zn and Mg formed local ilmenite structures intergrow with rutile blocks that resulted in reduction in current density in chloride electrolyte solutions.85,86 In addition, the CER selectivity of RuO2 decreased with Zn doping,83 while selectivity was increased with Mg doping.86

IrO2 has a higher CER selectivity than RuO2 in dilute chloride solutions despite its lower activity, as shown by Kuhn and Motimer.45 A conflicting result was reported by Vos and Koper using a RRDE.47 The discrepancy was partly caused by a static solution and the high temperature (70 °C) used by Kuhn and Motimer that facilitate chlorate formation. On the other hand, the differences were also attributed to the catalyst fabrication methods. The electrochemical generation of chlorine species over RuO2 and IrO2 electrodes was further examined by Yoon et al.93 under constant current condition at room temperature. Higher rates of both free chlorine and chlorate production were observed for RuO2 in dilute chloride solution. Based on the above results, RuO2 had a higher CER selectivity than IrO2, but also higher catalytic activity for hypochlorite oxidation. IrO2 may have had a higher effective CER selectivity under the experimental conditions of high temperature and hypochlorite concentration.

Ir-doping causes a shift in the selectivity of RuO2 electrodes towards the CER.94 Given that RuO2 and IrO2 with the same rutile structure and similar lattice parameters, their different electrocatalytic selectivity may be attributed to differences in electronic properties. In spite of the differences between RuO2 and IrO2 electrodes, iridium oxides have been used for the CER.47,48,95 In addition to bimetallic electrodes, electrodes containing three or more elements have also been developed in efforts to enhance electrode performance.5,74  For example, a ternary RuO2–IrO2–TiO2 electrode has been shown to have both enhanced activity and improved stability.14 However, the detailed catalytic mechanisms of ternary electrodes are poorly characterized.

The Sabatier principle also provides a semi-empirical strategy for tuning the activity of CER active anodes. For example, an ideal CER electrode should have “just right” affinity for chloride to be located at the apex of the Sabatier volcano, while the opposite should be expected for the OER in order have an electrode with high activity and selectivity for the CER. However, this may be challenging to achieve in practice considering the dynamic nature of the catalyst surface, as influenced by applied potential, solution pH, the formation of surface hydroxy groups (e.g., >MOH2+, >MOH, and >MO-) on hydrated surfaces, and the presence of competitive adsorbates or complexing ligands at electrode surface.70,96 As illustrated by the DFT calculations of Hansen et al., further complication arise due to the intertwining of the mechanisms for the OER and CER (Figure 2 3).70

Modulating the affinity toward surfaces of the target reactants and resulting products with on electrode surfaces may allow for higher efficiency CER catalysis by tuning the surface properties of the electrodes, by changing either steric or electronic factors. Steric factors include surface morphology, lattice structure, and the potential stacking of catalytically active sites.  The electronic factors include the intrinsic electronic properties of each catalytic site as reflected in the time-dependent valence states, surface charges, and surface potentials.

In terms of steric factors, the influence of surface morphology of Ru-based electrodes on their CER and OER activities has been investigated. For example, Zeradjanin et al.27 attributed improved performance of an RTO electrode in concentrated NaCl solutions to larger microscopic “cracks” as revealed by SEM, which were thought to lead to enhanced mass transport of both reactants to and products away from the active surface sites.27 Their observations were supported by the results of Trieu et al.,97 who emphasized the importance of accessible “outer surface area” for electrode activity. In related study, microscopic cracks were introduced into RuO2 by Sn doping in order to enhance OER catalytic activity by facilitating gas bubble detachment.98 Lower Ru leaching under the same applied potential profile was observed in the study as well. Chen et al. had contradictive argument that Ru0.3Sn0.7O2 electrodes with “mud-crack” morphology had compromised stability because of the electrolyte penetrating the cracks to oxidize the Ti substrate, based on the L-edge XAS spectra.99 However, control experiments with compact-morphological samples are needed to solidify the conclusion. They also reported comparable CER activity of crack-free electrodes compared to the “mud-crack” ones. The discrepancy in activity in the two studies might be due to the different techniques used. High-performance CER catalysis has been achieved using “superaerophobic” nanoarray-structured RTO electrodes that repelled gas bubbles and had fast product detachment.34 In contrast, lowered CER selectivity and a decrease in overall activity with Zn-doped RuO2 was attributed to the formation of inclusions ilmenite-like structures.83,85

Modification of catalytic surfaces at the nano or atomic scale is limited by available fabrication methods and a lack of understanding the mechanistic details of the CER. On the other hand, there appears to be a relationship between CER catalytic activity and the rutile crystal structure, as shown in the cases of RuO2, IrO2, PtO2, RTO, and RuO2-IrO2-TiO2 anodes. In addition to the PGM-based anodes, a series of transition metal antimonate catalysts with rutile structures (MSbOx, M = Ni, Co, Mn) have been shown to have high activity and stability for both the OER and CER in acidic electrolytes.40,100 These results suggest that the crystal structures and crystalline facets may have an intrinsic influence on CER catalysis. For example, the different crystal facets of RuO2 have substantially different OER catalytic activities.101 Additional experimental and computational studies need to be focused on resolving the effects of both crystal structure and specific crystalline facet for catalysts that have polymorphs such as PbO2 and MnO2.

Figure 2. (a) Computational Sabatier volcano plots for CER and OER catalysis over the rutile (110) facet adapted with permission from the PCCP Owner Societies from Hansen et al.70 Copyright 2010 Royal Society of Chemistry. Black dotted lines denote the overpotential as a function of material descriptor 𝛥E(Oc) for CER mediated by ClOc, Cl(Oc)2 and Clc (from left to right), while dashed blue lines marked the calculated volcano plot for OER. The domains of the most stable surface structure as function of potential and oxygen binding energy (details shown in (b)) is marked by gray. To be truly active, the intermediate should form at sites that are stable, as this makes the active site abundant. The solid black line shows the combined Sabatier volcano taking into account the stability of the active sites for a given mechanism. The activity of IrO2 and RuO2 are indicated with error bars derived from the variation of the Oc adsorption energy with varying Oc coverage.

In comparison to steric factor, modification of the electronic valance state of the catalytic sites may lead to an improved mechanistic understanding of the catalytic activity for both the PGM oxides and MMO electrodes. Mozota et al. noted that cyclic-voltammetry pretreated Ir and Ru electrodes showed substantially higher CER catalytic activity.102 The authors argued that it was due to a change in oxidation state of surface Ir and Ru atoms. XPS analyses together with DFT calculations suggest that the higher OER catalytic activity of amorphous hydrous IrOx is due to the existence of Ir(III/IV) mixed valence states compared to rutile IrO2.103  Furthermore, the activity of RTO electrodes has been correlated with valence change of metals as studied by Finke et al.39 via atomic layer deposition (ALD) and by Näslund et al.104 via scanning electrochemical microscopy (SECM), respectively. In both studies, the authors attributed the higher observed electrochemical activity of RTO electrodes compared to pure RuO2 to decreases in the XPS binding energy (BE) of Ti 2p states (Figure 3 4). These results suggested the presence of a partially reduced Ti state within the binary RTO matrix. Also, an increase in the BE of Ru 3d as observed by Näslund et al., implied a more oxidized state of Ru that resulted from electron polarization within the “RuOx𝛿+-TiOx𝛿-” matrix that in turn could account for the enhanced activity of RTO electrodes. Näslund et al., favored RuOx𝛿+ as the catalytically active site, while Finke et al., favored TiOx𝛿- as the primary catalytically active site. Negative shifts in the BE of the XPS peak for TiOx in the Ti-Ir mixture were observed by Finke et al.39, while Yang et al,6 indicated that the electronic interaction of the metals may contribute to the catalytic activity of conventional DSAs. The electronic interaction indicates that Ti plays a more active role in CER catalysis than simply serving as an inactive stabilizer in MMO electrodes. Although TiO2 is a wide band-gap semiconductor with low conductivity in its normal state, when it is partially reduced to a lower valence state (e.g. Ti3+) it becomes an active CER and OER.23,105 Photochemical studies also show similar effects are achieved by doping aliovalent atoms in to the TiO2 lattice (Figure 4 5).106 It is quite clear both electrochemically and photochemically that TiOx𝛿- serves as an active catalytic center. Partially reduced Ti as induced by doping rather than by chemical reduction, also leads to improved electrode stability. Valence tuning as observed for Ti has also been observed for Sn and Nb oxides that are doped with Ru, Sb or N (Figure 3 4) in the TiO2 structure.107–109

Although well-known and extensively used in photocatalysis, the strategy of valence tuning should be further explored in electrochemistry. Questions that remain to be answered include: 1) does partially reduced TiOx really serve as an active site in RTO electrodes; 2) can other non-PGM elements also lead to the partial reduction of TiOx; and 3) does valence tuning activate other valve metals for CER catalysis. Activating valve metals by valence tuning may be a promising route for future developments of CER electrodes with increased stability as well as reduced electrode costs.

Figure 3. XPS spectra of valence-tuned valve metals. (a) Ti 2p XPS peak displacement after Ru doping adapted from Näslund et al.104 Copyright 2013 American Chemical Society. The XPS spectra correspond to pure RuO2, Ru0.5Ti0.5O2, Ru0.3Ti0.7O2 and pure TiO2 from top to bottom. (b) Ti 2p XPS peak evolution during TiO2 ALD on RuO2 surface adapted from Finke et al.39 Copyright 2019 Royal Society of Chemistry. Deposited TiO2 with low cycle numbers had core-level peaks agreeing to that of Ti3+, while 100-cycle TiO2 produced XPS signal of bulk TiO2. This clearly showed that the valence tuning effect of TiO2 is limited to a certain range. (c) Sn 3d XPS spectra of Sn3N4 and N-doped SnO2 prepared by annealing Sn3N4 at different temperatures adapted from Pan et al.107 Copyright 2012 Springer. N doping led to significant Sn 3d peak shift towards low BE. (d) XPS spectra of SnO2 doped with different levels of Sb adapted from Babar et al.108 Copyright 2010 Elsevier. Sb doping led to shift of Sn 3d XPS peaks towards high BE. (e) Nb 3d XPS spectra of Ru-Nb/Al2O3 catalysts adapted from Jeon et al.109 Copyright 2018 Elsevier. Numbers in the parentheses refer to different Nb/Ru molar ratios.

Developing new CER catalysts with both improved activity and selectivity requires an in-depth understanding of the CER catalytic mechanism	. Given the limited number of in situ spectroscopic tools for probing reaction intermediates, DFT calculations can be a useful guiding tool for understanding catalytic processes at the atomic level. Most often, the computational studies of the CER have focused primarily on rutile systems, especially on RuO2. The classical CER mechanisms based on kinetic studies, include the Volmer-Tafel mechanism:

|  | 2*+2Cl-→2Cl*+2e- | (12) |
| --- | --- | --- |
|  | 2Cl*→2*+Cl2 | (13) |

the Volmer–Heyrovsky mechanism:

|  | *+Cl-→Cl*+e- | (14) |
| --- | --- | --- |
|  | Cl*+Cl-→*+Cl2+e- | (15) |

and the Krishtalik mechanism:

|  | *+Cl-→Cl*+e- | (16) |
| --- | --- | --- |
|  | Cl*→Cl*++e- | (17) |
|  | Cl*++Cl-→*+Cl2 | (18) |

where * denotes an active catalytic site, which can be either a surface bound oxygen atom or a metal atom. The Volmer-Tafel mechanism consists of the initial binding of active sites with aqueous chloride (Equation 12, 14 and 16, denoted as the Volmer step) followed by combination of two adjacent adsorbed chlorine atoms into molecular chlorine (Equation 13, denoted as the Tafel step). The Volmer–Heyrovsky mechanism consists of a similar Volmer step but invokes consecutive adsorption of another Cl- and release of Cl2 (Equation 1415, which is known as Heyrovsky step). The Krishtalik mechanism differs from Volmer–Heyrovsky mechanism in the adsorption of the second chloride, while the Volmer–Heyrovsky mechanism assumes a concomitant electron transfer.  Only one active site is needed for either the Volmer–Heyrovsky or the Krishtalik mechanisms, while two active sites are required for the Volmer-Tafel mechanism.

Even though the above mechanisms provide simple two or three elementary reaction pathways for the CER, they do not explicitly define the specific nature of the active catalytic sites. DFT calculations were first applied to the study of the catalytic oxidation of HCl in gas-phase (i.e., the Deacon process) to provide a fundamental basis to interpret experimental results in light of a sequence of elementary steps.110,111 Hansen et al. used DFT calculations to investigate the room-temperature aqueous phase CER over the (110) facet of the rutile phases of RuO2 and IrO2.70 Surface Pourbaix diagrams of RuO2 (110) and IrO2 (110) were constructed based on the adsorption free energies of the various possible reaction intermediates. The formation energy of surface oxygen, 𝛥E(Oc) was proposed as a universal “descriptor” because of its linear relationship with to the different chlorine-containing intermediates, where the superscript (c) denotes a coordinatively unsaturated site (CUS). Hansen et al. established the ground work for a series of follow-up investigations that improved the thermodynamic computational results by considering the effects of the solvent,112 bridging lattice oxygen atoms,113 overpotential,114 and the uncertainties involved in DFT calculations.96

It should be emphasized that the use of a specific descriptor, such as 𝛥E(Oc), significantly generalizes the calculational results leading to identification of different CER mechanisms based on the computed values of 𝛥E(Oc). According to Hansen et al.,70 Sumaria et al.96 and Exner et al.,113 the Volmer-Heyrovsky mechanism was identified as the favored CER mechanism over the rutile (110) surfaces of RuO2, IrO2, TiO2, SnO2, PtO2 and RhO2.  The reaction intermediates varied in the order of ClOc → Cl(Oc)2 → Clc with increasing 𝛥E(Oc). Thus, the CER is predicted to be mediated by the ClOc species on IrO2 and RuO2 and by Clc on TiO2 under the conditions of T = 298.15 K, pH = 0, and aCl- = 1.70,115 Karlsson et al., also used thermodynamic calculations to shed light on the activity and selectivity of rutile-structured RTO electrodes.115 𝛥E(Oc) of TiO2 was found to decrease with Ru doping, which lowered the thermodynamic energy barrier for the CER, thus enhancing CER activity. Furthermore, the shift of the 𝛥E(Oc) also resulted in a higher thermodynamic barrier for the OER than for the CER by 0.4 eV resulting in an enhanced CER selectivity. On the other hand, 𝛥E(Oc) of RuO2 was changed slightly upon Ti doping. The computational study by Karlsson et al. suggests that TiOx in RTO electrodes functions as catalytic active centers. Exner et al.116 found that coating of a TiO2 monolayer on top of RuO2 lowered the formation energy of the ClOc intermediate, but raised the formation energy for OER intermediate OOHc. These two opposing effects enhanced both the catalytic activity and selectivity of the CER.116 The conclusions above rely on the assumption that the energy barriers for CER and OER are well represented by the ΔG0f of the ClOc and OOHc intermediates, which are, in turn, linearly related to 𝛥E(Oc). Even though the Brønsted−Evans−Polanyi principle argues that activation energy barriers are linearly related to the corresponding reaction enthalpies, Exner et al. stated that this principle only applies to the Volmer step in the CER, and that the overall energy barrier, as dictated by kinetic energy barrier of Heyrovsky step, may be inversely related to the free energy of ClOc.117 However, postulation of a reaction mechanisms based thermodynamic calculations, may lead to large uncertainties in the prediction of catalytic activity as pointed out by Sumaria et al.96 Besides the uncertainties caused by DFT calculations, a lack of knowledge about the pre-exponential factor in Arrhenius equation may be another contributor to the large error in kinetics computation.118 Thus, further kinetic studies are needed to fully understand the activity and selectivity of CER electrodes. It should also be noted that hydrolysis of surface >M-O-M< sites into >MOH112,119,120 and the amphoteric behavior of the >MOH sites also leads to the protonated and deprotonated surface species  >MOH2+ and >MO-. These important surface sites in aqueous electrochemistry are often overlooked or ignored in computational studies. In addition, as pointed out by Ooka et al., there are also various other important factors that current DFT calculations have failed to fully account for, including the influence of the electrolyte, crystal defects, mass transfer limitation, and charged reaction intermediates.67 All of these contribute to the gap between computational and experimental results.

Relatively few studies have been focused exclusively on the CER selectivity of MMO electrodes. Most studies of the chlor-alkali process employ high chloride activities and low pH, which leads to conditions for a highly selective CER. Other non-OER O2-contributing reactions have also been identified.1 These factors make CER selectivity over OER not very interesting under chlor-alkali conditions. However, it is impractical to manipulate either pH or {Cl-} in water or wastewater treatment applications. Typical chloride concentration are ~30 mM in domestic wastewater with pH ranging from 6 to 8.6 Thus for onsite wastewater treatment applications, CER selectivity plays a crucial role in determining performance and energy efficiency. Similar limitations are present in the case of electrochemical surface water treatment. CER selectivity is also a key parameter in seawater electrolysis for Cl2 production considering that the average pH of seawater is8.3) with lower [Cl-] = 0.5 M than employed in the chlor-alkali industry.

The competitive mechanisms underlying the CER and OER present challenges for developing CER-selective electrodes for use given the conditions encountered wastewater and sea water. In this regard, several experimental efforts to tune the CER selectivity have been made by doping of RuO2 or IrO2. Cu, Ni, and Mg doping were shown to increase CER selectivity of RuO2.42,86,121 The effects of Cu doping were attributed to the reduction in binding energy of OER-related intermediates (e.g., HOc, Oc, HOOc), resulting in larger OER overpotentials.121 However. the effects of Ni and Mg doping are not fully understood. Ni doping enhances the CER selectivity of IrO2, while Co and Zn doping shift the selectivity towards OER.122

Multi-layer electrodes containing an Ir0.7Ta0.3Ox active layer coupled with mixed metal oxide coatings of Sn, Bi, Ti and Co oxides have been developed for electrochemical water and wastewater treatment, trace organic contaminant remediation, and for the oxidation of the toxic form of arsenic, arsenite, to arsenate.6,7,9–12,32,123,124 The coated MMO electrodes were shown to have a higher CER selectivity compared to uncoated Ir0.7Ta0.3Ox electrodes.6,32

An atomically dispersed Pt-N4 catalyst doped on to carbon nanotubes was reported to have both a higher CER activity and better selectivity compared to commercially available DSA electrodes.125 The Pt-N4 catalyst maintained a CER selectivity > 95% in a pH neutral 0.1 M NaCl electrolyte.  The high selectivity was ascribed to the active role of the intermediate Clc instead of the more commonly identified ClOc intermediate for IrO2 and RuO2. In spite of the high activity and selectivity of Pt-N4 on CNTs, practical applications may be limited due to the small particle size of the Pt-N4/CNT hybrid material and concerns over its long-term stability.

DFT calculations and 𝛥E(Oc) values as a material descriptor should be used to provide insight for rationally designing CER-selective electrodes. Based on the different slopes of CER and OER volcano plots, a 𝛥E(Oc) of ∼ 3.2 eV appears to be a critical point that produces the largest difference in the thermodynamic barrier between the OER and CER and thus result in the highest CER selectivity as discussed by Karlsson et al.115 On the other hand, Exner119 proposed that (𝛥E(OOHc) - 𝛥E(ClOc)) provides another useful material descriptor for screening of materials for CER selectivity and electrode stability. Of course, other factors including steric effects, crystal defects, and crystalline imperfections may also be key factors. Therefore, an improved understanding of the catalytic mechanism leading to the CER is crucial step toward future developments of CER-selective anodes.

Figure 4. Schematic illustration of influence of aliovalent metal dopants on the TiO2, adapted from Takata and Domen.106 Copyright 2009 American Chemical Society. It is generally believed that to maintain charge neutrality, (a) lower-valence dopants induce oxygen vacancies while (b) higher-valence dopants induce reduced Ti3+ species.

4. Surface Chemistry of CER on RuO2, IrO2, RTO, and Other MMO Electrodes

In spite of the computational studies have identified the catalytic sites in rutile RuO2 systems for the CER, there is still a gap between the computational and experimental results since the catalyst surface properties are rarely considered. Metal oxides such as TiO2 form surface hydroxy groups upon exposure to water or humid air.126–128 The same basic surface chemistry also applies to the hydration of RuO2, IrO2, and SnO2.129–132

Surface ‘titanol’ groups (>TiOH) are formed upon exposure of anhydrous TiO2 to water or humid air. Analogous hydrolysis reactions for SiO2 or Al2O3 result in the formation of surface silanol ((>SiOH) and aluminol (>AlOH) groups. Surface titanol groups, >TiOH, have surface concentrations ranging from 3 and 6 hydroxyl groups per nm2,133 up to a total of 17 groups per nm2.134–138

Surface hydroxy groups are amphoteric such that the >TiOH surface groups undergo protonation and deprotonation depending on pH. A hydrated TiO2 surface has four distinctly identifiable surface species that include >TiOH2+, >TiOH, and >TiO- and bridging >Ti-O-Ti< groups. In water, these primary surface species dominate surface charges compared to oxygen or cation vacancies. The balancing of charges on the TiO2 surface is established when [>TiOH2+]s = [>TiO-]s.  The charge-balanced state is experimentally determined by measurement of the “pH of zero point of charge” (pHzpc) or by determination of the “iso-electric point” (IEP).135,139 The pHzpc is the experimentally-determined pH at which the activity of the positively charged titanol groups {>TiOH2+} is balanced by the activity of negatively charged group {>TiO-}. This equivalency leads to a net zero surface charge that is approximately equal to what is obtained at the isoelectric point.139 Adsorption of organic or inorganic ligands (e.g., Cl-) to TiO2 thus occurs in part via inner-sphere ligand substitution of surface hydroxy groups (e.g., >TiOH) as a function of pH.140,141 Inner-sphere coordination of formate and acetate on TiO2 over the pH range of 3 to 9 on the rutile (110) surface has been fully characterized.142

The surface adsorption of formate and acetate on rutile is analogous to the formation of a metal-ligand complexes in aqueous solution via a conventional ligand substitution reaction:

|  | >TiOH+HCOOH⇌TiO2CH+H2O | (1819) |
| --- | --- | --- |
|  | >TiOH+HCO2-⇌TiO2CH+OH- | (1920) |

The surface chemistries of MMO electrodes are dominated by their corresponding surface hydroxy groups (e.g., >RuOH + Cl- + H+ ⇌ >RuCl + H2O; >IrOH + Cl- + H+ ⇌ IrCl + H2O; and >TiOH + Cl- + H+ ⇌  >TiCl  + H2O). The pHzpc or IEP values for TiO2, IrO2, and RuO2 in the rutile phases are 5.8, 3.0, and 5.8, respectively.130–132,143 Kleijn and Lyklema reported that the pHzpc of colloidal RuO2 was 5.75 in a KNO3 solution, while the IEP was determined to occur at pH 5.8.131,132 However, in KCl solutions, the pHzpc and the IEP shifted to higher and lower values, respectively.  This shift was attributed to the specific adsorption (i.e., surface complexation) of Cl-.132

Given constraints imposed by the pHzpc or IEP values, the primary surface species at pH < 3 for RuO2 and IrO2 in an aqueous electrolyte (e.g., NaCl) will be >RuOH2+, >RuOH, >IrOH2+ and >IrOH.  Considering the strong evidence for Cl- adsorption via ligand substitution, a more detailed CER mechanism than that given by the legacy mechanisms of Equation 12-18 should take place at specific surface sites as follows in the case of RuO2:

|  | >RuOH2+⇌ >RuOH+H+ (pKa1,surf) | (21) |
| --- | --- | --- |
|  | >RuOH⇌ >RuO-+H+ (pKa2,surf) | (22) |

where the pHzpc = (pKa1,surf + pKa2,surf)/2.  Thus, for RuO2 and IrO2, the net zero charge surfaces are given defined by pHzpc = 5.75 and pHzpc = 3.0, respectively. Thus, in an NaCl electrolyte, the following CER surface reactions will take place at an applied potential (Eapp) or by UV irradiation at energies greater than the band gap, Eg, which is 2.7 eV for hydrous RuO2:

|  | >RuIVOH2++Cl-⇌ >RuIVCl+H2O | (23) |
| --- | --- | --- |
|  | >RuIVOH+Cl-+H+⇌ >RuIVCl+H2O | (24) |
|  | >RuIVCl+H2O+Eapp⇌ >RuIIIOH2+Cl· | (25) |
|  | Cl·+Cl-⇌ Cl2·- | (26) |
|  | 2Cl·⇌ Cl2 | (27) |
|  | >RuIVOH+Cl2·-⇌ >RuIIIOH-+Cl2 | (28) |
|  | 2>RuIIIOH-+Eapp⇌ 2>RuIVOH | (29) |
|  | 2>RuIVOH+2H+⇌ 2>RuIVOH2+ | (30) |

For two adjacent hydroxylated surface sites under an applied potential, Eapp,

|  | 2>RuIVCl+2H2O+Eapp⇌ 2>RuIVOH2+Cl2 | (31) |
| --- | --- | --- |
|  | 2>RuIIIOH2+Eapp⇌ 2>RuIVOH2+ | (32) |

Additional CER pathways may also involve ion pair formation close to the positively charged surfaces at pH < 3, coupled with a high concentration of Cl- within the electrical double layer (EDL). In this case, surface bound hydroxyl radical is generated by the first electron transfer step in the OER.

|  | >RuIVOH2++Cl-⇌ >RuIVOH2+:Cl- | (33) |
| --- | --- | --- |
|  | >RuIVOH+Eapp⇌ >RuIVOH· | (34) |
|  | >RuIVOH∙+ H2O⇌ >RuIVOH2+ ∙OH | (35) |
|  | >RuIVOH2+:Cl-+ ·OH⇌ >RuIVOH2++Cl·+ OH- | (36) |

A similar sequence of reactions will take place on each metal oxide surface of an MMO anode or on the surface of an individual metal oxide. In addition to the alternative CER mechanism proposed herein, we must also consider the total charge on anode surface, the surface potential under a given applied potential, and the ionic strength of the electrolyte. These factors will affect the thickness or shape of the EDL and near anode surface concentration of chloride relative to its bulk water phase concentration. Equation 23 is a ligand substitution reaction involving the surface complexation of Cl- and the displacement of water from the specific surface site >RuOH2+. This initial step in the CER mechanism can be described in terms of the following equilibrium constant for a charged RuO2 surface reaction with a complexing ligand:

|  | KappS=KintSexp⁡(-FΨ/RT) | (37) |
| --- | --- | --- |

where Ksapp and Ksint are the apparent and intrinsic constants for complexation of Cl- at a protonated surface ‘rutinol’ site (i.e., >RuOH + H+ ⇌ >RuOH2+). Equation 37 arises from a consideration of the total ΔGo for formation of the surface complex, which takes into account both the chemical and electrical contributions to the total complexation/sorption energy (e.g., ΔGotot = ΔGoint + ΔGocoul) where ΔGoint is the chemical term and ΔGocoul is the electrostatic or coulombic term. This can be expressed as follows:

|  | ΔGtoto=ΔGinto+ΔzFΨ | (38) |
| --- | --- | --- |

where Ψ is the surface potential and Δz is the change in charge of the surface complex species. Identical treatments apply to the surface acidity constants (e.g., pKsa1 and pKsa2, vide supra) and each subsequent step in the above reaction mechanism. Detailed treatments of metal oxide surface complexation and sorption thermodynamics have been presented by Stumm and Morgan,144 Dzombak and Morel,145 Schindler and Stumm,146 Rodriquez et al.147 and Faust et al.148

5. Stability of CER catalysts

Deactivation of conventional DSA’s such as the MMO, RTO, RuO2-IrO2-TiO2 anodes, involves dissolution of the PGM elements and growth of insulating TiO2 layers between the catalytic coating and Ti substrate.14 Similar deactivation mechanism was also found for OER in proton exchange membrane electrolyzers, and it is important to examine both processes to gain mechanistic insights into electrode stability.149 Dissolution of Ru and Ir is predicted given the predictions of the corresponding Pourbaix diagrams at pH < 2.  For example, RuO2 and IrO2 under typical applied potentials for the chlor-alkali or electrochemical oxidation processes at pH < 2 are likely to form RuO4 and IrO4-, respectively.150 Both Ir(VIII) and Ru(VIII) oxides are highly unstable. The electrochemically oxidized amorphous oxides are reported to have substantially higher dissolution rates compared to their crystalline counterparts. However, some of the amorphous oxides have been shown to have higher OER catalytic activities.55,59,151 For example, the dissolution of RuO2 was found to be transformed into RuO2(OH)2 and RuO3(OH) before forming RuO4. Amorphous hydrated oxides including RuO2(OH) and RuO2(OH)2 were identified as reaction intermediates in the OER.152 In a similar fashion, IrO2(OH) is predicted to form on the surface of IrO2. IrVO2(OH) forms IrIII(OH)3 at low applied potentials and IrVIO3 at high applied potentials.153 Additionally, Ir(V)- Ir(III) and Ir(V)-Ir(VI) were identified as two distinct pathways for Ir dissolution, both of which contributed to the OER catalytic activity.154 Analogously, crystal defects of Pt electrodes were also reported to have higher catalytic activity.155 However, in the case of crystalline RuO2, the OER catalytic activity of different crystalline facets did not establish a clear correlation between catalytic activity and stability.101 This again highlighted the necessity of unraveling the influence of crystal facets for the overall CER catalytic performance of MMO electrodes beyond pure RuO2 electrodes. In addition to OER-related dissolution under constant potential conditions, transient dissolution triggered by electrochemical modification of the Ru valence state also leads to dissolution of Ru even when the applied potential is lower than the OER potential.151

High chloride activity and low pH conditions favor the CER and they also extend anode lifetimes by suppressing the OER. However, the lifetime of electrodes in low ionic strength and circum-neutral pH wastewater can be impacted by more favorable conditions for the OER. On the other hand, the evolution of anode selectivity during deactivation is unclear for either the RuO2/IrO2 or MMO anodes. For example, the deactivation of IrOx may involve the deterioration of IrOx surface sites even before their dissolution as suggested by Tan et al.55 The loss of catalytic activity may be due to changes in the surface crystalline structure and the extent of surface hydroxylation, which may also influence CER selectivity. Experimentally, the evolution in selectivity over time can be monitored over time using an RRDE47 or DEMS.42,43

The stability of the PGM oxides is enhanced by mixing in acid-resistive valve metals including Ti, Zr, Nb, Ta, and Sn.156 The valve metals also influence the deactivation mechanism of electrodes. The deactivation of conventional MMO anodes begins with dissolution of surface active Ru or Ir, followed by the electrolyte or the products penetrating the coating layer to reach the Ti base metal.14 Furthermore, electrode fabrication using thermal deposition methods also complicates the deactivation process by forming microscopically inhomogeneous surfaces, which allows for the electrolyte to penetrate via surface cracks and then through the deposited MMO layers. At the same time, deactivation of catalytic sites and loss of specific activity may accompany the dissolution of active components (loss of ECSA) as pointed out by Tan et al.55 For example, the dissolution of Ru reduces the intensity of localized electron polarization effects such as RuOx𝛿+-TiOx𝛿- and further decreases the electrode activity., which has rarely been studied so far. Along with the loss of ECSA, future research should focus more closely on the evolution of catalytic sites during the electrode deactivation process. In addition, the adhesion of Cl2(g) bubbles has been shown to lead to a gradual delamination of deposited thin-film catalysts resulting in a reduction in electrode stability. Nano-structuring of electrode surfaces can serve as an effective strategy for modulating electrode surface affinity for Cl2(g) bubbles.34

6. PGM-free CER electrodes

High prices and limited availability of the PGMs constrains their use in large-scale applications as electrodes. Therefore, alternative electrode materials are being explored for use in CER catalysis (Figure 5 6). Suitable metals have been used primarily as dopants to enhance the performance of the PGM-based electrodes. Consequently, PGM-free electrodes are rarely used on a large scale due to either their instability or lower catalytic activity. For example, Co-based catalysts have shown moderate activity despite concerns over their stability due to anodic dissolution. In the past, Co3O4 was used as an active catalytic layer in chlor-alkali industry due to its high selectivity for CER.1,157 However, Co3O4 nanobelt array electrodes that were synthesized by hydrothermal methods have been shown to have a comparable catalytic CER activity to that of RuO2. With respect to the OER, Co3O4 in KOH solutions is reported to be a good catalyst.158 The surprising performance of Co3O4 nanobelt array electrode is attributed to its nanobelt morphology and its high surface area. Co-N-C nanocluster catalysts synthesized by pyrolyzing a Co-oxime complex were reported to be bifunctional catalysts for both anodic CER and cathodic oxygen reduction reactions (ORR) with catalytic activities superior to that of a RuO2/TiO2 electrode in 0.4 M HCl solution.159 In addition to suitable catalytic activity, improved stability was observed for the Co3O4 nanobelt array electrodes compared to pure RuO2 electrodes in side-by side chronoamperometry tests. While the Co-N-C electrodes were stable for at least 30 days at 1.2 V vs. RHE in 5 M HCl, additional performance benchmarks are needed to compare it with the state-of-art RTO or RuO2-IrO2-TiO2 ternary oxide electrodes. Lead oxide (PbO2) has also been used for CER catalysis, but it is limited by high overpotentials and the reductive leaching of Pb2+ ions under open circuit conditions.160–162

Antimonates have been shown to inhibit the anodic dissolution of Co, Ni and Mn oxides in acidic solutions.40,100 Antimonate catalysts have been synthesized by co-sputtering of metal alloys followed by thermal oxidation to produce crystalline CoSb2Ox and MnSb2Ox, which more stable than RTO electrodes for CER in acidified and concentrated NaCl solutions inspite of their higher overpotentials.40 Other antimonates have also been used as acid-stable OER catalysts.100 Thus, it appears possible to stabilize the catalytically active metals (e.g., Co, Mn, Ni) through the formation of stable crystalline phases by alloying with other elements like Sb. However, given its altered composition and lattice structure, the catalytic mechanism of antimonate catalysts may differ from that of pure CoOx.  In the case of amorphous CoSb2O6163, formation of Co(IV) sites and oxygen vacancies appear to be responsible for the OER catalytic activity However, formation of oxygen vacancies were not observed in crystalline CoSb2O6.

Figure 5. Timeframes for the use of metals in DSA electrodes for CER catalysis.

Defective TiOx nanotubes have also been used for CER catalysis.23,105 The TiO2 nanotubes are prepared by anodization of Ti-metal sheets or Ti-metal foil in a fluoride electrolyte. Oxygen vacancies and Ti+(4-x) species are introduced into the TiO2 lattice by either electrochemical cathodization or thermal hydrogen reduction. The reduced Ti-nanotube array electrodes have been shown to have comparable CER selectivity with commercially available DSAs. The  anodic stability of reduced TiO2 is substantially improved by selective Co3+ doping105 or by a spray pyrolysis deposition of a thin TiO2 “superficial skin” layer.23

The rational design of novel PGM-free catalysts remains a challenge due to a poor understanding of the detailed CER mechanism for non-rutile systems. For the non-PGM catalysts studied so far, the multivalent capability of Co and the non-stoichiometric nature of Ti(IV)/Ti(III) nanotubes have present an additional challenge to resolve the catalytic CER and OER mechanisms over a broad range of pH. Computational chemistry should be focused on transition metal antimonate systems in order to validate the applicability of 𝛥E(Oc) as an appropriate material descriptor for the synthesis of PGM-free DSAs.

7. Future outlook

The wide application of the CER in the chlor-alkali industry and water and wastewater treatment should motivate the development of alternative anodes that are active, selective, and stable for CER catalysis. Cross-comparisons among different studies require evaluation of CER catalytic performance under a consistent set of testing conditions. Quantitative evaluation of CER activity, as characterized by overpotential, requires Tafel analyses under CER-favorable conditions such as those presented by concentrated and highly acidic chloride solutions. Saturating the electrolyte with chlorine gas is necessary for a stable thermodynamic CER potential determination. Moreover, accurate measurements of CER selectivity, as characterized by FE, require quantification of all produced chlorine species in both the gaseous and aqueous phases. Even though ALT procedures have been extensively used to estimate the lifetime of CER anodes, a detailed characterization of the evolution of catalytic sites over electrolysis timeframes are needed to unravel the deactivation mechanisms of MMO electrodes.

To develop more efficient and stable CER anodes, we suggest that future studies focus on the following aspects:

- Resolving the effects of both crystal structure and specific crystalline facet for performance of catalysts that have multiple polymorphs, such as PbO2 and MnO2.

- Understanding the catalytic sites in RTO electrodes and the effects of “RuOx𝛿+-TiOx𝛿-” electron polarization and extrapolating the model to other valve metals.

- Studying the deterioration of catalytic sites and loss of specific activity during the deactivation of MMO electrodes, especially with the electron polarization effects in consideration.

- Extending the computational chemistry method from rutile RuO2 to trirutile transition metal antimonate systems to unveil their catalytic sites.

Despite the knowledge about catalytic sites, unraveling CER kinetics requires the development of in situ material characterization techniques and more sophisticated computational models that consider the solvent environment, charged catalyst surfaces, crystal defects, and mass transport.

References:

(1) 	Karlsson, R. K. B.; Cornell, A. Selectivity between Oxygen and Chlorine Evolution in the Chlor-Alkali and Chlorate Processes. Chem. Rev. 2016, 116 (5), 2982–3028. https://doi.org/10.1021/acs.chemrev.5b00389.

(2) 	Chadwick, S. S. Ullmann’s Encyclopedia of Industrial Chemistry. Reference Services Review 1988, 16 (4), 31–34. https://doi.org/10.1108/eb049034.

(3) 	Spagnoletto, G. Innovation in Food Grade Hypochlorination Generation and Injection Plant at Al Taweelah Site. Desalination 2005, 182 (1–3), 259–265. https://doi.org/10.1016/j.desal.2005.04.016.

(4) 	Jeong, H. J.; Kim, H. R.; Kim, K. I.; Kim, K. Y.; Park, K. H.; Kim, S. T.; Yoo, Y. D.; Song, J. Y.; Kim, J. S.; Seong, K. A.; et al. NaOCl Produced by Electrolysis of Natural Seawater as a Potential Method to Control Marine Red-Tide Dinoflagellates. Phycologia 2002, 41 (6), 643–656. https://doi.org/10.2216/i0031-8884-41-6-643.1.

(5) 	Chen, S.; Zheng, Y.; Wang, S.; Chen, X. Ti/RuO2–Sb2O5–SnO2 Electrodes for Chlorine Evolution from Seawater. Chemical Engineering Journal 2011, 172 (1), 47–51. https://doi.org/10.1016/j.cej.2011.05.059.

(6) 	Yang, Y.; Shin, J.; Jasper, J. T.; Hoffmann, M. R. Multilayer Heterojunction Anodes for Saline Wastewater Treatment: Design Strategies and Reactive Species Generation Mechanisms. Environ. Sci. Technol. 2016, 50 (16), 8780–8787. https://doi.org/10.1021/acs.est.6b00688.

(7) 	Cho, K.; Qu, Y.; Kwon, D.; Zhang, H.; Cid, C. A.; Aryanfar, A.; Hoffmann, M. R. Effects of Anodic Potential and Chloride Ion on Overall Reactivity in Electrochemical Reactors Designed for Solar-Powered Wastewater Treatment. Environ. Sci. Technol. 2014, 48 (4), 2377–2384. https://doi.org/10.1021/es404137u.

(8) 	Yang, Y.; Lin, L.; Tse, L. K.; Dong, H.; Yu, S.; Hoffmann, M. R. Membrane-Separated Electrochemical Latrine Wastewater Treatment. Environ. Sci.: Water Res. Technol. 2019, 5 (1), 51–59. https://doi.org/10.1039/C8EW00698A.

(9) 	Jasper, J. T.; Yang, Y.; Hoffmann, M. R. Toxic Byproduct Formation during Electrochemical Treatment of Latrine Wastewater. Environ. Sci. Technol. 2017, 51 (12), 7111–7119. https://doi.org/10.1021/acs.est.7b01002.

(10) 	Cho, K.; Hoffmann, M. R. Urea Degradation by Electrochemically Generated Reactive Chlorine Species: Products and Reaction Pathways. Environ. Sci. Technol. 2014, 48 (19), 11504–11511. https://doi.org/10.1021/es5025405.

(11) 	Cho, K.; Kwon, D.; Hoffmann, M. R. Electrochemical Treatment of Human Waste Coupled with Molecular Hydrogen Production. RSC Adv. 2014, 4 (9), 4596–4608. https://doi.org/10.1039/C3RA46699J.

(12) 	Jasper, J. T.; Shafaat, O. S.; Hoffmann, M. R. Electrochemical Transformation of Trace Organic Contaminants in Latrine Wastewater. Environ. Sci. Technol. 2016, 50 (18), 10198–10208. https://doi.org/10.1021/acs.est.6b02912.

(13) 	Beer, H. B. The Invention and Industrial Development of Metal Anodes. Journal of The Electrochemical Society 1980, 127 (8), 303C. https://doi.org/10.1149/1.2130021.

(14) 	Hoseinieh, S. M.; Ashrafizadeh, F.; Maddahi, M. H. A Comparative Investigation of the Corrosion Behavior of RuO2–IrO2–TiO2 Coated Titanium Anodes in Chloride Solutions. J. Electrochem. Soc. 2010, 157 (4), E50. https://doi.org/10.1149/1.3294569.

(15) 	Liu, B.; Wang, C.; Chen, Y.; Ma, B. Electrochemical Behavior and Corrosion Mechanism of Ti/IrO2-RuO2 Anodes in Sulphuric Acid Solution. Journal of Electroanalytical Chemistry 2019, 837, 175–183. https://doi.org/10.1016/j.jelechem.2019.02.039.

(16) 	Burrows, I. R.; Denton, D. A.; Harrison, J. A. Chlorine and Oxygen Evolution on Various Compositions of RuO2/TiO2 Electrodes. Electrochimica Acta 1978, 23 (6), 493–500. https://doi.org/10.1016/0013-4686(78)85026-9.

(17) 	Yi, Z.; Kangning, C.; Wei, W.; Wang, J.; Lee, S. Effect of IrO2 Loading on RuO2–IrO2–TiO2 Anodes: A Study of Microstructure and Working Life for the Chlorine Evolution Reaction. Ceramics International 2007, 33 (6), 1087–1091. https://doi.org/10.1016/j.ceramint.2006.03.025.

(18) 	Kameyama, K.; Shohji, S.; Onoue, S.; Nishimura, K.; Yahikozawa, K.; Takasu, Y. Preparation of Ultrafine RuO2‐TiO2 Binary Oxide Particles by a Sol‐gel Process. Journal of the Electrochemical Society 1993, 140 (4), 1034.

(19) 	Comninellis, Ch.; Vercesi, G. P. Problems in DSA® Coating Deposition by Thermal Decomposition. J Appl Electrochem 1991, 21 (2), 136–142. https://doi.org/10.1007/BF01464294.

(20) 	Comninellis, Ch.; Vercesi, G. P. Characterization of DSA®-Type Oxygen Evolving Electrodes: Choice of a Coating. J Appl Electrochem 1991, 21 (4), 335–345. https://doi.org/10.1007/BF01020219.

(21) 	Trasatti, S. Progress in the Understanding of the Mechanism of Chlorine Evolution at Oxide Electrodes. Electrochimica Acta 1987, 32 (3), 369–382. https://doi.org/10.1016/0013-4686(87)85001-6.

(22) 	Conway, B. E.; Novak, D. M. Chloride Ion Adsorption Effects in the Recombination-Controlled Kinetics of Anodic Chlorine Evolution at Pt Electrodes. J. Chem. Soc., Faraday Trans. 1 1979, 75 (0), 2454. https://doi.org/10.1039/f19797502454.

(23) 	Yang, Y.; Hoffmann, M. R. Synthesis and Stabilization of Blue-Black TiO2 Nanotube Arrays for Electrochemical Oxidant Generation and Wastewater Treatment. Environ. Sci. Technol. 2016, 50 (21), 11888–11894. https://doi.org/10.1021/acs.est.6b03540.

(24) 	Cid, C. A.; Jasper, J. T.; Hoffmann, M. R. Phosphate Recovery from Human Waste via the Formation of Hydroxyapatite during Electrochemical Wastewater Treatment. ACS Sustainable Chem. Eng. 2018, 6 (3), 3135–3142. https://doi.org/10.1021/acssuschemeng.7b03155.

(25) 	Duby, P. The History of Progress in Dimensionally Stable Anodes. JoM 1993, 45 (3), 41–43.

(26) 	Tilak, B. V.; Tari, K.; Hoover, C. L. Metal Anodes and Hydrogen Cathodes: Their Activity Towards O2 Evolution and ClO3- Reduction Reactions. 1988, 135 (6), 8.

(27) 	Zeradjanin, A. R.; Menzel, N.; Schuhmann, W.; Strasser, P. On the Faradaic Selectivity and the Role of Surface Inhomogeneity during the Chlorine Evolution Reaction on Ternary Ti–Ru–Ir Mixed Metal Oxide Electrocatalysts. Phys. Chem. Chem. Phys. 2014, 16 (27), 13741–13747. https://doi.org/10.1039/C4CP00896K.

(28) 	Vos, J. G.; Liu, Z.; Speck, F. D.; Perini, N.; Fu, W.; Cherevko, S.; Koper, M. T. M. Selectivity Trends Between Oxygen Evolution and Chlorine Evolution on Iridium-Based Double Perovskites in Acidic Media. ACS Catal. 2019, 9 (9), 8561–8574. https://doi.org/10.1021/acscatal.9b01159.

(29) 	Kuo, D.-Y.; Paik, H.; Nelson, J. N.; Shen, K. M.; Schlom, D. G.; Suntivich, J. Chlorine Evolution Reaction Electrocatalysis on RuO2 (110) and IrO2 (110) Grown Using Molecular-Beam Epitaxy. J. Chem. Phys. 2019, 150 (4), 041726. https://doi.org/10.1063/1.5051429.

(30) 	Gedam, N.; Neti, N. R.; Kormunda, M.; Subrt, J.; Bakardjieva, S. Novel Lead Dioxide-Graphite-Polymer Composite Anode for Electrochemical Chlorine Generation. Electrochimica Acta 2015, 169, 109–116. https://doi.org/10.1016/j.electacta.2015.04.058.

(31) 	Cao, H.; Lu, D.; Lin, J.; Ye, Q.; Wu, J.; Zheng, G. Novel Sb-Doped Ruthenium Oxide Electrode with Ordered Nanotube Structure and Its Electrocatalytic Activity toward Chlorine Evolution. Electrochimica Acta 2013, 91, 234–239. https://doi.org/10.1016/j.electacta.2012.12.118.

(32) 	Cho, K.; Hoffmann, M. R. BixTi1xOz Functionalized Heterojunction Anode with an Enhanced Reactive Chlorine Generation Efficiency in Dilute Aqueous Solutions. Chem. Mater. 2015, 27 (6), 2224–2233. https://doi.org/10.1021/acs.chemmater.5b00376.

(33) 	Menzel, N.; Ortel, E.; Mette, K.; Kraehnert, R.; Strasser, P. Dimensionally Stable Ru/Ir/TiO2-Anodes with Tailored Mesoporosity for Efficient Electrochemical Chlorine Evolution. ACS Catal. 2013, 3 (6), 1324–1333. https://doi.org/10.1021/cs4000238.

(34) 	Jiang, M.; Wang, H.; Li, Y.; Zhang, H.; Zhang, G.; Lu, Z.; Sun, X.; Jiang, L. Superaerophobic RuO2-Based Nanostructured Electrode for High-Performance Chlorine Evolution Reaction. Small 2017, 13 (4), 1602240. https://doi.org/10.1002/smll.201602240.

(35) 	Ferro, S.; De Battisti, A. Electrocatalysis and Chlorine Evolution Reaction at Ruthenium Dioxide Deposited on Conductive Diamond. J. Phys. Chem. B 2002, 106 (9), 2249–2254. https://doi.org/10.1021/jp012195i.

(36) 	Santana, M. H. P.; De Faria, L. A. Oxygen and Chlorine Evolution on RuO2+TiO2+CeO2+Nb2O5 Mixed Oxide Electrodes. Electrochimica Acta 2006, 51 (17), 3578–3585. https://doi.org/10.1016/j.electacta.2005.09.050.

(37) 	Sohrabnejad-Eskan, I.; Goryachev, A.; Exner, K. S.; Kibler, L. A.; Hensen, E. J. M.; Hofmann, J. P.; Over, H. Temperature-Dependent Kinetic Studies of the Chlorine Evolution Reaction over RuO2 (110) Model Electrodes. ACS Catal. 2017, 7 (4), 2403–2411. https://doi.org/10.1021/acscatal.6b03415.

(38) 	Rojas, M. I.; Esplandiu, M. J.; Avalle, L. B.; Leiva, E. P. M.; Macagno, V. A. The Oxygen and Chlorine Evolution Reactions at Titanium Oxide Electrodes Modified with Platinum. Electrochimica Acta 1998, 43 (12–13), 1785–1794. https://doi.org/10.1016/S0013-4686(97)10002-0.

(39) 	Finke, C. E.; Omelchenko, S. T.; Jasper, J. T.; Lichterman, M. F.; Read, C. G.; Lewis, N. S.; Hoffmann, M. R. Enhancing the Activity of Oxygen-Evolution and Chlorine-Evolution Electrocatalysts by Atomic Layer Deposition of TiO2. Energy Environ. Sci. 2019, 12 (1), 358–365. https://doi.org/10.1039/C8EE02351D.

(40) 	Moreno-Hernandez, I. A.; Brunschwig, B. S.; Lewis, N. S. Crystalline Nickel, Cobalt, and Manganese Antimonates as Electrocatalysts for the Chlorine Evolution Reaction. Energy Environ. Sci. 2019, 12 (4), 1241–1248. https://doi.org/10.1039/C8EE03676D.

(41) 	Neodo, S.; Rosestolato, D.; Ferro, S.; De Battisti, A. On the Electrolysis of Dilute Chloride Solutions: Influence of the Electrode Material on Faradaic Efficiency for Active Chlorine, Chlorate and Perchlorate. Electrochimica Acta 2012, 80, 282–291. https://doi.org/10.1016/j.electacta.2012.07.017.

(42) 	Macounová, K.; Makarova, M.; Jirkovský, J.; Franc, J.; Krtil, P. Parallel Oxygen and Chlorine Evolution on Ru1−xNixO2−y Nanostructured Electrodes. Electrochimica Acta 2008, 53 (21), 6126–6134. https://doi.org/10.1016/j.electacta.2007.11.014.

(43) 	Palma-Goyes, R. E.; Vazquez-Arenas, J.; Ostos, C.; Manzo-Robledo, A.; Romero-Ibarra, I.; Calderón, J. A.; González, I. In Search of the Active Chlorine Species on Ti/ZrO2-RuO2-Sb2O3 Anodes Using DEMS and XPS. Electrochimica Acta 2018, 275, 265–274. https://doi.org/10.1016/j.electacta.2018.04.114.

(44) 	Lide, D. R. CRC Handbook of Chemistry and Physics: A Ready-Reference Book of Chemical and Physical Data; CRC press, 1995.

(45) 	Kuhn, A. T.; Mortimer, C. J. The Efficiency of Chlorine Evolution in Dilute Brines on Ruthenium Dioxide Electrodes. J Appl Electrochem 1972, 2 (4), 283–287. https://doi.org/10.1007/BF00615275.

(46) 	Rius, A.; Llopis, J. Sobre La Oxidacion Anodica De Los Hipocloritos Alcalinos. In Anales De Fisica y Quimica; 1945; Vol. 41, pp 1030–1053.

(47) 	Vos, J. G.; Koper, M. T. M. Measurement of Competition between Oxygen Evolution and Chlorine Evolution Using Rotating Ring-Disk Electrode Voltammetry. Journal of Electroanalytical Chemistry 2018, 819, 260–268. https://doi.org/10.1016/j.jelechem.2017.10.058.

(48) 	Chung, C. M.; Hong, S. W.; Cho, K.; Hoffmann, M. R. Degradation of Organic Compounds in Wastewater Matrix by Electrochemically Generated Reactive Chlorine Species: Kinetics and Selectivity. Catalysis Today 2018, 313, 189–195. https://doi.org/10.1016/j.cattod.2017.10.027.

(49) 	Wellington, T. C. Modern Chlor-Alkali Technology; Springer Science & Business Media, 2012; Vol. 5.

(50) 	Kelsall, G. H.; Robbins, D. J. Thermodynamics of Ti-H2O-F(-Fe) Systems at 298 K. Journal of Electroanalytical Chemistry and Interfacial Electrochemistry 1990, 283 (1–2), 135–157. https://doi.org/10.1016/0022-0728(90)87385-W.

(51) 	Hoseinieh, S. M.; Ashrafizadeh, F. Influence of Electrolyte Composition on Deactivation Mechanism of a Ti/Ru0.25Ir0.25Ti0.5O2 Electrode. Ionics 2013, 19 (1), 113–125. https://doi.org/10.1007/s11581-012-0737-5.

(52) 	Hu, J. M.; Meng, H. M.; Zhang, J. Q.; Cao, C. N. Degradation Mechanism of Long Service Life Ti/IrO2–Ta2O5 Oxide Anodes in Sulphuric Acid. Corrosion Science 2002, 44 (8), 1655–1668. https://doi.org/10.1016/S0010-938X(01)00165-2.

(53) 	Xu, L. K.; Scantlebury, J. D. A Study on the Deactivation of an IrO2–Ta2O5 Coated Titanium Anode. Corrosion Science 2003, 45 (12), 2729–2740. https://doi.org/10.1016/S0010-938X(03)00108-2.

(54) 	Bock, C.; Spinney, H.; MacDougall, B. A Study of the Deactivation and Service Life of Ir Oxide Anodes Supported on Al Substrates. Journal of Applied Electrochemistry 2000, 30 (5), 523–532. https://doi.org/10.1023/A:1003961701335.

(55) 	Tan, X.; Shen, J.; Semagina, N.; Secanell, M. Decoupling Structure-Sensitive Deactivation Mechanisms of Ir/IrOx Electrocatalysts toward Oxygen Evolution Reaction. Journal of Catalysis 2019, 371, 57–70. https://doi.org/10.1016/j.jcat.2019.01.018.

(56) 	Mazhari Abbasi, H.; Jafarzadeh, K.; Mirali, S. M. An Investigation of the Effect of RuO2 on the Deactivation and Corrosion Mechanism of a Ti/IrO2 + Ta2O5 Coating in an OER Application. Journal of Electroanalytical Chemistry 2016, 777, 67–74. https://doi.org/10.1016/j.jelechem.2016.07.036.

(57) 	Lassali, T. A. F.; Boodts, J. F. C.; Bulhões, L. O. S. Faradaic Impedance Investigation of the Deactivation Mechanism of Ir-Based Ceramic Oxides Containing TiO2 and SnO2. Journal of Applied Electrochemistry 2000, 30 (5), 625–634. https://doi.org/10.1023/A:1003901520705.

(58) 	Panić, V.; A. Dekanski; Mišković-Stanković, V. B.; Milonjić, S.; Nikolić, B. On the Deactivation Mechanism of RuO2–TiO2/Ti Anodes Prepared by the Sol–Gel Procedure. Journal of Electroanalytical Chemistry 2005, 579 (1), 67–76. https://doi.org/10.1016/j.jelechem.2005.01.026.

(59) 	Jovanovič, P.; Hodnik, N.; Ruiz-Zepeda, F.; Arčon, I.; Jozinović, B.; Zorko, M.; Bele, M.; Šala, M.; Šelih, V. S.; Hočevar, S.; et al. Electrochemical Dissolution of Iridium and Iridium Oxide Particles in Acidic Media: Transmission Electron Microscopy, Electrochemical Flow Cell Coupled to Inductively Coupled Plasma Mass Spectrometry, and X-Ray Absorption Spectroscopy Study. J. Am. Chem. Soc. 2017, 139 (36), 12837–12846. https://doi.org/10.1021/jacs.7b08071.

(60) 	Hu, J.-M.; Sun, X.-J.; Hou, Y.-Y.; Zhang, J.-Q.; Cao, C.-N. Degradation Characteristics of IrO2-Type DSA® in Methanol Aqueous Solutions. Electrochimica Acta 2008, 53 (7), 3127–3138. https://doi.org/10.1016/j.electacta.2007.11.045.

(61) 	Stevens, M. B.; Enman, L. J.; Batchellor, A. S.; Cosby, M. R.; Vise, A. E.; Trang, C. D. M.; Boettcher, S. W. Measurement Techniques for the Study of Thin Film Heterogeneous Water Oxidation Electrocatalysts. Chemistry of Materials 2016, 29 (1), 120–140. https://doi.org/10.1021/acs.chemmater.6b02796.

(62) 	Moysiadou, A.; Hu, X. Stability Profiles of Transition Metal Oxides in the Oxygen Evolution Reaction in Alkaline Medium. Journal of Materials Chemistry A 2019, 7 (45), 25865–25877. https://doi.org/10.1039/C9TA10308B.

(63) 	Enman, L. J.; Burke, M. S.; Batchellor, A. S.; Boettcher, S. W. Effects of Intentionally Incorporated Metal Cations on the Oxygen Evolution Electrocatalytic Activity of Nickel (Oxy)Hydroxide in Alkaline Media. ACS Catalysis 2016, 6 (4), 2416–2423. https://doi.org/10.1021/acscatal.5b02924.

(64) 	Lu, X.; Zhao, C. Electrodeposition of Hierarchically Structured Three-Dimensional Nickel–Iron Electrodes for Efficient Oxygen Evolution at High Current Densities. Nat Commun 2015, 6 (1), 6616. https://doi.org/10.1038/ncomms7616.

(65) 	Yang, C.; Batuk, M.; Jacquet, Q.; Rousse, G.; Yin, W.; Zhang, L.; Hadermann, J.; Abakumov, A. M.; Cibin, G.; Chadwick, A.; et al. Revealing PH-Dependent Activities and Surface Instabilities for Ni-Based Electrocatalysts during the Oxygen Evolution Reaction. ACS Energy Lett. 2018, 3 (12), 2884–2890. https://doi.org/10.1021/acsenergylett.8b01818.

(66) 	Song, F.; Bai, L.; Moysiadou, A.; Lee, S.; Hu, C.; Liardet, L.; Hu, X. Transition Metal Oxides as Electrocatalysts for the Oxygen Evolution Reaction in Alkaline Solutions: An Application-Inspired Renaissance. J. Am. Chem. Soc. 2018, 140 (25), 7748–7759. https://doi.org/10.1021/jacs.8b04546.

(67) 	Ooka, H.; Huang, J.; Exner, K. S. The Sabatier Principle in Electrocatalysis: Basics, Limitations, and Extensions. Front. Energy Res. 2021, 9, 654460. https://doi.org/10.3389/fenrg.2021.654460.

(68) 	Zeradjanin, A. R.; Menzel, N.; Strasser, P.; Schuhmann, W. Role of Water in the Chlorine Evolution Reaction at RuO2-Based Electrodes-Understanding Electrocatalysis as a Resonance Phenomenon. ChemSusChem 2012, 5 (10), 1897–1904. https://doi.org/10.1002/cssc.201200193.

(69) 	Dickens, C. F.; Nørskov, J. K. A Theoretical Investigation into the Role of Surface Defects for Oxygen Evolution on RuO2. J. Phys. Chem. C 2017, 121 (34), 18516–18524. https://doi.org/10.1021/acs.jpcc.7b03481.

(70) 	Hansen, H. A.; Man, I. C.; Studt, F.; Abild-Pedersen, F.; Bligaard, T.; Rossmeisl, J. Electrochemical Chlorine Evolution at Rutile Oxide (110) Surfaces. Phys. Chem. Chem. Phys. 2010, 12 (1), 283–290. https://doi.org/10.1039/B917459A.

(71) 	de Moura, D. C.; de Araújo, C. K. C.; Zanta, C. L. P. S.; Salazar, R.; Martínez-Huitle, C. A. Active Chlorine Species Electrogenerated on Ti/Ru0.3Ti0.7O2 Surface: Electrochemical Behavior, Concentration Determination and Their Application. Journal of Electroanalytical Chemistry 2014, 731, 145–152. https://doi.org/10.1016/j.jelechem.2014.08.008.

(72) 	Cheng, H.; Scott, K.; Ramshaw, C. Chlorine Evolution in a Centrifugal Field. Journal of Applied Electrochemistry 2002, 32 (7), 831–838. https://doi.org/10.1023/A:1020170627227.

(73) 	Gaudet, J.; Tavares, A. C.; Trasatti, S.; Guay, D. Physicochemical Characterization of Mixed RuO2−SnO2 Solid Solutions. Chem. Mater. 2005, 17 (6), 1570–1579. https://doi.org/10.1021/cm048129l.

(74) 	Vazquez-Gomez, L.; Ferro, S.; De Battisti, A. Preparation and Characterization of RuO2–IrO2–SnO2 Ternary Mixtures for Advanced Electrochemical Technology. Applied Catalysis B: Environmental 2006, 67 (1–2), 34–40. https://doi.org/10.1016/j.apcatb.2006.03.023.

(75) 	Palma-Goyes, R. E.; Vazquez-Arenas, J.; Torres-Palma, R. A.; Ostos, C.; Ferraro, F.; González, I. The Abatement of Indigo Carmine Using Active Chlorine Electrogenerated on Ternary Sb2O5-Doped Ti/RuO2-ZrO2 Anodes in a Filter-Press FM01-LC Reactor. Electrochimica Acta 2015, 174, 735–744. https://doi.org/10.1016/j.electacta.2015.06.037.

(76) 	Zeradjanin, A. R.; La Mantia, F.; Masa, J.; Schuhmann, W. Utilization of the Catalyst Layer of Dimensionally Stable Anodes—Interplay of Morphology and Active Surface Area. Electrochimica Acta 2012, 82, 408–414. https://doi.org/10.1016/j.electacta.2012.04.101.

(77) 	Arikawa, T.; Murakami, Y.; Takasu, Y. Simultaneous Determination of Chlorine and Oxygen Evolving at RuO2/Ti and RuO2-TiO2/Ti Anodes by Differential Electrochemical Mass Spectroscopy. 6.

(78) 	Macounová, K.; Makarova, M.; Franc, J.; Jirkovský, J.; Krtil, P. Influence of Oxygen on Reactivity of Ru1−xFexO2−y-Doped Materials. Electrochem. Solid-State Lett. 2008, 11 (12), F27. https://doi.org/10.1149/1.2978963.

(79) 	Petrykin, V.; Macounová, K.; Okube, M.; Mukerjee, S.; Krtil, P. Local Structure of Co Doped RuO2 Nanocrystalline Electrocatalytic Materials for Chlorine and Oxygen Evolution. Catalysis Today 2013, 202, 63–69. https://doi.org/10.1016/j.cattod.2012.03.075.

(80) 	Petrykin, V.; Bastl, Z.; Franc, J.; Macounova, K.; Makarova, M.; Mukerjee, S.; Ramaswamy, N.; Spirovova, I.; Krtil, P. Local Structure of Nanocrystalline Ru1−xNixO2−δ Dioxide and Its Implications for Electrocatalytic Behavior—An XPS and XAS Study. J. Phys. Chem. C 2009, 113 (52), 21657–21666. https://doi.org/10.1021/jp904935e.

(81) 	Macounova, K.; Makarova, M.; Krtil, P. Oxygen Evolution on Nanocrystalline RuO2 and Ru0.9Ni0.1O2−δ Electrodes – DEMS Approach to Reaction Mechanism Determination. Electrochemistry Communications 2009, 11 (10), 1865–1868. https://doi.org/10.1016/j.elecom.2009.08.004.

(82) 	Macounová, K.; Jirkovský, J.; Makarova, M. V.; Franc, J.; Krtil, P. Oxygen Evolution on Ru1−xNixO2−y Nanocrystalline Electrodes. J Solid State Electrochem 2009, 13 (6), 959–965. https://doi.org/10.1007/s10008-008-0624-1.

(83) 	Petrykin, V.; Macounova, K.; Shlyakhtin, O. A.; Krtil, P. Tailoring the Selectivity for Electrocatalytic Oxygen Evolution on Ruthenium Oxides by Zinc Substitution. Angewandte Chemie International Edition 2010, 49 (28), 4813–4815. https://doi.org/10.1002/anie.200907128.

(84) 	Makarova, M. V.; Jirkovský, J.; Klementová, M.; Jirka, I.; Macounová, K.; Krtil, P. The Electrocatalytic Behavior of Ru0.8Co0.2O2−x—the Effect of Particle Shape and Surface Composition. Electrochimica Acta 2008, 53 (5), 2656–2664. https://doi.org/10.1016/j.electacta.2007.01.084.

(85) 	Petrykin, V.; Macounova, K.; Franc, J.; Shlyakhtin, O.; Klementova, M.; Mukerjee, S.; Krtil, P. Zn-Doped RuO2 Electrocatalyts for Selective Oxygen Evolution: Relationship between Local Structure and Electrocatalytic Behavior in Chloride Containing Media. Chem. Mater. 2011, 23 (2), 200–207. https://doi.org/10.1021/cm1028782.

(86) 	Abbott, D. F.; Petrykin, V.; Okube, M.; Bastl, Z.; Mukerjee, S.; Krtil, P. Selective Chlorine Evolution Catalysts Based on Mg-Doped Nanoparticulate Ruthenium Dioxide. J. Electrochem. Soc. 2015, 162 (1), H23–H31. https://doi.org/10.1149/2.0541501jes.

(87) 	Audichon, T.; Mayousse, E.; Morisset, S.; Morais, C.; Comminges, C.; Napporn, T. W.; Kokoh, K. B. Electroactivity of RuO2–IrO2 Mixed Nanocatalysts toward the Oxygen Evolution Reaction in a Water Electrolyzer Supplied by a Solar Profile. International Journal of Hydrogen Energy 2014, 39 (30), 16785–16796. https://doi.org/10.1016/j.ijhydene.2014.07.170.

(88) 	Audichon, T.; Napporn, T. W.; Canaff, C.; Morais, C.; Comminges, C.; Kokoh, K. B. IrO2 Coated on RuO2 as Efficient and Stable Electroactive Nanocatalysts for Electrochemical Water Splitting. J. Phys. Chem. C 2016, 120 (5), 2562–2573. https://doi.org/10.1021/acs.jpcc.5b11868.

(89) 	Pfeifer, V.; Jones, T. E.; Wrabetz, S.; Massué, C.; Velasco Vélez, J. J.; Arrigo, R.; Scherzer, M.; Piccinin, S.; Hävecker, M.; Knop-Gericke, A.; et al. Reactive Oxygen Species in Iridium-Based OER Catalysts. Chem. Sci. 2016, 7 (11), 6791–6795. https://doi.org/10.1039/C6SC01860B.

(90) 	Angelinetta, C.; Trasatti, S.; Atanososka, Lj. D.; Atanasoski, R. T. Surface Properties of RuO2 + IrO2 Mixed Oxide Electrodes. Journal of Electroanalytical Chemistry and Interfacial Electrochemistry 1986, 214 (1–2), 535–546. https://doi.org/10.1016/0022-0728(86)80122-X.

(91) 	Danilovic, N.; Subbaraman, R.; Chang, K. C.; Chang, S. H.; Kang, Y.; Snyder, J.; Paulikas, A. P.; Strmcnik, D.; Kim, Y. T.; Myers, D.; et al. Using Surface Segregation To Design Stable Ru-Ir Oxides for the Oxygen Evolution Reaction in Acidic Environments. Angew. Chem. Int. Ed. 2014, 53 (51), 14016–14021. https://doi.org/10.1002/anie.201406455.

(92) 	De Battisti, A.; Brina, R.; Gavelli, G.; Benedetti, A.; Fagherazzi, G. Influence of the Valve Metal Oxide on the Properties of Ruthenium Based Mixed Oxide Electrodes. Journal of Electroanalytical Chemistry and Interfacial Electrochemistry 1986, 200 (1–2), 93–104. https://doi.org/10.1016/0022-0728(86)90048-3.

(93) 	Yoon, Y.; Cho, E.; Jung, Y.; Kwon, M.; Yoon, J.; Kang, J.-W. Evaluation of the Formation of Oxidants and By-Products Using Pt/Ti, RuO2/Ti, and IrO2/Ti Electrodes in the Electrochemical Process. Environmental Technology 2015, 36 (3), 317–326. https://doi.org/10.1080/09593330.2014.946098.

(94) 	Eberil’, V. I.; Fedotova, N. S.; Novikov, E. A.; Mazanko, A. F. Studying the Link between the Potential of a Metal-Oxide Anode, the Current Efficiency for Chlorate, and the Current Losses for the Oxygen and Chlorine Evolution in a Wide Range of the Chlorate Electrolysis Conditions. 2000, 36 (12), 7.

(95) 	Serna-Galvis, E. A.; Jojoa-Sierra, S. D.; Berrio-Perlaza, K. E.; Ferraro, F.; Torres-Palma, R. A. Structure-Reactivity Relationship in the Degradation of Three Representative Fluoroquinolone Antibiotics in Water by Electrogenerated Active Chlorine. Chemical Engineering Journal 2017, 315, 552–561. https://doi.org/10.1016/j.cej.2017.01.062.

(96) 	Sumaria, V.; Krishnamurthy, D.; Viswanathan, V. Quantifying Confidence in DFT Predicted Surface Pourbaix Diagrams and Associated Reaction Pathways for Chlorine Evolution. ACS Catal. 2018, 8 (10), 9034–9042. https://doi.org/10.1021/acscatal.8b01432.

(97) 	Trieu, V.; Schley, B.; Natter, H.; Kintrup, J.; Bulan, A.; Hempelmann, R. RuO2-Based Anodes with Tailored Surface Morphology for Improved Chlorine Electro-Activity. Electrochimica Acta 2012, 78, 188–194. https://doi.org/10.1016/j.electacta.2012.05.122.

(98) 	Zeradjanin, A. R.; Topalov, A. A.; Van Overmeere, Q.; Cherevko, S.; Chen, X.; Ventosa, E.; Schuhmann, W.; Mayrhofer, K. J. J. Rational Design of the Electrode Morphology for Oxygen Evolution – Enhancing the Performance for Catalytic Water Oxidation. RSC Adv. 2014, 4 (19), 9579. https://doi.org/10.1039/c3ra45998e.

(99) 	Chen, R.; Trieu, V.; Zeradjanin, A. R.; Natter, H.; Teschner, D.; Kintrup, J.; Bulan, A.; Schuhmann, W.; Hempelmann, R. Microstructural Impact of Anodic Coatings on the Electrochemical Chlorine Evolution Reaction. Phys. Chem. Chem. Phys. 2012, 14 (20), 7392. https://doi.org/10.1039/c2cp41163f.

(100) 	Moreno-Hernandez, I. A.; MacFarland, C. A.; Read, C. G.; Papadantonakis, K. M.; Brunschwig, B. S.; Lewis, N. S. Crystalline Nickel Manganese Antimonate as a Stable Water-Oxidation Catalyst in Aqueous 1.0 M H2SO4. Energy Environ. Sci. 2017, 10 (10), 2103–2108. https://doi.org/10.1039/C7EE01486D.

(101) 	Roy, C.; Rao, R. R.; Stoerzinger, K. A.; Hwang, J.; Rossmeisl, J.; Chorkendorff, I.; Shao-Horn, Y.; Stephens, I. E. L. Trends in Activity and Dissolution on RuO2 under Oxygen Evolution Conditions: Particles versus Well-Defined Extended Surfaces. ACS Energy Lett. 2018, 3 (9), 2045–2051. https://doi.org/10.1021/acsenergylett.8b01178.

(102) 	Mozota, J.; Vukovic, M.; Conway, B. E. Enhanced Electrocatalysis for Chlorine Evolution on Oxidized Ir and Ru Anodes Modified by Potential Cycling. Journal of Electroanalytical Chemistry and Interfacial Electrochemistry 1980, 114 (1), 153–157. https://doi.org/10.1016/S0022-0728(80)80443-8.

(103) 	Pfeifer, V.; Jones, T. E.; Velasco Vélez, J. J.; Massué, C.; Greiner, M. T.; Arrigo, R.; Teschner, D.; Girgsdies, F.; Scherzer, M.; Allan, J.; et al. The Electronic Structure of Iridium Oxide Electrodes Active in Water Splitting. Phys. Chem. Chem. Phys. 2016, 18 (4), 2292–2296. https://doi.org/10.1039/C5CP06997A.

(104) 	Näslund, L.-Å.; Sánchez-Sánchez, C. M.; Ingason, Á. S.; Bäckström, J.; Herrero, E.; Rosen, J.; Holmin, S. The Role of TiO2 Doping on RuO2 -Coated Electrodes for the Water Oxidation Reaction. J. Phys. Chem. C 2013, 117 (12), 6126–6135. https://doi.org/10.1021/jp308941g.

(105) 	Yang, Y.; Kao, L. C.; Liu, Y.; Sun, K.; Yu, H.; Guo, J.; Liou, S. Y. H.; Hoffmann, M. R. Cobalt-Doped Black TiO2 Nanotube Array as a Stable Anode for Oxygen Evolution and Electrochemical Wastewater Treatment. ACS Catal. 2018, 8 (5), 4278–4287. https://doi.org/10.1021/acscatal.7b04340.

(106) 	Takata, T.; Domen, K. Defect Engineering of Photocatalysts by Doping of Aliovalent Metal Cations for Efficient Water Splitting. J. Phys. Chem. C 2009, 113 (45), 19386–19388. https://doi.org/10.1021/jp908621e.

(107) 	Pan, S. S.; Wang, S.; Zhang, Y. X.; Luo, Y. Y.; Kong, F. Y.; Xu, S. C.; Xu, J. M.; Li, G. H. P-Type Conduction in Nitrogen-Doped SnO2 Films Grown by Thermal Processing of Tin Nitride Films. Appl. Phys. A 2012, 109 (2), 267–271. https://doi.org/10.1007/s00339-012-7288-5.

(108) 	Babar, A. R.; Shinde, S. S.; Moholkar, A. V.; Bhosale, C. H.; Kim, J. H.; Rajpure, K. Y. Structural and Optoelectronic Properties of Antimony Incorporated Tin Oxide Thin Films. Journal of Alloys and Compounds 2010, 505 (2), 416–422. https://doi.org/10.1016/j.jallcom.2010.06.091.

(109) 	Jeon, S.; Park, Y. M.; Park, J.; Saravanan, K.; Jeong, H.-K.; Bae, J. W. Synergistic Effects of Nb2O5 Promoter on Ru/Al2O3 for an Aqueous-Phase Hydrodeoxygenation of Glycerol to Hydrocarbons. Applied Catalysis A: General 2018, 551, 49–62. https://doi.org/10.1016/j.apcata.2017.12.006.

(110) 	López, N.; Gómez-Segura, J.; Marín, R. P.; Pérez-Ramírez, J. Mechanism of HCl Oxidation (Deacon Process) over RuO2. Journal of Catalysis 2008, 255 (1), 29–39. https://doi.org/10.1016/j.jcat.2008.01.020.

(111) 	Crihan, D.; Knapp, M.; Zweidinger, S.; Lundgren, E.; Weststrate, C. J.; Andersen, J. N.; Seitsonen, A. P.; Over, H. Stable Deacon Process for HCl Oxidation over RuO2. Angew. Chem. Int. Ed. 2008, 47 (11), 2131–2134. https://doi.org/10.1002/anie.200705124.

(112) 	Exner, K. S.; Anton, J.; Jacob, T.; Over, H. Chlorine Evolution Reaction on RuO2(110): Ab Initio Atomistic Thermodynamics Study - Pourbaix Diagrams. Electrochimica Acta 2014, 120, 460–466. https://doi.org/10.1016/j.electacta.2013.11.027.

(113) 	Exner, K. S.; Anton, J.; Jacob, T.; Over, H. Microscopic Insights into the Chlorine Evolution Reaction on RuO2(110): A Mechanistic Ab Initio Atomistic Thermodynamics Study. Electrocatalysis 2015, 6 (2), 163–172. https://doi.org/10.1007/s12678-014-0220-3.

(114) 	Exner, K. S. Beyond the Traditional Volcano Concept: Overpotential-Dependent Volcano Plots Exemplified by the Chlorine Evolution Reaction over Transition-Metal Oxides. J. Phys. Chem. C 2019, 123 (27), 16921–16928. https://doi.org/10.1021/acs.jpcc.9b05364.

(115) 	Karlsson, R. K. B.; Hansen, H. A.; Bligaard, T.; Cornell, A.; Pettersson, L. G. M. Ti Atoms in Ru0.3Ti0.7O2 Mixed Oxides Form Active and Selective Sites for Electrochemical Chlorine Evolution. Electrochimica Acta 2014, 146, 733–740. https://doi.org/10.1016/j.electacta.2014.09.056.

(116) 	Exner, K. S.; Anton, J.; Jacob, T.; Over, H. Controlling Selectivity in the Chlorine Evolution Reaction over RuO2-Based Catalysts. Angew. Chem. Int. Ed. 2014, 53 (41), 11032–11035. https://doi.org/10.1002/anie.201406112.

(117) 	Exner, K. S.; Anton, J.; Jacob, T.; Over, H. Full Kinetics from First Principles of the Chlorine Evolution Reaction over a RuO2 (110) Model Electrode. Angew. Chem. Int. Ed. 2016, 55 (26), 7501–7504. https://doi.org/10.1002/anie.201511804.

(118) 	He, Z.; Chen, Y.; Santos, E.; Schmickler, W. The Pre‐exponential Factor in Electrochemistry. Angew. Chem. Int. Ed. 2018, 57 (27), 7948–7956. https://doi.org/10.1002/anie.201800130.

(119) 	Exner, K. S. Controlling Stability and Selectivity in the Competing Chlorine and Oxygen Evolution Reaction over Transition Metal Oxide Electrodes. ChemElectroChem 2019, 6 (13), 3401–3409. https://doi.org/10.1002/celc.201900834.

(120) 	Exner, K. S. Activity‐Stability Volcano Plots for Material Optimization in Electrocatalysis. ChemCatChem 2019, 11 (14), 3234–3241. https://doi.org/10.1002/cctc.201900500.

(121) 	Kishor, K.; Saha, S.; Parashtekar, A.; Pala, R. G. S. Increasing Chlorine Selectivity through Weakening of Oxygen Adsorbates at Surface in Cu Doped RuO2 during Seawater Electrolysis. J. Electrochem. Soc. 2018, 165 (15), J3276–J3280. https://doi.org/10.1149/2.0361815jes.

(122) 	Kuznetsova, E.; Petrykin, V.; Sunde, S.; Krtil, P. Selectivity of Nanocrystalline IrO2-Based Catalysts in Parallel Chlorine and Oxygen Evolution. Electrocatalysis 2015, 6 (2), 198–210. https://doi.org/10.1007/s12678-014-0233-y.

(123) 	Kim, J.; Kwon, D.; Kim, K.; Hoffmann, M. R. Electrochemical Production of Hydrogen Coupled with the Oxidation of Arsenite. Environ. Sci. Technol. 2014, 48 (3), 2059–2066. https://doi.org/10.1021/es4046814.

(124) 	Park, H.; Vecitis, C. D.; Hoffmann, M. R. Solar-Powered Electrochemical Oxidation of Organic Compounds Coupled with the Cathodic Production of Molecular Hydrogen. J. Phys. Chem. A 2008, 112 (33), 7616–7626. https://doi.org/10.1021/jp802807e.

(125) 	Lim, T.; Jung, G. Y.; Kim, J. H.; Park, S. O.; Park, J.; Kim, Y.-T.; Kang, S. J.; Jeong, H. Y.; Kwak, S. K.; Joo, S. H. Atomically Dispersed Pt–N4 Sites as Efficient and Selective Electrocatalysts for the Chlorine Evolution Reaction. Nat Commun 2020, 11 (1), 412. https://doi.org/10.1038/s41467-019-14272-1.

(126) 	Boehm, H.-P.; Schneider, M. Über die Hydroxylgruppen an der Oberfläche des Amorphen Siliciumdioxyds „Aerosil" und ihre Reaktionen. Z. Anorg. Allg. Chem. 1959, 301 (5–6), 326–335. https://doi.org/10.1002/zaac.19593010516.

(127) 	Boehm, H.-P.; Schneider, M.; Arendt, F. Der Wassergehalt „getrockneter" Siliciumdioxyd-Oberflächen. Z. Anorg. Allg. Chem. 1963, 320 (1–4), 43–53. https://doi.org/10.1002/zaac.19633200107.

(128) 	Peri, J. B. Infrared and Gravimetric Study of the Surface Hydration of γ-Alumina. J. Phys. Chem. 1965, 69 (1), 211–219. https://doi.org/10.1021/j100885a032.

(129) 	Viganoò, R.; Taraszewska, J.; Daghetti, A.; Trasatti, S. The Point of Zero Charge of RuO2 + IrO2 Mixed Oxides. Journal of Electroanalytical Chemistry and Interfacial Electrochemistry 1985, 182 (1), 203–209. https://doi.org/10.1016/0368-1874(85)85455-1.

(130) 	Kosmulski, M. Isoelectric Points and Points of Zero Charge of Metal (Hydr)Oxides: 50 Years after Parks’ Review. Advances in Colloid and Interface Science 2016, 238, 1–61. https://doi.org/10.1016/j.cis.2016.10.005.

(131) 	Kleijn, J. M.; Lyklema, J. Colloid-Chemical Properties of Ruthenium Dioxide in Relation to Catalysis of the Photochemical Generation of Hydrogen. Colloid & Polymer Sci 1987, 265 (12), 1105–1113. https://doi.org/10.1007/BF01417469.

(132) 	Kleijn, J. M.; Lyklema, J. The Electrical Double Layer on Oxides: Specific Adsorption of Chloride and Methylviologen on Ruthenium Dioxide. Journal of Colloid and Interface Science 1987, 120 (2), 511–522. https://doi.org/10.1016/0021-9797(87)90378-X.

(133) 	Kobayakawa, K.; Nakazawa, Y.; Ikeda, M.; Sato, Y.; Fujishima, A. Influence of the Density of Surface Hydroxyl Groups on TiO2 Photocatalytic Activities. Berichte der Bunsengesellschaft für physikalische Chemie 1990, 94 (12), 1439–1443. https://doi.org/10.1002/bbpc.199000056.

(134) 	Wu, C.-Y.; Tu, K.-J.; Deng, J.-P.; Lo, Y.-S.; Wu, C.-H. Markedly Enhanced Surface Hydroxyl Groups of TiO2 Nanoparticles with Superior Water-Dispersibility for Photocatalysis. Materials 2017, 10 (5), 566. https://doi.org/10.3390/ma10050566.

(135) 	Schindler, P. W.; Walti, E.; Furst, B. Role of Surface Hydroxyl Groups in Surface Chemistry of Metal Oxides. Chimia 1976, 30 (2), 107–109.

(136) 	McCafferty, W. Determination of the Concentration of Surface Hydroxyl Groups on Metal Oxide Films by a Quantitative XPS Method. Surf. Interface Anal. 1998, 16.

(137) 	Oosawa, Y.; Grätzel, M. Effect of Surface Hydroxyl Density on Photocatalytic Oxygen Generation in Aqueous TiO2 Suspensions. J. Chem. Soc., Faraday Trans. 1 1988, 84 (1), 197. https://doi.org/10.1039/f19888400197.

(138) 	Di Paola, A.; Bellardita, M.; Palmisano, L.; Barbieriková, Z.; Brezová, V. Influence of Crystallinity and OH Surface Density on the Photocatalytic Activity of TiO2 Powders. Journal of Photochemistry and Photobiology A: Chemistry 2014, 273, 59–67. https://doi.org/10.1016/j.jphotochem.2013.09.008.

(139) 	Schindler, P. W.; Gamsjäger, H. Acid — Base Reactions of the TiO2 (Anatase) — Water Interface and the Point of Zero Charge of TiO2 Suspensions. Kolloid-Z.u.Z.Polymere 1972, 250 (7), 759–763. https://doi.org/10.1007/BF01498568.

(140) 	Frei, H.; Fitzmaurice, D. J.; Graetzel, M. Surface Chelation of Semiconductors and Interfacial Electron Transfer. Langmuir 1990, 6 (1), 198–206. https://doi.org/10.1021/la00091a032.

(141) 	Moser, J.; Grätzel, M. Photoelectrochemistry with Colloidal Semiconductors; Laser Studies of Halide Oxidation in Colloidal Dispersions of TiO2 and α-Fe2O3. HCA 1982, 65 (5), 1436–1444. https://doi.org/10.1002/hlca.19820650517.

(142) 	Rotzinger, F. P.; Kesselman-Truttmann, J. M.; Hug, S. J.; Shklover, V.; Grätzel, M. Structure and Vibrational Spectrum of Formate and Acetate Adsorbed from Aqueous Solution onto the TiO2 Rutile (110) Surface. J. Phys. Chem. B 2004, 108 (16), 5004–5017. https://doi.org/10.1021/jp0360974.

(143) 	Kosmulski, M. The Significance of the Difference in the Point of Zero Charge between Rutile and Anatase. Advances in Colloid and Interface Science 2002, 99 (3), 255–264. https://doi.org/10.1016/S0001-8686(02)00080-5.

(144) 	Stumm, W.; Morgan, J. J. Aquatic Chemistry: Chemical Equilibria and Rates in Natural Waters, 3rd ed.; Environmental science and technology; Wiley: New York, 1996.

(145) 	Dzombak, D. A.; Morel, F. M. M. Surface Complexation Modeling: Hydrous Ferric Oxide; Wiley: New York, 1990.

(146) 	Schindler, P. W.; Stumm, W. The Surface Chemistry of Oxides, Hydroxides, and Oxide Minerals. IN: Aquatic Surface Chemistry: Chemical Processes at the Particle-Water Interface. John Wiley and Sons, New York. 1987. p 83-110, 13 fig, 7 tab, 49 ref. 1987.

(147) 	Rodrı́guez, R.; Blesa, M. A.; Regazzoni, A. E. Surface Complexation at the TiO2(Anatase)/Aqueous Solution Interface: Chemisorption of Catechol. Journal of Colloid and Interface Science 1996, 177 (1), 122–131. https://doi.org/10.1006/jcis.1996.0012.

(148) 	Blesa, M. A.; Weisz, A. D.; Morando, P. J.; Salfity, J. A.; Magaz, G. E.; Regazzoni, A. E. The Interaction of Metal Oxide Surfaces with Complexing Agents Dissolved in Water. Coordination Chemistry Reviews 2000, 196 (1), 31–63. https://doi.org/10.1016/S0010-8545(99)00005-3.

(149) 	Geiger, S.; Kasian, O.; Mingers, A. M.; Nicley, S. S.; Haenen, K.; Mayrhofer, K. J. J.; Cherevko, S. Catalyst Stability Benchmarking for the Oxygen Evolution Reaction: The Importance of Backing Electrode Material and Dissolution in Accelerated Aging Studies. ChemSusChem 2017, 10 (21), 4140–4143. https://doi.org/10.1002/cssc.201701523.

(150) 	Wang, Z.; Guo, X.; Montoya, J.; Nørskov, J. K. Predicting Aqueous Stability of Solid with Computed Pourbaix Diagram Using SCAN Functional. npj Comput Mater 2020, 6 (1), 160. https://doi.org/10.1038/s41524-020-00430-3.

(151) 	Hodnik, N.; Jovanovič, P.; Pavlišič, A.; Jozinović, B.; Zorko, M.; Bele, M.; Šelih, V. S.; Šala, M.; Hočevar, S.; Gaberšček, M. New Insights into Corrosion of Ruthenium and Ruthenium Oxide Nanoparticles in Acidic Media. J. Phys. Chem. C 2015, 119 (18), 10140–10147. https://doi.org/10.1021/acs.jpcc.5b01832.

(152) 	Klyukin, K.; Zagalskaya, A.; Alexandrov, V. Role of Dissolution Intermediates in Promoting Oxygen Evolution Reaction at RuO2 (110) Surface. J. Phys. Chem. C 2019, 123 (36), 22151–22157. https://doi.org/10.1021/acs.jpcc.9b03418.

(153) 	Zagalskaya, A.; Alexandrov, V. Mechanistic Study of IrO2 Dissolution during the Electrocatalytic Oxygen Evolution Reaction. J. Phys. Chem. Lett. 2020, 11 (7), 2695–2700. https://doi.org/10.1021/acs.jpclett.0c00335.

(154) 	Kasian, O.; Grote, J.-P.; Geiger, S.; Cherevko, S.; Mayrhofer, K. J. J. The Common Intermediates of Oxygen Evolution and Dissolution Reactions during Water Electrolysis on Iridium. Angew. Chem. Int. Ed. 2018, 57 (9), 2488–2491. https://doi.org/10.1002/anie.201709652.

(155) 	Maciá, M. D.; Herrero, E.; Feliu, J. M.; Aldaz, A. Formic Acid Self-Poisoning on Bismuth-Modified Stepped Electrodes. Journal of Electroanalytical Chemistry 2001, 500 (1–2), 498–509. https://doi.org/10.1016/S0022-0728(00)00389-2.

(156) 	Metikoš-Huković, M.; Rešeti’c, A.; Gvozdić, V. Behaviour of Tin as a Valve Metal. Electrochimica Acta 1995, 40 (11), 1777–1779. https://doi.org/10.1016/0013-4686(95)00243-8.

(157) 	Boggio, R.; Carugati, A.; Lodi, G.; Trasatti, S. Mechanistic Study of Cl2 Evolution at Ti-Supported Co3O4 Anodes. Journal of Applied Electrochemistry 1985, 15 (3), 335–349. https://doi.org/10.1007/BF00615986.

(158) 	Zhu, X.; Wang, P.; Wang, Z.; Liu, Y.; Zheng, Z.; Zhang, Q.; Zhang, X.; Dai, Y.; Whangbo, M.-H.; Huang, B. Co3O4 Nanobelt Arrays Assembled with Ultrathin Nanosheets as Highly Efficient and Stable Electrocatalysts for the Chlorine Evolution Reaction. J. Mater. Chem. A 2018, 6 (26), 12718–12723. https://doi.org/10.1039/C8TA03689F.

(159) 	Singh, V.; Nagaiah, T. C. In Situ Incorporation of Cobalt Nanoclusters and Nitrogen into the Carbon Matrix: A Bifunctional Catalyst for the Oxygen Depolarized Cathode and Chlorine Evolution in HCl Electrolysis. J. Mater. Chem. A 2019, 7 (16), 10019–10029. https://doi.org/10.1039/C9TA00675C.

(160) 	Wang, Y.; Wu, J.; Giammar, D. E. Kinetics of the Reductive Dissolution of Lead(IV) Oxide by Iodide. Environ. Sci. Technol. 2012, 46 (11), 5859–5866. https://doi.org/10.1021/es2038905.

(161) 	Guo, D.; Robinson, C.; Herrera, J. E. Role of Pb(II) Defects in the Mechanism of Dissolution of Plattnerite (β-PbO2) in Water under Depleting Chlorine Conditions. Environ. Sci. Technol. 2014, 48 (21), 12525–12532. https://doi.org/10.1021/es502133k.

(162) 	Lin, Y.-P.; Valentine, R. L. The Release of Lead from the Reduction of Lead Oxide (PbO2) by Natural Organic Matter. Environ. Sci. Technol. 2008, 42 (3), 760–765. https://doi.org/10.1021/es071984w.

(163) 	Ham, K.; Hong, S.; Kang, S.; Cho, K.; Lee, J. Extensive Active-Site Formation in Trirutile CoSb2O6 by Oxygen Vacancy for Oxygen Evolution Reaction in Anion Exchange Membrane Water Splitting. ACS Energy Lett. 2021, 6 (2), 364–370. https://doi.org/10.1021/acsenergylett.0c02359.

Table of contents graphic:

Acknowledgements:

The authors acknowledge generous financial support from Bill and Melinda Gates Foundation (Grant No. INV003227).

Author biographies:

Heng Dong is currently a Ph.D. student in the group of Prof. Michael R. Hoffmann at California Institute of Technology (Caltech). He obtained his B.S. degree (2018) in School of Environment in Tsinghua University, China. His research focuses on development of efficient, stable, and cost-effective electrochemical systems for decentralized wastewater treatment and disinfection.

Dr. Weilai Yu earned his Ph.D in Chemistry from California Institute of Technology (Caltech) in 2021, working with Prof. Nathan S. Lewis. His thesis focuses on understanding the stability of photo-electrochemical interfaces for solar fuels. He received his B.S. in Chemistry (Honor) from Wuhan University in 2016. He is currently a postdoctoral scholar of Chemical Engineering at Stanford University, working with Prof. Zhenan Bao.

Michael R. Hoffmann is the John S. and Sherry Chen Professor of Engineering and Applied Science at the California Institute of Technology.  He received his BA in chemistry from Northwestern University, his PhD in chemistry from Brown University, and his post-doctoral education in engineering at Caltech. He is a member of the National Academy of Engineering and a Foreign Member of the Chinese Academy of Engineering.