Supplementary Materials

Tetracycline adsorption on magnetic sludge biochar: size effect of the Fe3O4 nanoparticles

Suxing Luo* ab,1, Jun Qin a,1, Yuanhui Wu bc, and Feng Feng*a

a College of Chemistry and Environmental Engineering, Shanxi Datong University, Datong, 037009, P. R. China

b Department of Chemistry and Chemical Engineering, Zunyi Normal College, Zunyi, 563006, P. R. China.

c Special Key Laboratory of Electrochemistry for Materials of Guizhou Province, Zunyi, 563006, P. R. China

1 These authors contributed equally to this work.

The concentration of tetracycline (TC) in the supernatant was determined by UV-VIS. Since pH value has important effect on the existing forms, stabilities and characteristic absorption peaks of TC, the characteristic absorption peaks could be affected by pH value. As shown in Figure S1, the peak at 357 nm was almost insensitive to pH (2-8). Therefore, the peak of 357 nm was selected for detection. This observation was in agreement with Tang et al. in the study of TC sorption on magnetic biochar. As shown in Figure S2 and S3, the absorbance values increased with the increase in concentration of TC, with linear regressions of A=-0.003+0.0311C(1-15 ppm, R=0.999),

and A=1.17+0.015C(20-120ppm, R=0.997).

Fig. S1 UV-VIS full scan spectrum for TC at different pH values.

Fig.S2 UV-VIS full scan spectrum for different concentrations of TC (1-15 ppm). Inset: calibration curve.

Fig.S3 UV-VIS full scan spectrum for different concentrations of TC (20-120 ppm). Inset: calibration curve.

Fig.S4 The magnetic separation property of MS-1.

Fig. S5 Various structures of TC.

The various structures of TC were shown in Fig. S3. The dissociation constants (pKa) of TC are 3.3, 7.7, and 9.7, which resulted in multiple ionizable functional groups of TC.