Thesis for the Degree of Master of Science in Construction Management

Assessment of Concrete Strength in Existing Structures Using Nondestructive Tests at Kachankawal Rural Municipality, Nepal

Amit Dhungana

(2019-1-06-0015)

School of Engineering

Faculty of Science and Technology

Madan Bhandari Memorial Academy Nepal

Joint Constituent College of Pokhara University, Nepal

November, 2021

Thesis for the Degree of Master of Science in Construction Management

Assessment of Concrete Strength in Existing Structures Using Nondestructive Tests at Kachankawal Rural Municipality, Nepal

Supervised by Dr. Binod Aryal

A thesis submitted in partial fulfillment of the requirements for the degree of Master of Science in Construction Management

Amit Dhungana

(2019-1-06-0015)

School of Engineering

Faculty of Science and Technology

Madan Bhandari Memorial Academy Nepal

Joint Constituent College of Pokhara University, Nepal

November, 2021

# Declaration

I hereby declare that this study entitled “Assessment of concrete strength in existing structures using nondestructive tests at Kachankawal Rural Municipality, Nepal” is based on my original research work. Related works on the topic by other researchers have been duly acknowledged. I owe all the liabilities relating to the accuracy and authenticity of the data and any other information included hereunder.

Signature:

Name of the Student: Amit Dhungana

P.U. Registration Number: 2019-1-06-0015

Date: November, 2021

# Recommendation

This is to certify that this thesis entitled "Assessment of concrete strength in existing structures using nondestructive tests at Kachankawal Rural Municipality, Nepal",Prepared and submitted by Amit Dhungana, in partial fulfillment of the requirements of the degree of Master of Science (M.Sc.) in Construction Management awarded by Pokhara University,has been completed under my supervision. I recommend the same for acceptance by Pokhara University.

Signature:

Name of Supervisor: Dr. Binod Aryal

Organization: Madan Bhandari Technological University Development Board

Designation: Executive Director

Date: November, 2021

# Acknowledgements

It is really wonderful feeling that I got the opportunity to submit thesis on "Assessment of concrete strength in existing structures using nondestructive tests at Kachankawal Rural Municipality ". My heart full thanks go to Madan Bhandari Memorial Academy Nepal for granting me this opportunity to study on this topic.

It is my immensepleasure to thank Kachankawal Rural Municipality for grating sponsorship of my master’s study.

I would like to thank my respected thesis supervisor Dr. Binod Aryal and co supervisor Assoc. Prof.Anjay Kumar Mishra, Ph.D. The door to Prof. Mishra for his valuable guidance, advice and continuous encouragement which proved very helpful in completing this project.

I would also like to extend my sincere thanks to all the despondence, key informant and other helping hands who has supported me directly or indirectly.

Finally, I would like to express my sincere thanks to my family, friends and well-wishers for their immense support throughout the preparation of this summer project report.

Thank you

Signature:

Name of the Student: Amit Dhungana

P.U. Registration Number: 2019-1-06-0015

Date: November, 2021

# Abstract

Concreteis an integral material used for construction purposes which determines strength of structures also. For assuring strength of existing structures, Nondestructive testing (NDT) methods are used to inspect or measure the materials or structures without destroying their surface texture, product integrity and future usefulness.The overall objective of the research is to assess the strength of concrete in existing structures using Nondestructive Tests at Kachankawal Rural Municipality, Jhapa District of Nepal.

Rebound hammer test and ultrasonic pulse velocity tests were used for determining the compressive strength of concrete. The existing Reinfored Concrete Cement culverts were used for 9 existing structures. Average rebound number were taken and calculated from each sample. From the average rebound number were taken to determine the grade of concrete along with corresponding compressive strength.Similarly, the Ultrasonic Pulse Velocity tests were done on same existing structures and path length and time were noted for assessing the corresponding compressive strength and the quality of concrete. Triangulation among rebound hammer test, ultrasonic pulse velocity test and proposed initial grading were validated using chi square test. Relation between compressive strength with rebound hammer and ultrasonic pulse velocity were analyzed using linear regression model. Key informant interview were done to assure concreting practices.Out of 9 selected samples  2 good  and 7 fair were found based on rebound hammer test whereas, 4,2 and 3 samples were very good, good and satisfactory respectively based on ultrasonic pulse velocity test.Chi square confirms variation in compressive strength between calculated compressive strength and standard compressive strength.The relation of compressive strength(y) at R² = 1 with  rebound number(x) and ultrasonic pulse velocity(x) could be expressed  asy = 0.9306x - 2.7233and y = 2.904x + 10.119 respectively. Systematic methods of concreting were not found applicable as tests and measurements were not performed at sites due to lack of knowledge and skills. Proper concreting procedure should be enforced for systematic concreting practices through tests at sites, measurements, training, site supervision and motivation. NDT should be promoted along with systematic practise of concreting to over come the issues of quality of construction works.The study is  a guiding tool for concern authority and professionals  to make effective decision regarding further structural development and budget allocation of the existing structures.

Keywords:Compressive strength, Rebound hammer, Ultrasonic pulse velocity, Ingredients of concrete, Practice of concreting.

# TABLE OF CONTENTS

Declaration	iii

Recommendation	iv

Certificate	v

Acknowledgements	vi

Abstract	vii

Table of Contents	viii

List of Tables	x

List of Pictures	xi

CHAPTER I:  INTRODUCTION

1.1	 Background of the Study	1

1.2 	Statement of Problem	2

1.3 	Research Questions	4

1.4 	Research Objectives	4

1.5 	Significance of study	4

1.6 	Scope & Limitation of the study	5

CHAPTER II:  LITERATURE REVIEW

2.1	Theoretical Review	8

2.2 	Rebound Hammer	8

2.3 	Ultra sonic pulse velocity:	11

CHAPTER III:  METHODOLOGY

3.1 	Study Area	17

3.2 	Research Flowchart	18

3.3 	Sampling	18

3.4 	Data Collection	19

3.5 	Analysis of data	21

CHAPTER IV:  RESEARCH AND DISCUSSION

4.1 	Schmidt Hammer (Rebound Hammer Test)	25

4.2 	Ultrasonic Pulse Velocity Tester	26

4.3 	Comparison of compressive strength obtained from rebound hammer using Chi- square test	27

4.4 	Relation between rebound number and compressive strength.	28

4.5	Comparison of compressive strength obtained from ultrasonic pulse velocity using Chi- square test	28

4.6 	Relation between Ultrasonic Pulse Velocity and compressive strength.	29

4.7 	Researcher observation on Concrete Practices	30

CHAPTER V:  CONCLUSION AND RECOMMENDATION

5.1 	Conclusion	37

5.2 	Recommendations	57

5.3 	Recommendations for Further Studies	38

References	41

Annex	42

# LIST OF TABLES

Table 2.2 	Rebound Number and Concrete Quality	9

Table 2.3 	Velocity Criterions for Concrete Quality Grading	16

Table 3.7 	Methodology summary	23

Table 4.1	 Schmidt Hammer test results.	25

Table 4.2 	Ultrasonic pulse velocity test results	26

Table 4.3 	Rebound Hammer test data calculations	27

Table 4.4 	Ultrasonic pulse velocity test data calculations	29

# LIST OF PICTURES

Pictures 1 	Schematic of Rebound Hammer	1

Pictures 2	Pulse Velocity Devices	12

Pictures 3	Configurations of transducers	14

Pictures 4 	Map of Kachankawal showing study area	17

Pictures 5 	Flow chart of research process	18

Pictures 6 	Map showing sample sites 	20

Pictures 7	Cement bags without manufactured date	31

Pictures 8 	Improper Stackinng of Cement bags	31

Pictures 9 	Rough cement, sand & water calculations by labour	32

Pictures 10 	Labour Based Slab Casting Works	33

Pictures 11	Lack of Weather Prediction	33

Pictures 12	Improper Shuttering and Formworks	34

Pictures 13 	Unequal Bar Spacing	33

Pictures 14 	Less or no curing after construction works	33

Pictures 15 	Present Condition of Existing Culvert1	39

Pictures 16 	Collecting data using Rebounce Hammer of Culvert	39

Pictures 17 	Collecting data using Rebounce Hammer of Culvert	40