Edges more electroactive than basal planes in synthetic bulk crystals of TiS2 and TiSe2

Stefan Werta,b, Christian Iffelsbergera, Katarina A. Novčića, Frank-Michael Matysikb and Martin Pumera*a,c,d,e

aFuture Energy and Innovation Laboratory, Central European Institute of Technology, Brno University of Technology, Purkyňova 123, 61200 Brno, Czech Republic

bInstitute of Analytical Chemistry, Chemo- and Biosensors, University of Regensburg, 93053 Regensburg, Germany

cDepartment of Chemistry and Biochemistry, Mendel University in Brno, Zemedelska 1, CZ-613 00, Brno, Czech Republic

dDepartment of Chemical and Biomolecular Engineering, Yonsei University, 50 Yonsei-ro, Seodaemun-gu, Seoul 03722, Korea

eDepartment of Medical Research, China Medical University Hospital, China Medical University, No. 91 Hsueh-Shih Road, Taichung 40402, Taiwan

Keywords: Transition metal dichalcogenides, scanning electrochemical microscopy, 2D materials, titanium disulfide, titanium diselenide, anisotropy

Abstract

Layered materials and derived 2D material couples such as graphite/graphene, layered and single layer pnictogens (i.e., black phosphorus and phosphorene) and transition metal dichalcogenides (TMDs) have gained a lot of attention due to their electrocatalytic properties and as potential materials for energy storage. Previous studies have shown that electrochemical reactions at graphite, MoS2 and pnictogens mainly occur at the edges and steps of crystals rather than on the basal plane. The persisting question is if this is a general trend in nature within bulk crystals of 2D materials. To come closer to the answer to this question, we studied the surface of artificially grown TiS2 and TiSe2 crystals regarding their local electrochemical activity via scanning electrochemical microscopy (SECM). Both TMDs have shown increased electrochemical activity near crystal steps/edges. For correlation, optical and topographical analysis were performed via scanning electron microscopy (SEM) and atomic force microscopy (AFM). We show that the increased electrochemical activity at edges is persistent for these layered crystalline materials, thus expanding the knowledge their properties, which is important for future application in the energy sector.

Introduction

In the search for earth-abundant and environmental-friendly materials for energy storage, 2D materials such as graphite,1–4 graphene,5,6 and layered pnictogens6,7-11 (e.g., black phosphorous)6,8-10 were found to be powerful candidates. Layered transition metal dichalcogenides (TMDs) are another large group of potential materials for energy-related applications.12–19 With their chemical composition of MX2, where M is a transition metal from groups IV to VII B (like Mo, W, Ti) and X is a chalcogenide (S, Se, Te), numerous elemental combinations can be realized. Due to their layered structure and strong covalent bonding within single layers, but weak interaction between layers because of van der Waals forces, these materials show anisotropy with respect to their electrical, mechanical, and electrochemical properties. Single or few layers can be prepared easily via exfoliation20–22 and the resulting 2D materials show promising properties for a wide range of potential applications such as for energy storage,23,24 sensing,25 and solar cells.26 Among TMDs, group VI members have been studied extensively so far, with MoS2 being the most popular as it is a promising catalyst for the hydrogen evolution reaction.27,28

Most notably, graphene,5,6,29 layered pnictogens6,7–11 (e.g., black phosphorous),6,8–10 and group VI TMDs12–15,30–33 show increased electron transfer rates and increased electrocatalytic and electrochemical activity at the edges compared to basal planes (illustrated in Figure 1A, with crystal structure in Figure 1B). It is an important question whether the increased electrochemical activity at edges is a phenomenon generally occurring in 2D materials and if this property persists in bulk crystals. For group IV TMDs, studies regarding their local electrochemical activity are scarce. However, knowledge about this property is needed to expand the range of potential electrocatalysts and energy storage materials in the future. Therefore, we decided to study the local electrochemical activity of TiS2 and TiSe2 as representatives of group IV TMDs, which have not been investigated in this regard so far.

Figure 1A. Schematic view of the surface structure of layered 2D-materials like graphite, layered pnictogens and TMDs. B: Crystal structure of group IV B TMDs, with M being coordinated octahedrally (1T phase).

Generally, due to different coordination in the individual layers, group IV (octahedral 1T-phase) and VI TMDs (prismatic 2H phase) show different properties.34,35 Group IV TMDs have attracted attention as they provide advantages over group VI TMDs like enhanced thermoelectric performance,36 high room-temperature mobility,37 ability to exhibit charge density wave,38 and high conductivity and theoretical capacity when used as anode material in sodium ion batteries.39,40 Furthermore, they are considered as storage material in potassium ion batteries as another alternative to lithium ion batteries.41

To investigate if group IV TMDs crystals exhibit differences in the electrochemical activity between basal plane and edges, we used scanning electrochemical microscopy (SECM) over pristine TiS2 and TiSe2 surfaces for the localized imaging of the electrochemical activity. The obtained recordings were compared to scanning electron microscope (SEM), energy dispersive X-ray spectroscopy (EDS), atomic force microscope (AFM) images and X-ray photoelectron spectra (XPS) for correlating the electrochemical response with surface morphology and elemental composition.

Experimental

Materials and methods

TMD crystals (TiS2, TiSe2) were obtained from 2d-age.com. Two-component epoxy resin was purchased from Struers Aps, Denmark. Graphite powder (<20 µm, synthetic) was bought from Sigma-Aldrich. Carbon SEM stubs were purchased from Micro to Nano, Netherlands. Polydimethylsiloxane (PDMS, SYLGARDTM 184) was obtained from Dow Inc., Michigan, USA. Potassium ferricyanide (K3Fe(CN)6) and potassium chloride (KCl) were purchased from Merck, Germany. Solutions were prepared with deionized water with a resistivity >18.2 MΩ cm (Milli-Q Advantage A10 system, Merck Millipore, Germany). All chemicals were of analytical grade and used as bought.

Crystal preparation

The sample preparation process is schematically shown in Figure 2. For the fabrication of flat samples, the TMD crystals were embedded in an electrically conductive blend of graphite powder and epoxy resin with a mass ratio of 1:1 on carbon SEM stubs. About 250 mg of the mixture were spread on the stub surface and pressed on a TMD crystal placed on a flat PDMS layer in a petri dish. After 24 h, the graphite/epoxy blend hardened, and the sample was carefully removed from the PDMS. Furthermore, as the crystal was embedded within a conductive matrix, electrical contact was established at the upper layers of the crystal. Eventually, a clean sample with a pristine crystal surface was ensured by removal of the upper crystal layers according to the “scotch tape” method.42 To introduce well-designed edges in the crystal surface, the upper layers of the TiS2 crystal were cut with a scalpel, and the surface was rinsed to remove any residues.

Figure 2. Preparation of crystal samples. A sample holder covered with graphite epoxy mixture (Gr-Epoxy) was pressed onto a crystal placed on a thin layer of PDMS. After 24 h, the sample holder with the crystal was removed as the epoxy resin had hardened.

Characterization

Electrochemical experiments were carried out with a commercial SECM (Sensolytics, Germany) and connected to a bipotentiostat (PGSTAT302N, Autolab, Netherlands). All potentials refer to a Ag/AgCl (3 M KCl) reference electrode. A Pt wire served as counter electrode. Electrical contact to sample stubs was established with conductive copper tape. The electrochemical cell consisted of two parts screwed together, with the sample placed in between. Images of the assembly are shown in Figure S1.

SECM imaging was conducted with 10 and 25 µm diameter Pt disk ultramicroelectrodes (UMEs, RG > 10, Sensolytics, Germany) in a solution of K3Fe(CN)6 (10 mM in 0.1 M KCl). Prior to imaging, the probe was positioned by performing probe approach curves (PACs) above the respective crystal surface (shown in Figure S2). The probe was approached until the probe made contact to the sample, yielding a reference PAC for estimating the substrate-to-tip distance. Prior to SECM imaging, the probe was then polished and reapproached until a well-established feedback response was obtained. Fitting this PAC to the reference PAC, an estimation about the substrate-to-tip distance at the beginning of the SECM images was possible. For images of TiS2, the initial distance was 18 µm; for TiSe2 it was 6 µm. SECM images were recorded with a pixel size of 10 µm and a maximum probe velocity of 300 µm s−1. Feedback mode images were obtained with a probe potential of EUME = −0.2 V applied and the substrate remaining at open circuit potential, while substrate generation/ tip collection (SG/TC) images were recorded with substrate and probe potentials of ESubstrate = −0.5 and EUME = 0.4 V, respectively. The potential values were set to ensure steady current responses and were derived from cyclic voltammograms recorded with probes and samples (Figure S3). Data processing of SECM images was done with Gwyddion 2.55 and Origin 2020 software.

Correlation of the AFM positions was achieved via optical images recorded prior to performing AFM (Dimension Icon with Airasyst cantilever, Bruker, USA). SEM and EDS images were obtained with a MIRA 3 SEM (Tescan, Czech Republic) and a Bruker XFlash 5010 EDS with an accelerating voltage of 20 kV used. Elemental composition of the samples was further confirmed by XPS (AXIS SupraTM, Kratos, United Kingdom). Spectra were recorded using a monochromatic Al Ka (1486.7 eV) excitation source and calibrated against the carbon 1s signal at 284.8 eV. Evaluation was performed with Casa XPS software.

Results and discussion

Images of TiS2 obtained via SEM (Figure 3A) revealed a flat crystal structure surrounded by highly conductive graphite/epoxy resin blend. Multiple edges and cracks within the crystal were visible. EDS (Figure S4) showed the presence of mainly Ti and S in the crystal. A homogeneous oxygen distribution was indicated with slight deviations at the cracks in the surface. XPS analysis indicated the presence of sulfides and oxides on the crystal surface (Figure S5). In Table S1, the measured atomic percentages are listed. A ratio between Ti and S of ca. 1.45 is observable, which is explainable by the formation of oxides, which is also indicated by the EDS analysis. Generally, high C and O content was measured from the graphite-epoxy mixture surrounding the crystal.

The local electrochemical activity was analyzed (yellow box in Figure 3A) via SECM performed in feedback and SG/TC mode (Figure 3B and C, respectively). The processes occurring in the respective SECM measurement /modes are illustrated in Figure S6. The feedback mode imaging, where the mediator species is converted at the probe in dependence of the sample conductivity, revealed a uniform conductivity over the entire crystal area. The orange-colored area corresponds to the highly conductive carbon surface of the graphite-epoxy mixture, which was surrounding the crystal. On the crystal itself, small deviations correlate with material grains visible in the SEM image (Figure 3A). Due to the large probe diameter of 25 µm, small topographical variations remain undetected in the feedback mode SECM image. The white hole in the top part of the image corresponds to a rough portion within the epoxy resin. Figure S7 showing the image in full current scale. In contrast, the SG/TC mode indicated differences in the local electrochemical activity as the mediator is reduced at the sample and the generated species is subsequently collected at the probe. The comparison with the SEM image shows that some of the poorly visible edges exhibit a high activity, while other more visible edges did not appear to be considerably electrochemically active. In addition, the bottom right area of the crystal, showing a high density of cracks in the SEM image, appears highly active in the SG/TC image while a low current was measured in feedback mode. Both observations are indicating a high electrochemical activity of crystal edges. To further analyze size and morphology of the edges at which the increased activity occurred, AFM was conducted at two different locations of the crystal to cover regions of high (position D) and low (position G) electrochemical activity. Their positions relative to SEM and SECM images are indicated in Figure 3A-C. From the optical overview image recorded prior to AFM (Figure S8), the edge at spot D can be localized. In Figure 3D, an AFM image of a highly electrochemically active edge is shown. It appeared as a sharp step of 200 nm height difference. Comparing the extracted lines from the SECM (Figure 3E) and AFM (Figure 3F) images, the sharp step appeared considerably broader in the SECM image due to the probe size of 25 µm. In contrast, another AFM image of an edge exhibiting no noticeable increase of activity was obtained at position G (Figure 3G). The edge appeared convoluted and considerably rougher than the edge investigated in Figure 3D. The extracted AFM line in Figure 3I shows that the edge consisted of a convolution of about 1 µm thickness followed by another step of 800 nm height. The extracted line from the SG/TC SECM image in Figure 3H which covers the edge does not indicate noticeable activity differences. In contrast, at the 200 nm edge in Figure 3D, a current increase of about 2 nA was detected. This nm-sized edge is visible in the µm-scaled SECM image due to two reasons. 1) The diffusion layer at the active sites was growing for several minutes before the SG/TC SECM image was recorded. 2) Due to its electroactive diameter of 25 µm, the SECM is in contact with this diffusion layer over a long lateral distance, which eventually leads to the active edge appearing more than 50 µm wide in the SG/TC SECM image.

To confirm the increased activity observed at the TiS2 crystal edges, we additionally investigated the electrochemical activity at well-designed crystal edges. Therefore, a second TiS2 crystal was studied, which contained artificially created edges (introduced by cutting the top layers of the TiS2 crystal with a scalpel). Figure S9A and S9B show the crystal before and after cutting, respectively. SG/TC mode SECM imaging (Figure S9C) shows that both edges naturally occurring in the crystal, as well as artificially created edges exhibit increased electrochemical activity. The presence of the natural edge was confirmed by AFM (Figure S9D-F), while the artificial edge was too rough to be measured.

Since previous localized studies with MoS2 and WS2 have shown increased electrochemical activity at edges compared to basal planes,30,32,33 and considering the obtained results we conclude that the same occurs in case of TiS2. However, not in any case did the edge size correlate with activity, which could be due inconsistent electrical connections inside the crystal.

Figure 3. Characterization of the TiS2 crystal. A: Scanning electron micrograph including indicators for the imaging locations of AFM images D/G (dots). B/C: SECM images of the crystal recorded in feedback (B) and SG/TC (C) mode in 10 mM K3Fe(CN)6 as mediator. Probe diameter: 25 µm; Pixel size: 10 µm; Substrate-to-tip distance: 18 µm. EUME = −0.2 V (B), 0.4 V (C). ESubstrate = −0.5 V (C) D/G: AFM images of crystal edges at the positions indicated in A-C. E/H: Current profiles extracted from C, crossing spots D and G, respectively. F/I: Line profiles extracted from D and G.

As second representative of group IV TMDs, a TiSe2 crystal was investigated. The SEM micrograph of the crystal (Figure 4A) shows a very rough surface at the crystal borders and in the top left region. However, the crystal appears predominantly flat, especially in the top right region. Notably, a slightly brighter appearing area can be seen in the bulk crystal (red boxes in Figures 4A-D), where a lower amount of oxygen compared to the other parts of the crystal was determined via EDS (Figure 4B) which might indicate a local difference in surface composition. EDS maps of other elements are presented in Figure S11, showing a homogeneous distribution along the crystal surface. XPS analysis (Figure S12) of the sample showed presence of Ti and Se. Atomic percentages in Table S2 show 1.75% Ti vs 0.86% Se. The area highlighted by a yellow box in the SEM image was studied via SECM in feedback and SG/TC mode (Figure 4C and D). The feedback image shows a low but uniform conductivity in the parts of the crystal that appear smooth in the SEM image. At the crystal border, higher current deviations were measured due to more pronounced height differences stemming from larger cracks in the crystal. The orange areas in Figure 4C correlate with the rough and dark areas visible in the SEM image showing the graphite-epoxy resin. In SG/TC mode, the crystal surface shows apparent differences in the electrochemical activity. Especially within the regions of the crystal with a rough topography small, remarkably active spots appear (predominantly in the dark green area in Figure 4C), which are caused by edges being exposed due to cracks in the crystal surface. In addition, protrusions from the crystal surface that are associated with the cracks result in a lower substrate-to-tip distance, increasing the measured current even further. Smaller differences in electrochemical activity can be linked to cracks revealing active edges, which are visible in the SEM image, for example at the spots marked with “x” in SEM and SECM images.

Furthermore, the region corresponding to a decreased oxygen content visible in the EDS image exhibited an increased electrochemical activity. This observation is in line with activity differences occurring at group VI TMDs due to the formation of surface oxides.43 In this region, the surface topography at the transition from high to low oxygen content was investigated via AFM imaging. For comparison, a second edge within the low oxygen area was imaged. The exact locations are indicated in Figures 4A-D. Figure 4E shows the AFM image obtained at the transition from low to high oxygen content showing a straight and clear edge. The bright part below the edge corresponds to the area of high oxygen content, while low amounts of oxygen were determined to be on the other side. The extracted line in Figure 4F shows a sharp edge with a height difference of 300 nm and a higher surface roughness in the low oxygen area. The increased roughness (and thus surface area) and the decreased oxygen content, both might contribute to the increased electrochemical activity.43 However, we assume that the oxygen content only has a minor effect on electrochemical activity since no conductivity difference was observed in the feedback mode SECM image. Similar to TiS2, not all edges were observed to be electrochemically active. Spot G did not show any activity in the SG/TC image despite an edge being present (see AFM in Figure 4G and the extracted line profile in Figure 4H), which might be due to differences in electrical connection inside the crystal (Note that these crystals are multi-layered structures). However, the exact impact of the crystallographic structure of the edges on the electrochemical activity of the investigated crystals could not be resolved because of their multilayered and randomized structure and technical limitations. Nevertheless, the observations above show that microscopic cracks and edges can induce increased electrochemical activity. Furthermore, local differences in oxygen content on the surface might contributed to inhomogeneities in activity, as areas of higher oxygen concentration (shown by EDS in Figure 4B) showed a reduced electrochemical activity of TiSe2. Our experiments with TiS2 and TiSe2 so far show that electrochemical model reactions occur predominantly at crystal edges.

Figure 4. Characterization of the TiSe2 crystal. A: Scanning electron micrograph of the TiSe2 crystal. Imaging locations of SECM recordings C/D (yellow box) and AFM images E/G (dots) are highlighted. B: EDS map showing the oxygen distribution in the area covered by A. The red boxes in A-D highlight the location of low oxygen content. C/D: SECM images of the crystal recorded in feedback (C) and SG/TC (D) mode recorded in 10 mM K3Fe(CN)6. Probe diameter: 10 µm. Pixel size: 10 µm. Substrate-to-tip distance: 15 µm. EUME = −0.2 V (C), 0.4 V (D). ESubstrate = −0.5 V (D) E/G: AFM images of different crystal edges. F/H: Line profiles extracted from E/G. “x” in A, C and D mark exemplary locations of active crystal edges.

Conclusions

In this work, we tackled the persisting question if a higher electrochemical activity at the edges of crystals is a general trend in nature for layered materials. Localized electrochemical investigations performed via SECM over crystalline TiS2 and TiSe2 have shown an increased electrochemical activity at crystal edges and microscopic cracks compared to basal planes. With these results, we showed that differences in electrochemical activity between basal planes and crystal edges exist within the group IV TMDs TiS2 and TiSe2 − in analogy to other 2D materials like graphite, layered pnictogens and group VI TMDs. Further analysis utilizing SEM, EDS and AFM were employed to support these findings. Nevertheless, basal planes did not appear completely electrochemically inactive. As bulk TMD crystals were studied herein, the observed edges were mostly multi-layered, and consequently of mixed crystallographic structure. Since crystallographic structure of single edges could impact their electrochemical activity, future studies on single layer TMDs could help to answer this question. Nevertheless, these results are important for the future development of alternative energy storage materials and electrocatalysts based on group IV TMDs.

ASSOCIATED CONTENT

Supporting Information. The supporting information contains optical images of a typical TMD single crystal sample and the measurement cell, scanning electron micrographs, EDS elemental maps and XPS wide scan spectra of the investigated samples. An optical image for AFM position correlation of the TiS2 sample is included as well.

AUTHOR INFORMATION

Corresponding Author

*Martin Pumera

*Future Energy and Innovation Laboratory, Central European Institute of Technology, Brno University of Technology, Purkyňova 123, 61200 Brno, Czech Republic

E-mail: pumera.research@gmail.com

Author Contributions

S.W. performed prepared the crystal samples and characterized them via SECM. C. I. performed and SEM, EDS, and AFM measurements. K. A. N. optimized the graphite-epoxy mixture used for sample preparation and performed XPS analysis. F.-M. M. and M. P. supervised this work. M.P. conceptualized the idea. The manuscript was written through contributions of all authors. All authors have given approval to the final version of the manuscript.

Funding Sources

ACKNOWLEDGMENT

M.P. acknowledges the financial support of Grant Agency of the Czech Republic (EXPRO: 19-26896X). S.W. would like to thank the Bayerisch-Tschechische Hochschulagentur for financial support (Project: BTHA-MOB-2020-10). C.I. acknowledges the financial support by the European Union’s Horizon 2020 research and innovation program under the Marie Skłodowska-Curie grant agreement No. 888797. K.A.N. acknowledge the financial support from Quality Internal Grants of BUT (KInG BUT) (Reg.No. CZ.02.2.69/0.0/0.0/19_073/0016948), financed from the OP RDE. The authors gratefully acknowledge the CzechNanoLab project LM2018110 funded by MEYS CR for the financial support of the measurements/sample fabrication at CEITEC Nano Research Infrastructure.

ABBREVIATIONS

AFM, atomic force microscope, EDS, energy dispersive X-ray spectroscopy; PAC, probe approach curve; PDMS, polydimethylsiloxane; SECM, scanning electrochemical microscopy; SEM, scanning electron microscope; SG/TC, substrate generation/tip collection; TMD, transition metal dichalcogenide.

REFERENCES

(1) Banks, C. E.; Davies, T. J.; Wildgoose, G. G.; Compton, R. G. Electrocatalysis at graphite and carbon nanotube modified electrodes: edge-plane sites and tube ends are the reactive sites. Chem. Commun.2005 (7), 829–841. DOI: 10.1039/b413177k.

(2) Davies, T. J.; Hyde, M. E.; Compton, R. G. Nanotrench arrays reveal insight into graphite electrochemistry. Angew. Chem. Int. Ed. 2005, 44 (32), 5121–5126. DOI: 10.1002/anie.200462750.

(3) Neumann, C. C. M.; Batchelor-McAuley, C.; Downing, C.; Compton, R. G. Anthraquinone monosulfonate adsorbed on graphite shows two very different rates of electron transfer: surface heterogeneity due to basal and edge plane sites. Chem. Eur. J. 2011, 17 (26), 7320–7326. DOI: 10.1002/chem.201002621.

(4) Yuan, W.; Zhou, Y.; Li, Y.; Li, C.; Peng, H.; Zhang, J.; Liu, Z.; Dai, L.; Shi, G. The edge- and basal-plane-specific electrochemistry of a single-layer graphene sheet. Sci. Rep. 2013, 3, 2248. DOI: 10.1038/srep02248.

(5) Wang, L.; Sofer, Z.; Pumera, M. Will Any Crap We Put into Graphene Increase Its Electrocatalytic Effect? ACS Nano 2020, 14 (1), 21–25. DOI: 10.1021/acsnano.9b00184.

(6) Pumera, M. Materials Electrochemists’ Never-Ending Quest for Efficient Electrocatalysts: The Devil Is in the Impurities. ACS Catal. 2020, 10 (13), 7087–7092. DOI: 10.1021/acscatal.0c02020.

(7) Marvan, P.; Huber, Š.; Luxa, J.; Mazánek, V.; Sedmidubský, D.; Sofer, Z.; Pumera, M. Edge vs. basal plane electrochemistry of layered pnictogens (As, Sb, Bi): Does edge always offer faster electron transfer? Appl. Mater. Today 2019, 16, 179–184. DOI: 10.1016/j.apmt.2019.05.009.

(8) Sofer, Z.; Sedmidubský, D.; Huber, Š.; Luxa, J.; Bouša, D.; Boothroyd, C.; Pumera, M. Layered Black Phosphorus: Strongly Anisotropic Magnetic, Electronic, and Electron-Transfer Properties. Angew. Chem. Int. Ed. 2016, 55 (10), 3382–3386. DOI: 10.1002/anie.201511309.

(9) Sturala, J.; Sofer, Z.; Pumera, M. Chemistry of Layered Pnictogens: Phosphorus, Arsenic, Antimony, and Bismuth. Angew. Chem. Int. Ed. 2019, 58 (23), 7551–7557. DOI: 10.1002/anie.201900811.

(10) Beladi-Mousavi, S. M.; Pumera, M. 2D-Pnictogens: alloy-based anode battery materials with ultrahigh cycling stability. Chem. Soc. Rev. 2018, 47 (18), 6964–6989. DOI: 10.1039/C8CS00425K.

(11) Pumera, M.; Sofer, Z. 2D Monoelemental Arsenene, Antimonene, and Bismuthene: Beyond Black Phosphorus. Adv. Mater. 2017, 29 (21), 1605299. DOI: 10.1002/adma.201605299.

(12) Tan, S. M.; Ambrosi, A.; Sofer, Z.; Huber, Š.; Sedmidubský, D.; Pumera, M. Pristine Basal- and Edge-Plane-Oriented Molybdenite MoS2 Exhibiting Highly Anisotropic Properties. Chem. Eur J. 2015, 21 (19), 7170–7178. DOI: 10.1002/chem.201500435.

(13) Tsai, C.; Chan, K.; Abild-Pedersen, F.; Nørskov, J. K. Active edge sites in MoSe2 and WSe2 catalysts for the hydrogen evolution reaction: a density functional study. Phys. Chem. Chem. Phys. 2014, 16 (26), 13156–13164. DOI: 10.1039/c4cp01237b.

(14) Tuxen, A.; Kibsgaard, J.; Gøbel, H.; Laegsgaard, E.; Topsøe, H.; Lauritsen, J. V.; Besenbacher, F. Size threshold in the dibenzothiophene adsorption on MoS2 nanoclusters. ACS Nano 2010, 4 (8), 4677–4682. DOI: 10.1021/nn1011013.

(15) Jaramillo, T. F.; Jørgensen, K. P.; Bonde, J.; Nielsen, J. H.; Horch, S.; Chorkendorff, I. Identification of Active Edge Sites for Electrochemical H2 Evolution from MoS2 Nanocatalysts. Science 2007, 317 (5834), 100–102. DOI: 10.1126/science.1141483.

(16) Chia, X.; Eng, A. Y. S.; Ambrosi, A.; Tan, S. M.; Pumera, M. Electrochemistry of Nanostructured Layered Transition-Metal Dichalcogenides. Chem. Rev. 2015, 115 (21), 11941–11966. DOI: 10.1021/acs.chemrev.5b00287.

(17) Ghosh, K.; Pumera, M. Free-standing electrochemically coated MoSx based 3D-printed nanocarbon electrode for solid-state supercapacitor application. Nanoscale 2021, 13 (11), 5744–5756. DOI: 10.1039/D0NR06479C.

(18) Chia, X.; Pumera, M. Characteristics and performance of two-dimensional materials for electrocatalysis. Nat. Catal. 2018, 1 (12), 909–921. DOI: 10.1038/s41929-018-0181-7.

(19) Tan, S. M.; Pumera, M. Two-Dimensional Materials on the Rocks: Positive and Negative Role of Dopants and Impurities in Electrochemistry. ACS Nano 2019, 13 (3), 2681–2728. DOI: 10.1021/acsnano.8b07795.

(20) Novoselov, K. S.; Jiang, D.; Schedin, F.; Booth, T. J.; Khotkevich, V. V.; Morozov, S. V.; Geim, A. K. Two-dimensional atomic crystals. PNAS 2005, 102 (30), 10451–10453. DOI: 10.1073/pnas.0502848102.

(21) Nicolosi, V.; Chhowalla, M.; Kanatzidis, M. G.; Strano, M. S.; Coleman, J. N. Liquid Exfoliation of Layered Materials. Science 2013, 340 (6139), 1226419. DOI: 10.1126/science.1226419.

(22) Gusmão, R.; Sofer, Z.; Bouša, D.; Pumera, M. Pnictogen (As, Sb, Bi) Nanosheets for Electrochemical Applications Are Produced by Shear Exfoliation Using Kitchen Blenders. Angew. Chem. Int. Ed. 2017, 56 (46), 14417–14422. DOI: 10.1002/anie.201706389.

(23) Muller, G. A.; Cook, J. B.; Kim, H.-S.; Tolbert, S. H.; Dunn, B. High performance pseudocapacitor based on 2D layered metal chalcogenide nanocrystals. Nano Lett. 2015, 15 (3), 1911–1917. DOI: 10.1021/nl504764m.

(24) Chen, D.; Ji, G.; Ding, B.; Ma, Y.; Qu, B.; Chen, W.; Lee, J. Y. In situ nitrogenated graphene-few-layer WS2 composites for fast and reversible Li+ storage. Nanoscale 2013, 5 (17), 7890–7896. DOI: 10.1039/c3nr02920d.

(25) Wu, S.; Zeng, Z.; He, Q.; Wang, Z.; Wang, S. J.; Du, Y.; Yin, Z.; Sun, X.; Chen, W.; Zhang, H. Electrochemically reduced single-layer MoS₂ nanosheets: characterization, properties, and sensing applications. Small 2012, 8 (14), 2264–2270. DOI: 10.1002/smll.201200044.

(26) Yu, X.; Sivula, K. Toward Large-Area Solar Energy Conversion with Semiconducting 2D Transition Metal Dichalcogenides. ACS Energy Lett. 2016, 1 (1), 315–322. DOI: 10.1021/acsenergylett.6b00114.

(27) Voiry, D.; Salehi, M.; Silva, R.; Fujita, T.; Chen, M.; Asefa, T.; Shenoy, V. B.; Eda, G.; Chhowalla, M. Conducting MoS₂ nanosheets as catalysts for hydrogen evolution reaction. Nano Lett. 2013, 13 (12), 6222–6227. DOI: 10.1021/nl403661s.

(28) Pumera, M.; Sofer, Z.; Ambrosi, A. Layered transition metal dichalcogenides for electrochemical energy generation and storage. J. Mater. Chem. A 2014, 2 (24), 8981–8987. DOI: 10.1039/C4TA00652F.

(29)	Yuan, W.; Zhou, Y.; Li, Y.; Li, C., Peng, H.; Zhang, J.; Liu, Z.; Dai, L.; Shi, G. The edge- and basal-plane-specific electrochemistry of a single-layer graphene sheet. Sci. Rep. 2013, 3, 2248. DOI: 10.1038/srep02248.

(30) Bentley, C. L.; Kang, M.; Maddar, F. M.; Li, F.; Walker, M.; Zhang, J.; Unwin, P. R. Electrochemical maps and movies of the hydrogen evolution reaction on natural crystals of molybdenite (MoS2): basal vs. edge plane activity. Chem. Sci. 2017, 8 (9), 6583–6593. DOI: 10.1039/c7sc02545a.

(31) Takahashi, Y.; Kobayashi, Y.; Wang, Z.; Ito, Y.; Ota, M.; Ida, H.; Kumatani, A.; Miyazawa, K.; Fujita, T.; Shiku, H.; Korchev, Y. E.; Miyata, Y.; Fukuma, T.; Chen, M.; Matsue, T. High-Resolution Electrochemical Mapping of the Hydrogen Evolution Reaction on Transition-Metal Dichalcogenide Nanosheets. Angew. Chem. Int. Ed. 2020, 59 (9), 3601–3608. DOI: 10.1002/anie.201912863.

(32) Tao, B.; Unwin, P. R.; Bentley, C. L. Nanoscale Variations in the Electrocatalytic Activity of Layered Transition-Metal Dichalcogenides. J. Phys. Chem. C 2020, 124 (1), 789–798. DOI: 10.1021/acs.jpcc.9b10279.

(33) Bentley, C. L.; Kang, M.; Unwin, P. R. Nanoscale Surface Structure-Activity in Electrochemistry and Electrocatalysis. J. Am. Chem. Soc. 2019, 141 (6), 2179–2193. DOI: 10.1021/jacs.8b09828.

(34) Yan, C.; Gong, C.; Wangyang, P.; Chu, J.; Hu, K.; Li, C.; Wang, X.; Du, X.; Zhai, T.; Li, Y.; Xiong, J. 2D Group IVB Transition Metal Dichalcogenides. Adv. Funct. Mater. 2018, 28 (39), 1803305. DOI: 10.1002/adfm.201803305.

(35) Toh, R. J.; Sofer, Z.; Pumera, M. Catalytic properties of group 4 transition metal dichalcogenides (MX2 ; M = Ti, Zr, Hf; X = S, Se, Te). J. Mater. Chem. A 2016, 4 (47), 18322–18334. DOI: 10.1039/C6TA08089H.

(36) Wan, C.; Gu, X.; Dang, F.; Itoh, T.; Wang, Y.; Sasaki, H.; Kondo, M.; Koga, K.; Yabuki, K.; Snyder, G. J.; Yang, R.; Koumoto, K. Flexible n-type thermoelectric materials by organic intercalation of layered transition metal dichalcogenide TiS2. Nat. Mater. 2015, 14 (6), 622–627. DOI: 10.1038/nmat4251.

(37) Zhang, W.; Huang, Z.; Zhang, W.; Li, Y. Two-dimensional semiconductors with possible high room temperature mobility. Nano Res. 2014, 7 (12), 1731–1737. DOI: 10.1007/s12274-014-0532-x.

(38) Sun, L.; Chen, C.; Zhang, Q.; Sohrt, C.; Zhao, T.; Xu, G.; Wang, J.; Wang, D.; Rossnagel, K.; Gu, L.; Tao, C.; Jiao, L. Suppression of the Charge Density Wave State in Two-Dimensional 1T-TiSe2 by Atmospheric Oxidation. Angew. Chem. Int. Ed. 2017, 56 (31), 8981–8985. DOI: 10.1002/anie.201612605.

(39) Tao, H.; Zhou, M.; Wang, R.; Wang, K.; Cheng, S.; Jiang, K. TiS2 as an Advanced Conversion Electrode for Sodium-Ion Batteries with Ultra-High Capacity and Long-Cycle Life. Adv. Sci. 2018, 5 (11), 1801021. DOI: 10.1002/advs.201801021.

(40) Tang, J.; Huang, X.; Lin, T.; Qiu, T.; Huang, H.; Zhu, X.; Gu, Q.; Luo, B.; Wang, L. MXene derived TiS2 nanosheets for high-rate and long-life sodium-ion capacitors. Energy Storage Mater. 2020, 26, 550–559. DOI: 10.1016/j.ensm.2019.11.028.

(41) Li, P.; Zheng, X.; Yu, H.; Zhao, G.; Shu, J.; Xu, X.; Sun, W.; Dou, S. X. Electrochemical potassium/lithium-ion intercalation into TiSe2: Kinetics and mechanism. Energy Storage Mater. 2019, 16, 512–518. DOI: 10.1016/j.ensm.2018.09.014.

(42) Novoselov, K. S.; Geim, A. K.; Morozov, S. V.; Jiang, D.; Zhang, Y.; Dubonos, S. V.; Grigorieva, I. V.; Firsov, A. A. Electric field effect in atomically thin carbon films. Science 2004, 306 (5696), 666–669. DOI: 10.1126/science.1102896.

(43) Eng, A. Y. S.; Ambrosi, A.; Sofer, Z.; Šimek, P.; Pumera, M. Electrochemistry of transition metal dichalcogenides: strong dependence on the metal-to-chalcogen composition and exfoliation method. ACS Nano 2014, 8 (12), 12185–12198. DOI: 10.1021/nn503832j.

For table and contents only.

Supporting Information

Impact of corrosion caused by the hydrogen evolution reaction in transition metal dichalcogenide bulk crystals

Stefan Werta, Christian Iffelsbergera, Katarina A. Novčića, and Martin Pumera*a,b,c,d

aFuture Energy and Innovation Laboratory, Central European Institute of Technology, Brno University of Technology, Purkyňova 123, 61200 Brno, Czech Republic

bDepartment of Chemistry and Biochemistry, Mendel University in Brno, Zemedelska 1, CZ-613 00, Brno, Czech Republic

cDepartment of Chemical and Biomolecular Engineering, Yonsei University, 50 Yonsei-ro, Seodaemun-gu, Seoul 03722, Korea

dDepartment of Medical Research, China Medical University Hospital, China Medical University, No. 91 Hsueh-Shih Road, Taichung 40402, Taiwan

Fig. S1: PACs towards the graphite/epoxy regions of TiS2 (A), TiSe2 (B), and MoS2 (C) samples. To determine the substrate-to-tip distance of SECM images, a PAC was performed until the probe made contact to the substrate (dashed line), followed by a PAC which stopped at the working distance (solid line). Parameters: Max speed: 1.0 µm s−1, step width: 1.0 µm, 0.5 V.

Fig. S2. A: SEM + EDS images of pristine TiS2. A: SEM image, B-E: EDS images for Ti, S, C, O.

Figure S2. Probe approach curves towards TiS2 (A, 25 µm probe diameter), TiSe2 (B, 10 µm probe diameter) and graphite-epoxy resin (C, 25 µm probe diameter) in 10 mM ferricyanide solution. Parameters: Max speed: 5 µm s-1 (A); 4 µm s-1 (B), step width: 1.0 µm (A); 0.2 µm (B), UME potential: -0.2 V. For TiS2 and TiSe2, another set of PACs was recorded until surface contact was made (blue curves), in order to estimate the substrate-to-tip distance during SECM imaging.

Figure S3: Cyclic voltammograms of probes and samples prior to SECM imaging. A: TiS2 sample, B: 25 µm diameter UME for TiS2 imaging, C: TiSe2 sample, D: 10 µm diameter UME for TiS2 imaging,

Figure S4. Scanning electron micrograph (A) and EDS elemental maps of TiS2 for Ti (B), S (C), C (D) and O (E).

Figure S5. XPS wide scan spectrum of the TiS2 crystal.

Table 1. Data about major peaks within the TiS2 crystal XPS wide scan spectrum.

| Name | Pos. | FWHM | Area | At% |
| --- | --- | --- | --- | --- |
| O 1s | 530.63 | 4.87 | 5231.75 | 15.89 |
| C 1s | 283.63 | 5.37 | 8438.85 | 71.92 |
| N 1s | 397.63 | 6.30 | 1525.06 | 7.57 |
| S 2p | 163.63 | 4.85 | 354.05 | 1.26 |
| Si 2p | 100.63 | 4.97 | 344.99 | 2.49 |
| Ti 2p | 459.63 | 4.60 | 734.19 | 0.87 |

Figure S6A. Tip and substrate processes occurring during feedback mode SECM imaging using a ferricyanide (Fe3+, Fe(CN)63-) redox probe. In case of a conductive substrate, a feedback loop is established, leading to high mediator conversion rates and thus high currents measured at the probe tip. In the isolating case, the mediator conversion at the tip is limited by diffusion. B: SG/TC mode processes. A potential is applied at the substrate to generate ferrocyanide (Fe2+, Fe(CN)64-), which in turn is oxidized at the SECM probe.

Figure S7. Feedback SECM image of the TiS2 sample from Figure 3B with expanded current range.

Figure S8. Optical microscope image prior to AFM image of spot D in Figure 3. The area where AFM was performed is highlighted.

Figure S9A, B. Microscopic images of the TiS2 crystal before and after addition of artificial edges, respectively. C: SG/TC SECM of the crystal in 10 mM K3Fe(CN)6 as mediator. Probe diameter: 25 µm; Pixel size: 10 µm; Substrate-to-tip distance: 18 µm. EUME = 0.4 V. ESubstrate = −0.5 V. D: Optical image recorded prior to AFM. E: AFM image covering an active edge naturally occurring within the crystal. F: Extracted line from the AFM image (E).

Figure S10. Scanning electron micrograph (A) and EDS elemental maps of TiSe2 for Ti (B), Se (C), C (D), and O (E).

Figure S11. XPS wide spectrum of the TiSe2 crystal.

Table 2. Data about major peaks within the TiSe2 crystal XPS wide scan spectrum.

| Name | Pos. | FWHM | Area | At% |
| --- | --- | --- | --- | --- |
| O 1s | 531.70 | 4.55 | 6088.41 | 24.32 |
| C 1s | 284.70 | 3.64 | 5741.08 | 64.34 |
| N 1s | 400.70 | 3.91 | 495.45 | 3.24 |
| Ti 2p | 457.70 | 3.11 | 1125.73 | 1.75 |
| Si 2p | 101.70 | 3.76 | 577.05 | 5.48 |
| Se 3p | 152.70 | 3.42 | 352.04 | 0.86 |