1.  Method for stopped-flow fluorescence studies for water permeation

To acquire the osmotic single-channel water permeability pf from the raw data, we first calibrated the relative fluorescence of CF (F) by its concentration [CF] (mM) (1):

F=-0.4781CF+1.2338

Assuming that the initial concentration of CF (0.5 mM) became three times higher (1.5 mM) due to the volume shrinkage as the concentration difference between the salt inside ([NaCl] = 100 mM) and the outside ([NaCl] = 300 mM) the vesicle was relaxed, we normalized the raw fluorescence intensities to [F [CF]=1.5 mM, F [CF]=0.5 mM].  Then, the relative fluorescence intensities RFL(t) were converted to the relative intravesicular volumes V(t) using the calibration curve (1):

Vt=-0.2391/(RFLt-1.2338)

The converted data V(t) were fitted using a single-exponential function.  The values of V(t) in the initial stage were obtained by extrapolating the fitted curve.  The osmotic water permeability coefficient Pf (cm s–1) was determined using Equation (2):

dV(t)dt=PfSAVMVW[(CinV(t))-Cout]

where V(t) is the relative intravesicular volume as a function of time; SAV is the initial vesicular surface-area-to-volume ratio; MVW is the molar volume of water (18 cm3 mol–1); and Cin and Cout are the initial concentrations of total solutes inside and outside the vesicle, respectively.

From the slope Pf(SAV)(MVW)Cin of the plot dV(t)/dt versus 1/V(t) in the initial stage, we obtained Pf.  The single-channel osmotic water permeability pf (cm3 s–1 channel–1) was calculated from Pf as follows:

pf=(Pf with channel-Pf without channel)M

where Pf with channel and Pf without channel denote the osmotic water permeability coefficients of vesicles with channels and without channels, respectively.  The latter value is reported to be negligible for DPPC phospholipid bilayer membranes at 25 °C (3).  M is the number of channels in the vesicle per unit area.  The number of channels in the vesicle was calculated using the following method.  First, the average number of lipid molecules in one vesicle was calculated considering the cross-sectional area of a lipid molecule (0.665 nm2 for DPPC) and the vesicle surface area obtained from the dimeter of the vesicles based on the DLS measurement (4, 5).  The number of nanorings per channel was 10 which was estimated using the DFT (density functional theory)-optimized stacking distance of the nanorings and the membrane thickness of DPPC vesicles (3.7 nm) (1).  By dividing the number of nanorings in one vesicle by that required for one channel, we could obtain the average number of channels in the vesicle.  We analyzed the individual raw data and averaged them to obtain the water permeability values together with the standard deviation.

2.  Method for stopped-flow light-scattering studies

To acquire the osmotic single-channel water permeability pf from the raw data, we first normalized the raw light scattering data to [0, 1] and fitted the normalized light scattering data with a sum of two exponential functions, and obtained two exponential coefficients, k1 and k2.  Since the water permeation through the channel likely occurred in the initial stage, we first fitted the initial stage of the normalized light scattering data and then expanded the fitting to the whole range.  The smaller exponential coefficient k1 was assigned to the water permeation through the phospholipid bilayer of vesicles and not that through the channel, because its value was close to that obtained using DOPC vesicles without a nanoring.  The larger exponential coefficient k2 was assigned to water permeation through the channels, as its value changed with χ.  The osmotic water permeability coefficient Pf (cm s–1) due to the channel was determined using the following equation (6):

Pf=k2[SAV∙MVW∙Cin-Cout]

where SAV is the initial vesicular surface-area-to-volume ratio; MVW is the molar volume of water (18 cm3 mol–1); and Cin and Cout are the initial concentrations of total solutes inside and outside the vesicle, respectively.

The single-channel osmotic water permeability pf (cm3 s–1 channel–1) was calculated from Pf as follows:

pf=Pf,channelM

where Pf,channel is the osmotic water permeability coefficient of vesicles with channels and M is the number of channels in the vesicle per unit area.  The number of channels in the vesicle was calculated using the following method.  First, the average number of lipid molecules in one vesicle was calculated considering the cross-sectional area of a lipid molecule (0.701 nm2 for DOPC) and the vesicle surface area obtained from the diameter of the vesicles based on the DLS measurement (4, 5).  The number of nanorings per channel was 10 which was estimated using the DFT (density functional theory)-optimized stacking distance of the nanorings and the membrane thickness of DOPC vesicles (3.8 nm) (1).  By dividing the number of nanorings in one vesicle by that required for one channel, we could obtain the average number of channels in the vesicle.  We analyzed the individual raw data and averaged them to obtain the water permeability values together with the standard deviation.

3. References

- Y. Itoh et al., Science. 376, 738–743 (2022).

- X. Zhou et al., Nat. Commun. 3, 949 (2012).

- M. Jansen, A. Blume, Biophys. J. 68, 997–1008 (1995).

- L. T. Mimms, G. Zampighi, Y. Nozaki, C. Tanford, J. A. Reynolds, Biochemistry 20, 833–840 (1981).

- Y. Shen et al., Proc. Natl. Acad. Sci. U.S.A. 112, 9810–9815 (2015).

- R. H. Tunuguntla et al., Science 357, 792–796 (2017).