Recent Advances in Seed Coating Technologies: Transitioning Toward Sustainable Agriculture

Mariam Sohail, Tahira Pirzada, Charles H. Opperman, Saad A. Khan*

Mariam Sohail#, Dr. Tahira Pirzada#, Prof. Saad A. Khan*

Department of Chemical & Biomolecular Engineering, 911 Partners Way, North Carolina State University, Raleigh, 27606, NC, USA.

khan@eos.ncsu.edu

Prof. Charles H. Opperman*

Department of Entomology & Plant Pathology, 840 Method Road, North Carolina State University, Raleigh, 27695, NC.  USA.

warthog@ncsu.edu

#co-first authors

*co-corresponding authors

Abstract

The practice of coating seeds has evolved from ancient agriculture traditions to one of the most widely used aids in achieving enhanced crop yields. Wide-scale usage of seed coatings has come with its own share of challenges, including agrochemical overuse, carrier pollution caused due to non-biodegradable coating material and increased cost. Modern seed coating research aims to overcome these challenges through maintaining a careful balance between high crop yields and a minimum environmental footprint. Herein, we discuss recent developments with an emphasis on the overall agricultural and environmental viability focusing on the coating material synthesis, energy and chemical utilization, effect on seed growth and ultimate fate of the material in the environment. This review features sections on microbe inoculated, polysaccharide based, nanofibrous, hydrogel and nanomaterials based seed coatings along with elucidation of biomass derived seed treatment strategies aimed to close the loop for a circular seed coating agroindustry. We provide an overall comparative analysis of the discussed coating materials and identify future research directives.

Keywords: precision agriculture; targeted delivery; fibrous seed coats; microbe inoculation; bioplastics; circular agroindustry

TOC

OR

This review provides a sustainability perspective on existing seed coating research through comparing potential agricultural benefits with the associated energy, chemical and environmental footprints.

1. Introduction

The term ‘seed coating’ refers to the practice of applying materials (solids, liquids or dispersions) to the external surface of seeds, resulting in the formation of a continuous layer on the surface.1  Seed coating is an ancient practice with early evidence of its use being dated back to as far as 2000 years ago by the ancient Chinese to use mud coated rice seeds in order to secure their position in flooded fields.2 The earliest scientific literature on seed coatings can be traced back to 1866 in the form of a patent3 which proposed the use of wheat flour paste to treat cottonseed to increase their germination rates. Commercially, seed coatings were first produced by a British company in the 1930s followed by wide-scale commercial usage by the 1960s. Since then, with the increase in scientific and agricultural prowess, the world seed market has evolved into a billion dollar industry having an estimated value of 41.6 billion USD in 2018.4 Figure 1 shows recent statistics on the global seed market including (1) the estimated value of the world seed market (Figure 1a); (2) market share by crop type (Figure 1b) where we observe maize, soybean and vegetables to be the major ones with maize being predominant by a large factor (~43% of the market); (3) documented pesticide usage for seed treatments (Figure 1c); which reveals insecticide use (~3,700 tons) to be almost twice that of fungicide (~1500 tons); and (4) top twenty seed exporting countries in 2019 (Figure 1d), with the Netherlands showing the highest export value in horticulture seeds while France reported the highest export rates for field seeds in 2019.

Figure 1: a) Estimated value of global seed market from 2013-2018. (b) Percent crop share of global seed market in 2018. Data for (a) and (b) replotted from independent report published by IHS Markit.4 (c) Amount of reported pesticide used for seed treatment. Data replotted from FAO website.5 (d) Estimated export value of field and horticulture seeds by top twenty seed exporting countries in 2019. Data replotted from International Seed Federation website.6

Seed coating serves a variety of purposes. It modifies the physical characteristics of seeds to achieve uniform seed dimensions which in turn facilitate seed handling and accurate sowing. It controls (delay or expedite) seed germination to facilitate hybrid seed production through synchronizing flowering times of parental lines with different maturities3 and enables early sowing for no-tillage systems.7 Seed coatings can also act as a carrier of agricultural active ingredients (AI) and thus assist seed germination, growth, and protection from pests8–10 before and following germination. Seed weight can be increased through coating which can protect seeds from being displaced by the wind when sown or being blown away during aerial sowing.11 And finally, the precise application of the AI on the seed through coatings minimizes the need to apply the AI over the entire field in addition to reducing off-target exposure. This would make the AI treatment process more sustainable and environmentally friendly compared to aerial spraying.12 Currently, a wide variety of vegetables, field and flower crops use seed coatings. Seed treatment details of some major crops are listed in Table 1.

The rising need to achieve food security for a rapidly increasing world population at minimum environmental damage has increased research interest to provide innovative crop protection solutions, particularly via the use of biopolymers13 and biologics.14 Some recently published reviews13,14 have summarized accomplishments achieved in the area as of now, however herein we have summarized seed coating research from a green chemistry perspective. In particular, we have targeted six out of the total twelve principles of green chemistry.15 Firstly, we have examined coating material synthesis schemes to critique the adherence to green chemistry principle three, four and five highlighting the importance of safer chemical synthesis, design of less hazardous chemicals and use of benign solvents respectively. Secondly, the energy footprint of the coating material synthesis has been evaluated to gauge adherence to principle six discussing importance of energy utilization. Lastly, through investigating raw material source, renewability and ultimate fate of the coating material in the environment, principles seven and ten have been investigated discussing the importance of renewable feed source and material degradation respectively. This discussion on green chemistry has been accompanied by characterizing the effect of the seed coating material on crop yields and existing life cycle assessment (LCA) data to provide a comprehensive analysis of the potential pros and cons of the critiqued research. We start with a brief overview of seed coatings discussing their types, manufacture and applications. Following this we discuss some of the major challenges being faced by the seed coating industry including agrochemical overuse, plastic pollution, and increased cost. Subsequently, innovative solutions to the existing limitations as proposed through modern research are discussed. We conclude with a comparative analysis on various seed coating solutions in terms of their efficacy and environmental impact, identifying information gaps that future research needs to address.

Table 1. Global production (million tonnes) of major crops with their common pests, diseases, and active ingredients (AI) used for seed treatments, and major suppliers. Data summarized and updated from multiple references.4,5,12

| Crop | World production 2020 (Million tonnes)5 | Common pests | Common diseases | Seed treatment solutions | Major suppliers |
| --- | --- | --- | --- | --- | --- |
| Corn | 1,162 | Southern corn billbug; Southern green/brown stinkbug; Sugarcane beetle; Chinch bug and early season aphid; Corn rootworm; Wireworm; White grub Seed corn maggot; Black cutworm; Flea beetle Nematode | Pythium (Midwest); Head smut | Clothianidin; Imidacloprid; Thiamethoxam; Combinations of captan, carboxin, diazinon, maneb, or metalaxyl Metalaxyl and captan Abamectin and Bacillus firmus; Triticonazole; Prothioconazole | Bayer, Corteva, Syngenta, Vilmorin, KWS, AgReliant |
| Cotton | 83 | Nematode; Thrip; Wireworm | Pythium; Rhizoctonia; Thielaviopsis black root | Metalaxyl; Triadimenol or myclobutanil; Abemectin and Larvin; Imidacloprid and thiamethoxam; Disulfoton | Corteva, Bayer, Syngenta |
| Sorghum | 59 | Chinch bug; Aphid (greenbug, yellow sugarcane aphid); Red fire ant |  | Imidacloprid; Thiamethoxam; Fluxofenim | Vilmorin, KWS, Syngenta |
| Canola | 72 | Crucifer flea beetle, cabbage root fly | Seed-borne black leg | Benzimidazole; Dicarboximide; Morpholine; Imidacloprid; Clothianidin; Thiamethoxam; Flupyradifurone | Bayer |
| Small grains - Oat - Wheat - Barley | 25, 760, 157 | Hessian fly; Wireworm; Aphid – vector of barley yellow dwarf virus (BYDV) | Dwarf bunt; Loose smut; Black point (Fusarium scab); Pythium; Loose and covered smut; Dry seed decay | Difenoconazole; Carboxin; Imidacloprid; Triticonazole; Thiamethoxam; Imazalil; Clothianidin; Metalaxyl | Vilmorin, KWS |
| Potato | 359 | Colorado potato beetle | Late blight (Phytophthora infestans); Fusarium dry rot | Maneb; Mancozeb; Cymoxanil; Flutolanil; Fludioxonil; Thiophanate-methyl; Imidacloprid; Thiamethoxam, Fludioxonil | Europlant, HZPC, Syngenta |
| Soybean | 353 | Bean leaf beetle – vector of bean pod mottle virus (BPMV); Bean leaf beetle Thrip; Three-cornered alfalfa hopper; Aphid; Soybean cyst nematode | Pod and stem blight; Pythium; Phytophthora; White mold; Rhizoctonia | Carboxin; Metalaxyl; Mefenoxam; Imidacloprid; Thiram; Azoxystrobin; Clothianidin; Thiabendazole; Captan; Abamectin; Bacillus firmus | Bayer, Corteva, Syngenta, Agreliant |
| Sunflower | 50 | Pale striped flea beetle; Sunflower beetle; Wireworm | Downy mildew | Azoxystrobin; Thiamethoxam; Fenamidone; Mefenoxam; Metalaxyl | Syngenta, Pioneer |
| Sugarbeet | 253 | Beet leafhopper – vector of curly top | Aphanomyces | Hymexazol; Imidacloprid; Clothianidin; Thiamethoxam | KWS |
| Rice | 757 | Rice water weevil; Grape colaspis | Pythium, rice blast, Bakanea | Metalaxyl; Thiamethoxam; Mefenoxam; Azoxystrobin, Fludioxonil, Clothianidin; Trifloxystrobin, Isotianil; Chlorantraniliprole | Bayer, Corteva, Syngenta |

2. Seed coatings types and equipment

2.1 Types of seed coatings

Seed coatings can be characterized as pellets, encrusting or film coatings1,10

Seed pelleting refers to the process of covering seeds with an external material to achieve an overall globular shape. Initially developed to achieve uniform seed dimensions for precision sowing, seed pellets can be used for multiple purposes including seed protection and germination enhancement16. Pellet size and density can vary depending on the nature of the crop and planting conditions. Larger seeds are typically pelleted into smaller sizes whereas smaller seeds typically require larger builds-up17. Pelleting process consists of first stamping the seeds with an adhesive following which the pelleting material is stuck on the seeds through sprinkling. The coated seeds are then rolled achieving a uniform build-up on top of the seeds18. Typical seed pelleting fillers include materials like sand, chalk and peat. Owing to their high porosity and water holding capacity, some fillers such as peat also function as carriers for beneficial microbes in seed pellets.19,20

During seed encrusting or intermediate pelleting, external material is build-up on the seed surface without significantly changing the original seed shape21. Encrusting may increase the seed weight by 20-200%. Similar to pelleting, encrusting is used to achieve uniform seed dimensions as well as loading the seeds with the desired AI22.

Film coatings involve covering the seeds with a thin film layer resulting in nominal (1-10%) weight increase23. These enable accurate AI incorporation24 within the seed coating in addition to facilitating seed flowability within planters24. They are also used to improve seed aesthetics through the use of dyed films25 and are safer for farmers due to reduced chemical dust release18.

2.2 Seed Coating equipment

The earliest seed coating equipment was the rotating pan or drum. In a typical coating cycle, the drum is continuously rotated resulting in coating of the seeds contained within by the wetting liquid and pelleting powder being sprinkled from the top. Seeds are coated to the desired build-up size followed by drying. Typical limitations include low production rates and high labor costs per batch. 26,3

A more standardized seed coating equipment is the rotary seed coater consisting of a rotating cylinder. Seeds and pelletizing materials are continuously rotated within the cylinder, being forced back within the center upon collision with the baffles fitted on the sides achieving a uniform coating on the seeds.26

Modern seed coating equipment includes fluidized beds and side vented drums25 used to produce precise film coatings and encrustings.1,10,27 These equipment achieve coating through the provision of a constant air flow for suspending the seeds while the coating mixture is sprinkled through spray nozzles.

# 3. Key challenges

The vast scale usage of polymeric seed coating treatments has given rise to concerns regarding the overall sustainability of the approach and its effect on the environment and non-target organisms. Some potential challenges are summarized below:

3.1. Pesticide-rich seed dust

Abrasion of pesticide containing seed coatings during seed (1) planting, (2) handling, and (3) storage can result in the production of pesticide-laden seed dust. Figure 2 shows various pathways through which abraded dust from coated seeds can pollute the environment. This abraded dust containing the pesticide can be transported through air movement to off-target sites (adjacent fields, subsurface ground layer, water bodies) resulting in dust drift which can prove fatal to bees and other pollinators in addition to posing health concerns to farmers.27 Furthermore, deposition of the seed dust in surface and ground water reservoirs can result in water pollution.28–31 Moreover, it is also suggested that risks associated with dust-off losses from coated seeds may potentially be underestimated. Foque and coworkers compared seed drift potential of commercially available pre-treated seeds, calculated from Heubach dust meter (traditional method to determine drift potential from treated seeds) with values calculated from dust released from mechanical sieving of seed bags and from individual sowing element of a pneumatic seed drill.28 Drift potential values calculated from Heubach readings were much lower than those obtained from mechanical and individual sowing techniques. This suggests that current methods to quantify drift potential from seed coatings should be corroborated with alternate approaches to accurately identify potential risks and adopt the necessary safety counter-measures. Researchers are also probing mitigation techniques focusing on the design of safer seed coatings with reduced drift potential. In a recent patent, Reichert and coworkers disclosed a method to minimize pesticide dust from coated seeds through lubrication of treated seeds with a wax composition (polyethylene carnauba, paraffin, polypropylene, and oxidized polyethylene wax) in lieu of conventional planting lubricants (talc, graphite). The reduced dust emissions after wax lubrication of insecticide treated corn seeds was shown via calculating dust levels with a Heubach Dustmeter.32 In addition to design alterations, other proposed mitigation strategies include: (1) use of air deflectors in sowing sites to direct dust drift from seeds into sowing channels, (2) use of point of care detectors to gauge and control pesticide levels in the field,33 and (3) rigorous monitoring by regulating authorities to ensure best coating and planting practices are adopted by agrochemical companies and farmers.30

3.2. Pesticide overuse

Seed coatings have been associated with agrochemical overuse, in particular, concerns have been raised over the use of neonicotinoid seed treatments (NSTs). Neonicotinoids are insecticides widely used in seed treatments that are documented to possess low toxicity towards mammals but are highly toxic to bees and other pollinators.34,35 They also pose a threat to predators through transferring down in the food chain (plant-pest-predator) and due to their high water solubility resulting in their rapid mobility in waterways and subsequent penetration into aquatic wildlife and vegetation.36–40 While unwanted environmental dissemination of neonicotinoids may result from either spray or seed treatments, the latter have been identified as their major route of application and thus require more scrutiny. Douglas et al41 compiled data from public (USGC, USDA, North Dakota State University and Minnesota Department of Agriculture) and corporate (Pioneer Hi-Bred International) sources subtracting reported NSTs amounts from the total reported usage to estimate the relative amounts applied as seed treatments. Their findings reveal that from 2000 to 2012 for maize, soybean and wheat, nearly 100% of the total reported neonicotinoid used was applied in the form of seed treatments while for cotton the value ranged around 60-70% after 2004. Furthermore, the relative importance of these figures can be gauged from the fact that for maize for the year 2004, NST alone accounted for 43% of the total documented insecticide use.

Accurate risk assessment of neonicotinoids or any agrochemical for that matter requires precise data on application rates to monitor variations in field conditions and insect populations. While pesticides have increasingly been applied as seed treatments, regulatory data on pesticide usage has mainly been focused on directly applied field pesticides overlooking amounts contained in seed coatings.42,43 Farmers are also generally less aware of pesticides applied through seed treatments compared to the amounts applied directly to crops.43 All these factors have resulted in a general dearth of accurate data on pesticidal seed treatments. The prophylactic use of seed treatments and the difficulty in accessing uncoated seeds has further augmented this issue resulting in pesticide use even when the need does not exist.44 Thus, seed coatings may result in pesticide overuse having catastrophic effects on bees and other beneficial predatory insects.  Recent research in seed treatments to reduce pesticide and other agrochemical intakes has focused on the use of microbe inoculated seed coatings as bio-control agents (details in section 4.1).

3.3. Microplastic coating film (MPCF)

Seed coatings have been reported as a possible route through which microplastics can enter the soil. Detachment of non-biodegradable polymer films from seed coatings can result in persistent polymer fragments in the soil. The term microplastic coating film (MPCF) fragments was first coined by Accinelli et al to define detached seed coating fragments referring to their similarity with microplastics (MP) but with significantly lower thicknesses (< 5-10 μm).29 MPCF has been identified as a potential source of MP in the soil (Refer to Figure 2).45,46 The presence of MP in the soil can change the physical properties of the soil as well as significantly alter soil fertility. Furthermore, their degradation can result in the release of toxic additives in the soil, which can play havoc with the ecosystem and have uncharted effects on the soil quality. They can also be ingested by soil organisms and be transported within the food chain,31 posing a threat to human health. Considering their potential toxicity, regulatory bodies in the EU have proposed banning the use of primary MP in consumer as well as in agriculture products.46

To address this serious issue, academic and industrial research is actively looking into the design of biodegradable and environmentally friendly seed coatings. Recently, Van Trump and coworkers disclosed a method to produce biodegradable coatings for agricultural granules (seeds, fertilizers, pesticides).47 Their biodegradable coatings consisted of a first layer synthesized primarily from polyhydroxyalkanoates along with a second layer composed of alternate biodegradable polymers (polylactic acid, polycaprolactone, polysaccharides, etc). Exposure of the coatings to moisture and microbes in soil would result in hydrolysis-induced decomposition leading to release of encapsulated material (seeds or agrochemicals). Whereas the biodegradability of the proposed coatings makes them environmentally friendly, the microbe driven decomposition of the coatings allows controlled release of the enclosed agrochemical within the coatings. It has also been shown29 that the degradation rate of detached seed coat fragments can be expedited by replacing conventional polymers with biodegradable formulations. We discuss in a subsequent section (4.2) details of recent research done on the design of bio-derived polysaccharide-based polymers as a safer alternative to conventional polymeric seed coatings. In summary though, further research is needed to provide a quantifiable measure of MP accumulation in soil due to the use of plastic-based seed coatings and the replacement of non-biodegradable coatings with biodegradable environmentally friendly materials.

Figure 2: Schematic showing pollution pathways from abraded seed coating fragments containing microplastic particles and pesticide-rich dust. These drift particles can be carried by air movement to neighboring fields and be deposited in both surface and groundwater reservoirs. Ingestion by surrounding flora and fauna can lead to local population decline and contamination of the food chain.

3.4. Other challenges

One potential limitation of film-coated seeds is the restricted oxygen diffusion across the growing embryo and reduced leaching of oxygen consuming inhibitors from the seeds due to the physical barrier presented by the coated layer.48 To counter these limitations, an exciting approach has been the use of polymer fibrous seed coatings which by virtue of partial seed area coverage can overcome the discussed limitation. Details are discussed in section 4.3.

Also, the use of expensive raw materials and complicated processing steps can be a deterrent to achieving benefits from existing seed coating techniques, particularly in developing countries. Thus, there is a need for alternate, easy to implement approaches that can be adopted by smallholder farmers. A recently proposed strategy entailing the use of plant-based fibers to coat seeds prior to planting is discussed in section 5.2.

4. Recent approaches

In this section, we discuss recent investigations to develop seed coatings to address some of the key issues raised in Section 3. Proposed seed coating solutions are evaluated in terms of their effects on seed germination, growth and their environmental impact.

4.1 Plant growth promoting microorganisms (PGPM) inoculated seed coatings

Increasing concerns about the environmental impact of agrochemicals have motivated research on alternative agricultural practices which are sustainable and eco-friendly. In this regard, the application of PGPM is gaining increasing precedence, with many recent studies proposing their use (1) as biofertilizers or biocontrol agents over conventional agrochemicals to achieve the desired crop protection treatment, (2) for enhanced nitrogen fixation, and (3) for promoting phosphate solubilization.25  Figure 3 shows possible types of PGPM and how they can affect plant growth. For instance, plant growth promoting bacteria (PGPB) residing in the rhizosphere (soil vicinity around the root system) could have beneficial effects on plant growth and have applications as biopesticides, bio-fertilizers, and rhizoremediators.1 Rhizobia- the group of bacteria with N2 fixation characteristics, could enable root nodulation in leguminous plants. And finally, there is Arbuscular Mycorrhizal Fungi (AMF), soil-borne fungi with the ability to enhance plant nutrient uptake. They are largely being researched as bio-fertilizers to reduce the amount of synthetic fertilizer in soil.49

Figure 3: Schematic depicting three types of plant growth promoting microbes (PGPM) and their role in enhancing plant growth.

Seed inoculation has been proposed as a suitable method to introduce the desired PGPM in the soil and around the rhizosphere.50 Ensuring the availability of the microorganisms to the root during the early germination stage, allows for timely plant development and enhanced stress resistance. Consequently, current research in seed treatment techniques is investigating the use of bioplastic film coatings as carriers for PGPM. Such a film coating should be able to serve as a suitable growth medium for the loaded microorganism with high survival rates for the inoculated PGPM. In addition, it should possess the necessary attributes of a practical seed coat such as durability to endure stresses during handling, permeability to allow free air movement during germination and ablitlity to crack under the soil to not hinder germination.

Accinelli et al. coated corn and canola seeds with a proprietary starch-based bioplastic treated with (1) imidacloprid plus metalaxyl-M pesticide mixture and (2) spores of Trichoderma harzianum -  a plant growth-boosting fungus as a biocontrol agent.51 They reported that seed germination was significantly higher in the T.harzianum incorporated coated seeds than the pesticide-laden coated seeds, with enhanced growth as observed by the shoot height and root length of the seedlings. The authors have attributed the enhanced growth to the intense colonization of the T.harzianum in the rhizosphere made possible due to the successful incorporation and compatibility of the loaded fungi with the bioplastic-based seed coat. Similarly, Rojas et al.52 investigated different biopolymer-based seed coatings inoculated with the fungus, Trichoderma koningiopsis, a strain of the trichoderma fungal species that are widely used as biopesticides. Out of various biopolymers analyzed in the study, gelatin and pectin showed the highest survival results for the fungus. However, all the coated seeds exhibited delayed germination and seed emergence rates. Thus, whereas the water and gas blocking properties of the polymer films on the seeds provided a viable environment for the survival of the microbes, it also inhibited embryo development resulting in delayed radicle emergence. Further research is needed to optimize the properties of the seed coating such that the coatings can provide a viable medium for the inoculated PGPM and yet not retard seed germination. Table 2 summarizes the results of recently conducted studies on microbe inoculated seed coatings synthesized from various coating materials.

Table 2. Summary of PGPM inoculated seed coatings

| Microbe | Coating material | Plant | Microbe survival count | Performance as seed coating | Reference |
| --- | --- | --- | --- | --- | --- |
| Fungus Trichoderma harzianum | Proprietary bioplastic (starch based) | corn (Zea mays L.) and canola (Brassica napus L.) | Not reported | Growth chamber study Germination significantly improved compared to treatment with synthetic pesticide but no significant improvememts compared to untreated controls. Significant improvements in root and shoot length compared to control. | 51 |
| Fungus Trichoderma koningiopsis | Gelatine, pectin | Rice (Oryza sativa) | 106CFU per seed after 60 days of storage at 6⁰C | Pot trials Samples exhibited delayed germination compared to control 6 days after sowing however this trend was homogenized after 11 days. | 52 |
| PGPB Azospirillum brasilense Cd (ATCC 29710) | Alginate | wheat (Triticum) and tomato (Solanum lycopersicum) | maximum 105 CFU g–1 inoculant bacterial release after 10 days of storage at 4⁰C | Pot trials Significant improvement in plant height and root and leaf dry mass compared to controls. | 53 |
| Fungi Trichoderma spp. | Chitosan/PEG blend | castor (Ricinus communis L.) | 108–1010 spores/ml blend after 3 months of storage at room temperature | Germination assay. Significant improvements in seedling germination, vigor index, shoot and root length were reported compared to untreated controls. | 54 |
| PGPB Pseudomonas libanensis | Pyrovac and Dynamotive Biochar | Corn (Zea mays) | Maximum count of 1.73*103CFU/ml biochar inoculant at 4⁰C storage temperature | Greenhouse trials. Biochar and PGPB combination did not significantly improve growth characteristics. Only significant improvement in seedling root length was reported. | 55 |
| PGPR Burkholderia sp. strain L2 | Biochar | tomato (Lycopersicon esculentum Mill.) | 107 cfu g−1) at 240 days. Storage temperature not mentioned. | Pot trials Significant improvement in seed germination and biometric growth parameters compared to controls | 56 |
| PGPR Pantoea agglomerans ISIB55, Burkholderia caribensis ISIB40 | Polyvinyl alcohol nanofibers | Soybean (Glycine max L.) | 1.6*104 CFU per seed after 30days of storage at room temperature. | Greenhouse trials Significant improvement in seedling vigor index compared to controls. | 57 |
| PGPB Bacillus subtilis NH-100, Seratia marcescens FA-4 | poly(vinyl alcohol) (PVA) and poly(vinylpyrrolidone) (PVP) nanofibers | Canola (Brassica napus L.) | 1.3*104 CFU/seed at the 25th day at room temperature. | Pot trials Improvements in seed germination, root and shoot growth (weight and length), leaf area in addition to increasing soil pH and bioavailability of zinc (Zn) and phosphorus (P). | 58 |
| AMF Rhizophagus irregularis | poly(ethylene oxide) (PEO) | bean seeds (Phaseolus vulgaris L var. José Beta) | not reported | Pot trials. No significant improvement in root and plant length was observed but increased number of flower buds was reported. | 59 |
| PGPR Bacillus pumilus TUAT1 | Calcium peroxide (CaO2), iron powder (Fe), and Benmoly (Mn + Fe) | Monster Rice 1 (Oryza sativa L., line LTAT-29) | not reported | Double coating with PGPR and Benmoly significantly enhanced growth (root and shoot fresh weight) | 60 |
| PGPR Rhizobium tropici CIAT 899 PGPR | Double layer consisting of silk fibroin and trehalose and pectin and carboxy-methylcellulose | Phaseolus vulgaris | not reported | Pot and field trials Pot trials showed 100% nodulation in samples and positive controls. Field trials in semiarid soils showed enhanced germination and an increase in shoot dry mass under mild and severe water stress conditions with double layer coating. | 61 |

Table 2 shows that despite the potential of PGPM to reduce or replace the use of conventional agrochemicals, published data on microbe inoculated seed coatings has shown conflicting results. While the majority reports53, 56,57,58 have maintained a favorable outlook on their use, some have also reported delayed germination52 or no significant improvement in growth compared to controls. 51,55 Furthermore, not all the reported studies include data on laboratory, greenhouse, and field results. It is reported that only 3% of studies conducted on PGPM inoculated seed coatings from 1960 to 2019 contain data across all three analysis scales.1 Addition of PGPM in any field/area may have unaccounted effects on the surrounding ecosystem. Thus both long and short-term environmental assessment is needed before promoting their use. To reach an unequivocal verdict on the utility of PGPM and their inoculation in seed coatings, further data with supportive and consistent results across diverse experimental scales and conditions is needed.

4.2. Polysaccharide based seed coatings

Concerns about the use of plastic-based seed coatings and the potential soil pollution caused due to detachment of the plastic film fragments from the seed coat (Section 3.3), have propelled researchers to develop biocompatible and biodegradable coating materials. In this regard, the design and use of polysaccharide-based seed coatings has gained impetus across academic and industrial research programs. In the following sections, we have discussed some widely studied polysaccharide materials investigated as seeds coatings including sub-sections reviewing their performance as sustainable carriers in terms of raw material renewability and extraction processes.

4.2.1. Alginate

Alginates are biopolymers found in brown algae as well as in soil bacteria. These are polysaccharides composed of a varying sequence of D-mannuronic (M) (Figure 4a) and (1 → 4)-linked L-guluronic (G) (Figure 4b) blocks. Alginates are typically used in the form of gels prepared either by ionic crosslinking or through acid precipitation. Depending on the gelation method, the physical and chemical properties of alginate gels can be adjusted. Due to their versatile adjustable properties, ability to retain water, ease of availability and low cost, alginates are actively being researched for applications in the food and biomedical industries.62–67 In seed treatment research, the use of both crosslinked53,68,69 and un-crosslinked70 alginate has been explored. While some reports mention direct coating of a layer of alginate on seeds,68 others propose designing alginate microbeads53,69 containing an enclosed AI/microbe which can then be stuck on seeds through an adhesive.

An early patent70 disclosed the use of a dried liquid free-flowing composition containing a mixture of non-crosslinked alginates and a suspension of microorganisms to produce inoculated seed coatings. The viability of the alginate seed coatings to provide a suitable survival medium for various microbes was demonstrated through microbe survival assays on soybean and canola seeds. In another study,53 microbe inoculated alginate beads were produced by spraying the bacteria inoculated alginate solution in a hardening calcium chloride (CaCl2) bath (Figure 4c, d, e). The produced microbeads were stuck to tomato and wheat leaves through the use of an adhesive. Pot trials of the coated seeds showed significant improvement in plant height and dry leaf and root weight (Figure 4f). Although promising, production of the inoculated alginate microbeads followed by coating on individual seeds may pose challenges on a commercial scale. To overcome these challenges, another patent68 disclosed a more commercially feasible technique of producing alginate seed coatings wherein either the alginate coating (premixed with a suitable AI) and the divalent metal ion (Ca+2, Ba+2, Zn+2) crosslinking solution could be applied on the seeds via spraying to achieve larger throughputs at lower costs.

For alginate bead based seed coatings, Berninger and coworkers have argued that smaller bead sizes are more suitable for achieving a uniform coating on the seeds and maintaining a favorable distance between the inoculated microbe and the seed.69 They identified a range of lab-scale approaches to produce small-sized alginate beads loaded with PGPB. Techniques tested included (1) contact spotting wherein using an automated microarray system alginate drops were spotted on a reservoir following which the hardening CaCl2 solution was dropped on top of the alginate dots (Figure 4g), (2) syringe based extrusion of alginate solution into the hardening bath (Figure 4h, i), (3) automatic pipetting of the alginate solution into the hardening bath (Figure 4j) and (4) production of alginate beads from commercial nanodispenser, and encapsulator instruments. Contact spotting produced the smallest bead sizes however at very low throughputs of 10-7ml.min-1. The maximum throughput was achieved by manually dropping a drop of alginate solution in a CaCl2 hardening bath at 5 ml.min-1, producing beads in mm size range. Surface coverage of seeds with smaller sized beads was reported to be higher as compared to larger sized beads. The authors have argued that crushing larger sized beads prior to coating on seeds may help overcome low-throughput limitations associated with the production of smaller bead sizes.

Alginates have also been used in combination with other materials to produce hybrid seed coating materials. Recently Castro et al. proposed the use of a composite film consisting of alginate and a layered double hydroxide (LDH) of Zn and aluminum (Al) as bean (Phaseolus vulgaris L.) seed coatings. These hybrid coatings were incorporated with plant growth regulating auxins. Results of the pot trials showed enhanced biometric parameters (root surface area and fresh matter and shoot length) however germination rate and speed were lower in all the samples compared to untreated controls (Figure 4k, l).71 Although the intercalation of the auxins within the LDH can facilitate their slow release and reduce the amount of AI required, the inhibited germination of coated seeds can be a drawback due to potential reduction in crop yield. Recently researchers have also explored the use of quaternary ammonium alginate salts as seed coatings. Sequeira et al72 extracted alginic acid directly through the dissolution of seaweed in HCl followed by treatment with an aqueous solution of tetramethyl ammonium hydroxide resulting in the formation of tetramethyl ammonium alginate (TMAA). In addition, they extracted cellulose from the remaining seaweed biomass through bleaching with H2O2 and pH adjustment. Germination assays showed significant improvements in shoot and root weight compared to controls. Although the synthesis scheme involves large amounts of water and reagents (acids/alkali) during the washing stage, cellulose extraction is a step towards improving the sustainability of the extraction process. However, the toxic nature of quaternary ammonium compounds for aquatic organisms and microrganisms is a major concern, particularly for use in agriculture applications.

From a sustainability view point, alginates represent a renewable resource harvested from various species of brown seaweeds such as Macrocystis sp. (US), Lessonia sp. and Durvillaea sp. (Chile), Laminaria sp., and Ecklonia sp (Far East), Laminaria digitata (France).73 Brown seaweed, which is present in abundance in the world oceans,73–75  represents a fast growing organisms and their renewability fortifies their position as an unlimited raw material source.

The typical alginate extraction process involves milling the washed seaweed into dry powder followed by chemical treatment to remove un-wanted materials. This is proceeded by breaking the cell wall through an acid or alkaline treatment. The pH is then neutralized through washing with water and alginate salts are extracted through sodium carbonate extraction. Thus, from a green chemistry perspective, whereas alginate usage is favourable over fossil fuel derived coating materials due to raw-material renewability, existing extraction strategies present significant environmental burdens. Use of large amounts of acids, alkalis, and toxic chemicals such as formaldehyde, together with high water and energy requirements are some of the potential issues that need to be optimized. Green alginate extraction techniques including ultrasound, microwave and enzyme assisted extractions are being researched but are expensive and possess scale-up challenges.76

Overall, it can be surmised that alginate is a promising seed coating material. However, concerns related to (1) inhibited seed germination rates, (3) green extraction strategies and (2) the design of continuous and cost-effective strategies for synthesizing alginate coatings need to be addressed.

Figure 4. (a-b) Chemical structures of alginate monomers. Adapted with permission.62 Copyrights Taylor & Francis 2017. (a) D-mannuronic acid (b) L-guluronic acid. (c-f) Micrographs of Azospirillum brasilense Cd (PGPB) inoculated alginate microbeads. Adapted with permission.53 Copyrights Springer Nature 2002. SEM image showing (c) wet and (d) dry (lyophilized) alginate microbeads colonized by A. brasilense Cd. (e) TEM image showing interior of a wet microbead containing A. brasilense Cd. (f) Pot trial results showing increase in leaf and root dry weight after seedling treatment with inoculated alginate microbeads. Similar alphabets indicate statistically similar groups at P ≤ 0.05. (g-j) Digital images showing the set-up of different techniques used to produce alginate microbeads. Adapted with permission.69 Copyrights Taylor & Francis 2016. (g) Contact-spotting of alginate beads through use of spinning pin to drop alginate solution into multi-channel reservoir troughs. (h) syringe fitted into falcon tube used to drop alginate solution into hardening bath. (i) use of peristaltic pump to pump alginate solution into hardening bath. (j) pumping of alginate solution through automated liquid handler.(k-l) Graphs showing results of germination trials of bean seeds coated with sodium alginate and Zn and Al layered double hydroxide (LDH) and the synthetic auxin 1-naphthalenoacetic acid (ZnAl-NAA-LDH). Figures adapted from open source article.71 Treatments tested included (1) untreated controls, (2) alginate coating (M1) (2) alginate + ZnAl-CO3-LDH coating (M2), (3) alginate + NAA coating (M3), (4) alginate + ZnAl-NAA-LDH coating (M4). (k) All tested coated seeds exhibited germination rates lower than uncoated seeds. (l) Germination speed index (GSI) of the three test samples compared to uncoated control showing reduced germination behavior of the coated seeds.

4.2.2. Chitosan

Chitosan is a naturally occurring biopolymer consisting of glucosamine (~70-80%) and N-acetyl glucosamine (~20-30%%) residues.77 It is produced by the deacetylation of chitin,78 a natural polysaccharide found in the exoskeleton of crustaceans, insects, and nematodes. The chemical structure of chitosan (Figure 5a) offers ease of processability due to the presence of the highly reactive hydroxyl and amino groups which can react with a large number of other molecules. This chemical reactivity combined with its biodegradability, biocompatibility, bio-safety, and antimicrobial properties has made chitosan an actively researched material for diverse agricultural applications including use as a carrier for AI, biofertilizer, soil remedial agents, seed priming agent and as a plant growth booster.79,80 Chitosan has also been demonstrated as an effective seed coating agent with promising results.54,77,81 Freepons summarized results from different field trials conducted to measure the efficacy of chitosan seed coats for (1) drill-seeded rice grown in humid soil, (2) water-seeded rice grown in humid soil with high-disease pressures, (3) and rice cultivated under flood conditions in semi-arid soil.77 Despite the variability in crop and soil conditions, chitosan seed treatments produced consistent crop yields. Reddy and coworkers81 investigated the potential of chitosan coatings to prevent a seed-borne infection F. graminearum in wheat seeds. Four replicate batches containing 100 wheat seeds with susceptibility to the infection were sterilized and immersed in chitosan solution followed by drying to achieve chitosan-coated seeds. Germination trials showed increased seed germination and vigor for the coated seeds compared to untreated controls with a significant reduction in seed infections (Figure 5b). The results suggest that chitosan prevents seed infection spread by creating a barrier between the seed and soil-borne organisms inhibiting fungal spread. The fact that infection spread was inhibited without the use of fungicide treatment or toxic residues shows the vast potential of chitosan-based seed coatings to achieve environmentally benign and sustainable crop protection.

Blends of chitosan with other materials are also being explored as seed coatings. Chandrika et al. synthesized chitosan blends with polyethylene glycol and glycerol, and loaded those with a biocontrol agent, Trichoderma, followed by coating on castor seeds.54 The coated seeds exhibited enhanced germination rates and seedling vigor as corroborated through germination assays, while spore germination assays demonstrated the viability of the microbe in the hybrid blend (Figure 5c). Although promising, the results of the study need to be followed up with greenhouse and field trials to elucidate the effects of the hybrid materials and the loaded quantities of the biocontrol agent on long-term plant health. In another study, Ziani et al. studied the effect of chitosan coatings on artichoke seeds, reporting that the performance of the coating was dependent on various factors, including the chitosan molecular weight, chitosan concentration, pH, and presence of the surfactant and AI.82 Seeds coated with two different molecular weights (400kDa, 149 kDa) of chitosan under diverse pH, surfactant concentration and layer thickness were analyzed. Lower Mw chitosan coatings incorporated with fungicide TMTD (tetramethylthiuram disulfide) gave the best results in terms of higher observed germination rates and superior antifungal performance (Figure 5d). Researchers have hypothesized that chitosan treatment influences the plant physiology to increase crop yield by producing more grains rather than higher foliar growth which increases the promise of higher crop yields at lower fertilizer inputs.77 Similarly, the inherent anti-fungal properties of chitosan can also be exploited to achieve fungicide function in the absence of potent AI.

From a sustainability perspective, seafood waste can serve as an ample raw material source for chitosan production. FAO estimates83 indicate that in 2018 shelled mollusks accounted for 56.3% of the global marine aquaculture production while crustaceans alone represented 18.5%. Waste shells typically end up in landfill sites or are just dumped in the sea. Unaccounted dumping can result in ocean acidification, and disease occurrence while landfill is expensive.84,85 Thus, seafood waste can serve as a rich material source of chitosan while also providing an ingenious reuse solution. The second factor to be considered is the extraction strategy. Typically, chitosan can be extracted through chemical and biological methods. The chemical method involves various processing steps including deproteinization (alkali treatment), demineralization (acid treatment) deacetylation (treatment with concentrated NaOH at 107 ⁰C for 6 hours) and decoloration (hydrogen peroxide, NaClO treatment).86 Thus, while chemical extraction is more established on an industrial scale, with scale-up it involves harsh chemicals and processing at elevated temperatures in addition to requiring large volumes of water to adjust pH. Biological extraction employs the use of fermentation techniques to achieve greener conversion of chitin into chitosan. Bio-extraction is environmentally more friendly but is still under research and issues related to commercial scalability need to be resolved.87

To sum up, chitosan is a highly promising seed coating material with multiple applications both as a fungicide, and as a carrier for PGPM with positive effects on plant yield. Future research in this area needs to focus on optimizing existing challenges associated with green extraction of chitosan.

Figure 5. (a) Chemical structure of chitosan. Adapted from an open source article.88 (b) Results from germinations assays conducted on two types of spring wheat (Triticum aestivum L.) seed samples, (1) cv. Norseman and (2) cv. Max treated with chitosan solutions. Seeds treated with (1) sterile water, (2) HCl and (3) benomyl were used as controls. Results demonstrate a significantly increased germination rate in all test samples compared to untreated controls. Reprinted with permission.81 Copyright 1999 American Chemical Society. (c) Microscope images showing germination of Trichoderma spores in Chitosan-PEG films demonstrating the viability of the blends for the microbes. The images represent results of spore germination assays which showed viability of 108-1010 spores per ml of formulation. Figure adapted with permission.54 Copyright Elsevier 2019. (d) Results from germination trials of chitosan coated artichoke seeds. Data replotted with permission.82 Copyright Elsevier 2010. Treatments tested included (1) 1 layer (L) coating of 4 wt.% Chitosan with Mw=149kDa (B), (2) 3 L coating of 4% B, (3) 1 L coating of 4% B + 5 % Span surfactant, (4) 3 L coating of 4% B + 5 % Span surfactant, (5) 1 L coating of 4% B + 0.037 % (TMTD) fungicide, (6) 1 L coating of 4% B + 0.075 % (TMTD) fungicide, (7) 1 L coating of 4% B + 0.15 % (TMTD) fungicide. As controls uncoated seeds and seeds treated with TMTD were used. Pink spheres show the number of germinated seeds. All test samples show higher germination rates than untreated controls, with a significant rise observed in Chitosan and TMTD combinations. Similar alphabets indicate statistically similar groups as per Duncan test (P < 0.05). Bars show number of seeds contaminated by fungal attacks in addition to showing the distribution of the types of fungi found. Results show the high efficacy of TMTD containing chitosan coatings against Rhizopus contamination, a highly damaging fungi type.

4.2.3. Guar gum

Guar gum extracted from seeds of the guar plant (Cyamopsis tetragonolobus) is one of the most widely used commercial sources of galactomannan, linear polysaccharides consisting of a mannose backbone with attached galactose side chains (Figure 6a). High molecular weights combined with an abundance of hydroxyl groups contribute towards highly viscous galactomannan solutions in water which enable its utilization as a gelling, thickening, stabilizing and binding agent.89 Guar gum as a cost-effective source of galactomannan, has been widely explored for industrial and drug-delivery applications,89,90 along with uses in the food industry.91 There have been few reports89,92 on the utilization of guar gum for agricultural applications, where it has been mainly explored as a soil conditioning agent to enhance soil moisture retention (Figure 6b-e). A few patents93–95 have reported the use of guar gum in seed coatings. Duke93 in 1992 disclosed the use of hydroxypropyl guar solution to coat fuzzy cotton seeds, achieving better flowability through planting equipment. In a more recent patent,94 Chen and coworkers disclosed a method to develop guar gum seed coatings to enhance water retention around the seed to promote seedling establishment (expeditious and homogeneous seedling emergence in field96), particularly in hostile croplands with limited or scarce irrigation. Furthermore, the use of derivatized guar to form coating layers allowed the grouping of multiple seeds in agglomerates which is sometimes desirable in precision sowing. Methods mentioned to coat seeds with the guar layer included coating in rotary coaters, drum coaters, fluidized beds and in-situ coatings wherein the uncoated seeds are planted in a hole in the ground followed by immediate spraying of the coating mixture in the hole to completely or partially surround the seed. More recently, researchers95 have disclosed the use of dry seed coatings consisting of a cross-linked biopolymer (amylose or amylopectin) and a binder layer of guar, starch, or a mixture of the two. As an example, corn seeds were coated with a dispersion of starch and guar biostimulant (derivatized cationic guar) powder in DI water. The treated seeds showed no caking, were visually dry and left no observable residues in the coating chamber. Dust measurements showed reduced emissions from the coated seeds compared to untreated seeds (Figure 6g). Moreover, no detrimental effects on seed germination were observed due to the coating (Figure 6f).

The source plant of guar gum C. tetragonoloba native to South Asia, is used both for human and animal consumption. Guar can be considered as a low emission crop97,98. Environmental results of an LCA analysis98 conducted for the irrigation of guar in the US Southwest indicate lesser or equivalent emissions at 2.67kg CO2 eq per kg guar gum compared to crops like wheat, barley and corn. Drawbacks associated with large-scale usage of guar gum for seed coatings relate to utilization of agricultural land for producing industrial raw materials. Also, extraction of guar gum from C. tetragonoloba seeds involves various steps including dehusking through heat treatment, milling and polishing.91 with significant water and energy intake.

Thus, guar gum can be considered a potentially promising seed coating material based on patent literature; however, more experimental studies are needed to ascertain its utility as an effective seed coating material. Moreover, LCA studies are needed to gauge its environmental impact compared to existing coating materials.

Figure 6. (a) Chemical structure of guar gum. Adapted with permission.90 Copyright Elsevier 2011. SEM images of (b) guar gum film, (c) acrylic acid grafted guar gum crosslinked with ethylene glycol di methacrylic acid (EGDMA) (GG-AA-EGDMA) dried hydrogel at 100 X magnification, (d) GG-AA-EGDMA dried hydrogel at 2000 X magnification and (e) hydrated GG-AA-EGDMA hydrogel. Adapted with permission.92 Copyright Elsevier 2018. Whereas guar gum exhibits a compact, non-porous structure, GG-AA-EGDMA hydrogels display a porous network with interspatial voids. The pores enable high water penetration resulting in high water absorption rates. The difference in dried and hydrated hydrogels is evident from the transformation of the distinct boundary network structure in dry conditions to the web-like morphology in wet conditions. This transformation can be attributed to water imbibition by the hydrogels. The high water retention capacity of these guar based hydrogels can be exploited for soil conditioning applications. (f-g) Germination and dust emission test results of corn seeds coated with mixtures of DV-12 and DV-89 (starch powder), guar biostimulant powder DCG-1 and derivatized cationic guar DCD-2. Data replotted from reference.95 (f) DV-89 + DCG-1 combination shows the highest normal germination rates whereas the other three tested coatings show slightly lower germination compared to untreated control. (g) Dust measurement results conducted on a Heubach dust meter equipment for 4 different coating combinations and untreated controls. All tested coatings show lower dust emission rates compared to controls.

4.3. Electrospun nanofibrous seed coatings

Electrospinning is a versatile technique to produce nano to micron size ranged nanofibers from a viscous solution (typically a polymer) by applying an electrical field (Figure 7a, b).99 The ability to electrospin a diverse range of solutions to produce fibers with the desired morphology combined with their unique characteristics (porosity, high surface to volume ratio and lack of residual solvent) presents electrospun nanofibers as interesting candidates for agricultural applications.100 In seed coating research, nanofibers loaded with the requisite AI/PGPM have been used to coat a variety of different seeds with promising preliminary results. Seeds can either be (a) directly coated by nanofibers through electrospinning the solution on top of the seeds (Figure 7c) or (b) indirectly coated wherein the fiber mats are prepared first and are then wrapped around the seeds. (Figure 7d). By virtue of the partial surface area coverage of seeds, nanofibers help to overcome restricted gas permeability across the coating- a limitation present in conventional film coatings.

In an early study on the subject, researchers101 coated soybean seeds with electrospun fibers prepared from a rhizobia inoculated polyvinyl alcohol (PVA) solution. Exposure to a fungicide solution toxic to the incorporated microbe showed a greater microbe survival rate in the seeds coated with the PVA nanofibers compared to the control sample containing only the bacteria inoculate. Their findings signified that electrospun fibers protected the loaded microorganisms from harmful chemicals, resulting in an increase in their survival rates. In another study, Castañeda et al. coated rice seeds with ethyl cellulose-based electrospun nanofibers containing commercial fungicide formulations (carboxin, thiram and carbendazim).102 Germination trials showed improved seed germination rates, which signified the enhanced anti-fungal performance of the loaded fungicide as well as the fact that nanofiber coating did not restrict seed germination. These initial pioneering studies laid the foundation for further investigation of electrospun polymer fibers for seed coatings and ultimately led to the investigation of biodegradable and biocompatible polymers for producing environmentally friendly seed coatings. Krishnamoorthy et al. coated cowpea seeds with water-soluble polymer polyvinylpyrrolidone (PVP) mixed with urea and cobalt nanoparticles to coat cowpea seeds through electrospinning and dip coating techniques.103 While both film and fiber coatings exhibited sustained nutrient release, the lack of residual solvents, ease of gas flow through the coated seeds and lesser seed pore clogging compared to the dip-coated film coatings, signified the superior performance of the fiber-based coating. De Gregorio et al. showed the use of PVA electrospun fibers loaded with two rhizobacteria Pantoea agglomerans ISIB55 and Burkholderia caribensis ISIB40, as coatings for soybean seeds.57 The bacteria were shown to successfully survive and colonize on the fibrous seed coatings for 30 days, in addition to promoting plant growth as demonstrated through germination assays and greenhouse trials.

The use of hydrophilic nanofibrous seed coatings may suffer from moisture-driven dissolution in the soil leading to burst release of the encapsulated AI. To counter this issue, Krishnamoorthy et al. in a follow-up work to their previous study, used a blend of the hydrophilic PVP with a hydrophobic polymer poly (diethoxy) phosphazene (PPZ) with phosphorus and nitrogen-basedbackbone to produce electrospun seed coats(Figure 7i).104 The hydrophobicity of the coating fibers enabled increased retention of the seed coat, particularly in the wet soil. The biocompatibility of the polymer blend was complimented by the fact that degradation of PPZ produces phosphates and ammonia, which can act as plant nutrients.

Figure 7. Synthesis procedure and morphology of electrospun nanofibrous seed coatings. Schematic showing (a) vertical105 and (b) horizontal electrospinning set-up58 for producing nanofibers. (c) Seed coating process through direct deposition of the AI loaded electrospun fibers on top of seeds.105 (d) Indirect seed coating through first preparation of polymer fiber mats followed by loading of mycorrhizal inoculant powder. Seeds are then wrapped within the inoculated fiber sheets.59 Adapted with permission from references.105, 58, 59 Copyrights 2019, 2020 American Chemical Society. SEM images of (e) PEO, and (f) Arbuscular Mycorrhizal Fungi loaded PEO electrospun nanofibers,59 (g) CDA and (h) Abamectin loaded CDA nanofibers,106 (i) PVP+PPZ104 nanofibers, and (j) PVA electrospun nanofibers107. Adapted with permission. 59, 106, 104, 107 Copyrights 2019, 2020 American Chemical Society, Elsevier 2018, and Springer Nature 2020.

To overcome the limitations presented by the high cost of PPZ, which deters its wide-scale usage for seed coating applications, Farias and Pirzada et al. proposed the usage of cellulose diacetate (CDA) electrospun fibers as seed coatings (Figure 7g, h).106 The hydrophobic nature of CDA facilitated retention of the polymer fibers on the seed coat, particularly in moist soil. Two model AIs, abamectin (an anthelminthic) and fluopyram (a fungicide) were separately incorporated into the polymer fiber mats. Efficacy of the nanofibrous seed coat was verified via sustained release of AI measured through HPLC (Figure 8a, b) and bioavailability of the AI through in-vitro bioassays. The viability of nanofibers as carriers for PGPB was demonstrated by Hussain et al. who showed use of PVA/PVB hybrid electrospun fibers loaded with Bacillus subtilis NH-100 and Seratia marcescens FA-4 as seed coatings for canola seeds (Figure 8i).58 In-vitro functional studies verified that the electrospun biocomposite membranes provided a viable growth media for the inoculated PGPB in addition to demonstrating their superior antifungal and phosphorus solubilizing properties (Figure 8c-h). Furthermore, the enhanced functional (anti-fungal and stable nutrient acquisition) performance of the coated seeds was exhibited through pot trials whereas stability studies indicated that the seed coat was stable at room temperature for 15 days. In another recent work, Xu and coworkers coated tomato and lettuce seeds with cellulose acetate electrospun nanofibers encapsulating copper (Cu) as the model AI.105 Greenhouse trials showed the enhanced germination rates (70% rise for tomato seeds and 25% increase for lettuce seeds) of the coated seeds in fungal pathogen (Fusarium) infected soils as compared to untreated soils (Figure 8k, l). Raja et al. demonstrated the enhanced bio-efficacy of plant growth-promoting hormones (gibberellic acid and indole acetic acid)  loaded on PVA electrospun nanofibrous coatings on (Figure 7j) black gram and ground nut seeds which showed increased seedling germination and vigor as compared to controls (Figure 8m, n). 107 More recently, researchers59 have proposed the use of polyethylene oxide (PEO) fibrous seed coatings as loading media for Arbuscular Mycorrhizal Fungi (section 4.1) (Figure 7e, f). PEO nanofibers showed superior performance as AMF inoculated carriers (Figure 8j) and treated bean plant seeds showed enhanced flower bud growth.

Figure 8. Summarized results demonstrating diverse applications of electrospun nanofibrous seed coating. (a-b) Graphs demonstrating sustained release of (a) abamectin and (b) fluopyram from CDA nanofibers. Adapted with permission.106 Copyrights 2019 American Chemical Society. (c-h) Digital images showing antifungal performance of PGPB inoculated nanofibers. Zone of inhibition potential against (c) M. phaseolina (15 ± 0.5mm),  (d) R. solani (13  ± 1.0 mm), (e) F. oxysporum (14 ± 0.6 mm).(f) Hollow zone around inoculated nanofibers shows the phosphate solubilizing activity of the inoculated bacteria in Pikovskaya agar medium (g-h) Representative (g) pink and (h) white creamy dots showing bacterial colonies on the agar plates demonstrate that electrospinning does not affect biological functions of the loaded bacteria. Adapted with permission.58 Copyrights 2019 American Chemical Society. (i-j) Survival rates of inoculated microbes on electrospun fibers. (i) Viable cell count of inoculated PGPB in colony forming unit (CFU) as a function of days stored incorporated in PVA/PVP/Glycerol membrane –A, PVA+PVP+Gly dispersions - B, and PVA/PVP/Glycerol coated canola seeds.-C.58  (j) Bar Graph showing AMF colonization rate in soil inoculated seeds – CP and seeds coated with AMF loaded PEO nanofibers – SNM.59  Nanofiber coatings contained 97% less inoculum dose per seed compared to tradition soil based inoculation. Adapted with permission.58,59 Copyrights 2019, 2020 American Chemical Society. (k-l) Enhanced germination rates of Cu-loaded CA nanofiber coated (k) tomato and (l) lettuce seeds as compared to untreated controls in Fusarium infected diseased soils. Adapted with permission.105 Copyright 2020 American Chemical Society (m-n) Enhanced seedling (n) germination and (m) vigor index of hormone-loaded PVA nanofibrous coated seeds at different water stress levels. Reproduced with permission.107 Copyright Springer Nature 2020.

An environmental assessment of the proposed nanofibrous seed coatings requires an evaluation of the impacts of the polymer as well as the electrospinning parameters. The properties of the major electrospun polymers are discussed in Table 4 Section 6. Addressing the operational parameters of typical electrospinning systems, the use of high voltage conditions and halogenated organic solvents pose significant environmental and operational hazards and hence are barriers for large scale implementation of this otherwise feasible technique.108 GSK has developed a solvent guide allotting a color to commonly used solvents considering the safety (boiling point, flammability, reactivity) and health (exposure limits) and environmental (emissions, recycling, land and water impact) impacts. 109 A color rating of green indicates few hazards, while amber and red denote some and major hazards respectively. Table 3 shows the classification of solvents used in the above discussed publications on electrospun fibrous seed coatings as per the GSK solvent guide. It is obvious that water appears the best solvent choice followed by acetic acid and acetone whereas DMAC, dichloromethane and chloroform are not suitable choices, particularly for agriculture usage.

Table 3. Summary of electrospun polymer and parameters investigated as seed coatings

| Polymer | Solvent | GSK solvent rating | Electrospinning voltage | Reference |
| --- | --- | --- | --- | --- |
| PVA | water | Green | 22 kV | 101 107 |
| Ethyl cellulose | dichloromethane, ethanol, N,N-dimethyl formamide | Red | 30 kV | 102 |
| PVP + PPZ | chloroform/ethanol (4 : 1) | Red | 30-16 kV | 104 |
| CDA | acetone (Ac), dimethyl acetamide (DMAc) (2:1) | Yellow, Red | 12.5 kV | 106 |
| PVA+PVP blend | water, glycerol as plasticizer | Green | 17 ± 1 kV | 58 |
| CA + gelatin | acetic acid/water (3:1) | Amber | 18 kV | 105 |
| PEO | water | Green | not specified | 59 |

Thus, where the consistently promising results of electrospun fibrous seed coatings show their potential in seed treatment applications, environmental concerns related to the use of toxic solvents and high energy inputs need to be addressed. Future studies on electrospun seed coatings need to focus on overcoming existing limitations mainly transforming the batch scale lab-based electrospinning process into an automated continuous material fabrication set-up to facilitate commercial production at lower costs. Furthermore, LCA studies can also aid in estimating the environmental footprint of electrospun seed coatings and their performance over longer periods.

4.4 Hydrogel based seed coatings

Hydrogels are hydrophilic three-dimensional polymer networks that can absorb a large amount of water.110 Due to their hydrophilicity and biocompatibility, hydrogels have found applications in diverse fields such as tissue engineering,111 drug formulations,112 wound dressing113, and as constituents of hygiene products.114 Recently, hydrogels are also being explored in agricultural applications as soil remediation agents, stimuli-responsive carriers for agricultural AI, and mini water reservoirs in arid regions.115 A unique application of hydrogels is their utilization as seed coatings for achieving crop protection through water retention around the seed. In dry conditions, where reduced water supply to seedlings can impair germination and crop establishment, the use of hydrogel based seed coatings offers an attractive solution; however, studies done in this regard have shown diverse and conflicting outcomes. An early study116 conducted on the effect of hydrogel seed coatings on Russian wildrye reported reduced germination rates and a failure to improve crop establishment rates in the field. Similarly, Sarrocco et al. coated wheat, cabbage, basil and radish seeds with sodium alginate hydrogels achieving a durable seed coating stable for 90 days.117 However, in-vitro and in-vivo germination trials showed a significant reduction in the germination rate of coated seeds compared to uncoated seeds.  Gorim et al. coated barley, rye and wheat seeds with (1) a commercial hydro-absorber, Stockosorb® and plant strengthener formulations (2) biplantol and (3) humic acid) comparing the performance of the coated seeds with uncoated controls.118 Germination trials showed all three seed coatings inhibited seedling germination compared to the uncoated seed controls.

Nevertheless, other research groups have reported positive effects of hydrogel-based seed coatings on seedling vigor and growth, particularly under drought related conditions.11,119 Su et al. coated Caragana korshinskii (pea shrub) seeds with five different hydrogel-based coatings. Field trials conducted under arid soil conditions showed a two-fold increase in the seedling survival rates of the coated seeds compared to uncoated control (Figure 9a).11 Pačuta et al. monitored the growth of sugarbeet seeds coated with a commercial seed treatment hydrogel-based agent aquaholder reporting significant beneficial effects on the seedling growth as observed through various growth markers like the leaf index area, root and white sugar yields, especially in the early growth phase.120 However, details of the chemical composition of aquaholder and its biodegradability were missing, which makes it difficult to comment on the overall sustainability of the approach. Pathak et al. coated corn seeds with a modified starch-based hydrogel and conducted growth assays of the coated seeds in the soil at different water availability levels.119 At moderate water stress in the soil, seedling emergence rate was much higher in coated seeds as compared to uncoated seeds, whereas at low and high water levels, no significant effect on germination was observed. The authors proposed that at a high moisture level, the extra water stored by the hydrogel would be redundant and at a low water level, even though the hydrogel would absorb water, this water would be lost to the dry soil before the plant can take it up. Therefore, the presence of the hydrogel coating would be most beneficial at intermediate water levels where the hydrogels would absorb water and provide it at a steady rate to the growing seedling (Figure 9b). The widely varying nature of reports warrants further research to gain an in-depth perspective on the utility of hydrogel-based seed coatings and shed light on their overall sustainability. Published literature suggests that rather than a holistic approach on the use of a similar hydrogel for coating seeds of different plants, successful utilization of these materials will require a case to case basis retrofitting taking into account the nature of the crop, soil and environmental factors.

Figure 9. (a) Results from germination tests of super absorbent polymer (SAP) coated Caragana korshinkii seeds. Treatments tested included (1)A = polyacrylamide, (2) B = sodium polyacrylate, (3) C = Balite efficient polyagent (SAP with denatured PVA as the active constituent), (4) D = Hankesho aquasorb (acrylamide and potassium acrylate copolymer as active constituents), (5) E = Zhengyuan aquasorb (acrylamide and sodium acrylate copolymer as active constituents). CK1 = uncoated seeds, and CK2 = seeds coated with clay and talcum served as controls. All SAP coated seeds showed significantly higher (P < 0.05) germination % (after 3 days), germination energy % (seeds germinated after 7 days), germination index, and vigor index compared to CK1 and CK2 control samples. Figure adapted with permission.11 Copyright Springer 2017. (b) Bar graph showing the effect of Modified Starch (MS) hydrogel coatings on emergence rates of corn plates at different Field Capacity (FC) levels (water availability levels in the soil which were varied through controlling soil water irrigation supply). The emergence rate was estimated through calculating the time to median emergence (MGT). 0% MS represents uncoated controls. As shown, emergence rate was significantly lower (P < 0.05) at 77% FC for 2.6 and 4.2% MS coatings, depicting faster emergence. Adapted with permission.119 Copyright Wiley 2020.

From an environmental and health perspective, toxic unreacted monomers and cross-linkers, lack of biodegradability and residual solvents may hinder wide-scale agriculture usage of hydrogels. The use of hydrogels derived from biodegradable and renewable materials like sodium alginate, starch enhances their environmental appeal. Whereas some119 have coupled the use of green hydrogels with superior on-field performance, many environmentally friendly hydrogels fail to show positive effects on seed growth. 117 Also, caution needs to be exercised before characterizing a system green or sustainable just based on the end product without assessing the reagents or processing parameters. For instance, the use of starch-based hydrogels over traditional fossil fuel based polymers like polyacrylamide (PAM) and sodium polyacrylate appears to be more sustainable on the surface.  However, the chemical footprint of the starch extraction process also needs to be accounted for. Starch can be extracted using either wet or dry milling processes. Wet milling entails multiple filtration and alkaline soaking and thus includes large volumes of water and alkalis in addition to sometimes including harsh chemicals like sodium sulfite, toluene, sodium bisulfite, and sodium metabisulphite. Dry milling on the other hand includes grain size reduction proceeded by separation through classification, involving less chemical usage but larger starch fragmentation along with a compromise on the purity level of the starch product.121,122 In addition, native starch is typically chemically modified or blended with other thermoplastics to improve mechanical properties. These modifications may negatively impact the biodegradability of the blend.123 As an example, chemical modification of starch as in the study119 by Pathak et al. involved the use of dimethylaminopyridine catalyst and sodium hydroxide and methanol as process solvents, chemicals posing significant safety and environmental concerns. Thus, a careful assessment of the synthesis parameters and benefits achieved in the field is a prerequisite before advocating the use of hydrogel seed coatings in farming.

4.5. Nanomaterial based seed coatings

Recent research in the agriculture sector has witnessed the development of innovative seed coating through integrating nanotechnology principles in seed treatment techniques to achieve unprecedented improvements in crop yields.61,105,124,125 A recent research area in this regard has been the utilization of metal nanoparticles (NP) for crop protection. Widely investigated as seed priming agents,126,127 studies have also investigated the integration of metal NPs in seed coatings. Adhikari and coworkers coated maize, soybean, pigeon pea and okra seeds with zinc oxide (ZnO) NP using Pine oleoresin (POR) as the seed coating agent.124 Pine oleoresin is a complex terpenes mixture extracted from living trees. It can be renewably sourced and represents an eco-friendly option. In addition to enhanced germination rate, greenhouse trials showed improved root development in plants grown from seeds coated with nano ZnO particles (Figure 10a). The authors attributed this improvement to the growth enhancing characteristics of Zn combined with the sustained Zn release obtained from the POR binding coat, which reduced losses ensuring enhanced fertilizer activity from the loaded ZnO NP. The seed coating protocol utilizes ethanol as the dispersion solvent for ZnO which can be considered benign as per the GSK solvent rating.109 While the overall technique seems promising, the synthesis process of the ZnO particles will have a significant impact on the overall sustainability of the method. Zhao et al. coated tomato seeds with a film coating agent (SC7709) mixed with copper (Cu), iron (Fe) and Zn NPs.125 No significant difference in germination rates of the NPs coated seeds was observed compared to untreated controls whereas significant improvements were reported in the internode length (Fe and Zn NPs), average tomato weight (Cu and Fe NPs) and tomato yield (Cu and Fe NPs) (Figure 10 b). In addition to showing enhanced growth symptoms, plants grown from metal NP coated seeds also exhibited resistance to infections (Fusarium and bacterial wilt, late blight). Although the environmental risk assessment of metal NPs still needs to be ascertained, the study shows that metal NPs can act as both growth-promoting and anti-pathogenic agents in seed treatments and hold the potential to replace conventional agrochemicals (section 3.2). The NPs were produced by the flow levitation method in which molten metal suspended in an electromagnetic field is condensed into nano-sized particles through tuning the metal temperature and pressure. This technique produces high purity metal powders via container less metal melting and does not involve the use of toxic solvents and is thus environmentally friendly.128,129 However, the high costs associated with the equipment and energy consumption might be a deterrent for agricultural applications for both resource deficient regions and also for mechanized farming in developed countries. Recently, Abeywardana and coworkers have demonstrated the development and use of novel Zinc-doped hydroxyapatite (HA)/urea nanohybrid materials for coating seeds to achieve seed based crop protection.130 The seed coatings were synthesized with sodium alginate, CMC and calcium chloride while the hybrids were produced through dropwise addition of phosphoric acid into a suspension of urea and calcium hydroxide. Loading of Zn and urea within the hybrids enabled sustained delivery of Zn and Nitrogen whereas the HA NPs served as Phosphorus source- a macronutrient required during early growth period. Seedling growth assays on maize seeds showed significant improvements in germination rates (Figure 10c), plant height and dry weight (Figure 10d) with the proposed Zn-HA/urea coating compared to HA only, Zinc-HA and untreated controls, revealing the synergistic effect of Zn, Nitrogen and Phosphorus release attained from the hybrid materials in enhancing plant growth. Soil leachate analysis from the coated seeds revealed negligible amounts of Nitrogen and Zn verifying their utilization by the coated seeds. The promising results from the study need to be followed up by field trials to corroborate their superior performance in enhancing plant growth in actual field conditions. However, the batch scale synthesis process and the use of acid and alkalis during the synthesis necessitates caution for ensuring safe handling and preventing emissions and any leakage of unreacted chemicals in the finished products. The environmental footprint can be improved through adoption of sustainable production methods for HA.131 Another concern that needs to be addressed is the biodegradability of the proposed nanohybrid. Thus, it can be concluded that nanotechnology in addition to being widely investigated for various agricultural applications has also permeated the domains of seed treatment with promising results being reported by various researchers.

Sustainability concerns related to agriculture usage of nanoparticles include associated safety concerns132 and the operational and environmental hazards encountered during the synthesis process. Typical nanoparticle synthesis involves the use of capping and reducing agents and reaction solvents. Capping agents arrest particle growth and agglomeration and are typically long-chain hydrocarbons with heteroatom functionalities. Typical reducing agents include reactive compounds like formaldehyde, hydrazine and sodium borohydride. The chemical toxicities and safety issues associated with both capping and reducing agents present significant challenges in the sustainable scaling-up of nanoparticle synthesis. Transition to green reagents and microbe assisted synthesis of nanoparticles may appease some of these concerns. However, more fundamental studies are needed to fully understand the pathways of microbe-derived nanoparticle synthesis to achieve optimum control over particle size to facilitate their utilization in value added applications. 133

Figure 10. (a) Results from greenhouse trials of ZnO coated maize, soybean, pigeon pea and ladies finger seeds. Treatments tested included 25 and 50 mg of Zn/g seed obtained from nano (<100 nm) and normal (< 3 µm) ZnO powder, whereas uncoated seeds and seeds sown in soil treated with zinc sulphate (ZnSO4.7H2O) were used as controls. For all vegetables, ZnO coating showed higher dry matter weight compared to untreated controls. 50 mg nano Zn/g seed, resulted in the highest dry shoot weight amongst all the samples and controls. Adapted with permission.124 Copyright Taylor & Francis 2016. (b) Results from greenhouse trials of tomato seeds coated with (1) Cu, (2) Fe, (3) Zn nanoparticles incorporated seed coating. NP1 and NP2 refer to lower and higher NP concentration respectively such that for Cu: NP1 = 2x10-9mM and NP2 = 2 x 10-8mM, Fe: NP1 = 1.18 x 10-5mM, NP2 = 1.8 x 10-4mM, Zn: NP1 = 4.6 x 10-6mM, NP2 = 4.6 x 10-5 Mm. CK denotes uncoated seeds as controls. Figure adapted from an open access article.125 Cu and Fe NP incorporated seed coating significantly increased tomato yield per plant (c-d) Germination and pot trial results of maize seeds coated with zinc-doped urea−hydroxyapatite nanohybrid. Similar letters represent statistically similar means (P > 0.05). (e) Image and scatter plot showing enhanced growth of HA-Zinc-urea coating compared to controls 14 days after germination. (d) Zinc-HA/urea coated seedlings showed significantly higher plant height and dry weight compared to uncoated seeds. Figure adapted with permission.130 Copyright 2021 American Chemical Society.

4.6. Multilayered seed coatings

The variability and complex nature of required seed treatments have motivated the design of multilayered customized seed coatings to cater to various biotic and abiotic stresses hindering plant growth. In an early patent,134 Lynch disclosed the design of a bi-layer seed coating consisting of an internal polymer coating enclosed within an external augmentation coating layer. Whereas the internal polymer coating would protect the seeds from environmental and osmotic damage, the secondary coat would be incorporated with requisite AI that would wash away from the polymer layer and provide a local concentration of the AI around the seed. The patent mentioned the use of cellulose acetate phthalate for the synthesis of the inner coat, which owing to its strength yet simultaneous gas permeability, would be ideal for the application. For the secondary augmentation layer, any suitable cellulose derivative or polymers like PVA, copolyvidone are mentioned as examples. Although promising, specific examples of plants or crops that can potentially benefit from the proposed dual coating would have further strengthened the claims of the invention. In an innovative nature-inspired approach Halter et al135 proposed cyanogenic seed protection through coating seeds with cyanogenic precursors and enzymes separated via biodegradable polymer layers. Cyanogenic is an internal defense mechanism through which plants can resist pest infestations by producing hydrogen cyanide which acts as a toxin against the pest. As proof of concept, wheat seeds were coated with layers of cyanogenic precursor mandelonitrile and enzyme hydroxynitrile lyase separated via polylactic acid layers. Upon attack by a herbivore, the separating layers would rupture leading to contact between the precursor and enzyme resulting in hydrogen cyanide production. Although promising, germination trials showed reduced germination in coated wheat seeds compared to untreated controls. In a follow-up article136 by the same group, a modified cyanogenic multilayered seed coating was proposed consisting of amygdalin as the precursor and β-glucosidase as the enzyme separated by the polylactic acid layers. Germination trials of coated wheat seeds showed germination rates similar to untreated controls, while field trials demonstrated reduced infestation rates against common pests including T. molitor, R. dominica, and P. interpunctella. Although some negative impacts like reduced seedling leaves, and reduced germination were observed in field experiments, the proposed coatings offer an ingenious method to control pest infestations without the use of conventional agrochemicals.

A recent pioneering study61 has demonstrated the use of programmable seed coatings. The proposed coatings consisted of an inner layer consisting of a mixture of silk fibroin and trehalose incorporated with growth-promoting rhizobacteria and an outer layer of pectin/carboxymethylcellulose (CMC) hydrogel, which would provide a suitable growth medium for the rhizobia as well as a water jacket for the seed in arid soils (Figure 11a). The pectin/CMC gels were prepared by the addition of CaCl2 crosslinker to a pectin/CMC mixture followed by addition of NaOH to increase pH leading to gelation. The silk fibroin/trehalose inoculated films were drop casted from an aqueous solution. Field trials conducted on bean (P. vulgaris) seeds under water stress conditions showed significantly enhanced plant health with the dual seed coatings compared to uncoated and single layer coated seeds (Figure 11b, c). The study is a stepping stone for the design of specialized seed coatings for countering specific crop and soil related requirements. However, the batch scale and time consuming approach, and use of crosslinker and alkali in the synthesis  require optimization from a sustainability and economic perspective. In addition, while silk fibroin is biodegradable, its extraction strategy might not necessarily be green which raises concerns in terms of sustainability. Extraction typically involves degumming of silk worm cocoons to remove sericin and extract fibroin. While various degumming techniques are documented, the most common method involves treatment with sodium carbonate in an energy and water intensive extraction cycle. Following degumming, the extracted fibers are dissolved in an aqueous solution before being processed into the desired physical form. Here also, multiple dissolution techniques can be employed but the most common one involves the use of environmentally toxic lithium bromide. That aspect together with high energy and water usage makes this process far from green.137 DeBari et al.19 in their recent review on silk fibroin have highlighted various green extraction techniques. Thus, to achieve sustainable usage of silk fibroin based seed coatings, a shift towards sustainable extraction strategies is required.

In another recent study, Agake et al reported a double coating seed treatment to enhance early growth in direct-seeded rice cultivation.60 The seeds were first coated with a PVA layer inoculated with a biofertilizer following which a second layer consisting of commercial coating materials was applied. Materials investigated for the secondary layer included CALPER (calcium peroxide), Benmoly (98% ferric oxide + 1.5% molybdenum trioxide) and iron powder. The synergistic action of the optimized double seed coating containing the biofertilizer rhizobacteria was most pronounced with the Benmoly outer layer (Figure 11d). Rather than the development of new coating material from scratch, the study investigates the optimization of existing commercial seed coating materials for seed inoculation with PGPM and thus offers a practical and immediate solution for the development of PGPM compatible seed coats. Also, PVA although derived majorly from non-renewable fossil fuel resources, is biodegradable, approved by FDA as an indirect food contact and is exempted from having a tolerance limit in pesticides as per CFR 40, part 180.138 As such, this work can serve as a role model for further studies on the subject.

Design of multiple seed coatings from different materials to offer synergistic crop protection appears to offer a unique and customizable solution across various crops and field conditions. However, the complicated synthesis mechanism seems to be a drawback that can hinder large-scale adoption of this approach. Thus, future research needs to focus on simplifying the synthesis and seed coating steps and lower production costs to enable easy adoption across agriculture systems.

Figure 11. (a) Schematic and digital images showing fabrication of programmable double layered seed coatings. P. vulgaris seeds are dip coated with layer 1 consisting of silk/trehalose inoculated with rhizobacteria R. tropici CIAT 899. Layer 2 consisting of pectin/CMC can be either dip coated or sprayed on top of Layer 1. Upon watering, Layer 2 can swell into a hydrogel and hydrate Layer 1, providing an appropriate release and growth environment for the inoculated rhizobacteria. (b) Digital images showing the difference in 6-week growth of P. vulgaris in water stress conditions from uncoated and double layered coated seeds. (c) Scatter plots showing results of greenhouse trials of coated P. vulgaris seeds between (1) uncoated control (C), (2) seeds coated with only Layer 1 (L1), (3) bi-layer coated seeds (L2).  Seeds were grown in sandy soils prone to drought stress. Altered watering conditions were used to vary water stress from -10 kPa to -20kPa replicating mild to severe water stress conditions. Significant increase in root length, lower total phenolic compounds (plants release phenolic compounds to combat water deficit, therefore low phenolic compounds would imply lower water deficit) and higher stomatal conductance by bilayer coated seeds signify the potential of the coating to enhance seed growth in drought-prone soils. Figure a-c adapted with permission.61 Copyright Springer Nature 2021 (d) Graph showing the effect of bilayer coating consisting of biofertilizer/PVA + commercial seed coating on growth of rice seeds. The bars represent the ratio of growth parameters attained with proposed double layer to values observed with single commercial coating layer. Benmoly double coating significantly increased growth as per Tukey’s test (P ≤ 0.05). Figure adapted with permission.60 Copyright Wiley 2021.

5. Transitioning towards a circular agro-industrial economy

The need to provide sufficient and quality food to an exponentially increasing global population with minimal damage to the environment calls for a more sustainable approach for seed treatment. Furthermore, environmental concerns related to rising carbon footprints because of the use of petroleum-based synthetic polymers or chemically processed bio-based materials as seed coats have further increased the need for more sustainable solutions to establish green seed treatment technologies that can help in carbon sequestration and recycling of wastes.

To achieve a circular agriculture economy, it is critical to efficiently utilize waste streams in value added applications. Recently there has been significant progress in this regard particularly with work being done on multiple fronts. In the proceeding sub-sections we discuss major breakthroughs pertaining to lignocellulosic, biochar and biomass derived seed treatments discussing their progress with a focus on the sustainability of the approach.

5.1. Biochar

A recent exciting advancement in seed treatment technology is the use of biochar-based seed coatings. Biochar is a porous carbon-rich solid material produced from pyrolysis of biomass under reduced oxygen conditions (Figure 12a). Depending on the feedstock and the pyrolysis conditions, biochars can have widely differing chemical and physical properties (Figure 12c-f).139 The organic portion of biochar is mainly composed of carbon, while the inorganic components can contain minerals such as calcium, potassium, magnesium and inorganic carbonates. These are multifunctional materials and have found uses in various environmental (carbon sequestration, waste-water treatment) and agricultural applications (soil remediation, hydroponics).140–142 Widely researched as soil remediation agents,143 some recent reports55,56,144,145  have suggested the utilization of biochars as seed coating materials. An early patent on the subject,144 has disclosed a method to coat seeds with biochar, emphasizing the need to first treat (Figure 12b) the biochar in order to (1) enhance the desirous properties like water and nutrient retention, (2) purge harmful impurities contained with the material pores, (3) remove variations in properties due to derivation from different feedstocks, and (4) load suitable AI or PGPM on the biochar particles. The seed coating method included mixing the seeds with starch or a suitable binder solution in a rotary tumbler and then adding the biochar material to the seed/binder mix to achieve the desired seed coating thickness. Another later study145 on biochar-based seed coatings was conducted by Williams and coworkers, who analyzed the effect of biochar-based seed coatings on the growth of native plants. Depending on the plant species, the coating either inhibited germination or had no noticeable effect signifying that biochar alone may not serve as a suitable coating material. However, positive results have also been reported when biochar based seed coatings are used in combination with PGPM. Glodowska et al. examined the efficacy of biochar as a carrier for P. libanensis, a phosphorus solubilizing bacteria, to create inoculated seed coatings.55 Corn seeds coated with inoculated biochar were sown in soil treated with soluble and insoluble phosphorus in order to identify (1) the ability of the inoculated microbes to solubilize inorganic phosphorus making it available for plant uptake, and (2) viability of biochar as the carrier material.  Greenhouse trials conducted on corn seeds showed improved seedling growth when soluble phosphorus (Hoagland solution) was applied (Figure 12h) but no significant improvement as compared to controls was observed when insoluble phosphate source (tricalcium phosphate) was applied (Figure 12i). The authors hypothesize that the water retention characteristics of the biochar maybe a more significant factor in the observed enhanced plant growth as compared to the phosphorus solubilization effect from the inoculated bacteria. In a subsequent report, Tripti et al. investigated the potential of bioformulations containing mixtures of biochar derived from agriculture waste and flyash (a byproduct of coal burning process) containing Plant Growth Promoting (PGP) rhizobacteria to coat tomato seeds.56 Biochar-based formulations showed retention of viable numbers of bacterial cells up to 180 days of storage, while seed germination trials showed a significant increase in the germination of coated seeds compared to uncoated controls. Biometric growth parameters assessed through pot trials also showed a significant increase as a result of the seed treatment (Figure 12g). While the promising results of the study indicate the efficacy of biochar as carrier material for PGPM with no inhibiting effects observed on seed germination and growth, the incorporation of biochar use in seed treatment techniques also offers an innovative solution for the reuse of organic (industrial and agriculture) waste which would otherwise be a source of environmental pollution. However, due to the conflicting results obtained by various researchers caution has to be taken while using biochar-based seed coatings.

To evaluate biochar use from a sustainability point of view, LCA studies have been conducted. A comparison across different LCA studies is complicated by the variation in biochar source, system boundaries, pyrolysis technique and choice of different functional units (mass of feedstock, product, or unit land, household). Matuštík et al.146 reviewed 27 studies on the subject considering the variability of the LCA baseline assumptions. Their results indicate a mostly negative Global Warming Potential (GWP) and thus an obvious benefit for the environment. The pyrolysis and feedstock processing step is generally the primary source of Green House Gases (GHG) which can be offset by the utilization of the pyrolysis co-products for energy production and the inherently CO2 sequestration characteristics of biochar. Regarding the raw material source, waste biomass generally appears as a favored choice since the production process can be excluded from the biochar production scheme. However, these benefits can be offset by the environmental implications of the material treatment steps since waste materials will have higher contaminant levels.

Tisserant et al147 in their review have provided a different perspective on the sustainability of biochar noting its use can have significant advantages for smallholder farmers in the tropics. The soil conditioning properties of biochar in these regions can potentially help curb agriculture-induced deforestation and thus provide social, and economic benefits in addition to the environmental advantages. All in all existing literature maintains a generally favorable outlook on the use of biochar on multiple levels. However, to attain the maximum benefits significant infrastructure development is inevitable to utilize the pyrolysis co-products during biochar generation, since the environmental effects of the pyrolysis step can be offset by the utilization of the co-products for energy generation. Moreover, past studies148 have raised concerns about the toxic substances present in biochars including carcinogenic polycyclic hydrocarbons, heavy metals and harmful free radicals. Zhang et al. investigated the effect of biochar nanoparticles on seedling growth, reporting that biochar nanoparticle toxicity risk was related to the nature of the feedstock.148 Thus, it can be surmised that use of biochar seed coatings is still in its nascent stage, and further research needs to be conducted to re-affirm their utility with a focus on pre-treatment to remove harmful substances present. Furthermore, environmental risk assessment studies need to be performed prior to any recommendations for their wide-scale usage can be made.

Figure 12. Biochar can be derived from pyrolysis of biomass derived from various precursors. Figure adapted and modified from an open source article reference.149 (b) Schematic showing one possible design of biochar pre-treatment steps. The raw biochar is washed with either only water or with acid/alkaline/surfactant treated water to clean pores and adjust characteristics like pore volume, VOC content and pH. The excess liquid from the treated biochar is removed through vacuum exfiltration and moisture levels are adjusted through centrifugation. The washed and moisture adjusted biochar can be bagged or further treated. Figure adapted and modified from reference.144 (c) Digital images of weed biomasses and derived biochar produced at pyrolysis temperature of 600⁰C. Figure adapted with permission.143 Copyright Elsevier 2020. SEM images of biochar derived from (d) pine, (e) birch and (f) coconut shells. (d-f) adapted from reference.144 (g) Bar graph summarizing results from pot trials of PGP rhizobacteria inoculated bioformulation tomato seed coatings. Figure adapted and modified with permission.56 Copyright Elsevier 2017. Treatments tested included: (1) Control - Soil without bioformulation, (2) L2 + FA = Soil + Flyash based bioformulation of Burkholderia sp. L2, (3) L2 + BC = Soil + Biochar based bioformulation of Burkholderia sp. L2, (4) L2 + FA + BC =  Soil + Flyash and biochar (1:1) based bioformulation of Burkholderia sp. L2, (5) A30 + FA = Soil+  Flyash based bioformulation of Bacillus sp. A30, (6) A30 + BC = Soil + Biochar based bioformulation of Bacillus sp.A30, (7) A30 + FA + BC = Soil + Flyash and biochar (1:1) based bioformulation of Bacillus sp. A30. All 6 treatments demonstrated significantly higher fruit weight and yield compared to untreated controls. (h-i) Results from greenhouse trials of phosphorus solubilizing bacteria P. libanensis inoculated biochar coated corn seeds. Plant growth was assessed for controls and treatments in presence of (h) Hoagland solution - soluble phosphorus and (i) Hoagland solution + tricalcum phosphate. Plant fresh weight and height were significantly increased only for biochar based coating in presence of soluble phosphorus indicating that phosphorus solubilization effect of the inoculated bacteria may not be a significant source of promoting plant growth. Data replotted from open source article.55

5.2. Lignocellulosics matrixes as Wrap and Plant – a unique and sustainable alternative to existing seed treatment methodologies

Lignocellulosics are plant-derived 3-D polymer composites comprising of lignin (10-25%), cellulose (35-50%) and hemicellulose (20-35%).150 Mainly produced as agriculture and industrial wastes, these are either mostly burnt or used as animal fodder. Recently, the recycling of these materials has been explored through their usage in diverse applications151 including synthesis of bioplastics,152 and specialty chemicals,153,154 dye-removal for industrial waste water treatment,155 and as biocide carriers.156 A unique application of lignocellulosic matrixes is their use in seed coatings. In a pioneering study, Cao and coworkers reported the use of plant-derived biodegradable controlled release matrix that can be used as seed wraps.157 These matrices were loaded with abamectin, a model nematicide with limited soil mobility. They termed the approach as “wrap and plant.” The efficacy of the matrixes synthesized from abaca, banana, softwood and hardwood fibers was tested by planting tomato seedlings wrapped by the matrixes. Banana fiber matrix gave the most promising results, which the authors have attributed to the sustained release of abamectin from the banana fiber matrix compared to the burst release observed from the other matrices (Figure 13a).

In a follow-up paper150 from the same group, the effect of processing conditions on the morphology of the matrixes and release profile of abamectin from the banana fiber-based matrices were analyzed. Utilizing banana harvest waste, they developed matrixes at different refining (mechanical beating) levels of the fiber pulp (Figure 13 b-f). Variation in the release of the loaded cargo showed a morphology dependent release from banana fiber matrices. In contrast, the controls (non-banana fiber matrices) showed a release rate dependent on the lignin content, with high lignin showing a slower release rate and low lignin content matrixes showing faster release rates for both hydrophobic and hydrophilic loaded cargoes (Figure 13g). This straightforward approach has the potential to significantly improve agriculture practices in resource deficient regions like sub-Saharan Africa where smallholder farmers cannot afford expensive seed treatment technologies. The simplicity and cost-effectiveness combined with the absence of any specialty chemicals or complicated processing steps makes this approach easy for smallholder farmers to adopt, achieving higher crop yields without compromising the soil quality. Furthermore, the wrapping matrixes are biodegradable which can facilitate carbon sequestration. The ease of designing the W&P matrixes into different sizes and shapes provides the flexibility to easily tailor these matrixes for a wide variety of seeds, seed pieces or seedlings. Field trials conducted in sub-Saharan Africa on yam and potato crops show enhanced crop health and effective control over plant parasitic nematodes (PPN) populations.158,159 More interestingly, during the potato field trails in Kenya, it was observed that even without a nematicide, banana-paper matrix substantially reduced potato cyst nematodes (PCN) field inoculum and increased potato yield.156 Further research reported the amazing role played by banana paper to disrupt parasite-host chemical signaling by absorbing PCN hatching chemicals. This novel attribute together with effective control of PPN population and improved yield and quality of crops via sustained release of the ultra-low dose of AI from a matrix developed from agricultural wastes holds a promise for the future of precision agriculture. In addition, a recently published investigation of the acceptance of ‘wrap and plant’ technology in terms of social and economic impacts  is supporting evidence for the efficiency and impact of this approach.160 While smallholder farmers can easily adopt this unique approach owing to the availability of working hands to wrap the seed/seed pieces for a small farm, implementation of the ‘wrap and plant’ approach for mechanized farming will require significant modifications in terms of design and implementation.

Figure 13. Wrap and Plant technology as an alternative to conventional seed coatings. (a) Results from in-vitro assays depicting mortality of C. elegans nematodes through time and cycle dependent release from abamectin loaded lignocellulosic matrices made from abaca, banana, softwood, and softwood-hardwood fibers. Abamectin loaded abaca matrix shows high mortality within the first hour/cycle whereas banana matrix shows lower but stable action against the nematodes over the assay duration (time/cycle). The stable action of banana fiber can be attributed to sustained release of abamectin from the loaded matrix compared to the burst release from abaca matrixes. Figure adapted with permission.157 Copyright Springer Nature 2016. (b) Schematic depicting utilization of banana harvest waste to synthesize matrixes that can be used to wrap seeds achieving seed based crop protection. (c) Digital image depicting effect of refining time from 0 to 30 minutes on the appearance of banana fiber matrixes.  (d-e) SEM images of the fibrillar structure in banana fiber matrix. (f) Scatter plot showing the effect of refining time on strength (burst and tear index) of banana fiber sheets. (g) Abamectin release profile from P1 = liner paper, P2, P3, P4 = banana fiber with lignin contents of 11.96, 10.25, 7.2 % respectively, and P5 = copy paper. Whereas non-banana fiber matrixes P1 and P5 exhibit slow and fast abamectin release respectively, all banana fiber matrixes P2, P3, P4 show similar release profiles. Figures (b-g) adapted with permission.150 Copyright 2020 American Chemical Society.

5.3. Natural AI based seed coatings

A recent emerging area in seed coating research has been the incorporation of natural AI as an environmentally friendly alternate over synthetic AI. One particular class of biomass-derived natural AIs is protein hydrolysates (PHs) as biostimulants. PHs are defined as a mixture of amino acids, oligo and polypeptides derived from partial hydrolysis of protein sources. They have been identified to provide key benefits to promote plant growth through enhancing soil microbial and enzymatic activity, promoting micronutrient uptake, and increasing phytochemicals in fruits.161 Another key benefit of using PHs is that they can be derived from animal and plant biomass thus promising a sustainable raw material source as well as providing a suitable recycling solution for biological waste. While these have been largely investigated as foliar treatments,162,163 their use in seed coatings promises targeted delivery and lower drift losses. In a relevant work, Amirkhani et al164 analyzed the effect of coatings synthesized from a mixture of soy flour, cellulose fiber and diatomaceous earth on broccoli seeds. While coated seeds displayed delayed germination, greenhouse trials showed significant improvements in plant height, dry and fresh biomass, leaf area and total nitrogen content. Similarly, a recent patent165 has disclosed the use of soy PHs for use as adhesive for attaching fungal spores to vegetable seeds. The adhesion capacity quantified through measuring the adherence of fluorescent microspheres (substitutes for spores) on seeds after vigorous washing through fluorescence microscopy was significantly higher in the samples compared to controls using just sterile water as the adhesive. Similar improvements with animal-sourced proteins have also been reported. Wilson et al.166 investigated the effect of gelatin capsules on the growth of cucumber seeds by placing the capsules adjacent to the seeds in pots. They reported enhanced growth parameters of the seedlings over a 14 days interval. More recently, Lawinska et al167 explored the use of collagen hydrolysate derived from tanning waste as coatings from legume seeds. The coating consisted of an internal layer of fungicides covered by the collagen hydrolysate enclosed in outer mineral layer. Growth assays conducted in soil for 29 days under drought conditions showed enhanced seedling growth compared to controls.

Waste biomass can serve as an ample raw material source for PHs synthesis, however the impact of the synthesis process needs to be categorized for evaluating their overall sustainability. Currently chemical hydrolysis of leather waste accounts for 90% market share of PHs biostimulants while enzymatic conversion of plant biomass accounts for the remainder. Conventional hydrolysis entails the use of strong acids and high temperatures while enzymatic conversion proceeds through the use of enzymes under milder temperatures. Colantoni et al168 conduced an LCA  of PH derived from leather wastes and lupine seeds providing a comparative analysis of the overall impact of the two synthesis routes. The CO2 eq emissions were reported to be much lower with enzymatic hydrolysis at 743.2 CO2 eq g compared to 1532.2 CO2 eq g in case of chemical hydrolysis of leather waste. Similarly, the fossil energy and utilization values were also significantly lower. Overall the use of biomass derived PHs as natural biostimulants is a promising alternative to reduce dependence on synthetic fertilizer for achieving higher plant yields. More research in this regard, particularly for seed coating applications is needed to further validate their utility.

Researchers have also analyzed the use of plant oils as natural AI. De Castro e Silva  et al.169 have proposed the use of neem (Azadirachta indica) oil/pectin nanocomposites as soybean seed coatings recommending effective utilization of the antifungal properties of neem as a biopesticide against common soybean pathogens. Their results demonstrated positive effects of the treatment on shoot and seedling length. However tests evaluating seedling germination in presence of fungal pathogens would have further validated treatment efficacy. Similarly, Ben-Jabeur and coworkers170 have explored the potential of thyme essential oil as wheat seed coatings to fight biotic and abiotic stresses. Field trials of wheat seeds coated with a commercial seed coating product Agicote Rouge mixed with thyme oil over two crop seasons in semi-arid soils were conducted under severe and moderate water stress conditions. Their results demonstrated the positive impacts of thyme oil on straw yield under severe water stress conditions and on grain yield under less severe water stress. Thus plant derived oils show significant potential as natural AIs, however their sustainable use presents some concerns. A recent report171 assessed greenhouse gas emissions from vegetable (palm, soybean, rapeseed, sunflower) during oil production through analysis of published LCA data reporting a median value of 3.81 kg CO2 e per kg of refined oil. Although these values refer to food product oils, similar values have been reported for neem and thyme plant oils. Kumar et al172 conducted LCA analysis to gauge the environmental impacts of biodiesel derived from various vegetable oils in India reporting a total energy equivalent value of 6.508 MJ/kg of biodiesel for the plant cultivation and oil extraction systems. Similarly, results of an LCA173 conducted to gauge impacts of medicinal plants in Italy report a GWP of 18.22 kg CO2 e per kg of dried plant product. Although these LCA results mention different impact assessment indicators, they provide an estimate of the energy/global warming impact of the plant cultivation. Oil extraction occurs further downstream from cultivation and is so bound to have a higher energy footprint. Thus, to achieve sustainable utilization of plant oils as natural AI we will have to identify a sweet spot between the lowest environmental impact during production and the benefits achieved through cut down of synthetic agrochemical intake due to their usage.

6. Comparing performance across different coating materials

A comprehensive evaluation of the environmental consequences of any new seed coating material demands a risk assessment of the coating material as well as the effects of the change in agriculture practices. Table 4 shows a comparison across different coatings proposed in the previous sections in terms of the yield benefits gained through their use and their performance from a green chemistry perspective including raw material source, industrial and environmental footprints and regulatory compliances.

Polysaccharides offer a clear advantage in terms of renewable raw material, biodegradability and adherence to regulatory compliances. Alginate, guar gum and starch are GRAS specified by FDA for use in certain food applications whereas chitosan is an accepted pesticidal AI. Furthermore, alginate, chitosan and guar gum all are exempted from adhering to a maximum tolerance limit in pesticides as per 40 CFR 40, part 180. However, their current chemical extraction methods have a high chemical footprint requiring large amounts of water, energy and use of acids/alkalis. Future research needs to focus on environmentally friendly extraction techniques coupling benign synthesis with high crop yields. Moving on to nanofibrous seed coatings, both synthetic and bio-based polymers have been reported in this regard. Whereas biobased polymers like CA are preferred due to their renewability, a major limitation is the use of toxic solvents like DMAc to prepare an electrospinnable solution. An alternative is the use of water soluble polymers such as PVA and PEO. Despite their biodegradability, these polymers are majorly derived from fossil fuel sources and are thus non-renewable. Thus, there are associated limitations with both bio-derived and synthetic electrospinnable polymers that need to be resolved. The next research breakthrough discussed is the use of hydrogels for coating seeds. Hydrogels will definitely be of greater consequence in coming years for enabling agriculture in arid soils due to the increasing burden on global water resources. Whereas fossil fuel-derived hydrogels like PAM, and sodium acrylate have been investigated as seed coatings, the use of sustainably sourced materials like starch and alginate appears as a better choice provided the chemical footprint of their extraction processes is optimized. Next, we have highlighted nanoparticle incorporated seed coatings to reduce synthetic fertilizer inputs. Although research in this area has shown promising results with enhanced seed germination and growth at low dosage volumes, there are question marks regarding the long term effects of nanoparticle usage on the ecosystem. Thus, research is required both at academic levels and by regulatory bodies to provide clear answers in this regard. Finally, we have shed light on the use of biomass-derived seed treatment techniques in order to close the loop for achieving a circular agriculture economy. Research in this area is at a very introductory stage and there is a lack of regulatory compliance and concerns like non-uniform source material and energy extensive treatment processes. Despite these limitations, researchers have shown the multifaceted huge potential of these materials/techniques Lignocellulosic seed wraps, for instance, have not only shown superior on-field performance, their thrift and ease of use facilitates their usage in resource deficient areas where farmers cannot afford expensive seed coating treatments.

Table 4. Comparison of seed coating materials on basis of their raw material source, industrial and energy footprint, regulatory compliance status and progress observed as seed coatings.

| Material |  | Raw material source | Industrial footprints | Energy consumption | Regulatory compliance/ Active list statusa |  | Environmental fate |  | Performance as seed coating |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Green chemistry principle |  | 7- Feedstock renewability | 4, 5 – Design and usage of safer chemicals and solvents | 6 – Energy utilization | 4 – Safer chemical design |  | 10 – Material degradation |  |  |  |
| Polysaccharides | Alginate | Brown seaweed | Chemical extractions involve utilization of acids/alkalis and toxic chemicals. | Water and energy-intensive | calcium, sodium, postassium alginate GRAS FDA as food additives in some categories. Sodium alginate -40 CFR 180 - pesticide tolerance exemption, Approved under 40 CFR 152.25 as an inert in exempted minimum risk pesticides | Biodegradable |  | Suitable carrier material for PGPM53 and NPK fertilizer, performance verified through pot trials. |  |
|  | Chitosan | crustacean, nematodes, insects | Chemical extraction involves harsh chemicals, acid and alkalis and elevated temperatures. Deacetylation step utilizes 40-50% concentrated NaOH. | Water and energy intensive | Pesticides - Active Ingredients EPA-USA 40 CFR 180 - pesticide tolerance exemption | Biodegradable |  | Demonstrated performance as antifungal agent.81, 82 Performance verified through pot trials. |  |
|  | Guar gum | C. tetragonoloba plant | Extracted from guar seeds. Water and ethanol typically used during extraction. Acids typically used for separating seed hulls. | Water intensive. | GRAS, FDA 40 CFR 180 - pesticide tolerance exemption, Approved under 40 CFR 152.25 as an inert in exempted minimum risk pesticides | Biodegradable |  | Discussed as a suitable coating material in patent literature94, 95 |  |
| Silk fibroin |  | Silkworm (Bombyx mori) | Typical extraction involves use of sodium carbonate and lithium bromide | Water and energy intensive | NA | Biodegradable |  | Used as PGPM inoculant carrier in multilayered seed coatings. Performance verified through field trials at water stress conditions. |  |
| Nanofibers | PVA | Fossil fuel | Water used as electrospinning solvent | Energy intensive due to high voltage source required | 40 CFR 180 - pesticide tolerance exemption | Biodegradable |  | Used as a carrier for PGPM101, 57,58 fertilizer103, 104 and fungicide102, 106 to achieve targeted delivery. Performance verified through greenhouse and germination trials. |  |
|  | Ethyl cellulose | Plants | toxic electrospinning solvents dichloromethane, ethanol, N,N-dimethyl formamide |  | GRAS in animal feed 2020 CDR Full Exempt | Biodegradable |  |  |  |
|  | PVP | Fossil fuel | chloroform/ethanol |  | Pesticides - Active Ingredients EPA-USA, 40 CFR 180 - pesticide tolerance exemption, 2020 CDR Full Exempt, 2020 CDR Full Exempt | Non-biodegradable |  |  |  |
|  | CA | Plant biomass | Has been electrospun with harsh solvents like dimethyl acetamide (DMAc) and milder options like acetone, acetic acid |  | Approved under 40 CFR 152.25 as an inert in exempted minimum risk pesticides, 40 CFR 180 - pesticide tolerance exemption | Biodegradable |  |  |  |
|  | PEO | Fossil fuel | Water used as electrospinning solvent |  | Pesticides - Active Ingredients EPA-USA, 40 CFR 180 - pesticide tolerance exemption | Biodegradable upto Mw 20,000Da |  |  |  |
| Hydrogels | PAM | Fossil fuel | Produced by polymerization of monomers which may entail use of organic solvents, intitiators and catalylsts. | Energy-intensive | 2020 CDR Full Exempt | Biodegradable |  | Used to enhance water retention around seeds under water stress conditions. 11,119 Growth studies in soil conducted to verify performance. |  |
|  | Sodium Polyacrylate | Fossil fuel |  |  | 2020 CDR Full Exempt Pesticides - Active Ingredients EPA-USA | Landfill |  |  |  |
|  | Starch | Plant source | Wet milling extraction processes involve harsh chemicals and repeated water and alkaline washes. | Water and energy-intensive | Unmodified starch GRAS in certain food appilications. 2020 CDR Full Exempt | Biodegradable |  |  |  |
| Nanoparticles |  | Ores | Conventional capping, reducing agents and solvents pose significant safety and toxicity hazards. | Energy-intensive | If used as pesticide, subject to e Federal Insecticide, Fungicide, and Rodenticide Act (FIFRA section 2(u) and 3(a)). If present as residue in animal feed or food, tolerance limit needs to be designated as per the Federal Food, Drug and Cosmetic Act (FFDCA) | Unknown |  | Used as a doping material as a to achieve enhanced fertilizer activity. 124, 125, 130 Performance verified through pot trials. |  |
| Biomass | Biochar | Agriculture and industrial biomass waste | High temperatures required during pyrolitic conversion of biomass | Energy and water-intensive | NA | NA |  | Used as a carrier material for PGPM inoculated seed coatings as well as to enhance seed water retention. 55 Performance validated through greenhouse trials. |  |
|  | Lignocellulosics |  | Handsheets are prepared by dewatering aqueous slurry of chopped banana fibers | Water-intensive. | 2020 CDR Full Exempt | Biodegradable |  | Used as seed wraps prior to planting. 150, 158 Performance verified through field trials. |  |

aPesticide tolerance exemption as per Code of Federal Regulations (CFR) 40, part 180 implies that the material is deemed safe enough such that establishment of maximum tolerance limits is not required for the end-use described in the exemption. Chemical Data Reporting (CDR) exempt implies the material is exempt from reporting as per the Toxic Substances Control Act (TSCA). GRAS stands for Generally Regarded as Safe by US Food and Drug Administration (FDA). Data extracted from EPA Substance Registry Services.174

The final question to be addressed is the long-term effect on crop yields due to the adoption of a new seed coating/treatment. LCA studies offer a suitable choice to classify the sustainability of any new material/practice. However, comparison across different LCA is complicated due to variations in the selection of functional units, process boundaries and conditions. These challenges are even more diverse across agriculture systems due to the inherent existing diversity and nature of these changes like variations in climatic conditions, agrochemical inputs, watering rates and effects on biotic and abiotic stresses. This necessitates some form of LCA framework to consistently characterize the effects of the suggested change in order to make preemptive decisions on their suitability. This need for improved methodology guidelines for conducting risk assessments across agriculture systems has been highlighted by many researchers.175,176 Recently Kløverpris et al.178 proposed a method to evaluate impacts resulting from a shift in agriculture practice through expanding the effects of the shift (upstream, downstream, field and yield changes) elsewhere in order to quantify the resultant environmental impacts. Furthermore, they proposed the use of geochemical modeling to quantify emission changes due to the shift in practice. These proposed LCA techniques can be a significant aid in the search for sustainable and efficacious seed coating materials allowing a way to simultaneously gauge environmental and yield based performances.

7. Future trends

The last decade has been wrought with increased academic and industrial research on the development of environmentally friendly seed treatments with sufficient efficacy to achieve the desired level of crop protection with minimal environmental damage. The multidisciplinary nature of the research has brought together material scientists, agronomists, and plant pathologists in increased collaborations toward the design of custom-made seed coatings as per the nature of the crop and the pest treatment required. The use of biodegradable and biocompatible polymer coatings has been the key focus of many recent publications. In general, the trend has been the investigation of a polysaccharide-based seed coating developed in a laboratory scale apparatus with a handful of studies looking at greenhouse and field data on the performance of the proposed coatings.

A paradigm shift in existing industrial practices has also been observed to accommodate the increasing focus on sustainability by both consumers and regulatory bodies. Industrial seed coating giants like BASF177, Syngenta178, and Corteva179 have set sustainability goals as part of their commitment. Also, there has been a rise in seed coating start-ups that are bringing in innovative sustainable seed coating solutions and thus diminishing the gap between academic research and on-field implementation. Table 5 summarizes information on recently established companies providing seed coating products and services. While the exact composition of the available commercial products is proprietary information but companies are offering microplastic free and biological solutions reflecting their increasing importance.

Table 5. Some recent seed coating industrial ventures

| Company | Year of establishment | Location | Seed coating product/service |
| --- | --- | --- | --- |
| SilviBio180 | 2019 | Scotland, UK | Biobased seed treatment coatings and additives |
| Agrynex181 | 2015 | USA | Enzyme based seed coating offers one-stop protection against multiple pathogens |
| Ad Terram182 | 2014 | Netherlands | Microplastic-free biodegradable seed coatings |
| Indigo Ag183 | 2013 | Massachusetts, USA | PGPM-based seed coating powders and slurries |
| Green and Seed Corp.184 | 2013 | Republic of Korea | Biodegradable seed films composed of polylactic acid and polybutylene adipate terephthalate to enable rice cultivation without flooding |
| Summit Seed Coatings185 | 2002 | Idaho, Indiana USA | Multiple seed coating solutions including fungicide, inoculant, and hydrogel coatings. |

Some key trends that future researchers on the subject should strive to focus on include:

- Increased field trial investigations: to validate the performance of many newly designed hybrid polymeric seed coatings.

- Commercialization: to give insights into whether the proposed seed treatments proposed are viable to be used on a large scale basis or not. A cost/benefit analysis along with the overall impact of the proposed seed treatment on the soil rhizosphere will provide a more comprehensive analysis of the viability of the technique.

- Although the risks associated with the release of pesticide-laden seed dust from coated seeds are well documented, to our knowledge very few studies32,95 on the design of novel seed coatings have discussed or reported the drift risk factor associated with the proposed coating. Thus, in addition to seed germination and material stability analysis, the associated dust drift factors should also be investigated.

- Shelf life stability and safety is another crucial aspect of any proposed seed coating material that needs to be thoroughly investigated. While some aspect of long-term storage viability has been reported for microbe inoculated seed coatings (Table 2) generally with reference to the microbe survival count in the coated seed or inoculate over a period of time, there is little work done on investigating the chemical stability of proposed coatings. Such an analysis is vital for newly proposed biodegradable materials, as in addition to the known additives, monomers, and stabilizers in conventional plastics, they may also contain lower molecular weight intermediates released over time due to partial degradation.186 The characterization of the biosafety and exposure limits of these intermediates is needed before any newly proposed seed coating material is short-listed for further use.

- The use of bioplastics derived from biopolymers for seed coatings may appear to be a promising solution to the ongoing MP pollution debate, however, their usage is not without limitations. Concerns related to the long-term use of bioplastics include (1) high production costs, (2) concerns about increased global warming due to higher degradation-induced release of CO2 and methane gas (Figure 14a), (2) slow degradation rates, and (3) utilization of agriculture land for catering to plant-derived biopolymer demand instead of food cultivation, which in turn will increase agriculture demand.187 Figure 14 shows data on energy usage and greenhouse gas emissions resulting from the production of bio-based plastics compared to conventional plastics. LCA studies can play a crucial role in identifying whether the use of the proposed bio-derived materials offers any significant benefit over existing materials. Depending on the outcomes of the study, prudent decisions can be made on material suitability.188

Figure 14. Comparison of (a) Greenhouse gas emissions (b) Nonrenewable energy use (NREU) during biopolymer production compared to conventional plastics. Adapted with permission.188 Copyright Elsevier 2016. Acronyms in x-axis denote polylactide (PLA), polyhydroxyalkanoates (PHAs), polycaprolactone (PCL), polyethylene (PE), low-density polyethylene (LDPE), high-density polyethylene (HDPE), polypropylene (PP), polyethylene terephthalate (PET), polystyrene (PS), Acrylonitrile butadiene styrene (ABS), Polyamide 6,6 (PA 66).

Acknowledgments

The authors would like to thank the Bill and Melinda Gates Foundation [OPP1196989] for supporting this work. The authors also acknowledge the Kenan Institute of Engineering, Technology and Science (KIETS) at NC State for supporting this work.

REFERENCES

1	I. Rocha, Y. Ma, P. Souza-Alonso, M. Vosátka, H. Freitas and R. S. Oliveira, Front. Plant Sci., 2019, 10, 1357.

2	K. Vanangamudi, Seed hardening, pelleting and coating : principles and practices, Satish Serial Pub, Delhi, 2006.

3	F. E. Porter and J. M. Scott, in Proceedings of the Short Course for Seedsmen, Mississippi State : Seed Technology Laboratory, Mississippi State University., Mississippi, 1979.

4	I. M. Phillips Mcdougall, ANALYSIS ON SALES AND PROFITABILITY WITHIN THE SEED SECTOR: INDEPENDENT REPORT BY IHS MARKIT (PHILLIPS MCDOUGALL) FOR THE CO-CHAIRS OF THE AD-HOC OPEN-ENDED WORKING GROUP TO ENHANCE THE FUNCTIONING OF THE MULTILATERAL SYSTEM OF FAO’S INTERNATIONAL TREATY ON PLANT GENETIC RESOURCES FOR FOOD AND AGRICULTURE, 2019.

5	FAO, FAOSTAT, http://www.fao.org/faostat/en/#data/RP/metadata, (accessed 2 October 2021).

6	ISF, Seed statistics, https://www.worldseed.org/resources/seed-statistics/, (accessed 2 October 2021).

7	R. W. Gesch, D. W. Archer and K. Spokas, F. Crop. Res., 2012, 125, 109–116.

8	G. Kaufman, HortTechnology horttech, 1991, 1, 98–102.

9	I. R. J. Legro, in Challenges and Opportunities for Organic Agriculture and the Seed Industry, ed. A. Martinez, International Federation of OrganicAgricultureMovements, Bonn, Germany, 2004, p. 109.

10	S. Pedrini, D. J. Merritt, J. Stevens and K. Dixon, Trends Plant Sci., 2017, 22, 106–116.

11	L.-Q. Su, J.-G. Li, H. Xue and X.-F. Wang, J. Zhejiang Univ. Sci. B, 2017, 18, 696–706.

12	CropLife Foundation, The Role of Seed Treatment in Modern U.S. Crop Production, 2013.

13	H. Sun, Y. Cao, D. Kim and B. Marelli, Adv. Funct. Mater., 2022, n/a, 2201930.

14	E. Kavusi, B. Shahi Khalaf Ansar, Z. Dehghanian, B. Asgari Lajayer, K. Nobaharan, Y. Ma and B. R. Glick, J. Plant Growth Regul., , DOI:10.1007/s00344-022-10597-2.

15	H. C. Erythropel, J. B. Zimmerman, T. M. de Winter, L. Petitjean, F. Melnikov, C. H. Lam, A. W. Lounsbury, K. E. Mellor, N. Z. Janković, Q. Tu, L. N. Pincus, M. M. Falinski, W. Shi, P. Coish, D. L. Plata and P. T. Anastas, Green Chem., 2018, 20, 1929–1961.

16	M. Ashraf and M. R. Foolad, in Advances in Agronomy, Volume 88, ed. D. L. Sparks, Elsevier Science, Netherlands, 2005, p. 257.

17	A. G. Taylor, P. S. Allen, M. A. Bennett, K. J. Bradford, J. S. Burris and M. K. Misra, Seed Sci. Res., 1998, 8, 245–256.

18	G. R. and S. P. Komala NT, Basava arya BR, Sumalatha GM, J Pharmacogn Phytochem, 2018, 7, 3124–3128.

19	E. Hartley, L. Greg Gemell and D. F. Herridge, Soil Biol. Biochem., 2004, 36, 1289–1294.

20	B. Shaharoona, M. Naveed, M. Arshad and Z. A. Zahir, Appl. Microbiol. Biotechnol., 2008, 79, 147–155.

21	E. F. Durner, Principles of Horticultural Physiology, CABI, UK, 2013.

22	A. G. Taylor, in The Physiology of Vegetable Crops, eds. H. C. Wien and H. Stützel, CABI, 2nd edn., 2020, p. 23.

23	L. O. Copeland and M. F. McDonald, Principles of Seed Science and Technology, Springer, US, 4th edn., 2012.

24	P. Halmer, in Handbook of seed physiology : applications to agriculture, eds. R. L. Benech-Arnold and R. A. Sanchez, New York : Food Products Press : Haworth Reference Press, New York, USA, 2004, p. 129.

25	P. Halmer, in Seed technology and its biological basis, eds. M. Black and J. D. Bewley, Sheffield, England : Sheffield Academic Press ; Boca Raton, FL : CRC Press., 2000, pp. 274–283.

26	B. Gregg and G. Billups, Seed Conditioning, Volume 2: Technology--Parts A \& B, CRC Press, 2016.

27	S. Pedrini, A. Balestrazzi, M. D. Madsen, K. Bhalsing, S. P. Hardegree, K. W. Dixon and O. A. Kildisheva, Restor. Ecol., 2020, 28, S266–S275.

28	D. Foqué, B. Beck, W. Devarrewaere, P. Verboven and D. Nuyttens, Pest Manag. Sci., 2017, 73, 1908–1920.

29	C. Accinelli, H. K. Abbas, W. T. Shier, A. Vicari, N. S. Little, M. R. Aloise and S. Giacomini, Chemosphere, 2019, 226, 645–650.

30	D. Nuyttens, W. Devarrewaere, P. Verboven and D. Foqué, Pest Manag. Sci., 2013, 69, 564–575.

31	B. Zhang, X. Yang, L. Chen, J. Chao, J. Teng and Q. Wang, J. Chem. Technol. Biotechnol., 2020, 95, 2052–2068.

32	US Pat., 10258034B2, 2013.

33	M. Amit, R. K. Mishra, Q. Hoang, A. M. Galan, J. Wang and T. N. Ng, Mater. Horizons, 2019, 6, 604–611.

34	M. Rundlöf, G. K. S. Andersson, R. Bommarco, I. Fries, V. Hederström, L. Herbertsson, O. Jonsson, B. K. Klatt, T. R. Pedersen, J. Yourstone and H. G. Smith, Nature, 2015, 521, 77–80.

35	A. R. Main, E. B. Webb, K. W. Goyne, R. Abney and D. Mengel, Sci. Total Environ., 2021, 786, 147299.

36	A. M. Alford and C. H. Krupke, Environ. Sci. Technol., 2019, 53, 14368–14376.

37	M. Yamamuro, T. Komuro, H. Kamiya, T. Kato, H. Hasegawa and Y. Kameda, Science (80-. )., 2019, 366, 620 LP – 623.

38	S. D. Frank and J. F. Tooker, Proc. Natl. Acad. Sci., 2020, 117, 22609 LP – 22613.

39	C. Botías, A. David, E. M. Hill and D. Goulson, Sci. Total Environ., 2016, 566–567, 269–278.

40	J. Radolinski, J. Wu, K. Xia and R. Stewart, Sci. Total Environ., 2018, 618, 561–568.

41	M. R. Douglas and J. F. Tooker, Environ. Sci. Technol., 2015, 49, 5088–5097.

42	A. Allington, Bloom. Law, 2020.

43	C. Hitaj, D. J. Smith, A. Code, S. Wechsler, P. D. Esker and M. R. Douglas, Bioscience, 2020, 70, 390–403.

44	L. Walker and G. Naylor, Hill, 2015.

45	D. M. Mitrano and W. Wohlleben, Nat. Commun., 2020, 11, 1–12.

46	S. N. Akanyange, X. Lyu, X. Zhao, X. Li, Y. Zhang, J. C. Crittenden, C. Anning, T. Chen, T. Jiang and H. Zhao, Sci. Total Environ., 2021, 777, 146020.

47	US Pat., 20200367490A1, 2020.

48	X. Duan and J. S. Burris, Crop Sci., , DOI:https://doi.org/10.2135/cropsci1997.0011183X003700020034x.

49	N. Begum, C. Qin, M. A. Ahanger, S. Raza, M. I. Khan, M. Ashraf, N. Ahmed and L. Zhang, Front. Plant Sci., 2019, 10, 1068.

50	Y. Ma, Biotechnol. Adv., 2019, 37, 107423.

51	C. Accinelli, H. K. Abbas, N. S. Little, J. K. Kotowicz, M. Mencarelli and W. T. Shier, Crop Prot., 2016, 89, 123–128.

52	D. Cortés-Rojas, C. Beltrán-Acosta, Y. Zapata-Narvaez, M. Chaparro, M. Gómez and M. Cruz-Barrera, Appl. Microbiol. Biotechnol., 2021, 105, 1889–1904.

53	Y. Bashan, J.-P. Hernandez, L. A. Leyva and M. Bacilio, Biol. Fertil. Soils, 2002, 35, 359–368.

54	K. S. V. P. Chandrika, R. D. Prasad and V. Godbole, Int. J. Biol. Macromol., 2019, 126, 282–290.

55	M. Głodowska, B. Husk, T. Schwinghamer and D. Smith, Agron. Sustain. Dev., 2016, 36, 21.

56	Tripti, A. Kumar, Z. Usmani, V. Kumar and Anshumali, J. Environ. Manage., 2017, 190, 20–27.

57	P. R. De Gregorio, G. Michavila, L. Ricciardi Muller, C. de Souza Borges, M. F. Pomares, E. L. Saccol de Sá, C. Pereira and P. A. Vincent, PLoS One, 2017, 12, e0176930.

58	Z. Hussain, M. A. Khan, F. Iqbal, M. Raffi and F. Y. Hafeez, J. Agric. Food Chem., 2019, 67, 5085–5095.

59	J. M. Campaña and M. Arias, ACS Appl. Polym. Mater., 2020, 2, 5033–5038.

60	S. Agake, M. D. Artigas Ramirez, K. Kojima, T. Ookawa, N. Ohkama-Ohtsu and T. Yokoyama, Agron. J., , DOI:https://doi.org/10.1002/agj2.20747.

61	A. T. Zvinavashe, J. Laurent, M. Mhada, H. Sun, H. M. E. Fouda, D. Kim, S. Mouhib, L. Kouisni and B. Marelli, Nat. Food, 2021, 2, 485–493.

62	S. H. Ching, N. Bansal and B. Bhandari, Crit. Rev. Food Sci. Nutr., 2017, 57, 1133–1152.

63	H. Hecht and S. Srebnik, Biomacromolecules, 2016, 17, 2160–2167.

64	O. Jeon, Y. Bin Lee, H. Jeong, S. J. Lee, D. Wells and E. Alsberg, Mater. Horizons, 2019, 6, 1625–1631.

65	Y. Yu, G. Chen, J. Guo, Y. Liu, J. Ren, T. Kong and Y. Zhao, Mater. Horizons, 2018, 5, 1137–1142.

66	T. Miao, J. Wang, Y. Zeng, G. Liu and X. Chen, Adv. Sci., 2018, 5, 1700513.

67	L.-H. Chen, L.-C. Cheng and P. S. Doyle, Adv. Sci., 2020, 7, 2001677.

68	US Pat., 20160249620, 2014.

69	T. Berninger, B. Mitter and C. Preininger, J. Microencapsul., 2016, 33, 127–136.

70	US Pat. 5292507A, 1992.

71	V. A. de Castro, V. G. O. Duarte, D. A. C. Nobre, G. H. Silva, V. R. L. Constantino, F. G. Pinto, W. R. Macedo and J. Tronto, Beilstein J. Nanotechnol., 2020, 11, 1082–1091.

72	R. A. Sequeira, M. M. Pereira, P. Vaghela, A. Bhayani, A. Dhimmar, D. Maru, A. Ghosh, R. Dineshkumar, P. B. Shinde, S. Ray and K. Prasad, ACS Agric. Sci. Technol., 2021, 1, 674–683.

73	S. Bor, İ. H. Kalkan, A. Çelebi, D. Dinçer, F. Akyüz, P. Dettmar and H. Özen, Turk. J. Gastroenterol., 2019, 30, 109–136.

74	K. S. Vuoristo, L. Fredriksen, M. Oftebro, M. Ø. Arntzen, O. A. Aarstad, R. Stokke, I. H. Steen, L. D. Hansen, R. B. Schüller, F. L. Aachmann, S. J. Horn and V. G. H. Eijsink, J. Agric. Food Chem., 2019, 67, 2936–2945.

75	L. B. Ladah, J. A. Zertuche-González and G. Hernández-Carmona, J. Phycol., 1999, 35, 1106–1112.

76	S. Saji, A. Hebden, P. Goswami and C. Du, Sustain. , 2022, 14.

77	D. Freepons, in Applications of Chitin and Chitosan, ed. M. F. A. Goosen, CRC Press, Boca Raton, Florida, USA, 1st edn., 1997, pp. 133–138.

78	J. Revuelta, I. Fraile, D. T. Monterrey, N. Peña, R. Benito-Arenas, A. Bastida, A. Fernández-Mayoralas and E. García-Junceda, Mater. Horizons, 2021, 8, 2596–2614.

79	J. Yu, D. Wang, N. Geetha, K. M. Khawar, S. Jogaiah and M. Mujtaba, Carbohydr. Polym., 2021, 261, 117904.

80	D. Chouhan and P. Mandal, Int. J. Biol. Macromol., 2021, 166, 1554–1569.

81	M. V Bhaskara Reddy, J. Arul, P. Angers and L. Couture, J. Agric. Food Chem., 1999, 47, 1208–1216.

82	K. Ziani, B. Ursúa and J. I. Maté, Crop Prot., 2010, 29, 853–859.

83	FAO, The State of World Fisheries and Aquaculture 2020. Sustainability in action., Rome, 2020.

84	N. Yan and X. Chen, Nature, 2015, 524, 155–157.

85	R. Chilakala, C. Thannaree, E. J. Shin, T. Thenepalli and J. W. Ahn, Recycl. , 2019, 4.

86	M. Maddaloni, I. Vassalini and I. Alessandri, Sustain. Chem. , 2020, 1.

87	S. M. Joseph, S. Krishnamoorthy, R. Paranthaman, J. A. Moses and C. Anandharamakrishnan, Carbohydr. Polym. Technol. Appl., 2021, 2, 100036.

88	I. Younes and M. Rinaudo, Mar. Drugs , 2015, 13.

89	N. Thombare, U. Jha, S. Mishra and M. Z. Siddiqui, Int. J. Biol. Macromol., 2016, 88, 361–372.

90	M. Prabaharan, Int. J. Biol. Macromol., 2011, 49, 117–124.

91	D. Mudgil, S. Barak and B. S. Khatkar, J. Food Sci. Technol., 2014, 51, 409–418.

92	N. Thombare, S. Mishra, M. Z. Siddiqui, U. Jha, D. Singh and G. R. Mahajan, Carbohydr. Polym., 2018, 185, 169–178.

93	US Pat., 5787640A, 1992.

94	US Pat., 20120220454A1, 2012.

95	US Pat., 20190150354A1, 2019.

96	M. Black and J. D. Bewley, Seed technology and its biological basis, Sheffield, England : Sheffield Academic Press ; Boca Raton, FL : CRC Press, 2000., Sheffield, England, 2000.

97	F. Gresta, A. I. De Luca, A. Strano, G. Falcone, C. Santonoceto, U. Anastasi and G. Gulisano, Ital. J. Agron., 2014, 9, 20–24.

98	H. M. Summers, E. Sproul, C. Seavert, S. Angadi, J. Robbs, S. Khanal, P. Gutierrez, T. Teegerstrom, D. A. Zuniga Vazquez, N. Fan and J. C. Quinn, Agric. Syst., 2021, 191, 103146.

99	J. Xue, T. Wu, Y. Dai and Y. Xia, Chem. Rev., 2019, 119, 5298–5415.

100	S. Meraz-Dávila, C. E. Pérez-García and A. A. Feregrino-Perez, Mater. Res. Express, 2021, 8, 42001.

101	R. Damasceno, I. Roggia, C. Pereira and E. de Sá, Can. J. Microbiol., 2013, 59, 716–719.

102	L. Castañeda, C. Genro, I. Roggia, S. Bender, R. Bender and C. Pereira, J. Res. Updat. Polym. Sci., 2014, 3, 33–39.

103	V. Krishnamoorthy, G. Elumalai and S. Rajiv, New J. Chem., 2016, 40, 3268–3276.

104	V. Krishnamoorthy and S. Rajiv, J. Clean. Prod., 2018, 177, 69–78.

105	T. Xu, C. Ma, Z. Aytac, X. Hu, K. W. Ng, J. C. White and P. Demokritou, ACS Sustain. Chem. Eng., 2020, 8, 9537–9548.

106	B. V. Farias, T. Pirzada, R. Mathew, T. L. Sit, C. Opperman and S. A. Khan, ACS Sustain. Chem. Eng., 2019, 7, 19848–19856.

107	K. Raja, C. Prabhu, K. S. Subramanian and K. Govindaraju, Polym. Bull., , DOI:10.1007/s00289-020-03435-6.

108	C. Z. Mosher, P. A. P. Brudnicki, Z. Gong, H. R. Childs, S. W. Lee, R. M. Antrobus, E. C. Fang, T. N. Schiros and H. H. Lu, Biofabrication, , DOI:10.1088/1758-5090/ac0964.

109	C. M. Alder, J. D. Hayler, R. K. Henderson, A. M. Redman, L. Shukla, L. E. Shuster and H. F. Sneddon, Green Chem., 2016, 18, 3879–3890.

110	N. Srivastava, Richa and A. Roy Choudhury, Colloids Surfaces B Biointerfaces, 2021, 205, 111891.

111	F. Gao, Z. Xu, Q. Liang, H. Li, L. Peng, M. Wu, X. Zhao, X. Cui, C. Ruan and W. Liu, Adv. Sci., 2019, 6, 1900867.

112	G. He, S. Chen, Y. Xu, Z. Miao, Y. Ma, H. Qian, Y. Lu and Z. Zha, Mater. Horizons, 2019, 6, 711–716.

113	Z. Yang, R. Huang, B. Zheng, W. Guo, C. Li, W. He, Y. Wei, Y. Du, H. Wang, D. Wu and H. Wang, Adv. Sci., 2021, 8, 2003627.

114	E. Caló and V. V Khutoryanskiy, Eur. Polym. J., 2015, 65, 252–267.

115	N. Singh, S. Agarwal, A. Jain and S. Khan, Agric. Water Manag., 2021, 253, 106939.

116	J. D. Berdahl and R. E. Barker, Agron. J., 1980, 72, 1006–1008.

117	S. Sarrocco, R. Raeta and G. Vannacci, Seed Sci. Technol., 2004, 32, 649–661.

118	L. Gorim and F. Asch, J. Agron. Crop Sci., 2012, 198, 81–91.

119	V. Pathak and R. P. K. Ambrose, J. Appl. Polym. Sci., 2020, 137, 48523.

120	V. Pačuta, M. Rašovský, B. Michalska-Klimczak and Z. Wyszyňski, Plants (Basel, Switzerland), 2021, 10, 757.

121	S. L. M. El Halal, D. H. Kringel, E. da R. Zavareze and A. R. G. Dias, Starch - Stärke, 2019, 71, 1900128.

122	D. H. Kringel, S. L. M. El Halal, E. da R. Zavareze and A. R. G. Dias, Starch - Stärke, 2020, 72, 1900234.

123	C. Rivard, L. Moens, K. Roberts, J. Brigham and S. Kelley, Enzyme Microb. Technol., 1995, 17, 848–852.

124	T. Adhikari, S. Kundu and A. S. Rao, J. Plant Nutr., 2016, 39, 136–146.

125	X. Zhao, Y. Chen, H. Li and J. Lu, IET Nanobiotechnology, , DOI:https://doi.org/10.1049/nbt2.12064.

126	P. Acharya, G. K. Jayaprakasha, K. M. Crosby, J. L. Jifon and B. S. Patil, Sci. Rep., 2020, 10, 5037.

127	N. Sundaria, M. Singh, P. Upreti, R. P. Chauhan, J. P. Jaiswal and A. Kumar, J. Plant Growth Regul., 2019, 38, 122–131.

128	A. N. Markov, A. V Vorotyntsev, A. A. Kapinos, A. N. Petukhov, V. I. Pryakhina, O. V Kazarina, A. A. Atlaskin, K. V Otvagina, V. M. Vorotyntsev and I. V Vorotyntsev, ACS Sustain. Chem. Eng., , DOI:10.1021/acssuschemeng.2c00940.

129	A. Vahid Mohammadi and M. Halali, RSC Adv., 2014, 4, 7104–7108.

130	L. Abeywardana, M. de Silva, C. Sandaruwan, D. Dahanayake, G. Priyadarshana, S. Chathurika, V. Karunaratne and N. Kottegoda, ACS Agric. Sci. Technol., 2021, 1, 230–239.

131	N. I. Agbeboh, I. O. Oladele, O. O. Daramola, A. A. Adediran, O. O. Olasukanmi and M. O. Tanimola, Heliyon, 2020, 6, e03765.

132	S. Zhu, L. Gong, Y. Li, H. Xu, Z. Gu and Y. Zhao, Adv. Sci., 2019, 6, 1802289.

133	H. Duan, D. Wang and Y. Li, Chem. Soc. Rev., 2015, 44, 5778–5792.

134	US Pat., 20040077498A1, 2003.

135	J. G. Halter, W. D. Chen, N. Hild, C. A. Mora, P. R. Stoessel, F. M. Koehler, R. N. Grass and W. J. Stark, J. Mater. Chem. A, 2014, 2, 853–858.

136	C. A. Mora, J. G. Halter, C. Adler, A. Hund, H. Anders, K. Yu and W. J. Stark, J. Agric. Food Chem., 2016, 64, 3501–3507.

137	B. D. Lawrence, ed. S. C. B. T.-S. B. for T. E. and R. M. Kundu, Woodhead Publishing, 2014, pp. 78–99.

138	EPA, Substance Registry Services (SRS) Polyvinyl alcohol, https://sor.epa.gov/sor_internet/registry/substreg/searchandretrieve/advancedsearch/externalSearch.do?p_type=CASNO&p_value=9002-89-5#, (accessed 21 June 2022).

139	C. Kalinke, P. R. de Oliveira, J. A. Bonacin, B. C. Janegitz, A. S. Mangrich, L. H. Marcolino-Junior and M. F. Bergamini, Green Chem., 2021, 23, 5272–5301.

140	A. Khan, N. Savidov, J. Zhang, J. Yang, T. Anderson, D. Harfield and A. O. Anyia, in Biochar : Production, Characterization, and Applications, eds. Y. S. Ok, S. M. Uchimiya, S. X. Chang and N. Bolan, CRC Press, Taylor & Francis Group, Boca Raton, Florida, USA, 2015, pp. 274–291.

141	T. K. Ralebitso-Senior and C. H. Orr, eds. T. K. Ralebitso-Senior and C. B. T.-B. A. H. Orr, Elsevier, 2016, pp. 1–40.

142	M. Genovese, J. Jiang, K. Lian and N. Holm, J. Mater. Chem. A, 2015, 3, 2903–2913.

143	S. K. Das, G. K. Ghosh and R. Avasthe, Environ. Technol. Innov., 2020, 20, 101074.

144	US Pat., 10550044B2, 2016.

145	M. I. Williams, R. K. Dumroese, D. S. Page-Dumroese and S. P. Hardegree, J. Arid Environ., 2016, 125, 8–15.

146	J. Matuštík, T. Hnátková and V. Kočí, J. Clean. Prod., 2020, 259, 120998.

147	A. Tisserant and F. Cherubini, L. , 2019, 8.

148	K. Zhang, Y. Wang, J. Mao and B. Chen, Environ. Pollut., 2020, 256, 113409.

149	Y. Ding, Y. Liu, S. Liu, Z. Li, X. Tan, X. Huang, G. Zeng, L. Zhou and B. Zheng, Agron. Sustain. Dev., 2016, 36, 36.

150	T. Pirzada, R. Mathew, R. H. Guenther, T. L. Sit, C. H. Opperman, L. Pal and S. A. Khan, ACS Sustain. Chem. Eng., 2020, 8, 6590–6600.

151	K. Liu, H. Du, T. Zheng, W. Liu, M. Zhang, H. Liu, X. Zhang and C. Si, Green Chem., , DOI:10.1039/D1GC02841C.

152	Q. Xia, C. Chen, Y. Yao, J. Li, S. He, Y. Zhou, T. Li, X. Pan, Y. Yao and L. Hu, Nat. Sustain., , DOI:https://doi.org/10.1038/s41893-021-00702-w.

153	M. Bilal, M. Asgher, H. M. N. Iqbal, H. Hu and X. Zhang, Int. J. Biol. Macromol., 2017, 98, 447–458.

154	R. A. Sheldon, Green Chem., 2014, 16, 950–963.

155	K. Bello, B. K. Sarojini, B. Narayana, A. Rao and K. Byrappa, Carbohydr. Polym., 2018, 181, 605–615.

156	B. D. Mattos, B. L. Tardy, W. L. E. Magalhães and O. J. Rojas, J. Control. Release, 2017, 262, 139–150.

157	J. Cao, R. H. Guenther, T. L. Sit, S. A. Lommel, C. H. Opperman and J. A. Willoughby, Cellulose, 2016, 23, 673–687.

158	J. Ochola, L. Cortada, O. Mwaura, M. Tariku, S. A. Christensen, M. Ng’ang’a, A. Hassanali, T. Pirzada, S. Khan, L. Pal, R. Mathew, D. Guenther, E. Davis, T. Sit, D. Coyne, C. Opperman and B. Torto, Nat. Sustain., , DOI:10.1038/s41893-022-00852-5.

159	H. Dedehouanou, Adv. Soc. Sci. Res. J., 2022, 9, 39–59.

160	H. Dedehouanou and A. Affokpon, Adv. Soc. Sci. Res. J., 2022, 9, 355–368.

161	G. Colla, S. Nardi, M. Cardarelli, A. Ertani, L. Lucini, R. Canaguier and Y. Rouphael, Sci. Hortic. (Amsterdam)., 2015, 196, 28–38.

162	S. Celletti, S. Astolfi, N. Guglielmo, G. Colla, S. Cesco and T. Mimmo, Agron. , 2020, 10.

163	A. Osman, A.-R. M. Merwad, A. H. Mohamed and M. Sitohy, Mol. , 2021, 26.

164	M. Amirkhani, A. N. Netravali, W. Huang and A. G. Taylor, HortScience, 2016, 51, 1121–1126.

165	WIPO (PCT) ES2837430T3, 2015.

166	H. T. Wilson, K. Xu and A. G. Taylor, Sci. World J., 2015, 2015, 391234.

167	K. Lawinska, M. Lasoń-Rydel, D. Gendaszewska, E. Grzesiak, K. Sieczyńska, C. Gaidau, D.-G. Epure and A. Obraniak, Fibres Text. East. Eur., 2019, 27, 59–64.

168	A. Colantoni, L. Recchia, G. Bernabei, M. Cardarelli, Y. Rouphael and G. Colla, Agric. , 2017, 7.

169	P. de Castro e Silva, L. A. S. Pereira, A. M. T. Lago, M. Valquíria, É. M. de Rezende, G. R. Carvalho, J. E. Oliveira and J. M. Marconcini, Food Biophys., 2019, 14, 456–466.

170	M. Ben-Jabeur, Z. Chamekh, S. Jallouli, S. Ayadi, M. D. Serret, J. L. Araus, Y. Trifa and W. Hamada, Ann. Appl. Biol., , DOI:https://doi.org/10.1111/aab.12754.

171	T. D. Alcock, D. E. Salt, P. Wilson and S. J. Ramsden, Sci. Total Environ., 2022, 829, 154539.

172	A. Kumar, J. Vachan Tirkey and S. Kumar Shukla, Renew. Energy, 2021, 169, 266–282.

173	E. De Falco, M. Pergola, A. Vece, C. Angiuoni and G. Celano, Ital. J. Agron., 2020, 15, 48–56.

174	EPA(USA), Substance Registry Services (SRS), https://sor.epa.gov/sor_internet/registry/substreg/LandingPage.do, (accessed 31 May 2022).

175	K. R. Caffrey and M. W. Veal, Sci. World J., 2013, 2013, 472431.

176	J. H. Kløverpris, C. N. Scheel, J. Schmidt, B. Grant, W. Smith and M. J. Bentham, Int. J. Life Cycle Assess., 2020, 25, 1991–2007.

177	BASF, https://www.basf.com/global/en/media/news-releases/2020/11/p-20-365.html, (accessed 23 May 2022).

178	Syngenta global, https://www.syngenta.com/en/sustainability/sustainable-development-goals, (accessed 23 May 2022).

179	Corteva Agriscience Sustainability Report 2020, 2020.

180	SilviBio, https://www.silvibio.com/, (accessed 3 June 2022).

181	Agrynex, https://agrynex.us/, (accessed 3 June 2022).

182	Ad Terram, https://ad-terram.nl/#, (accessed 3 June 2022).

183	Indigo Ag, https://www.indigoag.com/, (accessed 3 June 2022).

184	Green and Seed Corporation, http://www.seedfilm.co.kr/en/bbs/content.php?co_id=about, (accessed 3 June 2022).

185	Summit Seed Coatings, https://summitseedcoatings.com/products/plus-seed-treatment/, (accessed 3 June 2022).

186	L. Zimmermann, A. Dombrowski, C. Völker and M. Wagner, Environ. Int., 2020, 145, 106066.

187	E. Kabir, R. Kaur, J. Lee, K.-H. Kim and E. E. Kwon, J. Clean. Prod., 2020, 258, 120536.

188	A. D. La Rosa, in Biopolymers and Biotech Admixtures for Eco-Efficient Construction Materials, eds. F. Pacheco-Torgal, V. Ivanov, N. Karak and H. B. T.-B. and B. A. for E.-E. C. M. Jonkers, Woodhead Publishing, 2016, pp. 57–78.