Table 1: Exemplary content of the spectral reflectance material measurement data file for the material sample called "fabric\_cotton\_white\_1". The text file contains two columns: Incidence angle and the reflectance .

|  |  |
| --- | --- |
| Incidence angle (°) | Reflectance (%) |
| 80 | 16.99149 |
| 70 | 26.67892 |
| 60 | 38.928 |
| 50 | 51.29004 |
| 40 | 61.92666 |
| 30 | 72.27506 |
| 20 | 80.02045 |
| 10 | 84.91023 |
| 0 | 87.49143 |