## Slide 1: InAs Sn SAG
AGCBE100_2 (15 nm Sn)
Measured in Side Fridge on 08/14/22

## Slide 2: BL2.4
At Vg = 0 V :
Pinch off traces at Vbias = 10 mV

## Slide 3: BL2.4
IcRn from ~ 250 to 300 uV

## Slide 4: BL2.4 (for calculating IcRn)

## Slide 5: BL2.4
In plane parallel to NW critical magnetic field, obtained be vector sum of Bx and Bz
Vg = 0 V
Vg = 1 V
Vg = -0.32 mV
Theta = 145 deg, B = 1, Bx = B cos(theta), By = B sin(theta)
Bc = 0.595/cos(145) = 0.726 T
Bc = 0.7127/cos(145) = 1.1 T
Bc = 0.647/cos(145) = 0.79 T

## Slide 6: BL2.4
Vg = -0.385 V
Vg = -0.41 V
Vg = -0.31 V
Vg = 0 V

## Slide 7: BL2.4
Vg = 0.71 V
Vg = 1 V
Vg = 0.48 V
Vg = 0.15 V
Vg = 0.075 V

## Slide 8: BL2.4
4 terminal, plotted against Vmeasure
Colorbar should be 10^-7 A (I used 10 MA/V)
Vg = -0.61 V
4Δ
Δ ~ 500 uV
Mirage states

## Slide 9: BL2.4
Scanned next day with larger Imeasure gain
Vg = -0.685 V
Vg = -0.710 V
Notes: 4 terminal

## Slide 10: BL2.4, QPC
4 terminal, plotted against Vmeasure

## Slide 11: BL2.4, QPC, Lockin
B = 0 T
B = 4 T, parallel to NW
Vbias is not corrected for series resistance
Lots of states within the diamonds

## Slide 12: BL2.5
At Vg = 0 V :
Pinch off traces at Vbias = 10 mV

## Slide 13: BL2.5
Have observed this peak in previous SAG devices also

## Slide 14: BL2.5 (for IcRn)

## Slide 15: BL2.5
In plane parallel to NW critical magnetic field, obtained be vector sum of Bx and Bz
Vg = 0 V
Vg = -0.2 V
Vg = 0.5 V
Bc = 1.212/cos(145) = 1.48 T
Bc = 1.073/cos(145) = 1.31 T
Bc = 1.114/cos(145) = 1.36 T
Take more data at higher fields

## Slide 16: BL2.5
V across the device (4 point msmt)
Δ ~ 525 uV

## Slide 17: BL2.5
B = 0 T
B = 0.1 T
B = 0.2 T
B = 0.3 T
B = 0.4 T
B = 0.5 T
B = 0.6 T
B = 0.7 T

## Slide 18: BL2.5
B = 0.8 T
B = 0.9 T
B = 1 T
B = 1.1 T
B = 1.2 T
B = 1.3 T

## Slide 19: BL2.5
Vg = 0.3 V
Vg = 0.5 V
Vg = -0.305 V
For total B field along the nanowire, divide y axis by sin(145)

## Slide 20: BL2.5
Vg = 77.5*5 mV (green line)
Corresponds to the gate tunable feature in the Vg vs B plot

## Slide 21: BL2.2
At Vg = 0 V :
Pinch off traces at Vbias = 10 mV

## Slide 22: BL2.2
Large peak in the center
Vg = 0.25 V

## Slide 23: BL4.7 (NS)
Vbias = 10 mV,
Sweeping both gates simultaneously
G1
G2

## Slide 24: BL4.7
G1 = 0 V
G1 = 0.5 V
G1 = 1.5 V
G1 = 3 V
Zoom in

## Slide 25: BL4.8
Vbias = 10 mV, sweep both gates simultaneously
G1
G2

## Slide 26: BL4.8
G1 = 1 V
G1 = 0 V
G1 = 3 V
The first 6 diamonds from the left seem to be roughly of the same vertical height but there is no horizontal lines visible indicating gap

## Slide 27: Fig 1 (BL2.4)
Vg = -0.25 V
IcRn plot at different gate voltages goes here
Btot= Bx/cos(145)
Bc = 1.05 T
530-580 uV

## Slide 28: BL2.4
Vg = -136.4*5 mV
Vg = -134.2*5 mV

## Slide 29: Fig 1 (BL2.5)
IcRn plot at different gate voltages goes here
Btot= Bx/cos(145)
Bc = 1.6 T
500-540 uV

## Slide 30: BL2.5
Vg = -143.25*5 mV
Vg = -136*5 mV
Vg = -130*5 mV
Vbias vs Gate trace got shifted compared to previous plot

## Slide 31: BL2.4 Vbias vs Vg
Lockin, amp = 1 V, Vsource = 1 mV/V, Imeasure gain = 10 MA/V, Vmeas gain 1kV/V
Here the mirage states are not so prominent
Lockin, amp = 0.5 V, Vsource = 10 mV/V, Imeasure gain = 10 MA/V, Vmeas gain 100V/V

## Slide 32: BL2.4 Ibias vs B high res
Vg = -0.25 V
B field scan direction
B field scan direction
B field scan direction
The node has more of a “dip” on the left side
Ic on the left side is less than Ic on the right side
The “dip” does not decrease on changing the B field scan direction, Ic also doesn’t increase

## Slide 33: For IcRn
BL2.4
BL2.5