## Slide 1: AGCBE100_2_Cooldown2
Side Fridge
09/23/2022

## Slide 2: BR2.4
Vg = 0 V :
Pinch off traces at Vbias = 10 mV:

## Slide 3: BR2.4
Vg = -42 *5 mV
Vg = -56 *5 mV
Vg = 0 V
Vg = 0.5 V
Vg = 1 V
For total parallel field, divide x axis by cos(150 deg)
Skew
Different shapes
Bc ~ 0.86 T(left side) to 0.9 T (right side)

## Slide 4: BR2.4, in plane perpendicular magnetic field
Vg = -56 *5 mV
Vg = 0 V
Vg = 1 V
skew
2 transitions?

## Slide 5: BR2.4
4Δ
4Δ/3
2Δ

## Slide 6: BR2.4
Vg = -157*5 mV
Vg = -160*5 mV
Bc = 1.2 T

## Slide 7: BL2.3
Vg = 0 V :
Pinch off traces at Vbias = 10 mV:
Pin 17 which is bonded to the gate is broken so no gate control
Bc ~ 1.01, 1.02 T

## Slide 8: TL2.7
dac5 = 0
da10 = 0
dac10 = -159 mV

## Slide 9: TL2.7
Without lowpass
With lowpass
2e ?
1 e?

## Slide 10: TL2.7
Quantum dot states
B=0 T, dac10 =-159 mv

## Slide 11: TL2.7
B = 0 T, dac10 =-159 mV
B = 2 T, dac10 =-159 mV
?

## Slide 12: TL2.7
B = 0 T
0.7 mV approx.
Spacing here is closer to 1 mV
B = 1.8 T
B = 2 T, ~ 1 mV separation b/w dips
Dac10 = -159 mV

## Slide 13: TL4.1
dac5 = 0
dac10 = 0
Notes: Dac5 from 0.5 V to 224*5 mV, dac10 from 23*5 to 17*5 mV

## Slide 14: TL4.1

## Slide 15: TL4.1
Set dac10 = 108.5 mV
B = 0 T
B = 0.4 T
B = 0.8 T
B = 1.2 T
B = 1.6 T
B = 2 T
Ignore last few gate values for 1.6 T and 2 T on the left, magnet quench LED was on
B = 3 T
spacing at zero bias at 3 T is 3-4 mV.
spacing is 8-10 mV.
Notes: At dac5 = 756 mV, I saw that magnetX (in AMI box) was showing quench but the scan was still running. Not sure when the quench started. When I saw the magnet supply box, it was ramping down and at ~ -0.8 T. Was supposed to be at ~ 1.385 T. ramp rate is 0.002 T/s. Which means that it had been ramping down for ~ 5 mins. The scan took close to 3 hours. Which means that the last few gate points are unreliable.

## Slide 16: TL4.1