## Slide 1: Nanowood: Fully renewable, biodegradable, environmentally friendly, natural material for the next generation thermoelectrics
Ievgen Nedrygailov, Kamil Rahme, Scott Monaghan, Subhajit Biswas, Paul Hurley and Justin D. Holmes
School of Chemistry & Tyndall National Institute, University College Cork, Cork, Ireland
AMBER Centre, Environmental Research Institute, University College Cork, Ireland

## Slide 2: Introduction:
The production and consumption of energy plays a key role in our society
Heat recovery
Waste heat is one of the largest sources of clean and inexpensive energy available

## Slide 3: Introduction:
Thermoelectric energy conversion in solid-state devices
Hot side
Cold side
p-type
n-type
Highly doped Bi2Te3, PbTe
Low efficiency (1-8 %)
Small Seebeck coef. (100
Highly toxic
Expensive

## Slide 4: Introduction:
Bismuth
The energy transition will require the production of increased volumes of critical raw materials, which we do not have.

## Slide 5: Introduction:
Thermoelectric energy conversion in ionic liquid electrolytes
1. Bulk electrolyte (),
- Debye length

## Slide 6: Introduction:
Thermoelectric energy conversion in ionic liquid electrolytes
2. Bulk electrolyte (),
T1
T2
Soret effect - formation of a stationary non-uniform distribution of ions () when a temperature gradient (𝜟𝑻) is applied
Soret coefficient
VTE

## Slide 7: Introduction:
Thermoelectric energy conversion in ionic liquid electrolytes
3. Nanoconfined electrolyte (),
VTE
T1
T2
Predicted by theory :
Ionic thermoelectric effect can be enhanced when liquid is confined in a nanochannel
Y. Jin et al. J. Phys. Chem. Lett. 2021, 12, 1144

## Slide 8: Experiment:
SEM of Natural wood:
Step 2. Functionalization
Step 1. Delignification
NaOH, H2O2
T = 100 oC
TEMPO oxidation
T = 20 oC

## Slide 9: Experiment:
Experimental setup:
Wood-based TEG cell:
Peltier module 1
Peltier module 2

## Slide 10: Experiment:
Nanowood membrane:
NaCl electrolyte only:
Thermoelectric voltage
Thermoelectric current

## Slide 11: Experiment:
Nano
Bulk
 | Seebeck coefficient (mV/K)
Bulk electrolyte | 0.4
Nanoconfined electrolyte | 2.8
Seebeck coefficient (Bi2Te3):
0.17 mV/K

## Slide 12: Summary:
Wood is a natural, biodegradable and completely renewable material.
Delignified wood (nanowood) is a new material for thermoelectric waste heat recovery.
Electrolytes confined in the space of a nanochannel demonstrate an increased ionic thermoelectric effect.

## Slide 13
Thank you!
Projects:
https://translate-energy.eu/ https://biorbic.com/nxtgenwood/