## Slide 1: Atmospheric Pressure Plasma Treatment of Sized Glass Fibres for Wetting Control
Daan J.H. Cederløf, Yuki Kusano and Søren Fæster DTU Wind

## Slide 2: Contents
Background and motivation
Atmospheric pressure plasmas
  Dielectric barrier discharge (DBD)
  Plasma processing
Analysis of treated fibres
  X-ray photoelectron spectroscopy (XPS) (Elemental analysis)
  Dynamic micro-wetting test (Wetting characteristics)
  (Field emission type scanning electron microscope (FE-SEM) (Surface morphology))
Summary and Outlook
  New ‘Large DBD’ operational
  Future tests

## Slide 3: Background: DACOMAT
Damage Controlled Composite Materials
Objective: ‘To develop fibre reinforced plastic materials with high capacity to sustain damage and fractures, making them suitable for structures requiring high levels of durability.’
Photo: LM Wind Power
Photo: FiReCo

## Slide 4: Multiple delamination cracks
Mixed mode DCB specimen showing multiple cracks. Source: Rask & Sørensen 2012
Fracture resistance curves for mixed mode DCB specimen showing multiple cracks. Source: Rask & Sørensen 2012
Fracture Resistance

## Slide 5: Controlling the formation of multiple cracks
Multiple crack formation in composite structure.
x2
x1
ˆ
ˆ

## Slide 6: Controlling the formation of multiple cracks
Multiple crack formation in composite structure.
Cohesive law requirement for multiple crack formation:
Peak strength in x2 direction must be lower in secondary crack plane.
x2
x1
x2
x1
ˆ
ˆ
ˆ
ˆ
ˆ
Notes: Include reference to peak strength

## Slide 7: Controlling the formation of multiple cracks
Teflon/PTFE tape
  Physical barrier
  Prevents fibre bridging
  Zero interlaminar strength
Perforated PTFE tape
Plasma treatment in He/CF4
  Introduction of fluorine
  Controlled ‘mild’ PTFE like behaviour

## Slide 8: Atmospheric pressure plasmas
Characteristics of low temperature plasma
High treatment effect
Bulk property unchanged
Easily generated at low pressures, but also possible at atmospheric pressure
Surface modification with He/CF4 plasma
Surface cleaning and weak domain elimination
Mechanical interlocking due to roughening
Substitution of fluorine onto fibre sizing surface
  Decreased wetting
Localized treatment possible

## Slide 9: Atmospheric pressure plasma setup
Fig: Dielectric Barrier Discharge (DBD) setup
Specimen | Commercial sized glass fibre bundles from UD fabric Approx. 60mm length
Plasma source | Dielectric Barrier Discharge (DBD)
Power [W] | 50 & 100
Gas input [SLM] | He: 3 CF4: 0.22
Frequency [kHz] | Ca. 45
Time/exposure | 60 s
Standard liter per minute (SLM)
Fig: Prepared specimen
Electrode
Electrode
Dielectric Barrier
Specimen
Plasma
Gas input
Notes: Update drawing

## Slide 10: DBD Video

## Slide 11: Analysis of treated sized glass fibre surfaces
X-ray Photoelectron Spectroscopy, (XPS).
Dynamic micro-wetting test.
Field Emission Scanning Electron Microscopy, (FESEM) (extra slides)

## Slide 12: XPS Results – DBD He/CF4– Elemental Analysis
Fluorine is introduced on fibres from the bundle interior and exterior
Increased plasma power introduces more fluorine
Silicone contaminants are removed
Bundle cross-section
Interior
Fibres
Exterior
Fibres
Untreated interior
Untreated exterior
DBD 50W interior
DBD 50W exterior
DBD 100W interior
DBD 100W exterior

## Slide 13: Dynamic micro-wetting
Each specimen consists of multiple bundles
Glycerol is used as a substitute for vinyl ester
A ca.1μL droplet is placed on a fibre bundle
The following treatments are analysed:
Untreated
DBD CF4 (1min, 50W)
DBD CF4 (1min, 100W)
CCD camera
Specimen
Glycerol droplet
Fabric
Syringe

## Slide 14: Dynamic micro-wetting
Dynamic micro-wetting of sample treated with DBD in He/CF4 (100W). (20sec, realtime)
Needle
Vid: Dynamic micro-wetting of untreated sample. (20sec, realtime)

## Slide 15: Dynamic micro-wetting
Fig: Example of dynamic micro-wetting data analysis
d
h
q
q
assuming

## Slide 16: Dynamic micro-wetting results
More negative wetting rate () = faster wetting
Clear influence of DBD CF4 treatment
XPS results are consistent with contact angle wetting rate
2 separate treatments and measurements of 50W/60s shows that the method is repeatable
Fig: Summary of wetting rates after plasma treatments
Wetting rate
Notes: GRAPH TO BE CHANGED

## Slide 17: Summary and Outlook
Interlaminar tensile strength (ILTS) by curved beam test (ASTM D6415) @ DTU.
New ‘Large DBD’ device calibration @ DTU.
Time of flight secondary ion mass spectrometry (TOF-SIMS) @ SINTEF, Norway.
Single fibre contact angle measurement @ UNIS, Scotland.
Interfacial Shear Strength (IFSS) by microbond test @ UNIS, Scotland.
Future studies (with DACOMAT partners)
To facilitate multiple delaminations, a weaker interlaminar interface is required.
Fluorine can successfully be introduced on fibre sizing surface by plasma treatment.
A decrease in wetting rate is observed after plasma treatment.
Summary:
Notes: Include dcb test as final validation

## Slide 19: New ‘large DBD’
Treatment of ~250x400mm fabrics
Localised treatment possible
Possibility of applying ultrasound for enhanced plasma effect
Movable stage/electrode (with fabric sample mounted)
Water cooled electrode
Gas inlets

## Slide 20: VIDEO: First test of new DBD device
Movable stage/electrode (with fabric sample mounted)
Gas inlets
Water cooled electrode
(Video in separate file)

## Slide 21
VIDEO: First test of new DBD device

## Slide 22: FE-SEM Results 3000x Magnification (low magnification)
Untreated
DBD CF4 50W
Unevenness represents local shape and structure of the sizing

## Slide 23: FE-SEM Results 18-25Kx Magnification
Untreated
DBD CF4 50W