Supplementary information for

Deposition and Corrosion Performance of Phosphate-Polylactic Acid Composite Coatings on WE43 Magnesium Alloy

Andrei V. Paspelau, Aliaksandr A. Kasach, Jacek Gurgul, Grzegorz Mordarski, Konrad Skowron, Irina I. Kurilo, and Dzmitry S. Kharytonau

XRD measurements

JCPDS cards used for XRD data analysis

JCPDS card #00-035-0821 – Mg

JCPDS card #00-044-1482 – Mg(OH)2

JCPDS card #00-011-0293 – CaHPO4∙2H2O

JCPDS card #00-003-0398 – CaHPO4

JCPDS card #00-045-1031 – Mg41Nd5

Adhesion measurements

The adhesion of the obtained coatings to the WE43 alloy substrate was evaluated using a PosiTest AT-A adhesive meter. The separation surface diameter was 20 mm. The results are listed in Table S1 and Fig. S1.

Table S1 – Results of adhesion tests

| Sample | Breakout force [MPa] |  |
| --- | --- | --- |
|  | Before corrosion | After 14 days of corrosion tests |
| PLA | 2.03±0.12 | – |
| CaP-PLA | 1.50±0.25 | 0.57±0.13 |

Fig. S1. – SEM images of PLA (a) and CaP-PLA (b) samples after adhesion tests