README:

General scheme for synthesizing prepolymers and cross-linked polymers

Scheme 1. Shows the general scheme for synthesizing prepolymers and cross-linked polymers. Guruprasad has done polymer synthesis and characterization. The scheme is drawn by Guruprasad.

Substrate synthesis and properties

Fig 1. Shows the substrates synthesis and properties. (a) schematic Illustration of polymeric substrates S1–S3 synthesized on a glass mold. (b) photographs of flexible substrate demonstrating transparency underneath the University of Turku logo, relaxed, stretched, bending, twisting, and conformal attachment to Human ski shows the demonstration of the capacitive pressure sensor as an electronic skin. The substrate synthesis was carried out by Guruprasad.

Characterization of polymer substrates

Fig. 2. shows the characterization data of S1–S3. (a) FT–IR data. (b) Transmittance data. (c) Stress vs strain data. (d) Tensile strength and breaking strain. (e) Stress vs strain data of S2 substrate at 20, 40, and 60% of strain for 5 cycles. (f) Static contact angles of water droplets on substrates S1–S3. The FTIR and contact angle measurements is conducted by Timo. Mechanical properties data are conducted by Amit Barua and Guruprasad.

Pictorial representation of TCE fabrication process and flexible devices fabrication

Fig.3. shows that Pictorial representation for the fabrication process of TCE and layout of a strain sensor, capacitive pressure sensor, and curvature sensor. The picture is drawn by Akseli Vainio.

Characterization of Transparent Conducting Electrode (TCE)

Fig 4. shows the characterization details of Transparent conducting electrode (TCE). (a) SEM micrographs of electrospun PVA fabric network on S2 (inset showing high-resolution SEM micrographs of PVA fiber network on the substrate). (b) SEM image of AgNWs across the TCE (inset showing high-resolution SEM image of nano welded AgNWs on S2). (c) backscattered electrons for AgNWs network across TCE and corresponding EDS for silver, carbon, and oxygen elements in TCE. (d) Transmittance data of TCE fabricated with different concentrations of AgNWs (100, 150, 200, 250, 300 µg/mL) (inset: TCE loaded with 250 µg/mL AgNWs shows transparency with underneath of University of Turku logo along with blowing LED. (e) sheet resistance data of TCE fabricated with different concentrations of AgNWs (100, 150, 200, 250, 300 µg/mL). (f) resistance vs temperature profile of TCE. SEM analysis is conducted by Bahar. Sheet resistance data and transmittance studies data are taken by Amit and Guruprasad.

Video S1. Shows that visible decrease in brightness of LED when the TCE was stretched to 30 % and vice versa. The data is collected by Amit and Guruprasad.

Strain sensor characterization

Fig. 5. shows the strain sensor characterization data. (a) Strain sensor shows change in the R–R0/R0 with increase of strain from 5–45 % (i = 5 %, ii = 10 %, iii = 15 %, iv = 20 %, v = 25 %, vi = 30 %, vii = 35 %, viii = 40 %, ix = 45 %). (b) Stability of the strain sensor shows when stretched dynamically for 200 cycles under applied strain of 10 %. (c) Magnified image from (b) showing the change in resistance with the corresponding strain cycles. The experiments are conducted by Amit Barua and Guruprasad.

Curvature sensor and pressure sensor characterization

Fig. 6. shows the capacitive and curvature sensor characterization. (a) Displays the variation of ΔC/C0 with the applied pressure on the sensor ranging from 0.5–300 kPa (where i = 0.5 kPa, ii = 0.8 kPa, iii = 1 kPa, iv = 3 kPa, v = 5 kPa, vi = 10 kPa, vii = 20 kPa, viii = 30 kPa, ix = 50 kPa, x = 75 kPa, xi = 100 kPa, xii = 150 kPa, xiii = 200 kPa, xiv = 300 kPa), (b) shows relative capacitance plotted as a function of pressure. Inset showing the close–up of pressures below 10 kPa. (c) Shows the stability of the capacitive sensor when dynamically loaded for 2600 cycles with a pressure of 20 kPa. The stability in capacitance change is depicted in the magnified image. (d) Shows the calculated sensitivity derived from the data in (a &b), (e) Curvature sensor showing the relative change in capacitance (ΔC/C0) with applied curvature 0–600 m− 1. The experiments are conducted by Amit Barua and Guruprasad.

Demonstration of capacitive pressure sensor

Fig. 7. shows that the demonstration of capacitive sensor for gesture monitoring. (a) Smart glove shows the stable and distinguishable ΔC/C0 change for different finger gesture movements. (b) The capacitive sensor mounted on the hand wrist shows repeatable ΔC/C0 changing patterns for wrist movement. (c) Capacitive sensor shows ΔC/C0 change for different vocal cord vibrations speaking, swallowing, etc. The experiments are conducted by Amit Barua and Guruprasad.

Flexible heater fabrication and testing

Fig. 8. shows that the flexible heater characteristics and demonstration. (a) The heater shows a steady–state increase in heat with the stepwise increase of applied voltage from 0.5 V to 6 V. The corresponding IR images at different applied voltages show the uniform distribution of heat across the heater. (b) Time–dependent temperature profile of the heater at different applied voltages (0.5 V to 3.5 V) by turning the heater voltage on for 60 s. (c) The temperature response over heating cycles at different voltages (0.5 V to 3.5 V). (d) Temperature response over applied strains from 0-35 % at an applied bias of 5.5 V. (e–f) Camera and IR images of the TCE–based heater mounted on the windshield of a toy for defrosting in a cold environment under heater voltage–off conditions. (g) The IR image shows the even distribution of temperature across the heater surface mounted on a toy windshield when the heater is voltage–on.  The experiments are conducted by Timo, Amit and Guruprasad.

Degradability studies

Fig.9. shows that the degradability studies of synthesized elastomers. (a) Weight loss percentage of S2 films show degradation over time under pH = 0, pH = 7.4 (phosphate buffer solution (PBS)), and pH = 14 solutions. (b) Images of thin films show degradation under various pH solutions at day 0, days 14, and days 145. The experiments are conducted by Timo and Guruprasad

Characterization of prepolymer

Fig. S1.  shows that the characterization data of poly(glycerol-co-δ-valerolactone) compound 1. (a) FT-IR profile. (b) 1H-NMR spectrum. (c) TGA and DSC profile. The experiments are conducted by Timo and Guruprasad.

Transmittance and reflection studies

Fig. S2. shows that the transmittance data of S2 at different angles 15°, 30°, 45°, and 60°. The data is collected by Guruprasad.

Fig. S3. Shows the Reflection data of S1-S3. The data is collected by Guruprasad.

SEM analysis

Fig. S6. shows that the Comparison of AgNWs distribution density across the TCE surface (a) TCE fabricated with AgNWs concentration of 250 µg/mL, and (b) 300 µg/mL. The data is collected by Bahar.

Scotch tape test

Fig.S8. Stability test of AgNWs on TCE (40 Ω sq−1) using a scotch tape (inset showing the scotch was applied on the TCE and peeled-off after 10 sec). The data is collected by Amit.

Pressure sensor data of the device fabricated with double side tape

Fig.10. Pressure sensor data of the device fabricated with double side tape: (a) sensor shows variation of ΔC/C0 with the applied pressure on the sensor ranging from 0.5‒300 kPa (b) shows relative capacitance plotted as a function of pressure. Inset showing the close‒up of pressures below 15 kPa. The data is collected by Amit.

Stretchable characteristics of the heater

Fig. S12. IR thermal images showing the decrease in heater temperature with the increase of applied strain: (a) Heater at voltage-off state; heating performance of the heater at voltage-on (5.5V) state at (b) 0% strain, (c) 5% strain, (d) 10% strain, (e) 15% strain, (f) 20% strain, (g) 25% strain, (h) 30% strain, (i) 35% strain. The data are collected by Amit and Guruprasad.

Video S2. Shows that decrease in heater temperature with the increase of applied strain (0-35% strain) and vice versa. The data is collected by Amit and Guruprasad.

Stability test of the flexible heater

Fig.S13.  Flexible heater characteristics and demonstration of the two-month-old flexible heater: (a) The heater shows a steady‒state increase in heat with the stepwise increase of applied voltage from 1V to 7V. (b) Time‒dependent temperature profile of the heater at different applied voltages (2V, 3V, and 4V) by turning the heater voltage on for 60s. (d) The temperature response over heating cycles at different voltages (2V, 3V, and 4V). The data is collected by Guruprasad.

possible degradation mechanism for polymeric substrate in the acidic and basic media

Scheme S1. Possible mechanism for the hydrolytic cleavage of ester bonds in S2 catalyzed by H⁺ and OH⁻ under pH = 0 and pH = 14 aqueous solutions, respectively.  The scheme is drawn by Guruprasad.

_____________