Part A. Life cycle inventories of lab-scale PeLEDs

Contents

  - Blue LED technologies

    - EA-doped PeLED ………………...…………………..………….…...... 2

    - YCl3-doped PeLED ………………………………………………… 10

    - Quasi-2D PeLED ………………………………………..……………. 14

    - Solid-QD PeLED ………………………………………..……………. 18

  - Green LED technologies

    - Defect-suppressed PeLED ……………………….…………………. 22

    - Distribution-controlled PeLED …………….………....……………… 25

    - Phase-engineered PeLED ………………...…………………………... 29

    - Ultra-bright PeLED ………………………...……………………….... 33

  - Red LED technologies

    - Ligand-engineered PeLED ...……………………………….…...……. 36

    - PEA/NMA-doped PeLED …………..…………....……..…………… 39

    - Stabilized-QD PeLED …………………………………………....…. 42

    - Lead-free TEA-Sn PeLED ………………………..………………..…. 47

  - White LED technologies

    - Heterophase-QD PeLED ………………….………………..……...…. 50

    - Lead-free Cu PeLED …….……………….……..…………....……… 55

  - Near-infrared LED technologies

    - Molecular-passivated PeLED ……………….………..………………. 59

    - Submicrometric PeLED ………………………..……....…………..… 62

    - Ultrastable PeLED ………………………..……………..……………. 66

    - Lead-free Sn PeLED …………………….…………..…………..……. 69

A.1 Blue LED

A.1.1 EA-doped blue PeLED

Table A.1.1.1 | Raw material input of EA-doped blue PeLED

| Raw material input | Pure density/ Molar mass | Experimental concentration | Volume | Mass for one batch | Mass for one device | Note |
| --- | --- | --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |  |  |
| Glass | 2.5 g/cm3 | 100% | 2 cm2×1.1 mm |  | 0.55 g | Substrate |
| ITO | 6.8 g/cm3 | 100% | 2 cm2×100 nm |  | 0.000136 g | Anode |
| Deionized water | 1 g/mL | 100% | 4400 mL for 2000 cm2 | 4400 g | 4.4 g | Clean 2000 cm2 glasses |
| Acetone | 0.791 g/mL | ≥99.5% | 4400 mL for 2000 cm2 | 3480 g | 3.480 g |  |
| 2-Propanol | 0.785 g/mL | ≥99.5% | 4400 mL for 2000 cm2 | 3454 g | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |  |  |
| PEDOT:PSS | 1.18 g/mL | 4% in water |  |  | 0.000472 g |  |
| Water | 1 g/mL |  | 10 μL |  | 0.01 g |  |
| 3 Perovskite layer production |  |  |  |  |  |  |
| CsBr | 212.81 g/mol | 0.027 mol/L |  |  | 0.000057 g |  |
| PbBr2 | 367.01 g/mol | 0.1 mol/L |  |  | 0.000367 g |  |
| PEABr (phenylethylammonium bromide) | 202.09 g/mol | 0.067 mol/L |  |  | 0.000135 g |  |
| EABr (ethylammomium bromide) | 126.00 g/mol | 0.04 mol/L |  |  | 0.000050 g |  |
| DMSO (dimethyl sulfoxide) | 1.10 g/mL |  | 10 μL |  | 0.011 g | Solvent |

Table A.1.1.1 (continued) | Raw material input of EA-doped blue PeLED

| Raw material input | Pure density/ Molar mass | Experimental concentration | Volume | Mass for one batch | Mass for one device | Note |
| --- | --- | --- | --- | --- | --- | --- |
| 4 Electron transport layer production |  |  |  |  |  |  |
| TPBi | 1.267 g/cm3 |  | 0.001 cm3 | 0.001267 g | 0.000025 g | Deposition for 100 cm2 |
| 5 Cathode deposition |  |  |  |  |  |  |
| LiF | 2.64 g/cm3 |  | 0.000027 cm3 | 0.000071 g | 0.0000014 g |  |
| Al | 2.7 g/cm3 |  | 0.001728 cm3 | 0.004666 g | 0.0000933 g | 100 cm2 |
| 6 Encapsulation |  |  |  |  |  |  |
| UV-cured epoxy | 1.16 g/cm3 |  | 10 μL |  | 0.0116 g |  |
| 7 Other |  |  |  |  |  |  |
| Nitrogen gas | 1.25 g/L |  | 60 L/week |  | 0.00626 g | 12000 cm2 per week* |

*Calculated in Table A.1.1.3.6.

Table A.1.1.2 | Emission of EA-doped blue PeLED

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 1 Cleaning |  |  | Waste liquid. |
| Deionized water | 4.4 g |  |  |
| Acetone | 3.480 g |  | Can be reused for in industrial process. |
| 2-propanol | 3.454 g |  |  |
| 2 Solvent |  |  | Emission as waste liquid. |
| DMSO | 0.011 g |  |  |
| Water | 0.01 g |  |  |
| 3 Deposition |  |  |  |
| PEDOT:PSS | 0.000464 g | 98% | Spin coating: 0.000472 g – (1.18g/cm3 × 2cm2 × 35nm) |
| CsBr | 0.000056 g | 98% | Spin coating: 0.000057 g × 98% |
| PbBr2 | 0.000360 g | 98% | Spin coating: 0.000367 g × 98% |
| PEABr | 0.000132 g | 98% | Spin coating: 0.000135 g × 98% |
| EABr | 0.000049 g | 98% | Spin coating: 0.000050 g × 98% |
| TPBi | 0.0000146 g | 58% | Evaporation: 0.000025 – (1.3g/cm3 × 2cm2 × 40nm) |
| LiF | 0.00000087 g | 62% | Evaporation: 0.0000014 – (2.64g/cm3 × 2cm2 × 1nm) |
| Al | 0.0000555 g | 59% | Evaporation: 0.0000933 g – (2.7g/cm3 × 2cm2 × 70nm) |
| 4 Disposal materials |  |  |  |
| UV-cured Epoxy | 0.0116 g |  |  |
| ITO + glass | 0.000136 g + 0.55 g |  |  |
| 5 Other |  |  |  |
| Nitrogen gas | 0.00626 g | 100% |  |

Table A.1.1.3 | Electricity input of EA-doped blue PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Description | Elmasonic P60H Ultrasonic Cleaning Unit |
| Ultrasonic bath maximum power | 580 W |
| Maximum applicable volume a | 25.5×11.5×15 cm3 |
| Maximum applicable surface area b | 2000 cm2 |
| Mean utilization power percentage | 70% |
| Mean ultrasonication use factor for a 2 cm2 piece c | 0.07% |
| Mena ultrasonication bath power for a 2 cm2 piece | 0.406 W |
| Sonication time for deionized water | 15 min |
| Sonication time for acetone | 15 min |
| Sonication time for isopropanol | 15 min |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Description | Ossila UV Ozone Cleaner L2002A2 |
| Ozone maximum power | 50 W |
| Maximum applicable surface | 100 cm2 |
| Ozone system mean use factor for a 2 cm2 piece | 2% |
| Mean ozone power for a 2 cm2 piece | 1 W |
| Ozone time | 10 min |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |

a All volumes are considered at 273 K and 1 atm. b Industrial cleaning process uses the larger cleaner and the unit electricity consumption would be much reduced. c Estimated from the mean equipment use factor and the maximum capacity.

Table A.1.1.3 (continued) | Electricity input of EA-doped blue PeLED

| 2 Hole transport layer deposition |  |  |  |
| --- | --- | --- | --- |
| Spin coating a |  |  |
| Description | SPS Europe B.V. SPIN150i & Edwards RV12 Vacuum Pump |  |
| Maximum speed |  | 12,000 rpm |
| Maximum applicable surface a |  | 38 cm2 (6’’-inches) |
| Maximum spin coater power |  | 500 W |
| Spin speed |  | 9,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece |  | 3.95% |
| Mean spin coater power for a 2 cm2 piece a |  | 19.74 W |
| Maximum external vacuum pump power |  | 450 W |
| Mean pump utilization power percentage |  | 60% |
| Mean external pump use factor for a 2 cm2 piece |  | 3.16% |
| Mean external pump power for a 2 cm2 piece a |  | 14.22 W |
| Spin-coating time |  | 60 s |
| Electricity for a 2 cm2 piece |  | 2.038 kJ (0.00057 kWh) |
| Thermal annealing |  |  |
| Description | Thermo Scientific Cimarec Stirring Hot Plates SP88854105 |  |
| Maximum hotplate temperature |  | 540 °C |
| Maximum hotplate power |  | 384 W |
| Maximum applicable surface |  | 100 cm2 |
| Annealing temperature |  | 160 °C |
| Mean hotplate use factor for a 2 cm2 piece |  | 0.59% |
| Mean hotplate power for a 2 cm2 piece |  | 2.27 W |
| Annealing time | 15 min |  |
| Electricity for a 2 cm2 piece |  | 2.043 kJ (0.00057 kWh) |

a Industrial manufacturing normally uses larger area techniques like vapour deposition, slot-die coating, etc.

Table A.1.1.3 (continued) | Electricity input of EA-doped blue PeLED

| 3 Perovskite layer deposition |  |
| --- | --- |
| Spin coating |  |
| Description SPS Europe B.V. SPIN150i, Edwards RV12 Vacuum Pump |  |
| Maximum speed | 12,000 rpm |
| Maximum applicable surface | 38 cm2 (6’’-inches) |
| Maximum spin coater power | 500 W |
| Material | Perovskite |
| Spin speed | 3,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.32% |
| Mean spin coater power for a 2 cm2 piece | 6.58 W |
| Maximum external vacuum pump power | 450 W |
| Mean pump utilization power percentage | 60% |
| Mean external pump use factor for a 2 cm2 piece | 3.16% |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 2 min |
| Electricity for a 2 cm2 piece | 2.496 kJ (0.00069 kWh) |
| Thermal annealing |  |
| Description Thermo Scientific Cimarec Stirring Hot Plates SP88854105 |  |
| Maximum temperature | 540 °C |
| Maximum power | 384 W |
| Maximum applicable surface | 100 cm2 |
| Annealing temperature | 60 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.22% |
| Mean hotplate power for a 2 cm2 piece | 0.85 W |
| Annealing time | 20 min |
| Electricity for a 2 cm2 piece | 1.024 kJ (0.00028 kWh) |

Table A.1.1.3 (continued) | Electricity input of EA-doped blue PeLED

| 4 ETL/cathode deposition |  |  |  |  |
| --- | --- | --- | --- | --- |
| Thermal evaporation |  |  |  |  |
| Description | MBraun PROvap Platform, MB-RCC 1000 Cooler, Edwards RV12 Vacuum Pump |  |  |  |  |
| Maximum evaporator power |  | 800 W |  |  |
| Maximum Cooling system power |  | 1000 W |  |  |
| Maximum vacuum pump power |  | 450 W |  |  |
| Maximum applicable surface |  | 100 cm2 |  |  |
| Area use percentage for a 2 cm2 piece |  | 2% |  |  |
| Mean cooling system utilization power percentage |  | 20% |  |  |
| Mean pump utilization power percentage |  | 60% |  |  |
| Maximum evaporator temperature |  | 1800 °C |  |  |
| Evaporation melting temperature |  | TPBi 280 °C | LiF 850 °C | Al 660 °C |
| Mean evaporator temperature utilization percentage |  | 7.8% | 23.6% | 18.3% |
| Mean evaporator use factor for a 2 cm2 piece |  | 0.16% | 0.47% | 0.37% |
| Mean evaporator power for a 2 cm2 piece |  | 1.28 W | 3.76 W | 2.96 W |
| Cooling system mean power for a 2 cm2 piece |  | 4 W |  |  |
| Mean vacuum pump power for a 2 cm2 piece |  | 5.4 W |  |  |
| Evaporator working time |  | 3 min | 3 min | 3 min |
| Vacuum pump working time a |  | 20 min |  |  |
| Cooling system working time |  | 9 min |  |  |
| Electricity for a 2 cm2 piece |  | 10.08 kJ (0.0028 kWh) |  |  |

a The vacuum pumping working time contains times for both evacuation and deposition.

Table A.1.1.3 (continued) | Electricity input of EA-doped blue PeLED

| 5 Encapsulation |  |  |
| --- | --- | --- |
| UV radiation |  |  |
| Description |  | Thermo Scientific 3UV Lamp |
| Mean radiation power |  | 8 W |
| Maximum applicable surface |  | 20 cm2 |
| Mean system use factor for a 2 cm2 piece |  | 10% |
| Mean radiation power |  | 0.8 W |
| Radiation time |  | 1 min |
| Electricity for a 2 cm2 piece |  | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |  |
| N2 gas glovebox atmosphere |  |  |
| Description | MBraun Standard Glovebox Workstations 0.8 m3 |  |
| Mean glovebox system consumption power |  | 150 W |
| System working time per week a |  | 168 h |
| Mean antechamber pump power b |  | 100 W |
| Total producing time per week (worker in place) |  | 40 h |
| Pump operation time percentage during work |  | 20% |
| Mean pump operation time per week |  | 8 h |
| Maximum applicable surface at unit time |  | 100 cm2 |
| Mean time of producing a 100 cm2 device |  | 20 min |
| Estimated number of 100 cm2 pieces per week |  | 120 |
| Electricity consumption per week |  | 9.36 ×104 kJ |
| Number of producing a 2 cm2 piece per week |  | 6000 |
| Electricity for a 2 cm2 piece |  | 15.6 kJ (0.00433 kWh) |

a Glovebox system would operate the whole day automatically to keep the nitrogen gas atmosphere. b Antechamber would be only used when workers are present.

A.1.2 YCl3-doped blue PeLED

Table A.1.2.1 | Raw material input of YCl3-doped blue PeLED

| Raw material input a |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  |  | 0.55 g |  |
| ITO |  |  | 0.000136 g |  |
| Deionized water |  |  | 4.4 g |  |
| Acetone |  |  | 3.480 g |  |
| 2-Propanol |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  |  | 0.000472 g |  |
| Water |  |  | 0.01 g |  |
| 3 Perovskite layer production | (Density/molar) | (Volume) |  |  |
| CsBr | 212.81 g/mol | 0.25 mol/L |  | 0.000532 g |
| PbBr2 | 367.01 g/mol | 0.25 mol/L |  | 0.000918 g |
| Phenylethylammonium chloride (PEACl) | 157.64 g/mol | 1:1 (0.25M) |  | 0.000394 g |
| YCl3 | 195.26 g/mol | 2% (0.005M) |  | 0.000010 g |
| DMSO | 1.10 g/mL | 10 μL |  | 0.011 g |
| Chloroform | 1.492 g/mL | 10 μL |  | 0.01492 g |
| 4 Electron transport layer production |  |  |  |  |
| TPBi |  |  | 0.000025 g |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |
| Al b |  |  | 0.0001203 g |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |

a The calculation details are similar to those in Table A.1.1.1 and therefore presented briefly. This approach also applies to the subsequent tables.

b Al electrode has a typical thickness (100 nm) here.

Table A.1.2.2 | Emission of YCl3-doped blue PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| DMSO | 0.011 g |
| Chloroform | 0.01492 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.0004626 g | 98% | Spin.: 0.000472 g – (1.18g/cm3 × 2cm2 × 40nm) |
| CsBr | 0.0005214 g | 98% | Spin.: 0.000532 g × 98% |
| PbBr2 | 0.0008996 g | 98% | Spin.: 0.000918 g × 98% |
| PEACl | 0.0003861 g | 98% | Spin.: 0.000394 g × 98% |
| YCl3 | 0.0000098 g | 98% | Spin.: 0.000010 g × 98% |
| TPBi | 0.0000146 g | 58% | Evapor.: 0.000025 g – (1.3g/cm3×2cm2×40nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g– (2.7g/cm3×2cm2×100nm) |

Table A.1.2.3 | Electricity input of YCl3-doped blue PeLED*

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 3,500 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.54% |
| Mean spin coater power for a 2 cm2 piece | 7.68 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 40 s |
| Electricity for a 2 cm2 piece | 0.876 kJ (0.00024 kWh) |
| Thermal annealing |  |
| Annealing temperature | 125 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.46% |
| Mean hotplate power for a 2 cm2 piece | 1.78 W |
| Annealing time | 30 min |
| Electricity for a 2 cm2 piece | 3.2 kJ (0.00089 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 4,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.75% |
| Mean spin coater power for a 2 cm2 piece | 8.75 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 40 s |
| Electricity for a 2 cm2 piece | 0.9188 kJ (0.00026 kWh) |
| Thermal annealing |  |
| Annealing temperature | 90 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.33% |
| Mean hotplate power for a 2 cm2 piece | 1.27 W |
| Annealing time | 20 min |
| Electricity for a 2 cm2 piece | 1.524 kJ (0.00042 kWh) |

* The same details as Table A.1.1.3 are omitted here. This applies to the subsequent tables.

Table A.1.2.3 | Electricity input of YCl3-doped blue PeLED

| 4 ETL/cathode deposition |  |
| --- | --- |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.1.3 Quasi-2D blue PeLED

Table A.1.3.1 | Raw material input of quasi-2D blue PeLED

| Raw material input |  |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |  |
| Glass |  |  |  | 0.55 g |  |
| ITO |  |  |  | 0.000136 g |  |
| Deionized water |  |  |  | 4.4 g |  |
| Acetone |  |  |  | 3.480 g |  |
| 2-Propanol |  |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |  |
| PEDOT:PSS |  |  |  | 0.000472 g |  |
| Water |  |  |  | 0.01 g |  |
| 3 Perovskite layer production | (Density/molar) | (Volume) |  |  |  |
| CsBr | 212.81 g/mol | 0.156 mol/L |  |  | 0.000332 g |
| PbBr2 | 367.01 g/mol | 0.05 mol/L |  |  | 0.000184 g |
| PbCl2 | 278.10 g/mol | 0.06 mol/L |  |  | 0.000167 g |
| pF-PEABr (4-Fluorophenylethylammonium bromide) | 220.08 g/mol | 0.045 mol/L |  |  | 0.000099 g |
| KBr | 119.00 g/mol | 0.028 mol/L |  |  | 0.000033 g |
| DMSO | 1.10 g/mL | 10 μL |  |  | 0.011 g |
| PHDI (poly(hexamethylene diisocyanate)) |  | 0.5 mg/mL |  |  | 0.000005 g |
| 4 Electron transport layer production |  |  |  |  |  |
| TPBi |  |  | 0.000025 g |  |  |
| 5 Cathode deposition |  |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |  |
| Al |  |  | 0.0001203 g |  |  |
| 6 Encapsulation |  |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |  |
| 7 Other |  |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |  |

Table A.1.3.2 | Emission of quasi-2D blue PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| DMSO | 0.011 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.0004626 g | 98% | Spin.: 0.000472 g – (1.18g/cm3×2cm2×35nm) |
| CsBr | 0.000325 g | 98% | Spin.: 0.000332 g×98% |
| PbBr2 | 0.000180 g | 98% | Spin.: 0.000184 g×98% |
| PbCl2 | 0.000164 g | 98% | Spin.: 0.000167 g×98% |
| pF-PEABr | 0.000097 g | 98% | Spin.: 0.000099 g×98% |
| KBr | 0.000032 g | 98% | Spin.: 0.000033 g×98% |
| PHDI | 0.000005 g | 98% | Spin.: 0.000005 g×98% |
| TPBi | 0.0000146 g | 58% | Evapor.: 0.000025 g – (1.3g/cm3×2cm2×42nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g–(2.7g/cm3×2cm2×100nm) |

Table A.1.3.3 | Electricity input of quasi-2D blue PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 4,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.75% |
| Mean spin coater power for a 2 cm2 piece | 8.77 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 45s |
| Electricity for a 2 cm2 piece | 1.035 kJ (0.00029 kWh) |
| Thermal annealing |  |
| Annealing temperature | 140 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.52% |
| Mean hotplate power for a 2 cm2 piece | 2 W |
| Annealing time | 15 min |
| Electricity for a 2 cm2 piece | 1.8 kJ (0.0005 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 3,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.32% |
| Mean spin coater power for a 2 cm2 piece | 6.58 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.248 kJ (0.00035 kWh) |
| Thermal annealing |  |
| Annealing temperature | 70 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.26% |
| Mean hotplate power for a 2 cm2 piece | 1 W |
| Annealing time | 7 min |
| Electricity for a 2 cm2 piece | 0.42 kJ (0.00012 kWh) |

Table A.1.3.3 (continued) | Electricity input of quasi-2D blue PeLED

| 4 ETL/cathode deposition |  |
| --- | --- |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.1.4 Solid-QD blue PeLED

Table A.1.4.1 | Raw material input of solid-QD blue PeLED

| Raw material input |  |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |  |
| Glass |  |  |  | 0.55 g |  |
| ITO |  |  |  | 0.000136 g |  |
| Deionized water |  |  |  | 4.4 g |  |
| Acetone |  |  |  | 3.480 g |  |
| 2-Propanol |  |  |  | 3.454 g |  |
| 2 Hole transport layer production | (Density/molar) | (Volume) |  |  |  |
| Ni(CH3COO)2∙4H2O | 248.84 g/mol | 0.1 M × 10 μL |  |  | 0.000249 g |
| NH2CH2CH2OH | 61.08 g/mol | 0.1 M × 10 μL |  |  | 0.000061 g |
| Ethanol | 0.789 g/mL | 10 μL |  |  | 0.00789 g |
| PVK (Poly(9-vinycarbazole)) | 4 mg/mL | 10 μL |  |  | 0.00004 g |
| Chlorobenzene | 1.11 g/mL | 10 μL |  |  | 0.0111 g |
| 3 Perovskite layer production | (Density/molar) | (Volume) |  |  |  |
| CsBr | 212.81 g/mol | 0.13 mol/L |  |  | 0.000277 g |
| PbBr2 | 367.01 g/mol | 0.2 mol/L |  |  | 0.000073 g |
| Br-MBA (α-methyl-4-bromide-benzylammonium) | ~200 g/mol | 0.2 mol/L |  |  | 0.00004 g |
| DMSO | 1.10 g/mL | 10 μL |  |  | 0.011 g |
| Chlorobenzene | 1.11 g/mL | 10 μL |  |  | 0.0111 g |
| TFPPO (tris(4-fluorophenyl)phosphine oxide) | 0.3 mg/mL | 10 μL |  |  | 0.000003 g |
| Methyl acetate | 0.932 g/mL | 10 μL |  |  | 0.00932 g |
| 4 Electron transport layer production |  |  |  |  |  |
| TPBi |  |  | 0.000025 g |  |  |
| 5 Cathode deposition |  |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |  |
| Al |  |  | 0.0001203 g |  |  |
| 6 Encapsulation |  |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |  |
| 7 Other |  |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |  |

Table A.1.4.2 | Emission of solid-QD blue PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| DMSO | 0.011 g |
| Ethanol | 0.00789 g |
| Chlorobenzene | 0.0222 g |
| Methyl acetate | 0.00932 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| Ni(CH3COO)2∙4H2O | 0.000244 g | 98% | Spin.: 0.000249 g×98% |
| NH2CH2CH2OH | 0.000006 g | 98% | Spin.: 0.000061 g×98% |
| PVK | 0.000039 g | 98% | Spin.: 0.00004 g×98% |
| CsBr | 0.000271 g | 98% | Spin.: 0.000277 g×98% |
| PbBr2 | 0.000072 g | 98% | Spin.: 0.000073 g×98% |
| Br-MBA | 0.000039 g | 98% | Spin.: 0.00004 g×98% |
| TPBi | 0.0000146 g | 58% | Evapor.: 0.000025 g–(1.3g/cm3×2cm2×40nm) |
| LiF | 0.0000009 g | 62% | Evapor.: 0.0000014g–(2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.00012 g–(2.7g/cm3×2cm2×100nm) |

Table A.1.4.3 | Electricity input of solid-QD blue PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating (NiOx) |  |
| Spin speed | 2,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 0.875% |
| Mean spin coater power for a 2 cm2 piece | 4.385 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.116 kJ (0.00031 kWh) |
| Thermal annealing (NiOx) |  |
| Annealing temperature | 275 °C |
| Mean hotplate use factor for a 2 cm2 piece | 1.02% |
| Mean hotplate power for a 2 cm2 piece | 3.91 W |
| Annealing time | 45 min |
| Electricity for a 2 cm2 piece | 10.56 kJ (0.00293 kWh) |
| Spin coating (PVK) |  |
| Spin speed | 4,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.75% |
| Mean spin coater power for a 2 cm2 piece | 8.77 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 30 s |
| Electricity for a 2 cm2 piece | 0.690 kJ (0.00019 kWh) |

Table A.1.4.3 (continued) | Electricity input of solid-QD blue PeLED

| 3 Perovskite layer deposition |  |
| --- | --- |
| Spin coating |  |
| Spin speed | 5,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2.2% |
| Mean spin coater power for a 2 cm2 piece | 10.97 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.511 kJ (0.00042 kWh) |
| Thermal annealing |  |
| Annealing temperature | 80 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.3% |
| Mean hotplate power for a 2 cm2 piece | 1.14 W |
| Annealing time | 10 min |
| Electricity for a 2 cm2 piece | 0.686 kJ (0.00019 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.2 Green LED

A.2.1 Defect-suppressed green PeLED

Table A.2.1.1 | Raw material input of defect-suppressed green PeLED

| Raw material input |  | Mass for one device |  |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  | 0.55 g |  |  |
| ITO |  | 0.000136 g |  |  |
| Deionized water |  | 4.4 g |  |  |
| Acetone |  | 3.480 g |  |  |
| 2-Propanol |  | 3.454 g |  |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  | 0.000472 g |  |  |
| PFI (nafion perfluorinated ionomer) |  | 0.000472 g |  |  |
| Water |  | 0.01 g |  |  |
| 3 Perovskite layer production | (Molar) |  | (Volume) |  |
| FABr (formamidinium bromide) | 124.97 g/mol |  | 0.36 mol/L | 0.000450 g |
| GABr (guanidinium bromide) | 139.98 g/mol |  | 0.04 mol/L | 0.000056 g |
| PbBr2 | 367.01 g/mol |  | 0.4 mol/L | 0.001468 g |
| DMF | 0.944 g/mL |  | 10 μL | 0.009440 g |
| TBTB (1,3,5-tris(bromomethyl)-2,4,6-triethylbenzene) | 10 mg/mL |  |  | 0.000100 g |
| Toluene | 0.867 g/mL |  | 10 μL | 0.008670 g |
| 4 Electron transport layer production |  |  |  |  |
| TPBi |  | 0.000025 g |  |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  | 0.0000014 g |  |  |
| Al |  | 0.0001203 g |  |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  | 0.0116 g |  |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  | 0.00626 g |  |  |

Table A.2.1.2 | Emission of defect-suppressed green PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| DMF | 0.009440 g |
| Toluene | 0.008670 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| PFI | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| FABr | 0.000441 g | 98% | Spin.: 0.000450 g×98% |
| GABr | 0.000055 g | 98% | Spin.: 0.000056 g×98% |
| PbBr2 | 0.001439 g | 98% | Spin.: 0.001468 g×98% |
| TBTB | 0.000098 g | 98% | Spin.: 0.000100 g×98% |
| TPBi | 0.000012 g | 48% | Evapor.: 0.000025 g–(1.3g/cm3×2cm2×50nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g–(2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g–(2.7g/cm3×2cm2×100nm) |

Table A.2.1.3 | Electricity input of defect-suppressed green PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 2.18 kJ (0.00061 kWh) |
| Thermal annealing |  |
| Annealing temperature | 150 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.56% |
| Mean hotplate power for a 2 cm2 piece | 2.13 W |
| Annealing time | 30 min |
| Electricity for a 2 cm2 piece | 3.834 kJ (0.00107 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 1,000 + 3,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 0.4% + 1.32% |
| Mean spin coater power for a 2 cm2 piece | 2.0 + 6.6 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 60 + 60 s |
| Electricity for a 2 cm2 piece | 2.222 kJ (0.00062 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 0.10 kJ (0.0001 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.2.2 Distribution-controlled green PeLED

Table A.2.2.1 | Raw material input of distribution-controlled green PeLED

| Raw material input |  |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |  |
| Glass |  |  |  | 0.55 g |  |
| ITO |  |  |  | 0.000136 g |  |
| Deionized water |  |  |  | 4.4 g |  |
| Acetone |  |  |  | 3.480 g |  |
| 2-Propanol |  |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |  |
| PEDOT:PSS |  |  |  | 0.000472 g |  |
| PFI (nafion perfluorinated ionomer) |  |  |  | 0.000472 g |  |
| Water |  |  |  | 0.01 g |  |
| 3 Perovskite layer production | (Density/molar) | (Volume) |  |  |  |
| PEABr (phenylethylammonium bromide) |  | 0.4mol/L×20% |  |  | 0.000162 g |
| CsBr | 212.81 g/mol | 0.32mol/L×20% |  |  | 0.000136 g |
| MABr (methylammonium bromide) |  | 0.08mol/L×20% |  |  | 0.000018 g |
| PbBr2 | 367.01 g/mol | 0.6 mol/L×20% |  |  | 0.000440 g |
| DMSO | 1.10 g/mL | 2 μL |  |  | 0.0022 g |
| DMF | 0.944 g/cm3 | 8 μL |  |  | 0.007552g |
| TFPPO (tris(4-fluorophenyl)phosphine oxide) | 10 mg/mL | 10 μL |  |  | 0.0001 g |
| Chloroform | 1.49 g/mL | 10 μL |  |  | 0.0149 g |
| 4 Electron transport layer production |  |  |  |  |  |
| 3TPYMB (tris[2,4,6-trimethyl-3-(pyridin-3-yl)phenyl]borane) |  |  | 0.0000226 g |  |  |
| 5 Cathode deposition |  |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |  |
| Al* |  |  | 0.0001823 g |  |  |
| 6 Encapsulation |  |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |  |
| 7 Other |  |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |  |

* Al electrode is thicker (150 nm) here than a typical thickness (100 nm), and thus the input is larger.

Table A.2.2.2 | Emission of distribution-controlled green PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| DMSO | 0.0022 g |
| DMF | 0.007552 g |
| Chloroform | 0.0149 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000452 g | 96% | Spin.: 0.000472 g–(0.9425g/cm3×2cm2×105nm) |
| PFI | 0.000452 g | 96% | Spin.: 0.000472 g×96% |
| PEABr | 0.000159 g | 98% | Spin.: 0.000162 g×98% |
| CsBr | 0.000133 g | 98% | Spin.: 0.000136 g×98% |
| MABr | 0.000017 g | 98% | Spin.: 0.000018 g×98% |
| PbBr2 | 0.000431 g | 98% | Spin.: 0.000440 g×98% |
| TFPPO | 0.000098 g | 98% | Spin.: 0.000100 g×98% |
| 3TPYMB | 0.000014 g | 60% | Evapor.: 0.0000226 g– (1.13g/cm3×2cm2×40nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0001013 g | 56% | Evapor.: 0.0001823 g– (2.7g/cm3×2cm2×150nm) |

Table A.2.2.3 | Electricity input of distribution-controlled green PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 4,500 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2% |
| Mean spin coater power for a 2 cm2 piece | 10 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 90 s |
| Electricity for a 2 cm2 piece | 2.18 kJ (0.00061 kWh) |
| Thermal annealing |  |
| Annealing temperature | 150 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.56% |
| Mean hotplate power for a 2 cm2 piece | 2.13 W |
| Annealing time | 20 min |
| Electricity for a 2 cm2 piece | 2.56 kJ (0.00071 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 1,000 + 5,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 0.4% + 2.2% |
| Mean spin coater power for a 2 cm2 piece | 2.0 + 10.97 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 10 + 50 s |
| Electricity for a 2 cm2 piece | 0.9717 kJ (0.00027 kWh) |
| Thermal annealing |  |
| Annealing temperature | 90 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.3% |
| Mean hotplate power for a 2 cm2 piece | 1.15 W |
| Annealing time | 5 min |
| Electricity for a 2 cm2 piece | 0.10 kJ (0.0001 kWh) |

Table A.2.2.3 (continued) | Electricity input of distribution-controlled green PeLED

| 4 ETL/cathode deposition |  |
| --- | --- |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.2.3 Phase-engineered green PeLED

Table A.2.3.1 | Raw material input of phase-engineered green PeLED

| Raw material input |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  |  | 0.55 g |  |
| ITO |  |  | 0.000136 g |  |
| Deionized water |  |  | 4.4 g |  |
| Acetone |  |  | 3.480 g |  |
| 2-Propanol |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  |  | 0.000472 g |  |
| Water |  |  | 0.01 g |  |
| 3 Perovskite layer production | (Molar) | (Volume) |  |  |
| FABr | 124.97 g/mol | 0.4 mol/L |  | 0.000500 g |
| PEABr | 202.09 g/mol | 0.4 mol/L |  | 0.000808 g |
| PbBr2 | 367.01 g/mol | 0.6 mol/L |  | 0.002202 g |
| MACl (methylammonium chloride) | 67.52 g/mol | 0.06 mol/L |  | 0.000041 g |
| DMSO | 1.10 g/mL | 10 μL |  | 0.011 g |
| Chlorobenzene | 1.11 g/mL | 100 μL |  | 0.11 g |
| TOPO (trioctylphosphine oxide) | 2 mg/mL | 20 μL |  | 0.000040 g |
| 4 Electron transport layer production |  |  |  |  |
| TPBi |  |  | 0.000025 g |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |
| Al a |  |  | 0.0000722 g |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |

a Al electrode is thinner (60 nm) here than a typical thickness (100 nm), and thus the input is less.

Table A.2.3.2 | Emission of phase-engineered green PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| DMSO | 0.011 g |
| Chlorobenzene | 0.11 g |
| TOPO | 0.000040 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| FABr | 0.000490 g | 98% | Spin.: 0.000500 g×98% |
| PEABr | 0.000792 g | 98% | Spin.: 0.000808 g×98% |
| PbBr2 | 0.002158 g | 98% | Spin.: 0.002202 g×98% |
| MACl | 0.000040 g | 98% | Spin.: 0.000041 g×98% |
| TPBi | 0.000012 g | 48% | Evapor.: 0.000025 g – (1.3g/cm3×2cm2×50nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000398 g | 55% | Evapor.: 0.0000722 g – (2.7g/cm3×2cm2×60nm) |

Table A.2.3.3 | Electricity input of phase-engineered green PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 2,500 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.1% |
| Mean spin coater power for a 2 cm2 piece | 5.48 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 40 s |
| Electricity for a 2 cm2 piece | 0.788 kJ (0.00022 kWh) |
| Thermal annealing |  |
| Annealing temperature | 160 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.59% |
| Mean hotplate power for a 2 cm2 piece | 2.28 W |
| Annealing time | 15 min |
| Electricity for a 2 cm2 piece | 2.052 kJ (0.00057 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 3,000 + 7,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.32% + 3.08% |
| Mean spin coater power for a 2 cm2 piece | 6.6 + 15.4 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 120 + 60 s |
| Electricity for a 2 cm2 piece | 4.276 kJ (0.00119 kWh) |
| Thermal annealing |  |
| Annealing temperature | 90 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.3% |
| Mean hotplate power for a 2 cm2 piece | 1.15 W |
| Annealing time | 1 h |
| Electricity for a 2 cm2 piece | 4.14 kJ (0.00115 kWh) |

Table A.2.3.3 (continued) | Electricity input of phase-engineered green PeLED

| 4 ETL/cathode deposition |  |
| --- | --- |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.2.4 Ultra-bright green PeLED

Table A.2.4.1 | Raw material input of ultra-bright green PeLED

| Raw material input |  | Mass for one device |  |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  | 0.55 g |  |  |
| ITO |  | 0.000136 g |  |  |
| Deionized water |  | 4.4 g |  |  |
| Acetone |  | 3.480 g |  |  |
| 2-Propanol |  | 3.454 g |  |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  | 0.000472 g |  |  |
| PFI (nafion perfluorinated ionomer) |  | 0.000472 g |  |  |
| Water |  | 0.01 g |  |  |
| 3 Perovskite layer production | (Molar) |  | (Volume) |  |
| FABr (formamidinium bromide) | 124.97 g/mol |  | 0.84 mol/L | 0.00105 g |
| MABr (methylammonium bromide) | 111.97 g/mol |  | 0.12 mol/L | 0.000134 g |
| GABr (guanidinium bromide) | 139.98 g/mol |  | 0.24 mol/L | 0.000336 g |
| CsBr | 212.81 g/mol |  | 0.18 mol/L | 0.000383 g |
| PbBr2 | 367.01 g/mol |  | 1.2 mol/L | 0.001468 g |
| BPA (benzylphosphonic acid) | 170.11 g/mol |  | 0.12 mol/L | 0.000204 g |
| DMSO | 0.944 g/mL |  | 10 μL | 0.009440 g |
| 4 Electron transport layer production |  |  |  |  |
| TPBi |  | 0.000025 g |  |  |
| Chlorobenzene |  | 0.00555 g |  |  |
| 9,10-Di(naphthalene-2-yl)anthracen-2-yl-(4,1-phenylene)(1-phenyl-1H-benzo[d]imidazole) (ZADN) |  | 0.00003 g |  |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  | 0.0000014 g |  |  |
| Al |  | 0.0001203 g |  |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  | 0.0116 g |  |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  | 0.00626 g |  |  |

Table A.2.4.2 | Emission of ultra-bright green PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| DMSO | 0.009440 g |
| Chlorobenzene | 0.00555 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| PFI | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| FABr | 0.00103 g | 98% | Spin.: 0.00105 g×98% |
| MABr | 0.000131 g | 98% | Spin.: 0.000134 g×98% |
| GABr | 0.000329 g | 98% | Spin.: 0.000336 g×98% |
| CsBr | 0.000375 g | 98% | Spin.: 0.000383 g×98% |
| PbBr2 | 0.001439 g | 98% | Spin.: 0.001468 g×98% |
| BPA | 0.0002 g | 98% | Spin.: 0.000204 g×98% |
| TPBi | 0.000024 g | 98% | Spin.: 0.000025 g×98% |
| ZADN | 0.000021 g | 70% | Evapor.: 0.00003 g–(~1g/cm3×2cm2×45nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g–(2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g–(2.7g/cm3×2cm2×100nm) |

Table A.2.4.3 | Electricity input of ultra-bright green PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 2.18 kJ (0.00061 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 3.834 kJ (0.00107 kWh) |
| 3 Perovskite/ETL layer deposition |  |
| Spin coating (perovskite & TPBi) |  |
| Spin speed | 6,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2.64% |
| Mean spin coater power for a 2 cm2 piece | 13.2W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.645 kJ (0.00046 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 0.10 kJ (0.0001 kWh) |
| 4 Cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 8.72 kJ (0.0024 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.3 Red LED

A.3.1 Ligand-engineered red PeLED

Table A.3.1.1 | Raw material input of ligand-engineered red PeLED

| Raw material input |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  |  | 0.55 g |  |
| ITO |  |  | 0.000136 g |  |
| Deionized water |  |  | 4.4 g |  |
| Acetone |  |  | 3.480 g |  |
| 2-Propanol |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  |  | 0.000472 g |  |
| Water |  |  | 0.01 g |  |
| Poly-TPD (poly(N,N′–bis(4-butylphenyl)-N,N′-bisphenylbenzidine)) a 0.000075 g |  |  |  |  |  |
| Chlorobenzene |  |  | 0.00555 g |  |
| TFB (poly((9,9-dioctylfluorenyl-2,7-diyl)-co-(4,4′-(N-(4-s-butylphenyl)diphenylamine))) b 0.0001 g |  |  |  |  |
| p-xylene |  |  | 0.0043 g |  |
| 3 Perovskite layer production | (Molar) | (Volume) |  |  |  |
| MABr | 111.97 g/mol | Total 40 mg/mL |  | 0.000078 g |  |
| PbI2 | 461.01 g/mol |  |  | 0.000392 g |  |
| Toluene | 0.865 g/mL | 10 μL |  | 0.00865 g |  |
| EDTA (ethylenediaminetetraacetic acid) | 292.24 g/mol | 0.67 mol/L, 10 μL |  | 0.001958 g |  |
| L-glutathione | 307.32 g/mol |  |  | 0.002059 g |  |
| 4 Electron transport layer production |  |  |  |  |
| TPBi |  |  | 0.000025 g |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |
| Al c |  |  | 0.0000962 g |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |

a Poly-TPD is 15 mg/mL in chlorobenzene. b TFB is 20 mg/mL in p-xylene. c Al electrode is thinner (80 nm) here than a typical thickness (100 nm), and thus the input is less.

Table A.3.1.2 | Emission of ligand-engineered red PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| Chlorobenzene | 0.00555 g |
| p-xylene | 0.0043 g |
| Toluene | 0.00865 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| Poly-TPD | 0.000074 g | 98% | Spin.: 0.000075 g×98% |
| TFB | 0.000098 g | 98% | Spin.: 0.0001 g×98% |
| MABr | 0.000076 g | 98% | Spin.: 0.000078 g×98% |
| PbI2 | 0.000384 g | 98% | Spin.: 0.000392 g×98% |
| EDTA | 0.001919 g | 98% | Spin.: 0.001958 g×98% |
| L-glutathione | 0.002018 g | 98% | Spin.: 0.002059 g×98% |
| TPBi | 0.000016 g | 63% | Evapor.: 0.000025 g– (1.13g/cm3×2cm2×70nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000432 g | 45% | Evapor.: 0.0000962 g – (2.7g/cm3×2cm2×80nm) |

Table A.3.1.3 | Electricity input of ligand-engineered red PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 4,500 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2% |
| Mean spin coater power for a 2 cm2 piece | 10 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 80 s |
| Electricity for a 2 cm2 piece | 1.94 kJ (0.00054 kWh) |
| Thermal annealing |  |
| Annealing temperature | 140 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.52% |
| Mean hotplate power for a 2 cm2 piece | 1.99 W |
| Annealing time | 70 min |
| Electricity for a 2 cm2 piece | 8.36 kJ (0.00232 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 2,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 0.88% |
| Mean spin coater power for a 2 cm2 piece | 4.39 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 40 s |
| Electricity for a 2 cm2 piece | 0.744 kJ (0.00021 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.3.2 PEA/NMA-doped red PeLED

Table A.3.2.1 | Raw material input of PEA/NMA-doped red PeLED

| Raw material input |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  |  | 0.55 g |  |
| ITO |  |  | 0.000136 g |  |
| Deionized water |  |  | 4.4 g |  |
| Acetone |  |  | 3.480 g |  |
| 2-Propanol |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  |  | 0.000472 g |  |
| Water |  |  | 0.01 g |  |
| Poly-TPD (poly(N,N′–bis(4-butylphenyl)-N,N′-bisphenylbenzidine)) a 0.000075 g |  |  |  |  |  |
| Chlorobenzene |  |  | 0.00555 g |  |
| TFB (poly((9,9-dioctylfluorenyl-2,7-diyl)-co-(4,4′-(N-(4-s-butylphenyl)diphenylamine))) b 0.0001 g |  |  |  |  |
| p-xylene |  |  | 0.0043 g |  |
| 3 Perovskite layer production | (Molar) | (Volume) |  |  |  |
| PEAI (phenethylammonium iodide) | 249.09 g/mol | 0.05 mol/L |  | 0.0001245 g |  |
| NMAI (1-Naphthylmethylammonium iodide) | 285.12 g/​mol | 0.05 mol/L |  | 0.0001426 g |  |
| CsI | 259.81 g/mol | 0.05 mol/L |  | 0.0001299 g |  |
| PbI2 | 461.01 g/mol | 0.1 mol/L |  | 0.000461 g |  |
| DMF | 0.944 g/mL | 10 μL |  | 0.00944 g |  |
| TPPCl (tetraphenylphosphonium chloride) | 1.27 g/ml | 5% |  | 0.000635 g |  |
| 4 Electron transport layer production |  |  |  |  |
| TPBi |  |  | 0.000025 g |  |
| 5 Cathode deposition |  |  |  |  |
| LiF c |  |  | 0.0000028 g |  |
| Al d |  |  | 0.0000962 g |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |

a Poly-TPD is 15 mg/mL in chlorobenzene. b TFB is 20 mg/mL in p-xylene. c Two LiF layers were used in this device. d Al electrode is thinner (80 nm) here than a typical thickness (100 nm), and thus the input is less.

Table A.3.2.2 | Emission of PEA/NMA-doped red PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| Chlorobenzene | 0.00555 g |
| p-xylene | 0.0043 g |
| DMF | 0.00944 g |
| TPPCl | 0.000635 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| Poly-TPD | 0.000074 g | 98% | Spin.: 0.000075 g×98% |
| TFB | 0.000098 g | 98% | Spin.: 0.0001 g×98% |
| PEAI | 0.000122 g | 98% | Spin.: 0.0001245 g×98% |
| NMAI | 0.000140 g | 98% | Spin.: 0.0001426 g×98% |
| CsI | 0.000127 g | 98% | Spin.: 0.0001299 g×98% |
| PbI2 | 0.000452 g | 98% | Spin.: 0.000461 g×98% |
| TPBi | 0.000016 g | 63% | Evapor.: 0.000025 g– (1.13g/cm3×2cm2×70nm) |
| LiF | 0.0000017 g | 62% | Evapor.: 0.0000028 g – (2.64g/cm3×2cm2×2nm) |
| Al | 0.0000432 g | 45% | Evapor.: 0.0000962 g – (2.7g/cm3×2cm2×80nm) |

Table A.3.2.3 | Electricity input of PEA/NMA-doped red PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV Ozone plasma |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 4,500 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2% |
| Mean spin coater power for a 2 cm2 piece | 10 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 80 s |
| Electricity for a 2 cm2 piece | 1.94 kJ (0.00054 kWh) |
| Thermal annealing |  |
| Annealing temperature | 140 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.52% |
| Mean hotplate power for a 2 cm2 piece | 1.99 W |
| Annealing time | 70 min |
| Electricity for a 2 cm2 piece | 8.36 kJ (0.00232 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 2,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 0.88% |
| Mean spin coater power for a 2 cm2 piece | 4.39 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 40 s |
| Electricity for a 2 cm2 piece | 0.744 kJ (0.00021 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.3.3 Stabilized QD red PeLED

Table A.3.3.1 | Raw material input of stabilized QD red PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Anode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| PEDOT:PSS | 0.000472 g |
| PFI (nafion perfluorinated ionomer) | 0.000472 g |
| Water | 0.01 g |
| Poly-TPD (poly(N,N′–bis(4-butylphenyl)-N,N′-bisphenylbenzidine)) a 0.000075 g |  |  |
| Chlorobenzene | 0.00555 g |
| 4 Electron transport layer production b |  |
| TPBi | 0.000025 g |
| 5 Cathode deposition |  |
| LiF | 0.0000014 g |
| Al | 0.0001203 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

a Poly-TPD is 15 mg/mL in chlorobenzene. b Section 3 on the next page.

Table A.3.3.1 (continued) | Raw material input of stabilized QD red PeLED

| Raw material input | Pure density/ Molar mass | Volume | Mass for one batch | Mass for one device | Note |
| --- | --- | --- | --- | --- | --- |
| 3 Perovskite layer production |  |  |  |  |  |
| Cs2CO3 | 325.82 g/mol |  | 0.31 g | 0.00062 g | Chemicals for synthesizing maximum 1 mmol CsPbI3 QD. With the assumption of a synthesis transfer efficiency of ~ 20%, we will eventually obtain 0.2 mmol (144 mg) QD. A typical molar concentration of QD ink for spin coating is 0.025 mol/L. For per 2 cm2 device it takes 20 μL ink, i,.e. 0.29 mg. Thus, the chemicals can provide 500 devices. |
| Oleic acid | 0.89 g/mL | 3.2 mL | 0.002848 g | 0.0000057 g |  |
| 1-Octadecene | 0.789 g/mL | 13 mL | 0.010257 g | 0.0000205 g |  |
| PbI2 | 461.01 g/mol | 1 mmol | 0.46101 g | 0.000922 g |  |
| ZnI2 | 319.22 g/mol | 1 mmol | 0.32 g | 0.00064 g |  |
| Manganese(II) acetate tetrahydrate | 245.09 g/mol | 1 mmol | 0.24509 g | 0.00049 g |  |
| HI | 1.7 g/mL | 180 μL | 0.306 g | 0.000612 g |  |
| Methyl acetate | 0.934 g/mL | 50 mL | 0.0467 g | 0.0000934 g |  |
| Toluene | 0.865 g/mL | 50 mL | 0.04325 g | 0.0000865 g |  |
| Phenethylammonium iodide | 10 mg/mL | In DMF |  | 0.00002 g | Anti-solvent |
| DMF | 0.944 g/mL | 20 μL |  | 0.01888 g | Anti-solvent |

Table A.3.3.2 | Emission of stabilized QD red PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| Chlorobenzene | 0.00555 g |
| Oleic acid | 0.0000057 g |
| 1-Octadecene | 0.0000205 g |
| Manganese(II) acetate tetrahydrate | 0.00049 g |
| HI | 0.000612 g |
| Methyl acetate | 0.0000934 g |
| Toluene | 0.0000865 g |
| Phenethylammonium iodide | 0.00002 g |
| DMF | 0.01888 g |
| ZnCO3 a | 0.00025 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

a Zn2+ and CO32– are merged here.

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| PFI | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| Poly-TPD | 0.000074 g | 98% | Spin.: 0.000075 g×98% |
| CsI | 0.001277 g | 98% | Spin.: 0.001303 g×98% |
| PbI2 | 0.000904 g | 98% | Spin.: 0.000922 g×98% |
| TPBi | 0.0000103 g | 41% | Evapor.: 0.000025 g– (1.13g/cm3×2cm2×65nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g–(2.7g/cm3×2cm2×100nm) |

Table A.3.3.3 | Electricity input of stabilized QD red PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 4,500 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2% |
| Mean spin coater power for a 2 cm2 piece | 10 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 80 s |
| Electricity for a 2 cm2 piece | 1.94 kJ (0.00054 kWh) |
| Thermal annealing |  |
| Annealing temperature | 170 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.63% |
| Mean hotplate power for a 2 cm2 piece | 2.42 W |
| Annealing time | 30 min |
| Electricity for a 2 cm2 piece | 4.352 kJ (0.00121 kWh) |
| 3 Perovskite layer deposition |  |
| Magnetic stirring (QD synthesis) |  |
| Description | BioSan MSH-300 Magnetic Stirrer |
| Maximum stirring speed | 1250 rpm |
| Maximum stirring power | 8.5 W |
| Maximum applicable volume | 15 L |
| Stirring speed | 600 rpm |
| Perovskite volume for a 2 cm2 piece | 10 μL |
| Mean stirrer use factor for a 2 cm2 piece | 0.000032% |
| Mean stirrer power for a 2 cm2 piece | 2.72 × 10−6 W |
| Stirring time | 4 h |
| Electricity for a 2 cm2 piece | 3.92 × 10−5 kJ (1 × 10−8 kWh) |

| 3 Perovskite layer deposition |  |
| --- | --- |
| Heating (QD synthesis) |  |
| Description Thermo Scientific Cimarec Stirring Hot Plates SP88854105 |  |
| Maximum hotplate temperature | 540 °C |
| Maximum hotplate power | 384 W |
| Maximum applicable surface | 100 cm2 |
| Heating temperature | 150 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.56% |
| Mean hotplate power for a 2 cm2 piece | 2.15 W |
| Heating time | 10 min |
| Electricity for a 2 cm2 piece | 1.29 kJ (0.00035 kWh) |
| Centrifugation (QD synthesis) |  |
| Description | Biosan Microspin 12 |
| Maximum centrifugate speed | 14,500 rpm |
| Maximum centrifugate capacity | 24 mL |
| Maximum centrifugate power | 60 W |
| Centrifugate speed | 7800 rpm |
| Centrifugate volume for a 2 cm2 piece | 20 μL |
| Mean centrifugation use factor for a 2 cm2 piece | 0.044% |
| Mean centrifugate power for a 2 cm2 piece | 0.027 W |
| Centrifugate time | 15 min |
| Electricity for a 2 cm2 piece | 0.024 kJ (0.000007 kWh) |
| Spin coating |  |
| Spin speed | 3,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.32% |
| Mean spin coater power for a 2 cm2 piece | 6.58 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.248 kJ (0.00035 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.3.4 Lead-free TEA-Sn red PeLED

Table A.3.4.1 | Raw material input of lead-free TEA-Sn red PeLED

| Raw material input |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  |  | 0.55 g |  |
| ITO |  |  | 0.000136 g |  |
| Deionized water |  |  | 4.4 g |  |
| Acetone |  |  | 3.480 g |  |
| 2-Propanol |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  |  | 0.000472 g |  |
| Water |  |  | 0.01 g |  |
| 3 Perovskite layer production | (Molar) | (Volume) |  |  |  |
| TEAI (2-thiopheneethylamine iodide) | 255.12 g/mol | 0.44 mol/L |  | 0.0001123 g |  |
| SnI2 | 372.52 g/mol | 0.2 mol/L |  | 0.0000745 g |  |
| DMF | 0.944 g/mL | 8 μL |  | 0.007552 g |  |
| DMSO | 1.10 g/mL | 2 μL |  | 0.0022 g |  |
| CA (cyanuric acid) | 2.5 g/ml | 5%×10 μL |  | 0.00125 g |  |
| 4 Electron transport layer production |  |  |  |  |
| TPBi a |  |  | 0.000012 g |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |
| Al b |  |  | 0.0001203 g |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |

a TPBi is 30 nm thick here. b Al electrode is 100 nm thick here.

Table A.3.4.2 | Emission of lead-free TEA-Sn red PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| DMF | 0.007552 g |
| DMSO | 0.0022 g |
| CA (cyanuric acid) | 0.00125 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| TEAI | 0.000110 g | 98% | Spin.: 0.0001123 g×98% |
| SnI2 | 0.000073 g | 98% | Spin.: 0.0000745 g×98% |
| TPBi | 0.00000522 g | 44% | Evapor.: 0.000012 g– (1.13g/cm3×2cm2×30nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000422 g | 44% | Evapor.: 0.0000962 g–(2.7g/cm3×2cm2×100nm) |

Table A.3.4.3 | Electricity input of lead-free TEA-Sn red PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 4,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.75% |
| Mean spin coater power for a 2 cm2 piece | 8.75 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 30 s |
| Electricity for a 2 cm2 piece | 0.6891 kJ (0.00019 kWh) |
| Thermal annealing |  |
| Annealing temperature | 150 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.56% |
| Mean hotplate power for a 2 cm2 piece | 2.13 W |
| Annealing time | 20 min |
| Electricity for a 2 cm2 piece | 2.556 kJ (0.00071 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 0.6891 kJ (0.00019 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 2.556 kJ (0.00071 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.4 White LED

A.4.1 Heterophase-QD white PeLED

Table A.4.1.1 | Raw material input of heterophase-QD white PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Anode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| PEDOT:PSS | 0.000472 g |
| Water | 0.01 g |
| TFB (poly[(9,9-dioctylfluorenyl-2,7-diyl)-alt-(4,4′-(N-(4-butylphenyl)) a | 0.00005 g |
| Chlorobenzene | 0.00555 g |
| 3 Electron transport layer production |  |
| TPBi | 0.000025 g |
| 4 Cathode deposition |  |
| LiF | 0.0000014 g |
| Al | 0.0001203 g |
| 5 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 6 Other |  |
| Nitrogen gas | 0.00626 g |

a TFB is 5 mg/mL in chlorobenzene.

Table A.4.1.1 (continued) | Raw material input of heterophase-QD white PeLED

| Raw material input | Pure density/ Molar mass | Volume | Mass for one batch | Mass for one device | Note |
| --- | --- | --- | --- | --- | --- |
| 7 Perovskite layer production |  |  |  |  |  |
| Cs2CO3 | 325.82 g/mol | 0.5 mmol | 0.163 g | 0.000326 g | For 500 devices |
| PbI2 | 461.01 g/mol | 1 mmol | 0.46101 g | 0.000922 g |  |
| Oleic acid | 0.89 g/mL | 3.2 mL | 0.002848 g | 0.0000057 g |  |
| 1-Octadecene | 0.789 g/mL | 13 mL | 0.010257 g | 0.0000205 g |  |
| HI | 1.7 g/mL | 180 μL | 0.306 g | 0.000612 g |  |
| Ethyl acetate | 0.902 g/mL | 50 mL | 0.0451 g | 0.0000902 g |  |
| Toluene | 0.865 g/mL | 50 mL | 0.04325 g | 0.0000865 g |  |
| n-octane | 0.703 g/mL | 20 μL |  | 0.01406 g | Solvent |

Table A.4.1.2 | Emission of heterophase-QD white PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| Chlorobenzene | 0.00555 g |
| Oleic acid | 0.0000057 g |
| 1-Octadecene | 0.0000205 g |
| HI | 0.000612 g |
| Ethyl acetate | 0.0000902 g |
| Toluene | 0.0000865 g |
| n-octane | 0.01406 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| TFB | 0.000049 g | 98% | Spin.: 0.00005 g×98% |
| CsI | 0.000509 g | 98% | Spin.: 0.000519 g×98% |
| PbI2 | 0.000904 g | 98% | Spin.: 0.000922 g×98% |
| TPBi | 0.0000103 g | 41% | Evapor.: 0.000025 g–(1.13g/cm3×2cm2×65nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g–(2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g–(2.7g/cm3×2cm2×100nm) |

Table A.4.1.3 | Electricity input of heterophase-QD white PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 3,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.3% |
| Mean spin coater power for a 2 cm2 piece | 6.58 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.248 kJ (0.00035 kWh) |
| Thermal annealing |  |
| Annealing temperature | 130 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.48% |
| Mean hotplate power for a 2 cm2 piece | 1.85 W |
| Annealing time | 30 min |
| Electricity for a 2 cm2 piece | 3.328 kJ (0.00092 kWh) |
| 3 Perovskite layer deposition |  |
| Heating (QD synthesis) |  |
| Description Thermo Scientific Cimarec Stirring Hot Plates SP88854105 |  |
| Maximum hotplate temperature | 540 °C |
| Maximum hotplate power | 384 W |
| Maximum applicable surface | 100 cm2 |
| Heating temperature | 140 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.52% |
| Mean hotplate power for a 2 cm2 piece | 1.99 W |
| Heating time | 30 min |
| Electricity for a 2 cm2 piece | 3.584 kJ (0.00099 kWh) |

Table A.4.1.3 (continued) | Electricity input of heterophase-QD white PeLED

| 3 Perovskite layer deposition |  |
| --- | --- |
| Centrifugation (QD synthesis) |  |
| Centrifugate speed | 7800 rpm |
| Centrifugate volume for a 2 cm2 piece | 20 μL |
| Mean centrifugation use factor for a 2 cm2 piece | 0.044% |
| Mean centrifugate power for a 2 cm2 piece | 0.027 W |
| Centrifugate time | 15 min |
| Electricity for a 2 cm2 piece | 0.024 kJ (0.000007 kWh) |
| Spin coating |  |
| Spin speed | 2,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 0.88% |
| Mean spin coater power for a 2 cm2 piece | 4.39 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.116 kJ (0.00031 kWh) |
| Thermal annealing |  |
| Annealing temperature | 120 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.44% |
| Mean hotplate power for a 2 cm2 piece | 1.71 W |
| Annealing time | 30 min |
| Electricity for a 2 cm2 piece | 3.072 kJ (0.00085 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.4.2 Lead-free Cu white PeLED

Table A.4.2.1 | Raw material input of lead-free Cu white PeLED

| Raw material input |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  |  | 0.55 g |  |
| ITO |  |  | 0.000136 g |  |
| Deionized water |  |  | 4.4 g |  |
| Acetone |  |  | 3.480 g |  |
| 2-Propanol |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  |  | 0.000472 g |  |
| Water |  |  | 0.01 g |  |
| 3 Perovskite layer production* | (Molar) | (Volume) |  |  |  |
| CsI | 259.81 g/mol | 1 mmol |  | 0.00088 g |  |
| CuI | 190.45 g/mol | 1 mmol |  | 0.00065 g |  |
| polyethylene glycol sorbitan monooleate | 604.8 g/mol | 0.006 mmol |  | 0.0000123 g |  |
| DMSO | 1.10 g/mL | 10 μL |  | 0.011 g |  |
| 4 Electron transport layer production |  |  |  |  |
| TmPyPB (1,3,5-Tri(m-pyridin-3-ylphenyl) benzene) |  |  | 0.0000233 g |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |
| Al |  |  | 0.0001203 g |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |

* CsI, CuI and polyethylene glycol sorbitan monooleate are dissolved in DMSO with 14% wt.

Table A.4.2.2 | Emission of lead-free Cu white PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| polyethylene glycol sorbitan monooleate | 0.0000123 g |
| DMSO | 0.011 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| CsI | 0.00086 g | 98% | Spin.: 0.00088 g×98% |
| CuI | 0.00064 g | 98% | Spin.: 0.00065 g×98% |
| TmPyPB | 0.0000128 g | 55% | Evapor.: 0.0000233g–(1.166g/cm3×2cm2×45nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g–(2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g–(2.7g/cm3×2cm2×100nm) |

Table A.4.2.3 | Electricity input of lead-free Cu white PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 3,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.3% |
| Mean spin coater power for a 2 cm2 piece | 6.58 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.248 kJ (0.00035 kWh) |
| Thermal annealing |  |
| Annealing temperature | 140 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.52% |
| Mean hotplate power for a 2 cm2 piece | 1.99 W |
| Annealing time | 15 min |
| Electricity for a 2 cm2 piece | 1.792 kJ (0.0005 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Spin speed | 2,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 0.88% |
| Mean spin coater power for a 2 cm2 piece | 4.39 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin coating time | 60 s |
| Electricity for a 2 cm2 piece | 1.116 kJ (0.00031 kWh) |
| Thermal annealing |  |
| Annealing temperature | 100 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.37% |
| Mean hotplate power for a 2 cm2 piece | 1.42 W |
| Annealing time | 5 min |
| Electricity for a 2 cm2 piece | 0.427 kJ (0.00012 kWh) |

Table A.4.2.3 (continued) | Electricity input of lead-free Cu white PeLED

| 4 ETL/cathode deposition |  |
| --- | --- |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

A.5 Near-infrared LED

A.5.1 Molecular-passivated NIR PeLED

Table A.5.1.1 | Raw material input of molecular-passivated NIR PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Cathode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| TFB (poly[(9,9-dioctylfluorenyl-2,7-diyl)-alt-(4,4′-(N-(4-butylphenyl)) | 0.0001 g |
| Toluene | 0.00865 g |
| 3 Perovskite layer production |  |
| EDEA (2,2′-(ethylenedioxy)diethylamine) | 0.00010678 g |
| FAI (formamidinium iodide) | 0.00044712 g |
| PbI2 | 0.00059931 g |
| DMF | 0.00944 g |
| 4 Electron transport layer production |  |
| ZnO | 0.0002 g |
| 2-propanol | 0.008 g |
| PEIE (polyethylenimine ethoxylated) | 0.004 g |
| Water | 0.01 g |
| 5 Anode deposition |  |
| MoOx | 0.0000094 g |
| Au | 0.0006516 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

Table A.5.1.2 | Emission of molecular-passivated NIR PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Toluene | 0.005 g |
| DMF | 0.00944 g |
| 2-propanol | 0.008 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| TFB | 0.00008746 g | 87% | Spin.: 0.0001 g–(1.567g/cm3×2cm2×40nm) |
| FAI | 0.00043818 g | 98% | Spin.: 0.00044712 g×98% |
| PbI2 | 0.00058733 g | 98% | Spin.: 0.00059931 g×98% |
| EDEA | 0.00010464 g | 98% | Spin.: 0.00010678 g×98% |
| ZnO | 0.00016634 g | 83% | Spin.: 0.0002 g – (5.61g/cm3×2cm2×30nm) |
| PEIE | 0.00332 g | 83% | Spin.: 0.004 g×83% |
| MoOx | 0.000002834 g | 30% | Evapor.: 0.0000094 g–(4.69g/cm3×2cm2×7nm) |
| Au | 0.00042 g | 64% | Evapor.: 0.0006516 g–(19.3g/cm3×2cm2×60nm) |

Table A.5.1.3 | Electricity input of molecular-passivated NIR PeLED*

| 1 Cathode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Electron transport layer deposition |  |
| Spin coating (ZnO) |  |
| Electricity for a 2 cm2 piece | 0.690 kJ (0.00019 kWh) |
| Spin coating (PEIE) |  |
| Electricity for a 2 cm2 piece | 0.756 kJ (0.00021 kWh) |
| Thermal annealing (PEIE) |  |
| Electricity for a 2 cm2 piece | 0.853 kJ (0.00024 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 0.62 kJ (0.00017 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 0.85 kJ (0.000237 kWh) |
| 4 HTL/anode deposition |  |
| Thermal evaporation (similar to Table A.1.1.3) |  |
| Electricity for a 2 cm2 piece | 10.57 kJ (0.0029 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | - kJ (0.00433 kWh) |

* Due to the same structure as the submicrometric NIR PeLED devices, Table A.5.2.3 shares the same data as Table A.5.1.3.

A.5.2 Submicrometric NIR PeLED

Table A.5.2.1 | Raw material input of submicrometric NIR PeLED

| Raw material input* | Mass for one device |
| --- | --- |
| 1 Cathode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| TFB (poly[(9,9-dioctylfluorenyl-2,7-diyl)-alt-(4,4′-(N-(4-butylphenyl)) | 0.0001 g |
| Toluene | 0.00865 g |
| 3 Perovskite layer production |  |
| 5AVA (5-aminovaleric acid) | 0.0001128 g |
| FAI (formamidinium iodide) | 0.0003385 g |
| PbI2 | 0.0001612 g |
| DMF | 0.00944 g |
| 4 Electron transport layer production |  |
| ZnO | 0.0002 g |
| 2-propanol | 0.008 g |
| PEIE (polyethylenimine ethoxylated) | 0.004 g |
| Water | 0.01 g |
| 5 Anode deposition |  |
| MoOx | 0.0000094 g |
| Au | 0.0006516 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

* For NIR devices, the device structure is inverted, i.e., ITO is used as the cathode and Au is used as the anode.

Table A.5.2.2 | Emission of submicrometric NIR PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Toluene | 0.00865 g |
| 5AVA (5-aminovaleric acid) | 0.0001128 g |
| DMF | 0.00944 g |
| 2-propanol | 0.008 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| TFB | 0.00008746 g | 87% | Spin.: 0.0001 g–(1.567g/cm3×2cm2×40nm) |
| FAI | 0.0003114 g | 92% | Spin.: 0.0003385 g×92% |
| PbI2 | 0.0001483 g | 92% | Spin.: 0.0001612 g×92% |
| ZnO | 0.00016634 g | 83% | Spin.: 0.0002 g – (5.61g/cm3×2cm2×30nm) |
| PEIE | 0.00332 g | 83% | Spin.: 0.004 g×83% |
| MoOx | 0.000002834 g | 30% | Evapor.: 0.0000094 g–(4.69g/cm3×2cm2×7nm) |
| Au | 0.00042 g | 64% | Evapor.: 0.0006516 g–(19.3g/cm3×2cm2×60nm) |

Table A.5.2.3 | Electricity input of submicrometric NIR PeLED

| 1 Cathode deposition* |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating (ZnO) |  |
| Spin speed | 4,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 1.75% |
| Mean spin coater power for a 2 cm2 piece | 8.77 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 30 s |
| Electricity for a 2 cm2 piece | 0.690 kJ (0.00019 kWh) |
| Spin coating (PEIE) |  |
| Spin speed | 5,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2.19% |
| Mean spin coater power for a 2 cm2 piece a | 10.96 W |
| Mean external pump power for a 2 cm2 piece a | 14.22 W |
| Spin-coating time | 30 s |
| Electricity for a 2 cm2 piece | 0.756 kJ (0.00021 kWh) |
| Thermal annealing (PEIE) |  |
| Annealing temperature | 100 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.37% |
| Mean hotplate power for a 2 cm2 piece | 1.42 W |
| Annealing time | 10 min |
| Electricity for a 2 cm2 piece | 0.853 kJ (0.00024 kWh) |

* For NIR devices, the device structure is inverted, i.e., ITO is used as the cathode and Au is used as the anode.

| 3 Perovskite layer deposition |  |  |  |
| --- | --- | --- | --- |
| Spin coating |  |  |  |
| Spin speed | 3,000 rpm |  |  |
| Mean spin coater use factor for a 2 cm2 piece | 1.32% |  |  |
| Mean spin coater power for a 2 cm2 piece | 6.58 W |  |  |
| Mean external pump power for a 2 cm2 piece | 14.22 W |  |  |
| Spin coating time | 60 s |  |  |
| Electricity for a 2 cm2 piece | 0.62 kJ (0.00017 kWh) |  |  |
| Thermal annealing |  |  |  |
| Annealing temperature | 100 °C |  |  |
| Mean hotplate use factor for a 2 cm2 piece | 0.37% |  |  |
| Mean hotplate power for a 2 cm2 piece | 1.42 W |  |  |
| Annealing time | 10 min |  |  |
| Electricity for a 2 cm2 piece | 0.85 kJ (0.000237 kWh) |  |  |
| 4 ETL/anode deposition |  |  |  |
| Thermal evaporation (similar to Table A.1.1.3) |  |  |  |
| Evaporation melting temperature |  | MoOx 800°C | Au 1100°C |  |
| Mean evaporator temperature utilization percentage |  | 44.4% | 61.1% |  |
| Mean evaporator use factor for a 2 cm2 piece |  | 0.89% | 1.22% |  |
| Mean evaporator power for a 2 cm2 piece |  | 7.12 W | 9.76W |  |
| Cooling system mean power for a 2 cm2 piece | 4 W |  |  |
| Mean vacuum pump power for a 2 cm2 piece | 5.4 W |  |  |
| Evaporator working time | 6 min |  |  |
| Vacuum pump working time | 20 min |  |  |
| Cooling system working time | 9 min |  |  |
| Electricity for a 2 cm2 piece | 10.57 kJ (0.0029 kWh) |  |  |
| 5 Encapsulation |  |  |  |
| UV radiation |  |  |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |  |  |
| 6 Other |  |  |  |
| N2 gas glovebox atmosphere |  |  |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |  |  |

A.5.3 Ultrastable NIR PeLED

Table A.5.3.1 | Raw material input of ultrastable NIR PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Cathode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| TFB (poly[(9,9-dioctylfluorenyl-2,7-diyl)-alt-(4,4′-(N-(4-butylphenyl)) | 0.0001 g |
| Toluene | 0.00865 g |
| 3 Perovskite layer production |  |
| SFB10 (3-(Decyldimethylammonio)­propane­sulfonate inner salt) | 0.0000615 g |
| FAI (formamidinium iodide) | 0.00044712 g |
| PbI2 | 0.00059931 g |
| DMF | 0.00944 g |
| 4 Electron transport layer production |  |
| ZnO | 0.0002 g |
| 2-propanol | 0.008 g |
| PEIE (polyethylenimine ethoxylated) | 0.004 g |
| Water | 0.01 g |
| 5 Anode deposition |  |
| MoOx | 0.0000094 g |
| Au | 0.0006516 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

Table A.5.3.2 | Emission of ultrastable NIR PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Toluene | 0.005 g |
| DMF | 0.00944 g |
| 2-propanol | 0.008 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| TFB | 0.00008746 g | 87% | Spin.: 0.0001 g–(1.567g/cm3×2cm2×40nm) |
| FAI | 0.00043817 g | 98% | Spin.: 0.00044712 g×98% |
| PbI2 | 0.00058732 g | 98% | Spin.: 0.00059931 g×98% |
| SFB10 | 0.0000603 g | 98% | Spin.: 0.0000615 g g×98% |
| ZnO | 0.00016634 g | 83% | Spin.: 0.0002 g – (5.61g/cm3×2cm2×30nm) |
| PEIE | 0.00332 g | 83% | Spin.: 0.004 g×83% |
| MoOx | 0.000002834 g | 30% | Evapor.: 0.0000094 g–(4.69g/cm3×2cm2×7nm) |
| Au | 0.00042 g | 64% | Evapor.: 0.0006516 g–(19.3g/cm3×2cm2×60nm) |

Table A.5.3.3 | Electricity input of ultrastable NIR PeLED*

| 1 Cathode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating (ZnO) |  |
| Electricity for a 2 cm2 piece | 0.690 kJ (0.00019 kWh) |
| Spin coating (PEIE) |  |
| Electricity for a 2 cm2 piece | 0.756 kJ (0.00021 kWh) |
| Thermal annealing (PEIE) |  |
| Electricity for a 2 cm2 piece | 0.853 kJ (0.00024 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 0.62 kJ (0.00017 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 0.85 kJ (0.000237 kWh) |
| 4 ETL/anode deposition |  |
| Thermal evaporation (similar to Table A.1.1.3) |  |
| Electricity for a 2 cm2 piece | 10.57 kJ (0.0029 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

* Due to the same structure as the submicrometric NIR PeLED device, Table A.5.3.3 shares the same data as Table A.5.1.3.

A.5.4 Lead-free Sn NIR PeLED

Table A.5.4.1 | Raw material input of lead-free Sn NIR PeLED

| Raw material input |  |  | Mass for one device |  |
| --- | --- | --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |  |  |
| Glass |  |  | 0.55 g |  |
| ITO |  |  | 0.000136 g |  |
| Deionized water |  |  | 4.4 g |  |
| Acetone |  |  | 3.480 g |  |
| 2-Propanol |  |  | 3.454 g |  |
| 2 Hole transport layer production |  |  |  |  |
| PEDOT:PSS |  |  | 0.000472 g |  |
| Water |  |  | 0.01 g |  |
| 3 Perovskite layer production | (Molar) | (Volume) |  |  |  |
| VmB1 (Vitamin B1) | 0.15M/2.65M | 14wt% |  | 0.00008 g |  |
| PEAI (phenylethylammonium iodide) | 0.3M/2.65M | 14wt% |  | 0.00016 g |  |
| FAI | 0.9M/2.65M | 14wt% |  | 0.00049 g |  |
| CsI | 0.1M/2.65M | 14wt% |  | 0.00005 g |  |
| SnI2 | 1M/2.65M | 14wt% |  | 0.00054 g |  |
| SnF2 | 0.2M/2.65M | 14wt% |  | 0.00011 g |  |
| DMF | 0.944 g/mL | 5 μL |  | 0.00472 g |  |
| DMSO | 1.10 g/mL | 5 μL |  | 0.00550 g |  |
| 4 Electron transport layer production |  |  |  |  |
| TPBi |  |  | 0.000012 g |  |
| 5 Cathode deposition |  |  |  |  |
| LiF |  |  | 0.0000014 g |  |
| Al |  |  | 0.0001203 g |  |
| 6 Encapsulation |  |  |  |  |
| UV-cured epoxy |  |  | 0.0116 g |  |
| 7 Other |  |  |  |  |
| Nitrogen gas |  |  | 0.00626 g |  |

Table A.5.4.2 | Emission of lead-free Sn NIR PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| DMF | 0.00472 g |
| DMSO | 0.0055 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| VmB1 | 0.000078 g | 98% | Spin.: 0.00008 g×98% |
| PEAI | 0.000157 g | 98% | Spin.: 0.00016 g×98% |
| FAI | 0.000480 g | 98% | Spin.: 0.00049 g×98% |
| CsI | 0.000049 g | 98% | Spin.: 0.00005 g×98% |
| SnI2 | 0.000530 g | 98% | Spin.: 0.00054 g×98% |
| SnF2 | 0.000108 g | 98% | Spin.: 0.00011 g×98% |
| TPBi | 0.00000522 g | 44% | Evapor.: 0.000012 g– (1.13g/cm3×2cm2×30nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000422 g | 44% | Evapor.: 0.0000962 g–(2.7g/cm3×2cm2×100nm) |

Table A.5.4.3 | Electricity input of lead-free Sn NIR PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Spin speed | 5,000 rpm |
| Mean spin coater use factor for a 2 cm2 piece | 2.19% |
| Mean spin coater power for a 2 cm2 piece | 10.94 W |
| Mean external pump power for a 2 cm2 piece | 14.22 W |
| Spin-coating time | 50 s |
| Electricity for a 2 cm2 piece | 1.258 kJ (0.00035 kWh) |
| Thermal annealing |  |
| Annealing temperature | 150 °C |
| Mean hotplate use factor for a 2 cm2 piece | 0.56% |
| Mean hotplate power for a 2 cm2 piece | 2.13 W |
| Annealing time | 10 min |
| Electricity for a 2 cm2 piece | 1.278 kJ (0.00036 kWh) |
| 3 Perovskite layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 2.113 kJ (0.00059 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 0.511 kJ (0.00014 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

Part B. Life cycle inventories of simulated industrial PeLEDs

Contents

B.1	Industrial YCl3-doped blue PeLED …………………………..……..…..……. 73

B.2	Industrial distribution-controlled green PeLED …………..……...………..…. 76

B.3	Industrial ligand-engineered red PeLED ……………...…..……...………..…. 79

B.4	Industrial lead-free Cu white PeLED …………………......……..…..……..…. 82

B.5	Industrial submicrometric NIR PeLED …………………..….…..….……..…. 85

B.1 Industrial YCl3-doped blue PeLED

Table B.1.1 | Raw material input of industrial YCl3-doped blue PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Anode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| PEDOT:PSS | 0.000472 g |
| Water | 0.01 g |
| 3 Perovskite layer production |  |
| CsBr (50 nm×2 cm2×4.44 g/cm3)/60% = 0.0000740 g |  |
| PbBr2 (50 nm×2 cm2×6.66 g/cm3)/60% = 0.0001110 g |  |
| PEACl (50 nm×2 cm2×~1 g/cm3)/60% = 0.0000167 g |  |
| YCl3 (50 nm×2%×2 cm2×2.67 g/cm3)/60% = 0.0000009 g |  |
| 4 Electron transport layer production |  |
| TPBi | 0.000025 g |
| 5 Cathode deposition |  |
| LiF | 0.0000014 g |
| Al | 0.0001203 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

Table B.1.2 | Emission of industrial YCl3-doped blue PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.0004626 g | 98% | Spin.: 0.000472 g ×98% |
| CsBr | 0.0000296 g | 40% | Evapor.: 0.0000740 g×40% |
| PbBr2 | 0.0000444 g | 40% | Evapor.: 0.0001110 g×40% |
| PEACl | 0.0000067 g | 40% | Evapor.: 0.0000167 g×40% |
| YCl3 | 0.0000004 g | 40% | Evapor.: 0.0000009 g×40% |
| TPBi | 0.0000146 g | 58% | Evapor.: 0.000025 g – (1.3g/cm3×2cm2×40nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g– (2.7g/cm3×2cm2×100nm) |

Table B.1.3 | Electricity input of industrial YCl3-doped blue PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 0.876 kJ (0.00024 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 3.2 kJ (0.00089 kWh) |
| 3 Perovskite layer deposition |  |
| Thermal evaporation a |  |
| Maximum evaporator temperature | 1800 °C |
| Evaporation melting temperature | CsPbBr3 560 °C |
| Mean evaporator temperature utilization percentage 15.6% |  |
| Mean evaporator use factor for a 2 cm2 piece | 0.312% |
| Mean evaporator power for a 2 cm2 piece | 2.5 W |
| Cooling system mean power for a 2 cm2 piece | 4 W |
| Mean vacuum pump power for a 2 cm2 piece | 5.4 W |
| Evaporator working time | 3 min |
| Vacuum pump working time | 3 min |
| Cooling system working time | 3 min |
| Electricity for a 2 cm2 piece | 2.14 kJ (0.00059 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

a The same details with Table A.1 are omitted here.

B.2 Industrial distribution-controlled green PeLED

Table B.2.1 | Raw material input of industrial distribution-controlled green PeLED

| Raw material input |  | Mass for one device |
| --- | --- | --- |
| 1 Anode substrate: ITO glass preparation |  |  |
| Glass |  | 0.55 g |
| ITO |  | 0.000136 g |
| Deionized water |  | 4.4 g |
| Acetone |  | 3.480 g |
| 2-Propanol |  | 3.454 g |
| 2 Hole transport layer production |  |  |
| PEDOT:PSS |  | 0.000472 g |
| PFI (nafion perfluorinated ionomer) |  | 0.000472 g |
| Water |  | 0.01 g |
| 3 Perovskite layer production |  |  |
| PEABr (60 nm×2 cm2×0.5×~1 g/cm3)/60% = 0.0000100 g |  |  |
| CsBr (60 nm×2 cm2×0.4×4.44 g/cm3)/60% = 0.0000355 g |  |  |
| MABr (60 nm×2 cm2×0.1×~1 g/cm3)/60% = 0.0000020 g |  |  |
| PbBr2 (60 nm×2 cm2×6.66 g/cm3)/60% = 0.0001332 g |  |  |
| 4 Electron transport layer production |  |  |
| 3TPYMB (tris[2,4,6-trimethyl-3-(pyridin-3-yl)phenyl]borane) | 0.0000226 g |  |
| 5 Cathode deposition |  |  |
| LiF | 0.0000014 g |  |
| Al | 0.0001823 g |  |
| 6 Encapsulation |  |  |
| UV-cured epoxy | 0.0116 g |  |
| 7 Other |  |  |
| Nitrogen gas | 0.00626 g |  |

Table B.2.2 | Emission of industrial distribution-controlled green PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000453 g | 96% | Spin.: 0.000472 g–(0.9425g/cm3×2cm2×105nm) |
| PFI | 0.000453 g | 96% | Spin.: 0.000472 g×96% |
| PEABr | 0.0000040 g | 40% | Evapor.: 0.0000100 g×40% |
| CsBr | 0.0000142 g | 40% | Evapor.: 0.0000355 g×40% |
| MABr | 0.0000008 g | 40% | Evapor.: 0.0000020 g×40% |
| PbBr2 | 0.0000533 g | 40% | Evapor.: 0.0001332 g×40% |
| 3TPYMB | 0.000014 g | 60% | Evapor.: 0.0000226 g– (1.13g/cm3×2cm2×40nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0001013 g | 56% | Evapor.: 0.0001823 g–(2.7g/cm3×2cm2×150nm) |

Table B.2.3 | Electricity input of industrial distribution-controlled green PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 2.18 kJ (0.00061 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 2.56 kJ (0.00071 kWh) |
| 3 Perovskite layer deposition |  |
| Thermal evaporation |  |
| Maximum evaporator temperature | 1800 °C |
| Evaporation melting temperature | PEA2Cs1.6MA0.4Pb3Br10 ~560 °C |
| Electricity for a 2 cm2 piece | 2.14 kJ (0.00059 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

B.3 Industrial ligand-engineered red PeLED

Table B.3.1 | Raw material input of industrial ligand-engineered red PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Anode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| PEDOT:PSS | 0.000472 g |
| Water | 0.01 g |
| Poly-TPD | 0.000075 g |
| Chlorobenzene | 0.00555 g |
| TFB | 0.0001 g |
| p-xylene | 0.0043 g |
| 3 Perovskite layer production |  |
| MABr (20 nm×2 cm2×~1 g/cm3)/60% = 0.0000067 g |  |
| PbI2 (20 nm×2 cm2×6.16 g/cm3)/60% = 0.0000411 g |  |
| 4 Electron transport layer production |  |
| TPBi | 0.000025 g |
| 5 Cathode deposition |  |
| LiF | 0.0000014 g |
| Al | 0.0000962 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

Table B.3.2 | Emission of industrial ligand-engineered red PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| Poly-TPD | 0.000074 g | 98% | Spin.: 0.000075 g×98% |
| TFB | 0.000098 g | 98% | Spin.: 0.0001 g×98% |
| MABr | 0.0000027 g | 40% | Evapor.: 0.0000067 g×40% |
| PbI2 | 0.0000164 g | 40% | Evapor.: 0.0000411 g×40% |
| TPBi | 0.000016 g | 63% | Evapor.: 0.000025 g– (1.13g/cm3×2cm2×70nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000432 g | 45% | Evapor.: 0.0000962 g – (2.7g/cm3×2cm2×80nm) |

Table B.3.3 | Electricity input of industrial ligand-engineered red PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 1.94 kJ (0.00054 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 8.36 kJ (0.00232 kWh) |
| 3 Perovskite layer deposition |  |
| Thermal evaporation |  |
| Maximum evaporator temperature | 1800 °C |
| Evaporation melting temperature | MAPb(IxBr1−x)3 ~150 °C |
| Mean evaporator temperature utilization percentage 4.2% |  |
| Mean evaporator use factor for a 2 cm2 piece | 0.083% |
| Mean evaporator power for a 2 cm2 piece | 0.664 W |
| Cooling system mean power for a 2 cm2 piece | 4 W |
| Mean vacuum pump power for a 2 cm2 piece | 5.4 W |
| Evaporator working time | 3 min |
| Vacuum pump working time | 3 min |
| Cooling system working time | 3 min |
| Electricity for a 2 cm2 piece | 1.81 kJ (0.00050 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

B.4 Industrial lead-free Cu white PeLED

Table B.4.1 | Raw material input of industrial lead-free Cu white PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Anode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| PEDOT:PSS | 0.000472 g |
| Water | 0.01 g |
| 3 Perovskite layer production |  |
| CsI (60 nm×2 cm2×4.51 g/cm3)/60% = 0.0000902 g |  |
| CuI (60 nm×2 cm2×5.67 g/cm3)/60% = 0.0001134 g |  |
| 4 Electron transport layer production |  |
| TmPyPB (1,3,5-Tri(m-pyridin-3-ylphenyl) benzene) | 0.0000233 g |
| 5 Cathode deposition |  |
| LiF | 0.0000014 g |
| Al | 0.0001203 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

Table B.4.2 | Emission of industrial lead-free Cu white PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| PEDOT:PSS | 0.000463 g | 98% | Spin.: 0.000472 g×98% |
| CsI | 0.0000361 g | 40% | Evapor.: 0.0000902 g×40% |
| CuI | 0.0000454 g | 40% | Evapor.: 0.0001134 g×40% |
| TmPyPB | 0.0000128 g | 55% | Evapor.: 0.0000233g–(1.166g/cm3×2cm2×45nm) |
| LiF | 0.00000087 g | 62% | Evapor.: 0.0000014 g – (2.64g/cm3×2cm2×1nm) |
| Al | 0.0000663 g | 55% | Evapor.: 0.0001203 g– (2.7g/cm3×2cm2×100nm) |

Table B.4.3 | Electricity input of industrial lead-free Cu white PeLED

| 1 Anode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating |  |
| Electricity for a 2 cm2 piece | 1.248 kJ (0.00035 kWh) |
| Thermal annealing |  |
| Electricity for a 2 cm2 piece | 1.792 kJ (0.0005 kWh) |
| 3 Perovskite layer deposition |  |
| Thermal evaporation |  |
| Maximum evaporator temperature | 1800 °C |
| Evaporation melting temperature | Cs3Cu2I5/CsCu2I3 ~350 °C |
| Mean evaporator temperature utilization percentage 9.7% |  |
| Mean evaporator use factor for a 2 cm2 piece | 0.19% |
| Mean evaporator power for a 2 cm2 piece | 1.56 W |
| Cooling system mean power for a 2 cm2 piece | 4 W |
| Mean vacuum pump power for a 2 cm2 piece | 5.4 W |
| Evaporator working time | 3 min |
| Vacuum pump working time | 3 min |
| Cooling system working time | 3 min |
| Electricity for a 2 cm2 piece | 1.97 kJ (0.00055 kWh) |
| 4 ETL/cathode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.08 kJ (0.0028 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |

B.5 Industrial submicrometric NIR PeLED

Table B.5.1 | Raw material input of industrial submicrometric NIR PeLED

| Raw material input | Mass for one device |
| --- | --- |
| 1 Cathode substrate: ITO glass preparation |  |
| Glass | 0.55 g |
| ITO | 0.000136 g |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Hole transport layer production |  |
| TFB (poly[(9,9-dioctylfluorenyl-2,7-diyl)-alt-(4,4′-(N-(4-butylphenyl)) | 0.0001 g |
| Toluene | 0.00865 g |
| 3 Perovskite layer production |  |
| FAI (50 nm×2 cm2×1 g/cm3)/60% = 0.0000167 g |  |
| PbI2 (50 nm×2 cm2×6.16 g/cm3)/60% = 0.0001027 g |  |
| 4 Electron transport layer production |  |
| ZnO | 0.0002 g |
| 2-propanol | 0.008 g |
| PEIE (polyethylenimine ethoxylated) | 0.004 g |
| Water | 0.01 g |
| 5 Anode deposition |  |
| MoOx | 0.0000094 g |
| Au | 0.0006516 g |
| 6 Encapsulation |  |
| UV-cured epoxy | 0.0116 g |
| 7 Other |  |
| Nitrogen gas | 0.00626 g |

Table B.5.2 | Emission of industrial submicrometric NIR PeLED

| Emission | Mass for one device |
| --- | --- |
| 1 Cleaning |  |
| Deionized water | 4.4 g |
| Acetone | 3.480 g |
| 2-Propanol | 3.454 g |
| 2 Solvent |  |
| Toluene | 0.00865 g |
| 2-propanol | 0.008 g |
| Water | 0.01 g |
| 3 Disposal materials |  |
| UV-cured epoxy | 0.0116 g |
| ITO | 0.000136 g |
| Glass | 0.55 g |
| 4 Other |  |
| Nitrogen gas | 0.00626 g |

| Emission | Emission mass | Emission rate | Emission process/note |
| --- | --- | --- | --- |
| 5 Deposition |  |  |  |
| TFB | 0.00008746 g | 87% | Spin.: 0.0001 g– (1.567g/cm3×2cm2×40nm) |
| FAI | 0.0000067 g | 40% | Evapor.: 0.0000167 g×40% |
| PbI2 | 0.0000411 g | 40% | Evapor.: 0.0001027 g×40% |
| ZnO | 0.00016634 g | 83% | Spin.: 0.0002 g – (5.61g/cm3×2cm2×30nm) |
| PEIE | 0.00332 g | 83% | Spin.: 0.004 g×83% |
| MoOx | 0.000002834 g | 30% | Evapor.: 0.0000094 g – (4.69g/cm3×2cm2×7nm) |
| Au | 0.00042 g | 64% | Evapor.: 0.0006516 g–(19.3g/cm3×2cm2×60nm) |

Table B.5.3 | Electricity input of industrial submicrometric NIR PeLED

| 1 Cathode deposition |  |
| --- | --- |
| Ultrasonic cleaning |  |
| Electricity for a 2 cm2 piece | 1.096 kJ (0.0003 kWh) |
| UV ozone |  |
| Electricity for a 2 cm2 piece | 0.6 kJ (0.00017 kWh) |
| 2 Hole transport layer deposition |  |
| Spin coating (ZnO) |  |
| Electricity for a 2 cm2 piece | 0.690 kJ (0.00019 kWh) |
| Spin coating (PEIE) |  |
| Electricity for a 2 cm2 piece | 0.756 kJ (0.00021 kWh) |
| Thermal annealing (PEIE) |  |
| Electricity for a 2 cm2 piece | 0.853 kJ (0.00024 kWh) |
| 3 Perovskite layer deposition |  |
| Thermal evaporation |  |
| Maximum evaporator temperature | 1800 °C |
| Evaporation melting temperature | FAPbI3 ~250 °C |
| Mean evaporator temperature utilization percentage 6.94% |  |
| Mean evaporator use factor for a 2 cm2 piece | 0.139% |
| Mean evaporator power for a 2 cm2 piece | 1.11 W |
| Cooling system mean power for a 2 cm2 piece | 4 W |
| Mean vacuum pump power for a 2 cm2 piece | 5.4 W |
| Evaporator working time | 3 min |
| Vacuum pump working time | 3 min |
| Cooling system working time | 3 min |
| Electricity for a 2 cm2 piece | 1.71 kJ (0.00048 kWh) |
| 4 ETL/anode deposition |  |
| Thermal evaporation |  |
| Electricity for a 2 cm2 piece | 10.57 kJ (0.0029 kWh) |
| 5 Encapsulation |  |
| UV radiation |  |
| Electricity for a 2 cm2 piece | 0.048 kJ (0.000013 kWh) |
| 6 Other |  |
| N2 gas glovebox atmosphere |  |
| Electricity for a 2 cm2 piece | 15.6 kJ (0.00433 kWh) |