Supporting Information

Breakthrough in Luminescence Thermometry - Supersensitive Emission Line Shift of Whispering Gallery Modes in Rhodamine B-doped Cellulose Fiber Microresonators

Przemysław Woźny,a,* Kevin Soler-Carracedo,a Małgorzata Skwierczyńska,a Inocencio R. Martin,b  Piotr Kulpiński,c Marcin Runowski a

a Faculty of Chemistry, Adam Mickiewicz University, Poznań 61-614, Poland

b Departamento de Física, Instituto de Materiales y Nanotecnología (IMN), Universidad de La Laguna, San Cristóbal de La Laguna E-38200, Santa Cruz de Tenerife, Spain

c Department of Mechanical Engineering, Informatics and Chemistry of Polymer Materials, Lodz University of Technology, Żeromskiego 116, Łódź 90-924, Poland

Figure. S1 Average displacement of the selected WGMs in heating-cooling cycles.

Figure. S2 Emission spectra measured at different temperature values with narrow WGMs and their thermal shift (a); the calculated position of the selected WGMs as a function of temperature for second cellulose fibers@Rhodamine B (b); average WGMs shift for second fiber (c).

Figure. S3 Histograms obtained based on the recorded series of 100 emission spectra, showing spectral resolution of the WGM mode at ≈629 nm (a) and the corresponding temperature values (b), calculated using calibration curve from Eq. 5, with their respective standard deviation (σ) values; the σ represents the experimental temperature resolution of the system.

Table. S1 List of maximum relative and absolute sensitivities of different WGM-based sensors.

| Max Sr (% nm K-1) |  | Max Sa (nm K-1) | Matrix | Ref. |
| --- | --- | --- | --- | --- |
| 8.4×10-2 | 4.5×10-1 |  | Cellulose fiber | This work |
| 2.0×10-3 | 1.5×10-2 |  | Silica microspheres | 1 |
| 2.0×10-3 | 1.7×10-2 |  | Oxyfluoride glass microsphere | 2 |
| 1.5×10-3 | 1.4×10-2 |  | Nd3+ doped yttria–alumina–silica (YAS) microsphere | 3 |
| 8.1×10-4 | 5.3×10-3 |  | Ho3+ doped yttria–alumina–silica (YAS) microsphere | 4 |
| 6.0×10-4 | --- |  | Silica microcavity | 5 |
| 5.3×10-4 | 8.2×10-3 |  | Silica fiber | 6 |

References

1	K. Soler-Carracedo, A. Ruiz, I. R. Martín and F. Lahoz, J. Alloys Compd., 2019, 777, 198–203.

2	F. Paz-Buclatin, S. Ríos, I. R. Martín and L. L. Martin, Opt. Mater. Express, 2019, 9, 4126.

3	D. Walo-Martín, F. Paz-Buclatin, S. Ríos, I. R. Martín, L. L. Martin, A. Ródenas, V. N. Sigaev, V. I. Savinkov and G. Y. Shakhgildyan, Appl. Sci., 2021, 11, 1117.

4	L. de Sousa-Vieira, S. Ríos, I. R. Martín, L. García-Rodríguez, V. N. Sigaev, V. I. Savinkov and G. Yu Shakhgildyan, Opt. Mater. (Amst)., 2018, 83, 207–211.

5	T. Carmon, L. Yang and K. J. Vahala, in Integrated Photonics Research and Applications/Nanophotonics for Information Systems, OSA, Washington, D.C., 2005, vol. 12, p. IWE4.

6	E. Rivera-Perez, I. L. Villegas, A. Diez, M. V. Andres, J. L. Cruz and A. Rodriguez-Cobos, IEEE Photonics Technol. Lett., 2013, 25, 2498–2500.