Platinum nanoparticles in nanobiomedicine

Deborah Pedone1,2,3, Mauro Moglianetti1,2, Elisa De Luca1,2, 
Giuseppe Bardi1, and Pier Paolo Pompa1,2*

1. Istituto Italiano di Tecnologia, Nanobiointeractions&Nanodiagnostics, Via Morego 30 – 16163 Genova, Italy

2. Istituto Italiano di Tecnologia, Nanobiointeractions&Nanodiagnostics, Center for Bio-Molecular Nanotechnologies, Via Barsanti – 73010 Arnesano (Lecce), Italy

3. University of Salento, Department of Engineering for Innovation, Via per Monteroni, Lecce, Italy

* Corresponding author: pierpaolo.pompa@iit.it

Abstract

Oxidative stress-dependent inflammatory diseases represent a major concern for the population’s health worldwide. Biocompatible nanomaterials with enzymatic properties could play a crucial role in the treatment of such pathologies. In this respect, platinum nanoparticles (PtNPs) are promising candidates, showing remarkable catalytic activity, able to reduce the presence of intracellular ROS and impair the downstream pathways leading to inflammation. This review reports a critical overview of the growing evidence revealing the anti-inflammatory ability of PtNPs and their potential applications in nanomedicine. It provides a detailed description of the wide variety of synthetic methods recently developed, with particular attention to the aspects influencing biocompatibility. Special attention is paid to the studies describing PtNP toxicological profile with the attempt to draw critical conclusions. The emerging picture suggests that the material per se is not causing cytotoxicity, while other physico-chemical features related to the synthesis and surface functionalization may play a crucial role in determining the observed impairment of cellular functions. The enzymatic activity of PtNPs is also summarized, analyzing their action against the reactive oxygen species produced by pathological conditions within cells. In particular, we extensively discuss the potential of these properties in nanomedicine to down-regulate inflammatory pathways or to be employed as diagnostic tools with colorimetric readout. A brief overview of other biomedical applications of nano-platinum is also presented.

Outline

- Introduction

- Synthesis of PtNPs

- Toxicology of PtNPs

- Enzymatic properties of PtNPs and their applications

  - PtNPs in Nanomedicine

  - PtNPs in Nanodiagnostics

- Other biomedical applications of PtNPs

  - PtNPs in Cancer therapy

  - PtNPs in Photothermal therapy and Radiotherapy

  - Antibacterial applications of PtNPs

- Conclusions and outlook

- Introduction

Catalytic nanomaterials, such as platinum, cerium, or fullerene nanoparticles, display unique surface-related physico–chemical properties and high surface area, both enabling valuable applications in several areas. In particular, the interest in platinum nanoparticles (PtNPs) is rapidly growing, as they represent novel nano-sized tools for the automotive sector, chemical industry, and production of biomedical devices.1, 2 Automotive and chemical industry aims at developing more efficient materials based on PtNPs for catalytic convertors and high-added-value chemicals. For instance, Pt-catalyzed hydrogenation reactions are used for the synthesis of fats, vitamins3 and biofuel4. Pt also plays a crucial role in other chemical reactions of industrial relevance, such as oxidation in the process of organic acids production,5 isomerization and dehydrogenation,6-9 as well as the oxidation of carbon monoxide.10 Furthermore, the request for “green technologies” enforces the increasing demand of environmentally friendly energy sources, like photochemical solar energy harvesting,11 decomposition of highly polluting aromatic compounds,12 and water treatment,13, 14 all reactions that can be improved by Pt catalytic properties. Although the high demand of this material for technological applications and luxury sector is increasing, Pt abundance in Earth’s crust is rather scarce (around 0.01 ppm). Nowadays, the highest percentage of Pt (up to 35-40%) is used in the catalytic converters, closely followed by jewelry.15 Such wide use and the foreseen demand for future applications are enormously raising its value. Pt optimization, by handling its structure at the nanoscale, can thus provide important solutions to its limited availability. Several examples are already present in the literature, showing key applications in fuel cells,16-19 gas-sensors,18, 20, 21 bio-imaging,22-26 detection of biological molecules,27-40 as well as nanomedicine.41-43

In particular, the medical field could benefit from the intrinsic catalytic properties of nanoPt, to develop or improve diagnostics and treatments. For instance, the design of a new class of synthetic nanozymes (nano-enzymes) may allow to overcome some limits of biological enzymes.44-52 Actually, PtNPs have been already proposed as efficient and selective radical scavengers for therapies of oxidative stress diseases.41-43, 53-69 However, their clinical potential has been slowed down by some toxicological concerns. Homogenous data about PtNPs biocompatibility are still missing, because of the differences in size, shape, surface coatings, and purity of the particles produced in the different laboratories/companies. Nevertheless, the use of PtNPs as additive in consumer products and cosmetics has been already approved by the Ministry of Health, Labour and Welfare of Japan.53 This suggests that PtNPs will likely register an increase in the next future in a wide range of applications, including healthcare devices, diagnostics, and cosmetics. The broad applicative potential of nanoPt and the intense ongoing research on it are well reflected by the fast increase in the number of papers published over the last decade, with more than 1400 articles in 2016 (Figure 1A). Accordingly, the number of patents is witnessing a strong upward trend, with ca. 440 patent applications in 2016 and more than 4200 patents filed in the last decade, with East-Asia (especially China, South Korea, and Japan) playing a major role (Figure 1B). Most of this literature deals with material science, chemistry and engineering, focusing on the design and synthesis of PtNPs with improved catalytic activity, specifically for particular industrial sectors. On the other hand, despite their promising features, the prospective medical use of PtNPs has not been deeply investigated. This review aims at representing a reference for healthcare and in vitro diagnostic sectors, discussing the available information on the development and biocompatibility of nanomaterials based on Pt. Special attention will be paid to PtNPs synthesis, nanobiointeractions and antioxidant activity, comprehensively describing their novelty in nanomedicine and diagnostics.

- Synthesis of PtNPs

Industrial and biomedical applications of PtNPs are strongly affected by their size, shape, elemental composition, electronic surface structure, and capping agent, pushing the researchers to develop new synthetic techniques to optimize such features2, 15, 18, 70-89 (Figure 2). The engineering of PtNPs for biomedical applications is also guided by recent data revealing that their physico-chemical properties, as well as their dispersion state and stability in biological environment, play a major role in defining their safety or toxicity. Considering the possible use of PtNPs as drug carriers and antioxidant material, a crucial challenge is the production of biocompatible PtNPs, with precisely defined properties and absence of contaminants (e.g., endotoxin, Pt precursors, toxic unreacted reagents, organic solvents, etc.) in their production.90 We will here describe several classes of synthetic methods, namely chemical, physical, and biologically assisted procedures.

Among chemical processes, Wet Chemical Reduction (WCR),71 electrochemical reduction,91-99, galvanic displacement,15, 100-102 and chemical vapor deposition103, 104 have recently gained interest in the attempt to accurately control NP chemical-physical properties. In particular, WCR is often applied in laboratory research, as it guarantees a better control on NP characteristics. WCR, which involves the use of a reducing agent to produce PtNPs from Pt precursors in solution,71 permits a strict control of shape and size, by varying the Pt compounds concentration, the temperature of the reaction,15 and the use of organic or inorganic ligands.73, 74, 105, 106 Substantial research has also been devoted to the development of WCR methods to obtaining shaped PtNPs with improved catalytic performances. Several shape-directing agents have been employed to favor the asymmetric growth of the NPs. To this aim, several polymers, surfactants and capping agents have been exploited. Multiphase synthetic setups have also been designed,107-109 such as the use of reducing agents in gas phase to achieve better control of the reaction parameters.110 The limit of this approach to produce PtNPs for nanomedicine is the use of large amounts of capping agents, surfactants, and organic solvents that could affect the toxicological profile of NPs. Moreover, their large scale production can pose environmental risks. To allow for industrial scale-up and lower the environmental impact, microwave heating and glycerol have been proposed both as reducing agent and solvent.111, 112 The use of thiol-chemistry is also often exploited to synthesize NPs with increased stability in aqueous environment or in organic media. Pt clusters with controlled size and shape were obtained and stabilized by thiol ligands, such as alkane thiols113-118 or thiols bearing polar groups.106, 119-121 These methods allow further decreasing the NP size, thus increasing the surface/volume ratio. Although thiols presence on the surface of PtNPs can decrease their catalytic performance, such chemistry could provide advantages to modulate their properties, e.g. by combining hydrophobic and hydrophilic ligands122 on the same NP to favour selective interaction with substrates and the biological environment. On the other hand, these chemicals show potential adverse effects, as aliphatic, aromatic, and amino-terminated thiols could be toxic in vitro and in vivo.123 To achieve biocompatible PtNPs, the more promising strategy is to use “green reagents”, such as ascorbic acid and sodium citrate, with strong control on solvent and reagents purity.41, 123-125 These synthetic procedures can also guarantee accurate control on size, shape, and catalytic properties, together with reasonable production yield.123 For instance, it has been recently shown that citrate-capped PtNPs show good cytocompatibility together with high antioxidant abilities.41 Furthermore, these synthetic strategies permit easy functionalization of the NP surface. This is crucial to design PtNPs for biomedical applications, as the biological identity of nanomaterials strongly depends on their exposed surface area. In this framework, as the NP surface coating was reported to affect particle toxicity and specific targeting,126, 127 biogenic syntheses using biomolecules as templates have been developed. For example, encapsulation of PtNPs within apoferritin protein was shown to improve the cellular uptake and reduce eventual membrane damage.128-131 A similar strategy was reported by Wang et al., mimicking catalytic centers inside natural enzymes, by encapsulating PtNPs within dendrimers.132 The use of dendrimers for the synthesis of small PtNPs and clusters has also been investigated.133, 134 Yamamoto et al. showed great improvement of catalytic activity of Pt clusters synthesized within dendrimers that act as template, favoring controlled growth of the nanomaterial.133

Among physical methods, laser ablation technique,135, 136 aerosol-assisted deposition,137 electron-beam-induced reduction138 and flame synthesis139, 140 have recently gained interest in the attempt to overcome some limits of the chemical procedures (e.g., toxic reagents, organic solvents, etc.). Laser ablation method exploits a high power laser beam to evaporate nanoparticles from a solid source.141 The laser beam could be applied in continuous or pulsed mode. This flexible approach is based on the control of pulses, temperature, and ambient gas pressure to achieve specific NP properties.141 The main advantage of this technique is the lack of unwanted coatings, stabilizers, and solvent contaminations that may represent an issue in nanomedicine.141 On the other hand, the mechanism of NPs production is not completely understood, and the high dilution and the difficulties in tuning the NP size, shape, and production yield are limiting their use.123, 142, 143 Also, the stability of these NPs in biological environment could raise some issues. NPs obtained by laser ablation are stable in aqueous solution in absence of stabilizers, due to electrical repulsion effects resulting from charges present on the surface of the NPs.144, 145 However, this could represent an issue in biological experiments, as aggregation and precipitation might occur when NPs are incubated in complex environments, such as cell culture media and high ionic strength solutions. Another simple physical method to produce PtNPs for several applications consists in the use of cathodic corrosion, converting a bulk alloy electrode in a suspension of NPs with the same composition.146 This latter approach has similar constraints, i.e. limited production yield and size tunability.

Bio-assisted syntheses, based on biological processes by unicellular and multicellular organisms, have been suggested as an alternative to chemical and physical methods. They offer some advantages for biomedical applications, including the absence of undesired reaction solvents. Biological syntheses have been reported mainly for noble metal nanomaterials, as they can be easily reduced by weak reducing agents.147-149 Only a few reports in the literature described the synthesis of PtNPs.150-152 Successful protocols have been developed to produce monodisperse and stable PtNPs through biosynthesis within bacteria,153-161 cyanobacteria,162, 163 seaweeds,125, 164 fungi,165-167 plants,61, 168-178 as well as by means of bio-derived products, such as aqueous honey solutions.179-181 Several manuscripts reported the reduction of Pt (IV) into PtNPs in sulphate-reducing bacteria, exploiting the activity of specific hydrogenase enzymes.155, 182 Similar to WCR, in biogenic synthesis, Pt salt and protein concentrations play an important role to control NP shape and size.183 PtNPs synthesis using fungi, such as Neurospora crassa167 and Fusarium oxysporum165, 166, 184 has been likewise reported as a valuable “scale-up” strategy. Biological synthesis of metal NPs was also performed using plant extracts171 and wood,168, 169 exploiting their phytochemical constituents as capping agents. Pt phyto-reduction biosynthesis in plants was described for the first time in 2010 by Song et al., who obtained 2-12 nm PtNPs using leaf extracts with ca. 90% yield, by using very low concentration of leaf biomass.185 Nowadays, the literature describes a diverse set of vegetable-derived products to synthesize PtNPs, such as Diopyros kaki,185 Ocimum sanctum,186 Medicago sativa, and Brassica juncea.187 Raut et al. reported a rapid protocol to produce monodisperse spherical 1-6 nm PtNPs in an aqueous medium at room temperature, using root extract of Asparagus racemosus Linn.188 The number of reports describing a variety of organism-mediated PtNP syntheses is rapidly increasing. All these protocols demonstrated several ecological, low-toxic and cost-effective routes to produce NPs, often avoiding complex laboratory setups. However, their large-scale use for nanomedicine applications could be limited by the presence of undesired contaminants, such as endotoxins and fragments of biological materials with unwanted biological activity, which require difficult, expensive, and time-consuming purification procedures. Moreover, even if bio-assisted procedures are promising, up to now they typically failed to achieve fine control on the NP properties.

In conclusion, the richness of the available methods for PtNP synthesis together with the complexity of the biological environment makes difficult to select the “universal” strategy to achieve biocompatibility, stability, and productivity, since each technique presents some advantages and drawbacks (Table 1). However, synthetic methods based on “green reagents”, such as ascorbic acid and sodium citrate, seem to be particularly promising, as they offer an accurate control of some important properties for biomedical applications, i.e. size, shape, stability, catalytic properties, and production efficiency, coupled to the possibility of post-synthesis surface functionalization.123

- Toxicology of PtNPs

Nowadays, the application of nanoPt in biomedicine is still debated, due to its unclear toxicological characterization. Despite the statement of FDA about the safety of Pt in the zero oxidation state189 and the approved use in consumer products in Japan, published results on PtNPs cytotoxicity are still conflicting and the possible harmful mechanisms are not completely understood. The toxic effect of other types of NPs is frequently characterized by the induction of oxidative stress, DNA damage, and cell cycle arrest,190-195 leading to specific organ failure.190 196 However, several data demonstrate that a significant role in cell function impairment is often played by the presence of different contaminants, like endotoxins, harmful coatings, or NP synthesis reaction by-products.90, 197-199 Although it has been proved that diverse metallic NPs release ions once inside the cell, there are no definitive data demonstrating that cell damages observed after PtNP administration could be similarly due to the release of Pt ions.200-204

In particular, several in vitro and in vivo studies showed negligible cytotoxic effects by pristine PtNPs or PtNPs coated with cell compatible materials41, 53, 55, 56, 58, 69, 124, 125, 205-207 (Figure 3). Specifically, in vitro, Horie et al. observed that 5-10 nm pristine PtNPs did not release Pt ions after incubation into culture media and did not induce cytotoxic effects, oxidative stress, or cell death in A549 and HaCaT cells up to 17.4 µg/mL.124 In agreement with these reports, we recently demonstrated that 5 and 20 nm citrate-capped PtNPs show excellent cytocompatibility in vitro, even up to 100 µg/mL. TEM images displayed that PtNPs were abundantly internalized within endosomal/lysosomal vesicles41 (Figure 4A).

Investigations focused on the role of PtNP size in cytotoxicity208-212 indicate that it could represent an important parameter affecting molecular mechanisms inside the cell, though with contradictory results. While 8 nm NPs did not show adverse effects, administration of 1 nm PtNPs to renal cells in culture induced cytotoxicity in a dose dependent manner in the same range of concentrations.210 Manikandan et al. tested NP sizes ranging from 1 to 21 nm on Neuro 2 cell line, observing that PtNPs of 5-6 nm were fully cytocompatible, whereas the other sizes induced cellular damages.208 On the other hand, Konieczny et al. observed that PVP-PtNPs of 6 nm induced a decrease of metabolic activity and genotoxic effects, even though they did not alter morphology, viability and migration capability of primary keratinocytes.211 The same authors found that 57 nm PtNPs are less harmful for keratinocytes than the smaller ones. This study did not experimentally excluded a possible role of the PVP coating in the induced toxicity nor the instability of the Pt core-coating complex, often happening with multimaterial NPs (see below). Anyway, smaller NPs presented stronger ability than 57 nm ones to produce DNA instability and metabolic dysfunction at concentration of 25 μg/mL.211 In a meticulous study, Hamasaki and colleagues did not observe cytotoxicity in a wide set of other types of adherent cells (i.e., TIG-1, HeLa, HepG2, WI-38, and MRC-5) after exposure to 1-5 nm PtNPs at concentrations as high as 50 μg/mL.206 In the same paper, the authors expanded their investigation in vivo without reporting negative effects in mice after intraperitoneal administration.206 The absence of oxidative stress and cytotoxicity, both in vitro and in vivo, was also demonstrated for differently shaped, pure 11-35 nm PtNPs up to 500 μg/mL205 (Figure 4B), emphasizing the possibility to produce specifically shaped biocompatible PtNPs. Intriguingly, the administration of PtNPs was found to decrease inflammatory cytokine production in monocytes/macrophages in vitro, suggesting that PtNPs could avoid uprising innate immune responses.213, 214 In particular, Rehman et al. described the anti-inflammatory inhibition of LPS-induced NF-kB activation in mouse macrophages, as a consequence of Akt and ERK suppressed phosphorylation by pectin coated-PtNPs.214

Some studies focused on the role of different coatings as well as the generation of Pt ions as consequence of NP endocytosis in the acidic endosome/lysosome compartments, followed by the degradation of the particles.25, 26, 88, 170, 200-202, 215-232 For instance, high concentrations (80 and 160 µg/mL) of 5-8 nm PtNPs covered by PVA cause mild toxicity after 72 hours.201 Polymer coated-PtNPs were observed in the cytoplasm and in cellular vesicles, and their internalization was correlated to ROS overproduction, DNA damage, and cell division termination. The authors proposed a possible combined effect of NPs and Pt2+ ions in ROS overproduction and DNA damage. However, the fate of Pt ions released within the cells from potential NPs dissolution was not confirmed and the impact of the different coating was not clarified. Coated-PtNP cytotoxicity mechanism should be deeply investigated considering all the components of the particles and their own specific cell interaction mechanism. For instance, folic acid-capped PtNPs were found to be more cytotoxic on two cancer cell lines in comparison to PVP capped-PtNPs. This is due to the increased interaction of NPs with the folic acid receptor, highly expressed in these cell lines, followed by receptor-mediated endocytosis222 (Figure 4C,D,E). Further observations supporting Pt2+ ions role in the induced toxicity derive from studies on human colon carcinoma cells exposed to particle of different sizes (from 20 to 100 nm) deposited on a β-cyclodextrin matrix.203, 204 The authors observed that PtNPs do not cause toxicity, though DNA damage was detected. They suggested that DNA strand-breaks are caused by the direct interaction between DNA and soluble Pt2+ ions. They also commented that PtNP cytotoxicity observed in the study conducted by Asharani et al. was due to the small particle size and the high concentration used, which increased the release of Pt2+ ions.203, 204 In view of PtNP systemic administration, PVA-capped PtNP biointeractions were also tested with human red blood cells,233 describing a good degree of biocompatibility, though with some alteration in membrane topography. Other studies134, 231 involving polymer-PtNPs were performed with very small, dendrimer-encapsulated PtNPs of 1 nm, showing toxicity only upon oxidation or aging step. The explanation of such behavior is not completely clear, though the oxidation of the Pt atoms on the NP surface after their exposure to air was considered responsible for the release of toxic ions.

The release of Pt ions as a mechanism of cytotoxicity and cellular damage was also described in the case of multimaterial-PtNPs.200 However, the correlation between cell death and its causes is of difficult interpretation, due to the involvement of several materials, structures (alloys, core-shell, heterodimers, heterotrimers, etc.) and the nature of their bio-nano interaction. Given the complexity of these nanomaterials and the number and diversity of the physico-chemical properties involved, it is very challenging to distinguish the single material contribution to the observed toxic effects, and even more the mechanisms behind them. As an example, mitochondrial and nucleic DNA damage, causing apoptotic death of HeLa cells, was related to Pt ions release by multicomponent 2 nm FePt@CoS2 yolk-shell NPs.200 However, the adverse effects of released Fe ions and multimaterial debris on the cytotoxicity induced by these nanocrystals should be also taken into consideration, as they can play a major role in cell damaging. These data suggest the idea that pure PtNPs or PtNPs coated with non-toxic molecules show high degree of cytocompatibility, at least in vitro. Multimaterial NPs may decrease their stability in the acidic lysosomal environment producing harmful particle degradation. The purity of the used PtNPs is often underestimated, increasing the contradiction in the outcomes.

Several studies examined the effects of different PtNPs in vivo.53, 54, 56-61, 202, 205, 207, 209, 210, 221, 228, 234-241 Toxicological research in the entire organisms, especially in the vertebrates, is conditioned by the diverse experimental parameters and analyzed tissues. The chosen routes of administration (i.e. oral, intra-venous, sub-dermal, etc.) to release the NPs can dramatically change the starting concentration once at the target. Furthermore, the adsorption of small molecules, proteins, sugars and lipids encountered in the biological fluids determines the NP coating, finally regulating the targeting and the interaction with the immune system. Species specificity, sex, age, pathological and hormonal state of the animal must be also considered to interpret the outcomes. For example, to understand the impact of PtNPs through the generations, PVA-PtNPs of 20 nm were tested in mice by oral administration up to 1 mg/kg, during premating, gestation, lactation periods, and postnatal development of the pups. PtNPs were detected in the lungs of the mothers at 0.5 and 1 mg/kg but not in the body of pups, likely due to their inability to pass the placenta-barrier. It was also demonstrated that PtNPs increase pup mortality during lactation period and decrease the infant growth rate of mouse pups.221 On the other hand, Prasek et al. demonstrated that PtNPs of 2-19 nm did not show any adverse or mutagenic effects on the chicken embryogenesis and did not affect liver functionality and brain morphology, at concentrations ranging from 1 to 20 μg/mL (0.3 mL per egg). This latter work specified that PtNPs did not influence the growth and development of embryos.235 However, they observed signs of mitochondria deformation and apoptosis in brain cells. Evidences of PtNP biocompatibility during embryogenesis are also supported by the experiments of Asharani et al. with zebrafish.234 The exposure to PVA-PtNPs of 3-10 nm at concentrations up to 100 μg/mL did not cause toxic effects on growth and development, as embryos maintained normal phenotypic development and mortality rate.

Many other in vivo reports described the safety profile of PtNPs as they are applied in nanomedicine as antioxidants. On the contrary, different in vivo experiments showed that intratracheal instillation of 21 nm PtNPs may provoke inflammatory responses associated to time-dependent decrease of antioxidant molecules221 emphasizing the difficulties to evaluate the immune responses of whole organisms. Mice treated with 1 nm PtNPs suffered acute and chronic nephrotoxicity, but no sign of toxicity was present in the other examined tissues (heart, lung, spleen, liver). Akin to in vitro data, 8 nm PtNPs did not show negative effects on any tissue, showing a safe biocompatibility profile.209

As previously mentioned, the surface properties of nanomaterials, along with protein corona effects, govern the interactions with tissues and cells, significantly influencing their fate. NPs coating/functionalization/corona interact with numerous protein receptors exposed on the cell membrane, modulating the efficacy of NP internalization.131, 220, 222 The high heterogeneity of PtNP synthetic methods, sizes, shapes, coatings, purity, cell types used for toxicity assessments, and the variability of experimental conditions make a clear picture of the toxic profile of PtNPs difficult. It is worth to stress that the presence of potential contaminants in solution,90, 198, 199 such as reaction by-products, endotoxins, and Pt ions, could play a considerable role in the cellular toxicity of PtNP preparations. Therefore, also according to the general guidelines of the National Cancer Institute’s Nanotechnology Characterization Laboratory (NCL),90 we would like to recommend the following procedures to achieve safe and biocompatible PtNP preparations:

- Complete batch-to-batch physico-chemical assessment of NP properties, in particular in complex environment like cell culture media (size distribution, stability, zeta potential, aggregation state, protein corona formation).

- Extensive purification procedures, crucial to minimizing the presence of pathogenic spores or bioactive molecules, like bacterial toxins, that can easily overcome the beneficial effects of the pure material and the green coatings.

- Assessment of the toxicological effect of each reagent, including the solvent of the PtNPs (e.g., after NPs precipitation).

- Control of the absence of endotoxin and bacterial contamination (i.e. by LAL test)

- Evaluation of the toxicity of the coating materials per se.

- Enzymatic properties of PtNPs and their applications

Catalytic properties of materials are crucial in many technologies. The design of new nanocatalysts with tailored properties can enhance the efficiency and selectivity of chemical conversion processes. Breakthroughs in catalysis may have a huge impact in easing the process as well as the energy requirements for separation and purification of fossil raw materials and reducing the chemical waste.9 In the latest years, the massive research devoted to nanotechnology has revolutionized this field, thanks to the rational design and manipulation of catalysts at the nanometer scale.9 The peculiar properties of metal NPs, such as the large surface-to-volume ratio and high surface energy, are improving many industrial processes involving catalysis.242 Furthermore, the possibility to produce medical nanotools in standardized biocompatible compositions can pave the way to promising applications in nanomedicine. Encouraging results are coming from the development of enzymes based on NPs, called nanozymes.44-52, 243 The major goal of this research field is the design of specific, efficient, highly selective, and environment-insensitive nanozymes able to mimic natural enzyme functions. Although a direct comparison between artificial NPs and naturally occurring enzymes, composed of proteins and RNAs, could be considered inappropriate, their size similarity and ability to accomplish similar tasks make artificial NPs ideal candidates to replace compromised enzymes in several diseases.44-46

An important class of enzymes under intense nanotechnological investigation is the one devoted to the control of reactive oxygen species (ROS) homeostasis, including hydrogen peroxide (H2O2), superoxide anions (O2-), hydroxyl radicals (OH), and hyperchlorous acid.244, 245 ROS are a class of molecules produced by metabolic pathways and normally used by cells as signaling and defense systems.244, 245 Intracellular ROS levels are mainly regulated by glutathione peroxidase (HRP), superoxide dismutase (SOD), catalase (CAT), and small non-enzymatic molecules like glutathione.246 However, the abnormal activation or interruption of some steps in these pathways leads to the oxidative stress condition, a cellular state in which the presence of oxidants overcome the balancing antioxidants.246 As a result, inflammation is triggered, and several human pathologies, like diabetes, cardiovascular and neurodegenerative diseases, can progress.244, 245 Fullerene, metal and metal oxide NPs have been suggested as antioxidant enzyme-mimetic nanomaterials, scavenging ROS in biological systems.44-47, 50, 247-256 Among these, PtNPs have attracted particular interest41-43, 53-61, 63-69, 126, 238-241, 254, 255, 257-262 owing to their high efficiency and selectivity as artificial CAT, HRP and SOD enzymes41, 128, 129, 263-265 (Figure 5). In particular, PtNPs are able to catalyze the reduction of H2O2 into water and molecular oxygen acting as the biological enzyme CAT, or to promote the oxidation of a reduced substrate in order to decompose H2O2 to water, as HRP mimics. They are also able to act as the natural SOD, catalyzing the dismutation of O2-  into molecular oxygen and H2O2 (Figure 6).

The ability of PtNPs to quench H2O2 and O2-, acting as artificial enzymes, was reported for the first time by Kajita et al. with 3-10 nm bimetallic alloy-structured Au/PtNPs stabilized with citrate and pectin. By spectrophotometric methods and the Spin-Trapping technique, they demonstrated, by varying the Pt-to-Au molar ratio from 0 to 100%, that the quenching ability of NPs against H2O2 and O2- increased as a function of the Pt concentration. In particular, they did not report scavenging activities for AuNPs. The mechanism of ROS quenching was not fully discussed by the authors.266 PtNPs could also mimic the mitochondrial complex I NADH ubiquinone oxidoreductase,267 possessing catechol oxidase-like activity268 and the ability to suppress lipid peroxidation.63, 269 It has been recently demonstrated that 3 nm Au@PtNPs show polyphenol oxidase (PPO) activity, exhibiting higher affinity for PPO substrates than the natural enzyme.270 Moreover, PtNPs were reported to have specific ascorbate oxidase-like activity.271, 272 As an interesting feature for diagnostic purposes, PtNPs are able to oxidize chromogenic substrates (HRP-like), such as 3,3’,5,5’-tetramethylbenzidine (TMB) or 3,3'-diaminobenzidine (DAB), in presence of H2O2,129, 263, 273-277 catalyzing the reaction between H2O2-derived OH radicals adsorbed on their surface and the substrate.274, 276, 278 Recent studies revealed that the peroxidase and catalase mimetic activities of PtNPs are dependent on the particle diameter276 and shape,263 and could be affected by protein shells275, 279-281 or environmental pH.132, 274, 282-284 Moreover, they can be selectively modulated in a concentration-dependent way by typical inhibitors of natural enzymes, such as 3-amino-1,2,4-triazole, NaN3 and Hg2+, which can be probably adsorbed on the surface of NPs.276, 285, 286

The analysis of the kinetic reaction parameters revealed that PtNPs are active over a broad range of pH and temperature. PtNPs efficiency is maintained at extreme concentrations of H2O2, which would inhibit the native HRP and CAT. Higher affinity to TMB compared to the biological enzyme has also been shown, likely enhanced by the large NP surface area.129, 275, 287, 288 Overall, the recent results about the radical quenching ability of PtNPs clearly show their great potential in nanomedicine, as scavengers in oxidative stress related diseases, or their promising use as artificial enzymes in nanodiagnostics.

4.1 PtNPs in Nanomedicine

As mentioned above, PtNPs are promising candidates as nanozymes for the treatment of oxidative-stress related diseases, due to their ability to act as artificial CAT, HRP and SOD enzymes (Figure 6). Recent results with fullerene and cerium oxide NPs on models of autoimmune and neurodegenerative diseases, diabetes, endometriosis, and ischemia have pushed the research towards the realization of efficient nanozymes.44, 45, 247-252, 255, 289-292 In this framework, PtNPs are showing safe applications to several human pathologies, as demonstrated in recently published works.41-43, 53-61, 63, 64, 66-69, 126, 238-241, 255, 257-262, 293, 294 Differently from other metal nanoparticles,193 PtNPs possess high stability in acidic cellular vesicle environments, forecasting cytocompatibility and tolerance in vivo.

In vitro enzyme-like properties of PtNPs suggest a wide field of application in nanomedicine, even hypothesizing PtNP use as preventive therapy for some type of cancer and cardiovascular diseases.42 Several studies demonstrated that the scavenging abilities of PtNPs are maintained in cellular environment,62, 63, 254, 294-296 since PtNPs are able to protect cells from ROS-induced death after exposure to UV-A,206 X-rays,259 or ultrasound.261 Very recently, PtNPs embedded in dendrimers were described as peroxidase and catalase-mimetic enzymes,132, 284 while PtNPs encapsulated within the cavity of apoferritin were reported to show peroxide- and superoxide-quenching activities both in cell-free solution and within cells, reducing H2O2-induced apoptotic cell death in a concentration-dependent way. The combined action of apoferritin encapsulating PtNPs improved their antioxidant properties, exploiting cell target specificity by apoferritin receptor-mediated internalization.128 In comparison to cerium oxide NPs, the antioxidant activity of PtNPs was demonstrated to be more efficient, by evaluating apoptosis prevention in HT-1080 human breast fibrosarcoma cells exposed to 200 μM H2O2. This result is likely due to PtNP chemical stability and resistance to aggregation, despite their lower SOD activity in vitro.55 Likewise, it was reported in vivo that 1-2 nm PVP-PtNPs are able to extend the lifespan of the short-lived mutant nematode Caenorhabditis elegans, affected by high level of oxidative stress. The effect of the nanomaterial was more pronounced than that obtained with EUK-8, a well-known SOD/catalase mimetic, used in the same range of concentrations238-241 (Figure 7). Furthermore, 2 nm polyacrylic acid coated-PtNPs demonstrated therapeutic effects on pulmonary inflammation in mice exposed to cigarettes smoke. PtNPs nasal administration prevented ROS-induced NF-kB phosphorylation, neutrophil activation, resulting in protection of pulmonary epithelial cells, as demonstrated by in vitro experiments on A549 cells.53

An important translational medicine application of PtNPs might be the protection of keratinocytes from ROS-induced apoptosis, upon UV irradiation.54 The topical application of PtNPs-based gel protected model mice of a photosensitivity dermatitis against UVA-induced skin damage.54 The development of PtNP-based dermal formulations could have great impact on the medical and cosmetic market.

The administration of 2–3 nm PtNPs in mice exerted neuroprotective effects, after transient middle cerebral artery occlusion, as well as after exposure to a thrombolytic agent, with the reduction of the infarct volume in the cerebral cortex. Furthermore, PtNP-mediated inhibition of matrix metalloproteinases seems to be crucial for the motor function improvement. Antioxidant and neuro-rescue activities on zebrafish model of Parkinson’s disease were obtained with Bacopa monnieri phytochemicals coated PtNPs.61 A possible novel application of PtNPs as alternative therapy for osteoporosis has also been proposed in the ovariectomy-induced bone loss, relying on the intragastric administration of the NPs.56, 58

The high oxygen affinity and antioxidant action shown by HSA-PtNP complexes let foresee new developments for oxygen transportation in the blood. This perspective has been described as an alternative material to red blood cells (RBCs) for transfusion in some clinical pathologies.42 Moreover, synergistic scavenging effect of PtNPs of 2-4 nm with small antioxidant molecules, such as 2-amino-6-mercaptopurine, 3-amino-1,2,4-triazole-5-thiol and 2-mercap-toimidazole used as capping agents has been demonstrated. On a blood vessel-mimicking microfluidic chip, it was shown that low concentrations of PtNPs (2 μg/mL) are able to reduce ROS overproduction induced by glucose, angiotensin, and cholesterol treatments in endothelial cells. These results suggest the potential use of PtNPs as antioxidant drug for the treatment of vascular diseases, such as atherosclerosis.68 Other uses of PtNPs as nano-drugs have been proposed for scavenging ROS in hepatic Kupffer cells, preventing hepatic ischemia,60 or to inhibit heat-induced apoptosis in human lymphoma U937 and HH cells.69 Recently, the use of citrate-capped PtNPs as radical scavenging materials was described in a cellular model of Cerebral Cavernous Malformation, a rare cerebrovascular oxidative stress-related disease. Low concentrations of PtNPs were demonstrated to completely restore the cellular physiological homeostasis in 48 hours of treatment,41 giving the hope for new approaches to rare diseases.

4.2 PtNPs in Nanodiagnostics

Other properties of PtNPs have attracted attention in recent years for biomedical applications. For instance, fluorescent Pt nanoclusters have been successfully synthesized as novel biocompatible bioimaging probes for diagnostic purposes.22, 84, 86, 297, 298 Moreover, a really interesting approach relies on the use of Pt nanomaterial as part of catalytic nanomotors to build-up molecular machines and motion-based detection methods. For instance, the motion of chemically powered nanomotors based on bisegment Au-Pt nanowires has been recently exploited to detect silver ions, DNA and ribosomal RNA, opening the way to new concepts in diagnostics (Figure 8).299-307

On the other hand, several assays exploit oxidoreductase reactions catalyzed by HRP and CAT, with colorimetric or fluorometric readout, for the detection of several target molecules of biomedical, environmental, or chemical interest. However, the high cost of enzyme isolation and purification, associated with their significant sensitivity to proteases and pH/temperature variations, pushed the research towards the development of artificial substitutes of HRP and CAT.44-52 In this framework, PtNPs emerged as ideal candidates as enzyme alternatives in diagnostic assays.28, 29, 308 PtNPs present many advantages, including easy and cost-effective production and purification, stability, resistance to proteases, high catalytic activity even at extreme pH and temperature, and affinity to peroxidase substrates. For instance, it has been reported that the affinity of DNA-stabilized PtNPs to TMB is 8 times higher compared to that of natural HRP enzyme.287 The potential of PtNPs in bioassays was already described by Gill et al. more than 10 years ago. They proposed an assay for protein detection, exploiting the chemiluminescent reaction of luminol with H2O2 catalyzed by aptamer-PtNP complexes309 and an amperometric biosensor for the detection of thrombin.310 Later, many PtNP-based colorimetric assays have been developed,284, 308, 311-319 including detection of DNA,310, 320-323 cancer cells,28, 129, 277, 324 tumor markers,29, 325-327 metal ions,286, 328-332 penicillin antibiotics,333 drugs,334 hydrogen peroxide,281, 335-340 glucose,271, 281, 283, 284, 338, 340-346 cholesterol,271, 347 L-cysteine,348-350 choline and acetylcholine,351 proteins,310, 352-356 viruses,357, 358 bacteria,359, 360 and antibodies.27, 309, 361, 362 Irregularly shaped PtNPs labeled with anti-RIgG antibodies were shown to act as HRP-like mimics in an Enzyme-Linked Immunosorbent Assays (ELISA) for the colorimetric detection of rabbit IgG, using TMB and H2O2 as substrates362 (Figure 9A). The oxidase, catalase, and peroxidase mimetic activities of Au nanorods coated with Pt nanodots were used by He et al. to develop an ELISA for the detection of mouse interleukin 2, in presence of HRP substrates (TMB and OPD) and oxygen or H2O2361. The CAT-like activity of PtNPs was also exploited in combination with a V-chip platform to detect cancer biomarkers on the cell surface and in serum.29 Moreover, folic acid functionalized PtNPs on graphene oxide nanosheets have been proposed as a naked-eye colorimetric assay for the detection of cancer cells.324 A highly sensitive and selective glucose colorimetric biosensor, based on glucose oxidase and Pt–DNA complexes adsorbed on disposable PVDF membranes, was proposed by Chen et al. The glucose detection was based on the production of H2O2 by the glucose oxidation and the consequent Pt-DNA catalyzed TMB oxidation.338 The peroxidase-like activity of polyammidoamine dendrimer PtNPs conjugated with glucose oxidase was also used to develop a sensitive colorimetric detection for glucose.284

Applied biomedical research was also focused on developing more versatile tools based on multi-component systems. Clinical attention has been paid to nanohybrids consisting of Fe3O4 magnetic NPs and PtNPs immobilized on the surface of graphene oxide aimed at rapid TMB-based colorimetric detection of breast cancer cells28 (Figure 9B). Moreover, a simple label-free DNA detection method was proposed by Wang et al.,321 encapsulating PtNPs into mesoporous silica matrix (mSiO2). In particular, the hybridization between a target DNA and ss-DNA probe electrostatically adsorbed on the surface of mSiO2 promoted the release of the probes, switching mSiO2 from a “close gate” to an “open gate” state. This resulted in an efficient oxidation of TMB by PtNPs, through the silica pores, with a clear color change of the solution. A similar method was recently proposed also by Sun et al. as the first colorimetric assay for the quantitative detection of biothiols in biological fluids308 (Figure 9C). For the food sector, a highly sensitive, naked-eye colorimetric method for the detection of Escherichia coli was also proposed by Su et al., exploiting the TMB oxidation catalyzed by 4-mercaptophenylboronic acid-functioned Au@Pt nanoparticles359 (Figure 9D).

Considering the environmental impact of mercury and the need of simple methods to detect it, several attempts to develop reliable sensors, based on PtNPs, have been made. As PtNPs catalytic activity can be inhibited by Hg2+,276, 285, 286 Tseng et al. developed a biosensor for the detection of mercury ions in aqueous solution, based on the Au/PtNPs-catalyzed conversion of an uncolored substrate into a colored one. The interaction of Hg2+ ions with the surface of Pt/AuNPs switches the enzymatic activity of PtNPs from peroxidase-like to catalase-like, inhibiting the production of the fluorophore328 (Figure 9E). A similar mechanism was exploited for detecting Hg2+ using TMB and BSA embedded PtNPs, showing high selectivity and sensitivity.330

Overall, the engineering of PtNPs and the detailed study of their mechanism of interactions with biological systems may have a huge impact for the development of novel and simple point-of-care systems for the detection of environmental pollutants or biomarkers in complex diseases.

- Other biomedical applications of PtNPs

5.1 PtNPs in Cancer therapy

Pt-based compounds with a defined geometrical distribution of the ligands around the Pt atom are among the most important drugs currently available to treat several types of cancers. The reference agent in this area is cisplatin, which exerts its cytotoxic effect by selectively binding the N7 atom of purine bases in DNA,363, 364 with the formation of a DNA-platinum adduct that distorts the structure of DNA duplex, impairing its replication and transcription. Such toxicity mechanism was proved to be specifically driven by the ligands geometry (i.e. the cis-conformation), and strong efforts have been devoted to find analogues of cisplatin with lower side effects and improved efficacy.365-367 In this stream of research, in some reports, Pt nanomaterials have been associated to cisplatin and studied as possible alternative for anticancer treatment.25, 88, 127, 134, 164, 200, 202, 218, 224, 225, 227, 229, 231, 368-376 Basing their research on the studies showing PtNPs cytotoxicity, in fact, several groups have tried to develop a nanoparticulate chemotherapeutic agent. However, as highlighted in the toxicological section, the lack of clarity in the data on PtNPs cytotoxicity and related mechanisms has strongly limited this field. A few in vivo studies, based on commercial Pt nanomaterials with high level of polydispersity and lack of data on presence of endotoxins and contaminants, have shown toxic effects on embryos. In particular, the effects on brain embryo growth of 2-19 nm PtNPs at concentrations up to 20 μg/mL have been investigated.235 The ability to activate cellular apoptosis together with the ability to cross the blood brain barrier suggested the use of PtNPs in brain cancer therapy.235 The efficacy of PtNPs as anticancer agent was compared to that of cisplatin by Kutwin et al. on chicken embryo RBCs. Spherical PtNPs of 2-19 nm were able to induce cell cycle arrest, membrane deformations (formation of knizocytes and echinocytes) and hemolysis at lower concentrations than cisplatin.229 In a later work from the same group, the anticancer activities of PtNPs and cisplatin were compared in U87 glioma cell line and glioblastoma multiforme tumor. It was observed that PtNPs induce apoptotic cell death of U87 cells, through mitochondria degradation, vacuoles formation, and up-regulation of caspase-3 and p53 gene levels, at a higher level than those treated with cisplatin. Also in vivo (in ovo U87 tumor model), PtNPs showed antitumor properties, reducing the weight and volume of tumor after 2 days.202

To improve the toxic performance of PtNPs, some researchers have tried to introduce a second material, inducing critical changes in the physico-chemical properties of NPs to increase their dissolution within cells. In the case of bimetallic NPs, the release of Pt ions could become relevant, as the strength of Pt-Pt bond may be weakened by the presence of another metallic ion, favoring the acidic degradation of the material.25, 26, 170, 200, 224-226 FePt@CoS2 yolk-shell nanocrystals were reported to release Pt ions in cellular environment as a consequence of FePt core dissolution, causing time-dependent apoptosis in HeLa cells.200 However, the role of Fe ions was not investigated in these studies. Also Lopez et al. proposed new nanostructures based on TiO2 and SiO2 containing 3-4% of Pt in the form of NPs for local cancer therapy. They observed a decrease in tumor size, weight and aggressiveness in the experimental model of C6 brain tumors, correlated to the release of toxic ions.224, 225

The use of PtNPs embedded in an in-situ cross-linkable hyaluronic acid gel was investigated for applications in intraperitoneal chemotherapy.223 The release of PtNPs in the tumor site was attenuated by the presence of hyaluronic acid carboxyl groups complexed with Pt. After 3 days, the authors suggested that all Pt ions were released from the PtNPs hybrid system, showing cytotoxic effects, probably due to the combined degradation of hyaluronic acid and Pt ions release.223

As previously mentioned, NPs functionalization can modulate their internalization and facilitate intracellular mechanisms interference by the NPs. In many reports, folic acid was used as NPs capping and cell-internalization agent220, 222, 377 as several types of cancer cells overexpress folate receptor.378, 379 The presence of folic acid on PtNPs of 10-15 nm causes higher cytotoxicity than PVP-PtNPs on MCF7 breast cancer cells, probably due to increased receptor-mediated endocytosis.222 The possible use of 2-3 nm PtNPs stabilized with folic acid in cancer treatment protocols was foreseen, considering their higher specificity for keratinocytes and mammary breast cancer cells.220 However, the mechanism of cytotoxicity has never been proved, despite the speculation about Pt ions release and Pt-DNA adducts formation. This is a crucial point, as many papers clearly showed, e.g by electron microscopy, PtNPs confinement in endo-lysosomal vesicles. To further prove the key role of the coating in cancer therapy, the functionalization of bimetallic NPs was exploited by Xu et al. to develop a new anticancer drug, based on cubic FePtNPs coated with LHRH peptide. The higher uptake of these NPs, due to the overexpression of LHRH receptors, combined with the acidic pH of tumor cells induces the release of Fe and Pt ions. Only Fe ions were related to toxicity by causing the production of hydroxyl radicals by the Fenton reaction, leading to oxidative stress-induced cell death.88 Lipophilic FePtNPs of 3 nm coated with oleic acid/oleylamine were used by Sun et al. to suppress the proliferation of three different glioma cell lines. These multimaterial NPs resulted to be more efficient to stop the cell growth than hydrophilic cysteine-capped FePtNPs. The capping agent was supposed to be essential for the intracellular NP stability, leading to different toxicity profiles, independent of the amount of NPs uptaken by the cells.227

Despite some in vitro and in vivo reports of PtNPs anticancer ability, further studies are required to assess the role of the pristine NPs and the contribution of the ions and coatings to the chemotherapeutic effect, as well as the purity and polydispersity of the NP preparation and other elements included in the NP complex.

5.2 PtNPs in photothermal therapy and radiotherapy

Due to the toxic side effects of anticancer chemotherapies, medical researchers are developing more efficient and site-specific treatments against malignant tumors. Among them, Photothermal Therapy (PTT) is a non-invasive treatment based on the use of NP plasmonic effect to locally increase the cellular temperature upon irradiation, causing DNA and RNA damage, protein denaturation, membrane rupture, eventually leading to cancer cells death.380, 381 In this context, research efforts were mainly focused on carbon nanotubes, graphene, copper sulfide NPs, and noble metal NPs (i.e. gold nanoshells, nanocages, and nanorods), able to absorb NIR laser light and to dissipate it into heat. In principle, cytocompatibility and catalytic characteristics of PtNPs could be combined to develop novel tools for PTT. However, the plasmon resonance of this material lies in the UV region,382, 383 so that its efficiency is expected to be significantly lower than that of other metal nanostructures mentioned above. Nonetheless, few reports suggested the possible application of PtNPs in this field.23, 24, 208, 384-387 Manikandan et al. analyzed the optimal PtNP dimensions to be used in PTT and demonstrated that PVP-PtNPs photo-toxicity was related to the particle size. They found that 5-6 nm PtNPs have minor or non-toxic effects themselves, but they are able to cause cell death once irradiated by near-IR laser. The procedure could generate an increase of 9 °C in cellular compartments.208 Also clusters of ca. 1 nm in size were demonstrated to be effective in causing cancer cells death after the exposure to NIR laser.23 The optical properties of bimetallic FePtNPs have also been exploited to perform PTT of solid tumors. 12 nm folate-functionalized 3-mercaptopropionic acid FePtNPs with a cubic shape, excited by NIR laser, elicited intracellular damage proportional to NPs number, causing necrosis of cancer cells similarly to Au nanorods384 (Figure 10). This result was observed even though the absorption intensity at 800 nm of FePtNPs is five-fold lower than that of AuNRs, as shown in the paper. Recently, the use of biocompatible 13 nm trifolium-like PtNPs (TPNs) has been investigated as possible new photothermal agent. Cancer cells death was achieved after 4 h incubation with TPNs, followed by irradiation with an 808 nm NIR laser for 5 minutes. Similar results were obtained in vivo on a bone metastasis tumor model with a clear reduction in osteolysis and tumor growth.385

A promising area of research involves the amplification of radiotherapy through the presence of high atomic number NPs in the tumor site. Noble metal NPs have been extensively investigated as radiosensitizers,388-393 i.e. materials able to enhance the efficacy of radiotherapy by increased absorption of ionizing radiation energy, or X-ray contrast agents.394-396 PtNPs could thus play a role in such applications, based on their high atomic number (78). However, there are only few reports present in the literature to date based on nanoPt.397-400 Proton therapy was investigated by Porcel et al. with 3 nm Poly(acrylic acid) (PAA)-PtNPs,400 obtaining results comparable to those found with 5 nm AuNPs exposed to X-rays.401 It was observed that the carbon ion irradiation on plasmid DNA, previously loaded with PtNPs, was able to cause a number of DNA breaks proportional to the NPs dose. The reason of this effect lies on the auto-amplification of electronic cascades generated inside NPs able to augment the hydroxyl radicals production and, hence, DNA damages consequent to double-strand breaks.400

Overall, PtNPs have shown to be possible candidates for PTT and radiotherapy, as they are able to induce cellular damages in selective area, following laser irradiation or radiation exposure. However, more studies are needed to better understand the full potential of this nanomaterial in this expanding area of research in comparison with other noble metal NPs.

5.3 Antibacterial applications of PtNPs

The development of new bactericidal agents is one of the greatest challenges in the scientific community, considering the growing concern about bacterial resistance to antibiotics. Metallic NPs could play a role in this field. Several NPs, such as Ag, Pd, Au, Cu, ZnO and TiO2, have shown promising results,402 but their therapeutic use is limited by undesired side effects in vivo. Although the antimicrobial activities of Pt ions on Escherichia coli have been described since 1965,403-405 antibacterial activity of PtNPs has been poorly explored. However, their enzyme mimetic activity could be exploited to induce intracellular iperproduction of ATP, causing bacterial growth inhibition, DNA damage, and bacteriotoxic effects.406 Indeed, it has been recently hypothesized that antibacterial effect of PtNPs is due to their ability to increase ATP levels, causing the overexpression of a kinase responsible for the bacteria growth arrest. It has been also suggested that PtNPs could inhibit the synthesis of ATP-dependent proteins leading to increased ATP levels, as  human immune system and the antibiotic chloramphenicol act against pathogens.406

Up to now, few publications have shown PtNP antibacterial properties,173, 174, 200, 207, 211, 406-412 which have been reported to be size and surface chemistry dependent. Gopal et al. investigated the antibacterial properties of differently shaped PVP-PtNPs with sizes ranging from 1 to 20 nm on P. aeruginosa. They found significant bacterio-toxic properties with the smaller 1-3 nm PtNPs, independently of their shape, even at low concentration (8.5 μg/mL). TEM analysis confirmed that NP size plays a major role, since larger PtNPs (>5 nm) only interact with cell membranes, whilst smaller ones were reported to enter bacteria.410 Size-dependent toxicity of PtNPs was further demonstrated by using PVP-PtNPs of 6 and 57 nm against Gram-negative (E. coli) and Gram-positive (S. aureus) bacteria.211 It was observed that smaller PtNPs were effective in promoting growth inhibition at lower doses only on Gram-negative bacteria, in line with previous reports with AgNPs.413 This effect can be likely ascribed to the thin peptidoglycan layer of the Gram-negative cell wall, which allows the penetration of Pt ions/nanoclusters inside microorganisms.211 Another relevant factor modulating the antibacterial effect of PtNPs is their surface chemistry. PtNPs with zeta potential values more negative than those of the membrane potential of bacterial cells were reported to show cell-damaging properties, inducing the rupture of both membrane and cellular wall, with consequent release of cytoplasmatic content.409 A systematic study on pectin-capped PtNPs (2 to 5 nm) showed toxicity against Gram positive (B. subtilis, S. aureus) and Gram negative (P. aeruginosa, E. coli) bacteria, demonstrating a clear toxic effects both in vitro and in vivo. The mechanism of PtNPs action in vitro was correlated to ROS overproduction and bacterial membrane disruption. The antibacterial activity of PtNPs in vivo was demonstrated using adult zebrafish animal model. At the concentration used, PtNPs were found to be not toxic to the animal, while showing the ability to inhibit bacterial proliferation and completely rescue the bacterial infection. Overall, this study demonstrated that PtNPs are safe to zebrafish cells, and have antimicrobial properties able to eradicate bacterial infections.207

Despite these results, PtNP antibacterial properties and the mechanism of action are still matters of debate. A recent report showed that bimetallic AuPtNPs are potent antibacterial agents, contrarily to pure Au and Pt NPs. The mechanism of toxicity was related to increased intracellular ATP levels and to enzyme mimetic activity of AuPtNPs rather than to oxidative stress and disruption of cell membrane.406 Considering the microorganism ability to move in precise regions of the body and survive in intracellular environment, metal NPs could be engineered to develop new drug delivery systems. In particular, exploiting the wide variety of possible surface functionalizations, the construction of PtNP-bacteria vehicles was proposed as promising system able to transport drugs to specific targets in the body.411, 414

- Conclusions and outlook

Pt-based nanomaterials are key players in many realms of science and technology. In particular, as discussed in the previous sections, they are promising candidates in biomedical applications, integrating the functions of nanocarriers and nanozymes. In point-of-care diagnostic technology, PtNPs can be used as artificial enzymes to replace expensive and sensitive peroxidase and catalase in new colorimetric and fluorometric biosensors, and to develop novel naked-eye diagnostic approaches. This is a particularly interesting field, since the very high catalytic efficiency of nanoPt combined to their stability in a wide range of conditions (including pH and temperature) can lead to the development of ultrasensitive, low-cost, and portable tests, which can be stored for months at room temperature and performed outside specialized laboratories, with no temperature control or instrumental requirements. In nanomedicine, PtNPs can be useful for combination therapy in the treatment of complex diseases caused by the accumulation of intracellular ROS. By exploiting NP versatile surface functionalization with their intrinsic antioxidant property, PtNPs can be used to produce multifunctional nanoformulations with ROS scavenging properties. Moreover, it may be envisioned that PtNPs could be further engineered to replace damaged proteins in defective molecular pathways leading to diseases. Interestingly, several reports have shown the higher potential of PtNPs compared to other nanozymes, such as ceria and fullerenes, for the therapy of several human pathologies. To completely disclose the potential of PtNPs in biomedicine, however, a detailed picture of their diverse properties is still required, including a precise investigation of the underlying anti-oxidant mechanisms and their toxicological aspects.

We discussed the numerous synthetic methods developed to date, including the strategies to produce pure and controlled Pt nanomaterials for biomedical applications. We highlighted that small differences in the synthesis and purification procedures, as well as the aging and surface coating, may have direct consequences on the potential application of PtNPs. The main challenge for the scientific community is thus to develop synthetic strategies and purification procedures able to manufacture medical-grade PtNPs with precise control of their physico-chemical properties in biological fluids. This will allow to achieve fine tuning of their interaction with living systems, paving the way towards their use for precision medicine.

Our analysis of the toxicological data about PtNPs suggests that the material per se does not cause detectable toxicity, rather it can significantly counteract oxidative stress damage, due to its strong catalytic properties. Furthermore, it has been observed that aging of PtNP suspensions may cause corrosion and, hence, cellular toxicity, due to the presence of ions/debris of the material. As proven for several other nanomaterials, by-products, ionic contaminants, and endotoxins are key players in determining the toxicity outcomes. Similarly, they may have contributed to some of the observations of PtNPs induced cytotoxicity, rising contradicting interpretations within the scientific community. A consequent guideline for nanoPt toxicity assessment and/or nanomedicine applications is thus the use of ultrapure, well-characterized particle suspensions, previously tested for contaminations. Concerning cisplatin-like toxic effects by PtNPs, further studies are needed to clarify such possible behaviour, since the anticancer mechanism of this drug is based on DNA intercalation of Pt, provided a cis-geometry of the ligands around the Pt ion. So far, no reports have elucidated in which way PtNPs could exert a similar effect.

On the other side, pioneering studies have proposed PtNPs as new nanozymes for scavenging ROS in complex oxidative stress related disease models. Moreover, their ability to reduce ROS was shown to have diverse positive consequences on the intracellular pathways leading to inflammation. The observed reduction of LPS-induced ROS-mediated signal transduction, followed by the decrease of inflammatory cytokine release in mouse macrophages, emphasizes PtNPs potential as novel anti-inflammatory nano-drug. While these results need to be confirmed in other human immune cells and additional inflammatory pathologies, they foresee a promising field of application in nanomedicine for Pt-based nanozymes. For instance, it is interesting to speculate the design of PtNP-enriched dermal preparations for skin rashes occurring from a variety of factors, including infections, immune system disorders, allergens, and side-effects of medications. The idea of balancing immune-stimulating treatments, such as the adjuvants of vaccine preparations, could be reached by mixing PtNPs in the injected solution. In this way, the Pt nanozymes would be dispersed in the same target-tissue area without NP-dose decrease. Differently, the systemic release of PtNPs in the bloodstream could pose some problems related to NPs opsonization. Actually, the protein corona quickly covering the NPs as soon as in the blood includes circulating IgG and complement proteins. This “immune-coating” could facilitate the internalization by phagocytes through the Fc and complement receptors, quenching the stimulation of the innate immune cellular populations.

PtNP properties and the combinations with other materials (e.g., metals, polymers, targeting agents, etc.) could also suggest other applications, such as photothermal- and radio-therapies, or the control of bacterial growth. Further research is needed in this latter fields, as only a small number of results by a restricted group of researchers have been presented on the various intriguing roles and mechanisms of PtNPs. Overall, the emerging field of PtNP applications in nanomedicine is growing fast, and it is possible to foresee numerous and promising outcomes for this nanomaterial in the next future.

References

1.	Y. Shi, M. Lin, X. Jiang and S. Liang, Journal of Nanomaterials, 2015, 2015, 13.

2.	Y. Liu, D. Li and S. Sun, Journal of Materials Chemistry, 2011, 21, 12579-12587.

3.	I. Lee, F. Delbecq, R. Morales, M. A. Albiter and F. Zaera, Nat Mater, 2009, 8, 132-138.

4.	A. T. Madsen, E. H. Ahmed, C. H. Christensen, R. Fehrmann and A. Riisager, Fuel, 2011, 90, 3433-3438.

5.	X. Huang, Z. Zhao, J. Fan, Y. Tan and N. Zheng, Journal of the American Chemical Society, 2011, 133, 4718-4721.

6.	C.-K. Tsung, J. N. Kuhn, W. Huang, C. Aliaga, L.-I. Hung, G. A. Somorjai and P. Yang, Journal of the American Chemical Society, 2009, 131, 5816-5822.

7.	M. Miyake and K. Miyabayashi, Catalysis Surveys from Asia, 2012, 16, 1-13.

8.	E. Schmidt, A. Vargas, T. Mallat and A. Baiker, Journal of the American Chemical Society, 2009, 131, 12358-12367.

9.	Y. Li and G. A. Somorjai, Nano Letters, 2010, 10, 2289-2295.

10.	J. N. Kuhn, C.-K. Tsung, W. Huang and G. A. Somorjai, Journal of Catalysis, 2009, 265, 209-215.

11.	Kasem and K. K., Platinum Metals Review, 2012, 56, 221-228.

12.	C. J. Kliewer and G. A. Somorjai, Catalysis Letters, 2010, 137, 118-122.

13.	I. Kumakiri, S. Diplas, C. Simon and P. Nowak, Industrial & Engineering Chemistry Research, 2011, 50, 6000-6008.

14.	Y. Li, K. Zhang, S. Peng, G. Lu and S. Li, Journal of Molecular Catalysis A: Chemical, 2012, 363–364, 354-361.

15.	G. J. Leong, M. C. Schulze, M. B. Strand, D. Maloney, S. L. Frisco, H. N. Dinh, B. Pivovar and R. M. Richards, Applied Organometallic Chemistry, 2014, 28, 1-17.

16.	E. Antolini, Applied Catalysis B: Environmental, 2007, 74, 337-350.

17.	B. Krishnamurthy and S. Deepalochani, Int. J. Electrochem. Sci, 2009, 4, 386.

18.	A. Chen and P. Holt-Hindle, Chemical Reviews, 2010, 110, 3767-3804.

19.	N. V. Long, T. Duy Hien, T. Asaka, M. Ohtaki and M. Nogami, International Journal of Hydrogen Energy, 2011, 36, 8478-8491.

20.	W. P. Kang and C. K. Kim, Applied Physics Letters, 1993, 63, 421-423.

21.	A. Harley-Trochimczyk, T. Pham, J. Chang, E. Chen, M. A. Worsley, A. Zettl, W. Mickelson and R. Maboudian, Advanced Functional Materials, 2016, 26, 314-314.

22.	S.-I. Tanaka, J. Miyazaki, D. K. Tiwari, T. Jin and Y. Inouye, Angewandte Chemie International Edition, 2011, 50, 431-435.

23.	D. Chen, S. Gao, W. Ge, Q. Li, H. Jiang and X. Wang, RSC Advances, 2014, 4, 40141-40145.

24.	D. Chen, C. Zhao, J. Ye, Q. Li, X. Liu, M. Su, H. Jiang, C. Amatore, M. Selke and X. Wang, ACS applied materials & interfaces, 2015, 7, 18163-18169.

25.	X. Zheng, W. Chen, P. Cui, Z. Wang and W. Zhang, RSC Advances, 2014, 4, 58489-58494.

26.	W. Chen, X. Zheng, S. Li, W. Zhang, X. Wen, L. Yue and J. Wang, Journal of Nanoparticle Research, 2015, 17, 1-10.

27.	A. Higuchi, Y.-D. Siao, S.-T. Yang, P.-V. Hsieh, H. Fukushima, Y. Chang, R.-C. Ruaan and W.-Y. Chen, Analytical Chemistry, 2008, 80, 6580-6586.

28.	M. I. Kim, M. S. Kim, M.-A. Woo, Y. Ye, K. S. Kang, J. Lee and H. G. Park, Nanoscale, 2014, 6, 1529-1536.

29.	Y. Song, X. Xia, X. Wu, P. Wang and L. Qin, Angewandte Chemie, 2014, 126, 12659-12663.

30.	X.-Y. Dong, X.-N. Mi, L. Zhang, T.-M. Liang, J.-J. Xu and H.-Y. Chen, Biosensors and Bioelectronics, 2012, 38, 337-341.

31.	X.-M. Fu, Z.-J. Liu, S.-X. Cai, Y.-P. Zhao, D.-Z. Wu, C.-Y. Li and J.-H. Chen, Chinese Chemical Letters, 2016, 27, 920-926.

32.	M. F. Hossain and J. Y. Park, RSC Advances, 2016, 6, 74453-74461.

33.	S. Hrapovic, Y. Liu, K. B. Male and J. H. T. Luong, Analytical chemistry, 2004, 76, 1083-1088.

34.	N. Liu, D. Nie, Y. Tan, Z. Zhao, Y. Liao, H. Wang, C. Sun and A. Wu, Microchimica Acta, 2017, 184, 147-153.

35.	H. Mei, W. Wu, B. Yu, H. Wu, S. Wang and Q. Xia, Sensors and Actuators B: Chemical, 2016, 223, 68-75.

36.	S.-y. Niu, Y.-q. Qin and B. Han, Asian Journal of Chemistry, 2013, 25, 4375.

37.	D. Rao, Q. Sheng and J. Zheng, Journal of Chemical Sciences, 2016, 128, 1367-1375.

38.	E. Skotadis, K. Voutyras, M. Chatzipetrou, G. Tsekenis, L. Patsiouras, L. Madianos, S. Chatzandroulis, I. Zergioti and D. Tsoukalas, Biosensors and Bioelectronics, 2016, 81, 388-394.

39.	K. G. Sun and S. H. Hur, Sensors and Actuators B: Chemical, 2015, 210, 618-623.

40.	I. Taurino, G. Sanzó, F. Mazzei, G. Favero, G. De Micheli and S. Carrara, Scientific reports, 2015, 5.

41.	M. Moglianetti, E. De Luca, D. Pedone, R. Marotta, T. Catelani, B. Sartori, H. Amenitsch, S. F. Retta and P. P. Pompa, Nanoscale, 2016, 8, 3739-3752.

42.	H. Hosaka, R. Haruki, K. Yamada, C. Böttcher and T. Komatsu, PLoS ONE, 2014, 9, e110541.

43.	S. Shibuya, Y. Ozawa, K. Watanabe, N. Izuo, T. Toda, K. Yokote and T. Shimizu, PLoS ONE, 2014, 9, e109288.

44.	H. Wei and E. Wang, Chemical Society Reviews, 2013, 42, 6060-6093.

45.	F. Caputo, M. De Nicola and L. Ghibelli, Biochemical Pharmacology, 2014, 92, 112-130.

46.	X. Wang, Y. Hu and H. Wei, Inorganic Chemistry Frontiers, 2016, 3, 41-60.

47.	E. Kuah, S. Toh, J. Yee, Q. Ma and Z. Gao, Chemistry – A European Journal, 2016, n/a-n/a.

48.	W. He, W. Wamer, Q. Xia, J.-j. Yin and P. P. Fu, Journal of Environmental Science and Health, Part C, 2014, 32, 186-211.

49.	X. Hu, J. Liu, S. Hou, T. Wen, W. Liu, K. Zhang, W. He, Y. Ji, H. Ren and Q. Wang, Science China Physics, Mechanics and Astronomy, 2011, 54, 1749-1756.

50.	Y. Lin, J. Ren and X. Qu, Accounts of Chemical Research, 2014, 47, 1097-1105.

51.	H. Y. Shin, T. J. Park and M. I. Kim, Journal of Nanomaterials, 2015, 2015.

52.	X. Wang, W. Guo, Y. Hu, J. Wu and H. Wei, in Nanozymes: Next Wave of Artificial Enzymes, Springer, 2016, pp. 57-91.

53.	S. Onizawa, K. Aoshiba, M. Kajita, Y. Miyamoto and A. Nagai, Pulmonary Pharmacology & Therapeutics, 2009, 22, 340-349.

54.	Y. Yoshihisa, A. Honda, Q.-L. Zhao, T. Makino, R. Abe, K. Matsui, H. Shimizu, Y. Miyamoto, T. Kondo and T. Shimizu, Experimental Dermatology, 2010, 19, 1000-1006.

55.	A. Clark, A. Zhu, K. Sun and H. R. Petty, J Nanopart Res, 2011, 13.

56.	M. Nomura, Y. Yoshimura, T. Kikuiri, T. Hasegawa, Y. Taniguchi, Y. Deyama, K.-i. Koshiro, H. Sano, K. Suzuki and N. Inoue, Journal of Pharmacological Sciences, 2011, 117, 243-252.

57.	M. Takamiya, Y. Miyamoto, T. Yamashita, K. Deguchi, Y. Ohta, Y. Ikeda, T. Matsuura and K. Abe, Journal of neuroscience research, 2011, 89, 1125-1133.

58.	W.-K. Kim, J.-C. Kim, H.-J. Park, O.-J. Sul, M.-H. Lee, J.-S. Kim and H.-S. Choi, Experimental & Molecular Medicine, 2012, 44, 432-439.

59.	M. Takamiya, Y. Miyamoto, T. Yamashita, K. Deguchi, Y. Ohta and K. Abe, Neuroscience, 2012, 221, 47-55.

60.	H. Katsumi, K. Fukui, K. Sato, S. Maruyama, S. Yamashita, E. Mizumoto, K. Kusamori, M. Oyama, M. Sano and T. Sakane, Metallomics, 2014, 6, 1050-1056.

61.	J. Nellore, C. Pauline and K. Amarnath, Journal of neurodegenerative diseases, 2013, 2013.

62.	H. Nakanishi, T. Hamasaki, T. Kinjo, H. Yan, N. Nakamichi, S. Kabayama, K. Teruya and S. Shirahata, Nano Biomedicine & Engineering, 2013, 5.

63.	M.-R. Choi, L. T. Do, Y.-H. Chung, H. Yoo and R. Yu, Journal of nanoscience and nanotechnology, 2015, 15, 5571-5576.

64.	S. Kato, R. Hokama, H. Okayasu, Y. Saitoh, K. Iwai and N. Miwa, Journal of nanoscience and nanotechnology, 2012, 12, 4019-4027.

65.	Y. J. Kim, D. Kim, Y. Lee, S. Y. Choi, J. Park, S. Y. Lee, J. W. Park and H. J. Kwon, BMB reports, 2009, 42, 304-309.

66.	R. Nishikawa, K. Teruya, Y. Katakura, K. Osada, T. Hamasaki, T. Kashiwagi, T. Komatsu, Y. Li, J. Ye, A. Ichikawa, K. Otsubo, S. Morisawa, Q. Xu and S. Shirahata, Cytotechnology, 2005, 47, 97-105.

67.	F. Yusof and N. Ismail, Journal of Applied Pharmaceutical Science, 2015, 140-145.

68.	W. Zheng, B. Jiang, Y. Hao, Y. Zhao, W. Zhang and X. Jiang, Biofabrication, 2014, 6, 045004.

69.	Y. Yoshihisa, Q.-L. Zhao, M. A. Hassan, Z.-L. Wei, M. Furuichi, Y. Miyamoto, T. Kondo and T. Shimizu, Free radical research, 2011, 45, 326-335.

70.	N. Toshima and T. Yonezawa, New Journal of Chemistry, 1998, 22, 1179-1201.

71.	H. Bönnemann and Ryan M. Richards, European Journal of Inorganic Chemistry, 2001, 2001, 2455-2480.

72.	M. Subhramannia and V. K. Pillai, Journal of Materials Chemistry, 2008, 18, 5858-5870.

73.	A. R. Tao, S. Habas and P. Yang, Small, 2008, 4, 310-325.

74.	J. Chen, B. Lim, E. P. Lee and Y. Xia, Nano Today, 2009, 4, 81-95.

75.	Z. Peng and H. Yang, Nano Today, 2009, 4, 143-164.

76.	S. Cheong, J. D. Watt and R. D. Tilley, Nanoscale, 2010, 2, 2045-2053.

77.	L. Zhang, W. Niu and G. Xu, Nano Today, 2012, 7, 586-605.

78.	T. S. Ahmadi, Z. L. Wang, T. C. Green, A. Henglein and M. A. El-Sayed, Science, 1996, 272, 1924-1926.

79.	Y. Mei, G. Sharma, Y. Lu, M. Ballauff, M. Drechsler, T. Irrgang and R. Kempe, Langmuir, 2005, 21, 12229-12234.

80.	B. H. San, S. Kim, S. H. Moh, H. Lee, D.-Y. Jung and K. K. Kim, Angewandte Chemie International Edition, 2011, 50, 11924-11929.

81.	A. Sennuga, J. van Marwijk, A. Boshoff and C. G. Whiteley, Journal of Nanoparticle Research, 2012, 14, 1-11.

82.	S. Papst, M. A. Brimble, C. W. Evans, D. J. Verdon, V. Feisst, P. R. Dunbar, R. D. Tilley and D. E. Williams, Organic & biomolecular chemistry, 2015, 13, 6567-6572.

83.	M. Cueto, M. Sanz, M. Oujja, F. Gámez, B. Martínez−Haya and M. Castillejo, The Journal of Physical Chemistry C, 2011, 115, 22217-22224.

84.	X. Le Guével, V. Trouillet, C. Spies, G. Jung and M. Schneider, The Journal of Physical Chemistry C, 2012, 116, 6047-6051.

85.	W. Xu, R. P. Rajeev, V. S. Krishna, G. T. S. Andavan, T. Chunglin, L. Roger, O. Mihrimah and S. O. Cengiz, Nanotechnology, 2006, 17, 1177.

86.	X. Yuan, Z. Luo, Q. Zhang, X. Zhang, Y. Zheng, J. Y. Lee and J. Xie, ACS Nano, 2011, 5, 8800-8808.

87.	L. Zhang, L. T. Roling, X. Wang, M. Vara, M. Chi, J. Liu, S.-I. Choi, J. Park, J. A. Herron, Z. Xie, M. Mavrikakis and Y. Xia, Science, 2015, 349, 412-416.

88.	C. Xu, Z. Yuan, N. Kohler, J. Kim, M. A. Chung and S. Sun, Journal of the American Chemical Society, 2009, 131, 15346-15351.

89.	Y. Xiong, B. J. Wiley and Y. Xia, Angewandte Chemie International Edition, 2007, 46, 7157-7159.

90.	R. M. Crist, J. H. Grossman, A. K. Patri, S. T. Stern, M. A. Dobrovolskaia, P. P. Adiseshaiah, J. D. Clogston and S. E. McNeil, Integrative Biology, 2013, 5, 66-73.

91.	S. Mahima, R. Kannan, I. Komath, M. Aslam and V. K. Pillai, Chemistry of Materials, 2008, 20, 601-603.

92.	J. N. Tiwari, F.-M. Pan and K.-L. Lin, New Journal of Chemistry, 2009, 33, 1482-1485.

93.	J. M. Kim, H.-I. Joh, S. M. Jo, D. J. Ahn, H. Y. Ha, S.-A. Hong and S.-K. Kim, Electrochimica Acta, 2010, 55, 4827-4835.

94.	Z. Y. Zhou, Z. Z. Huang, D. J. Chen, Q. Wang, N. Tian and S. G. Sun, Angewandte Chemie International Edition, 2010, 49, 411-414.

95.	Y. Li, Y. Jiang, M. Chen, H. Liao, R. Huang, Z. Zhou, N. Tian, S. Chen and S. Sun, Chemical Communications, 2012, 48, 9531-9533.

96.	J. B. Raoof, R. Ojani and S. R. Hosseini, Journal of Solid State Electrochemistry, 2012, 16, 2699-2708.

97.	G. A. El-Nagar, A. M. Mohammad, M. S. El-Deab and B. E. El-Anadouli, Electrochimica Acta, 2013, 94, 62-71.

98.	F. Gao, N. Yang, H. Obloh and C. E. Nebel, Electrochemistry Communications, 2013, 30, 55-58.

99.	W. Zhao, X. Zhou, Z. Xue, B. Wu, X. Liu and X. Lu, Journal of Materials Science, 2013, 48, 2566-2573.

100.	M. A. Mahmoud and M. A. El-Sayed, Nano Letters, 2011, 11, 946-953.

101.	M. A. Mahmoud and M. A. El-Sayed, Langmuir, 2012, 28, 4051-4059.

102.	M. A. Mahmoud, F. Saira and M. A. El-Sayed, Nano Letters, 2010, 10, 3764-3769.

103.	K. Saminathan, V. Kamavaram, V. Veedu and A. M. Kannan, International Journal of Hydrogen Energy, 2009, 34, 3838-3844.

104.	M. Shafiei, A. R. Riahi, F. G. Sen and A. T. Alpas, Surface and Coatings Technology, 2010, 205, 306-311.

105.	S. I. Lim, I. Ojea-Jiménez, M. Varon, E. Casals, J. Arbiol and V. Puntes, Nano Letters, 2010, 10, 964-973.

106.	K. Miyabayashi, S. Nakamura and M. Miyake, Crystal Growth & Design, 2011, 11, 4292-4295.

107.	E. Shahbazali, V. Hessel, T. Noël and Q. Wang, Nanotechnology Reviews, 2014, 3, 65-86.

108.	R. Jurczakowski, A. Lewera and P. Kulboka, Google Patents, 2015.

109.	Y. Kang, X. Ye and C. B. Murray, Angewandte Chemie International Edition, 2010, 49, 6156-6159.

110.	W. Zhou, J. Wu and H. Yang, Nano Letters, 2013, 13, 2870-2874.

111.	A. Nirmala Grace and K. Pandian, Materials Chemistry and Physics, 2007, 104, 191-198.

112.	J. Kou, C. Bennett-Stamper and R. S. Varma, ACS Sustainable Chemistry & Engineering, 2013, 1, 810-816.

113.	K. V. Sarathy, G. Raina, R. T. Yadav, G. U. Kulkarni and C. N. R. Rao, The Journal of Physical Chemistry B, 1997, 101, 9876-9880.

114.	K. Vijaya Sarathy, G. U. Kulkarni and C. N. R. Rao, Chemical Communications, 1997, 537-538.

115.	F. Dassenoy, K. Philippot, T. Ould Ely, C. Amiens, P. Lecante, E. Snoeck, A. Mosset, M.-J. Casanove and B. Chaudret, New Journal of Chemistry, 1998, 22, 703-712.

116.	S.-Y. Zhao, S.-H. Chen, S.-Y. Wang, D.-G. Li and H.-Y. Ma, Langmuir, 2002, 18, 3315-3318.

117.	J. Yang, J. Y. Lee, T. C. Deivaraj and H.-P. Too, Langmuir, 2003, 19, 10361-10365.

118.	C. Yee, M. Scotti, A. Ulman, H. White, M. Rafailovich and J. Sokolov, Langmuir, 1999, 15, 4314-4316.

119.	H. Perez, J. P. Pradeau, P. A. Albouy and J. Perez-Omil, Chemistry of Materials, 1999, 11, 3460-3463.

120.	S. Chen and K. Kimura, The Journal of Physical Chemistry B, 2001, 105, 5397-5403.

121.	S. E. Eklund and D. E. Cliffel, Langmuir, 2004, 20, 6012-6018.

122.	A. Ghosh, F. Stellacci and R. Kumar, Catalysis Today, 2012, 198, 77-84.

123.	S. F. Adil, M. E. Assal, M. Khan, A. Al-Warthan, M. R. H. Siddiqui and L. M. Liz-Marzan, Dalton Transactions, 2015, 44, 9709-9717.

124.	M. Horie, H. Kato, S. Endoh, K. Fujita, K. Nishio, L. K. Komaba, H. Fukui, A. Nakamura, A. Miyauchi, T. Nakazato, S. Kinugasa, Y. Yoshida, Y. Hagihara, Y. Morimoto and H. Iwahashi, Metallomics, 2011, 3, 1244-1252.

125.	P. J. Shiny, A. Mukherjee and N. Chandrasekaran, Bioprocess and biosystems engineering, 2014, 37, 991-997.

126.	Y. Li, J. Zhang, J. Gu, S. Chen, C. Wang and W. Jia, Journal of Photochemistry and Photobiology B: Biology, 2017.

127.	Y. Tian, W. Zi, X. Li, L. Yanji, K. Bian, W. Cao, Y. He, H. Liu, K. Niu and D. Gao, New Journal of Chemistry, 2017.

128.	L. Zhang, L. Laug, W. Münchgesang, E. Pippel, U. Gösele, M. Brandsch and M. Knez, Nano Letters, 2010, 10, 219-223.

129.	J. Fan, J.-J. Yin, B. Ning, X. Wu, Y. Hu, M. Ferrari, G. J. Anderson, J. Wei, Y. Zhao and G. Nie, Biomaterials, 2011, 32, 1611-1618.

130.	Q. Y. Deng, B. Yang, J. F. Wang, C. G. Whiteley and X. N. Wang, Biotechnology letters, 2009, 31, 1505-1509.

131.	X. Liu, W. Wei, C. Wang, H. Yue, D. Ma, C. Zhu, G. Ma and Y. Du, Journal of Materials Chemistry, 2011, 21, 7105-7110.

132.	X. Wang, Y. Zhang, T. Li, W. Tian, Q. Zhang and Y. Cheng, Langmuir, 2013, 29, 5262-5270.

133.	K. Yamamoto, T. Imaoka, W.-J. Chun, O. Enoki, H. Katoh, M. Takenaga and A. Sonoi, Nat Chem, 2009, 1, 397-402.

134.	H.-J. Cheng, T.-H. Wu, C.-T. Chien, H.-W. Tu, T.-S. Cha and S.-Y. Lin, Small, 2016, n/a-n/a.

135.	P. Bommersbach, M. Chaker, M. Mohamedi and D. Guay, The Journal of Physical Chemistry C, 2008, 112, 14672-14681.

136.	R. K. Rakshit, S. K. Bose, R. Sharma, R. C. Budhani, T. Vijaykumar, S. J. Neena and G. U. Kulkarni, Journal of Applied Physics, 2008, 103, 023915.

137.	O. Paschos, P. Choi, H. Efstathiadis and P. Haldar, Thin Solid Films, 2008, 516, 3796-3801.

138.	X. Ke, C. Bittencourt, S. Bals and G. Van Tendeloo, Beilstein Journal of Nanotechnology, 2013, 4, 77-86.

139.	R. Strobel and S. E. Pratsinis, Platinum Metals Review, 2009, 53, 11-20.

140.	I. D. Choi, H. Lee, Y.-B. Shim and D. Lee, Langmuir, 2010, 26, 11212-11216.

141.	C. Dhand, N. Dwivedi, X. J. Loh, A. N. Jie Ying, N. K. Verma, R. W. Beuerman, R. Lakshminarayanan and S. Ramakrishna, RSC Advances, 2015, 5, 105003-105037.

142.	P. Kshirsagar, S. S. Sangaru, M. A. Malvindi, L. Martiradonna, R. Cingolani and P. P. Pompa, Colloids and Surfaces A: Physicochemical and Engineering Aspects, 2011, 392, 264-270.

143.	S. Scaramuzza, M. Zerbetto and V. Amendola, The Journal of Physical Chemistry C, 2016, 120, 9453-9463.

144.	J.-P. Sylvestre, S. Poulin, A. V. Kabashin, E. Sacher, M. Meunier and J. H. T. Luong, The Journal of Physical Chemistry B, 2004, 108, 16864-16869.

145.	F. Correard, K. Maximova, M.-A. Estève, C. Villard, M. Roy, A. Al-Kattan, M. Sentis, M. Gingras, A. V. Kabashin and D. Braguer, International Journal of Nanomedicine, 2014, 9, 5415-5430.

146.	A. I. Yanson, P. Rodriguez, N. Garcia-Araez, R. V. Mom, F. D. Tichelaar and M. T. M. Koper, Angewandte Chemie International Edition, 2011, 50, 6346-6350.

147.	E. Torres-Chavolla, R. J. Ranasinghe and E. C. Alocilja, IEEE Transactions on Nanotechnology, 2010, 9, 533-538.

148.	M. Shah, D. Fawcett, S. Sharma, S. Tripathy and G. Poinern, Materials, 2015, 8, 5377.

149.	Z. Abdullaeva, in Synthesis of Nanoparticles and Nanomaterials: Biological Approaches, Springer International Publishing, Cham, 2017, pp. 177-195.

150.	R. Isaac, S. Gobalakrishnan, G. Rajan, R.-J. Wu, S. R. Pamanji, M. Khagga, V. Baskaralingam and M. Chavali, Advanced Science, Engineering and Medicine, 2013, 5, 763-770.

151.	C. Whiteley, Y. Govender, T. Riddin and M. Rai, in Metal Nanoparticles in Microbiology, Springer, 2011, pp. 103-134.

152.	K. S. Siddiqi and A. Husen, Nanoscale Research Letters, 2016, 11, 482.

153.	Y. Konishi, K. Ohno, N. Saitoh, T. Nomura, S. Nagamine, H. Hishida, Y. Takahashi and T. Uruga, Journal of biotechnology, 2007, 128, 648-653.

154.	K. J. Rashamuse, C. C. Z. Mutambanengwe and C. G. Whiteley, African Journal of Biotechnology, 2008, 7.

155.	K. J. Rashamuse and C. G. Whiteley, Applied microbiology and biotechnology, 2007, 75, 1429-1435.

156.	J. A. Bennett, G. A. Attard, K. Deplanche, M. Casadesus, S. E. Huxter, L. E. Macaskie and J. Wood, ACS Catalysis, 2012, 2, 504-511.

157.	S. K. Srivastava and M. Constanti, Journal of Nanoparticle Research, 2012, 14, 1-10.

158.	S. V. Gaidhani, R. K. Yeshvekar, U. U. Shedbalkar, J. H. Bellare and B. A. Chopade, Process Biochemistry, 2014, 49, 2313-2319.

159.	B. Baskaran, A. Muthukumarasamy, S. Chidambaram, A. Sugumaran, K. Ramachandran and T. R. Manimuthu, IET Nanobiotechnology, 2016.

160.	M. Martins, C. Mourato, S. Sanches, J. P. Noronha, M. T. B. Crespo and I. A. C. Pereira, Water Research, 2017, 108, 160-168.

161.	B. Balraj, M. Arulmozhi, C. Siva, S. Abimanyu, R. Krithikadevi and M. Thaneswari Rasu, Cytotoxic potentials of biologically fabricated platinum nanoparticles from <i>Streptomyces sp.</i> on MCF-7 breast cancer cells, Institution of Engineering and Technology, 2017.

162.	M. F. Lengke, M. E. Fleet and G. Southam, Langmuir, 2006, 22, 7318-7323.

163.	R. Brayner, H. Barberousse, M. Hemadi, C. Djedjat, C. Yepremian, T. Coradin, J. Livage, F. Fievet and A. Coute, J Nanosci Nanotechnol, 2007, 7, 2696-2708.

164.	P. J. Shiny, A. Mukherjee and N. Chandrasekaran, RSC Advances, 2016, 6, 27775-27787.

165.	T. L. Riddin, M. Gericke and C. G. Whiteley, Nanotechnology, 2006, 17, 3482-3489.

166.	Y. Govender, T. Riddin, M. Gericke and C. G. Whiteley, Biotechnology letters, 2009, 31, 95-100.

167.	E. Castro-Longoria, S. D. Moreno-Velazquez, A. R. Vilchis-Nestor, E. Arenas-Berumen and M. Avalos-Borja, Journal of microbiology and biotechnology, 2012, 22, 1000-1004.

168.	X. Lin, M. Wu, D. Wu, S. Kuga, T. Endo and Y. Huang, Green Chemistry, 2011, 13, 283-287.

169.	F. Coccia, L. Tonucci, D. Bosco, M. Bressan and N. d'Alessandro, Green Chemistry, 2012, 14, 1073-1078.

170.	S. Ghosh, R. Nitnavare, A. Dewle, G. B. Tomar, R. Chippalkatti, P. More, R. Kitture, S. Kale, J. Bellare and B. A. Chopade, International journal of nanomedicine, 2015, 10, 7477.

171.	B. Zheng, T. Kong, X. Jing, T. Odoom-Wubah, X. Li, D. Sun, F. Lu, Y. Zheng, J. Huang and Q. Li, Journal of colloid and interface science, 2013, 396, 138-145.

172.	C. Yang, M. Wang, J. Zhou and Q. Chi, Materials Science and Engineering: C, 2017, 77, 1012-1016.

173.	P. Velmurugan, J. Shim, K. Kim and B.-T. Oh, Materials Letters, 2016, 174, 61-65.

174.	K. Tahir, S. Nazir, A. Ahmad, B. Li, A. U. Khan, Z. U. H. Khan, F. U. Khan, Q. U. Khan, A. Khan and A. U. Rahman, Journal of Photochemistry and Photobiology B: Biology, 2017, 166, 246-251.

175.	A. John Leo and O. S. Oluwafemi, Materials Letters, 2017, 196, 141-144.

176.	R. Dobrucka, Saudi Journal of Biological Sciences, 2016.

177.	R. Karthik, R. Sasikumar, S.-M. Chen, M. Govindasamy, J. V. Kumar and V. Muthuraj, Int. J. Electrochem. Sci, 2016, 11, 8245-8255.

178.	Y. Li, J. Zhang, J. Gu and S. Chen, Journal of Photochemistry and Photobiology B: Biology, 2017, 169, 96-100.

179.	R. Venu, T. S. Ramulu, S. Anandakumar, V. S. Rani and C. G. Kim, Colloids and Surfaces A: Physicochemical and Engineering Aspects, 2011, 384, 733-738.

180.	A. J. Leo and O. S. Oluwafemi, Materials Letters, 2017, 196, 141-144.

181.	H. Nadaroglu, A. A. Gungor, S. Ince and A. Babagil, Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 2017, 172, 43-47.

182.	T. L. Riddin, Y. Govender, M. Gericke and C. G. Whiteley, Enzyme and Microbial Technology, 2009, 45, 267-273.

183.	T. Riddin, M. Gericke and C. G. Whiteley, Enzyme and microbial technology, 2010, 46, 501-505.

184.	A. Syed and A. Ahmad, Colloids and Surfaces B: Biointerfaces, 2012, 97, 27-31.

185.	J. Y. Song, E.-Y. Kwon and B. S. Kim, Bioprocess and Biosystems Engineering, 2009, 33, 159-164.

186.	C. Soundarrajan, A. Sankari, P. Dhandapani, S. Maruthamuthu, S. Ravichandran, G. Sozhan and N. Palaniswamy, Bioprocess and biosystems engineering, 2012, 35, 827-833.

187.	R. Bali, R. Siegele and A. T. Harris, Journal of Nanoparticle Research, 2010, 12, 3087-3095.

188.	H. Raut, Malghe, Nikam, Kashid, Adv. Mat. Lett., 2013, 4, 650-654.

189.	http://www.fda.gov/MedicalDevices/ProductsandMedicalProcedures/ImplantsandProsthetics/BreastImplants/UCM064040.

190.	G. Oberdörster, E. Oberdörster and J. Oberdörster, Environmental Health Perspectives, 2005, 113, 823-839.

191.	R. B. A. Foldbjerg, Herman, Archives of Basic and Applied Medicine, 2013, 1, 5-15.

192.	S. Sabella, R. P. Carney, V. Brunetti, M. A. Malvindi, N. Al-Juffali, G. Vecchio, S. M. Janes, O. M. Bakr, R. Cingolani, F. Stellacci and P. P. Pompa, Nanoscale, 2014, 6, 7052-7061.

193.	V. De Matteis, M. A. Malvindi, A. Galeone, V. Brunetti, E. De Luca, S. Kote, P. Kshirsagar, S. Sabella, G. Bardi and P. P. Pompa, Nanomedicine: Nanotechnology, Biology and Medicine, 2014, 11, 731-739.

194.	A. R. Gliga, S. Skoglund, I. Odnevall Wallinder, B. Fadeel and H. L. Karlsson, Particle and Fibre Toxicology, 2014, 11, 11-11.

195.	Y. Teow, P. V. Asharani, M. P. Hande and S. Valiyaveettil, Chemical Communications, 2011, 47, 7025-7038.

196.	S. Sharifi, S. Behzadi, S. Laurent, M. Laird Forrest, P. Stroeve and M. Mahmoudi, Chemical Society Reviews, 2012, 41, 2323-2343.

197.	G. J. Oostingh, E. Casals, P. Italiani, R. Colognato, R. Stritzinger, J. Ponti, T. Pfaller, Y. Kohl, D. Ooms, F. Favilli, H. Leppens, D. Lucchesi, F. Rossi, I. Nelissen, H. Thielecke, V. F. Puntes, A. Duschl and D. Boraschi, Particle and Fibre Toxicology, 2011, 8, 8-8.

198.	B. W. Neun and M. A. Dobrovolskaia, in Characterization of Nanoparticles Intended for Drug Delivery, ed. S. E. McNeil, Humana Press, Totowa, NJ, 2011, pp. 121-130.

199.	M. A. Dobrovolskaia, B. W. Neun, J. D. Clogston, J. H. Grossman and S. E. McNeil, Nanomedicine, 2013, 9, 1847-1856.

200.	J. Gao, G. Liang, B. Zhang, Y. Kuang, X. Zhang and B. Xu, Journal of the American Chemical Society, 2007, 129, 1428-1433.

201.	P. V. Asharani, N. Xinyi, M. P. Hande and S. Valiyaveettil, Nanomedicine, 2010, 5, 51-64.

202.	M. Kutwin, E. Sawosz, S. Jaworski, M. Hinzmann, M. Wierzbicki, A. Hotowy, M. Grodzik, A. Winnicka and A. Chwalibog, 2016.

203.	H. Gehrke, J. Pelka, C. Hartinger, H. Blank, F. Bleimund, R. Schneider, D. Gerthsen, S. Bräse, M. Crone, M. Türk and D. Marko, Arch Toxicol, 2011, 85, 799-812.

204.	J. Pelka, H. Gehrke, M. Esselen, M. Türk, M. Crone, S. Bräse, T. Muller, H. Blank, W. Send, V. Zibat, P. Brenner, R. Schneider, D. Gerthsen and D. Marko, Chemical Research in Toxicology, 2009, 22, 649-659.

205.	A. Elder, H. Yang, R. Gwiazda, X. Teng, S. Thurston, H. He and G. Oberdörster, Advanced Materials, 2007, 19, 3124-3129.

206.	T. Hamasaki, T. Kashiwagi, T. Imada, N. Nakamichi, S. Aramaki, K. Toh, S. Morisawa, H. Shimakoshi, Y. Hisaeda and S. Shirahata, Langmuir, 2008, 24, 7354-7364.

207.	K. B. Ayaz Ahmed, T. Raman and V. Anbazhagan, RSC Advances, 2016, 6, 44415-44424.

208.	M. Manikandan, N. Hasan and H.-F. Wu, Biomaterials, 2013, 34, 5833-5842.

209.	Y. Yamagishi, A. Watari, Y. Hayata, X. Li, M. Kondoh, Y. Yoshioka, Y. Tsutsumi and K. Yagi, Nanoscale Res Lett, 2013, 8.

210.	Y. Yamagishi, A. Watari, Y. Hayata, X. Li, M. Kondoh, Y. Tsutsumi and K. Yagi, Die Pharmazie-An International Journal of Pharmaceutical Sciences, 2013, 68, 178-182.

211.	P. Konieczny, A. G. Goralczyk, R. Szmyd, L. Skalniak, J. Koziel, F. L. Filon, M. Crosera, A. Cierniak, E. K. Zuba-Surma, J. Borowczyk, E. Laczna, J. Drukala, E. Pyza, D. Semik, O. Woznicka, A. Klein and J. Jura, International Journal of Nanomedicine, 2013, 8, 3963-3975.

212.	H. Buchtelova, S. Dostalova, P. Michalek, S. Krizkova, V. Strmiska, P. Kopel, D. Hynek, L. Richtera, A. Ridoskova, P. Adam, J. Kynicky, M. Brtnicky, Z. Heger and V. Adam, Food and Chemical Toxicology, 2017, 105, 337-346.

213.	F. Gatto, P. P. Pompa and G. Bardi, unpublished data.

214.	M. U. Rehman, Y. Yoshihisa, Y. Miyamoto and T. Shimizu, Inflammation research : official journal of the European Histamine Research Society ... [et al.], 2012, 61, 1177-1185.

215.	M. Hashimoto, K. Kawai, H. Kawakami and S. Imazato, Journal of Biomedical Materials Research Part A, 2016, 104, 209-217.

216.	H. Kachi, M. Noda, J. C. Wataha, Y. Nakaoki and H. Sano, Journal of Biomedical Materials Research Part B: Applied Biomaterials, 2011, 96, 193-198.

217.	H. Mohammadi, A. Abedi, A. Akbarzadeh, M. J. Mokhtari, H. E. Shahmabadi, M. R. Mehrabi, S. Javadian and M. Chiani, International Nano Letters, 2013, 3.

218.	A. A. Alshatwi, J. Athinarayanan and P. Vaiyapuri Subbarayan, Journal of materials science. Materials in medicine, 2015, 26, 5330.

219.	J. Athinarayanan, V. S. Periasamy and A. A. Alshatwi, Process Biochemistry, 2016.

220.	T. Mironava, M. Simon, M. H. Rafailovich and B. Rigas, Toxicol In Vitro, 2013, 27.

221.	E. J. Park, H. Kim, Y. Kim and K. Park, Arch Pharm Res, 2010, 33.

222.	Y. Teow and S. Valiyaveettil, Nanoscale, 2010, 2, 2607-2613.

223.	E. J. Cho, B. Sun, K. O. Doh, E. M. Wilson, S. Torregrosa-Allen, B. D. Elzey and Y. Yeo, Biomaterials, 2015, 37, 312-319.

224.	T. López, M. Alvarez, R. D. González, M. J. Uddin, J. Bustos, S. Arroyo and A. Sánchez, Adsorption, 2011, 17, 573-581.

225.	T. Lopez, F. Figueras, J. Manjarrez, J. Bustos, M. Alvarez, J. Silvestre-Albero, F. Rodriguez-Reinoso, A. Martinez-Ferre and E. Martinez, European J of Medic Chem, 2011, 45.

226.	E. S. Morozkin, I. A. Zaporozhchenko, M. V. Kharkova, A. V. Cherepanova, P. P. Laktionov, V. V. Vlasov, B. G. Sukhov, G. F. Prozorova, B. A. Trofimov and M. V. Khvostov, 2013.

227.	H. Sun, X. Chen, D. Chen, M. Dong, X. Fu, Q. Li, X. Liu, Q. Wu, T. Qiu, T. Wan and S. Li, Int J Nanomedicine, 2012, 7, 3295-3307.

228.	E.-J. Park, H. Kim, Y. Kim and K. Park, J Environ Toxicol, 2010, 25, 279-286.

229.	M. Kutwin, E. Sawosz, S. Jaworski, N. Kurantowicz, B. Strojny and A. Chwalibog, Nanoscale Research Letters, 2014, 9, 1-6.

230.	A. A. Torrano, R. Herrmann, C. Strobel, M. Rennhak, H. Engelke, A. Reller, I. Hilger, A. Wixforth and C. Brauchle, Nanoscale, 2016, 8, 13352-13367.

231.	C. T. Chien, J. Y. Yan, W. C. Chiu, T. H. Wu, C. Y. Liu and S. Y. Lin, Advanced Materials, 2013, 25, 5067-5073.

232.	M. Hashimoto, S. Yamaguchi, J.-I. Sasaki, K. Kawai, H. Kawakami, Y. Iwasaki and S. Imazato, European Journal of Oral Sciences, 2016, 124, 68-74.

233.	P. V. Asharani, S. Sethu, S. Vadukumpully, S. Zhong, C. T. Lim, M. P. Hande and S. Valiyaveettil, Advanced Functional Materials, 2010, 20, 1233-1242.

234.	P. V. Asharani, Y. Lianwu, Z. Gong and S. Valiyaveettil, Nanotoxicology, 2011, 5, 43-54.

235.	M. Prasek, E. Sawosz, S. Jaworski, M. Grodzik, T. Ostaszewska, M. Kamaszewski, M. Wierzbicki and A. Chwalibog, Nanoscale Research Letters, 2013, 8, 1-9.

236.	O. S. Adeyemi, F. A. Sulaiman, M. A. Akanji, H. O. B. Oloyede, A. A. Sulaiman, A. Olatunde, S. T. Salman, A. R. Aransiola, A. G. Ajayi and M. M. Ekundayo, Comparative Clinical Pathology, 2016, 1-10.

237.	K. Katao, R. Honma, S. Kato, S. Watanabe and J.-i. Imai, Experimental Animals, 2011, 60, 33-45.

238.	J. Kim, T. Shirasawa and Y. Miyamoto, Biomaterials, 2010, 31, 5849-5854.

239.	J. Kim, M. Takahashi, T. Shimizu, T. Shirasawa, M. Kajita, A. Kanayama and Y. Miyamoto, Mechanisms of Ageing and Development, 2008, 129, 322-331.

240.	Y. Sakaue, J. Kim and Y. Miyamoto, Int J Nanomedicine, 2010, 5, 687-695.

241.	H. Yan, T. Kinjo, H. Tian, T. Hamasaki, K. Teruya, S. Kabayama and S. Shirahata, Bioscience, biotechnology, and biochemistry, 2011, 75, 1295-1299.

242.	S. Guo and E. Wang, Nano Today, 2011, 6, 240-264.

243.	A. Dumas and P. Couvreur, Chemical Science, 2015, 6, 2153-2157.

244.	G. Poli, G. Leonarduzzi, F. Biasi and E. Chiarpotto, Current Medicinal Chemistry, 2004, 11, 1163-1182.

245.	P. D. Ray, B.-W. Huang and Y. Tsuji, Cellular Signalling, 2012, 24, 981-990.

246.	H. Sies, Experimental Physiology, 1997, 82, 291-295.

247.	A. Karakoti, S. Singh, J. M. Dowding, S. Seal and W. T. Self, Chemical Society Reviews, 2010, 39, 4422-4432.

248.	T. Baati, F. Bourasset, N. Gharbi, L. Njim, M. Abderrabba, A. Kerkeni, H. Szwarc and F. Moussa, Biomaterials, 2012, 33, 4936-4946.

249.	J. Chen, S. Patil, S. Seal and J. F. McGinnis, Nat Nano, 2006, 1, 142-150.

250.	N. Gharbi, M. Pressac, M. Hadchouel, H. Szwarc, S. R. Wilson and F. Moussa, Nano Letters, 2005, 5, 2578-2585.

251.	F. Pagliari, C. Mandoli, G. Forte, E. Magnani, S. Pagliari, G. Nardone, S. Licoccia, M. Minieri, P. Di Nardo and E. Traversa, ACS Nano, 2012, 6, 3767-3775.

252.	A. Vincent, S. Babu, E. Heckert, J. Dowding, S. M. Hirst, T. M. Inerbaev, W. T. Self, C. M. Reilly, A. E. Masunov, T. S. Rahman and S. Seal, ACS Nano, 2009, 3, 1203-1211.

253.	K. M. Nash and S. Ahmed, Nanomedicine: Nanotechnology, Biology and Medicine, 2015, 11, 2033-2040.

254.	M. Aioub, S. R. Panikkanvalappil and M. A. El-Sayed, ACS Nano, 2017, 11, 579-586.

255.	J. Morry, W. Ngamcherdtrakul and W. Yantasee, Redox Biology, 2017, 11, 240-253.

256.	M. J. Akhtar, M. Ahamed, H. A. Alhadlaq and A. Alshamsan, Biochimica et Biophysica Acta (BBA) - General Subjects, 2017, 1861, 802-813.

257.	B. Xiong, R. Xu, R. Zhou, Y. He and E. S. Yeung, Talanta, 2014, 120, 262-267.

258.	J. Liu, X. Jiang, L. Wang, Z. Hu, T. Wen, W. Liu, J. Yin, C. Chen and X. Wu, Nano Research, 2015, 8, 4024-4037.

259.	P. Jawaid, M. u. Rehman, Y. Yoshihisa, P. Li, Q. l. Zhao, M. A. Hassan, Y. Miyamoto, T. Shimizu and T. Kondo, Apoptosis : an international journal on programmed cell death, 2014, 19, 1006-1016.

260.	P. Jawaid, M. U. Rehman, Q. L. Zhao, K. Takeda, K. Ishikawa, M. Hori, T. Shimizu and T. Kondo, Journal of Cellular and Molecular Medicine, 2016, 20, 1737-1748.

261.	P. Jawaid, M. U. Rehman, M. A. Hassan, Q. L. Zhao, P. Li, Y. Miyamoto, M. Misawa, R. Ogawa, T. Shimizu and T. Kondo, Ultrasonics Sonochemistry, 2016, 31, 206-215.

262.	K. Eid, A. Eldesouky, A. Fahmy, A. Shahat and R. AbdElaal, Am J Biomed Sci, 2013, 5, 242-249.

263.	H. Ye, Y. Liu, A. Chhabra, E. Lilla and X. Xia, ChemNanoMat, 2017, 3, 33-38.

264.	K. Hirakawa and S. Sano, Bulletin of the Chemical Society of Japan, 2009, 82, 1299-1303.

265.	J. Li, L. Lv, G. Zhang, X. Zhou, A. Shen and J. Hu, Analytical Methods, 2016, 8, 2097-2105.

266.	M. Kajita, K. Hikosaka, M. Iitsuka, A. Kanayama, N. Toshima and Y. Miyamoto, Free Radical Research, 2007, 41, 615-626.

267.	K. Hikosaka, J. Kim, M. Kajita, A. Kanayama and Y. Miyamoto, Colloids and Surfaces B: Biointerfaces, 2008, 66, 195-200.

268.	Y. Liu, H. Wu, Y. Chong, W. G. Wamer, Q. Xia, L. Cai, Z. Nie, P. P. Fu and J.-J. Yin, ACS Applied Materials & Interfaces, 2015, 7, 19709-19717.

269.	A. Watanabe, M. Kajita, J. Kim, A. Kanayama, K. Takahashi, T. Mashino and Y. Miyamoto, Nanotechnology, 2009, 20, 455105.

270.	J.-W. Lee, S. Yoon, Y. M. Lo, H. Wu, S.-Y. Lee and B. Moon, RSC Advances, 2015, 5, 63757-63764.

271.	J. Liu, X. Hu, S. Hou, T. Wen, W. Liu, X. Zhu, J.-J. Yin and X. Wu, Sensors and Actuators B: Chemical, 2012, 166, 708-714.

272.	C. Chen, S. Fan, C. Li, Y. Chong, X. Tian, J. Zheng, P. P. Fu, X. Jiang, W. G. Wamer and J.-j. Yin, Journal of Materials Chemistry B, 2016, 4, 7895-7901.

273.	M. Ma, J. Xie, Y. Zhang, Z. Chen and N. Gu, Materials Letters, 2013, 105, 36-39.

274.	M. Ma, Y. Zhang and N. Gu, Colloids and Surfaces A: Physicochemical and Engineering Aspects, 2011, 373, 6-10.

275.	S. B. He, H. H. Deng, A. L. Liu, G. W. Li, X. H. Lin, W. Chen and X. H. Xia, ChemCatChem, 2014, 6, 1543-1548.

276.	C.-J. Yu, T.-H. Chen, J.-Y. Jiang and W.-L. Tseng, Nanoscale, 2014, 6, 9618-9624.

277.	S. Cai, C. Qi, Y. Li, Q. Han, R. Yang and C. Wang, Journal of Materials Chemistry B, 2016, 4, 1869-1877.

278.	A. Harriman, G. R. Millward, P. Neta, M. C. Richoux and J. M. Thomas, The Journal of Physical Chemistry, 1988, 92, 1286-1290.

279.	B. H. San, S. H. Moh and K. K. Kim, Journal of Materials Chemistry, 2012, 22, 1774-1780.

280.	R. Bar‐Ziv, I. Zilbermann, M. Shandalov, V. Shevchenko and D. Meyerstein, Chemistry–A European Journal, 2015, 21, 19000-19009.

281.	Y. Dong, J. Zhang, P. Jiang, G. Wang, X. Wu, H. Zhao and C. Zhang, New Journal of Chemistry, 2015, 39, 4141-4146.

282.	J. Li, W. Liu, X. Wu and X. Gao, Biomaterials, 2015, 48, 37-44.

283.	Y. Liu, H. Wu, M. Li, J.-J. Yin and Z. Nie, Nanoscale, 2014, 6, 11904-11910.

284.	Y. Ju and J. Kim, Chemical Communications, 2015, 51, 13752-13755.

285.	U. Carmona, L. Zhang, L. Li, W. Munchgesang, E. Pippel and M. Knez, Chemical Communications, 2014, 50, 701-703.

286.	W. Li, H. Zhang, J. Zhang and Y. Fu, Analytical Methods, 2015, 7, 4464-4471.

287.	Y. Fu, X. Zhao, J. Zhang and W. Li, The Journal of Physical Chemistry C, 2014, 118, 18116-18125.

288.	Y.-T. Zhou, W. He, W. G. Wamer, X. Hu, X. Wu, Y. M. Lo and J.-J. Yin, Nanoscale, 2013, 5, 1583-1591.

289.	S. Matsuda, S. Matsui, Y. Shimizu and T. Matsuda, Environmental Science & Technology, 2011, 45, 4133-4138.

290.	L. De Marzi, A. Monaco, J. De Lapuente, D. Ramos, M. Borras, M. Di Gioacchino, S. Santucci and A. Poma, International journal of molecular sciences, 2013, 14, 3065.

291.	O. Gamucci and G. Bardi, in EURO-NanoTox-Letters, 2014, vol. 5, p. 1.

292.	E.-J. Park, J. Choi, Y.-K. Park and K. Park, Toxicology, 2008, 245, 90-100.

293.	Y.-J. Kim, D.-B. Kim, Y.-H. Lee, S.-Y. Choi, J.-S. Park, S.-Y. Lee, J.-W. Park and H.-J. Kwon, BMB reports, 2009, 42, 304-309.

294.	G. Tsuji, A. Hashimoto-Hachiya, M. Takemura, T. Kanemaru, M. Ichihashi and M. Furue, Journal of Investigative Dermatology, 2017.

295.	H. Nakanishi, T. Hamasaki, T. Kinjo, K. Teruya, S. Kabayama and S. Shirahata, BMC Proceedings, 2013, 7, 1-2.

296.	J.-W. Lee, J. Son, K.-M. Yoo, Y. M. Lo and B. Moon, RSC Advances, 2014, 4, 19824-19830.

297.	H. Kawasaki, H. Yamamoto, H. Fujimori, R. Arakawa, M. Inada and Y. Iwasaki, Chemical Communications, 2010, 46, 3759-3761.

298.	H. Lim, Y. Ju and J. Kim, Analytical chemistry, 2016, 88, 4751-4758.

299.	J. Wu, S. Balasubramanian, D. Kagan, K. M. Manesh, S. Campuzano and J. Wang, Nature Communications, 2010, 1, 36.

300.	D. Kagan, P. Calvo-Marzal, S. Balasubramanian, S. Sattayasamitsathit, K. M. Manesh, G.-U. Flechsig and J. Wang, Journal of the American Chemical Society, 2009, 131, 12082-12083.

301.	A. J. Bandodkar and J. Wang, Electroanalysis, 2016.

302.	E. L. Khim Chng, G. Zhao and M. Pumera, Nanoscale, 2014, 6, 2119-2124.

303.	J. Li, I. Rozen and J. Wang, ACS Nano, 2016, 10, 5619-5634.

304.	F. Peng, Y. Tu and D. A. Wilson, Chemical Society Reviews, 2017.

305.	D. A. Wilson, R. J. M. Nolte and J. C. M. van Hest, Nat Chem, 2012, 4, 268-274.

306.	Y. Tu, F. Peng, P. B. White and D. A. Wilson, Angewandte Chemie International Edition, 2017, n/a-n/a.

307.	W. F. Paxton, K. C. Kistler, C. C. Olmeda, A. Sen, S. K. St. Angelo, Y. Cao, T. E. Mallouk, P. E. Lammert and V. H. Crespi, Journal of the American Chemical Society, 2004, 126, 13424-13431.

308.	Y. Sun, J. Wang, W. Li, J. Zhang, Y. Zhang and Y. Fu, Biosensors and Bioelectronics, 2015, 74, 1038-1046.

309.	R. Gill, R. Polsky and I. Willner, Small, 2006, 2, 1037-1041.

310.	R. Polsky, R. Gill, L. Kaganovsky and I. Willner, Anal Chem, 2006, 78, 2268-2271.

311.	X. Hu, A. Saran, S. Hou, T. Wen, Y. Ji, W. Liu, H. Zhang, W. He, J.-J. Yin and X. Wu, RSC Advances, 2013, 3, 6095-6105.

312.	S. L. Xu and H. Cui, Luminescence, 2007, 22, 77-87.

313.	N. Xu, H.-W. Li, Y. Yue and Y. Wu, Nanotechnology, 2016, 27, 425602.

314.	K. Cai, Z. Lv, K. Chen, L. Huang, J. Wang, F. Shao, Y. Wang and H. Han, Chemical Communications, 2013, 49, 6024-6026.

315.	H. Wang, S. Li, Y. Si, N. Zhang, Z. Sun, H. Wu and Y. Lin, Nanoscale, 2014, 6, 8107-8116.

316.	K. Zhang, X. Hu, J. Liu, J.-J. Yin, S. Hou, T. Wen, W. He, Y. Ji, Y. Guo, Q. Wang and X. Wu, Langmuir, 2011, 27, 2796-2803.

317.	W. Zhang, X. Liu, D. Walsh, S. Yao, Y. Kou and D. Ma, Small, 2012, 8, 2948-2953.

318.	Y. Wang, G. Zhu, W. Qi, Y. Li and Y. Song, Biosensors and Bioelectronics, 2016, 85, 777-784.

319.	J. Yoon, T. Cho, H. Lim and J. Kim, Analytical and bioanalytical chemistry, 2016, 408, 7165-7172.

320.	N. Zhu, Z. Chang, P. He and Y. Fang, Analytica chimica acta, 2005, 545, 21-26.

321.	Z. Wang, X. Yang, J. Feng, Y. Tang, Y. Jiang and N. He, Analyst, 2014, 139, 6088-6091.

322.	L. Y. Chau, Q. He, A. Qin, S. P. Yip and T. M. H. Lee, Journal of Materials Chemistry B, 2016.

323.	W. Chen, X. Fang, H. Li, H. Cao and J. Kong, Biosensors and Bioelectronics, 2017, 94, 169-175.

324.	L.-N. Zhang, H.-H. Deng, F.-L. Lin, X.-W. Xu, S.-H. Weng, A.-L. Liu, X.-H. Lin, X.-H. Xia and W. Chen, Analytical chemistry, 2014, 86, 2711-2718.

325.	Z. Gao, M. Xu, M. Lu, G. Chen and D. Tang, Biosensors and Bioelectronics, 2015, 70, 194-201.

326.	H. Chang, H. Zhang, J. Lv, B. Zhang, W. Wei and J. Guo, Biosensors and Bioelectronics, 2016, 86, 156-163.

327.	G. Choi, E. Kim, E. Park and J. H. Lee, Talanta, 2017, 162, 38-45.

328.	C.-W. Tseng, H.-Y. Chang, J.-Y. Chang and C.-C. Huang, Nanoscale, 2012, 4, 6823-6830.

329.	G.-W. Wu, S.-B. He, H.-P. Peng, H.-H. Deng, A.-L. Liu, X.-H. Lin, X.-H. Xia and W. Chen, Analytical Chemistry, 2014, 86, 10955-10960.

330.	W. Li, B. Chen, H. Zhang, Y. Sun, J. Wang, J. Zhang and Y. Fu, Biosensors and Bioelectronics, 2015, 66, 251-258.

331.	L.-L. Wu, L.-Y. Wang, Z.-J. Xie, F. Xue and C.-F. Peng, RSC Advances, 2016, 6, 75384-75389.

332.	W. Chen, X. Fang, H. Li, H. Cao and J. Kong, Scientific Reports, 2016, 6, 31948.

333.	D. Kwon, W. Lee, W. Kim, H. Yoo, H.-C. Shin and S. Jeon, Analytical Methods, 2015, 7, 7639-7645.

334.	J.-G. You, Y.-W. Liu, C.-Y. Lu, W.-L. Tseng and C.-J. Yu, Biosensors and Bioelectronics, 2016.

335.	X. Sun, S. Guo, C.-S. Chung, W. Zhu and S. Sun, Advanced Materials, 2013, 25, 132-136.

336.	L. Chen, N. Wang, X. Wang and S. Ai, Microchimica Acta, 2013, 180, 1517-1522.

337.	L. Xing, Q. Rong and Z. Ma, Sensors and Actuators B: Chemical, 2015, 221, 242-247.

338.	X. Chen, X. Zhou and J. Hu, Analytical Methods, 2012, 4, 2183-2187.

339.	X. Feng, X. Li, H. Shi, H. Huang, X. Wu and W. Song, Analytica chimica acta, 2014, 852, 37-44.

340.	X. Hu, A. Saran, S. Hou, T. Wen, Y. Ji, W. Liu, H. Zhang and X. Wu, Chinese science bulletin, 2014, 59, 2588-2596.

341.	J. Xie, S. Wang, A. L. and V. V. K., Nanotechnology, 2007, 18, 065503.

342.	X. Kang, Z. Mai, X. Zou, P. Cai and J. Mo, Anal Biochem, 2007, 369, 71-79.

343.	J. Chen, J. Ge, L. Zhang, Z. Li and L. Qu, Sensors and Actuators B: Chemical, 2016, 233, 438-444.

344.	Q. Li, W. Luo, L. Su, J. Chen, K.-C. Chou and X. Hou, RSC Advances, 2016, 6, 92748-92753.

345.	D. Zhai, B. Liu, Y. Shi, L. Pan, Y. Wang, W. Li, R. Zhang and G. Yu, ACS nano, 2013, 7, 3540-3546.

346.	X. Ji, H. Y. Lau, X. Ren, B. Peng, P. Zhai, S.-P. Feng and P. K. L. Chan, Advanced Materials Technologies, 2016, 1, 1600042-n/a.

347.	W. Shi, H. Fan, S. Ai and L. Zhu, Sensors and Actuators B: Chemical, 2015, 221, 1515-1522.

348.	X.-Q. Lin, H.-H. Deng, G.-W. Wu, H.-P. Peng, A.-L. Liu, X.-H. Lin, X.-H. Xia and W. Chen, Analyst, 2015, 140, 5251-5256.

349.	N. Pan, W. Li-Ying, L.-L. Wu, C.-F. Peng and Z.-J. Xie, Microchimica Acta, 2016, 1-8.

350.	L.-L. Wu, L.-Y. Wang, Z.-J. Xie, N. Pan and C.-F. Peng, Sensors and Actuators B: Chemical, 2016, 235, 110-116.

351.	S.-B. He, G.-W. Wu, H.-H. Deng, A.-L. Liu, X.-H. Lin, X.-H. Xia and W. Chen, Biosensors and Bioelectronics, 2014, 62, 331-336.

352.	C. Zheng, A.-X. Zheng, B. Liu, X.-L. Zhang, Y. He, J. Li, H.-H. Yang and G. Chen, Chemical Communications, 2014, 50, 13103-13106.

353.	T. Jiang, Y. Song, D. Du, X. Liu and Y. Lin, ACS Sensors, 2016.

354.	S. Singal, A. K. Srivastava, A. M. Biradar and A. Mulchandani, Sensors and Actuators B: Chemical, 2014, 205, 363-370.

355.	S. K. Mishra, A. K. Srivastava, D. Kumar and Rajesh, RSC Advances, 2014, 4, 21267-21276.

356.	F. Gao, L. Du, Y. Zhang, F. Zhou and D. Tang, Biosensors and Bioelectronics, 2016, 86, 185-193.

357.	L. Chen, S. Ye, K. Cai, C. Zhang, G. Zhou, Z. He and H. Han, Talanta, 2015, 144, 324-328.

358.	Z.-H. Yang, Y. Zhuo, R. Yuan and Y.-Q. Chai, Biosensors and Bioelectronics, 2016, 78, 321-327.

359.	H. Su, H. Zhao, F. Qiao, L. Chen, R. Duan and S. Ai, Analyst, 2013, 138, 3026-3031.

360.	G. Dutta, S. Nagarajan, L. J. Lapidus and P. B. Lillehoj, Biosensors and Bioelectronics, 2017, 92, 372-377.

361.	W. He, Y. Liu, J. Yuan, J.-J. Yin, X. Wu, X. Hu, K. Zhang, J. Liu, C. Chen and Y. Ji, Biomaterials, 2011, 32, 1139-1147.

362.	Z. Gao, M. Xu, L. Hou, G. Chen and D. Tang, Analytica chimica acta, 2013, 776, 79-86.

363.	J. Comenge, C. Sotelo, F. Romero, O. Gallego, A. Barnadas, T. G.-C. Parada, F. Domínguez and V. F. Puntes, PLoS ONE, 2012, 7, e47562.

364.	D. Wang and S. J. Lippard, Nat Rev Drug Discov, 2005, 4, 307-320.

365.	T. C. Johnstone, K. Suntharalingam and S. J. Lippard, Chemical Reviews, 2016, 116, 3436-3486.

366.	L. Kelland, Nature reviews. Cancer, 2007, 7, 573-584.

367.	B. Teng, P. a. Ma, C. Yu, X. Zhang, Q. Feng, L. Wen, C. Li, Z. Cheng, D. Jin and J. Lin, Journal of Materials Chemistry B, 2017, 5, 307-317.

368.	V. R. Estrela-Llopis, A. V. Chevichalova, N. A. Trigubova and E. V. Ryzhuk, Colloid Journal, 2014, 76, 609-621.

369.	A. Ghoneum, H. Zhu, J. Woo, N. Zabinyakov, S. Sharma and J. K. Gimzewski, Nanotechnology, 2014, 25, 465101.

370.	B. Yogesh, B. Vineeta, N. Rammesh and P. Saili, Journal of Pharmacopuncture, 2016, 19, 114.

371.	M. Yamada, M. Foote and T. W. Prow, Wiley Interdisciplinary Reviews: Nanomedicine and Nanobiotechnology, 2015, 7, 428-445.

372.	H. Xia, F. Li, X. Hu, W. Park, S. Wang, Y. Jang, Y. Du, S. Baik, S. Cho, T. Kang, D.-H. Kim, D. Ling, K. M. Hui and T. Hyeon, ACS Central Science, 2016.

373.	A. Ghoneum, S. Sharma and J. Gimzewski, Int J Nanomed, 2013, 8, 2567-2573.

374.	M. Ghoneum, A. Ghoneum and J. Gimzewski, Anticancer Res, 2010, 30, 4075-4079.

375.	Y. Bendale, V. Bendale and S. Paul, Integrative Medicine Research, 2017.

376.	T. Yin, Z. Wang, X. Li, Y. Li, K. Bian, W. Cao, Y. He, H. Liu, K. Niu and D. Gao, New Journal of Chemistry, 2017, 41, 2941-2948.

377.	M. C. Evan Schneider, Lourdes Collazo, Tatsiana Mironova, Miriam Rafailovich, Cancer Research, 2012, 72 1956-1956.

378.	H. Elnakat and M. Ratnam, Advanced Drug Delivery Reviews, 2004, 56, 1067-1084.

379.	N. Parker, M. J. Turk, E. Westrick, J. D. Lewis, P. S. Low and C. P. Leamon, Analytical Biochemistry, 2005, 338, 284-293.

380.	L. Au, D. Zheng, F. Zhou, Z.-Y. Li, X. Li and Y. Xia, ACS Nano, 2008, 2, 1645-1652.

381.	W. Lu, A. K. Singh, S. A. Khan, D. Senapati, H. Yu and P. C. Ray, Journal of the American Chemical Society, 2010, 132, 18103-18114.

382.	N. C. Bigall, T. Härtling, M. Klose, P. Simon, L. M. Eng and A. Eychmüller, Nano Letters, 2008, 8, 4588-4592.

383.	E. Gharibshahi and E. Saion, International journal of molecular sciences, 2012, 13, 14723-14741.

384.	C. L. Chen, L. R. Kuo, S. Y. Lee, Y. K. Hwu, S. W. Chou, C. C. Chen, F. H. Chang, K. H. Lin, D. H. Tsai and Y. Y. Chen, Biomaterials, 2013, 34, 1128-1134.

385.	C. Wang, X. Cai, J. Zhang, X. Wang, Y. Wang, H. Ge, W. Yan, Q. Huang, J. Xiao, Q. Zhang and Y. Cheng, Small, 2015, 11, 2080-2086.

386.	J. Tang, X. Jiang, L. Wang, H. Zhang, Z. Hu, Y. Liu, X. Wu and C. Chen, Nanoscale, 2014, 6, 3670-3678.

387.	K. Shim, J. Kim, Y.-U. Heo, B. Jiang, C. Li, M. Shahabuddin, K. C. W. Wu, M. S. A. Hossain, Y. Yamauchi and J. H. Kim, Chemistry – An Asian Journal, 2017, 12, 21-26.

388.	F. H. James, N. S. Daniel and M. S. Henry, Physics in Medicine and Biology, 2004, 49, N309.

389.	J. W. J. Bergs, M. G. Wacker, S. Hehlgans, A. Piiper, G. Multhoff, C. Rödel and F. Rödel, Biochimica et Biophysica Acta (BBA) - Reviews on Cancer, 2015, 1856, 130-143.

390.	X.-D. Zhang, D. Wu, X. Shen, J. Chen, Y.-M. Sun, P.-X. Liu and X.-J. Liang, Biomaterials, 2012, 33, 6408-6419.

391.	P. Liu, Z. Huang, Z. Chen, R. Xu, H. Wu, F. Zang, C. Wang and N. Gu, Nanoscale, 2013, 5, 11829-11836.

392.	W. N. Rahman, N. Bishara, T. Ackerly, C. F. He, P. Jackson, C. Wong, R. Davidson and M. Geso, Nanomedicine: Nanotechnology, Biology and Medicine, 2009, 5, 136-142.

393.	A. Al Zaki, D. Cormode, A. Tsourkas and J. F. Dorsey, in Increasing the Therapeutic Ratio of Radiotherapy, eds. P. J. Tofilon and K. Camphausen, Springer International Publishing, Cham, 2017, pp. 241-265.

394.	G. Maiorano, E. Mele, M. C. Frassanito, E. Restini, A. Athanassiou and P. P. Pompa, Nanoscale, 2016, 8, 18921-18927.

395.	A. Astolfo, F. Qie, A. Kibleur, X. Hao, R. H. Menk, F. Arfelli, L. Rigon, T. M. Hinton, M. Wickramaratna, T. Tan and T. C. Hughes, Nanomedicine: Nanotechnology, Biology and Medicine, 2014, 10, 1821-1828.

396.	R. I. Jølck, J. S. Rydhög, A. N. Christensen, A. E. Hansen, L. M. Bruun, H. Schaarup-Jensen, A. S. von Wenck, B. Børresen, A. T. Kristensen, M. H. Clausen, A. Kjær, K. Conradsen, R. Larsen, P. M. af Rosenschöld and T. L. Andresen, Advanced Healthcare Materials, 2015, 4, 856-863.

397.	Z. Bao, M. He, H. Quan, D. Jiang, Y. Zheng, W. Qin, Y. Zhou, F. Ren, M. Guo and C. Jiang, RSC Advances, 2016, 6, 35124-35134.

398.	Q. Li, Y. Tanaka, Y. Saitoh and N. Miwa, Journal of Nanoscience and Nanotechnology, 2016, 16, 5345-5352.

399.	Q. Li, Y. Tanaka, Y. Saitoh, H. Tanaka and N. Miwa, Life Sci, 2015, 127, 106-114.

400.	E. Porcel, S. Liehn, H. Remita, N. Usami, K. Kobayashi, Y. Furusawa, C. Le Sech and S. Lacombe, Nanotechnology, 2010, 21.

401.	K. T. Butterworth, J. A. Wyer, M. Brennan-Fournet, C. J. Latimer, M. B. Shah, F. J. Currell and D. G. Hirst, Radiation research, 2008, 170, 381-387.

402.	N. Beyth, Y. Houri-Haddad, A. Domb, W. Khan and R. Hazan, Evidence-based complementary and alternative medicine : eCAM, 2015, 2015, 246012.

403.	B. Rosenberg, L. Van Camp, E. B. Grimley and A. J. Thomson, The Journal of biological chemistry, 1967, 242, 1347-1352.

404.	B. Rosenberg, L. Vancamp and T. Krigas, Nature, 1965, 205, 698-699.

405.	B. Rosenberg, L. VanCamp, J. E. Trosko and V. H. Mansour, Nature, 1969, 222, 385-386.

406.	Y. Zhao, C. Ye, W. Liu, R. Chen and X. Jiang, Angewandte Chemie International Edition, 2014, 53, 8127-8131.

407.	K.-Y. Nam, The journal of advanced prosthodontics, 2014, 6, 207-214.

408.	S. Ma, N. Izutani, S. Imazato, J.-h. Chen, W. Kiba, R. Yoshikawa, K. Takeda, H. Kitagawa and S. Ebisu, Dental materials journal, 2012, 31, 150-156.

409.	A. Chwalibog, E. Sawosz, A. Hotowy, J. Szeliga, S. Mitura, K. Mitura, M. Grodzik, P. Orlowski and A. Sokolowska, Int J Nanomedicine, 2010, 5, 1085-1094.

410.	J. Gopal, N. Hasan, M. Manikandan and H. F. Wu, Sci Rep, 2013, 3.

411.	J. Szeliga, F. Sawosz, T. Niemiec and K. Kacprzyk, International journal of nanomedicine, 2010, 5, 631-637.

412.	M. A. Kebede, T. Imae, Sabrina, C.-M. Wu and K.-B. Cheng, Chemical Engineering Journal, 2017, 311, 340-347.

413.	A. Taglietti, Y. A. Diaz Fernandez, E. Amato, L. Cucca, G. Dacarro, P. Grisoli, V. Necchi, P. Pallavicini, L. Pasotti and M. Patrini, Langmuir, 2012, 28, 8140-8148.

414.	E. Sawosz, A. Chwalibog, J. Szeliga, F. Sawosz, M. Grodzik, M. Rupiewicz, T. Niemiec and K. Kacprzyk, Int J Nanomedicine, 2010, 5, 631-637.

Figure 1. Schematic overview of PtNP scientific literature and published patents. (A) Plot of scientific literature trend related to PtNPs (source: Web of Science, TOPIC: "platinum nanoparticle" OR “platinum nano-particle” OR "Pt nanoparticle" OR “Pt nano-particle” OR "platinum nanocomposite" OR "Pt nanocomposite" OR "platinum nanomaterial" OR "Pt nanomaterial" OR "Pt NP" OR "PtNP". (B) Plot of patent trend related to PtNPs (source: Scopus, same keywords as in (A)). The pie chart shows the geographic analysis of the patents in the PtNP technology field (source: Patsnap).

Figure 2. TEM images of Pt NPs with controlled shape. (A) Apoferritin-encapsulated PtNPs after staining of the protein shell with uranyl acetate. Reprinted with permission from Ref. 128 Copyright 2010 American Chemical Society. (B) Icosahedral PtNPs. Reprinted with permission from Ref. 110 Copyright 2013 American Chemical Society. (C) Pt branched rods. Reprinted with permission from Ref. 110 Copyright 2013 American Chemical Society. (D) FePt@Fe2O3 yolk-shell NPs. Reprinted with permission from Ref. 200 Copyright 2007 American Chemical Society. (E) Pt cubes. Reprinted with permission from Ref. 110 Copyright 2013 American Chemical Society. (F) Pt octapods. Reprinted with permission from Ref. 110 Copyright 2013 American Chemical Society. (G) Pt nanoflowers. Reproduced from Ref. 41 by permission of The Royal Society of Chemistry. (H) FePt bimetallic NPs. Reprinted with permission from Ref. 88 Copyright 2009 American Chemical Society. (I) Pt tetrahexahedrons. Reproduced from Ref. 89 by permission of John Wiley and Sons.

Figure 3. Toxicological profile of PtNPs. (A) TUNEL assay performed on HeLa cells after exposure for 24 hours to PtNPs of 5 and 20 nm (50 μg/mL) compared to untreated cells (Ctrl), and DNase I treated cells (positive control, P). Reproduced from Ref. 41 by permission of The Royal Society of Chemistry. (B) Lung tissue sections stained with hematoxylin and eosin obtained from mice that received (a) saline and (b) PAA-Pt and were exposed to control air, (c) saline and (d) PAA-Pt and were exposed to cigarette smoke. Reproduced from Ref. 53 by permission of Elsevier.

Figure 4. PtNP uptake and intracellular localization. (A) 3D models extracted from double axis STEM HAADF electron tomography of late endosomes/phagosomes containing PtNPs of 5 nm. Endosomal membranes, multilamellar bodies, endosomal vesicles and PtNPs are respectively shown in green, cyan, violet and yellow. Scale bar is 200 nm. Reproduced from Ref. 41 by permission of The Royal Society of Chemistry. (B) TEM images of the internalization of 20 nm Pt multipods in HUVEC cells. Reproduced from Ref. 205 by permission of John Wiley and Sons. (C-E) CytoViv optical microscopy images of control IMR90 cells (C) compared to cells exposed for 48 h to PVP-PtNPs (D) and FA-PtNPs (E). Yellow arrows highlight the cellular organelles (endosomes and lysosomes) and green arrows aggregated PtNPs. Reproduced from Ref. 222 by permission of The Royal Society of Chemistry.

Figure 5. Enzymatic properties of PtNPs. (A) Superoxide dismutase-like activity: time-dependent SOD-like activity of apoferritin and apoferritin-encapsulated Pt NPs at increased protein concentrations. Reprinted with permission from Ref. 128 Copyright 2010 American Chemical Society. (B) Catalase-like activity: H2O2 decomposition activity of PtNPs (green), apoferritin (cyan), fresh-prepared (blue) apoferritin-encapsulated Pt NPs, and after two weeks storage in water at 4 °C (red). Reprinted with permission from Ref. 128 Copyright 2010 American Chemical Society. (C) Peroxidase-like activity: time-dependent UV-Vis absorbance curves of TMB-H2O2 reaction system in presence of 50 pM 5 nm (red) and 1 pM 20 nm (green) Pt NPs, H2O (black) and 50 pM HRP (blue). Reproduced from Ref. 41 by permission of The Royal Society of Chemistry.

Figure 6. Schemes of the main antioxidant chemical reactions catalyzed by PtNPs as peroxidase (A), catalase (B), and superoxide dismutase (C) mimics.

Figure 7. ROS scavenging properties of PtNPs. (A-C) Nomarski images and DCF staining of untreated (A), 0.5 mM PtNP treated (B), and 0.5 mM EUK-8 treated (C) Caenorhabditis elegans. (D) ROS levels comparison between worms exposed to PtNPs and EUK-8 (0.5 mM) for 48 h and control worms, evaluated by DCF assay. Reproduced from Ref. 239 by permission of Elsevier.

Figure 8. Diagnostic applications of nanomotors. (A) Au/Pt rod-shaped particle. Reprinted with permission from Ref. 307 Copyright 2004 American Chemical Society. Illustrations of the Pt nanomotor-based detection of (B) silver. Reprinted with permission from Ref. 300 Copyright 2009 American Chemical Society. (C) nucleic acids. Reprinted with permission from Ref. 299 Copyright 2010 Nature Publishing Group.

Figure 9. PtNP applications in nanodiagnostic. Illustrations of the Pt NP-based colorimetric detection of (A) antibodies. Reproduced from Ref. 361 by permission of Elsevier. (B) cancer cells. Reproduced from Ref. 28 by permission of The Royal Society of Chemistry. (C) DNA. Reproduced from Ref. 321 by permission of The Royal Society of Chemistry. (D) Escherichia coli. Reproduced from Ref. 359 by permission of The Royal Society of Chemistry. (E) mercury ions Reproduced from Ref. 328 by permission of The Royal Society of Chemistry.

Figure 10. Photothermal properties of PtNPs. (a-i) Confocal images showing the hyperthermic explosion of EMT-6 cancer cells incubated with FePtNPs after laser activation. Red and green stainings refer to propidium iodide and YOPRO-1 dyes, respectively. (j) Representative scheme of the photothermolysis of a cancer cell. Reproduced from Ref. 384 by permission of Elsevier.

Table 1. Summary of advantages and disadvantages of PtNP synthetic methods.