Strongly Emissive Perovskite Nanocrystal Inks for High Voltage Solar Cells

Quinten A. Akkerman†φ, Marina Gandini§∆, Francesco Di Stasio†, Prachi Rastogi†φ, Francisco Palazon†, Giovanni Bertoni†∇, James M. Ball§, Mirko Prato†, Annamaria Petrozza§* and Liberato Manna†*

†Nanochemistry Department, Istituto Italiano di Tecnologia, Via Morego 30, 16163 Genova, Italy

φUniversità degli Studi di Genova, Via Dodecaneso, 31, 16146, Genova, Italy

§ Center for Nano Science and Technology @Polimi, Istituto Italiano di Tecnologia, Via Giovanni Pascoli 70/3, 20133 Milano, Italy

∇IMEM-CNR, Parco Area delle Scienze 37/A, 43124 Parma, Italy

∆Dipartimento di Fisica, Politecnico di Milano, Piazza L. da Vinci 32, 20133 Milano, Italy

equal contribution

Lead halide perovskite semiconductors have recently gained wide interest following their successful embodiment in solid-state photovoltaic devices with impressive power conversion efficiencies, while offering a relatively simple and low cost processability. While the primary optoelectronic properties of these materials have already met the requirement for high efficiency optoelectronic technologies, industrial up-scale requires more robust processing methods and less toxic solvents than have been commonly used so successfully on the lab-scale. Here, we report a fast, room-temperature synthesis of inks based on CsPbBr3 perovskite nanocrystals using short, low boiling-point ligands and environmentally friendly solvents. Requiring no lengthy post-synthesis treatments, the inks are directly used to fabricate films of high optoelectronic quality, exhibiting photoluminescence quantum yields higher than 30% and an amplified spontaneous emission threshold as low as 1.5 J/cm2. Finally, we demonstrate the fabrication of a perovskite nanocrystal-based solar cells, with open circuit voltages as high as 1.5 V.

Colloidal semiconductor nanocrystals (NCs) enable solution processing and represent a powerful platform for tuning optical and electrical properties useful for optoelectronic devices.1-3 Over the past decades, the main challenges have been the synthesis of NC solutions with tailored properties (band gap, absorption, monodispersity) and the conversion of these solutions to high-quality NC films, with preservation of the properties.1, 2, 4 One major problem originates directly from the synthesis methods. The high temperature (100-350 °C) syntheses often required to fabricate crystalline monodisperse and shape-controlled NCs tend to employ ligands and solvents with long alkyl chains.5-7 These bulky ligands and the residual chemicals from the synthesis prevent the production of dense films and form an insulating layer around the NCs after deposition onto a substrate.8 Strategies have been developed to overcome these issues such as the addition of conductive polymers,9, 10 or post-synthesis ligand exchange.11-13Most surface passivation schemes reported so far have been based on solid-state ligand exchange, with long ligands used to stabilize the NC in solution being replaced by much shorter ligands that ensure closer NC packing and thus higher electrical conductivity.11-14 Progress in such schemes has allowed for a steady improvement of charge-carrier diffusion lengths in solid films (above 100 nm), enabling, for example, the fabrication of thick solar-cell devices while preserving efficient charge collection, leading to record efficiencies exceeding 10%.14, 15

Halide perovskite semiconductors can merge the highly efficient operational principles of conventional inorganic semiconductors with the low-temperature solution processability of emerging organic and hybrid materials, offering a promising route towards cheaply generating electricity as well as light.16-19 Perovskites not only show exceptional primary optoelectronic properties such as a direct bandgap,20 small exciton binding energy,21 low carrier recombination rates,22 ambipolar transport,23 and tunability of the bandgap covering a wavelength range from the near-infrared24 to the ultraviolet, but they are also very attractive for their ease of processability for mass production (e.g. printing from solution) and for the large availability of their chemical components. For the most efficient optoelectronic devices, the semiconductor films are currently processed from precursor solutions dissolved in organic solvents.25-28 After deposition, the constituent ions self-assemble during crystallization directly upon the selected substrate when treated at temperatures below 120 °C. Such a process can form high quality thin-films, but it also has drawbacks. Principally, it couples both the thin film morphology and the related optoelectronic properties/crystal quality in the same optimization step, making it more sensitive to processing conditions. The thin films are polycrystalline but can exhibit varying morphologies determined by different factors. These include precursor ratio, solvent, processing additives, substrate roughness and surface energy, atmospheric/environmental conditions, annealing temperature, and treatment time. As a result, the thin films contain a significant density of structural and chemical defects which introduce loss channels.

A key parameter for a rapid evaluation of the optoelectronic quality of the perovskite thin film is its photoluminescence quantum yield (PLQY). In solar cells  under steady-state solar illumination, electrons are photoexcited from the valence band into the conduction band, a process which splits the electron and hole quasi-Fermi levels. The extent of the splitting is determined by the charge density at which the recombination rate is equal to the carrier generation rate. Any additional non-radiative recombination process with a carrier lifetime shorter than the radiative decay will thus reduce the steady-state charge density and the open circuit voltage. Perovskite thin films hardly achieve 20% PLQY at excitation intensities that are relevant for PV applications, indicating a significant density of defects states.19, 28, 29 On the other hand, colloidally synthesized CsPbBr3 and MAPbBr3 (MA = methylammonium) perovskite NCs currently can exhibit PLQYs close to 90% and can be synthesized in a wide variety of sizes and shapes.30-38 However, the enhancement in PLQY comes at the expense of carrier extraction, because the bulky organic ligands used in the synthesis of these CsPbBr3 NCs to passivate and stabilize their surface inhibit inter-particle connectivity. This prevents their use as proper “inks” for the fabrication of dense conductive thin films.30, 31, 37 Traditional ligand exchange procedures, as explained above, are of little help in this case, due to intrinsic lability of these NCs and the additional difficulty of purifying solutions of halide perovskite NCs from excess surfactants and unreacted precursors.39 Thus only very recently, during the revision of this manuscript, it has been possible to demonstrate devices using  colloidal perovskite NCs as a starting material for the active layer.40

Here we report a fast and room temperature synthesis of CsPbBr3 perovskite NC inks using short, low boiling point ligands and solvents. These inks have optical qualities close to those of NCs made with high temperature hot-injection syntheses. The use of short ligands and solvents circumvents post-synthesis treatments and enables the production of thin films with high optoelectronic quality, i.e. PLQYs larger than 30% and an ASE (amplified spontaneous emission) threshold as low as 1.5 µJ/cm2. Importantly, the robustness of such properties are demonstrated by the fabrication of CsPbBr3 NCs based solar cells, with open circuit voltages as high as 1.5 V.

Synthesis and characterization of CsPbBr3 NC inks. The synthesis of the CsPbBr3 NC inks, as depicted in Fig. 1A, is carried out by a simple and fast one-step injection (see also Supplementary Video 1). We use propionic acid (PrAc) to dissolve Cs2CO3 and form a Cs+ propionate complex which is diluted in a polar/apolar solvent mixture of isopropanol (IPrOH), hexane (HEX), and butylamine (BuAm) at room temperature (RT). The dissolution reaction is exothermic and therefore does not require heating. Thus, unlike previous room temperature syntheses,36, 37 no degassing was required for the precursors and the whole process was carried out under nitrogen. A separate solution, prepared under air by dissolving PbBr2 in a similar mixture of chemicals (also at RT), was injected in the first solution. The NCs immediately nucleated and reached their maximum size already 10 seconds after the injection (see below for additional details on the growth). At this point, the NCs were separated by centrifugation and were redispersed in toluene, after which they could be directly used for device preparation. The size of the NCs could be controlled by varying the IPrOH to HEX ratio, as shown in Supplementary Figure 1. Here, an increase of this ratio, and thus an increase of the polarity of the solution, led to larger crystalline domains. This route however led to unstable colloidal solutions and was thus not investigated further. As the synthesis was performed under a nitrogen atmosphere (in the glovebox) at room temperature (RT), it could be easily up-scaled to a gram sized synthesis (900 ml, 1.9 g PbBr2), with no noticeable changes in the NC properties (Supplementary Figure 2).

Important differences between this reaction scheme and previous ones (for example the one reported by Protesescu et al.)31 are that here we use only RT reactions, and additionally the solvents and ligands of the current synthesis have much lower boiling points (Table 1). As will be discussed later in more detail, upon spin coating of a solution of these NCs on a substrate, all these solvents and ligands quickly evaporated at RT, ensuring a fast drying of the film and facilitating the fabrication of thick films by multiple layer depositions. Also, compared to most previous syntheses of halide perovskite NCs that involved two steps,30, 36 the present scheme is based on a single step. Finally, and equally important, the solvents used (IPrOH and HEX) are more environmentally friendly than the classical dimethyl formamide (DMF) used in the preparation of bulk perovskite films and therefore are more amenable to scale-up in industrial processes. We could additionally replace hexane and toluene with the even less hazardous heptane (bp = 98 0C) and still prepare NCs with the same features and properties (Supplementary Figure 3).

| CsPbBr3 NC inks |  |  | Cubic CsPbBr3 NCs31 |  |  |
| --- | --- | --- | --- | --- | --- |
|  | bp (oC) | mL |  | bp (oC) | mL |
| IPrOH | 82 | 4 | ODE | 314 | 5.46 |
| HEX | 69 | 2 |  |  |  |
| PrAc | 141 | 0.143 | OA | 360 | 0.55 |
| BuAm | 78 | 0.133 | OLAM | 350 | 0.5 |
|  | Amount (mmol) |  |  | Amount (mmol) |  |
| PbBr2 | 0.100 |  | PbBr2 | 0.188 |  |

Table 1. Boiling points and amounts of chemicals used for preparing CsPbBr3 NC inks. Table compares the boiling points and amounts with those of standard synthesis of cubic CsPbBr3 NCs stabilized with long ligands.31, 40 With propionic acid (PrAc), isopropanol (IPrOH), hexane (HEX), butylamine (BuAm), octadecene (ODE), oleic acid (OA) and oleylamine (OLAM).

As shown in Fig. 1a and c, the NCs prepared with this method tended to cluster in large aggregates. These aggregates were not formed due to the centrifugation of the NCs in the cleaning step, since similar clusters were also observed when the solution was investigated with transmission electron microscopy (TEM) directly after the injection of the PbBr2 precursor (and thus before washing, Supplementary Figure 4). Based on high resolution TEM (HRTEM) (Fig. 1d), they contain crystalline NCs with domains of roughly 15-20 nm in size and atomic planes matching those of orthorhombic CsPbBr3 (Supplementary Figure 5). The crystallinity of the NC domains and the orthorhombic crystal structure was further confirmed with X-ray diffraction (XRD) analysis,41 as reported in Fig. 1e. The surface Cs:Pb:Br ratios were 0.90:1.00:3.00 according to X-ray photoelectron spectroscopy (XPS) analysis, indicating a slightly Cs deficient CsPbBr3 composition (Supplementary Figure 6).42 XPS was further used to determine the carbon content in drop-cast samples. In a drop-cast film of 8.5 nm cubic CsPbBr3 NCs, synthesized with octadecene (ODE), oleic acid (OA) and oleylamine (OLAM) and washed twice at 12000 rpm (as described in previous works31, 43) 88 at.% of the sample surface consisted of carbon. This percentage is comparable to that reported for colloidal NCs in general (not necessarily based on halide perovskites) and synthesized under similar conditions.44 For the NCs reported here, and washed only once for 2 minutes at 1000 rpm, the carbon content significantly dropped to 22 at.%, which corresponds to a ∼25 fold decrease in the ratio of carbon to the overall CsPbBr3 inorganic component. Homogenous films (see scanning electron microscope (SEM) image, Supplementary Figure 7) could be easily prepared by spin coating and drop-casting of the NCs inks and only required about 10 min of drying under ambient conditions, whereas the 8.5 nm cubic CsPbBr3 NCs required multiple high speed centrifugation steps (to get rid of excess ligands) and long drying times under vacuum, as already reported.31, 45

Fig. 1. Overview of the synthesis method and structural characterization of the CsPbBr3 NCs passivated with short ligands. (a)  Schematic representation of synthesis, where the PbBr2 precursor solution is injected in a hexane/isopropanol mixture containing Cs+ cations. After centrifugation and redispersion in toluene, the inks can be directly used for fabrication of the films. (b-d) TEM (b, c) images and HRTEM (d) images of the CsPbBr3 NCs. (e) XRD pattern indicating an orthorhombic crystal lattice. (f) Photo of up-scaled 2-gram synthesis. Scale bars correspond to 0.2 µm in (a), 50 nm in (b), and 5 nm in (c).

Optical characterization

The growth of the NCs during the synthesis was monitored over time by following their photoluminescence (PL), as shown in Supplementary Figure 8. From the data collected it is evident that the reaction takes place within the first 10 seconds from the mixing of the two solutions (see Supplementary Video 1), and that even after 2 minutes no further growth was observed. The PL and optical absorption spectra recorded on the purified CsPbBr3 NCs, both for samples dispersed in toluene and after deposition from such dispersions to form a solid film, are shown in Fig. 2a. The NCs in solution had a PL peak centered at  515 nm with a full-width-half-maximum (FWHM) of 24 nm, similar to that of cubic 8.5 nm NCs.31, 43 In the NC film, the optical absorption edge was red-shifted of about 7 nm, namely from 515 nm to 522 nm (based on the band edge), which may be attributed to a change in the local strain of the NCs in the different phase.46, 47 The PL from the film consistently followed the absorption edge and retained the same Stoke shift (around 9 nm) and FWHM as in the solution. Similar PL dynamics were found in solutions and in films (Fig. 2b), in agreement with the fact that the PL quantum yield (PLQY) did not undergo a dramatic drop, from about 58 ±6% in solution to 35 ±4% in the film (excitation density around 250 W/cm2). Note that the PLQYs from these films were slightly higher than that typically observed from films of cubic CsPbBr3 NCs prepared with OA and OLAM (≈ 30%) which remained non-conductive.43

Measurements under femtosecond (fs)-excitation were carried out to investigate the presence of amplified spontaneous emission (ASE) from the NC films, which represents a good fingerprint of their optical quality.48 ASE was readily observed for films fabricated by spin-coating of the NCs solution onto soda-lime glass substrates (200-300 nm thick, Fig. 2c). The ASE peak had a FWHM between 4.3 and 4.6 nm and was red-shifted by 3 nm from the PL maximum (PL = 522 nm). We observed a reduced ASE red-shift compared to what reported for other CsPbBr3 NCs,49-51 which we tentatively ascribed to the increased Stoke-shift observed in our spin-coated films (9 nm, compared to other synthetic approaches,37 see Fig. 2a), since the optical gain arises in spectral positions where the optical re-absorption is reduced (Urbach tail).49 Fig. 2d reports the emission intensity vs pumping fluence, from which an ASE threshold around 2.44 µJ/cm2 could be extracted. It is known that the film morphology can induce optical feedback52, 53 (due to the relatively high refractive index of the NCs, n ≈ 2, with respect to that of air) and thus modify the ASE threshold and induce random lasing. For this reason, the ASE threshold was measured from 10 different films in different positions prepared from two batches (total of 62 measurements). The threshold varied from 1.5 µJ/cm2 up to 38 µJ/cm2 with a median value of 9 µJ/cm2. To our knowledge, 1.5 µJ/cm2 is the lowest value reported for CsPbBr3 NCs49-51 and overall for perovskite thin films (a geometry that is more suitable for the fabrication of devices such as electrically pumped lasers). This evidence supports the high optical and electronic quality of the ink and its related thin films, most likely due to a low density of electronic defects. The ASE threshold found here is actually among the lowest reported to date, even if compared to that of other inorganic NCs commonly used in laser devices (CdSe nanoplateles,54 CdSe/CdS giant-shells,52, 53 and CdSe/CdS dot-in-rods.55, 56

Fig. 2 Optical characterization of CsPbBr3 NC inks in solution and in films (a) Optical absorption and steady-state PL spectra of CsPbBr3 NCs in toluene solution (solid line) and from a spin-coated film (dashed line). (b) Time-resolved PL measured at the PL peak for the CsPbBr3 NCs in toluene solution (green line) and from a spin-coated film (black line). (c) Emission spectra under increasing fs-pulsed excitation fluence with (λexc = 405 nm) recorded from a spin-coated film of CsPbBr3 NCs. An ASE peak at 531 nm is observable for pumping fluences above 2.44 µJ/cm2. (d) Emission intensity vs excitation fluence curve for the film in panel. The red line is a linear fit of the data points above threshold.

High Voltage Solar cells

Wide band-gap halides perovskites such as such as CsPbBr3 can achieve high open-circuit voltages and are therefore of particular interest to multi-junction solar cells, visible light-emitting devices, and solar water splitting applications.57-59 Moreover, the replacement of the organic component (methylammonium and/or formamidinium - FA) in the lead halide framework with an inorganic cation such as cesium is sought as the most promising avenue for improving the thermal compositional stability,60, 61 which is important for solar cell operation. However, due to the relative insolubility of the CsBr precursor, it is difficult to achieve a high-level of control over the thin-film morphology and optoelectronic properties using conventional approaches and retain low processing temperatures. Thus, thin-film devices based on CsPbBr3 have remained relatively unexplored to date. For testing the NCs inks reported here in solar cell devices, we have selected a state of the art architecture, i.e. a stack comprised of FTO-coated glass, a compact layer of titanium dioxide (c-TiO2) as the electron-extracting layer, a layer of 2,2′,7,7′-Tetrakis-(N,N-p dimethoxyphenylamino)-9,9′- spirobifluorene (Spiro-MeOTAD) as the hole-transporting material and evaporated Au as the top contact. In Fig. 3a we report a sketch of the device stack and in Fig. 3b we report the energy levels of each layer. For the electrodes and the charge extracting layers we have used values reported in the literature,62 while for the NC thin films the energies of the conduction and valence band edges have been extracted by adding the optical bandgap to the position of the valence band maximum as determined by ultraviolet photoelectron spectroscopy (UPS) measurements (see Methods and Supplementary Figure 9).

With a single spin-coating step of the suspended CsPbBr3 ink on the c-TiO2 substrate, a complete coverage of the substrate was obtained. The solar cell, in this case, exhibited short circuit values (Jsc) of 1.26 mA cm-2, open circuit voltage (Voc) of 0.87 V, and fill factor (FF) of 0.65, leading to a power conversion efficiency (PCE) of 0.72% (see Supplementary Table 1). The reported FF and Voc suggest a good electronic quality for such an extremely thin layer of perovskite, however the photocurrent was low as the film was very thin (its optical density was 0.3, see Supplementary Figure 10). A thicker film could be prepared by performing sequential deposition cycles of the NC ink. This process, which was uniquely facilitated by the low boiling point of the ligands and solvents, enabled a fast drying of the film after each deposition step, with no need to anneal the film. In particular, the fact that we can deposit the perovskite from an apolar solvent means that the active layer is resistant to subsequent NC ink deposition cycles and other spin coating steps. 14, 15

By increasing the film thickness through sequential depositions, the optical density of the sample grew monotonically (see Supplementary Figure 10) while the NCs maintained their structural properties, as proven by comparing the XRD pattern of these films to the one obtained from a film deposited by simple drop casting (Supplementary Figure 11). As reported in Fig. 2c, increasing the number of NCs deposition cycles led to a direct increase of both Jsc and Voc of the devices, while the FF remained almost constant (Supplementary Figure 12 and Supplementary Table 2). An active layer with a thickness of 550±50 nm (Supplementary Figure 13), prepared by 9 sequential depositions, exhibited a PCE of 5.4 %, which is comparable to the best performing and fully optimized devices reported so far.43, 53, 55 The solar cell had Jsc and Voc of 5.6 mA cm-2 and 1.5 V. The value for Voc is among the highest reported for perovskite halides, underlining the high quality of the active layer (for reference, the calculated maximum Voc and Jsc are 2.05 V and 7.78 mA cm-2 under AM1.5 illumination63 considering a band-gap of about 2.38 eV 64). The use of TiO2 as the electron extracting layer in a flat junction architecture generally presents J-V characteristics that depend on the polarization history of the device, with a reduction of the photocurrent over time under polarization.62, 63 Interestingly, these devices show a rapid response of the photo-current under polarization, resulting in electrically stable steady-state power output (see Supplementary Figure 12 and Supplementary Figure 13). Finally, it is worth mentioning that, although there are several factors that determine the Voc and their relative contribution is still a completely open issue in perovskite solar cells, preliminary literature reports seem to suggest that further improvements will be possible by carefully designing the charge extracting layers65, thus highlighting the strong potential of our approach.

Fig. 3 | CsPbBr3 high voltage solar cells. (a) Scheme of the standard architecture of the solar cell (FTO/c-TiO2/CsPbBr3/spiro-MeOTAD/Au). (b) Energy-level diagram of the materials used. The upper and lower edges of the boxes represent the conduction band minimum and valence band maximum, respectively. The values are stated with respect to vacuum. (c) Short circuit current (dark green dots) and open circuit voltage (light green dots) evolution for photovoltaic devices measured under AM 1.5G white light illumination, depending on the number of NC deposition cycles.

Conclusions

In summary, we have developed a scalable and environmentally friendly synthesis of inks consisting of a colloidal suspension of CsPbBr3 NCs passivated with shorter ligands compared to previously reported syntheses. This has enabled the fabrication of compact, fast drying films of NCs with low carbon content. The effective passivating ability of these ligands was responsible for the high PLQYs of the particles both in solution (58%) and, remarkably, after their deposition into films (35%), without severe degradation of charge-carrier conduction in the film. Simple spin-coated films of these inks exhibited a record low ASE threshold of 1.5 µJ/cm2. The CsPbBr3 perovskite inks were then used to fabricate a halide perovskite NC-based photovoltaic prototype device. With this formulation we demonstrated a fully air-processed, electrically stable, solar cell exhibiting power-conversion efficiencies exceeding 5% and an open circuit voltage higher than 1.5 V. These values are among the highest achieved for wide band-gap perovskite-halides, and for Cs-based solar cells.

Methods

Chemicals. Lead(II) bromide (PbBr2, 99.999% trace metals basis), cesium carbonate (Cs2CO3, reagentPlus, 99%), butylamine (BuAm, 99.5%) 2-propanol (iPrOH, anhydrous, 99.5%), propionic acid (PrAc, ≥99.5%), n-hexane (HEX 99.5%), titanium(IV) isopropoxide (99.999%), 4-tert-butylpyridine, and lithium bis(trifluoromethylsulphonyl)imide (LiTFSI) were purchased from Sigma-Aldrich. Toluene (TOL, anhydrous, 99.8%) was purchased from Carlo Erba reagents. 2,2’,7,7’-tetrakis(N,N-di-p-methoxyphenylamine)-9,9-spirobifluorene (spiro-MeOTAD) was purchased from Lumtec. All chemicals were used without any further purification.

Synthesis and purification of CsPbBr3 NCs. The synthesis is an adaptation of the synthesis for CsPbBr3 nanoplatelets as reported in our previous work.36 Here, 2 mL HEX, 1 mL IPrOH, and 5 µL ml Cs-PrAc (3.6M Cs+, Cs2Co3 dissolved in pure PrAc at room temperature) were mixed in air and at room temperature, forming a clear solution. Swiftly, 100 µL PbBr2 precursor (0.5 M in 1:1:1 PrAc:IPrOH:BuAm) was injected. The solution immediately turned green and it then turned turbid within seconds. The CsPbBr3 NCs were centrifuged for 2 min at 1000 rpm and were then redispersed in toluene.

Device fabrication. FTO-coated glass sheets were etched with zinc powder and HCl (2 M) to obtain the required electrode pattern. The substrates were sonicated in sequence with detergent (Alconox), distilled water, 2-propanol, acetone and 2-propanol again for 10 min, respectively. The substrates were then blown dry with N2 and finally treated with oxygen plasma for 10 minutes to remove the last traces of organic residues. The TiO2 precursor solution was prepared by mixing 6 µL of 2M HCl in 1 mL of 2-propanol to a titanium isopropoxide solution in 2-propanol (140 µL titanium isopropoxide in 1 mL of 2-propanol). This solution was then spin-coated at 2000 rpm for 60 s and then sintered at 500°C following Ball et al.66 The CsPbBr3 suspension solution was spin coated at 1000 rpm for 45 s. In order to increase the active layer thickness with subsequent deposition cycles the samples were left drying for 5 minutes at room temperature between each spinning. The samples were then transferred into a N2-filled glove box for the deposition of spiro-MeOTAD as the hole transporting material (HTM). The HTM was spin-coated at 1000 rpm for 60 s. The solution was prepared by dissolving 75 mg of spiro-MeOTAD, 32 µL 4-tert-butylpyridine, 18.8 µL of a stock solution of 520 mg mL-1 Li-TFSI in acetonitrile in 1 mL anhydrous chlorobenzene. After 12 h of exposure to dry air, a 75 nm thick gold film was thermally evaporated through a shadow mask to prepare devices with total area of ca. 0.0935 cm2.

Transmission Electron Microscopy. Conventional transmission electron microscopy (TEM) images were acquired on a JEOL JEM-1011 microscope equipped with a thermionic gun at 100 kV accelerating voltage. High-resolution TEM (HRTEM) imaging was performed on a JEOL JEM-2200FS microscope equipped with a Schottky gun operated at 80-200 kV accelerating voltage, a CEOS spherical aberration corrector in objective lens enabling a spatial resolution of 0.9 Å, and an in column -filter. The samples were prepared by drop casting diluted NPLs colloidal suspensions onto 200 mesh carbon-coated copper grids for conventional TEM imaging, and 400 mesh ultrathin carbon-coated copper grids for HRTEM imaging, respectively. To avoid or reduce the diffusion of Pb induced by the electron beam, the images were taken by summing multiple fast acquisitions (0.2 sec) after drift correction, by using a K2 direct detection camera (Gatan, Inc.), allowing low doses (<5e-/pixel·sec).

X-ray and ultraviolet photoelectron spectroscopy . These analyses were performed on spin-cast films of CsPbBr3 NC inks, respectively, to evaluate the chemical composition and to estimate the position of the valence band maximum (VBM) of the materials under investigation. The measurements were carried out with a Kratos Axis UltraDLD spectrometer. For XPS measurements, high resolution spectra of Cs 3d, Pb 4f, Br 3d and C 1s peaks were acquired at pass energy of 10 eV using a monochromatic Al Kα source (15 kV, 20 mA). The UPS measurements were performed using a He I (21.22 eV) discharge lamp, on an area of 55 μm in diameter, at pass energy of 5 eV and with a dwell time of 100 ms. The work function (i.e. the position of the Fermi level with respect to vacuum level) was measured from the threshold energy for the emission of secondary electrons during He I excitation. A −9.0 V bias was applied to the sample in order to precisely determine the low kinetic energy cut-off, as discussed by Helander et al.67 Then, the position of the VBM vs vacuum level was estimated by measuring its distance from the Fermi level.68, 69

Optical Absorption Spectroscopy. The spectra were taken on a Varian Cary 5000 UV−vis−NIR spectrophotometer. Samples were prepared by diluting the NC solutions in toluene (20 μL in 1 mL) in 1 cm path length quartz cuvettes. Samples of thin films were prepared by spin-coating the NCs on a c-TiO2/FTO substrate or a soda-lime glass substrate.

PL and PL quantum yield measurements. PL measurements were carried out on solutions and films with an Edinburgh Instruments fluorescence spectrometer (FLS920), which included a Xenon lamp with monochromator for steady-state PL excitation, a calibrated integrating sphere for PL quantum yield (PLQY) measurements and a time-correlated single photon counting unit coupled with a pulsed laser diode (λ = 405 nm, pulse width = 50 ps) for time-resolved PL studies. Solutions were prepared in quartz cuvettes and carefully diluted to 0.1 optical density at the excitation wavelength (λ = 400 nm) while films were prepared via spin-coating in air on soda-lime glass substrates. PLQY measurements on films were carried out using the procedure developed by J. C. De Mello et al.70

Amplified Spontaneous Emission measurements. Films of CsPbBr3 NCs spin-coated on soda-lime glass were excited with λ = 405 nm using an amplified Ti:sapphire laser (Coherent Legend Elite seeded by a Ti:sapphire fs laser) with a 70 fs pulse (FWHM) and a repetition rate of 1 kHz. The ASE measurements were performed by focusing the excitation beam with a cylindrical lens onto the sample, thus obtaining a stripe shaped beam profile. All ASE spectra were collected at ∼90° with respect to the excitation beam with an Ocean Optics HR4000 spectrometer coupled with an optical fiber.

Powder X-ray Diffraction Analysis. XRD patterns were obtained using a PANalytical Empyrean X-ray diffractometer equipped with a 1.8 kW Cu Kα ceramic X-ray tube, PIXcel3D 2x2 area detector and operating at 45 kV and 40 mA. The diffraction patterns were collected in air at room temperature using parallel-beam (PB) geometry and symmetric reflection mode. All XRD samples were prepared by drop casting a concentrated solution on a zero diffraction silicon wafer. The annealing was performed on drop-cast samples, heated on a hotplate in a glovebox. The X-ray diffraction spectra on the thin film for the solar cell were collected using a BRUKER D8 ADVANCE diffractometer with Bragg-Brentano geometry equipped with a Cu Kα1 (λ = 1.544060 Å) anode, at operating voltage of 40 kV and operating current of 40 mA. All diffraction patterns were collected at room temperature over an angular range (2θ) between 10° and 60°, step size 0.020° and acquisition time of 1 second. The sample was prepared by spin coating (1000 rpm, 60 s) with multiple step, as specified previously, on compact TiO2/FTO).

J-V measurements setup. The current density-voltage (J-V) characteristics were measured with a computer-controlled Keithley 2400 source meter in air without any device encapsulation. The simulated Air Mass 1.5 Global (AM 1.5G) irradiance was provided with a class AAA Newport solar simulator. The light intensity was calibrated with a silicon reference cell with a spectral mismatch factor of 0.99. For the J-V measurement, the voltage step and delay time were 10 mV and 10 ms, respectively. The forward scan started from -0.5 V to 1.8 V, while reverse scan from 1.8 V to -0.5 V. The pre-condition for both scans was the same, that is, just with 5 s light exposure at 1.8 V. All devices were measured using a shadow mask of 0.0935 cm2.

Data availability statement

The data that support the plots within this paper and other findings of this study are available from the corresponding authors upon reasonable request.

Acknowledgements

The research leading to these results has received funding from the European Union 7th Framework Programme under Grant Agreement No. 614897 (ERC Consolidator Grant “TRANS-NANO”) from the Cariplo Foundation through grant agreement n. 2013-0656 (“Green nanomaterials for next-generation photovoltaics, GREENS)”.

Author contributions

Q.A.A., L. M., M. P. and A. P. conceived the experiments. Q. A. developed the synthesis of the nanocrystals inks, M.G and J.B fabricated and tested the solar cells, F.D.S. and P.R. studied the optical properties of the films and F.D.S performed the ASE measurements, P.R. performed the cross-section, F.P performed the XPS measurements, G.B. performed the HRTEM measurements and M.P. performed the UPS measurements. Q.A.A., M.G., J.B, A.P and L.M. wrote the manuscript, with contributions from all authors.

Additional information

Supplementary information is available online. Reprints and permissions information is available online at www.nature.com/reprints. *Correspondence and requests for materials to A. P. and L. M.

Competing interests

The authors declare no competing financial interests

References

1.	Boles, M. A., Ling, D., Hyeon, T., Talapin, D. V. The surface science of nanocrystals. Nat. Mater.  15, 141-153 (2016).

2.	Yang, J., Choi, M. K., Kim, D.-H., Hyeon, T. Designed assembly and integration of colloidal nanocrystals for device applications. Adv. Mater.  28, 1176-1207 (2016).

3.	Kamat, P. V. Quantum dot solar cells. Semiconductor nanocrystals as light harvesters. J. Phys. Chem. C  112, 18737-18753 (2008).

4.	Goodwin, E. D., et al. Effects of post-synthesis processing on cdse nanocrystals and their solids: Correlation between surface chemistry and optoelectronic properties. J. Phys. Chem. C  118, 27097-27105 (2014).

5.	Burda, C., Chen, X., Narayanan, R., El-Sayed, M. A. Chemistry and properties of nanocrystals of different shapes. Chem. Rev.  105, 1025-1102 (2005).

6.	Donega, C. d. M. Synthesis and properties of colloidal heteronanocrystals. Chem. Soc. Rev.  40, 1512-1546 (2011).

7.	Peng, X., et al. Shape control of Cdse nanocrystals. Nature  404, 59-61 (2000).

8.	Wang, R., et al. Colloidal quantum dot ligand engineering for high performance solar cells. Energy Environ. Sci.  9, 1130-1143 (2016).

9.	McDonald, S. A., et al. Solution-processed pbs quantum dot infrared photodetectors and photovoltaics. Nat. Mater.  4, 138-142 (2005).

10.	Li, G., et al. Efficient light-emitting diodes based on nanocrystalline perovskite in a dielectric polymer matrix. Nano Lett.  15, 2640-2644 (2015).

11.	Yoon, W., et al. Enhanced open-circuit voltage of PbS nanocrystal quantum dot solar cells. Sci. Rep.  3, 2225 (2013).

12.	Oh, S. J., et al. Engineering charge injection and charge transport for high performance Pbse nanocrystal thin film devices and circuits. Nano Lett.  14, 6210-6216 (2014).

13.	Koleilat, G. I., et al. Efficient, stable infrared photovoltaics based on solution-cast colloidal quantum dots. ACS Nano  2, 833-840 (2008).

14.	Lan, X., et al. 10.6% certified colloidal quantum dot solar cells via solvent-polarity-engineered halide passivation. Nano Lett.  16, 4630-4634 (2016).

15.	Zhang, H., Kurley, J. M., Russell, J. C., Jang, J., Talapin, D. V. Solution-processed, ultrathin solar cells from CdCl3–-capped cdte nanocrystals: The multiple roles of CdCl3– ligands. J. Am. Chem. Soc.  138, 7464-7467 (2016).

16.	Saliba, M., et al. A molecularly engineered hole-transporting material for efficient perovskite solar cells. Nat. Energy  1, 15017 (2016).

17.	Saliba, M., et al. Cesium-containing triple cation perovskite solar cells: Improved stability, reproducibility and high efficiency. Energy Environ. Sci.  9, 1989-1997 (2016).

18.	Yang, W. S., et al. High-performance photovoltaic perovskite layers fabricated through intramolecular exchange. Science  348, 1234-1237 (2015).

19.	Cho, H., et al. Overcoming the electroluminescence efficiency limitations of perovskite light-emitting diodes. Science  350, 1222-1225 (2015).

20.	Ke, X., Yan, J., Zhang, A., Zhang, B., Chen, Y. Optical band gap transition from direct to indirect induced by organic content of CH3NH3PbI3 perovskite films. Appl. Phys. Lett.  107, 091904 (2015).

21.	Miyata, A., et al. Direct measurement of the exciton binding energy and effective masses for charge carriers in organic-inorganic tri-halide perovskites. Nat. Phys.  11, 582-587 (2015).

22.	Stranks, S. D., et al. Electron-hole diffusion lengths exceeding 1 micrometer in an organometal trihalide perovskite absorber. Science  342, 341-344 (2013).

23.	Giorgi, G., Fujisawa, J.-I., Segawa, H., Yamashita, K. Small photocarrier effective masses featuring ambipolar transport in methylammonium lead iodide perovskite: A density functional analysis. J. Phys. Chem. Lett.  4, 4213-4216 (2013).

24.	Koh, T. M., et al. Formamidinium-containing metal-halide: An alternative material for near-IR absorption perovskite solar cells. J. Phys. Chem. C  118, 16458-16462 (2014).

25.	Zhang, W., et al. Enhanced optoelectronic quality of perovskite thin films with hypophosphorous acid for planar heterojunction solar cells. Nat. Commun.  6, 10030 (2015).

26.	He, H., et al. Exciton localization in solution-processed organolead trihalide perovskites. Nat. Commun.  7, 10896 (2016).

27.	Nie, W., et al. High-efficiency solution-processed perovskite solar cells with millimeter-scale grains. Science  347, 522-525 (2015).

28.	Deschler, F., et al. High photoluminescence efficiency and optically pumped lasing in solution-processed mixed halide perovskite semiconductors. J. Phys. Chem. Lett.  5, 1421-1426 (2014).

29.	Yantara, N., et al. Inorganic halide perovskites for efficient light-emitting diodes. J. Phys. Chem. Lett.  6, 4360-4364 (2015).

30.	Schmidt, L. C., et al. Nontemplate synthesis of CH3NH3PbBr3 perovskite nanoparticles. J. Am. Chem. Soc.  136, 850-853 (2014).

31.	Protesescu, L., et al. Nanocrystals of cesium lead halide perovskites (CsPbX3,Xx = Cl, Br, and I): Novel optoelectronic materials showing bright emission with wide color gamut. Nano Lett.  15, 3692-3696 (2015).

32.	Tyagi, P., Arveson, S. M., Tisdale, W. A. Colloidal organohalide perovskite nanoplatelets exhibiting quantum confinement. J. Phys. Chem. Lett.  6, 1911-1916 (2015).

33.	Sichert, J. A., et al. Quantum size effect in organometal halide perovskite nanoplatelets. Nano Lett.  15, 6521–6527 (2015).

34.	Hu, F., et al. Superior optical properties of perovskite nanocrystals as single photon emitters. ACS Nano  9, 12410–12416 (2015).

35.	Bekenstein, Y., Koscher, B. A., Eaton, S. W., Yang, P., Alivisatos, A. P. Highly luminescent colloidal nanoplates of perovskite cesium lead halide and their oriented assemblies. J. Am. Chem. Soc.  137, 16008-16011 (2015).

36.	Akkerman, Q. A., et al. Solution synthesis approach to colloidal cesium lead halide perovskite nanoplatelets with monolayer-level thickness control. J. Am. Chem. Soc.  138, 1010-1016 (2016).

37.	Sun, S., Yuan, D., Xu, Y., Wang, A., Deng, Z. Ligand-mediated synthesis of shape-controlled cesium lead halide perovskite nanocrystals via reprecipitation process at room temperature. ACS Nano  10, 3648–3657 (2016).

38.	Bai, S., Yuan, Z., Gao, F. Colloidal metal halide perovskite nanocrystals: Synthesis, characterization, and applications. J. Mater. Chem. C  4, 3898-3904 (2016).

39.	De Roo, J., et al. Highly dynamic ligand binding and light absorption coefficient of cesium lead bromide perovskite nanocrystals. ACS Nano  10, 2071-2081 (2016).

40.	Swarnkar, A., et al. Quantum dot–induced phase stabilization of α-CsPbI3 perovskite for high-efficiency photovoltaics. Science  354, 92-95 (2016).

41.	Stoumpos, C. C., et al. Crystal growth of the perovskite semiconductor CsPbBr3: A new material for high-energy radiation detection. Cryst. Growth Design  13, 2722-2727 (2013).

42.	Sebastian, M., et al. Excitonic emissions and above-band-gap luminescence in the single-crystal perovskite semiconductors cspbbr3 and CsPbCl3. Phys. Rev. B  92, 235210 (2015).

43.	Akkerman, Q. A., et al. Tuning the optical properties of cesium lead halide perovskite nanocrystals by anion exchange reactions. J. Am. Chem. Soc.  137, 10276-10281 (2015).

44.	Zorn, G., Dave, S. R., Gao, X., Castner, D. G. Method for determining the elemental composition and distribution in semiconductor core−shell quantum dots. Anal. Chem.  83, 866-873 (2011).

45.	Yakunin, S., et al. Low-threshold amplified spontaneous emission and lasing from colloidal nanocrystals of caesium lead halide perovskites. Nat. Commun.  6, 8056 (2015).

46.	Dou, L., et al. Atomically thin two-dimensional organic-inorganic hybrid perovskites. Science  349, 1518-1521 (2015).

47.	D’Innocenzo, V., Srimath Kandada, A. R., De Bastiani, M., Gandini, M., Petrozza, A. Tuning the light emission properties by band gap engineering in hybrid lead halide perovskite. J. Am. Chem. Soc.  136, 17730-17733 (2014).

48.	Arora, N., et al. Photovoltaic and amplified spontaneous emission studies of high-quality formamidinium lead bromide perovskite films. Adv. Funct. Mater.  26, 2846-2854 (2016).

49.	Yakunin, S., et al. Low-threshold amplified spontaneous emission and lasing from colloidal nanocrystals of caesium lead halide perovskites. Nat. Commun.  6, 8056 (2015).

50.	Xu, Y., et al. Two-photon-pumped perovskite semiconductor nanocrystal lasers. J. Am. Chem. Soc.  138, 3761-3768 (2016).

51.	Vybornyi, O., Yakunin, S., Kovalenko, M. V. Polar-solvent-free colloidal synthesis of highly luminescent alkylammonium lead halide perovskite nanocrystals. Nanoscale  8, 6278-6283 (2016).

52.	Park, Y.-S., Bae, W. K., Baker, T., Lim, J., Klimov, V. I. Effect of auger recombination on lasing in heterostructured quantum dots with engineered core/shell interfaces. Nano Lett.  15, 7319-7328 (2015).

53.	Gollner, C., et al. Random lasing with systematic threshold behavior in films of CdSe/CdS core/thick-shell colloidal quantum dots. ACS Nano  9, 9792-9801 (2015).

54.	Grim, J. Q., et al. Continuous-wave biexciton lasing at room temperature using solution-processed quantum wells. Nat. Nanotechnol.  9, 891-895 (2014).

55.	Moreels, I., et al. Nearly temperature-independent threshold for amplified spontaneous emission in colloidal CdSe/CdS quantum dot-in-rods. Adv. Mater.  24, OP231-OP235 (2012).

56.	Di Stasio, F., et al. Single-mode lasing from colloidal water-soluble CdSe/CdS quantum dot-in-rods. Small  11, 1328-1334 (2015).

57.	Edri, E., Kirmayer, S., Kulbak, M., Hodes, G., Cahen, D. Chloride inclusion and hole transport material doping to improve methyl ammonium lead bromide perovskite-based high open-circuit voltage solar cells. J. Phys. Chem. Lett.  5, 429-433 (2014).

58.	Giesbrecht, N., et al. Synthesis of perfectly oriented and micrometer-sized MAPbBr3 perovskite crystals for thin-film photovoltaic applications. ACS Energy Lett.  1, 150-154 (2016).

59.	Arora, N., et al. High open-circuit voltage: Fabrication of formamidinium lead bromide perovskite solar cells using fluorene–dithiophene derivatives as hole-transporting materials. ACS Energy Lett.  1, 107-112 (2016).

60.	Kulbak, M., et al. Cesium enhances long-term stability of lead bromide perovskite-based solar cells. J. Phys. Chem. Lett.  7, 167-172 (2016).

61.	Sutton, R. J., et al. Bandgap-tunable cesium lead halide perovskites with high thermal stability for efficient solar cells. Adv. Energy Mater., 10.1002/aenm.201502458 (2016).

62.	Gao, P., Gratzel, M., Nazeeruddin, M. K. Organohalide lead perovskites for photovoltaic applications. Energy Environ. Sci.  7, 2448-2463 (2014).

63.	Shockley, W., Queisser, H. J. Detailed balance limit of efficiency of p‐n junction solar cells. J. Appl. Phys.  32, 510-519 (1961).

64.	Kulbak, M., Cahen, D., Hodes, G. How important is the organic part of lead halide perovskite photovoltaic cells? Efficient CsPbBr3 cells. J. Phys. Chem. Lett.  6, 2452-2456 (2015).

65.	Ryu, S., et al. Voltage output of efficient perovskite solar cells with high open-circuit voltage and fill factor. Energy Environ. Sci.  7, 2614-2618 (2014).

66.	Ball, J. M., Lee, M. M., Hey, A., Snaith, H. J. Low-temperature processed meso-superstructured to thin-film perovskite solar cells. Energy Environ. Sci.  6, 1739-1743 (2013).

67.	Helander, M. G., Greiner, M. T., Wang, Z. B., Lu, Z. H. Pitfalls in measuring work function using photoelectron spectroscopy. Appl. Surf. Sci.  256, 2602-2605 (2010).

68.	Calloni, A., et al. Stability of organic cations in solution-processed CH3NH3PbI3 perovskites: Formation of modified surface layers. J. Phys. Chem. C  119, 21329-21335 (2015).

69.	Schulz, P., et al. Interface energetics in organo-metal halide perovskite-based photovoltaic cells. Energy Environ. Sci.  7, 1377-1381 (2014).

70.	de Mello, J. C., Wittmann, H. F., Friend, R. H. An improved experimental determination of external photoluminescence quantum efficiency. Adv. Mater.  9, 230-232 (1997).